Abstract Template

Abstract Title: Microstructure and mechanical property characterization of Incol718 alloy specimen printed by selective laser melting

JW. Kang1, JH. Yi1, CY Deng1, YL Feng2, PY. Wu2, T. Feng2

1 Tsinghua University, China

2Beijing e-Plus 3D Tech. Co. Ltd, China

Abstract (not more than 300 words)

Incol 718 alloy specimens were fabricated by the selective laser melting (SLM) method. The effect of parameters such as laser power and scanning speed on the microstructure and mechanical properties were investigated. It is found the energy density, a function of laser power, scanning speed and hatch distance is greatly related to the mechanical properties. The specimen fabricated with laser power 200W, scanning speed 1000mm/s, and hatch distance 0.1mm and layer height 0.02mm achieved best mechanical properties. The as-fabricated tensile strength reaches 800MPa in the fabrication direction, 15% higher than the standard property, while the elongation keeps 32%. Its microstructure in the vertical section is regular columnar grains, 20um wide. The stack of the melt pools are regular, and the level of each layer is smooth. The soundness and columnar grains result its high mechanical property.

Keywords—Incol718; Mechanical property; Microstructure; Selective laser melting

Professional Biography (100-150 words)

Jinwu Kang has completed his PhD at the age of 28 years from Tsinghua University. He is an associate professor of School of Materials Science and Engineering, Tsinghua University. During May, 2001 to Jan. 2003, he did research as research scientist at Worcester Polytechnic Institute, USA. He has been doing the research about the modelling and simulation of casting and heat treatment processes of castings, and 3D printing of sand moulds and metallic parts in recent years. He proposed the description methods for the deformation of castings, intensive riser cooling of castings after their solidification, and 3D printed hollow mould for castings to realize controlled cooling at whole scale. He has published 170 papers and got four academic awards from the Ministry of Education, China for his distinguished research. He is the Chief-Editor of Materials Science and Engineering International Journal.

Email Id: kangjw@tsinghua.edu.cn

Any Comments: