3rd International webinar on Advanced Materials

December 13th, 2021

‘’Inkjet printing of silver conductive ink on textiles for wearable electronic applications’’

# Mohamed Tahiri a , Abdelkrim Boumegananea,b*,  Ayoub Nadib, Omar Cherkaoui b

a Organic Chemistry, Extraction and Valorization Labiratory, Hassan II University of Casablanca, Km 8 Route d'El Jadida, B.P 5366 Maarif 20100. Casablanca, Morocco. mohtahiri@yahoo.fr

b Laboratory of Research on Textile Materials (REMTEX), Higher School of Textile and Clothing Industries (ESITH), 20230 Casablanca, Morocco

# Abstract

In this study, silver nanoparticles were synthesized with a starch-based reduction biosystem at room temperature. With this approach, high concentration silver nanoparticles were produced on a large scale with a low starch/AgNO3 mass ratio, which was very advantageous for the low cost and high conductivity. Conductive inks were prepared from the synthesized silver nanoparticles by dispersion of the nanoparticles in a non-conductive commercial ink. Various patterns have been developed by printing silver nanoparticles with different percentages from 5% to 25% on a cotton substrate using a syringe. The printed patterns show a resistivity drop depending on the sintering temperature and nanoparticle concentration in the range of 8M and 8× 10-5 MΩ by heat treatment varying between 60°C and 320°C for 10min. In addition, a LED test was successfully performed on the fabrics. These flexible patterns produced by inkjet printing would present a considerable success for textile-based electronic devices with low cost.