# The effect of 3D alginate hydrogel stiffness on cellular behavior

Alejandra Suarez-Arnedo, MSc, Universidad de Los Andes, Colombia

Homero F. Pastrana, PhD, Universidad de Los Andes, Colombia

Juan C. Cruz, PhD, Universidad de Los Andes, Colombia

Carolina Muñoz-Camargo, PhD, Universidad de Los Andes, Colombia

Diana Cárdenas, Universidad de Los Andes, Colombia

Helena Groot, MSc, Universidad de Los Andes, Colombia

Diana M. Narváez PhD, Universidad de Los Andes, Colombia

### Abstract (300 word limit)

Currently the design of extracellular matrices is directed towards mimicking the cellular microenvironment; however, these matrices also allow the study of cell behavior in response to various triggering properties. Several mechanical features such as stiffness have shown to affect cell differentiation, adhesion, and viability. These properties have been evaluated in multiple studies using two-dimensional (2D) substrates; nonetheless, it has been shown that three-dimensional (3D) microenvironments are most suitable to study native cellular behavior. This 3D microenvironment has been frequently design using alginate hydrogels; therefore, the aim of this study was to determine if the alginate hydrogels stiffness may affect cytoplasmic structure of encapsulated cells. Methods and materials: Hydrogels of 2% and 4% (w/v) of alginate were made by the diffusion method. Subsequently, hydrogels stiffness was determined using atomic force microscopy (AFM).  Finally, the cells were encapsulated in the hydrogels and the actin fillament conformation was analyzed using Confocal microscopy. Results and Discussion: Ther were significant differences (p-value <0.0001) between stiffness of the 2% (30.5 kPa) and the 4% (300.3 kPa) hydrogels. Additionally, it was observed that encapsulated cells in the 4% hydrogel may have a greater amount of actin filament than the 2% hydrogel. Accordingly, it is possible to suggest that, just as observed in 2D systems, a more rigid 3D microenvironment can lead to the increase of actin filaments. Furthermore, by observing the cell geometry, it can be assumed that the conformational changes of the cells are not only trigger by focal adhesions with the extracellular matrix but by sensing of the environmental mechanical properties.

### Image

Figure 1. Vero cells cultured in two different concentrations (1% and 2% w/v) alginate hydrogels. Cells were stained with DAPI (nuclei: blue) and Phalloidin (F-Actin: green) [Scale bar: 25 µm]

Recent publications (minimum 5)

- Cavo, M., Fato, M., Peñuela, L., Beltrame, F., Raiteri, R., Scaglione, S., … Scaglione, S. (2016). Microenvironment complexity and matrix stiffness regulate breast cancer cell activity in a 3D in vitro model. Scientific Reports, 6(October), 35367. https://doi.org/10.1038/srep35367

- Das, R. K., Gocheva, V., Hammink, R., Zouani, O. F., & Rowan, A. E. (2016). Stress-stiffening-mediated stem-cell commitment switch in soft responsive hydrogels. Nature Materials, 15(3), 318–25. https://doi.org/10.1038/nmat4483

- Das, R. K., & Zouani, O. F. (2014). A review of the effects of the cell environment physicochemical nanoarchitecture on stem cell commitment. Biomaterials, 35(20), 5278–5293. https://doi.org/10.1016/j.biomaterials.2014.03.044

- Discher, D. E., Mooney, D. J., & Zandstra, P. W. (2009). Growth Factors, Matrices, and Forces Combine and Control Stem Cells. Science, 324(June), 1673–1678.

- Harris, G., Piroli, M., & Jabbarzadeh, E. (2014). Deconstructing the Effects of Matrix Elasticity and Geometry in Mesenchymal Stem Cell Lineage Commitment. Adv Funct Mater., 24(16), 2396–2403. https://doi.org/10.1016/j.biotechadv.2011.08.021.Secreted

- Higuchi, A., Ling, Q., Chang, Y., Hsu, S., & Umezawa, A. (2013). Physical Cues of Biomaterials Guide Stem Cell Di ff erentiation Fate.

- Lv, H., Wang, H., Zhang, Z., Yang, W., Liu, W., Li, Y., & Li, L. (2017). Biomaterial stiffness determines stem cell fate. Life Sciences, 178, 42–48. https://doi.org/10.1016/j.lfs.2017.04.014

- Oyen, M. L. (2014). Mechanical characterisation of hydrogel materials. International Materials Reviews, 59(1), 44–59. https://doi.org/10.1179/1743280413Y.0000000022

- Tibbitt, M. W., & Anseth, K. S. (2009). Hydrogels as Extracellular Matrix Mimics for 3D Cell Culture, 103(4), 655–663. https://doi.org/10.1002/bit.22361

Biography (150 word limit)

Alejandra Suarez Arnedo studied Chemical Engineering and Microbiology at Universidad de Los Andes, and she is currently doing her Masters degree in biological sciences with an emphasis in Microbiology and Biomedical Engineering. She is working at the Laboratory of human genetics where she is working on her thesis, focused on cellular differentiation and design of extracellular matrices using alginate hydrogels. Finally, she has a great passion for improving the health and wellbeing via the study of tissue engineering.

Email:sa.suarez1912@uniandes.edu.co

Notes/Comments: