# 3D alginate hydrogels: impact of substrate stiffness on cellular response

Alejandra Suarez-Arnedo, MSc, Universidad de Los Andes, Colombia

Homero F. Pastrana, PhD, Universidad de Los Andes, Colombia

Juan C. Cruz, PhD, Universidad de Los Andes, Colombia

Carolina Muñoz-Camargo, PhD, Universidad de Los Andes, Colombia

Diana Cárdenas, Universidad de Los Andes, Colombia

Helena Groot, MSc, Universidad de Los Andes, Colombia

Diana M. Narváez PhD, Universidad de Los Andes, Colombia

### Abstract (300 word limit)

Currently, the design of extracellular matrices is directed towards mimicking the cellular microenvironment.  Additionally, these matrices allow the study of cell behavior in response to varying physicochemical and mechanical properties. For instance, mechanical properties such as stiffness have been reported to alter cell differentiation, adhesion, and viability. Thus far, t cellular response studies have been conducted on two-dimensional (2D) substrates; nonetheless, three-dimensional (3D) microenvironments appear most suitable to approach to native cellular behavior. Alginate hydrogels provide an appealing 3D microenvironment; however, a full characterization of mechanical property-function relationships is still elusive.  This study is therefore dedicated to determine if changes in the stiffness of alginate hydrogels might lead to significant structural changes in cells upon encapsulation. Methods and materials: Hydrogels with alginate contents of 2% and 4% (w/v) were prepared by the diffusion method. Subsequently, hydrogels stiffness was determined via atomic force microscopy (AFM).  Finally,  Vero cells were encapsulated in the hydrogels where actin fillaments were stained and  and imaged using Confocal microscopy. Results and Discussion: Stiffness values of the 2% and the 4% hydrogels were significantly different(p-value <0.0001) and approached 30.5 kPa and 300.3 kPa, respectively. Additionally, a simple inspection revealed tha actin filament was most abundant for  the 4% hydrogel (Figure 1).. Accordingly, it is possible to suggest that, as for the 2D systems, a more rigid 3D microenvironment can lead to an increase of actin filaments. Furthermore, the observed cell geometries suggest that  not only focal adhesions with the extracellular matrix but local changes in mechanical properties are responsible for important structural changes in cells.

### Image

Figure 1. Confocal imaging of Vero cells cultured on alginate hydrogels prepared at two different concentrations (1% and 2% w/v). Cells were stained with DAPI (nuclei: blue) and Phalloidin (F-Actin: green) [Scale bar: 25 µm]

Recent publications (minimum 5)

- Cavo, M., Fato, M., Peñuela, L., Beltrame, F., Raiteri, R., Scaglione, S., … Scaglione, S. (2016). Microenvironment complexity and matrix stiffness regulate breast cancer cell activity in a 3D in vitro model. Scientific Reports, 6(October), 35367. https://doi.org/10.1038/srep35367

- Das, R. K., Gocheva, V., Hammink, R., Zouani, O. F., & Rowan, A. E. (2016). Stress-stiffening-mediated stem-cell commitment switch in soft responsive hydrogels. Nature Materials, 15(3), 318–25. https://doi.org/10.1038/nmat4483

- Das, R. K., & Zouani, O. F. (2014). A review of the effects of the cell environment physicochemical nanoarchitecture on stem cell commitment. Biomaterials, 35(20), 5278–5293. https://doi.org/10.1016/j.biomaterials.2014.03.044

- Discher, D. E., Mooney, D. J., & Zandstra, P. W. (2009). Growth Factors, Matrices, and Forces Combine and Control Stem Cells. Science, 324(June), 1673–1678.

- Harris, G., Piroli, M., & Jabbarzadeh, E. (2014). Deconstructing the Effects of Matrix Elasticity and Geometry in Mesenchymal Stem Cell Lineage Commitment. Adv Funct Mater., 24(16), 2396–2403. https://doi.org/10.1016/j.biotechadv.2011.08.021.Secreted

- Higuchi, A., Ling, Q., Chang, Y., Hsu, S., & Umezawa, A. (2013). Physical Cues of Biomaterials Guide Stem Cell Di ff erentiation Fate.

- Lv, H., Wang, H., Zhang, Z., Yang, W., Liu, W., Li, Y., & Li, L. (2017). Biomaterial stiffness determines stem cell fate. Life Sciences, 178, 42–48. https://doi.org/10.1016/j.lfs.2017.04.014

- Oyen, M. L. (2014). Mechanical characterisation of hydrogel materials. International Materials Reviews, 59(1), 44–59. https://doi.org/10.1179/1743280413Y.0000000022

- Tibbitt, M. W., & Anseth, K. S. (2009). Hydrogels as Extracellular Matrix Mimics for 3D Cell Culture, 103(4), 655–663. https://doi.org/10.1002/bit.22361

Biography (150 word limit)

Alejandra Suarez Arnedo, completed her B.S. degrees in Chemical Engineering and Microbiology at Universidad de los Andes, she is currently a Master’s student in biological sciences with an emphasis in Microbiology and Biomedical Engineering. She conducts research on cellular differentiation and design of extracellular matrices using alginate hydrogels at the Laboratory of Human Genetics. Finally, she is very passionate about improving the health and wellbeing via the study of tissue engineering.

Email:sa.suarez1912@uniandes.edu.co

Notes/Comments: