ELECTROCHEMICAL PROPERTIES OF SYNTHESIZED Ni-Co HYDROXIDE BASED BI-PHASE NANOCOMPOSITES USING Ni-FOAM AND Ni-GRAPHENE-FOAM AS CURRENT COLLECTOR

O. Guellati 1,2,4*, A. Harat 1, A. Nait-Merzoug 1, D. Momodu 3, A. Bello 3, J.M. Moshawe 3, D. Begin 4, N. Manyala 3 and M. Guerioune 1

(1) LEREC Laboratory, Badji-Mokhtar University of Annaba, BP. 12, 23000 Annaba, ALGERIA.

(2) Mohamed Cherif Messadia University of Souk Ahras, BP. 1553, 41000-Souk-Ahras, ALGERIA.

(3) Department of Physics, Institute of Applied Materials, SARCHI Chair in Carbon Technology and Materials, University of Pretoria, Pretoria 0028, SOUTH AFRICA.

(4) Institut de Chimie et Procédés pour l'Energie, l'Environnement et la Santé (ICPEES) - ECPM - CNRS - UdS, 25 rue Becquerel, 67087 Strasbourg Cedex 2, FRANCE.

Contact@E-mail: guellati23@yahoo.fr

### Abstract:

In this investigation, we report firstly the effect of hydrothermal process parameters on the structural and morphological properties selectivity of Ni-Co hydroxide based bi-phase nanocomposites. These Nano-hybrid materials based on nanoporous transition metals hydroxides and carbonate hydroxides have attracted much attention as promising electroactive materials for mostly energy storage, environment and sensing applications. So, the structural, textural and morphological characterizations of the obtained products were carried out using different techniques such as: XRD, FTIR, FESEM, BET and XPS.

Secondly, we present the electrochemical properties of these synthesized electroactive products using two king of current collector: NiF (Ni Foam) and NiGF (Ni Graphene Foam). These electrochemical measurements were studied using three electrode configuration system through cyclic voltammetry (CV), electrochemical impedance spectroscopy (EIS) and chronopotentiometry (CP) measurements. The obtained results show a good cyclic stability of ∼ 98 % after 2000 charge-discharge cycles at 30 A. g-1 depicting their potential as suitable materials for energy storage devices.

Keywords: Nanohybrid materials, NiCo hydroxides, hydrothermal synthesis, NiCo carbonate hydroxides, pseudocapacitance, supercapacitors.

Recent Publications:

- O. Guellati, A. Harat, D. Momodu, J. Dangbegnon, T. Romero, D. Begin, C. PhamHuu, N. Manyala, M. Guerioune, Electrochimica Acta, vol. 275 (2018) 155-171. DOI : 10.1016/j.electacta.2018.04.112

- H. Kennaz, A. Harat, O. Guellati, D. Y. Momodu, F. Barzegar, J. K. Dangbegnon, N. Manyala, M. Guerioune, J Solid State Electrochem, vol. 22, pp. 835-847 (2018). https://doi.org/10.1007/s10008-017-3813-y.

Biography:

O. Guellati, permanent researcher in LEREC laboratory in Algeria, has completed her PhD from Badji-Mokhtar University of Annaba 2013, Algeria on production of Carbon nanotube (CNTs) using CCVD technique and their functionalization and macronisation. She has published 15 papers in reputed journals. She is current reviewer in Nanoscale Research Letters. Actually, she is working on the production of transition metal hydroxides, oxides and their nanocomposites / nanohybrids with CNTs and graphene for energy storage and environment application. She is working in collaboration with ICPEES at ECPM, Strasbourg – France, IMS at University of Valencia – Spain and SARChI Chair in Carbon Technology and Materials at Pretoria University, South Africa.

Email: guellati23@yahoo.fr