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Abstract 
Latent heat thermal energy storage (LHTES) represents advanced technology based on the use of reversible change of phase of materials. LHTES offers significantly higher heat storage density in narrow temperature interval compared to sensible heat storage. Integration of wide range of organic and inorganic of latent heat storage media known as Phase Change Materials (PCMs) was introduced in building industry during last decades as a substitution of heavy-weight structures. Organic PCMs are represented by paraffin or fatty acids, while salt hydrates are typical representatives of inorganic PCMs. Currently the origin of the heat storage materials is starting to play an important role in the design of the heat storage systems. Therefore the environmental impacts such as embodied energy associated with production of PCMs have to be considered too. That is why renewable bio-based non-paraffinic PCMs made from underused feedstock are at the forefront of the development of LHTES. This group of PCMs includes soybean oils, coconut oils and beef tallow.
This paper describes investigation of coconut oil as a representative of promising PCMs because of its availability at domestic market. The samples of coconut oil were subjected to periodical heating and cooling in small environmental chamber. Differential Scanning Calorimetry (DSC) analysis of the samples was performed as well. The results from DSC analysis show that tested coconut oil has melting enthalpy 103 J/g. Temperature ranges of melting and solidification of PCM in Fig. 1 indicate that coconut oil meets one of the conditions for application in buildings. Unfortunately the supercooling effect down to the 20 °C was observed during cooling of the samples. Therefore behavior of coconut oil and its thermal stability will be subject of our future work.
Presented work was supported by the Czech Science Foundation under project No. 19-20943S “Compatibility of plastics and metals with latent heat storage media for integration in buildings”.
Image
Fig.1 Temperature of the coconut oil and water during thermal cycling in environmental chamber
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