# Hydrogenation of Carbon Dioxide using Au Catalysts

# S.A.C. Carabineiro(1), A. Vourros(2,3), I. Garagounis(2,3), V. Kyriakou(2,3), F.J. Maldonado-Hódar(4), G.E. Marnellos(3,5,6), M. Konsolakis(7)

(1) Lab. Catalysis and Materials, LA LSRE-LCM, Faculty of Engineering, Univ. Porto, Portugal

(2) Department of Chemical Engineering, Aristotle University of Thessaloniki, Greece

(3) Chem. Process & Energy Res. Inst., Centre for Res. & Technol. Hellas, Thessaloniki, Greece

(4) Carbon Res. Group, Inorganic Chemistry Dept., Faculty of Science, Univ. Granada, Spain

(5) Department of Mechanical Engineering, Univ. of Western Macedonia, Kozani, Greece

(6) Department of Environmental Engineering, Univ. of Western Macedonia, Kozani, Greece

(7) School of Production Engineering and Management, Technical University of Crete, Greece

### Abstract

Fossil fuels are still the primary source of energy in the world, which makes the concentration of CO2 continuously increase. Appropriate measures need to be taken to decrease this tendency. CO2 can be hydrogenated to produce high added-value chemicals, such as methanol, methane and carbon monoxide.

In this work, gold nanoparticles were supported on different metal oxides (Al2O3, CeO2, Fe2O3, TiO2 and ZnO) by a deposition-precipitation method. The activity of these catalysts for CO2 hydrogenation was tested using an online gas chromatograph.

It was shown that the support had a critical influence on the process. Au/Al2O3 was nearly. Au/CeO2 and Au/ZnO were very selective to methanol production. Au/TiO2 and Au/Fe2O3, although showing higher CO2 conversion, produced mostly carbon monoxide and methane.

Au/CeO2 showed the best results for methanol formation, although CeO2 alone was inert. The high activity of Au/CeO2 can be attributed to a synergistic effect between Au and CeO2.

Acknowledgements: General Secretariat of Research and Technology of Greece (13CAPITA-13-8A), for funding (Project “CO2 and H2O toward methanol synthesis at atmospheric pressure in co-ionic electrochemical membrane reactors”, ERA-NET, 7th FP. SACC thanks Fundação para a Ciência e Tecnologia (FCT) for financial support through (IF/01381/2013/CP1160/CT0007) Investigador FCT program, with financing from the European Social Fund and the Human Potential Operational Program. This work was financially supported by Project POCI-01-0145-FEDER-006984 – Associated Laboratory LSRE-LCM funded by FEDER funds through COMPETE2020 - Programa Operacional Competitividade e Internacionalização (POCI) – and by national funds through FCT. Authors are thankful to CEMUP for assistance with XPS and SEM analyses.

Recent Publications

- A. Vourros, V. Kyriakou, I. Garagounis, S.A.C. Carabineiro, F.J. Maldonado-Hódar, G.E. Marnellos, M. Konsolakis (2017), Carbon Dioxide Hydrogenation to Methanol over Supported Au nanoparticles: Effect of the support, Journal of CO2 Utilization, 19, 247-256.

- V. Kyriakou, A. Vourros, I. Garagounis, S.A.C. Carabineiro, F.J. Maldonado-Hódar, G.E. Marnellos, M. Konsolakis (2017), Highly Active and Stable TiO2 supported Au nanoparticles for CO2 reduction, Catalysis Communications, 98, 52-5.

- S.A.C. Carabineiro, E. Papista, G.E. Marnellos, P.B. Tavares, F.J. Maldonado-Hódar, M. Konsolakis (2017), Catalytic decomposition of N2O on inorganic oxides: Εffect of doping with Au nanoparticles, Molecular Catalysis, 436, 78-89.

- L.M.D.R.S. Martins, S.A.C. Carabineiro, J. Wang, B.G.M. Rocha, F.J. Maldonado-Hódar, A.J.L. Pombeiro (2017), Supported gold nanoparticles as reusable catalysts for oxidation reactions of industrial significance, ChemCatChem, 9 (7), 1211- 1221

- M. Lykaki, E. Pahatouridou, E. Iliopoulou, S.A.C. Carabineiro, M. Konsolakis (2017), Impact of the synthesis parameters on the solid state properties and the CO oxidation performance of ceria nanoparticles, RSC Advances, 7, 6160–6169.

- M. Konsolakis, S.A.C. Carabineiro, G. Marnellos, M.F. Asad, O.S.G.P. Soares, M.F.R. Pereira, J.J.M. Órfão, J.L. Figueiredo (2017), Effect of cobalt loading on the solid state properties and ethyl acetate oxidation performance of cobalt-cerium mixed oxides, Journal of Colloid and Interface Science, 496, 141–149.

- A.P.C. Ribeiro, L.M.D.R.S. Martins, S.A.C. Carabineiro, J.L. Figueiredo, A.J.L. Pombeiro (2017), Gold nanoparticles deposited on surface modified carbon materials as reusable catalysts for cyclohexane hydrocarboxylation, Applied Catalysis A: General, 547, 124-131.

Biography (150 word limit)

Sonia Carabineiro ID graduated in Applied Chemistry (Biotechnology) and completed Ph.D. in Chemical Engineering (Catalysis) in 2001 at Universidade Nova de Lisboa (Portugal). She was a post doc in Leiden University (The Netherlands) and Instituto Superior Tecnico (Portugal). On December 2007 she joined the University of Porto (Portugal) as an Assistant Researcher, with a Ciencia 2007 grant from Foundation for Science and Technology (FCT). She became Principal Researcher in December 2013 (Investigador FCT grant) at the same lab. She published more than 115 papers in reputed journals and 19 book chapters. She has an h index of 30 and over 2400 citations (Scopus, January 2018, Orcid: 0000-0001-9913-4671). Her research work deals mostly with catalysis by gold nanoparticles, mixed metal oxides and nanostructured carbon materials for oxidation reactions, degradation and adsorption of air and water pollutants. She is currently the female reviewer in the world with more revisions (~500 reviews, Publons, January 2018).

Email: scarabin@fe.up.pt