# Selective catalytic reduction of NOx with ammonia – laboratory studies with the use of CuOx/Al2O3 catalysts

Marek Kulazynski, Ph.D., Wroclaw University of Science and Technology, Poland

Jerzy Walendziewski, Prof., Wroclaw University of Science and Technology, Poland

Katarzyna Pstrowska, Ph.D., Wroclaw University of Science and Technology, Poland

Lukasz Swiatek, Ph.D., Wroclaw University of Science and Technology, Poland

### Abstract

### Nitrogen oxides are among the most pervasive and difficult emissions to control. Currently, there are no commercial catalytic processes decomposing NOx without a reducing gas. Selective catalytic reduction (SCR) systems for NOx reduction use ammonia as the reducing agent. Ammonia SCR requires the handling of large quantities of toxic gases, tight temperature control, high reaction temperatures. Also effective NOx reduction requires large amount of catalyst because of the relatively low reaction rate. Lowering the cost of the reduction process by increase in the process efficiency and limiting the difficulty of handling the reducing agent would reduce the catalyst cost and decrease the operating temperature. Due to the above-mentioned arguments, the improvement of NOx reduction with ammonia SCR is important. It is also important because of the biomass use intensification (mainly due to the fact, that it is renewable energy source). Considering biomass chemical composition, NOx emission is much higher in the combustion processes comparing to the coal combustion.

### The aim of this study was to analyze the activity of copper oxide supported in the SCR laboratory scale studies. 0.1; 0.2; 0.5; 1.0 and 2.0% of CuO was loaded on two types of aluminosilicates (G) and tested in laboratory 200 mm long flow reactor. The  NOx reduction with ammonia SCR was tested at the temperature range of 
100-500 oC. Gas composition before and after the reactor was analyzed at each measurement point. Each time the result of the gas composition analysis was averaged from a measurement lasting 
1 minute. Gas flow rate was set at the level of 3 000 cm3·cm-3·h-1.

Fig 1. Ammonia conversion in the presence of CuOX /GI catalysts. 
Gas composition: 240 ppm NO, 240 ppm NH3, 21% O2, N2 up to 100%

Recent Publications (minimum 5)

- Narowska B, Kulazynski M., Lukaszewicz M, Burchacka E. (2019) Use of activated carbons as catalyst supports for biodiesel production. Renewable Energy 135, pp. 176-185

- Pstrowska K, Kaczmarczyk J., Czapor-Irzabek H., Kulazynski M. (2018) Characterization of activated beech wood char-methane storage application. Studia Universitatis Babes-Bolyai Chemia 63 (3), pp. 21-39.

- Kulazynski M, Jablonski S., Kaczmarczyk J., Swiatek L., Pstrowska K., Lukaszewicz M (2018) Technological aspects of sunflower biomass and brown coal co-firing. Journal of the Energy Institute 91(5), pp. 668-675

- Pyshyev, S., Prysiazhnyi, Y., Shved, M., Kulazynski, M., Miroshnichenko, D. (2018) Effect of hydrodynamic parameters on the oxidative desulphurisation of low rank coal. International Journal of Coal Science and Technology 5(2), pp. 213-229

- Jablonski, S.J., Kulazynski, M., Sikora, I., Lukaszewicz, M. (2017) The influence of different pretreatment methods on biogas production from Jatropha curcas oil cake. Journal of Environmental Management 203, pp. 714-719

Marek Kulazynski

The main interest of Dr. Kułażyński over last years encompasses the application of heterogeneous catalysts for environmental protection. Dr. Kułażyński possesses wide experience in preparation and investigation of catalysts for hydroprocessing of coal derived light fractions. He is occupying with investigation of various alternative fuels and diesel fuel derived from vegetable oils for mobile transport. Dr. Kułażyński is also interested in manufacturing, investigation and practical application of catalysts with honeycomb structure especially based on ceramic materials and active carbons for catalytic processes of diesel exhaust gases and flue gases purification. Other areas of his activity are: low- and high temperature denitrification and desulfurization of flue gases, preparation, studying and selection of carriers for denitrification catalysts and VOC combustion as well as preparation and investigation of catalytically active wash-coats on honeycomb structure carriers. Dr. Kułażyński was granted with patents concerning manufacturing catalysts and catalysts supports.

Email:

marek.kulazynski@pwr.edu.pl

Notes/Comments