Bioactive Silicone Composed of Porous 3D Cu-MOF

Do Nam Lee, Ingenium College of Liberal Arts (Chemistry), Kwangwoon University, Seoul 01897, Korea

Hyun-Chul Kim, and  Seong Huh, Department of Chemistry and Protein Research Center for Bio-Industry, Hankuk University of Foreign Studies, Yongin 17035, Korea

Sung-Jin Kim, and Youngmee Kim, Department of Chemistry and Nano Science, Ewha Womans University, Seoul 03760, Korea

Recently, owing to their high porous and regular structure properties, MOFs(Metal Organic Frameworks) make possible to expand in biology [1] and medicine [2]. Transition metal ions and metal nanoparticle containing Cu, Zn, Co, and Ag have gained prominance as substitutes for new antibacterial agent to effect on bacteria [3, 4]. However, it is known excessive metal ions leached from metal nanoparticle would be harmful to the normal tissue as well as to bacteria [5]. To solve theses leakage problems, many researchers tried to trap the metal ion in MOF through coordination of bio active metal ion to organic ligands. New antimicrobial material composed of robust and porous Cu-MOFs are designed in consideration of the inherent characteristics of the metal and organic ligand such as oxidation number, counter ion, the coordination mode, the size and bridging property of the ligand. We introduce here porous three-dimensional Cu-MOF representing antibacterial effect as well as high selective gas sorption synthesized by hydrothermal reaction. Bioactive Cu-MOF containing Cu2 dinuclear units connected by flexible glutarate and 1,2-bis(4-pyridyl)ethane ligands is formulated as [Cu2(Glu)2(μ-bpa)]·3(H2O) (Glu = glutarate, bpa = 1,2-bis(4-pyridyl) ethane), and was crystallize in monoclinic space group (C2/c). The single crystal X-ray study showed that Cu-MOF contains paddle-wheel Cu2 dinuclear units connected by glutarates to form two-dimensional (2D) sheets, and these sheets were bridged by 1,2-bis(4-pyridyl)ethane ligand to form three-dimensional (3D) frameworks. The number of solvent water molecules in MOF was calculated from elemental analysis and TGA. The solvent-free Cu-MOF has 28.3% of void volumes based on the PLATON analysis and contain well-defined 1D channels. Porous 3D Cu-MOF exhibited high selective sorption of quadrupolar CO2 over N2 and H2. The bactericidal rates of Cu-MOF applied on the silicone rubber against E.coli, S. aureus, and MRSA were observed 88.6%, 88.7

% and 81.5%, respectively and Cu-MOF showed  the possibility of new material for bioactive commercial applications.

1.  Horcajada P, et al (2012) Metal-​Organic Frameworks in Biomedicine,

Chem. Rev. 112: 1232-1268.

2.   Horcajada P. et al (2010) Porous metal-​organic-​framework

nanoscale carriers as a potential platform for drug delivery and

imaging Nat. Mater. 9:172-178.

3.  Islas  MS, et al (2014) Antitumoral, Antihypertensive, Antimicrobial,

and Antioxidant Effects of an Octanuclear Copper(II)-Telmisartan

Complex with an Hydrophobic Nanometer Hole. Inorg. Chem.

53:5724−5737.

4.  Lu X, et al (2014) Silver carboxylate metal-organic frameworks with

highly antibacterial activity and biocompatibility.J. Inorg. Biochem. 138: 114−121.

5.  Liu Z, et al (2014) Synthesis of polyethylenimine (PEI ) functionalized

silver nanoparticles by a hydrothermal method and  their

antibacterial activity study, Mater. Sci. Eng. C 42: 31–37.

Do Nam Lee received her B.S. and M.S. from Yonsei University in Chemistry. She earned her Ph.D. from Yonsei University(1992) under the supervision of Prof. Chang Hwan Kim and completed postdoctoral study as a member of the groups of Prof. Robert West at University of Wisconsin-Madison. She worked as visiting scholar at Peking University. She is currently an associate professor at Kwangwoon University, Republic of Korea and mostly focusing on researches of synthesis and application of coordination comlpexes, functional metal organic frameworks, and polymers.

Email:donamlee@hanmail.net

Notes/Comments