Title of the Abstract: The charge effect of insulin PLGA nanoparticles on cell uptake in vitro and bioavailability in vivo

Author Name: Elodie Czuba

Affiliation: UMR DIATHEC, EA 7294, Centre Européen d’Etude du Diabète, Université de Strasbourg (UdS), Boulevard René Leriche 67200 Strasbourg, France

University: Strasbourg

Country: France

Abstract:

Introduction: Poly (D,lactic-co-glycolic) acid (PLGA) particles (NP) are known to be effective drug carrier with a long acting profile, but have less than 20% of bioavailability. The aim of this work was to increase encapsulated insulin bioavailability modifying the surface properties like charge of NPs to improve their interaction with cell membrane.

Material and method: Particles were prepared in presence or not of polyvinyl alcohol (PVA), with Sodium dodecyl sulfate or coated with chitosan chloride in order to play on NPs charge. In vitro internalization was tested on epithelial coculture (Caco-2/RevHT29MTX) by flow cytometry. NPs were then administrated thanks to a pharmaceutical complex vector in vivo by oral route (10, 20 and 50UI) in diabetic rats.

Results: SDS-NPs and 1% PVA-NPs were smaller (141± 3 and 154 ± 24 nm) than chitosan coated NPs with size (236 ± 29 nm) which is increased in comparison to the control (200 ± 9 nm). Compared to classical NPs (PVA+), cells uptake was improved by SDS-NPs, in contrast to without PVA and chitosan coated NPs. Administration by oral route of vehicle contained SDS-NPs 20 and 50UI) reduced glycaemia faster than empty vehicles and vehicles with standard NPs. Negative charge of NPs could interact with cell membrane which is negatively charged too.

Conclusion: Mucoadhesive particles (chitosan) formulation is definitely not the good approach to improve the bioavailability of encapsulated insulin contrary to negative NPs are the most efficient both in vitro and in vivo, and represent a promising formulation for oral insulin delivery.

Biography:

Elodie Czuba, PhD student in “Centre Européen d’Etude du Diabète (CEED)

Research Interests: nanoencapsulation of drugs for a biological application

References: Nazar H, Tsibouklis J. Towards the nasal delivery of insulin. Ther Deliv. 2012;3(11):1241-3.

2.	Xuan B, McClellan DA, Moore R, Chiou GC. Alternative delivery of insulin via eye drops. Diabetes Technol Ther. 2005;7(5):695-8.

3.	Boateng JS, Mitchell JC, Pawar H, Ayensu I. Functional characterisation and permeation studies of lyophilised thiolated chitosan xerogels for buccal delivery of insulin. Protein Pept Lett. 2014;21(11):1163-75.

4.	Sheng J, Han L, Qin J, Ru G, Li R, Wu L, et al. N-trimethyl chitosan chloride-coated PLGA nanoparticles overcoming multiple barriers to oral insulin absorption. ACS Appl Mater Interfaces. 2015;7(28):15430-41.

Mail Id: e.czuba@ceed-diabete.org

Contact Number:+33390201212