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Electrochemical reduction of CO2 to low carbon organic compounds has been considered as a promising method to mitigate the greenhouse effect and produce useful energy carrying chemicals. However, the development of catalyst with high activity, selectivity, and good stability is still the bottleneck to accomplish this goal. Cu based catalysts have been reported to meet such requirement. In this work, we prepared CuO nano needle and CuO/graphene nano-flower catalysts using polyol method. The catalyst was examined using XRD, SEM/EDS and electrochemical testing methods etc. Results indicate that CuO/graphene nano-flower exhibits a high catalytic activity for CO2 conversion to formate with a Faradic efficiency of 60% (Nano needle) and 75% (Nano flower) under -1.1V vs.SHE. We also will demonstrate membrane electrolyte assembly based device for CO2 electrochemical reduction. In where, the CuO/graphene nano-flower catalyst is coated on gas diffusion layer as the cathode.  
[image: image3.png]



Figure 1. a) CuO nano needle and b) CuO/graphene nano-flower catalysts
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Figure 2. Sketch of the CO2 electrochemical reduction device
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