Influence of the chemical changes in the energy properties of several torrefied Portuguese biomasses

Abel Rodrigues

INIAV, Portugal

Leonel Jorge Ribeiro Nunes

DEGEIT - University of Aveiro, Portugal

Abstract

The need of mitigate the emission of greenhouse gases (GHGs) is gaining momentum as the effects of climate change are becoming more noticeable. Also, the predictions are that the world energy consumption will grow by around 56% till 2040.Thereby a mix of policies, coupling the reducing of GHGs with an increasing supply of renewable sources of energy, is needed and woody biomasses, whether derived from forests or shrubs, are an option in Europe among the available renewable energy sources. Biomass torrefaction, although not spread on a larger commercial scale, has attracted major interest in the last 20 years.  This process is very similar to coffee torrefaction, and can be defined as a thermochemical conversion, taking place in the absence of oxygen, at a temperature ranges of about 220ºC to 320ºC, and producing a material with reduced O/C ratio and H/C ratios. Torrefaction is an option for improving biomass properties for fuel application. Biomass undergoes chemical changes reflected on the upgrading of its properties as a biofuel, such as higher calorific power, lower O/C and H/C ratios, lower higroscopicity or better grindability. Objectives of this experimental study were to analyze the effects of torrefaction, under standart conditions of 265ºC, and residence time of 15 minutes in a nitrogen atmosphere and during a total 1h45m heating period, on a set of sixteen woody biomasses provenient from poplar short rotation coppice (SRC) and other Portuguese roundwoods. Average mass loss was higher than 40%. The set of poplar clones and common broom provided torrefied products with higher quality than the set of roundwood forest species. The results on other parameters for proximate and ultimate analysis corroborate this global picture. Correlation analysis showed a higher degree of interconnectedness between LHV and proximate analysis results, for poplar clones and common broom, comparatively with roundwood biomasses.

Biographies

Presenting author details 
Full name: Abel Rodrigues
Session name/ number: day 2, June 15, 4 pm, talks on bio refinery and fuel refineries and lectures on sustainable process product development through green economy; Track 13- Bio based chemistry, Track 13.1- Bio refinery and fuel refineries, Track 13.3- Biomass feedstock and green chemistry

Category: Poster

Email id: abel.rodrigues@iniav.pt

Contact number: 00351214403500

Dr. Abel Martins Rodrigues holds a MsC in Mechanical Engineering (Energy Profile) and PhD in Environmental Engineering, both degrees obtained in Instituto Suprior Técnico of Lisboa, and is a researcher in Portuguese, Instituto Nacional de Investigação Agrária for the last 34 years. His areas of research are now focused mainly in production of forest biomass for energy and in thermo-chemical biomass conversion Technologies. He is author of a book “Princípios fundamentais de physical ecology” (“Fundamental principles of physical ecology”) and author or co-author of about 40 research book chapters, articles and conference proceedings published in international and Portuguese journals.

Dr. Leonel Jorge Ribeiro Nunes holds a PhD in Industrial Engineering and Management, and concluded two Post Doctoral research projects about thermochemical conversion technologies at the University of Beira Interior and at the University of Aveiro. Presently isInvited Assistant Professor at DEGEIT of the University of Aveiro (Portugal), and Researcher at GOVCOPP. His areas of research focus mainly in Biomass Energy and in Thermochemical Conversion Technologies. He is author or co-author of more than 50 research articles published in several reputed international journals and conference proceedings.