# Abstract Title: Influence of double idealized shear flow zones on the torsional resistance in ultra-high performance fibre reinforced concrete beams

Karim F. R, Abu Bakar, B.H., Choong Kok Keong, Aziz, O.Q.

1 Lecturer (University of Sulaimani, Iraq)

2Professor, School of Civil Engineering (Universiti Sains Malaysia, Malaysia)

3 Associated Professor, School of Civil Engineering (Universiti Sains Malaysia, Malaysia)

4 Professor, College of Engineering,( Salahaddin University, Iraq)

Abstract

The  influence  of  double  idealized  shear  flow  zones  on  the  torsional  resistance  for  under-reinforced ultra-high performance fiber reinforced concrete beams subjected to pure torsion was investigated. The concrete beams section was reinforced with two layers of transverse and  longitudinal  reinforcements, which located  in  the  idealized  shear  flow  and tension  zones.  To  study  the  influence  of  double reinforcements on  the  torsional  resistance  of  under-reinforced ultra-high performance fiber reinforced concrete beams,  four  beams were  cast and  tested under pure  torsion. The beams designed in accordance with the American Concrete Institute. The main transverse and longitudinal reinforcements in  the shear flow zone are kept constant  in  the beams while the transverse reinforcement in the idealized tension zone was covered different percentage of this zone. The test results were confirmed that the torsional resistance at peak loads was improved up to 25.14%, due to covering 85.4% of the idealized core zone area by reinforcement. In addition, the twisting angle at peak loads decreased up to 34.09% due to enhancement in stiffness of the beam’s section  up to 82.45%. The value of shear strain was reduced up to 49.86% due to the enhancement of the strain in longitudinal reinforcement while the strain in transverse reinforcement was reduced at peak load. The spacing between spiral cracks and their inclination angle  were increased due to the inclusion of reinforcement in the core zone area. The space truss model was modified to cover the influence of reinforcement in the idealized tension zone. The proposed modification model was shown that it has a good agreement with the test results.

Keywords— Double shear flow zone, pure torsion, space truss analogy, and ultra-high performance fiber reinforced concrete

Professional Biography

Karim, F. R. has completed his PhD at the age of 42 years from University Sains Malaysia.  He  received his BSc  from University of Salahaddin;  and MSc  from  University  of  Sulaimani. He is  a  research  engineer  at  the Concrete  Structures  Division .His research  interests  include  behaviour  and strength of reinforced concrete beams under combined  action  and  pure  torsion  and  the mechanical properties of high strength concrete. He  is a lecturer in the University of Sulaimani, College of Engineering, Civil Engineering Department. He has published 17 papers in reputed journals and has been serving as an editorial board member and reviewer of reputed journals.

Email Id: f1974e1997m2004@gmail.com

Any Comments: