Title: Preparation of nano-EGCG loaded in situ gel for significantly enhancement of stability and long-term delivery

Name: Shufang Nie

Nutrilite Health Institute, Amway, Buena Park, CA 90622

Purpose: To prepare a new EGCG delivery system by utilizing nano-EGCG loaded thermoreversible in situ hydrogel to enhance EGCG stability and resident time in adipose tissue ablation.  The present study may poetically provide a better way to achieve a maximum therapeutically benefit of nano-EGCG on abdominal obesity treatment.

Methods: Nano-EGCG was prepared using a phase inversion-based process by encapsulating EGCG into chitosan coated nanostructured lipid carriers. Nano-EGCG was then dispersed into thermoreversible Pluronic® F127-based hydrogel by cold method. The sol-gel transition temperatures were evaluated using inverted tube method. The stability of native EGCG, nano-EGCG solution, nan-EGCG loaded gel were investigated in 1×PBS (pH=7.4) at 37°C for 15 days.  In vitro EGCG release from nano-EGCG loaded in situ gel were detected by a membrane-less diffusion method. In vitro cytotoxicity and cellular triglyceride accumulation in 3T3-L1 adipocytes cells were determined by MTT and an enzymatic method, respectively.

Results: The size of nano-EGCG obtained in this study was about 50nm in diameter and PI values was relative low (<0.3) which indicates a high level of uniformity. Chitosan was used as a coating material to enhance the stability and bioactivity of nano-EGCG. The inverted tube method showed 20% of F127 PBS (pH 7.4) solution with lipid nanocarrier amount equal to or lower than 6.25% exhibited reversal thermal gelation, transforming from liquid into a semisolid gel in 1–2 minutes at the characteristic sol-gel transition temperature 35.0°C. When nano-EGCG was incorporated into an in situ thermoreversible Pluronic® F127-based hydrogel, the stability of EGCG was dramatically improved which is in the order: nano-EGCG loaded gel > nano-EGCG solution > native EGCG. The stability of EGCG can be further improved by addition of 0.05%EDTA-Na in the formula. The results showed that 80.3% of EGCG was still remained in nano-EGCG loaded gel while 20.0% and 0% of EGCG could be detected in nano-EGCG and native EGCG solution, respectively, after storing in neutral 1×PBS at 37°C for up to 15 days.  As compared to 20uM of native EGCG, nano-EGCG with 0.05%EDTA-Na at the same concentration produced a lower triglyceride accumulation in mature 3T3-L1 adipose cells. In vitro release study showed that a steady sustained release of EGCG was realized by incorporating nano-EGCG into an in-situ hydrogel, which produced a desired EGCG concentration range (10-30uM) in the target tissue with the longer resident time (30 hours) for maintaining the continued anti-adipogenic effects. After treating mature 3T3-L1 adipose cells with 20uM of native EGCG, nano-EGCG or nano-EGCG loaded hydrogel (20%F127) for 48hours, cell viability was more than 85% among all treatments, which indicate they had a very low level of cellular toxicity.

Conclusion: Experiments in vitro in the present study demonstrated that the combination of nano-EGCG with in situ gel can dramatically enhance the stability and produced a localized and sustained delivery of EGCG to adipose tissue ablation, which may potentially provide a better way to reduce abdominal fat through intraperitoneal injection in abdominal obesity without inducing tissue toxicity.

Acknowledgments: The author would like to thank professor Wang Shu (Department of Nutritional Science, Texas Tech University, Lubbock, TX) for her helpful advice and experiment support on my initiation into work on this study.