LASER WRITING OF CRYSTALLINE TRACKS IN BARIUM TIANOSILICATE GLASS BY FEMTOSECOND LASER BEAM WAIST WITH ELLIPTICAL CROSS SECTION

Ivan A. Moiseev, Alexey S. Lipatiev, Sergey V. Lotarev, Tatiana O. Lipateva, Vladimir N. Sigaev

Mendeleev University of Chemical Technology of Russia, Russia

Abstract (not more than 300 words)

Barium titanosilicate glass system is of particular interest for of space-selective laser-induced precipitation of Ba2TiSi2O8 fresnoite crystals possessing high piezoelectric and pyroelectric properties. Recently, we have investigated the process of femtosecond laser writing of crystalline tracks in the bulk of 40BaO·20TiO2·40SiO2 (mol.%) glass and established the dependence of crystalline tracks morphology on the laser beam scanning speed and pulse energy.

In the present study, we report direct laser writing of Ba2TiSi2O8 crystalline tracks by the femtosecond laser beam with an elliptical cross-section of the waist formed by anamorphic prism pairs as compared to the conventional Gaussian beam. It is found that applying the anamorphic prism pair allows to increase the maximum laser writing speed enabling homogeneous crystalline track growth. The longitudinal and transverse cuts of the laser-written crystalline tracks have been investigated by polarized optical microscopy, Raman spectroscopy and transmission electron microscopy. It is for the first time revealed that the fine annealing of the laser-written crystalline tracks “erases” a lot of defects in their structure. These results pave the way to the formation of high-quality crystalline waveguides in glass and their application in novel photonic and optoelectronic devices.

This study was financially supported by the Russian Foundation for Basic Research (grants 16-03-00541 and 16-33-60081) and Russian Science Foundation (grant 17-73-20324).

Keywords— Ba2TiSi2O8 crystal, fresnoite, glass crystallization, femtosecond laser

Professional Biography (100-150 words)

Ivan A. Moiseev is a bachelor student of Mendeleev University of Chemical Technology of Russia. The research work has been started in 2016 in the field of the glass synthesis and modification the microstructure by the femtosecond laser beam. He has been working in the rank of laboratory assistant in the International Center of Laser Technology. He has publications in a literary miscellany of the International conference of students and graduate student also in the Glass and Ceramics journal. He also has a patent in the field of precipitation of nano- and microcrystals in the barium titanosilicate glass system using the femtosecond laser irradiation. Now he is writing his diploma work in the same research scope.

Email Id: mois.chem@yandex.ru

Contact Number: +7 977 168-78-35

Any Comments: