Synthesis of plated-like Bi4Ti3O12 templates using TiO2 nanostructures

Le Dai Vuong, Ph.D, School of Engineering and Technology from Hue University, Hue city,Vietnam

Pai Chun Wei, Prof, Department of Materials Science and Engineering from National Cheng Kung University, Taiwan

### Abstract

Plated-like Bi4Ti3O12 templates were synthesized through the molten salt method using TiO2 nanostructures. The TiO2 nanostructures was obtained by an ultrasound-assisted method using TiO2 commercial particles and sulfuric acid, as in our previous work. The as-prepared Bi4Ti3O12 templates were composed of plate-like morphologies of lengths 5–20 µm and widths 0.5–1 µm. The X-ray diffraction (XRD) analysis revealed the orthorhombic perovskite structure of Bi4Ti3O12 templates and reported no other impurities in the temperature range of 950–1050C. The presence of orthorhombic perovskite structure (the space group Fmmm) in all the Bi4Ti3O12 templates was confirmed by the Rietveld refinement technique. These results are in accordance with Raman spectroscopy analysis. The degree of orientation and the relative density of the synthesized templates increased with the increasing sintering temperature, and their highest values were achieved at 1050C. Further, the EDS spectrum at 1050 C expounded that the obtained Bi4Ti3O12 templates mainly consisted of Bi, Ti, and O elements.  .

Image

### Recent Publications (minimum 5)

- Dao Anh Quang, Le Dai Vuong (2022), Enhanced piezoelectric properties of Fe2O3 and Li2CO3 co-doped Pb[(Zr0.48Ti0.52)0.8(Zn1/3Nb2/3)0.125(Mn1/3Nb2/3)0.075]O3 ceramics for ultrasound transducer applications, Journal of Science: Advanced Materials and Devices, 2022, 7.2: 100436.

- Le Dai Vuong (2022), Densification behavior and electrical properties of the PZT-PZMnN-based ceramics prepared by two-step sintering, Journal of Materials Science: Materials in Electronics 33 (9), 6710-6721.

- Phan Dinh Gio, Le Dai Vuong, Le Tran Uyen Tu (2021), Enhanced piezoelectric and energy storage performance of 0.96(K0.48Na0.48Li0.04)(Nb0.95Sb0.05)O3–0.04Bi0.5(Na0.82K0.18)0.5ZrO3 ceramics using two-step sintering method, Journal of Materials Science: Materials in Electronics 32, 13738–13747.

- Phan Dinh Gio, Le Dai Vuong, Vo Thanh Tung (2021), Phase transition behavior and electrical properties of lead-free (1-x)KNLNS-xBNKZ piezoelectric ceramics. J Electroceram (2021).

- Nguyen Truong Tho, Le Dai Vuong (2021), Study on the strain behavior and piezoelectric properties of lead-free Bi0.5(Na0.8K0.2)0.5TiO3 ceramics modified with Sn4+ ions, Journal of Materials Science: Materials in Electronics, 1-11.

Photograph

Biography

Le Dai Vuong was born in Quang Binh province, Vietnam, in 1983. He received the Ph.D degree in piezoelectric ceramic from Institute of Materials Science, Vietnam Academy of Science and Technology in 2014. He has been a lecturer and researcher at Hue University, Hue city, Vietnam. His research interests are preparation and characterization of piezoelectric ceramics

Email: ldvuong@hueuni.eduvn

Notes/Comments: