# Improvement in wear resistance of AISI H13 Steel by Pack-Boronizing Method

Niketan Manthani1, a, , Akshay Joshi2, b, , Vinayak Pawar 3, c , Rajkumar Singh4, d

1Niketan Manthani aNiketan.Manthani@bharatforge.com  (Kalyani Centre for Technology and Innovation Bharat Forge Ltd Pune 411036 Maharashtra, India)

2 Akshay Joshi bakshay.joshi@bharatforge.com (Kalyani Centre for Technology and Innovation Bharat Forge Ltd Pune 411036 Maharashtra, India

3 Vinayak Pawar  cvinayak.pawar@bharatforge.com  (Kalyani Centre for Technology and Innovation Bharat Forge Ltd Pune 411036 Maharashtra, India)

4Rajkumar Singh dRajkumar.Singh@bharatforge.com (Kalyani Centre for Technology and Innovation, Bharat Forge Ltd Pune 411036, Maharashtra, India)

Abstract

Boronizing has been employed to increase the service life of parts such as orifices, ingot molds and dies for hot forming made of AISI H13steel. In this study, pack boronizing was done of AISI H13 Steel. Samples were boronized at 950OC for 0.5 hr, 1 hr and 4 hr. In all the specimens both the iron boride layers (FeB, Fe2B) were formed. It was seen that as soaking time increases, thickness of boride depth also increases. Continuous decrease in the hardness from surface to unboronized layer was observed. Boronized specimen at 950OC for 4 hr showed better hardness and so was studied for further investigation. This study was compared with Nitrocarburized cycle at 550OC for 12 hr. High wear resistance was observed in the boronized specimen than in nitrocarburized sample. COF was ranging from 0.40 to 0.70.

Keywords— Pack Boronizing, Boride layers, Wear resistance, Hardness, COF

Professional Biography

I am Niketan Manthani, have done my Post graduation from Metallurgy from IIT Bombay with experience in the industry across, metallurgy, Quality Assurance, Mechanical Functions, Production Line, Operations, Safety. My research interests include surface treatment process, failure analysis, new product development and currently spearheading as metallurgical researcher with Bharat Forge Limited, Pune. Bharat Forge Limited is metallurgical driven company which has expertise in material science and manufacturing process. Bharat forge is into many fields, and at present it is moving into non-automotive sector too. We are exploring our research into numerous fields ranging from Nanotechnology to Megastructures. Bharat Forge is rightly called the biggest forging company in world.

Email Id: Niketan.Manthani@bharatforge.com