Synthesis and characterization of solids with strong acidic and basic properties, applied as catalysts in the synthesis of Ionones

González Jiménez Rodrigo Rodolfo1, Portillo Reyes Roberto2, Hernández Espinosa Miguel Ángel3.

1PhD student in Chemical Sciences (Benemérita Universidad Autónoma De Puebla (BUAP), MX)

2Portillo Reyes Roberto (School of Chemical Sciences, BUAP, MX)

3Hernández Espinosa Miguel Ángel (Research Department in Zeolitas, ICUAP, MX)

Abstract

Ionones are fine compounds of isoprenoid nature of high commercial value that can be synthesized in two stages catalyzed in homogeneous phase: aldol condensation between citral and acetone catalyzed by a mineral base to produce pseudoionone (PI), and cyclization of pseudoionone catalyzed by mineral acid . This route generates operational problems and environmental pollution, which can be avoided or minimized by the use of heterogeneous catalysts. In the present work we report the synthesis of ionones using mixed oxides (MgO-Al2O3, CaO-Al2O3, SrO-Al2O3, MgO-CaO-Al2O3, CaO-SrO-Al2O3) and sulfated silica as possible catalysts. The materials were characterized by the techniques, EDS, DRX, SEM, DTP and nitrogen fisisorción. The reaction mixtures were analyzed by GC-MS technique, obtaining PI with yield up to 79% with the CaO-Al2O3 oxide, while the best ionone yield was obtained using silica SBA-15 treated with 1M aqueous solution in H2SO4: 16 % β-ionone at 60 ° C and 17% α-ionone at 80 ° C, under reflux conditions. The production of PS and retinoles during the condensation reaction suggests that it is possible to synthesize oxide materials with acid / base properties that promote ionone synthesis in a single step.

Keywords — Engineering materials, heterogeneous catalysis, ionone synthesis, material science.

Professional Biography

Rodrigo González, 34 years old, a PhD student in chemical sciences, a master's degree in semiconductor devices and a degree in chemical engineering. I have worked as a science teacher in different institutions an participation in international congresses as Japan or Mexico.

Email Id:pigoyoyo@hotmail.com

Contact Number: 01522211178483