# Ferroelectric Barium Titanate and Barium Strontium Titanate

Thin Films Monolithically Integrated on Silicon

Bryce I. Edmondson, Edward L. Lin, John G. Ekerdt

1 First Author Affiliation (University of Texas at Austin, USA)

2Second Author Affiliation (University of Texas at Austin, USA)

3Third Author Affiliation (University of Texas at Austin, USA)

Abstract

This talk explores the monolithic integration of perovskite oxides on Si(001) for applications in silicon nanophotonic devices and low-power transistors. Barium titanate (BTO) films, and BTO/LaxSr1-xTiO3 (x ≤ 0.15) perovskite heterostructures are grown on strontium titanate (STO)-buffered Si(001) using atomic layer deposition at 225 °C. X-ray diffraction confirms compressive strain in BTO films for films as thick as 66 nm with the c-axis oriented out-of-plane. Post-deposition annealing above 650 °C leads to in-plane c-axis orientation. Piezoresponse force microscopy (PFM) verified the ferroelectric (FE) switching. Electrical and electro-optic measurement of the Pockels coefficient confirm BTO film FE behavior at the µm-scale. The BTO/LaxSr1-xTiO3 perovskite heterostructures permit examination of a quantum metal between Si(001) and a FE film.  These heterostructures are strained to Si(001) and are c-axis out-of-plane.  PFM demonstrates the BTO FE behavior on the La-doped STO. Sheet resistance and capacitance-voltage measurements establish the conductivity of the La-doped STO layer and show the potential for these films in negative capacitance field effect transistors.  Optical second-harmonic generation in reflection characterized variations in the second-order nonlinear optical susceptibility of 10 to 50 nm-thick Ba1-xSrxTiO3 (BSTO) alloy films grown epitaxially on SrTiO3(001) as Sr molar ratio x changed from 0 to 1. The results reveal composition and strain control can optimize ferroelectric and electro-optic properties of BSTO films grown on STO buffer layers.  Insight gained through the second-harmonic generation studies was used to inform the composition and growth of BSTO films by atomic layer deposition and chemical solution deposition on (STO)-buffered Si(001) to explore their EO properties as lattice strain and c-axis orientation are varied.

Keywords—Atomic layer deposition, electro-optic properties, ferroelectric properties, perovskite film,

Professional Biography

John G. Ekerdt completed his PhD at the University of California, Berkeley in 1979 and is Associate Dean for Research in Engineering and the Dick Rothwell Endowed Chair in Chemical Engineering at the University of Texas at Austin.  He served as Chemical Engineering Department Chair from 1997-2005.  He has more than 310 refereed publications, two books and three book chapters, and seven U.S. patents.  He has supervised 52 Ph.D. and 9 M.S. students.  Using chemical and kinetic probes to unravel reaction pathways, mechanisms and reaction rates, his research explores: 1) the kinetics of single crystal, nanoparticle and ultrathin film growth, 2) the chemistry that controls film and nanoparticle nucleation on surfaces, and 3) the relationships between precursor molecular structure, its reactivity and the properties of the electronic material that is grown.  Current research interests focus on the surface, growth and materials chemistry of metal, dielectric and perovskite films and nanostructures.

Email Id: ekerdt@utexas.edu

Contact Number:1-512-471-4689