Fabrication of PAN/Fe3O4 nanofibers: photocatalysis and characterization antimicrobial properties

Mogomotsi N. Ranku1,2, Omolola E. Fayemi1,2,*, Elias E. Elemike1,2,3

1Department of Chemistry, Faculty of Natural and Agricultural Sciences, North-West University (Mafikeng Campus), Private Bag X2046, Mmabatho 2735, South Africa.

2Material Science Innovation and Modelling (MaSIM) Research Focus Area, Faculty of Natural and Agricultural Sciences, North-West University (Mafikeng Campus), Private Bag X2046, Mmabatho 2735, South Africa.

3 Department of Chemistry, College of Science, Federal University of Petroleum Resources,  P.M.B 1221, Effurun, Delta State, Nigeria.

*Corresponding author: email: Omolola.Fayemi@nwu.ac.za or omololaesther12@gmail.com

Abstract

The present study aimed at green mediated synthesized iron oxides nanoparticles from peel extracts of pomegranate plant which is of immense medical, biological, and environmental value. The synthesized nanoparticles were characterized by using FT-IR, UV-Visible spectroscopy, SEM and TEM. FTIR revealed OH characteristics peaks at 3271 cm-1 and 1600 cm-1 from the plant extract which serves as reducing agent for synthesis of Fe3O4 nanoparticles. SEM showed the morphology of Fe3O4 NPs. Photocatalysis studies reveal that Fe3O4 /PAN nanofibers and Fe3O4 nanoparticles showed increased efficiency towards the degradation of methylene-blue dye, which proof their potential application in waste water treatment. Synthesized Fe3O4 nanoparticles has degradation efficiency of 71.36 % and the nanofibers exhibited efficiency of 22.68 % towards methylene blue (MB) dye. However, further kinetic analysis of the degradation process put PAN/Fe3O4 nanofibers at a better correlation coefficient of 0.9239 than the Fe3O4 nanoparticles. The green mediated Fe3O4NPs also exhibit an excellent antimicrobial activity against some selected pathogens conducted by disc diffusion method.

Key words: Photocatalytic, Antimicrobial, Nanofibers, Pomegranate, Electrospinning

Professional Biography

Omolola Esther Fayemi has her expertise in synthesis, characterization and application of nano-based materials through both chemical and green mediated synthesis. The synthesized nanomaterials are applied in electrochemical sensors for analytes in biological and environmental medium and also for wound dressing. She is very passionate about her work. She has postgraduates and postdoctoral fellow under her leadership. She is a young researcher having collaborations with scholars in local and internationally institutions.

*Corresponding author: Omolola.Fayemi@nwu.ac.za; Tel: +27183892440

Full Name: Omolola Esther Fayemi

Email Id: omololaesther12@gmail.com or Omolola.Fayemi@nwu.ac.za

Contact No: Tel: +27183892440

Social Network Details (Esther Fayemi):