Abstract Title: Preparation of Polyaniline (PANI) , PANI/ MgO(30%) and PANI /MgO(40%) nanocomposites as a sensing material for the fabrication of a LPG sensor

Neetu Singh1, Prabhat Kumar Singh1 and  Poonam Tandon1

1 University of Lucknow, Lucknow-India

Abstract

Polyaniline (PANI), PANI/ MgO(30%) and PANI /MgO(40%) were successfully synthesized. Multifarious characterizations techniques were used to scrutinize the morphological, structural, elemental and optical properties of PANI and PANI/MgO nanocomposites such as SEM (Scanning electron microscopy), XRD (X-ray diffraction), EDX (Energy dispersive X-ray) analysis and FTIR (Fourier transform infrared) spectroscopy. Analysis of SEM results of PANI and PANI/MgO nanocomposites evinced the large number of pores on the surface of their morphology which shows that materials have the high porosity. This high porosity contributes to enhance the reactivity of the materials which is an advantage in the context of LPG sensing. The crystallite size was calculated employing XRD pattern of PANI, PANI/MgO(30%) and PANI/MgO(40%) i.e. 2 nm, 35 nm and 43 nm respectively. Further, all aforementioned synthesized materials were also deployed for LPG sensing. Significant parameters like response time, recovery time and sensitivity of all aforesaid materials were calculated. LPG sensing results manifest that PANI/MgO(40%) nanocomposite is a promising material for LPG sensors because of its excessive sensitivity towards LPG in comparison to PANI and PANI/MgO(30%).

Keywords—Polymer Nanocomposite, SEM, XRD, LPG sensing

Professional Biography

Ms. Neetu Singh has received her B.Sc. degree in 2010 and M.Sc. degree in 2012 from Chaudhary Charan Singh University, Meerut, Uttar Pradesh, India. Presently, She is a senior research fellow (CSIR-SRF) and pursuing her Ph.D. under the supervision of Professor Poonam Tandon, Department of Physics, University of Lucknow. She is working in the research area of “Synthesis and Characterizations of Polymer Nanocomposites and their Applications  as a Gas Sensing materials ”. She has published two papers in reputed journals.

Recent Publications (up to 5)

- Neetu Singh, Prabhat Kumar Singh, Anuradha Shukla, Satyendra Singh and Poonam Tandon, "Synthesis and Characterization of Nanostructured Magnesium Oxide: Insight from Solid-State Density Functional Theory Calculations, Journal of Inorganic and Organometallic Polymers and Materials,Vol. 26, pp-1413-1420, 2016, ISSN- 1574-1443, Springer, Impact Factor: 1.508

- Prabhat Singh, Neetu Singh, Satyendra Singh, Mridula Singh, Poonam Tandon, " Synthesis of ZnO nanostructures via sol-gel method and their nanostructural and optical characterization" has been published in the  e-book of ICOPVS-2016 proceedings, ISBN-978-93-5267-364-3

Email Id: neetusingh201989@gmail.com

Presenting author details

Full name: Neetu Singh

Contact number: +919044055861

Session name/ number: Nano Devices and structured materials (Track 3)

Category: (Oral presentation)