# Tunable work function and optical nonlinearity of nanocomposites

Dr AVESH KUMAR, Prof A TANEJA, PhD, Dr. B. R. Ambedkar University, Agra, Uttar Pradesh, India

Prof R P SINGH, PhD, Physical Research Laboratory, Navrangpura, Ahmedabad, India

T MOHANTY, PhD, chool of Physical Sciences, Jawaharlal Nehru University, New Delhi, India

### Abstract

The nonlinear optical response of Au-TiO2 nanocomposites is due to pure electronic transfer effects in Au nanoparticles. The observed nonlinearity is due to the dielectric constant of Au, which is due to the surface plasmon resonance and surface polarization between Au nanoparticles and TiO2. The dielectric constant of Au shows maximum value at 532 nm wavelength (2.33 eV). Surface plasmon resonance effect of Au nanoparticles is directly related to the metal dielectric constant, therefore it is increased. The increase in surface plasmon rsonance of Au-TiO2 nanocomposites can be observed from UV-visible absorption spectra. The optical nonlinearity depends strongly on the dielectric constant of Au. Therefore, the optical nonlinearity increases with the increase in surface plasmon resonance peak. The absorption peak of surface plasmon resonance at 544 nm is inversely proportional to the work function. Therefore, we can say that the Au dopant decreases the work function that effectively increases the surface plasmon resonance absorption peak at 544 nm, so that the nonlinear response is enhanced. The systematic change in the work function with Au concentration plays a major role in optical nonlinearity. The estimated optical nonlinearity was found to increase from 3.80×10-6 to 9.69×10-6 esu with increase in Au concentrations from 0 to 1.010-2 mole. This observed increment in nonlinearity is due to the enhancement of local electric field created by excitation of surface plasmon resonance that affects the work function. Therefore, the surface plasmon resonance and work function help in tuning the optical nonlinearity. The tunable nonlinear optical response of the Au-TiO2 nanocomposites may find applications in nonlinear optics at wavelength 532 nm and the development of materials for generating the higher order harmonics.

### Image

Recent Publications

- Kumar A, Mohanty T (2014) Electro-optic modulation induced enhancement in photocatalytic activity of N-doped TiO2 thin films. Journal of physical chemistry C 118: 7130-7138.

- Takai A, Kamat P V (2011) Capture, store, and discharge. shuttli photogenerated electrons across TiO2-silver interface ACS Nano 5: 7369-7376.

- Kumar A, Patel AS, Mohanty T. (2012) Correlation of photodegradation efficiency with surface potential of silver-TiO2 nanocomposite thin films. Journal of Physical Chemistry C 116: 20404-20408.

- Boyd R W, Shi Z, Leon I D (2014) The third-order nonlinear optical susceptibility of gold. Optical Communication 326: 74-79.

- Bahae MS, Said AA, Wei T-H, Hagan DJ, (1990) Stryland EWV Sensitive measurement of optical nonlinearities using a single beam 26: 760-769.

Photograph

Biography

Myself, Dr. Avesh Kumar am currently a post-doctoral Fellow at Dr. B. R. Ambedker, University, Agra. I have also done PDF work at Physical Research Laboratory, Ahmedabad, India. I did Ph.D. in material science form School of Physical Sciences, Jawaharlal Nehru University, New Delhi, India. My research work is related to synthesis of metal-oxide nanoparticles and growth of semiconductor nanocomposite thin films, study of their structural, optical and electrical properties.

I have published many research papers in reputed international journals with good impact factor. I have visited University of Marseille, Aix-en-Provence, France to present my research work in international conference.

Email: link.avesh@gmail.com

Notes/Comments: