Antibacterial activity of gold nanorods against Staphylococcus aureus and Propionibacterium acnes: misinterpretations and artifacts.

Nouf N Mahmoud1, Alaaldin M Alkilany1, Enam A Khalil1, Amal G Al-Bakri1

1 Department of Pharmaceutics and Pharmaceutical Technology, School of Pharmacy, The University of Jordan, Amman, Jordan

Abstract (not more than 300 words)

The antibacterial activity of gold nanorod (GNR) suspensions of different surface functionalities was investigated against standard strains of Staphylococcus aureus and Propionibacterium acnes, taking into consideration two commonly "overlooked" factors: the colloidal stability of GNR suspensions upon mixing with bacterial growth media and the possible contribution of "impurities/molecules" in GNR suspensions to the observed antibacterial activity. The results demonstrated that cationic polyallylamine hydrochloride (PAH)-GNR were severely aggregated when exposed to bacterial growth media compared to other GNR suspensions. In addition, the free cetyltrimethylammonium bromide (CTAB) present in GNR suspensions is most likely the origin of the observed antibacterial activity. However, the antibacterial activity of GNR themselves could not be excluded. Probing these two critical control studies prevents misinterpretations and artifacts of the antibacterial activity of nanoparticles. Unfortunately, these practices are usually ignored in the published studies and may explain the significant conflicting results. In addition, this study indicates that GNR could be a promising candidate for the treatment of skin follicular diseases such as acne vulgaris.

Keywords: antibacterial activity, supernatant, gold nanorods, colloidal stability, artifacts, acne vulgaris

Professional Biography

Dr. Nouf Nawaf Mhmoud completed a Bsc. in Pharmacy (the University of Jordan), a Msc. in Clinical Pharmacy (the University of Jordan) and a PhD in Pharmaceutical Technology (the University of Jordan) befor joining the academic staff at Al-Zaytoonah University of Jordan. Dr. Mahmoud is an Assisstant Professor of Pharmaceutics at the faculty of Pharmacy and a member of Quality Assurane committee at the faculty. Dr. Mahmoud's research focuses on the Nanotechnology and its biomedical applications, understanding the nano-bio interface and in particular the gold nanoparticles-skin interactions and developing advanced trasdermal delivery nano systems.