## Effect of humidity on mechanical, thermal and barrier properties of EVOH films

A. Blanchard1,*, F. Gouanvé 1, E. Espuche1

1 Ingénierie des Matériaux Polymères, UMR CNRS 5223, IMP@Lyon1

Université de Lyon

France

# Abstract:

Ethylene-vinyl alcohol (EVOH) copolymers are semi-crystalline materials composed of hydrophobic segments of polyethylene (PE) and hydrophilic segments of polyvinyl alcohol (PVOH). Due to its high barrier properties to gases, hydrocarbons and organic vapours at drying state [1], EVOH is more and more used in food packaging applications, allowing to extend the life span of the products [2]. Nevertheless, the major disadvantage of EVOH is its moisture content sensitivity that causes a significant decrease in the barrier properties in high relative humidity environments [3].

The main objective of this study is to get a better understanding of the mechanism of water sorption molecules in these copolymers determining the consequences on the mechanical, thermal, water and oxygen barrier properties. Consequently, these properties were analysed at several water activities (aw) ranging from 0 to 1 on films elaborated from a 32% ethylene containing copolymer.

Water vapour sorption behaviour, corresponding to a BET II type, reveals the sorption of water molecules on polar sites (Langmuir contribution) at low activities and the formation of water clusters at high activities [4].

GAB modelized isotherm[5] combined with the use of the clustering theory from Zimm & Lundberg[6] underline the existence of a critical water activity close to 0.5 corresponding to the presence of one water molecule linked every ten PVOH amorphous units. A strong modification of the mechanical and permeation properties was observed starting from this critical point, showing how important is the understanding of the water sorption mechanism and the consequences on the properties.

References

[1] K. Khanah Mokwena, J.Tang, Food Science and Nutrition, 2012, Vol 52, 640-650

[2] J.M Lagaron, E. Giménez, B. Altava, V. Del-Valle, R. Gavara, Macromolecular Symposia, 2003, Vol 198, 473-482

[3] Z. Zhang, I.J. Britt,  M.A. Tung, Journal of Applied Polymer Science, 2001, Vol 82, 1866-1872

[4] D. Cava, L. Cabedo, E. Gimenez, R. Gavara, J.M. Lagaron, Polymer Testing, 2006, Vol 25, 254-261

[5] S. Basu, U. S. Shivhare, A. S. Mujumdar, Drying Technology, 2006, Vol 25, 917-930

[6] J.L. Lundberg, Pure and Applied Chemistry, 1972, Vol 31, 261-281

# Biography:

In the final year of my phD, my researches are taking place at the IMP laboratory (Ingénierie des Matériaux Polymère) at Villeurbanne (France). This work is financially supported by FUI (Fonds unique Interministériel) in collaboration with several industrial and scientific partners. This project named NOX II is dealing with the improvement of the barrier properties of EVOH films for food packaging applications, in order to extend the life span of the products.

Research Interests: Thermoplastic polymers characterization, water vapour sorption, oxygen barrier properties, mechanical properties, plasticization effects.

References: Blanchard, A., Gouanvé, F. & Espuche, E. Effect of humidity on mechanical, thermal and barrier properties of EVOH films. J. Membr. Sci. 540, 1–9 (2017).

Mail Id: anthony.blanchard@live.fr

Contact Number: 0472432715

Suggestions of colleagues/Professors/scholars to send invitation (if any)

Suggestions of Sessions in the conference (if any)