# Exploration of dye adsorption using nanoporous Zn(II) coordination polymers

Betül Tuba Gemici*, Engineering Faculty, Bartın University, Turkey

Fatma Yetiren, Engineering Faculty, Bartın University, Turkey

Handan Ucun Özel, Engineering Faculty, Bartın University, Turkey

Onur Şahin, Sinop University, Turkey

Okan Zafer Yeşilel, Eskişehir Osmangazi University, Turkey

Andrew D. Burrows, Department of Chemistry, University of Bath, UK

Güneş Günay Sezer*, Vocational School of Health Services, Bartın University, Turkey

### Abstract

### Statement of the Problem: Dyes are used extensively as colorants in the manufacturing process of textiles, leather, paper, food, cosmetics, printing, plastics and pharmaceuticals [1]. The occurrence of dyes in the environment may lead to serious ecological and health problems [2]. There are many methods to remove dyes and, among these, adsorption is considered to be one of the best due to its high effectiveness, efficiency, simple design and low cost [3]. Coordination polymers (CPs) that have tunable chemical and physical properties excel at dye adsorption and capacities greatly exceed those of conventional adsorbent materials such as activated carbons and zeolites [3]. Although numerous CPs have been explored for dye removal from solution, to date there has been no systematic study concentrating on the effect of the dye charge and size [4-5].

### Methodology & Theoretical Orientation: In this work, neutral zinc-based CPs have been synthesized and structurally characterized. Moreover, the adsorption of Methylene blue (MB) and Eriochrome Black T (EBT) was studied, with the dyes selected to represent different sizes and charges.

### Findings: Complexes [Zn(μ-mpda)(µ-mbix)]n (1) and {[Zn(μ-mpda)(µ-mbix)]·2H2O}n (2), mpda=1,3-phenylenediacetate and mbix=1,3-bis(imidazol-1-ylmethyl)benzene), were found to form interpenetrated three-dimensional and two-dimensional coordination networks, respectively (Fig.1). When MB was used in the adsorption experiments carried out with the batch system, there was no removal of the dye from solution after 3 h but efficient removal was observed with EBT. The results indicated that the removal efficiency of EBT reached about 91% after 3 h for 2.

### Conclusion & Significance: Two new coordination polymers have been successfully synthesized under solvothermal conditions by reaction of H2mpda, mbix and a Zn(II) salt. Different reaction temperatures were found to trigger different assembly processes, and the two neutral CPs, 1 and 2, differed from each other in the coordination environment and framework, exhibiting distinct adsorption behaviors toward MB and EBT. The pore dimensions and pore volume were lower in 1 due to interpenetration, and this showed poorer dye uptake. In contrast, 2 is a potent candidate for dye removal, and it is selective for EBT over MB.

### Image

| (a) | (b) |
| --- | --- |

Figure 1. (a) View of the 3D framework in 1 and (b) the 2D framework in 2

Recent Publications

- Wang X, Zhao J, Le M, Lin H, Liu G, Wang X (2016) A series of bis(pyridyl)-bis(amide)-modulated metal-1,2-phenylenediacetate coordination polymers: construction and selective dye adsorption. CrystEngComm, 18:9316-9324.

- Günay Sezer G, Arıcı M, Erucar I, Yeşilel OZ, Ucun Özel H, Gemici BT, Erer H (2017) Zinc(II) and cadmium(II) coordination polymers containing phenylenediacetate and 4,4′-azobis(pyridine) ligands: Syntheses, structures, dye adsorption properties and molecular dynamics simulations. Journal of Solid State Chemistry 255:89–96

- Bibi R, Wei L, Shen Q, Tian W, Oderinde O, Li N, Zhou J (2017) Effect of Amino Functionality on the Uptake of Cationic Dye by Titanium-Based Metal Organic Frameworks. Journal of Chemical Engineering Data, 62:1615−1622

- Li CP, Zhou H, Wang S, Yuan HH, Zhang SZ, Du M (2017) A nanoporous Ag(I) coordination polymer for selective adsorption of carcinogenic dye Acid Red 26. Chemical Communications 53:4767

- Li Y, Yuan HH, Li CC, Li J (2017) A 2D Zn(II) metal-organic framework to show selective removal of Neutral Red (NR) from water. Inorganic Chemistry Communications 80: 36–40

Biography

Güneş Günay Sezer (1988) obtained her B.S., M.Sc. and Ph.D. degrees from the Department of Chemistry at Eskisehir Osmangazi University (Turkey), in 2010, 2011 and 2016, respectively. She joined Bartin University (Turkey) in 2013 where she currently works as a Lecturer in the Vocational School of Health Services. Her research focuses on the synthesis and applications of porous coordination networks.

Email: ggunay@bartin.edu.tr

Notes/Comments: The work was supported by The Scientific and Technological Research Council of Turkey (project no. 2209-A).