# Bismuth additives for silicon oils as a “green” alternative

Camila Müller, PLAPIQUI (DIQ-UNS), Argentina.

Mariana Dennehy, INQUISUR (UNS), Argentina.

Andrés Ciolino, PLAPIQUI (DIQ-UNS), Argentina.

Walter Tuckart, IFISUR (UNS) PhD, Argentina.

### Figure 1. Wear scar area vs. wt% of additive (error bars referes to standard error).

### Abstract

Fluids formulations with good properties were developed by using an environmentally friendly additive. The performance of these formulations was studied at high and low contact pressure conditions on steel/steel and polymer/steel systems. Bismuth (III) sulfide powder (Bi2S3) was obtained by employing solvothermal synthesis procedures. An orthorrombic crystal lattice (DRX) and a high-purity product (FRX) was evidenced for the powder obtained, which was added to a vinyl-terminated silicone fluid to obtain different wt% mixtures. The tribological performance of the formulations prepared was studied from Reichert´s (steel/steel system) and block on ring (polymer/steel tests), according to standardized methodologies. The results obtained for these formulations were compared with those formulations prepared with commercial Bi2S3, commercial molybdenum (IV) sulfide (MoS2) and graphite. Lubricity properties increased when wt% of solvothermal Bi2S3 increased. The wear area decreased up to 90% according to Reichert´s tests. In addition, it was observed that solvothermal Bi2S3 shows a better tribological behavior when compared to commercial Bi2S3, MoS2, and graphite. These results show the possibility to replace lead (Pb) or molybdenum (Mo) derivatives in lubricants´ formulations by an environmentally friendly additive, suitable for extreme pressure (EP) formulations. Moreover, solvothermal Bi2S3 displayed an excellent performance in silicon oil formulations when compared to commercially used additives that opens a window for its use in lubricant´s formulations at high-temperatures.

Recent Publications

- Li, Y., Wei, F., Ma, Y., Zhang, H., Gao, Z., Dai, L. and Qin, G. (2013), “Selected-Control Hydrothermal Synthesis and Photoresponse Properties of Bi2S3 micro/nanocrystals”, Cryst. Eng. Comm, Vol. 15 No. 33, pp. 6611-6616.

- Xu, X., Hu, J., Yang, S., Xie, F. and Guo, L. (2016), “Extreme Pressure Synergistic Mechanism of Bismuth Naphthenate and Sulfurized Isobutene Additives”, Surface Review and Letters, Vol. 24 No. 6, pp. 1–12.

- Heilig M, Egli M (2006) Pharmacological treatment of alcohol dependence: Target symptoms and target mechanisms. Pharmacology and therapeutics 111:855-876.

- Li X, SchwachaMG, Chaudry IH, Choudhry MA (2008) Acute alcohol intoxication potentiates neutrophil-mediated intestinal tissue damage after burn injury. Shock 29:377.

- Room R, BaborT, Rehm J (2005) Alcohol and public health. Lancet

365: 519-530.

Biography

Camila Müller is currently a PhD student at the Departamento de Ingeniería Química de la Universidad Nacional del Sur (DIQ-UNS). Dr. Mariana Dennehy is Researcher at the Instituto de Química del Sur (INQUISUR-CONICET UNS)). Dr. Andrés Ciolino is Researcher at the Planta Piloto de Ingeniería Química (PLAPIQUI-CONICET UNS). Dr. Walter Tuckart is a Researcher at the Instituto de Física del Sur (IFISUR-CONICET UNS).

Email: aciolino@plapiqui.edu.ar

Notes/Comments:

Authors wish to thank Consejo Nacional de Investigaciones Científicas y Técnicas de la República Argentina (CONICET) and Universidad Nacional del Sur (UNS) for their finantial support.

Presenting author details

Full name: Andrés Eduardo Ciolino

Contact number: +54 291 4861700

Mail id: aciolino@plapiqui.edu.ar

Category: (Poster presentation)