Characterization of the Oils of some Non-Edible Seeds as Biodiesel

Odia O. Osadolor and Ogheneme O. Clifford

Faculty of  Engineering and Technology,

Ambrose Alli University, Ekpoma,

Edo State, Nigeria.

E-mail: odiaoo@hotmail.com

ABSTRACT

In this study, oils of the seeds of Azadirachta indica(Neem), Mangnifera indica(Mango), Thevetia peruviana, Jatropha curcas and Hervia Brasilensis(Rubber) were extracted and transesterified via base-catalyzed with methanol. The resulting biodiesel free acid methyl ester (FAME) and their respective blends were characterized.  The oil and biodiesel yields were; Neem, 97%, Mango, 90%, Thevetia  98%, Jatropha, 95% and Rubber, 92%. Some parameters of the biodiesel and their blends showed that Neem oil biodiesel (NOB) had highest Cetane number of 66 at 20% blend, among the biodiesel, ROB 65 at 100% blend, JOB 60 at 10% blend, MOB 60% at 100% blend, TOB 60 at 100% blend, while petrol diesel had 50 at 100% blend and it’s the lowest. For flash point determination according ASTM D6751, JOB had the highest flash point of 200oC at 10% blend, while the petrol diesel PED had the lowest 120oC and considering ASTM D93 for flash point, JOB with the highest flash which is a better option compared with petrol diesel. For cloud point and pour point, the Biodiesels and their blends displayed encouraging results as energy resources. The result of exhaust emission conducted on CO,  NOx, etc,  shows biodiesel blends presenting better qualities with regards to the environment compared with petrol diesel. Similarly, the result of hydrocarbon particulate was higher with (TOB) 70% in the absence of load, but extremely higher with load (PED) 80%. Thus the investigation shows that biodiesel and its blends can be a good source of alternative energy source to petroleum diesel, technically and environmentally.

Keywords: Biodiesel, Emission, Non-Edible Oil, Transesterification,

INTRODUCTION

Energy has been a major concern to mankind, and more so now that energy demand is growing rapidly every day and has been projected to increase by more than 50 to 60 percent in 2025 with most of the increase coming from the emerging developing countries like Nigeria. Fossil fuels are non-renewable and when consumed cannot be replenished. This simply shows that a time will eventually come when the supply will run out. The observed depletion of world petroleum reserves and the problem associated with the environment have led to increase in energy insecurity and this has given way for the quest for alternative energy source (Devanesan et al., 2007, Alamu et al., 2007).  Any alternative to fossil fuel must be technically feasible, sustainable, environmentally acceptable, economically and readily available (Balat, 2008). Biodiesel haven met some of these conditions is gaining serious attention as the possible alternative to fossil diesel. One prominent fact in the search for alternative sources to fossil fuel is the concern over greenhouse gas emission from fossil fuel. The fossil resources comprises essentially of petroleum, coal and natural gas, which has been used to meet the energy need of man for some time now, unfortunately the resultant products of combustion consist of some gases that has serious negative impact on the environment. One of the effects of these green house gases is global warming(Munack et al., 2001 and Saravanan et al., 2007). The emission of greenhouse gasses such CO, NO2, CO2, NO, SO2, and SO3 are majorly believed to be responsible for the environmental problems associated with the urban and industrial areas and their entire surrounding by depleting the ozone layer resulting in global warming (Turner, 2005). Also, the energy generated from fossil fuel is no longer sufficient for our consumption and this is causing a serious negative impact on the economy of the nations knowing that, all nations rely on energy, which is the most fundamental requirement for human existence and activities (Ribeiro el al., 2011). Unfortunately, the non-renewable energy sources which presently contribute over 86% to the global energy pool (Atadashi et al., 2011) are depleting. As a consequence of the depleting natural petroleum based products as well as greenhouse gas emission resulting from their use, a serious search for alternative feedstock and sustainable technology that can counter the shortcomings of this natural energy sources became necessary. Among the alternative energy sources considered to replace the dwindling convectional transportation fuels are bio-diesels, straight-chain vegetable oil, and bio-ethanol, bio-oil, among other forms of bio-fuels that can be utilized as electricity and transportation fuel. Presently, agronomic efforts are being made on increasing feedstocks supply. Alternative feedstocks normally arise out of necessity from regions of the world, where the materials are not locally available or as part of concerted effort to reduce dependence on imported petroleum products (Moser, 2009). Jatropha, rubber and mango plants are majorly found and grown in Nigeria, predominantly in the southern part of Nigeria where rainfall is prominent throughout the year.

MATERIALS AND METHODS

Jatropha curcas seeds and rubber seeds were collected from Okpara Water side in Ethiope East Local Government Area of Delta State. Neem seeds(azadirachta indica) were collected from Gwadangaji Area, Birnin Kebbi, Kebbi State. Thevatia Peruviena and mango seeds were collected in Idumebo Ekpoma in Edo State.  The seeds were respectively sorted, cleaned and air-dried at ambient temperature of 250C for a month after which they were packaged in clean polythene bags and kept in a safe cool place. Other processes carried out prior to extraction includes; depulping, dehusking, drying and grinding. The seeds were pulverized to powdery mass, using a mill, after which a known mass (1kg) each, was soaked in an extraction jar with hexane solvent for 24hours. The filtrates were carefully decanted and the oils recovered using the vacuum rotary evaporator. The oils were then dried using air oven at 700C until the moisture content was reduced to 0.2%( Liauw et al., 2008).

Neem Seed	        Jatropha Seed          Rubber Seed       Thevetia Seed          Mango Seed

500g each of Jatropha  seed oil,  Rubber seed oil, Mango seed oil with Fatty Free Acid (FFA) content of 3%, were weighed and heated to 700C(Van Gerpen. 2005). The base catalyst was prepared by dissolving Sodium Hydroxide (NaOH) in methanol based on molar ratio of methanol to oil of 6:1. The mixture of the methanol NaOH solution was then added to the oils at about 600C for 1hr and catalyst dosage of 0.5 % by weight were used for the transesterification reaction. After the reaction, mixture was poured into a separatory funnel and allowed to separate into two layers. The bottom glycerine  layer was decanted while the upper methyl ester layer was purified by washing with hot water until a neutral pH  was reached after which the fatty acid methyl ester (Biodiesel), were dried using molecular sieve at 700C. The biodiesel oil obtained was weighed and the percentage oil yield was calculated using the equation bellow.

% yield =   weight of biodiesel produced (g)weight of raw oil used (g) x 100               	                  (1)

Table 1: showing the percentage yields of oil extracted.

| NOB | JOB | ROB | TOB | MOB |
| --- | --- | --- | --- | --- |
| YIELD (%) | 97 | 95 | 92 | 98 | 90 |

From Table 1 above, Thevetia peruviana seed has the highest yield of 98% , followed by Neem seed 97%. This indicate that these seeds, including, Jatropha, Rubber and Mango can be considered as good feedstock for biodiesel production. The biodiesels gotten from the processes were bended with 10%, 20% and 50% natural diesel. From the blend Cetane number, flash point, cloud point and density were determined.

Table 2: Results of Cetane number of various Biodiesel Blend

|  | Cetane Number |  |  |  |
| --- | --- | --- | --- | --- |
| Blend Fuel | BD 90:10 | BD 80:20 | BD 50:50 | BD 00:100 |
| NOB | 65 | 66 | 60 | 51 |
| JOB | 60 | 49 | 47 | 44 |
| ROB | 45 | 47 | 50 | 65 |
| TOB | 48 | 46 | 59 | 60 |
| MOB | 50 | 45 | 47 | 60 |
| PED | 35 | 45 | 48 | 50 |

Fig. 1 Graph showing c0omparison of cetane numbers at different blends

Table 3: Result of Flash Points at different Biodiesel Blends

|  | Flash Point (OC) |  |  |  |
| --- | --- | --- | --- | --- |
| Blend Fuel | BD 90:10 | BD 80:20 | BD 50:50 | BD 00:100 |
| NOB | 160 | 170 | 165 | 160 |
| JOB | 200 | 130 | 145 | 160 |
| ROB | 83 | 86 | 88 | 90 |
| TOB | 100 | 112 | 125 | 130 |
| MOB | 124 | 132 | 139 | 145 |
| PED | 112 | 100 | 110 | 120 |

Fig. 2 Graph showing comparison of flash points at different blend

Table 4: Comparison of Cloud Points of different Blend

|  | Cloud Points (OC) |  |  |  |
| --- | --- | --- | --- | --- |
| Blend Fuel | BD 90:10 | BD 80:20 | BD 50:50 | BD 00:100 |
| NOB | 11 | 6 | 5 | 3 |
| JOB | 11 | 9 | 7 | 4 |
| ROB | 7 | 3 | 2 | 1 |
| TOB | 3 | 4 | 7 | 2 |
| MOB | 6 | 5 | 3 | 7 |
| PED | 5 | 4 | 2 | 3 |

Fig.3 Graph showing comparison of cloud points at different blends

Table 5: Comparison of Pour Points at different Blend

|  | Pour Points (oC) |  |  |  |
| --- | --- | --- | --- | --- |
| Blend Fuel | BD 90:10 | BD 80:20 | BD 50:50 | BD 00:100 |
| NOB | 10 | 9 | 6 | 3 |
| JOB | 7 | 9 | 12 | 14 |
| ROB | 5 | 9 | 10 | 12 |
| TOB | 6 | 8 | 10 | 12 |
| MOB | 9 | 7 | 8 | 5 |
| PED | 8 | 6 | 9 | 7 |

Fig. 4 Graph showing comparison of pour points at different blends

The biodiesels were applied to a four stroke, single cylinder engine and tests on emissions were carried out on the exhaust gas using SV-SQ Automotive Gas Analyzer and the results are as depicted below.

Table 6: Result of Carbon monoxide (CO) Emission of various Biodiesel and its Blends

| Fuel | Carbon monoxide (CO) emission when load is not applied (%) | Carbon monoxide (CO) emission when load is applied (%) |
| --- | --- | --- |
| NOB | 0.13 | 0.16 |
| JOB | 0.15 | 0.18 |
| ROB | 0.15 | 0.30 |
| TOB | 0.15 | 0.20 |
| MOB | 0.18 | 0.18 |
| PED | 0.30 | 0.40 |

Fig. 5 Bar chart showing carbon monoxide emission at different blends

Table 7: Result of Nitrogen oxide (NOx) Emission of various Biodiesel and its Blend

| Fuel | Nitrogen oxide (NOx) emission when load is not applied (ppm) | Nitrogen oxide (NOx) emission when load is applied (ppm) |
| --- | --- | --- |
| NOB | 11 | 15 |
| JOB | 12 | 15 |
| ROB | 15 | 15 |
| TOB | 17 | 19 |
| MOB | 15 | 36 |
| PED | 20 | 38 |

Fig. 6 Bar chart showing nitrogen oxide at different blends

Table 8: Result of Hydrocarbon (HC) Emission of various Biodiesel and its Blend

| Fuel | Hydrocarbon (HC) emission when load is not applied (ppm) | Hydrocarbon (HC) emission when load is not applied (ppm) |
| --- | --- | --- |
| NOB | 55 | 65 |
| JOB | 20 | 60 |
| ROB | 64 | 50 |
| TOB | 70 | 50 |
| MOB | 25 | 70 |
| PED | 35 | 80 |

Fig. 7 Bar chart showing hydrocarbon emission at various blends

RESULTS AND DISCUSSION

It was observed that the colour of the Jatropha oil Biodiesel (JOB) , Rubber oil Biodiesel  (ROB), and Neem oil biodiesel (NOB) were brownish, while Mango oil Biodiesel (MOB)  was slightly yellow, and Thevetia peruviana was golden yellow after tranesterification. A diesel cetane number is a measure of the fuel’s ignition, the time period between start of ignition of fuel and the combustion of the fuel.  In general, a high cetane fuel will have a short ignition delay period than lower cetane fuel. With the increase in cetane number, a reduction of carbon monoxide (CO), hydrocarbon (HC), the volatile particulate fractions and even the noise could be achieved. High cetane number in the range of 49 to 52 can reduce particulate emissions by up to 0.01g/kW( Lorga and Ostonia, 2002). The results of cetane number of biodiesel, petrol diesel and their blends in Fig. 1 above shows that Neem oil biodiesel (NOB) has the highest cetane number of 66 at 20% blend, among the biodiesel produced in this study. ROB had 65 at 100%, JOB 60 at 10% blend, MOB 60 at 100%, TOB 60 at 100%, while petroleum diesel had 50 at 100%, petroleum diesel has the lowest cetane number among the fuels. Therefore, it can be concluded that the biodiesels (and their blends) are of a better quality compared to petroleum diesel. The flash point was determined according to ASTM D6751, using the Kehler Model K-16270 flash point apparatus. Results of the experiment on flash points as depicted in Fig. 2 shows that JOB has the highest flash point of 200oC at 10% blend, NOB, 170oC at 20% blend, MOB 145oC at 100%, TOB 130oC at 100%, ROB 90oC at 100%, PED 120oC at 100%. The highest flash point is observed in JOB with 200oC at 10% blend, while the petroleum diesel PED has the lowest flash point compared with the biodiesel, and considering ASTM D93 for flash point, JOB with the highest flash point of 200oC, is a better option, compared with petroleum diesel. The cloud point is the temperature at which wax first becomes visible when the fuel is cold. The crystal formation is treated as a solid equilibrium of paraffins between a solution and a solid (No SY, 2011). The cloud point is determined with Herzog HCP852 (ASTM D2500) at specific rate. The result of the cloud point in the study as depicted in Fig.3 shows that NOB, JOB had highest cloud point 11oC at 10%  blends, ROB, TOB, MOB had 7oC at 10%, 50%, and MOB 100% blends, respectively, while petroleum diesel (PED) 5oC at 10% blend which is the lowest. The pour point is the temperature at which the amount of wax, out of the solution, is sufficient to gel the fuel (Saloua et al, 2010). The standards pour point for biodiesel is between -15oC and 16oC as shown in ASTM D6751. Fig 4.4a and Fig 4.4b show that Jatropha biodiesel (JOB) had 14oC at 100% blend, ROB, TOB 12oC at 100% blend respectively, while that of MOB and PED had 9oC at 10% and 50% blends.  The pour points are within the acceptable range of the ASTM D6751. From Fig.5 it can be observed that when load was not  applied the carbon monoxide emission for  the various blends are NOB 0.13%, JOB 0.15%, ROB 0.15%, TOB 0.15%, MOB 0.18%, PED 0.30. And when load was applied they became NOB 0.16%, JOB 0.18%, ROB 0.30%, TOB 0.20%, MOB 0.18%, PED 0.40%. For the emissions when loaded, petroleum diesel has the highest of 0.40% carbon monoxide. This shows that biodiesel blends will be more environmentally friendly than petroleum diesel. From Fig. 6 it can also be observed that in the absence of load, the results of emission of (NOx) for the various blends are NOB 11%, JOB 12%, ROB 15%, TOB 17%, MOB 15%, and PED 20%. And when load was applied, they get modified to NOB 15%, JOB 15%, ROB 15%, TOB 19%, MOB 36%, PED 38%.  Again petroleum diesel has the highest of 38% of nitrogen oxide (NOx). Fig. 6 shows hydrocarbon emission when not loaded, the results of the emission for  the various blends are NOB 55%, JOB 20%, ROB 64%, TOB 70%, MOB 25%, PED 35%, while when loaded the results become NOB 65%, JOB 60%, ROB 50%, TOB 50%, MOB 70%, PED 80%.  Once more when loaded petroleum diesel has the highest HC emission of 80%.

CONCLUSION

From the experimental evaluation of the five non-edible seeds of Jatropha curcas, Neem, Rubber, Thevetia peruviana and Mango, it can be seen that they can favourably compete with petroleum diesel as fuel. The results suggest that these non-edible oils can be exploited as an alternative source of fuel as they are even more environmentally friendly than the present conventional petroleum diesel. Mango seed considered for this experiment for the first time also shows very good prospects as an alternative source of fuel.

REFERENCE

Alamu, O.J., Waheed, M. and Jekeyinfa, S.O. (2007. Alkalis catalyzed laboratory production and testing of biodiesel fuel from Nigeria palm Kernel oil. Agricultural Engineering International: The GIGR Journal of Scientific Research and Development, 9: 7 – 9.

Atadashi, I .M., Aroua, M.K., and Aziz, A.A. (2011. Biodiesel Separation and purification: a review. Renewable Energy. 36: 437-443.

Balat, M. (2010).  Potential alternative to edible oils for biodiesel production-a review of current work, ‘’ Energy coversion and management, 52: 1449 – 1492.

Devanesan, M. G., Vuruthegiri, T. and Sugumar, N. (2007). Transesterification of Jatropha oil using immobilized pseudomonas flourescence. African Journal of Biotechnology.

Liauw, M.Y., Natan, F.A., Widiyanti, P., Ikasari, D., Indraswati, N. and Soetaredjo, F.E. (2008). Extraction of neem oil (azadirachta indica A. Juss) using hexane and ethanol.

Lorga D, Chedli, Ostonia D. 2002. Modificarea Instalatiei de injectie a Unui moror diesel de la pompa norma lamonopunct la la o pompa de alternative multpunct. Targu Jiu: UTGJIU. international comference.

Miao, X.,  Li, R. and Yao, H. (2010). Effect acid catalyzed energy purification for biodiesel product conversion and management 10 : 2680- 4.

Moser, B.R. (2009). Biodiesel production, properties, and feedstocks, In Vitro cell. Dev. Bio - plant 45: 229 - 266.

Munack, A., Schroder, O., Krashl, J, and Bunger, J. (2001). Compression of relevant exhaust gas emisions from biodiesel and fossil diesel fuel. Agricultural Engineering International ;: GIGR, Journal of Science Resources Development, : 245 - 286.

No, S.Y. (2013). Inedible vegetable oils and their derivatives for alternative diesel fuels in CI engines: a review. Renewable and sustainable Energy Reviews,S 33 (1); 131-49.

Ohimain, E.I.  (2010). Emerging bioethanol projects in Nigeria. Their opportunities and challenges. Energy policy. 38: 7161 - 7168.

Oshewolo, S.. (2012). Designed to fail . Nigeria's quest for biofuel. Afro Asian Journal of Social Sciences. 3 (3): 1 - 15.

Ribeiro, A., Casro, F. and Carvaiho, J. (2011). Influence of free fatty acid content in biodiesel production of biodiesel Bioresource. Techno. 99: 3975 - 3981.

Saloua, F., Saber, C and Heedi Z. (2010). Methyl ester of (Maclura pomifera rafin), schneider seed oil, biodiesel production and characterization. Bioresource Technology, 101(9): 3091-6.

Salvi, B., Panwar, N. (2012). Biodiesel resources and production technologies – A review, Renewable and Sustainable Energy Reviews, 16:3680-3689.

Saravana, S., Nogarajan, G., Roa, G., Narana, L. and Sampath, S. (2007). Feasibility study of crude rice bran oil as diesel substitute in DI - CI engine without modification Energy for sustainable Development 11(3): 83 - 92.

Turner, J. (2005). Aspects of modern Antactic metrology and chemistry, Archives of Natural History, 32(2): 334 - 345.

Van Gerpen, J. (2005). Biodiesel Processing and Production. Fuel processing Technology, (86):  1097 - 1107.