Oil spill removal from water by mussel-inspired polydopamine/polyethylenimine-functionalized activated carbon derived from date palm waste

Adewale Giwa a*, Hanifa Taher b

a b Department of Chemical Engineering, Khalifa University of Science and Technology,

Masdar City Campus, P.O. Box 127788, Abu Dhabi, United Arab Emirates.

Presenting Author Name: Adewale Giwa

Affiliation: Department of Chemical Engineering

University: Khalifa University of Science and Technology

Country: United Arab Emirates

Scientific Session name / number: Track 12: Separation Techniques in Environmental Science

Category: Oral presentation

Abstract

Activated carbon was prepared from date palm leaves, modified with mussel-inspired polydopamine and cationic polyethylenimine by dip coating, and employed for the sorption/dispersion of crude oil in simulated seawater. The activated carbon was prepared from ZnCl2 activating agent using two impregnation ratios, i.e. 1:2 and 1:4. The pristine (unmodified activated carbon) prepared from 1:4 impregnation ratio showed the highest crude oil sorption efficiency of 53% but no crude oil dispersion. Modification of the activated carbon with 10% PDA/PEI increased the dispersion efficiency to 61% while still achieving a sorption efficiency of 30%. The dual sorption-dispersion property of this activated carbon was achieved through the abundant nucleophilic N-H chains in the modifier, which altered the morphology and pore structure of the activated carbon, improved its amphiphilicity, and ensured covalent C-N linkages with the activated carbon. However, a further increase in the % of the modifier from 10% to 20% resulted in a decrease in both sorption and dispersion efficiencies due to salting-in effect. Samples were characterized using Environmental Scanning Electron microscopy, Raman Spectroscopy, Infra-Red IR Attenuated Total Reflectance (ATR) spectra analysis, and Energy Dispersive X-Ray Spectroscopy. The modified activated carbon showed better sorption/dispersion characteristics compared to a commercial activated carbon. This study presents the potential for the formation of pickering emulsions of crude oil in saline water using activated carbon derived from date palm waste.

Biography:

Dr. Adewale Giwa is a researcher at Khalifa University of Science and Technology, Abu Dhabi, United Arab Emirates. He has co-authored over 50 publications and reviewed scientific articles for many journals.

Research Interests: Environmental Sciences, Water Treatment, Renewable Energy

Keywords: Date palm leaves; activated carbon; polydopamine; polyethylenimine; crude oil sorption; crude oil dispersion.

Mail Id: Adewale.giwa@ku.ac.ae

Contact Number: +971028109153

Twitter account: N/A

Linked In account: https://ae.linkedin.com/in/adewale-giwa

Facebook account: N/A