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Abstract (300 word limit)
 Undoped and cobalt doped Tin oxide (SnO2 and SnO2: Co) thin films of varying thickness were successfully fabricated by the sol-gel spin coating technique. The samples were characterized by X-ray diffraction (XRD) and scanning electron microscope (SEM). The effect of the number of layers on the structural and optical properties of SnO2 and SnO2: Co films were studied. The crystallite size of the pure SnO2 films increased from 7.7 to 31.1 nm by increasing the number of layers from 12 to 24. The crystallinity of the film was enhanced when the annealing temperature was increased from 400 to 500oC. However, it reduced by incorporating Co atoms. Transmittance and optical band gap of the SnO2 film decreased by increasing the number of layers or after Co doping. The 8% Co-doped film shows relatively higher sensitivity for CO2 gas at room temperature (RT) compared to un-doped SnO2 film with a rate of 0.116/sccm for Co-SnO2. In this study, the carbon dioxide gas acted as an oxidizing agent that caused the increase in the electrical resistance of the sensor signified by the increase in voltage reading. The trapped negative charges in the oxygen species caused an upward band bending in the SnO2 film, thus increasing its resistance compared to the situation before CO2 gas exposure. The response and recovery times increased as the CO2 concentration increased. These results demonstrate the possibility of optimizing the physical properties of the SnO2 film for sensing and optoelectronic applications 
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