# Adsorption-Desorption Cycle of Chemisorbed CO2 on the Surface of SnO2 and Co-SnO2 for Room Temperature Gas Sensor

Mohamed A. Basyooni, M.Sc. 1Department of Nano Science and Nano Engineering, Institute of Science and Technology, University of Konya Necmettin Erbakan, Konya 42060, Turkey & School of Materials Science and Engineering, Nanyang Technological University, 50 Nanyang Avenue, Singapore 639798

Dr.Mohamed Shaban, PhD, Nanophotonics and Applications (NPA) Lab, Department of Physics, Faculty of Science, Beni-Suef University, Beni-Suef 62514, Egypt

### Abstract (300 word limit)

Undoped and cobalt doped Tin oxide (SnO2 and SnO2: Co) thin films of varying thickness were successfully fabricated by the sol-gel spin coating technique. The samples were characterized by X-ray diffraction (XRD) and scanning electron microscope (SEM). The effect of the number of layers on the structural and optical properties of SnO2 and SnO2: Co films were studied. The crystallite size of the pure SnO2 films increased from 7.7 to 31.1 nm by increasing the number of layers from 12 to 24. The crystallinity of the film was enhanced when the annealing temperature was increased from 400 to 500oC. However, it reduced by incorporating Co atoms. Transmittance and optical band gap of the SnO2 film decreased by increasing the number of layers or after Co doping. The 8% Co-doped film shows relatively higher sensitivity for CO2 gas at room temperature (RT) compared to un-doped SnO2 film with a rate of 0.116/sccm for Co-SnO2. In this study, the carbon dioxide gas acted as an oxidizing agent that caused the increase in the electrical resistance of the sensor signified by the increase in voltage reading. The trapped negative charges in the oxygen species caused an upward band bending in the SnO2 film, thus increasing its resistance compared to the situation before CO2 gas exposure. The response and recovery times increased as the CO2 concentration increased. These results demonstrate the possibility of optimizing the physical properties of the SnO2 film for sensing and optoelectronic applications

Photograph

Recent Publications (minimum 5)

- Mohamed A. Basyooni, Ashour M. Ahmed, Mohamed Shaban, ‘’Plasmonic hybridization between two metallic nanorods’’, Optik (2018), doi.org/10.1016/j.ijleo.2018.07.135.

- Mohamed A. Basyooni, Mohamed Shaban, Adel M. El Sayed, ‘’Enhanced Gas Sensing Properties of Spin-coated Na-doped ZnO Nanostructured Films’’. Scientific Reports 7, 41716, (2017), doi: 10.1038/srep41716.

- Mohamed Shaban, G. F. Attia, Mohamed A. Basyooni, Hany Hamdy, ‘’Morphological and Structural Properties of spin coated Tin Oxide thin films’’, International Journal of Engineering and Advanced Research Technology 1 (3), (2015) 11-14.

- Mohamed Shaban, Mohamed A. Basyooni, G. F. Attia, Hany Hamdy, “Synthesis and Characterization of Tin Oxide thin Films and Effect of annealing on Multilayer Film, The 5th international conference on modern Trends in Physics Research (MTPR-014), 15-19 December 2014, Cairo University, Egypt. The WPS International Conference Proceedings of the Fifth MTPR-014 Conference, Volume 9914, June 2015.

- Mohamed A. Basyooni, Mohamed Shaban, G.F.Attia, SnO2 and Co-Doped SnO2 Thin Films: Fabrication, Characterization and CO2 Sensing, Material research express (under review).

- Mohamed A. Basyooni, Mohamed Rabie, Mohamed Shaban, Yasin Eker, Ashour M. Ahmed, ‘’FTO Decorated Graphene Oxide and Vanadium Oxide for Room Temperature Carbon Dioxide Gas Sensors’’, (Under review).

- Mohamed A. Basyooni, ‘’VO2 for Room Temperature Thermochromic Applications, strain-induced phase transition’’, (writing)

Biography (150 word limit)

Mohamed A. Basyooni has completed M.Sc. degree in Experimental Physical Chemistry with honors at Nanophotonics and Applications Lab, Faculty of Science, Beni-Suef University in 2016. Now, he is a Ph.D. research student at Department of Nano Science and Nano Engineering, Institute of Science and Technology, University of Konya Necmettin Erbakan-Turkey and Institute of Materials Research and Engineering (IMRE)-Singapore. He was working in semiconductor technology for many years to develop a room temperature gas sensors based on metal oxide semiconductors nanostructure thin films. He developed a room temperature gas sensor with more than 80% sensitivity towards carbon dioxide based on novel wrinkle porous net-work nanostructure-based sodium doped zinc oxide, published in Nature. Currently, he is working in energy efficient materials, vanadium dioxide (VO2) based smart coatings and the gas sensing behavior.

Email: Mohamed.basyooni@nriag.sci.eg   &   m170160@e.ntu.edu.sg