Title: Modification of Structure and Properties of Magnetorheological Elastomer via Heat Treatment

Author (s) Name: Alif Azizi Ayub1, Nur Azmah Nordin1*, Siti Aishah Abdul Aziz1,2, Mumtaz Hana Ahmad Khairi1,2, Saiful Amri Mazlan1,2 , Hafizal Yahaya1

1 Engineering Materials and Structures (eMast) iKohza, Malaysia-Japan International Institute of Technology (MJIIT), Universiti Teknologi Malaysia, Jalan Sultan Yahya Petra, 54100 Kuala Lumpur, Malaysia.

2Advanced Vehicle System (AVS) Research Group, Universiti Teknologi Malaysia, Jalan Sultan Yahya Petra, 54100 Kuala Lumpur, Malaysia.

Abstract

Modification of structure via heat treatment in different temperatures is known to result in a change of properties of Si-based magnetorheological elastomer (MRE). In this research, three different temperatures particularly 100, 125 and 150°C have been applied to MRE contained of 70 wt% CIP for 24 hours, individually and the resultant rheological changes of MREs were investigated. It was found that the MRE treated with 125°C exhibit the highest MR effect, about 88% respective to non-treated MRE. Furthermore, the corresponding initial storage modulus present the lowest, 0.284 MPa compared to 0.298 MPa of pure MRE indicating the improvement of an MRE’s modulus elasticity. Meanwhile, at temperature of 150°C, it can be seen that the MR effect of the MRE started to drop up to 50%. However, the storage modulus for all non-heat treated and heat-treated MREs increased exponentially as the frequencies and currents increased, respectively for both off- and on-state conditions. In fact, the increment trend of storage modulus as a result of frequency is followed by the increased of heat treatment temperatures; 20% for 100°C, 27% and 32% for 125 and 150°C, respectively compared to non-heat treated MRE, at 3A. The result shows that the heat treatment on the MREs enhanced the inter-particles bonding between the magnetic particles and rubber matrix that subsequently improve the structure and rheological properties of the MREs. (Up to 250 words)

Figures if any (BW/Color):

Fig. 1. Storage modulus vs magnetic flux density for all MRE samples

Fig. 2. MR effect of MREs correspond to the heat treatment temperatures

Fig 3. Storage modulus versus frequencies at 3A for non-heat treated and the heat treated MREs

Recent Publications If any:

S.A.A. Aziz, S.A. Mazlan, N.I.N. Ismail, Ubaidillah, S.B. Choi, N.A. Nordin and N. Mohamad, A Comparative Assessment of Different Dispersing Aids in Enhancing Magnetorheological Elastomer Properties, Smart Materials and Structures, Vol. 27, No. 11, 117002. 2018.

M.H.A. Khairi, S.A. Mazlan, Ubaidillah, S.B. Choi, N.A. Nordin, N. Mohamad, S.A.A. Aziz and N. Hapipi, The Role of Additives in Enhancing the Rheological Properties of Magnetorheological Solids - A Review, Advanced Engineering Materials. 2019, Accepted Manuscript.

D. Utami, Ubaidillah, S.A. Mazlan, F. Imaduddin, I. Bahiuddin, N.A. Nordin, S.A.A. Aziz, N. Mohamad and S.B. Choi, Material Characterization of a Magnetorheological Fluid Subjected to Long-Term Operation in Damper, Materials, Vol. 2018, No. 11, 2195. 2018.

D. Utami, S.A. Mazlan, Ubaidillah, I. Bahiuddin, F. Imaduddin and N.A. Nordin, The Changed of Behaviour of MR Fluid in MR Damper after a Long-Term Operation, Key Engineering Materials, Vol. 775 KEM, 171-176. 2018.

N.A.N.A. Rahman, S.A. Mazlan, S.A.A. Aziz, N.A. Nordin, Ubaidillah and N.M. Hapipi, Magnetorheological Elastomer Silicone-based Containing Corroded Carbonyl Iron Particles, Key Engineering Materials, Vol. 772 KEM, 51-55. 2018.

Biography

Nur Azmah Nordin is currently a senior lecturer in faculty of Malaysia-Japan International Institute of Technology, Universiti Teknologi Malaysia, Kuala Lumpur. She earned her PhD in Mechanical Engineering (Materials) from Universiti Teknologi Malaysia (UTM) in year 2017. Her research mainly focus on the fabrication and modification of metal composite, characterizations and evaluation of the morphologies as well as properties of the composite materials. She has presented papers in several international conferences. She also has published several in ISI journals and scopus index. Currently she has joined a research group who focus on the developtment, structure and properties of smart material namely magnetorheological materials (MR).

Presenting author details 
Full name: Nur Azmah Nordin
Contact number: +60167765440

Email id: nurazmah.nordin@utm.my
Category: (Oral presentation/ Poster presentation)

Session name:

Research interest:

Notes: