Chatting the Course for a New Paradigm Shift in Support of Higher Substitution of Waste Materials In Concrete

Professor Sunday Nwaubani

1 University of the Witwatersrand, Johannesburg, South Africa

Abstract

“Waste” they say, is “Wealth” nowadays.  Construction has proved a good avenue for utilizing various forms of waste materials, in a rational   and sustainable way, to minimise the use of energy-intensive materials. With a rising global population, infrastructural needs are rising exponentially with cement production contributing in a major way to the current global anthropogenic CO2 emissions. In a bid to reduce the cost and energy footprint of Portland cement(PC) production, the use of waste is rapidly emerging as a supra-disciplinary field in most parts of the world where the use of industrial wastes like fly ash(FA), granulated steel slag, silica fume, waste fibres etc., in construction has become very popular since the last half of the 20th century. However, their slower rate of strength gain hinders their usage in larger quantities. The construction industry seems to have adopted a “safe” concept of trying to match the strength of the blended mix with the strength of a cement only control mix made with 100% Portland cement at 28 days. This is hampering the increased use of a vast amount of waste materials which continue to contribute to environmental pollution worldwide.  This paper reports the result of an investigation into the effect of High Volume FA substitution on the mechanical property of concrete when cured by applying a chemical activator or high temperature to speed up the pozzolanic reactivity.

Increasing the FA content caused an increase in workability, reduced early strength development and lowered density. It was also found that calcium hydroxide reduced water demand but was an ineffective activator. The long-term strengths of the blended mixture were higher than that of the PC control mix especially when cured at higher temperatures. It was observed that even at 60% replacement, compressive strengths above 30MPa (general structural use) in 28 days was achievable.

Keywords: Activator, High Volume FA, Mechanical Properties, Pozzolanic reaction.

Professional Biography (100-150 words)

Professor Sunday Nwaubani completed his PhD from Leeds University in the UK in 1990. He has been involved for many years,  in research training and guidance of  postgraduate students.  His research is broadly concerned with sustainability issues in construction, including the use of waste materials to produce novel materials with enhanced properties that contribute to achieving resource efficiency. His main expertise is in assessing the properties, durability and microstructure of construction materials.  Main areas include High strength and  high performance concrete; blended cements produced  using natural, artificial and other materials (including industrial wastes) as replacements for cement in concrete; corrosion of rebar and corrosion inhibition in reinforced concrete; use of surface treatment materials in general; durability of surface-treated stone and concrete structures; polymer modified concrete.  He has a substantial body of  work (over 100 articles) published in reputable journals, national and international conference proceedings and other outlets.

Paste your Photograph here

Full Name: Prof S O Nwaubani

Email Id: Sunday.nwaubani@wits.ac.za

Contact No:+27 633563370

Social Network Details (FaceBook/LinkedIn):

Any Comments: