# Abstract Title:

A novel natural and patient-derived biomaterial fabricated using the polyphenol Oleuropein and the autologous blood-derived plasma for potential applications in bone tissue engineering

Francesco Paduano1, Massimo Marrelli1, Bruna Codispoti1, Marco Tatullo1

1 Tecnologica Research Institute and Marrelli Health, Biomedical Section, Stem Cells Unit, Crotone, Italy

# Abstract

To provide a bioactive and biocompatible environment for new bone formation, several materials have been used to mimic the bone-forming components. In this context, we examined the feasibility of the natural polyphenol oleuropein as a cross-linking agent for fabricating a polymerizable biomaterial for potential applications in bone tissue engineering.

Oleuropein is a natural-occurring iridoid glycoside especially found in the leaves and fruits of the olive tree (Olea Europa). It is well known for its antibacterial, antifungal, antiviral, antioxidant and anti-inflammatory activities. More importantly, it has also been shown that oleuropein is able to induce bone formation and inhibits bone resorption as well as bone tissue demineralization. Interestingly, the conversion of oleuropein glucoside to its aglycone by the enzyme β-glucosidase exhibits interesting cross-linking properties which make it a suitable cross-linking agent for biomedical applications. Here, the autologous patients derived-plasma and aglycone Oleuropein were used to fabricate a novel biomaterial. We invented a novel formulation in which autologous patients derived plasma is used as protein substrate that is able to polymerize when is mixed with the aglycone oleuropein. By using L929 mouse fibroblasts and dental pulp stem cells (DPSCs) we demonstrated that this biopolymer is nontoxic and biocompatible. Importantly, plasma-derived biomaterial contains biochemical signals necessary for tissue repair and regeneration and can be easily generated from patient’s autologous blood without the potential risk of foreign body reaction or infection. Although this biomaterial shows interesting potentiality, several investigations are required to elucidate the potential of this novel biomaterial for bone tissue engineering applications.

Keywords: Natural Biomaterials, Protein-based biomaterials, Autologous blood-derived plasma, Oleuropein, Blood-derived scaffolds, Bone tissue engineering.

# Submitted to Track 8: Advanced Materials (Natural Biomaterials, Protein based biomaterial).

# Professional Biography

Francesco Paduano has completed his Ph.D. from University “Magna Graecia” of Catanzaro, Campus “S. Venuta”, Catanzaro, Italy. Currently, he has a researcher position at Tecnologica Research Institute, a private research company in Italy that works in the field of dental stem cells biology and regenerative medicine. He has published more than 34 papers in reputed journals, 3 book chapters and was a co-inventor of a deposited patent (Biopolimeric film for the localized release of bioactive molecules) and has been serving as “Review Editor” of Molecular and Cellular Oncology, a specialty of Frontiers in Cell and Developmental Biology and Frontiers in Oncology.

Paste your

# Email Id: francesco.paduano@tecnologicasrl.com

# Any Comments:

# Our goal is to present this novel biomaterial to the academic world, industrial specialists, pharmaceutical company and decision producers. We would also like to find potential collaborations that can help us to study and produce this novel biomaterial.