Preclinical evaluation of skin substitute comprising biodegradable synthetic polymer and human derived extracellular matrix components for functional skin tissue regeneration

Rashmi Ramakrishnan1, Kalliyanakrishnan V2, Lissy K Krishnan1

1 Department of Applied Biology, 2Department of Biomaterial Science and Technology, Biomedical Technology Wing, Sree Chitra Tirunal Institute for Medical Sciences & Technology,  Thiruvananthapuram, India.

Abstract

Complex and chronic wounds represent significant health burden. For extensive and deep wounds, autografts are considered as gold standard. To solve the problem of limited availability of autografts, tissue engineering technologies have been developed resulting in complex skin equivalents suitable for wound healing and regeneration. Most of the approved skin equivalents in the market contain non-degradable, allogeneic/xenogenic scaffold materials. Our study aims to develop a non-immunogenic skin substitute for in vitro and in vivo guided tissue engineering. The developed skin substitute comprise electrospun terpolymer poly (lactide-glycolide-caprolactone) [PLGC], human-plasma derived fibrin (FIB) and umbilical cord derived hyaluronic acid (HA). The terpolymer PLGC is synthesized using monomers approved for clinical use. The fibrin is made from pharmacopoeia grade fibrin sealant and HA is proven to be highly pure. The function of synthetic electrospun scaffold is to provide mechanical strength to prevent wound contraction and FIBHA for promoting wound regeneration. In this study, it is proven that the combination scaffold (PLGCFIBHA) possesses appropriate mechanical strength, degradation profile, porosity, and further validated its application for in-vitro dermal tissue engineering after long term culture. The in-vivo hypersensitivity and irritation test suggested non-immunogenic and tissue compatible nature of the combination scaffold.  About 70 % in-vivo degradation of the PLGC within 120 days was proven based on molecular weight determination. The final lyophilized product PLGCFIBHA is hemostatic, self-adherent to acute/debrided wound, biodegradable, non-immunogenic, and stable during storage. The in- vivo dermal tissue regeneration potential was evaluated by applying on 4x4 cm2 PLGCFIBHA on burn wounds produced in rabbit model and were compared with untreated control after 28 days. Qualitative and quantitative analysis of the explanted wound site showed accelerated wound closure, epithelialisation, ECM deposition, angiogenesis and skin appendages regeneration when wounds were treated with PLGCFIBHA. Hence, the developed novel skin substitute is recommended for dermal regeneration in topical wounds.

Keywords: Biodegradable scaffold, Guided tissue engineering, Hemostatic, Skin substitute.

Professional Biography (100-150 words)

Ms Rashmi Ramakrishnan is currently pursuing her third year of PhD in skin tissue engineering at Department of Applied Biology in Sree Chithra Tirunal Institute for Medical Science and Technology, An institute of national importance under Govt of India, Thiruvananthapuram, India.  She has M.Phil degree in Biomedical Technology and Master’s degree in Medical Biochemistry. Her PhD work focuses on critical aspect of wound healing and aims to develop skin substitutes comprising of natural as well as polymeric materials for skin tissue regeneration. She has several conference proceedings and two patents applied for her credit and papers are under review.

Email Id: roshrashmi@gmail.com/ rashmir.bio16@gmail.com