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Burn lesions are frequently occurring injuries that exhibit poor healing ability. Scaffolds play a critical role in the reconstruction of damaged living tissue, and those produced using biopolymers, such as gelatin and chitosan, are biocompatible and have adequate functional properties. Mesenchymal stem cells (MSC) and fibroblasts are an excellent tool for studying the behavior of this kind of biomaterials and their ability to guide the growth and tissues repair. The aim of this study was the synthesis of freeze-dried scaffolds based on gelatin and chitosan added with aloe vera and snail mucus. The microstructure and in vitro cellular interaction with scaffolds were determined through SEM. Cell viability of cell seeded scaffolds was determined through the MTT assay. Wound healing in vivo studies were made by contact with incandescent metallic bar on dorsal female mice, then the scaffolds were subcutaneously implanted. For production of porous scaffolds, gelatin (G),  chitosan (CH), aloe vera (A) and snail mucus (S) suspensions was prepared. The scaffold forming suspensions (SFS) were frozen at −80ºC, prior to freeze-drying at −58ºC for 18h. The resulting sponge-like material was crosslinked and freeze-dried  again. Gelatin-based scaffolds showed what appeared to be a highly porous sponge displaying interconnected porosity and homogeneous pore diameters, as well as pore wall thickness. Important microstructural changes were observed in the scaffolds as a function of additives. Scanning electron micrographs revealed that the cells appeared to attach and spread well in all scaffolds, forming multiple protrusions and cellular aggregates that gradually increased in size. MTT assay showed that fibroblasts proliferated more rapidly on the scaffolds containing aloe vera and the mixture of aloe vera and snail mucus. The scaffold was observed to be biocompatible on subcutaneous implantation in mice model which was supported by scaffold integration with tissue and presence of blood vessels in histological studies.
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