Photograph

Title of the Abstract: Collagen scaffolds with tailored pore geometry for building

3-dimensional vascular networks

Author Name: Sasha Berdichevski

Affiliation: Department of Engineering

University: University of Cambridge

Country: United Kingdom

Abstract:

Therapies that promote angiogenesis have been successfully applied using various combinations of proangiogenic factors together with a biodegradable delivery vehicle [1, 2]. In this study we used bimodal non-invasive monitoring to show that the host response to a proangiogenic biomaterial can be drastically affected by the 3-dimensional geometry of the implant material. Fluorescence/MRI probes were covalently conjugated to VEGF-bearing biodegradable PEG-fibrinogen hydrogel implants and used to document the in vivo degradation and liberation of bioactive constituents in a subcutaneous rat implantation model. The hydrogel biodegradation and angiogenic host response with three types of VEGF-bearing implant configurations were compared: preformed cylindrical plugs, preformed injectable microbeads, and hydrogel precursor, injected and polymerized in situ. Although all three were made with identical amounts of precursor constituents, the MRI data revealed that in situ polymerized hydrogels were fully degraded within 2 weeks; microbead degradation was more moderate, and plugs degraded significantly more slowly than the other configurations. The presence of hydrogel degradation products containing the fluorescent label in the surrounding tissues revealed a distinct biphasic release profile for each type of implant configuration. The purported in vivo VEGF release profile from the microbeads resulted in highly vascularized tissue containing up to 16-fold more capillaries in comparison with controls. These findings demonstrate that the configuration of an implant can play an important role not only in the degradation and resorption properties of the materials, but also in consequent host angiogenic response.

Biography:

Dr Sasha Berdichevski is a post-doctoral research associate at the Engineering Department at the University of Cambridge, UK. She has obtained a Blavatnik Fellowship by the Blavatnik Family Foundation, British Council and University of Cambridge, and currently she holds a Marie Curie Fellowship. Dr Berdichevski has been awarded Outstanding Researcher in Engineering and Science Award and Prize for Excellence in Nano-science and Nanotechnology during her PhD in the Technion, Israel. Sasha has published her research in leading journal papers, and co-authored publications in 3 books.

Research Interests:

Biomaterials, tissue engineering, scaffold-tissue/cell interactions, scaffolds’ 3D geometry-function relationship.

References:

[1] Silva EA, Mooney DJ. (2007) Spatiotemporal control of vascular endothelial growth factor delivery from injectable hydrogels enhances angiogenesis. J Thromb Haemost 5(3):590–598.

[2] Formiga FR, et al. (2010) Sustained release of VEGF through PLGA microparticles improves vasculogenesis and tissue remodeling in an acute myocardial ischemia-reperfusion model. J Control Release 147(1):30–37.

Mail ID: sashenka125@gmail.com

Contact number: +44(0)7941541568

Suggestions of colleagues/Professors/scholars to send invitation (if any)

Suggestions of Sessions to the conference (if any):

- Track 4-1 Cellular Interaction of Biomaterials

- Track 4-5 Scaffold Product

- Track 11-4 Bio Fabrication of Scaffolds

- Track 14-5 Vascular Tissue Engineering