Title of the Abstract: 3D printing technology: study based on nano-sized calcium phosphate and PCL ink for bone tissue regeneration.

Author Name: Fernando Pozzi Semeghini Guastaldi

Affiliation: Postdoctoral Research Fellow

University: Massachusetts General Hospital, Boston, MA

Country: United States

Abstract:
The objective of this study was to obtain three-dimensionally (3D) printed Scaffolds from nano-sized calcium phosphate (amorphous calcium phosphate; ACP) and polycaprolactone (PCL) ink for bone tissue regeneration (BTR). The synthesis of the nano-sized calcium phosphate was performed by wet method. The material was characterized by X-ray diffraction (XRD), infrared spectroscopy (FTIR), scanning electron microscopy (SEM) and determination of the surface area by adsorption of nitrogen. After obtaining the ink, cylindrical Scaffolds (15x10 mm) were 3D printed. Mechanical strength, SEM, EDX and porosity were evaluated. Results of XRD analysis showed an intense peak at θ = 23.4 corresponding to ACP, as well as other peaks of lower intensities corresponding to HA, ACP and OCP. The FTIR spectrum confirmed that the sample obtained corresponded to the nano-sized calcium phosphate sample. Studies of viscosity showed that the composition of nano-sized calcium phosphate and PCL used was suitable for the preparation of the ink. The SEM analysis shows that the post-printed material maintains the cylindrical structure. It is also observed interconnected pores. On the other hand, the EDX analysis showed the presence of calcium and phosphorus. The analysis of microstructural characterization using the mercury intrusion porosimetry method showed that the porosity was around 70%. The mechanical resistance studies showed values within the range established for this type of material. The nano-sized calcium phosphate obtained through the synthesis process has the necessary quality to be used in the production of inks for 3D printing employed in BTR.

Biography:

Dr. Fernando P.S. Guastaldi has both MSc and PhD in Oral and Maxillofacial Surgery (UNESP, Brazil). In 2012 he was a Visiting Scholar at New York University College of Dentistry (Department of Biomaterials and Biomimetics). Currently he is a Postdoctoral Research Fellow at the Skeletal Biology Research Center (SBRC), Department of Oral and Maxillofacial Surgery at Massachusetts General Hospital (Boston, MA), where he works with 3D printing of biomaterials and stem cells for mandibular tissue engineering.

Research Interests:

Biomaterials for bone tissue engineering, 3D printing of biomaterials, bone regeneration.

References:

1. Amini A, Laurencin C, Nukavarapu S. Bone tissue engineering: recent advances and challenges. Critical of Review in Biomedical Engineering 2012;40:363-408.

Dorozhkin S. Amorphous calcium (ortho) phosphates. Acta Biomater. 2010a;6(12):4457-4475.

2. Guastaldi AC, Aparecida AH. Fosfatos de cálcio de interesse biológico: importância como biomateriais, propriedades e métodos de obtenção de recobrimentos. Quím. Nova 2010;33(6): p.1352-1358.

3. Rodriguez-Chanfrau JE, Olyveira GM, Santos ML, Basmaji P, Veranes-Pantoja Y, Guastaldi AC. Bacterial cellulose hydrogel treated with phosphoric acid for used as biomaterial on bone tissue regeneration. Advance Pharmaceutical Journal 2016;1(5):133-138.

4. Temple JP, Hutton DL, Hung BP, Huri PY, Cook CA, Kondragunta R, Jia X, Grayson WL. Engineering anatomically shaped vascularized bone grafts with hASCs and 3D-printed PCL scaffolds. J Biomed Mater Res A. 2014 Dec;102(12):4317-25.

Mail Id: guastaldi@gmail.com

Contact Number: +1 857 265-8690