A novel resource utilization method of the flue gas desulfurization residue for removing Cr(VI) from electroplating wastewater

Dean Fang1,2, Xuefei Zhang1,2, Xiangxin Xue1,2

1Department of resource and environment, Northeastern University, Shenyang, PR China

2Liaoning Key Laboratory of Recycling Science for Metallurgical Resources, Shenyang, PR China

Abstract

In this research, a novel resource utilization of the residue from magnesium-based wet and calcium-based semi-dry flue gas desulfurization were investigated. The main composition of magnesium-based wet FGD residue was MgSO3·3H2O, and the main composition of calcium-based semi-dry FGD residue was CaSO3·0.5H2O. Electroplating wastewater is a common chromium-containing wastewater, the main pollutants in the wastewater are hexavalent chromium(ρCr(VI)=45 mg/L) and total chromium(ρTCr=51 mg/L). In this progress, the FGD residue could be used as a low-cost reductant to reduce Cr(VI) to Cr(III), which are less toxic and easy to separate.

When the magnesium-based wet FGD residue was used as the reductant, the optimum conditions are as follows: in the stage of Cr(VI) reduction, the optimum pH=2.5, residue dosage is 0.55 g/L, reaction time 15.0 min; in the stage of TCr precipitation, the optimum pH=7.5, the reaction time is 15.0 min. Under the optimal conditions, the residual concentrations of hexavalent chromium and total chromium are 0.035 mg/L and 0.08 mg/L, respectively.When the calcium-based semi-dry FGD residue was used as the reductant, the optimum conditions are as follows: in the stage of Cr(VI) reduction, the optimum pH=2.5, byproduct dosage is 0.65 g/L, reaction time 15.0 min; in the stage of TCr precipitation, the optimum pH=7.5, the reaction time is 15.0 min. Under the optimal conditions, the residual concentrations of hexavalent chromium and total chromium are 0.021 mg/L and 0.08 mg/L, respectively. According to the government standard (GB21900-2008), the residual concentration of heavy metal pollutants were already well below the emission limits

Keywords:residue, flue gas desulfurization, electroplating wastewater, waste treated by waste

Professional Biography (100-150 words)

Dean Fang was the doctoral student from Department of resource and environment of Northeastern University. He worked on the sewage and waste treatment field, and he has published 3 academic in reputed journals.

Email Id: 123767899@qq.com