Abstract Template

## Abstract Title: Novel chitosan derivatives for recovery of platinum and palladium from aqueous acidic solutions

Tsegaye Girma Asere1,a, Stein Mincke2,a, Ivar Verheye2, Kim Verbeken3, Christian V. Stevens2, Gijs Du Laing1

1 Laboratory of Analytical Chemistry and Applied Ecochemistry, Ghent

University (UGent), Coupure Links 653, 9000 Ghent, Belgium

2 Department of Sustainable Organic Chemistry and Technology, Ghent University

(UGent), Coupure Links 653, 9000 Ghent, Belgium

3 Department of Materials Science and Engineering, Ghent University (UGent),

Technologiepark  903, 9052 Zwijnaarde, Belgium

aThese authors made equivalent contributions.

# Abstract

Platinum (Pt) and palladium (Pd) possess favorable physical and chemical properties for wide applications in many fields such as catalysts in industries, jewelry, fuel cells, and electronics. The market demand of Pt and Pd is increasing because of the natural reserves of these metals are limited and located in few regions of the world. Therefore, there is a great concern in recovery of Pt and Pd from secondary sources for sustainable use of these metals. Chitosan is a naturally occurring polymer which has been widely investigated by many researchers as a metal recovering agent. However, there are some limitations in the use of chitosan as a metal recovering agent including low acid stability and poor mechanical properties. In order to resolve these issues, three new chitosan derivatives were prepared in this work and employed for Pd(II) and Pt(IV) removal from acidic solution. The prepared derivatives are 1,10-phenanthroline-2,9-dicarbaldehyde cross-linked chitosan (Ch-PDC), [2, 2-bipyridine]-5, 5-dicarbaldehyde cross-linked chitosan (Ch-BPDC), and glutaraldehyde cross-linked chitosan followed by grafting with 8-hydroxyquinoline-2-carbaldehyde (Ch-GA-HQC). The adsorption was very fast and reach equilibrium within 30 min. The adsorption better simulated by Langmuir isotherm compared to Freundlich isotherm. The maximum adsorption capacity of Pd(II) was found to be 262, 155 and 340 mg Pd/g of Ch-PDC, Ch-BPDC, Ch-GA-HQC, respectively. And, the maximum adsorption capacity of Pt(IV) was 114, 96 and 204 mg Pt/g of Ch-PDC, Ch-BPDC, Ch-GA-HQC, respectively. Compared to other adsorbents in literature, the adsorption capacity of the synthesised chitosan derivatives was relatively high. Therefore, these adsorbents are very promising for Pd(II) and Pt(IV) recovery from aqueous acidic solutions. Finally, the rrelevance of these adsorbents for Pd(II) adsorption in an industrial setting was tested using palladium containing industrial wastewater.

Keywords: Adsorption, chitosan, palladium, platinum

Professional Biography (100-150 words)

Mr. Tsegaye has obtained a Master of Science degree in organic chemistry from Addis Ababa University, Ethiopia in 2006. Then, he got his second master degree from Ghent University, Belgium in International Master of Science in Environmental Technology and Engineering (IMETE)” in 2013. He is an academic staff of chemistry department, Jimma University, Ethiopia. He has more than 15 years of teaching experience in the department. Since 2014 he has awarded a BOF fellowship and studding at Ghent University for his terminal degree. He has published 3 papers in peer reviewed journals.

Recent Publications (up to 5)

- Asere, T. G., De Clercq, J., Verbeken, K., Tessema, D. A., Fufa, F., Stevens, C. V., & Du Laing, G. (2017a). Uptake of arsenate by aluminum (hydr)oxide coated red scoria and pumice. Applied Geochemistry, 78, 83-95.

- Asere, T. G., Mincke, S., De Clercq, J., Verbeken, K., Tessema, D. A., Fufa, F., Stevens, C. V., & Du Laing, G. (2017b). Removal of Arsenic (V) from Aqueous Solutions Using Chitosan-Red Scoria and Chitosan-Pumice Blends. International Journal of Environmental Research and Public Health, 14(8).

- Asere, T. G., Verbeken, K., Tessema, D. A., Fufa, F., Stevens, C. V., & Du Laing, G. (2017). Adsorption of As(III) versus As(V) from aqueous solutions by cerium-loaded volcanic rocks. Environmental Science and Pollution Research, 24(25), 20446-20458.

Paste your Photograph here

Email Id: tsegaye96@gmail.com or tsegayegirma.asere@ugent.be

Any Comments: