Abstract Title: Rapid removal of phosphates, nitrates, lead, and cadmium from wastewater using fast pyrolysis biochar.

Akila G. Karunanayake, Renel Anderson

1,2Biochar Supreme Inc. & Innovochar (Washington, USA)

Abstract (not more than 300 words)

Magnetic biochar was prepared by magnetite (Fe3O4) precipitation onto the biochar’s surface from an aqueous Fe3+/Fe2+ solution upon NaOH treatment. The resulting magnetic and raw biochar was used to remove phosphates, nitrates, lead, and cadmium from water. The surface chemistry and composition of the biochars were examined by TEM, SEM, SEM-EDX, XPS, XRD, PZC, elemental analysis, and surface area measurements. Batch sorption studies were carried out from pH 2 to 10 using different adsorbate concentrations at 25, 35 and 45°C. Magnetic biochar was suspensions in the contaminated solutions were vortexed for two min and then magnetically removed. Remediated solutions were then analyzed using UV-Visible spectroscopy and AAS. Sorption studies were carried out at 25, 35 and 45°C was evaluated using the Langmuir, Freundlich, Sips, Redlich–Peterson, and Toth adsorption isotherm models. The fast adsorption kinetics and high adsorption capacities of biochar could be advantageously employed in filtration devices, columns, or as shown here, in batch operations with stirring to speed adsorption, followed by magnetic separation of the adsorbent for regeneration.

Keywords—Adsorption, Nitrates, Phosphates, Lead

Professional Biography (100-150 words)

Dr. Akila G Karunanayake has completed her PhD from Mississippi State University in 2017. Her PhD dissertation, " Douglas fir biochar for water remediation", has been written under the guidance of Dr. Todd Mlsna. She is working as the Senior Research Scientist at Biochar Supreme Inc., a premier Biochar industry and lecturer at the Department of Chemistry at Mississippi State University. She has published more than 6 papers in reputed journals and has been serving as reviewer in several journals. Her research centres on the utilization of biochar in water remediation and agricultural applications through the preparation of pre-modified and post-modified biochar.

Recent Publications (up to 5)

- Akila G. Karunanayake, Olivia A. Todd, Morgan L. Crowley, Lindsey B. Ricchetti, Charles U. Pittman, Jr., Renel Anderson and Todd E. Mlsna. Lead and cadmium remediation using magnetized fast pyrolysis biochar from Douglas fir. Chemical Engineering Journal 331 (2018): 480-491.

- Akila G. Karunanayake, Olivia A. Todd, Morgan L. Crowley, Lindsey B. Ricchetti, Charles U. Pittman, Jr., Renel Anderson and Todd E. Mlsna. Rapid removal of salicylic acid, 4-nitroaniline, benzoic acid and phthalic acid from wastewater using magnetized fast pyrolysis biochar from waste Douglas fir. Chemical Engineering Journal 319 (2017): 75-88.

- Akila G Karunanayake, Narada Bombuwala Dewage, Olivia Adele Todd, Matthew Essandoh, Renel Anderson, Todd E Mlsna, Deb Mlsna. Salicylic Acid and 4-Nitroaniline Removal from Water Using Magnetic Bio-char: An Environmental & Analytical Experiment for the Undergraduate Laboratory. Journal of Chemical Education 93 (2016): 1935-1938.

- Akila G Karunanayake, Sameera R. Gunatilake, Fathima S. Ameer, Manuel Gadogbe, Laura Smith, Deb Mlsna, Dongmao Zhang. Undergraduate Laboratory Experiment Modules for Probing Nanoparticle Interfacial Phenomena. Journal of Chemical Education 92 (2015): 1924-1927.

- Rangana Wijayapala, Akila G Karunanayake, Damion Proctor, Fei Yu, Charles U. Pittman, Jr., and Todd E. Mlsna. Hydrodeoxygenation (HDO) of Bio-oil Model Compounds with Synthesis Gas Using a Water–Gas Shift Catalyst with a Mo/Co/K Catalyst. Handbook of Climate Change Mitigation and Adaptation. Springer Book (2015): 1-34.

Email Id: akila@innovochar.com

uak1@msstate.edu