Abstract Template

Abstract Title: A Study of Anthraquinone Dyes Removal by Using Nanoparticles of Chitosans

Pyar S. Jassal*1, Sonal Gupta2, Neema Chand3 and Priti Rani4, Rajani Johar5

1,2,3,4 Department of Chemistry, SGTB Khalsa College, University of Delhi, Delhi, India

5Department of Chemistry, Matreyi College, University of Delhi, Delhi, India

Abstract

In present study, Low molecular weight chitosan naoparticles (LMWCNP) were synthesized by using low molecular weight chitosan (LMWC) and sodium tripolyphosphate for the adsorption of anthraquinone dyes from waste water using the ionic-gel technique. Size of nanoparticles was determined by “scherrer equation”. The absorbance was carried out with UV-visible spectrophotometer for Acid Green 25 (AG25) and Reactive Blue 4 (RB4) dyes solutions at λmax 644 and 598 nm respectively. The removal of dyes was dependent on the pH and the optimum adsorption was between pH 2 to 9. The extraction of dyes was linearly dependent on temperature (30,40,50 and 600C). The equilibrium parameters RL, was calculated by using the Langmuir isotherm and shows that adsorption of dyes is favorable (0<RL<1) process on the LMWCNP. The XRD images of LMWC show a crystalline nature whereas LMWCNP is amorphous one. The thermo gravimetric analysis (TGA) shows that LMWCNP are thermally more stable than LMWC. As the contact time increases, percentage removal of Acid Green 25 and Reactive Blue 4 dyes also increases. TEM images reveals the size of the LMWCNP were in the range of 45-50 nm. The maximum adsorption capacities of two dyes Acid Green 25 and Reactive Blue 4 on LMWCNP have been determined to be 9.90 mg/g and 5.56 mg/g respectively whereas it was found to be 2.30 mg/g and 2.34 mg/g  on LMWC. So LMWCNP has been proved to be a better adsorbent in comparison to LMWC.

Keywords— Low molecular weight chitosan nanoparticles (LMWCNP), Anthraquinone Dye, removal efficiency, adsorption isotherm

Professional Biography (100-150 words)

Dr. PS Jassal did graduation and post graduation from University of Rajasthan, Jaipur in 1977 and 1979. He completed the MPhil and PhD in Chemistry from University of Delhi, Delhi, India in 1983 and 1986. Dr Jassal was also given the meritorious award in MSc (chemistry) for getting Ist position. Centre of  Advanced Study, Chemistry Department of Delhi University awarded a research fellowship (JRF) for PhD work. Presently working as Vice-Principal and Associate Professor in Chemistry Department of SGTB Khalsa College, University of Delhi, Delhi, India for the last 30 years.

Recent Publications (up to 5)

1) P.S. Jassal (2018) Magnetic chitosan nanocomposites for the removal of Cr+6 ions from    aqueous solution.  Journal of basic and applied engineering research 5(1) : 26-31.

2) P. S. Jassal1, Sonal Gupta2, Neema Chand3 and Rajendra Singh4 (2016)  Chitosan nanoparticles: Synthesis and their applications.  Journal of basic and applied engineering research 3(8) : 713-716.

3)  P.S. Jassal1, Sonal Gupta2, Neema Chand3, Rajendra Singh4 and Rajni Johar (2016) Recent modifications of adsorbent for adsorption applications of dyes. Journal of basic and applied engineering research 3(11) : 986-990

4)  PS Jassal*1, Neema Chand2 and Sonal gupta3, Rajendra Singh4  (2015) Harnessing magnetic chitosan nanocomposites for the adsorption of heavy-metal ions from aqueous
medium. Journal of water resource and hydraulic engineering 4 (2) : 191-197.

5) Jassal PS and Vaishali,P (2015) Removal of crystal violet from wastewater using

different chitosans and cross-linked derivatives. Water resource management 196 : 495-504.

Paste your Photograph here

Email Id: psj.sgtb57@gmail.com

Any Comments:

Mobile : +919911171446