Nanostructured Polysaccharides Materials for Water Purification

SABU THOMAS  
Mahatma Gandhi University, Priyadarshini Hills P. O. 
Kottayam, Kerala, India -686 560,

sabuthomas@mgu.ac.in,  www.sabuthomas.com, www.iiucnn.mgu.ac.in

The design and synthesis of nano-architected cellulose  and chitin can act as efficient materials for water purification.  The talk aims to study and compare the performance of a polyvinylidene fluoride (PVDF) electrospun membrane, unmodified cellulose nanofiber (CNF) based PVDF membrane, and Meldrum’s acid (2,2-dimethyl-1,3-dioxane-4,6-dione) modified CNF-based PVDF membranes against the Fe2O3 nanoparticle filtration and crystal violet (CV) dye adsorption. Herein, we introduced a facile method to produce a unique green adsorbent material from cellulose nanofibers (CNFs) via a nonsolvent assisted procedure using Meldrum’s acid as an esterification agent to enhance the adsorption toward positively charged crystal violet dyes. Most of the surface modifications of cellulose nanofibers have been done using toxic organic solvents like pyridine, dimethyl acetate, (2,2,6,6-tetramethylpiperidin-1-yl)oxyl (TEMPO), etc. So far, this is the first report on the surface modification of cellulose nanofibers via a nonsolvent assisted procedure. Both CNF-based PVDF membranes were prepared by successive coating of modified and unmodified CNFs on to the surface of a PVDF electrospun membrane. All the demonstrated membranes showed high filtration capacity against the Fe2O3 nanoparticles. With the 10 mg/L of crystal violet (CV) aqueous solution, CV adsorption of PVDF electrospun membrane, and unmodified CNF-based PVDF membrane was around 1.368 and 2.948 mg/g of the membrane respectively, whereas it was 3.984 mg/g of the membrane by Meldrum’s acid CNF-based PVDF membrane. The demonstrated Meldrum’s acid modified CNF-based PVDF membrane was proven to be the efficient media that can concurrently eliminate the Fe2O3 nanoparticles and CV dyes from the water. The investigation into the surface chemistries of cellulose nanofibers beyond the adoption of toxic solvents can enhance the economic usefulness of the process and also yield a new eco-friendly adsorbent material that is agreeable to adsorbing various toxic pollutants.

Biography

Sabu Thomas is currently the Vice-Chancellor of Mahatma Gandhi University, Kottayam, Kerala, India. He is a Professor at the International and Inter University Centre for Nanoscience and Nanotechnology and Full Professor of Polymer Science and Engineering at the School of Chemical Sciences of Mahatma Gandhi University, Kottayam, Kerala, India. His ground-breaking research has covered the areas of polymer science and engineering, polymer nanocomposites, elastomers, polymer blends, interpenetrating polymer networks, polymer membranes, green composites and nanocomposites, nanomedicine and green nanotechnology. Prof. Thomas has received several national and international awards in recognition for his work, and recently received Honoris Causa (DSc) from the University of South Brittany, Lorient, France, in recognition for his contributions to polymer science and engineering. Prof. Thomas has published over 1400 peer- reviewed research papers, reviews and book chapters. He has co-edited more than 200 books. Currently he is having a H index of 134 with  89000 citations.

Email:  sabuthomas@mgu.ac.in