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Abstract 

The surface supported metal organic framework thin film hybrid material has been grown by using highly crystalline and orderly arranged MOF thin film heterojunction. The heterojunctions which has been fabricated with metallo-porphyrin photosensitizer (Zn (II) tetraphenylpophyrin) and photoemitter (3,9-perylenedicarboxylic acid) for triplet triplet annihilation upconversion to enhance the energy. The hybrid MOF thin film materials can be effectively utilized to transform the low energy green light into high energy blue light by overcoming the Shockley–Queisser limit. The obtained data indicate that the hybrid material can be used as one of vibrant sources of TTA UC based enhanced energy conversion materials.
It’s very important to find the new materials for solar energy conversion technologies which would help us to save energy for future generation. Harnessing the idea of triplet triplet annihilation upconversion (TTA UC) requires a smart hybrid material overcoming required distance for smooth and efficient triplet energy transfer(TEnT)
 ADDIN EN.CITE 

[1-3]
. However, the TTA UC process is the one of the best wavelength shift methodology in which the two low energy photons (hu1) having high wavelength are absorbed and transformed into one high energy photons (hu2) with low wavelength via Dexter type energy transfer mechanism
 ADDIN EN.CITE 

[3, 4]
. In our previous demonstration we have reported the triplet energy transfer between PtOEP (PtOEP = Pt(II) octaethylporphine) as sensitizer and Zn-perylene SURMOF as acceptor in acetonitrile solution5[]
 by making solid liquid interface and surface modifications. Here we will put a novel idea of suing solid-solid interface by making SURMOF-SURMOF heterojunction to study TTA UC 

The TTA UC has been studied using variety of materials to enhance the contemporary demands of solar energy 
 ADDIN EN.CITE 

[1, 6, 7]
. Moreover, notable efforts has been made to utilize the modern surface-anchored metal-organic frameworks (SURMOFs) materials in gas separation,electronics, CO2 reduction, water splitting, photovoltaic, and most recently in TTA-UC system
 ADDIN EN.CITE 

[3, 5]
 due to its controlled growth orientation, tunable pore size and highest crystallinity.Moreover, previous studies showed that the random orientation of photosensitizer which was dissolved in the solution could also hinder the transfer of triplet energy in the photoelectrochemical cell5[]
.

It has been reported that the Zn (II) tetraphenylpophyrin molecules have s and p bond between N atom and Zn+2 transition metal. The Zn+2 and N atom have p coordination due to d electrons which strengthens the (T1 ← S1) transition.As a matter of fact the Zn (II) tetraphenylpophyrin photosensitizer can also effectively utilize the long-lived S2 state (1.5 and 2.4 ps) with strong transition ( S2 ← S0 ) followed by hopping process with S2 excitation energy which needs the 
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Figure 1:  Schematic Illustration (A) is The SURMOF-SURMOF Heterostructure on Top of Coarse Glass / FTO (B) The Controlled Growth of SURMOF-SURMOF Heterostructure Which Favors the Conversion of Green Light into Blue Light via TTA UC. Pophyrin: Zn (II) Tetraphenylpophyrindicarboxylic Acid.
emitter of higher energy level8[, 9]
.
Moreover, the blue emitter-perylene molecule has lower energy level which favors the triplet energy transfer (TEnT) followed by triplet triplet annihilation mechanism from sensitizer and the exchange of triplet energy with acceptor annihilating the triplets for the formation of singlets to generating the blue light with high energy. In this work we will introduce the formation of heterojunction with Zn (II) tetraphenylpophyrin molecules as sensitizer and 3,9-perpylenedicarboxylic acids as acceptor which will be used for triplet triplet annihilation upconversion (TTA UC) shown in Figure 1.
Results and Discussions
Comparative analysis of the ultraviolet-visible (UV-vis) spectrum of Zn-perylene SURMOF, Zn-porphysin SURMOF and Zn-perylene-Zn-porphyrin heterojunction is being shown in Figure 3. The UV​-vis spectrum of Zn-perylene alone SURMOF range from 358 nm to 470nm (in brown) which is also compared with the solution of free perylene dicarboxylic
 ADDIN EN.CITE 
[10]
 acids indicating a blue shift in MOF thin film sample. The UV-vis of Zn-porphyrin shows a Sorret Band at ~ 440nm and two Q bands between 530 nm to 614 nm. The Zn (II) tetraphenylpophyrin molecule shows two Q bands which are different from free base porphyrin generating four Q bands because Zinc+2 ion coordination with porphyrin  molecule changes the symmetry of the former molecule The combined UV vis of Zn-perylene SURMOF and Zn-porphyrin SURMOF heterostructure overlaps with all the bands of both MOF thin films shown in figure 3(red).The merging of all the bands in SURMOF heterostructure is very important for efficient absorption of green light and its conversion into blue light shown in Figure 3.
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Figure 3: UV-vis Spectra of Zn-perylene SURMOF(Brown)-Zn-porphyrin SURMOF (Black) and Zn-perylene SURMOF-Zn-porphyrin SURMOF Heterojunctions (Red).  

The SEM characterization of SURMOF-SURMOF heterojunction shows that the first 20 cycles of highly crystalline Zn-perylene MOF thin film have grown the ~200nm thick film Moreover, the addition of Zn-porphyrin SURMOF Zn-perylene SURMOF could grow more ~200 nm thick shown in Figure 4.
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Figure 4: Scanning electron microscope showing the thickness of SURMOF-SURMOF heterostructure.

The phenomenon of TTA UC has been studied with SURMOF-SURMOF heterojunction which showed enhanced energy shown in Figure 5 (a,b).This give us the idea that MOF thin film based highly crystalline and versatile materials is very useful for energy conversion devices.
The obtained quantum yield efficiency of Zn-perylene SURMOF+Zn-porphyrin SURMOF heterostructure is 0.182%. Following the same method of calculation mention in the reported literature, we found that the calculated value is consistent with the literature values 
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[11]
. However, it is highly recommended to use the heterojunction for future dye sensitized solar cell devices.
[image: image4.emf]10

 

 

 

Zn-perylene-Zn-porphyrin upconverion

 

Power Dennsity / mW cm

-2

Slope ~ 1.5

440 480 520 560 600

 

 

PL intensity / a.u.

Wavelength / nm

450 nm to 520 nm

Zn-perylene-Zn-porphyrin upconverion


Figure 5: (a) Demonstration of TTA UC with SURMOF-SURMOF heterojunctions. (b) The SURMOF-SURMOF Based Intensity Dependent Behavior under 532 nm Green Light Irradiation.

Conclusion & Significance: The MOF thin film based smart and hybrid materials can be used for enhanced energy conversion triplet triplet annihilation upconversion. The studied hybrid material can be used for the future energy conversion devices. The materials used in thi demonstration can be used for dye sensitized solar cell technology. Moreover, it has been demonstrated that the photocurrent can be significantly enhanced by overcoming the longer distance which finally may overcome Shockley–Queisser limit. Further efforts in such direction may open the new avenues for exploring more MOF thin film materials for solar energy conversion devices.
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