# Title: K-doped Mixed-Phase 1D TiO2 Nanofibers on Ti Foil for Electrochemical Supercapacitor: Annealing-Free Synthesis

Hasi Rani Barai, School of Mechanical and IT Engineering, Yeungnam University, Gyeongsan 712-749, Korea

### Abstract (300 word limit)

This study demonstrated the annealing-free synthesis of K-doped mixed-phase TiO2 (anatase and rutile, AR) nanofibers (K-TNF) on Ti foil at 150 C assisted by KOH(aq.)for electrochemical supercapacitors (ESCs) applications. The aggregated network and the average diameter of K-TNF was slightly decreased with the increase of KOH(aq.) concentrations from 1 to 3 M, while the amount of K-doping, Ti3+ interstitials, and –OH functional groups was substantially increased. The TiO2 phase was entirely a mixed of rutile and anatase, AR phase. All the  K-TNF modified Ti electrodes (K-TNF/Ti) exhibited quasi-rectangular shaped cyclic voltammograms (CVs) in a wide potential range and the specific capacitance (Cs) for the optimal electrode with mixed AR phase TiO2 was ca. 70.30⁓95.18 mF/cm2,obtainedfrom the CV (scan rate, 5mV/s) and charge-discharge (CD, current density, 50µA/cm2) measurements, respectively. The higher Cs for the optimal K-TNF/Ti electrode can be ascribed to the synergistic effect of mixed AR phase, high percentage of K-doping (ca.20.20%),and Ti3+ interstitials (ca.18.20 %), respectively. The directional electron transport through the 1D channel as well as the –OH functional groups on the K-TNF surface is also contribute to enhance Cs. TheK-TNF/Ti electrode discovered excellent stability with the Cs retention of ca. 95% and a very small change of internal series resistance (Rs) and charge transfer resistance (Rct) at the electrode‖electrolyte interface after 3000-CD cycles.

Keywords:TiO2 nanofibers, mixed-phase TiO2, K-doping, hydrothermal synthesis, supercapacitors.References/Bibliography

### 1. V.V.D. Rani, K. Manzoor, D. Menon, N. Selvamurugan, S.V. Nair, Nanotechnol. 20 (2009) 195101.

### 2. V.C. Anitha, A.N. Banerjee, S.W. Joo, B.K.Min,Nanotechnol.26 (2015) 355705.

### 3. J. Zhang, J. Jiang, H. Li, X.S. Zhao, Energy Environ. Sci. 4 (2011) 4009–40015.

### 4. T. Xia, W. Zhang, Z. Wang, Y. Zhang, X. Song, J. Murowchick, V. Battaglia, G.Liu, X. Chen, Nano Energy 6 (2014) 109–118.

### 5. X. Li, J. Rong, B. Wei, ACS Nano 4 (2010) 6039–6049.

### 6. H R Barai, M M Rahman, S W Joo Electrochimica Acta 253 (2017) 563–571

Biography (150 word limit)

Prof Hasi Rani Barai is the assistant professor in the school of Mechanical and IT Engineering, Yeungnam University, Gyeongsan, Korea, from 2015. She worked as a postdoctoral research fellow in dept. of Chemistry and Nanoscience, Ewha Womans University, Seoul, Korea. She worked as a postdoctoral research fellow in KCAP(Korea center for artificial photosynthesis) in dept. of Chemistry, Sogang University, Seoul, Korea.  She received her Ph.D.  in the dept. of Chemistry, Inha University , Korea,  Master of Science (Physical organic chemistry) and BSc in Chemistry in Dhaka University, Bangladesh. She published about 41scientific jouranls.She did several invited speaker/oral/poster presentations in national/international conferences. Research interest in nanotechnology, nanomaterials,materials preprocess, energy storage devices,electrochemistry and supercapacitors.

Email:falgunchem@gmail.com/hrbarai@ynu.ac.kr

- Full Name: Hasi Rani Barai

- Personal Email: falgunchem@gmail.com

- Mobile Number:+82-1086878163

- Linked In:

- Facebook:

- Session Name/ number:

- Category: (Oral presentation/ Poster presentation)

- Date of Birth:1981.12.12

- Postal Address: [140-825] Seoul Yongsan-gu Bogwang-dong, 400-1, Room 101(2 Jangmun-ro 15ga gil), Seoul, South Korea.

Notes or Comments: