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Abstract (300 word limit)
This study demonstrated the annealing-free synthesis of K-doped mixed-phase TiO2 (anatase and rutile, AR) nanofibers (K-TNF) on Ti foil at 150 C assisted by KOH(aq.)for electrochemical supercapacitors (ESCs) applications. The aggregated network and the average diameter of K-TNF was slightly decreased with the increase of KOH(aq.) concentrations from 1 to 3 M, while the amount of K-doping, Ti3+ interstitials, and –OH functional groups was substantially increased. The TiO2 phase was entirely a mixed of rutile and anatase, AR phase. All the  K-TNF modified Ti electrodes (K-TNF/Ti) exhibited quasi-rectangular shaped cyclic voltammograms (CVs) in a wide potential range and the specific capacitance (Cs) for the optimal electrode with mixed AR phase TiO2 was ca. 70.30⁓95.18 mF/cm2,obtainedfrom the CV (scan rate, 5mV/s) and charge-discharge (CD, current density, 50µA/cm2) measurements, respectively. The higher Cs for the optimal K-TNF/Ti electrode can be ascribed to the synergistic effect of mixed AR phase, high percentage of K-doping (ca.20.20%),and Ti3+ interstitials (ca.18.20 %), respectively. The directional electron transport through the 1D channel as well as the –OH functional groups on the K-TNF surface is also contribute to enhance Cs. TheK-TNF/Ti electrode discovered excellent stability with the Cs retention of ca. 95% and a very small change of internal series resistance (Rs) and charge transfer resistance (Rct) at the electrode‖electrolyte interface after 3000-CD cycles.
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