Novel synthetic approach to YbPO4:Eu3+ and luminescence of light-emitting YbPO4:Eu3+@SiO2 hybrid nanostructure
Tamara Gavrilović1, Ivita Bite1, Jurgis Grube1, Katrīna Laganovska1, Krisjanis Smits1, Dragana Jovanović2 and Miroslav Dramićanin2
1Institute of Solid State Physics, University of Latvia, Riga, LV-1063, Latvia
2Vinča Institute of Nuclear Sciences, University of Belgrade, Belgrade, 11000, Serbia

[image: ][image: ]
T Furuta et al., J Pai n Relief 2016, 5:3(Suppl) http://dx.doi.org/10.4172/2167-0846.C1.006


J Pain Relief
ISSN: 2167-0846 JPAR an open access journa
Fibromyalgia 2016
June 15-16, 2016
Volume 5, Issue 3(Suppl)
Page 40

Statement of the Problem: YbPO4:Eu3+ and YbPO4:Eu3+@SiO2 are developed to investigate Yb3+ sensitized up-/down-conversion luminescence of Eu3+ ions. New tetragonal light-emitting photonic materials YbPO4:Eu3+ were synthesized for the first time via sol-gel route. Optical properties of as obtained YbPO4:Eu3+ and YbPO4:Eu3+@SiO2 hybrid nanomaterials were investigated by varying the dopant concentration. The structural examination of YbPO4 revealed single phase tetragonal, I41/amd, zircon type structure. XRD data showed uniform morphology and extremely high crystallinity of all synthesized samples with an average particle size around 21.5 nm. Emission spectra showed intense typical transitions of Eu3+ ions. Emission spectra recorded under 320 nm excitation demonstrated dominant 5D0→7F1, 5D0→7F2, 5D0→7F4 Eu3+ transitions, which indicates that Eu3+ is not at a site with a center of symmetry. With increasing of Eu3+ doping concentration emission intensity increased. Emission spectra recorded under 978 NM excitation exhibited an increase of dominant emissions with doping concentration and possibility of color tuning. These insights are highly important in emerging applications of YbPO4:Eu3+ doped nanocrystals. All emission spectra displayed high energy transitions in the 450-570 nm region characteristic of Eu3+ ions which are rarely observed. This unusual result shows that the phonon energies are low enough to lead to the observation of high energy lines in this region, which are comparable with fluoride, germanate and tellurite glasses. The influence of SiO2 shell on up-/down-conversion emission of YbPO4:Eu3+ showed significant suppression of the UC/DC emission with SiO2 protection due to light-scattering effect caused by the amorphous silica layer. The presence of free silanol groups on the surface not only results in high solubility in water, but also allows further conjugation with various biomolecules, which opens the possibility of distinct bio-applications. Conclusion & Significance: We obtained novel up-/down shifting material which, among distinct applications should enhance the rational design of rare-earth spectral converters.
 
 
 
 
 
 
 
 
 
 
 
 

                                                                 Figure 1. Down-conversion spectra of Eu3+ (2, 5,10 mol%)
                                                                   doped YbPO4 and YbPO4:2mol%Eu3+@SiO2 samples
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