          [image: image1.jpg]


                                                         [image: image2.png]


                                                    

Title: Experimental Analysis of Carbon Fibre Impregnation Influence on 3D Printed Composites Mechanical Properties
Author (s) Name: Rūta Rimašauskienė, Marius Rimašauskas, Tomas Kuncius, Elena Jasiūnienė,        Vaidotas Cicėnas, Paulius Griškevičius
                          Kaunas University of Technology, Lithuania
Abstract 
Additive layer manufacturing (ALM) is mainly used for production of very complex geometrical shape products.  Important to mention that it is the main advantage of ALM because without the use of the moulds various products can be produced easier and faster.  In this study a novel 3D printing technique for continuous carbon fibre reinforced polymer composites is presented. First of all, preparation of carbon fibre and adhesion testing between matrix material (PLA) and reinforcement (1 K carbon fibre) is presented. Figure 1 shows the procedure of carbon fibre modification. Tendency of tensile force changes can be clearly seen in the Figure 2, when the carbon fibre impregnated with 4 % and 8 % concentration solutions tensile force average increased from 50 N till 134 N and 150 N respectively. 
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  Fig. 1 Procedure of carbon fibre modification          Fig. 2 Results of carbon fibre tensile tests

Adhesion results between matrix material and modified carbon fibre is presented in Figure 3. Moreover, it can be concluded that solution concentration and heating time is important and can influence mechanical properties of printed parts. For the printing of samples polylactic acid (PLA) was used as matrix material and 1K not twisted carbon fibre as reinforcement material. Quality of 3D printed samples were tested by using computer tomography and optical surface morphology. Tensile tests of printed samples showed (Fig. 4) that even low content of carbon fibre in polymeric composite can increase mechanical properties significantly.  
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             Fig. 3 Adhesion testing results                 Fig. 4 Mechanical properties of printed composites
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ABS 5 mm PC 8 proc

		Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)

		0.309		-4.17		0				0.246		-5.83		0				0.281		-9.17		0

		0.403		-4.17		0				0.308		-5		0				0.374		-6.67		0.001

		0.528		-0.833		0.001				0.402		2.5		0.002				0.437		6.67		0.003

		0.623		22.5		0.004				0.464		20		0.004				0.499		23.3		0.005

		0.716		38.3		0.006				0.496		35.8		0.006				0.562		40		0.007

		0.779		55		0.008				0.587		53.3		0.008				0.686		73.3		0.011

		0.842		71.7		0.011				0.65		78.3		0.011				0.749		88.3		0.013

		0.905		87.5		0.012				0.742		93.3		0.013				0.842		103		0.016

		0.968		104		0.015				0.804		109		0.015				0.874		118		0.018

		1.03		119		0.017				0.866		125		0.018				0.967		132		0.02

		1.09		134		0.019				0.928		140		0.02				0.998		146		0.022

		1.2		155		0.022				0.96		153		0.022				1.06		158		0.024

		1.23		170		0.025				1.05		165		0.024				1.12		170		0.026

		1.29		182		0.027				1.12		178		0.026				1.22		187		0.03

		1.39		193		0.029				1.18		196		0.029				1.28		198		0.031

		1.42		204		0.031				1.24		206		0.032				1.34		208		0.034

		1.48		214		0.033				1.3		218		0.034				1.4		218		0.036

		1.54		226		0.035				1.4		228		0.035				1.47		227		0.038

		1.64		238		0.037				1.43		239		0.038				1.53		236		0.04

		1.7		255		0.04				1.52		249		0.04				1.59		244		0.042

		1.79		267		0.042				1.58		260		0.042				1.68		253		0.044

		1.85		278		0.045				1.65		269		0.044				1.75		264		0.047

		1.92		289		0.047				1.74		284		0.047				1.81		271		0.049

		1.95		299		0.049				1.8		293		0.049				1.87		278		0.051

		2.04		308		0.051				1.87		301		0.051				1.93		285		0.053

		2.07		317		0.053				1.93		310		0.053				2		291		0.055

		2.13		326		0.055				1.99		318		0.055				2.06		298		0.058

		2.23		334		0.057				2.02		327		0.057				2.15		303		0.06

		2.32		347		0.06				2.08		334		0.06				2.18		309		0.062

		2.38		354		0.062				2.18		342		0.062				2.25		314		0.064

		2.45		362		0.064				2.21		350		0.064				2.37		324		0.068

		2.48		368		0.066				2.27		358		0.066				2.43		328		0.07

		2.54		376		0.068				2.36		365		0.068				2.53		333		0.072

		2.63		383		0.07				2.37		373		0.07				2.59		338		0.074

		2.7		390		0.073				2.46		380		0.072				2.62		342		0.076

		2.76		397		0.075				2.55		387		0.074				2.68		346		0.078

		2.85		406		0.078				2.61		394		0.076				2.75		350		0.08

		2.88		412		0.08				2.65		401		0.078				2.81		355		0.083

		2.95		418		0.082				2.71		408		0.08				2.93		363		0.087

		3.04		424		0.084				2.8		418		0.084				3		368		0.089

		3.07		429		0.086				2.9		425		0.086				3.06		372		0.091

		3.13		434		0.088				2.96		431		0.087				3.12		376		0.093

		3.23		439		0.09				2.99		437		0.09				3.18		381		0.095

		3.29		443		0.092				3.05		443		0.092				3.28		385		0.097

		3.36		452		0.096				3.15		449		0.094				3.31		389		0.099

		3.43		456		0.098				3.21		455		0.096				3.37		393		0.101

		3.52		461		0.1				3.24		460		0.098				3.43		398		0.103

		3.55		464		0.102				3.33		465		0.1				3.53		404		0.106

		3.61		468		0.104				3.43		475		0.104				3.59		408		0.109

		3.68		473		0.107				3.49		480		0.106				3.68		413		0.111

		3.74		478		0.109				3.55		484		0.108				3.71		417		0.113

		3.8		482		0.111				3.61		488		0.111				3.78		421		0.115

		3.96		490		0.115				3.68		492		0.113				3.84		425		0.117

		3.99		493		0.117				3.77		496		0.115				3.9		429		0.119

		4.08		498		0.119				3.83		499		0.117				3.96		433		0.121

		4.14		502		0.121				3.86		503		0.119				4.02		438		0.123

		4.21		507		0.123				3.99		510		0.123				4.12		443		0.126

		4.27		511		0.125				4.05		513		0.125				4.21		447		0.128

		4.33		514		0.127				4.11		518		0.127				4.24		451		0.13

		4.39		518		0.129				4.17		521		0.129				4.31		455		0.132

		4.49		528		0.133				4.27		524		0.131				4.37		458		0.134

		4.55		531		0.136				4.33		528		0.133				4.43		463		0.137

		4.64		535		0.138				4.39		532		0.135				4.49		466		0.139

		4.7		539		0.14				4.42		534		0.138				4.59		469		0.141

		4.74		543		0.142				4.55		541		0.142				4.66		477		0.145

		4.8		547		0.144				4.61		544		0.144				4.74		480		0.147

		4.86		551		0.146				4.67		548		0.146				4.84		483		0.149

		4.92		555		0.148				4.77		551		0.148				4.87		487		0.151

		5.02		561		0.151				4.83		554		0.15				4.93		490		0.153

		5.11		564		0.153				4.86		558		0.152				4.99		493		0.155

		5.14		568		0.155				4.92		561		0.154				5.05		497		0.158

		5.2		573		0.157				4.99		564		0.156				5.12		500		0.16

		5.3		577		0.159				5.11		571		0.161				5.24		507		0.164

		5.36		581		0.161				5.17		574		0.163				5.3		509		0.166

		5.42		584		0.163				5.27		577		0.165				5.37		513		0.168

		5.48		588		0.166				5.33		580		0.167				5.43		516		0.17

		5.61		596		0.17				5.36		583		0.169				5.52		519		0.172

		5.67		600		0.172				5.45		586		0.171				5.55		522		0.174

		5.73		603		0.174				5.48		589		0.173				5.62		525		0.176

		5.77		608		0.176				5.58		592		0.175				5.68		528		0.178

		5.86		611		0.178				5.64		595		0.177				5.8		533		0.182

		5.89		614		0.18				5.7		598		0.179				5.87		536		0.184

		5.95		618		0.182				5.73		601		0.182				5.93		538		0.187

		6.02		622		0.184				5.8		604		0.183				5.99		541		0.189

		6.08		625		0.187				5.86		607		0.185				6.05		543		0.191

		6.2		632		0.191				5.92		609		0.187				6.15		545		0.193

		6.26		635		0.193				6.02		612		0.19				6.18		547		0.195

		6.33		638		0.195				6.08		615		0.192				6.24		549		0.197

		6.39		642		0.197				6.11		618		0.194				6.36		553		0.201

		6.48		645		0.199				6.23		623		0.198				6.46		556		0.203

		6.51		648		0.201				6.3		627		0.2				6.52		558		0.205

		6.58		651		0.203				6.39		629		0.202				6.55		560		0.207

		6.67		654		0.205				6.45		632		0.204				6.61		563		0.21

		6.76		660		0.209				6.48		634		0.206				6.71		564		0.211

		6.83		663		0.211				6.55		638		0.208				6.74		567		0.213

		6.89		666		0.213				6.61		640		0.211				6.83		568		0.216

		6.98		669		0.216				6.67		643		0.213				6.93		573		0.22

		7.04		672		0.218				6.76		647		0.215				6.99		575		0.222

		7.08		675		0.22				6.83		650		0.218				7.05		577		0.224

		7.17		678		0.222				6.89		653		0.22				7.11		579		0.226

		7.23		681		0.224				6.95		656		0.222				7.21		581		0.228

		7.33		687		0.228				7.04		658		0.224				7.27		583		0.23

		7.42		689		0.23				7.11		661		0.226				7.33		585		0.232

		7.45		693		0.232				7.14		663		0.228				7.36		588		0.234

		7.54		695		0.234				7.2		667		0.23				7.46		591		0.238

		7.61		698		0.236				7.26		669		0.232				7.52		593		0.24

		7.67		701		0.238				7.42		675		0.236				7.61		595		0.242

		7.73		704		0.24				7.48		678		0.239				7.64		598		0.244

		7.79		707		0.243				7.54		680		0.241				7.71		600		0.246

		7.89		711		0.246				7.58		683		0.243				7.77		603		0.248

		7.95		713		0.248				7.64		686		0.245				7.86		605		0.25

		7.98		717		0.25				7.73		688		0.247				7.89		608		0.252

		8.04		719		0.252				7.76		691		0.249				7.99		609		0.254

		8.14		722		0.254				7.86		693		0.251				8.11		614		0.258

		8.2		724		0.256				7.98		698		0.255				8.14		617		0.26

		8.26		728		0.258				8.01		702		0.257				8.21		619		0.262

		8.32		730		0.26				8.11		704		0.259				8.3		622		0.265

		8.45		736		0.264				8.14		707		0.261				8.33		625		0.267

		8.51		738		0.267				8.23		709		0.263				8.39		627		0.269

		8.57		740		0.269				8.29		711		0.265				8.46		631		0.271

		8.64		743		0.27				8.36		713		0.268				8.52		633		0.273

		8.7		746		0.273				8.39		716		0.27				8.58		638		0.275

		8.76		748		0.275				8.48		719		0.272				8.67		643		0.278

		8.79		751		0.277				8.54		721		0.274				8.77		646		0.28

		8.85		753		0.279				8.6		723		0.276				8.8		650		0.282

		8.98		758		0.283				8.67		726		0.278				8.86		655		0.284

		9.04		762		0.285				8.7		728		0.28				8.95		661		0.286

		9.1		764		0.287				8.76		731		0.282				9.02		667		0.289

		9.2		767		0.289				8.85		733		0.284				9.05		673		0.291

		9.26		769		0.291				8.92		736		0.286				9.11		678		0.292

		9.29		772		0.294				8.98		738		0.289				9.17		683		0.295

		9.35		774		0.296				9.01		741		0.29				9.27		692		0.298

		9.45		778		0.298				9.17		746		0.295				9.33		697		0.3

		9.57		783		0.302				9.23		748		0.297				9.39		703		0.302

		9.6		787		0.304				9.26		751		0.299				9.45		708		0.304

		9.7		789		0.306				9.35		753		0.301				9.55		712		0.306

		9.76		793		0.308				9.38		756		0.303				9.61		718		0.308

		9.82		798		0.31				9.45		758		0.305				9.67		723		0.31

		9.85		802		0.312				9.51		761		0.307				9.7		728		0.312

		9.92		807		0.315				9.6		763		0.309				9.77		733		0.314

		9.98		812		0.317				9.7		768		0.313				9.89		743		0.319

		10.1		820		0.32				9.79		771		0.315				9.95		748		0.321

		10.2		827		0.322				9.85		773		0.318				10		753		0.323

		10.2		833		0.324				9.92		776		0.32				10.1		759		0.325

		10.3		840		0.326				9.98		778		0.322				10.2		764		0.327

		10.3		847		0.328				10		781		0.324				10.2		769		0.329

		10.4		853		0.33				10.1		783		0.326				10.3		773		0.331

		10.5		860		0.332				10.2		786		0.328				10.4		778		0.333

		10.5		867		0.334				10.2		788		0.33				10.4		786		0.336

		10.6		873		0.336				10.3		790		0.332				10.5		791		0.338

		10.7		886		0.34				10.4		793		0.334				10.5		796		0.34

		10.8		892		0.342				10.4		795		0.336				10.6		801		0.342

		10.8		898		0.345				10.5		798		0.338				10.7		805		0.345

		10.9		904		0.347				10.5		801		0.34				10.7		810		0.347

		10.9		910		0.349				10.6		803		0.342				10.8		814		0.349

		11		917		0.351				10.6		806		0.344				10.9		819		0.351

		11.1		923		0.353				10.7		808		0.347				11		826		0.354

		11.1		928		0.355				10.8		813		0.35				11		830		0.356

		11.3		939		0.359				10.9		816		0.352				11.1		835		0.358

		11.3		946		0.361				10.9		818		0.354				11.2		839		0.36

		11.4		952		0.363				11		822		0.356				11.2		843		0.362

		11.5		958		0.365				11.1		825		0.358				11.3		848		0.364

		11.5		963		0.367				11.1		830		0.36				11.3		852		0.367

		11.6		969		0.369				11.2		834		0.362				11.4		856		0.369

		11.6		974		0.372				11.2		839		0.364				11.5		860		0.371

		11.7		980		0.374				11.3		844		0.366				11.6		868		0.375

		11.8		989		0.377				11.4		856		0.371				11.6		872		0.377

		11.9		995		0.379				11.5		862		0.373				11.7		876		0.379

		11.9		1000		0.381				11.6		868		0.375				11.8		879		0.381

		12		1010		0.383				11.6		873		0.377				11.9		883		0.383

		12		1010		0.385				11.7		878		0.379				11.9		888		0.385

		12.1		1020		0.387				11.8		883		0.381				11.9		891		0.387

		12.2		1020		0.389				11.8		889		0.383				12		895		0.389

		12.3		1030		0.391				11.9		893		0.385				12.1		902		0.392

		12.4		1040		0.396				11.9		899		0.387				12.2		905		0.395

		12.4		1040		0.397				12.1		908		0.391				12.2		909		0.397

		12.5		1050		0.4				12.1		913		0.393				12.3		913		0.399

		12.6		1050		0.402				12.2		918		0.395				12.4		917		0.401

		12.6		1060		0.404				12.2		923		0.398				12.4		921		0.403

		12.7		1060		0.406				12.3		928		0.4				12.5		924		0.405

		12.7		1070		0.408				12.3		933		0.402				12.5		928		0.407

		12.8		1070		0.41				12.4		938		0.404				12.6		932		0.409

		12.9		1080		0.412				12.5		943		0.406				12.7		938		0.412

		12.9		1080		0.414				12.5		948		0.408				12.8		942		0.414

		13		1090		0.416				12.7		957		0.412				12.8		946		0.416

		13.1		1090		0.418				12.7		962		0.414				12.9		949		0.418

		13.1		1100		0.42				12.8		967		0.416				12.9		953		0.42

		13.2		1100		0.423				12.9		972		0.418				13		958		0.423

		13.2		1110		0.425				12.9		976		0.42				13.1		961		0.425

		13.3		1110		0.427				13		981		0.422				13.1		965		0.427

		13.4		1120		0.429				13		986		0.425				13.2		968		0.429

		13.5		1120		0.431				13.1		991		0.427				13.3		974		0.432

		13.6		1130		0.435				13.1		993		0.428				13.4		978		0.434

		13.6		1130		0.437				13.2		998		0.43				13.4		981		0.436

		13.6		1140		0.439				13.3		1010		0.433				13.5		985		0.438

		13.7		1140		0.441				13.4		1010		0.435				13.5		989		0.44

		13.8		1150		0.443				13.4		1010		0.437				13.6		993		0.442

		13.8		1150		0.445				13.5		1020		0.439				13.7		996		0.445

		13.9		1150		0.447				13.5		1020		0.441				13.8		999		0.447

		14		1160		0.449				13.6		1030		0.443				13.9		1010		0.451

		14.1		1170		0.452				13.7		1030		0.446				13.9		1010		0.453

		14.1		1170		0.454				13.7		1040		0.448				14		1020		0.455

		14.2		1170		0.456				13.8		1040		0.45				14		1020		0.457

		14.3		1180		0.458				13.9		1050		0.454				14.1		1020		0.459

		14.3		1180		0.461				14		1050		0.456				14.2		1030		0.461

		14.4		1190		0.463				14		1060		0.458				14.3		1030		0.463

		14.4		1190		0.465				14.1		1060		0.46				14.3		1030		0.465

		14.5		1190		0.467				14.2		1070		0.462				14.4		1040		0.467

		14.5		1200		0.469				14.2		1070		0.464				14.5		1040		0.47

		14.7		1210		0.473				14.3		1080		0.466				14.5		1050		0.473

		14.7		1210		0.475				14.3		1080		0.468				14.6		1050		0.475

		14.8		1220		0.477				14.4		1080		0.47				14.6		1050		0.477

		14.9		1220		0.479				14.6		1090		0.474				14.7		1060		0.479

		15		1220		0.482				14.6		1100		0.477				14.8		1060		0.481

		15		1230		0.483				14.7		1100		0.479				14.8		1070		0.483

		15		1230		0.485				14.8		1110		0.481				14.9		1070		0.485

		15.1		1240		0.487				14.8		1110		0.483				15		1070		0.487

		15.2		1240		0.492				14.8		1110		0.485				15		1080		0.49

		15.3		1250		0.494				14.9		1120		0.487				15.1		1080		0.492

		15.4		1250		0.496				15		1120		0.489				15.2		1090		0.495

		15.5		1260		0.498				15.1		1130		0.493				15.3		1090		0.497

		15.5		1260		0.5				15.2		1130		0.495				15.3		1090		0.499

		15.5		1260		0.502				15.3		1140		0.498				15.4		1100		0.501

		15.6		1270		0.504				15.3		1140		0.5				15.4		1100		0.503

		15.7		1270		0.506				15.4		1150		0.502				15.5		1100		0.505

		15.8		1280		0.509				15.4		1150		0.504				15.6		1110		0.508

		15.8		1280		0.512				15.5		1150		0.506				15.6		1110		0.51

		15.9		1290		0.514				15.6		1160		0.508				15.7		1120		0.512

		16		1290		0.516				15.6		1160		0.51				15.8		1120		0.514

		16		1290		0.518				15.7		1170		0.514				15.8		1120		0.516

		16.1		1300		0.52				15.8		1170		0.516				15.9		1130		0.518

		16.1		1300		0.522				15.9		1180		0.518				15.9		1130		0.52

		16.2		1310		0.524				15.9		1180		0.52				16		1130		0.522

		16.3		1310		0.526				16		1180		0.522				16.1		1140		0.525

		16.4		1320		0.53				16.1		1190		0.524				16.2		1140		0.529

		16.5		1320		0.532				16.1		1190		0.527				16.3		1150		0.531

		16.5		1320		0.534				16.2		1200		0.529				16.3		1150		0.533

		16.6		1330		0.536				16.2		1200		0.531				16.4		1150		0.535

		16.7		1330		0.539				16.4		1210		0.535				16.4		1160		0.537

		16.7		1340		0.541				16.4		1210		0.537				16.5		1160		0.539

		16.8		1340		0.543				16.5		1210		0.539				16.6		1160		0.541

		16.8		1340		0.545				16.5		1220		0.541				16.6		1170		0.543

		17		1350		0.549				16.6		1220		0.543				16.7		1170		0.546

		17		1350		0.551				16.7		1230		0.545				16.8		1170		0.547

		17.1		1360		0.553				16.7		1230		0.547				16.8		1180		0.549

		17.1		1360		0.555				16.8		1230		0.549				16.9		1180		0.552

		17.2		1360		0.557				16.9		1240		0.552				16.9		1190		0.554

		17.3		1370		0.559				17		1240		0.555				17		1190		0.556

		17.3		1370		0.561				17		1250		0.557				17.1		1190		0.558

		17.4		1380		0.563				17.1		1250		0.559				17.1		1200		0.56

		17.5		1380		0.568				17.1		1250		0.561				17.2		1200		0.562

		17.6		1390		0.57				17.2		1260		0.563				17.3		1200		0.565

		17.7		1390		0.572				17.2		1260		0.565				17.4		1210		0.567

		17.7		1390		0.574				17.3		1260		0.567				17.4		1210		0.569

		17.8		1400		0.576				17.4		1270		0.57				17.5		1210		0.571

		17.8		1400		0.578				17.5		1270		0.572				17.5		1220		0.574

		17.9		1400		0.58				17.6		1280		0.575				17.6		1220		0.576

		18		1410		0.582				17.6		1280		0.577				17.7		1220		0.578

		18		1410		0.584				17.7		1280		0.579				17.7		1230		0.579

		18.1		1420		0.588				17.7		1290		0.581				17.8		1230		0.582

		18.2		1420		0.591				17.8		1290		0.583				17.9		1230		0.585

		18.3		1420		0.593				17.8		1290		0.585				17.9		1240		0.587

		18.4		1430		0.595				17.9		1300		0.587				18		1240		0.589

		18.4		1430		0.597				18		1300		0.589				18.1		1240		0.591

		18.4		1430		0.599				18		1300		0.591				18.1		1250		0.593

		18.5		1430		0.601				18.1		1310		0.593				18.2		1250		0.595

		18.6		1440		0.603				18.2		1310		0.595				18.3		1250		0.597

		18.7		1440		0.606				18.2		1310		0.597				18.3		1260		0.599

		18.7		1450		0.608				18.3		1320		0.599				18.4		1260		0.601

		18.8		1450		0.61				18.3		1320		0.601				18.5		1260		0.605

		18.9		1450		0.612				18.4		1330		0.604				18.6		1270		0.607

		18.9		1450		0.614				18.5		1330		0.606				18.6		1270		0.609

		19		1460		0.616				18.6		1340		0.609				18.7		1270		0.611

		19		1460		0.619				18.7		1340		0.612				18.8		1280		0.613

		19.1		1460		0.621				18.7		1340		0.614				18.8		1280		0.615

		19.2		1470		0.623				18.8		1350		0.616				18.9		1280		0.617

		19.3		1470		0.627				18.8		1350		0.618				18.9		1290		0.619

		19.4		1480		0.629				18.9		1350		0.62				19		1290		0.621

		19.4		1480		0.631				19		1360		0.622				19.1		1300		0.625

		19.5		1480		0.633				19.1		1360		0.624				19.2		1300		0.627

		19.5		1490		0.635				19.2		1370		0.627				19.2		1300		0.629

		19.6		1490		0.637				19.2		1370		0.629				19.3		1310		0.632

		19.7		1490		0.639				19.2		1370		0.632				19.4		1310		0.634

		19.7		1500		0.642				19.3		1380		0.634				19.4		1310		0.636

		19.8		1500		0.645				19.4		1380		0.636				19.5		1310		0.638

		19.9		1500		0.647				19.5		1380		0.638				19.5		1320		0.64

		19.9		1510		0.649				19.5		1390		0.64				19.7		1320		0.644

		20		1510		0.651				19.6		1390		0.642				19.7		1330		0.646

		20.1		1510		0.653				19.6		1390		0.644				19.8		1330		0.648

		20.2		1520		0.655				19.8		1400		0.648				19.8		1330		0.65

		20.2		1520		0.657				19.8		1400		0.65				19.9		1340		0.653

		20.3		1520		0.659				19.9		1410		0.652				20		1340		0.655

		20.4		1520		0.661				20		1410		0.655				20.1		1340		0.657

		20.4		1530		0.664				20		1410		0.657				20.1		1350		0.659

		20.5		1530		0.666				20.1		1420		0.658				20.2		1350		0.661

		20.6		1530		0.669				20.1		1420		0.661				20.3		1350		0.665

		20.6		1540		0.671				20.2		1420		0.663				20.3		1360		0.667

		20.7		1540		0.673				20.3		1430		0.666				20.4		1360		0.669

		20.7		1540		0.675				20.4		1430		0.668				20.5		1360		0.671

		20.8		1550		0.677				20.4		1430		0.67				20.6		1370		0.673

		20.9		1550		0.679				20.5		1440		0.672				20.6		1370		0.675

		21		1550		0.683				20.6		1440		0.674				20.7		1370		0.677

		21		1560		0.685				20.6		1440		0.676				20.7		1380		0.679

		21.1		1560		0.687				20.6		1450		0.678				20.8		1380		0.683

		21.2		1560		0.689				20.7		1450		0.68				20.9		1380		0.685

		21.2		1570		0.691				20.8		1460		0.684				21		1390		0.687

		21.3		1570		0.693				20.9		1460		0.686				21		1390		0.689

		21.4		1570		0.695				20.9		1460		0.688				21.1		1390		0.691

		21.4		1580		0.698				21		1470		0.69				21.1		1390		0.693

		21.5		1580		0.701				21.1		1470		0.692				21.2		1400		0.695

		21.6		1580		0.703				21.1		1470		0.694				21.3		1400		0.697

		21.6		1580		0.705				21.2		1480		0.696				21.4		1410		0.701

		21.7		1590		0.707				21.3		1480		0.698				21.4		1410		0.704

		21.8		1590		0.709				21.3		1480		0.701				21.5		1410		0.706

		21.8		1590		0.711				21.4		1490		0.703				21.6		1420		0.708

		21.9		1600		0.713				21.4		1490		0.705				21.6		1420		0.71

		22		1600		0.715				21.5		1490		0.707				21.7		1420		0.712

		22		1600		0.718				21.6		1500		0.709				21.7		1420		0.714

		22.1		1610		0.72				21.6		1500		0.711				21.8		1430		0.716

		22.1		1610		0.722				21.7		1500		0.713				21.9		1430		0.719

		22.2		1610		0.724				21.7		1500		0.715				22		1430		0.721

		22.3		1610		0.726				21.8		1510		0.717				22		1440		0.723

		22.3		1620		0.728				22		1510		0.721				22.1		1440		0.725

		22.4		1620		0.73				22		1520		0.723				22.2		1440		0.727

		22.5		1620		0.732				22.1		1520		0.725				22.2		1440		0.729

		22.5		1620		0.734				22.1		1520		0.727				22.3		1450		0.732

		22.6		1630		0.736				22.2		1530		0.73				22.3		1450		0.734

		22.7		1630		0.738				22.2		1530		0.732				22.4		1450		0.736

		22.7		1630		0.74				22.3		1530		0.734				22.5		1460		0.739

		22.8		1640		0.742				22.4		1540		0.736				22.6		1460		0.741

		22.8		1640		0.744				22.5		1540		0.739				22.6		1460		0.743

		22.9		1640		0.746				22.6		1540		0.741				22.7		1460		0.745

		22.9		1640		0.749				22.6		1550		0.743				22.7		1470		0.747

		23		1650		0.751				22.6		1550		0.745				22.8		1470		0.749

		23.1		1650		0.753				22.7		1550		0.747				22.9		1470		0.751

		23.2		1650		0.757				22.8		1560		0.749				22.9		1480		0.753

		23.3		1660		0.759				22.8		1560		0.751				23		1480		0.756

		23.3		1660		0.761				22.9		1560		0.753				23.1		1480		0.759

		23.4		1660		0.763				23		1570		0.755				23.1		1490		0.761

		23.5		1670		0.765				23.1		1570		0.76				23.2		1490		0.763

		23.5		1670		0.767				23.1		1570		0.762				23.3		1490		0.765

		23.6		1670		0.77				23.2		1580		0.764				23.3		1490		0.767

		23.6		1670		0.772				23.3		1580		0.766				23.4		1500		0.769

		23.8		1680		0.775				23.4		1580		0.768				23.5		1500		0.771

		23.8		1680		0.778				23.4		1590		0.77				23.5		1500		0.773

		23.9		1680		0.78				23.5		1590		0.772				23.6		1500		0.775

		23.9		1690		0.782				23.5		1590		0.774				23.7		1510		0.778

		24		1690		0.784				23.6		1600		0.777				23.7		1510		0.78

		24.1		1690		0.786				23.7		1600		0.779				23.8		1510		0.783

		24.1		1690		0.788				23.8		1600		0.782				23.9		1520		0.785

		24.2		1700		0.79				23.8		1610		0.784				23.9		1520		0.787

		24.3		1700		0.792				23.9		1610		0.785				24		1520		0.788

		24.4		1710		0.796				23.9		1610		0.788				24.1		1520		0.791

		24.5		1710		0.799				24		1620		0.79				24.1		1530		0.793

		24.5		1710		0.801				24.1		1620		0.792				24.2		1530		0.795

		24.6		1710		0.803				24.1		1620		0.794				24.3		1530		0.799

		24.6		1720		0.805				24.3		1630		0.798				24.4		1540		0.801

		24.7		1720		0.807				24.3		1630		0.8				24.4		1540		0.803

		24.8		1720		0.809				24.4		1630		0.802				24.5		1540		0.805

		24.8		1720		0.811				24.4		1640		0.804				24.6		1540		0.807

		24.9		1730		0.814				24.5		1640		0.806				24.6		1550		0.809

		25		1730		0.816				24.6		1640		0.809				24.7		1550		0.812

		25		1730		0.818				24.6		1650		0.811				24.7		1550		0.814

		25.1		1740		0.82				24.7		1650		0.812				24.8		1550		0.816

		25.2		1740		0.822				24.8		1660		0.817				24.9		1560		0.819

		25.2		1740		0.824				24.9		1660		0.819				25		1560		0.821

		25.3		1740		0.826				25		1660		0.821				25.1		1560		0.823

		25.3		1750		0.828				25		1670		0.823				25.1		1570		0.825

		25.4		1750		0.83				25.1		1670		0.825				25.1		1570		0.827

		25.5		1750		0.834				25.1		1670		0.827				25.2		1570		0.829

		25.6		1760		0.836				25.2		1670		0.829				25.3		1570		0.831

		25.6		1760		0.838				25.2		1680		0.831				25.3		1580		0.833

		25.7		1760		0.84				25.3		1680		0.833				25.4		1580		0.835

		25.8		1770		0.842				25.4		1690		0.838				25.5		1580		0.839

		25.8		1770		0.844				25.5		1690		0.84				25.6		1590		0.841

		25.9		1770		0.846				25.5		1690		0.842				25.6		1590		0.843

		25.9		1770		0.849				25.6		1700		0.844				25.7		1590		0.845

		26		1780		0.851				25.7		1700		0.846				25.7		1590		0.847

		26.1		1780		0.855				25.7		1700		0.848				25.8		1600		0.849

		26.2		1780		0.857				25.8		1700		0.85				25.9		1600		0.851

		26.3		1790		0.859				25.9		1710		0.852				26		1600		0.853

		26.3		1790		0.861				25.9		1710		0.854				26.1		1610		0.856

		26.4		1790		0.863				26		1710		0.857				26.1		1610		0.858

		26.5		1790		0.865				26.1		1720		0.86				26.2		1610		0.861

		26.5		1800		0.867				26.1		1720		0.862				26.2		1620		0.863

		26.6		1800		0.869				26.2		1720		0.864				26.3		1620		0.864

		26.7		1800		0.872				26.3		1730		0.865				26.4		1620		0.867

		26.7		1810		0.874				26.3		1730		0.868				26.4		1620		0.869

		26.8		1810		0.877				26.4		1730		0.87				26.5		1630		0.871

		26.8		1810		0.879				26.5		1730		0.872				26.5		1630		0.873

		26.9		1810		0.881				26.6		1740		0.876				26.6		1630		0.876

		27		1820		0.883				26.6		1740		0.878				26.7		1630		0.878

		27		1820		0.885				26.7		1750		0.88				26.7		1640		0.88

		27.1		1820		0.887				26.8		1750		0.882				26.8		1640		0.882

		27.2		1820		0.889				26.9		1750		0.884				26.9		1640		0.884

		27.2		1830		0.892				26.9		1750		0.886				26.9		1650		0.886

		27.3		1830		0.894				27		1760		0.889				27		1650		0.889

		27.4		1830		0.896				27		1760		0.891				27		1650		0.891

		27.5		1840		0.899				27.1		1760		0.893				27.1		1650		0.893

		27.5		1840		0.901				27.1		1770		0.895				27.2		1660		0.896

		27.6		1840		0.902				27.2		1770		0.897				27.3		1660		0.898

		27.6		1850		0.905				27.3		1770		0.899				27.4		1660		0.9

		27.7		1850		0.907				27.4		1770		0.901				27.4		1660		0.902

		27.8		1850		0.909				27.4		1780		0.903				27.5		1670		0.904

		27.9		1860		0.912				27.5		1780		0.905				27.5		1670		0.906

		27.9		1860		0.914				27.5		1780		0.907				27.6		1670		0.908

		28		1870		0.916				27.6		1780		0.91				27.6		1670		0.911

		28.1		1870		0.918				27.6		1790		0.912				27.7		1680		0.913

		28.1		1870		0.92				27.8		1790		0.916				27.8		1680		0.915

		28.2		1880		0.922				27.9		1800		0.918				27.9		1680		0.918

		28.2		1880		0.924				27.9		1800		0.92				27.9		1690		0.92

		28.3		1880		0.927				28		1800		0.922				28		1690		0.922

		28.3		1880		0.929				28		1800		0.924				28		1690		0.924

		28.5		1890		0.933				28.1		1810		0.926				28.1		1690		0.926

		28.5		1890		0.935				28.1		1810		0.928				28.2		1700		0.928

		28.6		1890		0.937				28.2		1810		0.93				28.2		1700		0.93

		28.7		1900		0.939				28.3		1820		0.934				28.3		1700		0.932

		28.7		1900		0.941				28.4		1820		0.936				28.4		1710		0.935

		28.8		1900		0.943				28.5		1820		0.939				28.5		1710		0.937

		28.9		1910		0.945				28.5		1830		0.941				28.5		1710		0.94

		28.9		1910		0.947				28.6		1830		0.942				28.6		1710		0.942

		29		1910		0.949				28.7		1830		0.945				28.7		1720		0.944

		29.1		1920		0.952				28.7		1830		0.947				28.7		1720		0.946

		29.1		1920		0.955				28.8		1840		0.949				28.8		1720		0.948

		29.2		1920		0.957				28.9		1840		0.951				28.8		1730		0.95

		29.2		1920		0.959				29		1850		0.955				28.9		1730		0.952

		29.3		1930		0.961				29		1850		0.957				29		1730		0.955

		29.4		1930		0.963				29.1		1850		0.959				29.1		1740		0.957

		29.4		1930		0.965				29.2		1850		0.961				29.1		1740		0.959

		29.5		1930		0.967				29.2		1860		0.963				29.2		1740		0.961

		29.6		1940		0.969				29.3		1860		0.966				29.2		1750		0.963

		29.7		1940		0.973				29.4		1860		0.968				29.3		1750		0.965

		29.7		1950		0.975				29.4		1870		0.97				29.4		1750		0.968

		29.8		1950		0.977				29.4		1870		0.972				29.4		1750		0.97

		29.9		1950		0.979				29.6		1880		0.975				29.5		1760		0.972

		29.9		1950		0.981				29.6		1880		0.977				29.6		1760		0.976

		30		1960		0.983				29.7		1880		0.979				29.7		1760		0.978

		30.1		1960		0.986				29.7		1880		0.981				29.7		1770		0.98

		30.1		1960		0.988				29.8		1890		0.983				29.8		1770		0.982

		30.2		1960		0.99				29.9		1890		0.985				29.9		1770		0.984

		30.3		1970		0.994				29.9		1890		0.988				29.9		1770		0.986

		30.4		1970		0.996				30		1900		0.989				30		1780		0.989

		30.5		1970		0.998				30.1		1900		0.993				30.1		1780		0.991

		30.5		1980		1				30.2		1900		0.996				30.2		1780		0.994

		30.6		1980		1				30.2		1910		0.998				30.2		1790		0.996

		30.6		1980		1				30.3		1910		1				30.3		1790		0.998

		30.7		1980		1.01				30.4		1910		1				30.3		1790		1

		30.8		1990		1.01				30.4		1910		1				30.4		1790		1

		30.8		1990		1.01				30.5		1920		1.01				30.5		1800		1

		31		1990		1.02				30.5		1920		1.01				30.5		1800		1.01

		31		2000		1.02				30.7		1930		1.01				30.6		1800		1.01

		31.1		2000		1.02				30.7		1930		1.01				30.6		1800		1.01

		31.1		2000		1.02				30.8		1930		1.02				30.8		1810		1.01

		31.2		2000		1.02				30.9		1930		1.02				30.8		1810		1.02

		31.2		2010		1.03				30.9		1940		1.02				30.9		1810		1.02

		31.3		2010		1.03				31		1940		1.02				30.9		1810		1.02

		31.4		2010		1.03				31.1		1940		1.03				31		1820		1.02

		31.5		2020		1.03				31.1		1950		1.03				31		1820		1.02

		31.6		2020		1.04				31.2		1950		1.03				31.1		1820		1.03

		31.6		2020		1.04				31.3		1950		1.03				31.2		1820		1.03

		31.7		2020		1.04				31.3		1960		1.03				31.3		1830		1.03

		31.7		2030		1.04				31.4		1960		1.04				31.3		1830		1.03

		31.8		2030		1.04				31.4		1960		1.04				31.4		1830		1.04

		31.9		2030		1.05				31.5		1960		1.04				31.5		1840		1.04

		31.9		2030		1.05				31.6		1970		1.04				31.5		1840		1.04

		32.1		2040		1.05				31.7		1970		1.05				31.6		1840		1.04

		32.1		2040		1.05				31.7		1970		1.05				31.7		1840		1.04

		32.2		2040		1.06				31.8		1970		1.05				31.7		1840		1.05

		32.3		2050		1.06				31.9		1980		1.05				31.8		1850		1.05

		32.3		2050		1.06				31.9		1980		1.06				31.9		1850		1.05

		32.4		2050		1.06				32		1990		1.06				32		1850		1.05

		32.4		2050		1.07				32.1		1990		1.06				32.1		1860		1.06

		32.5		2060		1.07				32.1		1990		1.06				32.1		1860		1.06

		32.6		2060		1.07				32.2		1990		1.06				32.2		1860		1.06

		32.7		2060		1.07				32.3		2000		1.07				32.2		1860		1.06

		32.7		2070		1.08				32.3		2000		1.07				32.3		1870		1.07

		32.8		2070		1.08				32.4		2000		1.07				32.4		1870		1.07

		32.9		2070		1.08				32.5		2010		1.07				32.5		1870		1.07

		32.9		2070		1.08				32.6		2010		1.08				32.5		1880		1.07

		33		2070		1.08				32.6		2010		1.08				32.6		1880		1.08

		33.1		2080		1.09				32.7		2010		1.08				32.7		1880		1.08

		33.2		2080		1.09				32.8		2020		1.08				32.7		1880		1.08

		33.2		2080		1.09				32.8		2020		1.08				32.8		1890		1.08

		33.3		2090		1.09				32.9		2020		1.09				32.9		1890		1.08

		33.3		2090		1.1				33		2030		1.09				32.9		1890		1.09

		33.4		2090		1.1				33		2030		1.09				33		1890		1.09

		33.5		2090		1.1				33.1		2030		1.09				33.1		1900		1.09

		33.5		2100		1.1				33.2		2040		1.1				33.1		1900		1.09

		33.6		2100		1.1				33.2		2040		1.1				33.2		1900		1.1

		33.6		2100		1.11				33.3		2040		1.1				33.2		1900		1.1

		33.8		2100		1.11				33.4		2040		1.1				33.3		1910		1.1

		33.9		2110		1.11				33.4		2050		1.1				33.4		1910		1.1

		33.9		2110		1.11				33.5		2050		1.11				33.4		1910		1.1

		34		2110		1.12				33.6		2050		1.11				33.5		1910		1.11

		34		2120		1.12				33.7		2050		1.11				33.6		1920		1.11

		34.1		2120		1.12				33.7		2060		1.11				33.7		1920		1.11

		34.2		2120		1.12				33.8		2060		1.12				33.7		1920		1.11

		34.2		2120		1.12				33.8		2060		1.12				33.8		1930		1.12

		34.3		2130		1.13				33.9		2060		1.12				33.9		1930		1.12

		34.4		2130		1.13				34		2070		1.12				33.9		1930		1.12

		34.4		2130		1.13				34		2070		1.12				34		1930		1.12

		34.5		2130		1.13				34.1		2070		1.13				34.1		1930		1.12

		34.5		2140		1.14				34.2		2080		1.13				34.1		1940		1.13

		34.6		2140		1.14				34.2		2080		1.13				34.2		1940		1.13

		34.7		2140		1.14				34.3		2080		1.13				34.3		1940		1.13

		34.8		2140		1.14				34.4		2080		1.14				34.3		1950		1.13

		34.9		2150		1.15				34.4		2090		1.14				34.4		1950		1.14

		35		2150		1.15				34.5		2090		1.14				34.5		1950		1.14

		35		2150		1.15				34.5		2090		1.14				34.5		1950		1.14

		35		2160		1.15				34.6		2090		1.14				34.6		1960		1.14

		35.1		2160		1.15				34.8		2100		1.15				34.7		1960		1.14

		35.2		2160		1.16				34.8		2100		1.15				34.7		1960		1.15

		35.3		2160		1.16				34.8		2100		1.15				34.8		1960		1.15

		35.3		2170		1.16				34.9		2110		1.15				34.9		1970		1.15

		35.4		2170		1.16				35		2110		1.16				35		1970		1.15

		35.5		2170		1.17				35.1		2110		1.16				35		1970		1.16

		35.6		2180		1.17				35.1		2110		1.16				35.1		1970		1.16

		35.6		2180		1.17				35.2		2120		1.16				35.1		1980		1.16

		35.7		2180		1.17				35.3		2120		1.16				35.2		1980		1.16

		35.7		2180		1.18				35.3		2120		1.17				35.3		1980		1.16

		35.8		2180		1.18				35.3		2120		1.17				35.4		1990		1.17

		35.9		2190		1.18				35.4		2130		1.17				35.4		1990		1.17

		36		2190		1.18				35.5		2130		1.17				35.5		1990		1.17

		36		2190		1.18				35.5		2130		1.18				35.5		1990		1.17

		36.1		2200		1.19				35.6		2130		1.18				35.6		1990		1.18

		36.2		2200		1.19				35.7		2140		1.18				35.7		2000		1.18

		36.2		2200		1.19				35.8		2140		1.18				35.7		2000		1.18

		36.3		2200		1.19				35.9		2140		1.19				35.8		2000		1.18

		36.4		2210		1.2				35.9		2150		1.19				35.8		2000		1.18

		36.5		2210		1.2				36		2150		1.19				36		2010		1.19

		36.5		2210		1.2				36		2150		1.19				36		2010		1.19

		36.5		2210		1.2				36.1		2150		1.19				36.1		2020		1.19

		36.7		2220		1.21				36.2		2160		1.2				36.2		2020		1.19

		36.8		2220		1.21				36.3		2160		1.2				36.2		2020		1.2

		36.8		2220		1.21				36.3		2160		1.2				36.3		2020		1.2

		36.9		2230		1.21				36.4		2170		1.2				36.3		2030		1.2

		37		2230		1.22				36.5		2170		1.21				36.4		2030		1.2

		37		2230		1.22				36.6		2170		1.21				36.5		2030		1.21

		37.1		2230		1.22				36.6		2170		1.21				36.6		2030		1.21

		37.1		2230		1.22				36.7		2180		1.21				36.7		2040		1.21

		37.2		2240		1.22				36.7		2180		1.21				36.7		2040		1.21

		37.3		2240		1.23				36.8		2180		1.22				36.7		2040		1.21

		37.3		2240		1.23				36.8		2180		1.22				36.8		2040		1.22

		37.4		2250		1.23				37		2190		1.22				36.9		2050		1.22

		37.5		2250		1.23				37		2190		1.23				37		2050		1.22

		37.5		2250		1.23				37.1		2190		1.23				37.1		2050		1.22

		37.6		2250		1.24				37.2		2190		1.23				37.1		2060		1.23

		37.6		2250		1.24				37.2		2200		1.23				37.2		2060		1.23

		37.7		2260		1.24				37.2		2200		1.23				37.2		2060		1.23

		37.8		2260		1.24				37.3		2200		1.23				37.3		2060		1.23

		37.9		2260		1.25				37.4		2200		1.24				37.4		2070		1.23

		37.9		2270		1.25				37.4		2210		1.24				37.4		2070		1.24

		38		2270		1.25				37.6		2210		1.24				37.5		2070		1.24

		38.1		2270		1.25				37.7		2210		1.24				37.6		2070		1.24

		38.1		2270		1.25				37.7		2220		1.25				37.6		2080		1.24

		38.2		2270		1.26				37.7		2220		1.25				37.7		2080		1.25

		38.2		2280		1.26				37.8		2220		1.25				37.7		2080		1.25

		38.3		2280		1.26				37.9		2220		1.25				37.8		2080		1.25

		38.4		2280		1.26				37.9		2230		1.26				37.9		2090		1.25

		38.5		2290		1.27				38		2230		1.26				38		2090		1.25

		38.5		2290		1.27				38.2		2230		1.26				38		2090		1.26

		38.6		2290		1.27				38.2		2240		1.26				38.1		2090		1.26

		38.7		2290		1.27				38.3		2240		1.27				38.1		2100		1.26

		38.7		2290		1.27				38.3		2240		1.27				38.2		2100		1.26

		38.8		2300		1.28				38.4		2250		1.27				38.3		2100		1.27

		38.9		2300		1.28				38.4		2250		1.27				38.3		2100		1.27

		38.9		2300		1.28				38.5		2250		1.27				38.4		2110		1.27

		39		2310		1.28				38.6		2250		1.28				38.5		2110		1.27

		39.1		2310		1.29				38.7		2260		1.28				38.5		2110		1.27

		39.2		2310		1.29				38.7		2260		1.28				38.6		2110		1.28

		39.2		2310		1.29				38.7		2260		1.28				38.6		2120		1.28

		39.3		2310		1.29				38.8		2260		1.28				38.8		2120		1.28

		39.4		2320		1.3				38.9		2270		1.29				38.8		2120		1.28

		39.4		2320		1.3				39		2270		1.29				38.9		2120		1.29

		39.5		2320		1.3				39		2270		1.29				39		2130		1.29

		39.5		2320		1.3				39.1		2270		1.29				39		2130		1.29

		39.6		2330		1.3				39.1		2280		1.29				39.1		2130		1.29

		39.7		2330		1.31				39.2		2280		1.3				39.2		2130		1.29

		39.8		2330		1.31				39.3		2280		1.3				39.2		2140		1.3

		39.8		2330		1.31				39.4		2280		1.3				39.3		2140		1.3

		39.9		2340		1.31				39.4		2290		1.3				39.4		2140		1.3

		39.9		2340		1.32				39.5		2290		1.31				39.5		2150		1.3

		40.1		2340		1.32				39.6		2290		1.31				39.5		2150		1.31

		40.1		2350		1.32				39.6		2290		1.31				39.6		2150		1.31

		40.2		2350		1.32				39.7		2300		1.31				39.6		2150		1.31

		40.3		2350		1.33				39.7		2300		1.31				39.7		2150		1.31

		40.3		2350		1.33				39.8		2300		1.32				39.8		2160		1.31

		40.4		2360		1.33				39.9		2310		1.32				39.9		2160		1.32

		40.4		2360		1.33				40		2310		1.32				40		2160		1.32

		40.5		2360		1.33				40		2310		1.32				40		2170		1.32

		40.6		2360		1.34				40.1		2310		1.33				40.1		2170		1.32

		40.7		2370		1.34				40.1		2320		1.33				40.1		2170		1.33

		40.8		2370		1.34				40.2		2320		1.33				40.2		2170		1.33

		40.8		2370		1.34				40.3		2320		1.33				40.2		2180		1.33

		40.9		2370		1.35				40.3		2320		1.33				40.3		2180		1.33

		40.9		2380		1.35				40.4		2320		1.34				40.4		2180		1.33

		41		2380		1.35				40.4		2330		1.34				40.5		2180		1.34

		41.1		2380		1.35				40.5		2330		1.34				40.5		2190		1.34

		41.1		2380		1.35				40.6		2330		1.34				40.6		2190		1.34

		41.2		2390		1.36				40.6		2340		1.34				40.6		2190		1.34

		41.3		2390		1.36				40.7		2340		1.35				40.7		2190		1.35

		41.3		2390		1.36				40.7		2340		1.35				40.8		2200		1.35

		41.4		2400		1.36				40.8		2340		1.35				40.8		2200		1.35

		41.5		2400		1.37				40.9		2350		1.36				40.9		2200		1.35

		41.5		2400		1.37				41		2350		1.36				41		2200		1.36

		41.6		2400		1.37				41.1		2350		1.36				41		2210		1.36

		41.7		2410		1.37				41.1		2350		1.36				41.1		2210		1.36

		41.7		2410		1.38				41.2		2360		1.36				41.2		2210		1.36

		41.8		2410		1.38				41.2		2360		1.37				41.2		2210		1.36

		41.9		2420		1.38				41.3		2360		1.37				41.3		2220		1.37

		42		2420		1.38				41.4		2360		1.37				41.4		2220		1.37

		42		2420		1.39				41.5		2370		1.37				41.5		2220		1.37

		42.1		2420		1.39				41.5		2370		1.37				41.6		2220		1.37

		42.2		2430		1.39				41.6		2370		1.38				41.6		2230		1.38

		42.2		2430		1.39				41.6		2380		1.38				41.7		2230		1.38

		42.3		2430		1.39				41.7		2380		1.38				41.8		2230		1.38

		42.4		2430		1.4				41.8		2380		1.38				41.8		2230		1.38

		42.5		2440		1.4				41.9		2380		1.39				41.9		2240		1.38

		42.6		2440		1.4				41.9		2380		1.39				42		2240		1.39

		42.6		2440		1.4				42		2390		1.39				42		2240		1.39

		42.7		2450		1.41				42.1		2390		1.39				42		2240		1.39

		42.8		2450		1.41				42.1		2390		1.39				42.1		2250		1.39

		42.8		2450		1.41				42.2		2400		1.4				42.2		2250		1.4

		42.8		2450		1.41				42.2		2400		1.4				42.3		2250		1.4

		42.9		2460		1.41				42.3		2400		1.4				42.3		2250		1.4

		43		2460		1.42				42.4		2400		1.4				42.4		2260		1.4

		43.1		2460		1.42				42.4		2400		1.4				42.5		2260		1.4

		43.2		2470		1.42				42.5		2410		1.41				42.5		2260		1.41

		43.2		2470		1.43				42.6		2410		1.41				42.6		2270		1.41

		43.3		2470		1.43				42.6		2410		1.41				42.6		2270		1.41

		43.4		2470		1.43				42.7		2410		1.41				42.7		2270		1.41

		43.4		2480		1.43				42.8		2420		1.42				42.8		2270		1.42

		43.5		2480		1.43				42.8		2420		1.42				42.9		2280		1.42

		43.6		2480		1.44				42.9		2420		1.42				43		2280		1.42

		43.7		2490		1.44				43		2420		1.42				43		2280		1.42

		43.7		2490		1.44				43.1		2430		1.42				43		2280		1.42

		43.8		2490		1.44				43.1		2430		1.43				43.1		2290		1.43

		43.9		2490		1.45				43.2		2430		1.43				43.2		2290		1.43

		43.9		2500		1.45				43.2		2440		1.43				43.3		2300		1.43

		44		2500		1.45				43.3		2440		1.43				43.4		2300		1.43

		44		2500		1.45				43.4		2440		1.44				43.4		2300		1.44

		44.1		2500		1.45				43.4		2440		1.44				43.5		2300		1.44

		44.2		2510		1.46				43.5		2440		1.44				43.5		2310		1.44

		44.3		2510		1.46				43.6		2450		1.44				43.6		2310		1.44

		44.3		2510		1.46				43.6		2450		1.44				43.7		2310		1.45

		44.4		2520		1.46				43.7		2450		1.45				43.8		2310		1.45

		44.4		2520		1.47				43.8		2460		1.45				43.9		2320		1.45

		44.5		2520		1.47				43.9		2460		1.45				43.9		2320		1.45

		44.6		2530		1.47				43.9		2460		1.45				44		2330		1.46

		44.6		2530		1.47				44		2460		1.46				44		2330		1.46

		44.7		2530		1.47				44.1		2470		1.46				44.1		2330		1.46

		44.8		2530		1.48				44.1		2470		1.46				44.2		2330		1.46

		44.8		2540		1.48				44.2		2470		1.46				44.2		2340		1.46

		44.9		2540		1.48				44.2		2470		1.47				44.3		2340		1.47

		45		2540		1.48				44.4		2480		1.47				44.4		2340		1.47

		45		2540		1.49				44.5		2480		1.47				44.5		2350		1.47

		45.1		2550		1.49				44.5		2480		1.47				44.5		2350		1.47

		45.2		2550		1.49				44.5		2490		1.48				44.6		2350		1.48

		45.2		2550		1.49				44.6		2490		1.48				44.7		2350		1.48

		45.3		2550		1.49				44.7		2490		1.48				44.8		2360		1.48

		45.4		2560		1.5				44.7		2490		1.48				44.8		2360		1.48

		45.5		2560		1.5				44.8		2500		1.48				44.9		2360		1.48

		45.5		2560		1.5				44.9		2500		1.49				44.9		2370		1.49

		45.6		2560		1.5				45		2500		1.49				45		2370		1.49

		45.6		2570		1.51				45		2500		1.49				45.1		2370		1.49

		45.7		2570		1.51				45.1		2510		1.49				45.1		2370		1.49

		45.7		2570		1.51				45.1		2510		1.5				45.2		2380		1.5

		45.8		2580		1.51				45.2		2510		1.5				45.3		2380		1.5

		45.9		2580		1.51				45.3		2510		1.5				45.3		2380		1.5

		46		2580		1.52				45.4		2510		1.5				45.4		2380		1.5

		46.1		2580		1.52				45.4		2520		1.5				45.5		2380		1.5

		46.1		2590		1.52				45.5		2520		1.51				45.6		2390		1.51

		46.2		2590		1.52				45.6		2520		1.51				45.6		2390		1.51

		46.2		2590		1.53				45.6		2530		1.51				45.7		2390		1.51

		46.3		2590		1.53				45.7		2530		1.51				45.8		2390		1.51

		46.3		2590		1.53				45.8		2530		1.52				45.8		2400		1.52

		46.4		2600		1.53				45.8		2530		1.52				45.9		2400		1.52

		46.5		2600		1.53				45.9		2530		1.52				45.9		2400		1.52

		46.6		2600		1.54				46		2540		1.52				46		2400		1.52

		46.6		2600		1.54				46		2540		1.53				46		2410		1.52

		46.7		2610		1.54				46.1		2540		1.53				46.1		2410		1.53

		46.8		2610		1.54				46.2		2550		1.53				46.2		2410		1.53

		46.8		2610		1.54				46.2		2550		1.53				46.3		2420		1.53

		46.9		2610		1.55				46.3		2550		1.53				46.3		2420		1.53

		47		2620		1.55				46.4		2550		1.54				46.4		2420		1.54

		47		2620		1.55				46.4		2560		1.54				46.4		2420		1.54

		47.1		2620		1.55				46.5		2560		1.54				46.5		2420		1.54

		47.2		2620		1.56				46.6		2560		1.54				46.6		2430		1.54

		47.3		2630		1.56				46.7		2570		1.55				46.6		2430		1.54

		47.3		2630		1.56				46.7		2570		1.55				46.8		2430		1.55

		47.4		2630		1.56				46.8		2570		1.55				46.9		2440		1.55

		47.5		2630		1.57				46.9		2570		1.55				46.9		2440		1.55

		47.5		2640		1.57				46.9		2570		1.55				46.9		2440		1.55

		47.6		2640		1.57				47		2580		1.56				47		2440		1.56

		47.6		2640		1.57				47		2580		1.56				47.1		2450		1.56

		47.8		2640		1.58				47.1		2580		1.56				47.1		2450		1.56

		47.8		2650		1.58				47.2		2590		1.57				47.2		2450		1.56

		47.9		2650		1.58				47.3		2590		1.57				47.3		2450		1.56

		47.9		2650		1.58				47.4		2590		1.57				47.4		2460		1.57

		48		2650		1.58				47.5		2590		1.57				47.4		2460		1.57

		48.1		2660		1.59				47.5		2600		1.57				47.5		2460		1.57

		48.1		2660		1.59				47.5		2600		1.58				47.5		2460		1.57

		48.2		2660		1.59				47.6		2600		1.58				47.6		2470		1.58

		48.3		2660		1.59				47.7		2600		1.58				47.7		2470		1.58

		48.4		2670		1.6				47.8		2610		1.58				47.8		2470		1.58

		48.4		2670		1.6				47.8		2610		1.58				47.8		2470		1.58

		48.5		2670		1.6				47.9		2610		1.59				47.9		2480		1.58

		48.6		2670		1.6				48		2610		1.59				47.9		2480		1.59

		48.6		2670		1.6				48		2610		1.59				48		2480		1.59

		48.7		2680		1.61				48.1		2620		1.59				48.1		2480		1.59

		48.7		2680		1.61				48.1		2620		1.6				48.1		2490		1.59

		48.8		2680		1.61				48.2		2620		1.6				48.2		2490		1.6

		48.9		2680		1.61				48.3		2620		1.6				48.3		2490		1.6

		49		2690		1.62				48.4		2630		1.6				48.3		2490		1.6

		49		2690		1.62				48.4		2630		1.61				48.4		2490		1.6

		49.1		2690		1.62				48.5		2630		1.61				48.4		2500		1.6

		49.1		2690		1.62				48.6		2640		1.61				48.6		2500		1.61

		49.2		2690		1.62				48.7		2640		1.61				48.6		2500		1.61

		49.3		2700		1.63				48.7		2640		1.61				48.7		2510		1.61

		49.4		2700		1.63				48.8		2640		1.62				48.8		2510		1.61

		49.4		2700		1.63				48.8		2650		1.62				48.8		2510		1.62

		49.5		2710		1.63				48.9		2650		1.62				48.9		2510		1.62

		49.6		2710		1.64				49		2660		1.62				48.9		2510		1.62

		49.6		2710		1.64				49.1		2660		1.63				49		2520		1.62

		49.7		2710		1.64				49.2		2660		1.63				49.1		2520		1.63

		49.7		2710		1.64				49.2		2660		1.63				49.2		2520		1.63

		49.8		2720		1.64				49.3		2660		1.63				49.2		2520		1.63

		49.9		2720		1.65				49.4		2670		1.63				49.3		2530		1.63

		50		2720		1.65				49.4		2670		1.64				49.4		2530		1.63

		50		2720		1.65				49.5		2670		1.64				49.4		2530		1.64

		50.1		2730		1.65				49.6		2680		1.64				49.5		2530		1.64

		50.1		2730		1.66				49.6		2680		1.65				49.5		2540		1.64

		50.2		2730		1.66				49.7		2680		1.65				49.6		2540		1.64

		50.3		2730		1.66				49.8		2690		1.65				49.7		2540		1.65

		50.3		2740		1.66				49.9		2690		1.65				49.8		2540		1.65

		50.4		2740		1.66				49.9		2690		1.65				49.8		2550		1.65

		50.6		2740		1.67				50		2690		1.66				49.9		2550		1.65

		50.6		2740		1.67				50.1		2700		1.66				49.9		2550		1.65

		50.7		2750		1.67				50.2		2700		1.66				50		2550		1.66

		50.7		2750		1.67				50.2		2700		1.66				50.1		2550		1.66

		50.8		2750		1.68				50.3		2700		1.67				50.1		2560		1.66

		50.9		2750		1.68				50.3		2710		1.67				50.2		2560		1.66

		50.9		2750		1.68				50.4		2710		1.67				50.3		2560		1.67

		51		2760		1.68				50.4		2710		1.67				50.4		2560		1.67

		51.1		2760		1.69				50.5		2720		1.67				50.5		2570		1.67

		51.1		2760		1.69				50.6		2720		1.68				50.5		2570		1.67

		51.2		2770		1.69				50.7		2720		1.68				50.6		2570		1.67

		51.3		2770		1.69				50.7		2720		1.68				50.6		2570		1.68

		51.3		2770		1.69				50.8		2730		1.68				50.7		2580		1.68

		51.4		2770		1.7				50.8		2730		1.68				50.8		2580		1.68

		51.4		2770		1.7				50.9		2730		1.69				50.8		2580		1.68

		51.5		2780		1.7				51		2730		1.69				50.9		2580		1.69

		51.6		2780		1.7				51		2740		1.69				51		2590		1.69

		51.7		2780		1.71				51.1		2740		1.69				51.1		2590		1.69

		51.7		2780		1.71				51.2		2740		1.7				51.1		2590		1.69

		51.8		2790		1.71				51.3		2750		1.7				51.2		2590		1.69

		51.9		2790		1.71				51.3		2750		1.7				51.3		2600		1.7

		51.9		2790		1.72				51.4		2750		1.7				51.3		2600		1.7

		52		2790		1.72				51.5		2750		1.71				51.4		2600		1.7

		52.1		2800		1.72				51.5		2750		1.71				51.4		2600		1.7

		52.1		2800		1.72				51.6		2760		1.71				51.5		2610		1.71

		52.3		2800		1.73				51.7		2760		1.71				51.6		2610		1.71

		52.3		2800		1.73				51.8		2760		1.71				51.6		2610		1.71

		52.4		2800		1.73				51.8		2760		1.72				51.7		2610		1.71

		52.5		2790		1.73				51.9		2770		1.72				51.8		2620		1.71

		52.5		2790		1.73				51.9		2770		1.72				51.8		2620		1.72

		52.6		2790		1.74				52		2770		1.72				51.9		2620		1.72

		52.6		2800		1.74				52.1		2770		1.73				52		2620		1.72

		52.7		2800		1.74				52.1		2780		1.73				52.1		2620		1.72

		52.8		2800		1.74				52.2		2780		1.73				52.1		2630		1.73

		52.9		2810		1.75				52.3		2780		1.73				52.2		2630		1.73

		52.9		2810		1.75				52.3		2780		1.73				52.2		2630		1.73

		53		2810		1.75				52.4		2790		1.74				52.3		2630		1.73

		53		2810		1.75				52.4		2790		1.74				52.3		2640		1.73

		53.1		2810		1.75				52.5		2790		1.74				52.4		2640		1.74

		53.2		2810		1.76				52.6		2790		1.74				52.5		2640		1.74

		53.2		2820		1.76				52.6		2790		1.75				52.6		2640		1.74

		53.3		2820		1.76				52.7		2800		1.75				52.7		2650		1.74

		53.4		2820		1.76				52.8		2800		1.75				52.7		2650		1.75

		53.5		2820		1.77				52.9		2800		1.75				52.8		2650		1.75

		53.5		2820		1.77				52.9		2810		1.76				52.8		2650		1.75

		53.5		2820		1.77				53		2810		1.76				52.9		2660		1.75

		53.6		2830		1.77				53.1		2810		1.76				52.9		2660		1.75

		53.7		2830		1.77				53.2		2810		1.76				53		2660		1.76

		53.7		2830		1.78				53.2		2810		1.76				53.1		2670		1.76

		53.8		2830		1.78				53.3		2820		1.77				53.2		2670		1.76

		53.9		2830		1.78				53.3		2820		1.77				53.2		2670		1.76

		54		2830		1.78				53.4		2820		1.77				53.3		2670		1.77

		54.1		2840		1.79				53.5		2830		1.77				53.4		2670		1.77

		54.1		2840		1.79				53.6		2830		1.78				53.4		2680		1.77

		54.2		2840		1.79				53.6		2830		1.78				53.5		2680		1.77

		54.2		2840		1.79				53.7		2830		1.78				53.6		2680		1.77

		54.3		2840		1.79				53.8		2830		1.78				53.7		2690		1.78

		54.4		2840		1.8				53.8		2840		1.78				53.7		2690		1.78

		54.4		2850		1.8				53.9		2840		1.79				53.8		2690		1.78

		54.5		2850		1.8				53.9		2840		1.79				53.9		2690		1.79

		54.6		2850		1.8				54		2840		1.79				53.9		2690		1.79

		54.7		2850		1.81				54.2		2850		1.79				54		2690		1.79

		54.8		2850		1.81				54.2		2850		1.8				54.1		2700		1.79

		54.8		2850		1.81				54.3		2850		1.8				54.1		2700		1.79

		54.9		2860		1.81				54.3		2850		1.8				54.2		2700		1.8

		54.9		2860		1.82				54.4		2860		1.8				54.3		2700		1.8

		55		2860		1.82				54.4		2860		1.81				54.3		2710		1.8

		55		2860		1.82				54.5		2860		1.81				54.4		2710		1.8

		55.1		2860		1.82				54.6		2860		1.81				54.5		2710		1.8

		55.2		2860		1.83				54.7		2870		1.81				54.6		2710		1.81

		55.3		2860		1.83				54.8		2870		1.81				54.6		2710		1.81

		55.4		2860		1.83				54.8		2870		1.82				54.7		2710		1.81

		55.4		2860		1.83				54.8		2870		1.82				54.7		2710		1.81

		55.5		2860		1.83				54.9		2880		1.82				54.9		2720		1.82

		55.6		2850		1.84				55		2880		1.82				54.9		2720		1.82

		55.6		2850		1.84				55.1		2880		1.83				55		2720		1.82

		55.7		2840		1.84				55.1		2880		1.83				55		2720		1.82

		55.7		2840		1.84				55.2		2890		1.83				55.1		2720		1.83

		55.9		2800		1.85				55.3		2890		1.83				55.2		2730		1.83

		55.9		2770		1.85				55.4		2890		1.84				55.2		2730		1.83

		56		2740		1.85				55.4		2890		1.84				55.3		2730		1.83

		56.1		2720		1.85				55.5		2890		1.84				55.4		2730		1.84

		56.1		2710		1.85				55.5		2900		1.84				55.5		2740		1.84

		56.2		2700		1.86				55.6		2900		1.84				55.5		2740		1.84

		56.2		2690		1.86				55.7		2900		1.85				55.6		2740		1.84

		56.3		2690		1.86				55.7		2900		1.85				55.7		2740		1.84

		56.4		2680		1.87				55.9		2910		1.85				55.7		2740		1.85

		56.5		2680		1.87				55.9		2910		1.85				55.8		2740		1.85

		56.6		2680		1.87				56		2910		1.86				55.8		2740		1.85

		56.6		2670		1.87				56.1		2910		1.86				55.9		2750		1.85

		56.7		2470		1.87				56.1		2920		1.86				56		2750		1.86

		56.8		2410		1.88				56.2		2920		1.86				56.1		2750		1.86

		56.8		2390		1.88				56.2		2920		1.86				56.1		2750		1.86

		56.9		2380		1.88				56.3		2920		1.87				56.2		2750		1.86

		57		2380		1.88				56.4		2920		1.87				56.3		2750		1.87

		57		2380		1.89				56.5		2920		1.87				56.4		2750		1.87

		57.1		2380		1.89				56.5		2930		1.87				56.4		2760		1.87

		57.2		2380		1.89				56.6		2930		1.88				56.5		2760		1.87

		57.2		2390		1.89				56.7		2930		1.88				56.5		2760		1.87

		57.3		2380		1.89				56.7		2930		1.88				56.6		2760		1.88

		57.4		2360		1.9				56.8		2940		1.88				56.7		2760		1.88

		57.4		2360		1.9				56.8		2940		1.88				56.8		2760		1.88

		57.5		2360		1.9				56.9		2940		1.89				56.8		2760		1.88

		57.6		2360		1.9				57		2940		1.89				56.9		2740		1.89

		57.7		2360		1.91				57		2950		1.89				57		2730		1.89

		57.8		2360		1.91				57.1		2950		1.89				57.1		2710		1.89

		57.8		2360		1.91				57.1		2950		1.89				57.1		2670		1.89

		57.9		2360		1.91				57.2		2950		1.9				57.1		2640		1.89

		57.9		2370		1.91				57.2		2950		1.9				57.3		2580		1.9

		58		2370		1.92				57.3		2960		1.9				57.4		2550		1.9

		58.1		2370		1.92				57.4		2960		1.9				57.4		2530		1.9

		58.2		2370		1.92				57.4		2960		1.91				57.5		2520		1.9

		58.2		2370		1.93				57.6		2960		1.91				57.5		2510		1.91

		58.3		2370		1.93				57.7		2970		1.91				57.6		2500		1.91

		58.4		2370		1.93				57.7		2970		1.91				57.7		2500		1.91

		58.4		2370		1.93				57.7		2970		1.92				57.7		2490		1.91

		58.5		2380		1.93				57.8		2970		1.92				57.8		2490		1.92

		58.6		2380		1.94				57.9		2980		1.92				57.9		2490		1.92

		58.6		2380		1.94				58		2980		1.92				57.9		2490		1.92

		58.7		2380		1.94				58		2980		1.92				58		2490		1.92

		58.8		2380		1.94				58.1		2980		1.93				58.1		2490		1.92

		58.9		2380		1.95				58.2		2980		1.93				58.1		2490		1.93

		58.9		2390		1.95				58.2		2980		1.93				58.2		2490		1.93

		59		2390		1.95				58.3		2990		1.93				58.2		2490		1.93

		59		2390		1.95				58.4		2990		1.94				58.3		2490		1.93

		59.1		2390		1.95				58.4		2990		1.94				58.4		2490		1.94

		59.2		2400		1.96				58.5		2990		1.94				58.5		2490		1.94

		59.3		2400		1.96				58.5		3000		1.94				58.6		2490		1.94

		59.4		2400		1.96				58.6		3000		1.94				58.6		2490		1.94

		59.4		2400		1.96				58.7		3000		1.95				58.7		2490		1.95

		59.4		2400		1.97				58.7		3000		1.95				58.7		2490		1.95

		59.5		2410		1.97				58.8		3010		1.95				58.8		2490		1.95

		59.6		2410		1.97				58.9		3010		1.95				58.9		2490		1.95

		59.7		2410		1.97				59		3010		1.96				59		2490		1.96

		59.7		2410		1.98				59		3010		1.96				59.1		2490		1.96

		59.8		2410		1.98				59.1		3010		1.96				59.1		2490		1.96

		59.9		2420		1.98				59.2		3020		1.96				59.2		2490		1.96

		59.9		2420		1.98				59.3		3020		1.97				59.3		2490		1.96

		60		2420		1.98				59.3		3020		1.97				59.3		2490		1.97

		60		2420		1.99				59.4		3030		1.97				59.4		2480		1.97

		60.1		2420		1.99				59.4		3030		1.97				59.4		2480		1.97

		60.2		2420		1.99				59.5		3030		1.97				59.5		2480		1.97

		60.3		2430		1.99				59.6		3030		1.98				59.6		2480		1.98

		60.3		2430		2				59.6		3030		1.98				59.7		2480		1.98

		60.4		2430		2				59.7		3040		1.98				59.7		2480		1.98

		60.4		2430		2				59.8		3040		1.98				59.8		2480		1.98

		60.5		2430		2				59.9		3040		1.99				59.9		2480		1.98

		60.6		2440		2				59.9		3050		1.99				59.9		2480		1.99

		60.7		2440		2.01				60		3050		1.99				60		2480		1.99

		60.7		2440		2.01				60.1		3050		1.99				60		2480		1.99

		60.8		2440		2.01				60.1		3050		1.99				60.2		2480		2

		60.8		2450		2.01				60.2		3050		2				60.3		2480		2

		60.9		2450		2.02				60.2		3060		2				60.3		2480		2

		61		2450		2.02				60.3		3060		2				60.4		2480		2

		61.1		2460		2.02				60.4		3060		2				60.4		2480		2

		61.2		2460		2.02				60.5		3070		2.01				60.5		2480		2.01

		61.2		2460		2.02				60.6		3070		2.01				60.5		2480		2.01

		61.3		2460		2.03				60.6		3070		2.01				60.6		2480		2.01

		61.3		2460		2.03				60.7		3070		2.01				60.7		2480		2.01

		61.4		2470		2.03				60.7		3070		2.02				60.8		2480		2.01

		61.5		2470		2.03				60.8		3080		2.02				60.9		2480		2.02

		61.6		2470		2.04				60.9		3080		2.02				60.9		2480		2.02

		61.6		2480		2.04				61		3080		2.02				61		2480		2.02

		61.7		2480		2.04				61.1		3090		2.03				61		2480		2.02

		61.8		2480		2.04				61.1		3090		2.03				61.1		2480		2.03

		61.8		2480		2.04				61.2		3090		2.03				61.2		2480		2.03

		61.9		2490		2.05				61.2		3090		2.03				61.2		2480		2.03

		61.9		2490		2.05				61.3		3100		2.03				61.3		2480		2.03

		62.1		2490		2.05				61.4		3100		2.04				61.4		2480		2.03

		62.1		2490		2.06				61.5		3100		2.04				61.4		2480		2.04

		62.2		2490		2.06				61.6		3100		2.04				61.5		2480		2.04

		62.3		2500		2.06				61.6		3110		2.04				61.5		2480		2.04

		62.3		2500		2.06				61.7		3110		2.05				61.6		2480		2.04

		62.4		2500		2.06				61.7		3110		2.05				61.7		2480		2.05

		62.4		2500		2.07				61.8		3110		2.05				61.7		2480		2.05

		62.5		2500		2.07				61.9		3120		2.05				61.8		2490		2.05

		62.6		2500		2.07				62		3120		2.05				61.9		2490		2.05

		62.7		2500		2.07				62		3120		2.06				62		2490		2.05

		62.8		2510		2.08				62.1		3120		2.06				62		2490		2.06

		62.8		2510		2.08				62.2		3130		2.06				62.1		2490		2.06

		62.9		2510		2.08				62.3		3130		2.07				62.2		2490		2.06

		63		2510		2.08				62.3		3130		2.07				62.2		2490		2.06

		63		2510		2.08				62.4		3130		2.07				62.3		2490		2.06

		63.1		2520		2.09				62.4		3130		2.07				62.3		2490		2.07

		63.2		2520		2.09				62.5		3140		2.07				62.4		2500		2.07

		63.3		2520		2.09				62.6		3140		2.08				62.5		2500		2.07

		63.3		2520		2.09				62.6		3140		2.08				62.6		2500		2.08

		63.4		2530		2.1				62.8		3150		2.08				62.7		2500		2.08

		63.4		2530		2.1				62.8		3150		2.08				62.7		2500		2.08

		63.5		2530		2.1				62.9		3150		2.09				62.8		2500		2.08

		63.6		2530		2.1				63		3150		2.09				62.8		2510		2.08

		63.6		2530		2.11				63		3150		2.09				62.9		2510		2.09

		63.7		2530		2.11				63.1		3160		2.09				63		2510		2.09

		63.8		2540		2.11				63.1		3160		2.09				63.1		2510		2.09

		63.9		2540		2.11				63.2		3160		2.1				63.1		2510		2.09

		63.9		2540		2.12				63.2		3160		2.1				63.2		2510		2.1

		64		2540		2.12				63.3		3170		2.1				63.2		2510		2.1

		64.1		2550		2.12				63.4		3170		2.1				63.3		2510		2.1

		64.1		2550		2.12				63.5		3170		2.11				63.4		2520		2.1

		64.2		2550		2.12				63.5		3170		2.11				63.4		2520		2.1

		64.2		2550		2.13				63.6		3170		2.11				63.5		2520		2.11

		64.4		2560		2.13				63.6		3180		2.11				63.6		2520		2.11

		64.4		2560		2.13				63.7		3180		2.11				63.7		2520		2.11

		64.5		2560		2.13				63.8		3180		2.12				63.7		2520		2.11

		64.5		2560		2.13				63.8		3180		2.12				63.8		2520		2.12

		64.6		2560		2.14				63.9		3190		2.12				63.9		2530		2.12

		64.7		2560		2.14				64		3190		2.12				63.9		2530		2.12

		64.7		2560		2.14				64		3190		2.13				64		2530		2.12

		64.8		2570		2.14				64.1		3190		2.13				64		2530		2.12

		64.9		2570		2.15				64.2		3200		2.13				64.1		2530		2.13

		65		2570		2.15				64.2		3200		2.13				64.2		2530		2.13

		65		2570		2.15				64.3		3200		2.13				64.3		2530		2.13

		65.1		2580		2.15				64.4		3200		2.13				64.4		2540		2.13

		65.2		2580		2.16				64.4		3200		2.14				64.4		2540		2.13

		65.2		2580		2.16				64.5		3210		2.14				64.5		2540		2.14

		65.3		2580		2.16				64.6		3210		2.14				64.5		2540		2.14

		65.3		2580		2.16				64.7		3210		2.15				64.6		2540		2.14

		65.4		2580		2.16				64.7		3220		2.15				64.7		2540		2.14

		65.5		2590		2.17				64.8		3220		2.15				64.7		2540		2.15

		65.6		2590		2.17				64.9		3220		2.15				64.8		2550		2.15

		65.7		2590		2.17				65		3220		2.15				64.9		2550		2.15

		65.7		2590		2.17				65		3230		2.16				64.9		2550		2.15

		65.8		2600		2.18				65.1		3230		2.16				65		2550		2.16

		65.8		2600		2.18				65.1		3230		2.16				65.1		2550		2.16

		65.9		2600		2.18				65.2		3230		2.16				65.2		2560		2.16

		66		2600		2.18				65.3		3240		2.17				65.2		2560		2.16

		66.1		2610		2.19				65.4		3240		2.17				65.3		2560		2.16

		66.1		2610		2.19				65.4		3240		2.17				65.4		2560		2.17

		66.2		2610		2.19				65.5		3240		2.17				65.4		2570		2.17

		66.3		2610		2.19				65.5		3240		2.17				65.5		2570		2.17

		66.3		2620		2.19				65.6		3250		2.18				65.6		2570		2.18

		66.4		2620		2.2				65.7		3250		2.18				65.7		2570		2.18

		66.5		2620		2.2				65.8		3250		2.18				65.7		2570		2.18

		66.5		2620		2.2				65.9		3260		2.18				65.8		2570		2.18

		66.6		2630		2.2				65.9		3260		2.19				65.9		2580		2.18

		66.7		2630		2.21				66		3260		2.19				65.9		2580		2.19

		66.7		2630		2.21				66		3260		2.19				66		2580		2.19

		66.8		2630		2.21				66.1		3260		2.19				66.1		2580		2.19

		66.9		2630		2.21				66.1		3270		2.2				66.2		2580		2.19

		66.9		2630		2.21				66.2		3270		2.2				66.2		2580		2.2

		67		2640		2.22				66.3		3270		2.2				66.3		2580		2.2

		67		2640		2.22				66.4		3270		2.2				66.4		2590		2.2

		67.1		2640		2.22				66.5		3280		2.2				66.4		2590		2.2

		67.2		2640		2.22				66.5		3280		2.21				66.4		2590		2.2

		67.3		2640		2.23				66.5		3280		2.21				66.5		2590		2.21

		67.3		2650		2.23				66.6		3280		2.21				66.6		2590		2.21

		67.4		2650		2.23				66.7		3280		2.21				66.7		2590		2.21

		67.5		2650		2.23				66.7		3290		2.21				66.8		2600		2.21

		67.5		2650		2.24				66.8		3290		2.22				66.9		2600		2.22

		67.6		2650		2.24				66.9		3290		2.22				66.9		2600		2.22

		67.7		2650		2.24				66.9		3290		2.22				67		2600		2.22

		67.8		2660		2.24				67		3290		2.22				67		2600		2.22

		67.8		2660		2.25				67		3300		2.23				67.1		2600		2.23

		67.9		2660		2.25				67.1		3300		2.23				67.1		2600		2.23

		68		2660		2.25				67.2		3300		2.23				67.2		2610		2.23

		68.1		2660		2.25				67.3		3300		2.23				67.4		2610		2.23

		68.1		2670		2.25				67.3		3310		2.23				67.4		2610		2.24

		68.1		2670		2.26				67.4		3310		2.24				67.4		2610		2.24

		68.2		2670		2.26				67.4		3310		2.24				67.5		2610		2.24

		68.4		2670		2.26				67.5		3310		2.24				67.6		2620		2.24

		68.4		2670		2.26				67.6		3310		2.24				67.6		2620		2.24

		68.5		2680		2.27				67.7		3320		2.25				67.7		2620		2.25

		68.5		2680		2.27				67.7		3320		2.25				67.8		2620		2.25

		68.6		2680		2.27				67.8		3320		2.25				67.8		2620		2.25

		68.6		2680		2.27				67.8		3320		2.25				67.9		2630		2.25

		68.7		2680		2.27				67.9		3330		2.25				68		2630		2.26

		68.8		2680		2.28				67.9		3330		2.26				68		2630		2.26

		68.9		2690		2.28				68		3330		2.26				68.1		2630		2.26

		69		2690		2.28				68.1		3330		2.26				68.2		2630		2.26

		69		2690		2.29				68.2		3330		2.26				68.2		2640		2.26

		69.1		2690		2.29				68.3		3340		2.26				68.3		2640		2.27

		69.2		2700		2.29				68.3		3340		2.27				68.4		2640		2.27

		69.2		2700		2.29				68.4		3340		2.27				68.4		2640		2.27

		69.3		2700		2.29				68.4		3340		2.27				68.5		2640		2.27

		69.4		2700		2.3				68.5		3350		2.27				68.6		2640		2.27

		69.4		2700		2.3				68.5		3350		2.28				68.6		2650		2.28

		69.5		2710		2.3				68.7		3350		2.28				68.7		2650		2.28

		69.6		2710		2.3				68.7		3350		2.28				68.8		2650		2.28

		69.6		2710		2.3				68.8		3360		2.28				68.8		2650		2.28

		69.7		2710		2.31				68.9		3360		2.29				68.9		2650		2.29

		69.8		2710		2.31				68.9		3360		2.29				69		2660		2.29

		69.8		2720		2.31				69		3360		2.29				69.1		2660		2.29

		69.9		2720		2.31				69		3360		2.29				69.1		2660		2.29

		70		2720		2.32				69.1		3370		2.29				69.2		2660		2.3

		70		2720		2.32				69.2		3370		2.3				69.3		2660		2.3

		70.1		2720		2.32				69.3		3370		2.3				69.3		2670		2.3

		70.1		2720		2.32				69.4		3370		2.3				69.4		2670		2.3

		70.2		2730		2.32				69.4		3380		2.3				69.4		2670		2.3

		70.3		2730		2.33				69.5		3380		2.31				69.5		2670		2.31

		70.3		2730		2.33				69.5		3380		2.31				69.6		2670		2.31

		70.4		2730		2.33				69.6		3380		2.31				69.7		2680		2.31

		70.5		2730		2.33				69.7		3380		2.31				69.7		2680		2.31

		70.5		2740		2.33				69.7		3380		2.31				69.8		2680		2.32

		70.6		2740		2.34				69.9		3390		2.32				69.8		2680		2.32

		70.6		2740		2.34				69.9		3390		2.32				69.9		2680		2.32

		70.7		2740		2.34				70		3390		2.32				70		2690		2.32

		70.8		2740		2.34				70		3390		2.33				70		2690		2.32

		70.9		2750		2.35				70.1		3390		2.33				70.1		2690		2.33

		70.9		2750		2.35				70.2		3390		2.33				70.2		2690		2.33

		71		2750		2.35				70.2		3390		2.33				70.3		2690		2.33

		71		2750		2.35				70.3		3400		2.33				70.3		2700		2.33

		71.1		2750		2.35				70.4		3400		2.34				70.4		2700		2.34

		71.1		2760		2.36				70.5		3400		2.34				70.5		2700		2.34

		71.2		2760		2.36				70.6		3400		2.34				70.5		2700		2.34

		71.3		2760		2.36				70.6		3400		2.34				70.6		2700		2.34

		71.3		2760		2.36				70.7		3400		2.35				70.7		2710		2.34

		71.4		2760		2.36				70.7		3400		2.35				70.7		2710		2.35

		71.5		2770		2.37				70.8		3400		2.35				70.8		2710		2.35

		71.5		2770		2.37				70.9		3410		2.35				70.9		2710		2.35

		71.6		2770		2.37				70.9		3410		2.35				70.9		2710		2.35

		71.7		2770		2.37				71		3410		2.36				71		2720		2.36

		71.8		2780		2.38				71.1		3410		2.36				71		2720		2.36

		71.8		2780		2.38				71.2		3420		2.36				71.1		2720		2.36

		71.9		2780		2.38				71.3		3420		2.36				71.2		2720		2.36

		72		2780		2.38				71.3		3420		2.37				71.2		2720		2.36

		72		2780		2.38				71.3		3420		2.37				71.4		2730		2.37

		72.1		2790		2.39				71.4		3420		2.37				71.4		2730		2.37

		72.1		2790		2.39				71.5		3420		2.37				71.5		2730		2.37

		72.2		2790		2.39				71.6		3430		2.38				71.5		2730		2.37

		72.3		2790		2.39				71.7		3430		2.38				71.6		2740		2.38

		72.4		2790		2.4				71.8		3430		2.38				71.7		2740		2.38

		72.5		2800		2.4				71.8		3430		2.38				71.7		2740		2.38

		72.5		2800		2.4				71.9		3430		2.39				71.8		2740		2.38

		72.5		2800		2.4				71.9		3430		2.39				71.9		2750		2.39

		72.6		2800		2.4				72		3440		2.39				72		2750		2.39

		72.7		2800		2.41				72		3440		2.39				72		2750		2.39

		72.8		2800		2.41				72.2		3440		2.4				72.1		2750		2.39

		72.8		2810		2.41				72.2		3440		2.4				72.2		2750		2.39

		72.9		2810		2.41				72.3		3440		2.4				72.2		2760		2.4

		73		2810		2.42				72.3		3440		2.4				72.3		2760		2.4

		73		2810		2.42				72.4		3450		2.4				72.3		2760		2.4

		73		2810		2.42				72.5		3450		2.41				72.4		2760		2.4

		73.1		2820		2.42				72.5		3450		2.41				72.5		2760		2.41

		73.2		2820		2.42				72.6		3450		2.41				72.6		2770		2.41

		73.2		2820		2.43				72.7		3450		2.41				72.6		2770		2.41

		73.3		2820		2.43				72.8		3450		2.42				72.7		2770		2.41

		73.4		2820		2.43				72.8		3450		2.42				72.7		2770		2.41

		73.5		2820		2.43				72.9		3450		2.42				72.8		2770		2.42

		73.5		2820		2.44				73		3450		2.42				72.9		2780		2.42

		73.6		2830		2.44				73.1		3450		2.43				73		2780		2.42

		73.6		2830		2.44				73.1		3450		2.43				73.1		2780		2.42

		73.7		2830		2.44				73.2		3450		2.43				73.1		2780		2.43

		73.8		2830		2.44				73.3		3380		2.43				73.2		2790		2.43

		73.8		2840		2.45				73.3		3320		2.43				73.2		2790		2.43

		73.9		2840		2.45				73.4		3270		2.44				73.3		2790		2.43

		74		2840		2.45				73.4		3230		2.44				73.3		2790		2.43

		74.1		2850		2.45				73.5		3200		2.44				73.4		2790		2.44

		74.1		2850		2.46				73.6		3180		2.44				73.5		2790		2.44

		74.2		2850		2.46				73.6		3160		2.44				73.5		2800		2.44

		74.3		2850		2.46				73.7		3150		2.45				73.7		2800		2.44

		74.3		2850		2.46				73.8		3140		2.45				73.7		2800		2.45

		74.4		2850		2.46				73.9		3130		2.45				73.8		2800		2.45

		74.5		2860		2.47				73.9		3120		2.45				73.8		2810		2.45

		74.5		2860		2.47				74		3120		2.46				73.9		2810		2.45

		74.6		2860		2.47				74		3110		2.46				73.9		2810		2.45

		74.7		2860		2.47				74.1		3110		2.46				74		2810		2.46

		74.7		2870		2.48				74.2		3100		2.46				74.1		2810		2.46

		74.8		2870		2.48				74.2		3100		2.46				74.2		2820		2.46

		74.9		2870		2.48				74.3		3090		2.47				74.2		2820		2.46

		75		2870		2.48				74.4		3090		2.47				74.3		2820		2.47

		75		2870		2.48				74.5		3080		2.47				74.3		2820		2.47

		75.1		2880		2.49				74.6		3080		2.48				74.4		2820		2.47

		75.2		2880		2.49				74.6		3080		2.48				74.5		2830		2.47

		75.3		2880		2.49				74.7		3070		2.48				74.5		2830		2.47

		75.3		2880		2.49				74.8		3070		2.48				74.6		2830		2.48

		75.4		2880		2.5				74.8		3060		2.48				74.7		2830		2.48

		75.4		2890		2.5				74.8		3060		2.49				74.7		2840		2.48

		75.5		2890		2.5				75		3060		2.49				74.8		2840		2.48

		75.5		2890		2.5				75		3060		2.49				74.9		2840		2.49

		75.6		2890		2.5				75.1		3050		2.49				75		2840		2.49

		75.7		2890		2.51				75.2		3050		2.5				75		2840		2.49

		75.8		2900		2.51				75.2		3050		2.5				75.1		2850		2.49

		75.8		2900		2.51				75.3		3050		2.5				75.2		2850		2.49

		75.9		2900		2.51				75.3		3050		2.5				75.2		2850		2.5

		75.9		2900		2.52				75.4		3050		2.5				75.3		2850		2.5

		76		2900		2.52				75.6		3050		2.51				75.3		2850		2.5

		76.1		2910		2.52				75.6		3050		2.51				75.4		2860		2.5

		76.2		2910		2.52				75.7		3050		2.51				75.5		2860		2.51

		76.3		2910		2.53				75.7		3050		2.51				75.6		2860		2.51

		76.4		2910		2.53				75.8		3050		2.52				75.6		2860		2.51

		76.4		2910		2.53				75.9		3050		2.52				75.6		2860		2.51

		76.4		2920		2.53				75.9		3050		2.52				75.7		2870		2.51

		76.5		2920		2.53				76		3050		2.52				75.8		2870		2.52

		76.6		2920		2.54				76.1		3050		2.53				75.9		2870		2.52

		76.6		2920		2.54				76.1		3050		2.53				75.9		2870		2.52

		76.7		2920		2.54				76.2		3050		2.53				76		2880		2.52

		76.8		2930		2.55				76.2		3050		2.53				76.1		2880		2.52

		76.9		2930		2.55				76.3		3050		2.53				76.1		2880		2.53

		76.9		2930		2.55				76.4		3050		2.54				76.2		2880		2.53

		77		2930		2.55				76.4		3050		2.54				76.2		2880		2.53

		77.1		2940		2.55				76.5		3050		2.54				76.3		2890		2.53

		77.1		2940		2.56				76.6		3050		2.54				76.4		2890		2.54

		77.2		2940		2.56				76.7		3050		2.55				76.5		2890		2.54

		77.3		2940		2.56				76.7		3050		2.55				76.6		2890		2.54

		77.4		2940		2.56				76.8		3050		2.55				76.6		2900		2.54

		77.4		2940		2.56				76.9		3050		2.55				76.6		2900		2.54

		77.5		2940		2.57				77		3050		2.56				76.7		2900		2.55

		77.5		2950		2.57				77		3050		2.56				76.8		2900		2.55

		77.6		2950		2.57				77.1		3050		2.56				76.9		2900		2.55

		77.7		2950		2.57				77.1		3040		2.56				76.9		2910		2.55

		77.8		2950		2.58				77.2		3040		2.57				77		2910		2.56

		77.8		2950		2.58				77.3		3030		2.57				77.1		2910		2.56

		77.9		2960		2.58				77.4		3030		2.57				77.1		2910		2.56

		78		2960		2.58				77.4		3030		2.57				77.2		2910		2.56

		78		2960		2.58				77.5		3030		2.57				77.2		2920		2.56

		78.1		2960		2.59				77.6		3030		2.58				77.3		2920		2.57

		78.1		2960		2.59				77.6		3030		2.58				77.4		2920		2.57

		78.2		2970		2.59				77.7		3020		2.58				77.4		2920		2.57

		78.3		2970		2.59				77.8		3020		2.58				77.5		2920		2.57

		78.3		2970		2.6				77.9		3020		2.59				77.6		2930		2.58

		78.4		2970		2.6				77.9		3020		2.59				77.7		2930		2.58

		78.5		2970		2.6				78		3020		2.59				77.7		2930		2.58

		78.6		2980		2.6				78.1		3020		2.59				77.8		2930		2.58

		78.7		2980		2.61				78.1		3020		2.59				77.9		2930		2.58

		78.7		2980		2.61				78.2		3020		2.6				77.9		2930		2.59

		78.8		2980		2.61				78.2		3020		2.6				78		2940		2.59

		78.9		2980		2.61				78.4		3020		2.6				78.1		2940		2.59

		78.9		2990		2.61				78.4		3030		2.61				78.1		2940		2.59

		78.9		2990		2.62				78.5		3030		2.61				78.2		2940		2.6

		79.1		2990		2.62				78.6		3030		2.61				78.2		2950		2.6

		79.1		2990		2.62				78.6		3030		2.61				78.3		2950		2.6

		79.2		2990		2.62				78.7		3030		2.61				78.4		2950		2.6

		79.3		3000		2.63				78.7		3030		2.62				78.4		2950		2.6

		79.4		3000		2.63				78.8		3030		2.62				78.5		2960		2.61

		79.4		3000		2.63				78.9		3030		2.62				78.6		2960		2.61

		79.5		3000		2.63				79		3030		2.62				78.6		2960		2.61

		79.5		3000		2.63				79		3030		2.62				78.7		2960		2.61

		79.6		3010		2.64				79.1		3030		2.63				78.8		2970		2.62

		79.7		3010		2.64				79.2		3040		2.63				78.9		2970		2.62

		79.8		3010		2.64				79.2		3040		2.63				78.9		2970		2.62

		79.8		3010		2.64				79.3		3040		2.63				79		2970		2.62

		79.9		3010		2.65				79.4		3040		2.64				79.1		2970		2.62

		79.9		3020		2.65				79.5		3040		2.64				79.1		2980		2.63

		80		3020		2.65				79.6		3040		2.64				79.2		2980		2.63

		80.1		3020		2.65				79.6		3040		2.64				79.3		2980		2.63

		80.1		3020		2.65				79.6		3040		2.65				79.4		2980		2.64

		80.2		3020		2.66				79.7		3050		2.65				79.5		2980		2.64

		80.2		3030		2.66				79.8		3050		2.65				79.5		2990		2.64

		80.3		3030		2.66				79.8		3050		2.65				79.5		2990		2.64

		80.3		3030		2.66				79.9		3050		2.65				79.6		2990		2.64

		80.4		3030		2.66				80		3050		2.66				79.7		2990		2.65

		80.5		3030		2.67				80.1		3050		2.66				79.7		2990		2.65

		80.5		3030		2.67				80.1		3060		2.66				79.8		2990		2.65

		80.6		3040		2.67				80.2		3060		2.66				80		3000		2.65

		80.7		3040		2.67				80.3		3060		2.67				80		3000		2.66

		80.8		3040		2.68				80.3		3060		2.67				80		3000		2.66

		80.9		3050		2.68				80.4		3060		2.67				80.1		3000		2.66

		80.9		3050		2.68				80.5		3060		2.67				80.2		3010		2.66

		81		3050		2.68				80.6		3060		2.67				80.2		3010		2.66

		81.1		3050		2.69				80.6		3070		2.68				80.3		3010		2.67

		81.1		3050		2.69				80.7		3070		2.68				80.4		3010		2.67

		81.2		3060		2.69				80.8		3070		2.68				80.5		3010		2.67

		81.2		3060		2.69				80.8		3070		2.69				80.5		3020		2.67

		81.3		3060		2.69				80.9		3070		2.69				80.6		3020		2.68

		81.4		3060		2.7				81		3070		2.69				80.7		3020		2.68

		81.5		3070		2.7				81		3080		2.69				80.7		3020		2.68

		81.5		3070		2.7				81.1		3080		2.69				80.8		3020		2.68

		81.6		3070		2.7				81.2		3080		2.7				80.9		3030		2.68

		81.6		3070		2.71				81.2		3080		2.7				80.9		3030		2.69

		81.7		3070		2.71				81.3		3080		2.7				81		3030		2.69

		81.8		3070		2.71				81.4		3080		2.7				81.1		3030		2.69

		81.8		3080		2.71				81.5		3090		2.71				81.1		3030		2.69

		81.9		3080		2.71				81.5		3090		2.71				81.2		3030		2.7

		82		3080		2.72				81.6		3090		2.71				81.2		3040		2.7

		82		3090		2.72				81.6		3090		2.71				81.3		3040		2.7

		82.1		3090		2.72				81.7		3090		2.71				81.4		3040		2.7

		82.2		3090		2.72				81.8		3090		2.72				81.4		3040		2.7

		82.2		3090		2.73				81.8		3100		2.72				81.5		3040		2.71

		82.3		3090		2.73				81.9		3100		2.72				81.6		3040		2.71

		82.4		3090		2.73				82		3100		2.72				81.6		3050		2.71

		82.4		3090		2.73				82.1		3100		2.72				81.7		3050		2.71

		82.5		3100		2.73				82.1		3100		2.73				81.8		3050		2.72

		82.6		3100		2.74				82.2		3110		2.73				81.8		3050		2.72

		82.6		3100		2.74				82.2		3110		2.73				81.9		3050		2.72

		82.7		3100		2.74				82.3		3110		2.73				82		3060		2.72

		82.8		3110		2.74				82.4		3110		2.74				82		3060		2.72

		82.8		3110		2.74				82.5		3110		2.74				82.1		3060		2.73

		82.8		3110		2.75				82.5		3120		2.74				82.2		3060		2.73

		82.9		3110		2.75				82.6		3120		2.74				82.3		3060		2.73

		83		3110		2.75				82.6		3120		2.74				82.3		3070		2.73

		83.1		3120		2.75				82.7		3120		2.75				82.4		3070		2.73

		83.1		3120		2.75				82.8		3120		2.75				82.4		3070		2.74

		83.2		3120		2.76				82.9		3130		2.75				82.5		3070		2.74

		83.2		3120		2.76				82.9		3130		2.75				82.6		3070		2.74

		83.3		3120		2.76				83		3130		2.76				82.6		3070		2.74

		83.4		3120		2.76				83		3130		2.76				82.7		3080		2.75

		83.4		3130		2.76				83.1		3140		2.76				82.8		3080		2.75

		83.5		3130		2.77				83.2		3140		2.76				82.9		3080		2.75

		83.6		3130		2.77				83.3		3140		2.77				82.9		3080		2.75

		83.7		3140		2.77				83.3		3140		2.77				83		3080		2.76

		83.7		3140		2.77				83.4		3150		2.77				83.1		3090		2.76

		83.8		3140		2.78				83.5		3150		2.77				83.1		3090		2.76

		83.9		3140		2.78				83.5		3150		2.77				83.2		3090		2.76

		83.9		3140		2.78				83.6		3150		2.78				83.3		3090		2.76

		84		3150		2.78				83.7		3150		2.78				83.4		3090		2.77

		84		3150		2.79				83.7		3160		2.78				83.4		3100		2.77

		84.2		3150		2.79				83.8		3160		2.78				83.5		3100		2.77

		84.2		3150		2.79				83.8		3160		2.79				83.6		3100		2.77

		84.3		3160		2.79				83.9		3160		2.79				83.6		3100		2.78

		84.3		3160		2.8				84		3170		2.79				83.7		3100		2.78

		84.4		3160		2.8				84.1		3170		2.79				83.8		3100		2.78

		84.5		3160		2.8				84.1		3170		2.8				83.8		3110		2.78

		84.5		3160		2.8				84.2		3170		2.8				83.9		3110		2.78

		84.6		3160		2.8				84.3		3170		2.8				83.9		3110		2.79

		84.7		3170		2.81				84.3		3180		2.8				84		3110		2.79

		84.8		3170		2.81				84.4		3180		2.8				84		3110		2.79

		84.9		3170		2.81				84.5		3180		2.81				84.1		3110		2.79

		84.9		3170		2.81				84.5		3180		2.81				84.2		3120		2.8

		85		3170		2.82				84.7		3190		2.81				84.3		3120		2.8

		85		3180		2.82				84.7		3190		2.81				84.3		3120		2.8

		85.1		3180		2.82				84.8		3190		2.82				84.4		3120		2.8

		85.2		3180		2.82				84.8		3190		2.82				84.4		3120		2.8

		85.2		3180		2.83				84.9		3200		2.82				84.5		3120		2.81

		85.3		3180		2.83				85		3200		2.82				84.6		3130		2.81

		85.4		3190		2.83				85		3200		2.82				84.7		3130		2.81

		85.5		3190		2.83				85.1		3200		2.83				84.7		3130		2.81

		85.5		3190		2.83				85.2		3200		2.83				84.8		3130		2.81

		85.6		3190		2.84				85.3		3210		2.83				84.8		3130		2.82

		85.6		3190		2.84				85.3		3210		2.83				84.9		3130		2.82

		85.7		3200		2.84				85.4		3210		2.84				84.9		3130		2.82

		85.8		3200		2.84				85.5		3210		2.84				85.1		3140		2.82

		85.8		3200		2.84				85.5		3210		2.84				85.1		3140		2.83

		85.9		3200		2.85				85.6		3210		2.84				85.2		3140		2.83

		86		3200		2.85				85.6		3220		2.85				85.3		3140		2.83

		86		3200		2.85				85.7		3220		2.85				85.3		3140		2.83

		86.1		3210		2.85				85.8		3220		2.85				85.4		3140		2.83

		86.2		3210		2.86				85.9		3220		2.85				85.4		3140		2.84

		86.2		3210		2.86				85.9		3220		2.85				85.5		3140		2.84

		86.2		3210		2.86				86		3220		2.86				85.6		3150		2.84

		86.4		3220		2.86				86.1		3230		2.86				85.6		3150		2.84

		86.5		3220		2.87				86.1		3230		2.86				85.7		3150		2.85

		86.5		3220		2.87				86.2		3230		2.86				85.8		3150		2.85

		86.6		3220		2.87				86.3		3230		2.87				85.8		3150		2.85

		86.6		3220		2.87				86.4		3230		2.87				85.9		3150		2.85

		86.7		3220		2.87				86.4		3240		2.87				85.9		3150		2.85

		86.8		3230		2.88				86.5		3240		2.87				86		3150		2.86

		86.8		3230		2.88				86.5		3240		2.87				86.2		3160		2.86

		87		3230		2.88				86.6		3240		2.88				86.2		3160		2.86

		87		3230		2.88				86.7		3240		2.88				86.3		3160		2.86

		87.1		3240		2.89				86.7		3250		2.88				86.4		3160		2.87

		87.1		3240		2.89				86.8		3250		2.88				86.4		3160		2.87

		87.2		3240		2.89				86.9		3250		2.89				86.4		3160		2.87

		87.2		3230		2.89				87		3250		2.89				86.5		3170		2.87

		87.3		3230		2.89				87		3260		2.89				86.6		3170		2.88

		87.4		3230		2.9				87.1		3260		2.89				86.7		3170		2.88

		87.5		3230		2.9				87.1		3260		2.9				86.8		3170		2.88

		87.6		3240		2.9				87.2		3260		2.9				86.8		3170		2.88

		87.6		3240		2.9				87.3		3260		2.9				86.8		3170		2.88

		87.7		3240		2.91				87.4		3270		2.9				86.9		3170		2.89

		87.7		3240		2.91				87.4		3270		2.91				87		3180		2.89

		87.8		3240		2.91				87.5		3270		2.91				87.1		3180		2.89

		87.9		3250		2.91				87.6		3280		2.91				87.1		3180		2.89

		87.9		3250		2.92				87.7		3280		2.91				87.2		3180		2.9

		88		3250		2.92				87.7		3280		2.91				87.3		3180		2.9

		88.1		3250		2.92				87.8		3280		2.92				87.3		3180		2.9

		88.2		3250		2.92				87.8		3280		2.92				87.4		3180		2.9

		88.3		3250		2.93				87.9		3280		2.92				87.4		3180		2.9

		88.3		3250		2.93				87.9		3290		2.92				87.5		3190		2.91

		88.4		3260		2.93				88.1		3290		2.93				87.6		3190		2.91

		88.5		3260		2.93				88.2		3290		2.93				87.6		3190		2.91

		88.5		3260		2.93				88.2		3300		2.93				87.7		3190		2.91

		88.6		3260		2.94				88.3		3300		2.93				87.8		3190		2.91

		88.7		3270		2.94				88.4		3300		2.93				87.9		3190		2.92

		88.8		3270		2.94				88.4		3300		2.94				87.9		3190		2.92

		88.8		3270		2.94				88.5		3300		2.94				88		3190		2.92

		88.9		3270		2.95				88.5		3300		2.94				88.1		3200		2.92

		89		3270		2.95				88.6		3310		2.94				88.1		3200		2.93

		89		3280		2.95				88.7		3310		2.95				88.2		3200		2.93

		89.1		3280		2.95				88.8		3310		2.95				88.3		3200		2.93

		89.1		3280		2.95				88.8		3310		2.95				88.3		3200		2.93

		89.2		3280		2.96				88.9		3320		2.95				88.4		3200		2.94

		89.3		3280		2.96				88.9		3320		2.96				88.4		3200		2.94

		89.3		3290		2.96				89		3320		2.96				88.5		3200		2.94

		89.4		3290		2.96				89.1		3320		2.96				88.6		3200		2.94

		89.5		3290		2.97				89.1		3320		2.96				88.6		3200		2.94

		89.5		3290		2.97				89.2		3320		2.96				88.7		3200		2.95

		89.6		3290		2.97				89.3		3330		2.97				88.8		3210		2.95

		89.6		3300		2.97				89.4		3330		2.97				88.8		3210		2.95

		89.7		3300		2.97				89.4		3330		2.97				88.9		3210		2.95

		89.8		3300		2.98				89.5		3330		2.97				89		3210		2.96

		89.9		3300		2.98				89.5		3340		2.98				89.1		3210		2.96

		89.9		3300		2.98				89.6		3340		2.98				89.1		3210		2.96

		90		3310		2.98				89.7		3340		2.98				89.2		3210		2.96

		90.1		3310		2.99				89.7		3340		2.98				89.3		3210		2.96

		90.1		3310		2.99				89.8		3340		2.98				89.3		3210		2.97

		90.2		3310		2.99				89.9		3350		2.99				89.4		3220		2.97

		90.3		3310		2.99				90		3350		2.99				89.5		3220		2.97

		90.4		3320		3				90		3350		2.99				89.6		3220		2.97

		90.5		3320		3				90.1		3350		2.99				89.6		3220		2.98

		90.5		3320		3				90.2		3350		3				89.7		3220		2.98

		90.6		3320		3				90.2		3360		3				89.8		3220		2.98

		90.6		3320		3				90.3		3360		3				89.8		3220		2.98

		90.7		3330		3.01				90.4		3360		3				89.8		3220		2.98

		90.8		3330		3.01				90.5		3360		3.01				89.9		3220		2.99

		90.8		3330		3.01				90.5		3360		3.01				90		3230		2.99

		90.9		3330		3.01				90.6		3370		3.01				90		3230		2.99

		91		3330		3.02				90.7		3370		3.01				90.2		3230		2.99

		91		3330		3.02				90.7		3370		3.01				90.3		3230		3

		91.1		3330		3.02				90.8		3370		3.02				90.3		3230		3

		91.1		3340		3.02				90.8		3370		3.02				90.3		3230		3

		91.2		3340		3.02				90.9		3380		3.02				90.4		3230		3

		91.2		3340		3.03				91		3380		3.02				90.5		3240		3.01

		91.3		3340		3.03				91.1		3380		3.03				90.5		3240		3.01

		91.4		3340		3.03				91.2		3380		3.03				90.6		3240		3.01

		91.5		3350		3.03				91.2		3390		3.03				90.7		3240		3.01

		91.5		3350		3.03				91.3		3390		3.03				90.8		3240		3.02

		91.5		3350		3.04				91.3		3390		3.03				90.9		3240		3.02

		91.6		3350		3.04				91.4		3390		3.04				90.9		3240		3.02

		91.7		3360		3.04				91.4		3390		3.04				91		3250		3.02

		91.7		3360		3.04				91.5		3400		3.04				91		3250		3.02

		91.8		3360		3.04				91.7		3400		3.04				91.1		3250		3.03

		91.9		3360		3.05				91.7		3400		3.05				91.2		3250		3.03

		92		3360		3.05				91.8		3400		3.05				91.2		3250		3.03

		92		3360		3.05				91.8		3400		3.05				91.3		3250		3.03

		92.1		3360		3.05				91.9		3410		3.05				91.4		3250		3.04

		92.1		3370		3.05				91.9		3410		3.06				91.5		3260		3.04

		92.2		3370		3.06				92		3410		3.06				91.5		3260		3.04

		92.2		3370		3.06				92.1		3410		3.06				91.6		3260		3.04

		92.3		3370		3.06				92.2		3410		3.06				91.7		3260		3.04

		92.4		3370		3.06				92.2		3420		3.06				91.7		3260		3.05

		92.5		3380		3.07				92.3		3420		3.07				91.8		3260		3.05

		92.5		3380		3.07				92.3		3420		3.07				91.8		3260		3.05

		92.6		3380		3.07				92.4		3420		3.07				92		3260		3.06

		92.7		3380		3.07				92.5		3420		3.07				92.1		3260		3.06

		92.7		3380		3.08				92.5		3430		3.08				92.1		3270		3.06

		92.8		3390		3.08				92.6		3430		3.08				92.2		3270		3.06

		92.9		3390		3.08				92.7		3430		3.08				92.2		3270		3.06

		92.9		3390		3.08				92.8		3430		3.08				92.3		3270		3.07

		93		3390		3.08				92.8		3430		3.08				92.4		3270		3.07

		93		3390		3.09				92.9		3440		3.09				92.4		3270		3.07

		93.1		3400		3.09				93		3440		3.09				92.5		3270		3.07

		93.2		3400		3.09				93		3440		3.09				92.6		3270		3.07

		93.3		3400		3.09				93.1		3440		3.09				92.6		3280		3.08

		93.4		3400		3.1				93.1		3440		3.09				92.7		3280		3.08

		93.5		3400		3.1				93.2		3450		3.1				92.7		3280		3.08

		93.5		3410		3.1				93.3		3450		3.1				92.8		3280		3.08

		93.6		3410		3.1				93.4		3450		3.1				92.9		3280		3.09

		93.6		3410		3.1				93.5		3450		3.11				92.9		3280		3.09

		93.7		3410		3.11				93.5		3460		3.11				93		3290		3.09

		93.8		3410		3.11				93.6		3460		3.11				93.1		3290		3.09

		93.9		3410		3.11				93.7		3460		3.11				93.2		3290		3.09

		93.9		3420		3.11				93.7		3460		3.11				93.2		3290		3.1

		94		3420		3.12				93.8		3460		3.12				93.3		3290		3.1

		94		3420		3.12				93.8		3460		3.12				93.3		3290		3.1

		94.1		3420		3.12				94		3470		3.12				93.4		3300		3.1

		94.2		3420		3.12				94		3470		3.12				93.5		3300		3.11

		94.2		3430		3.12				94.1		3470		3.13				93.5		3300		3.11

		94.3		3430		3.13				94.1		3470		3.13				93.6		3300		3.11

		94.4		3430		3.13				94.2		3480		3.13				93.7		3300		3.11

		94.5		3430		3.13				94.3		3480		3.13				93.7		3300		3.11

		94.5		3430		3.13				94.3		3480		3.13				93.8		3300		3.12

		94.6		3430		3.14				94.4		3480		3.14				93.9		3310		3.12

		94.6		3440		3.14				94.5		3480		3.14				94		3310		3.12

		94.7		3440		3.14				94.6		3490		3.14				94		3310		3.12

		94.7		3440		3.14				94.6		3490		3.14				94.1		3310		3.12

		94.8		3440		3.14				94.7		3490		3.15				94.2		3310		3.13

		94.9		3440		3.15				94.8		3490		3.15				94.2		3310		3.13

		95		3440		3.15				94.8		3490		3.15				94.3		3320		3.13

		95		3450		3.15				94.9		3490		3.15				94.4		3320		3.13

		95		3450		3.15				95		3490		3.16				94.4		3320		3.14

		95.1		3450		3.15				95		3500		3.16				94.5		3320		3.14

		95.2		3450		3.16				95.1		3500		3.16				94.5		3320		3.14

		95.3		3450		3.16				95.2		3500		3.16				94.6		3320		3.14

		95.3		3450		3.16				95.2		3500		3.16				94.6		3320		3.14

		95.4		3460		3.16				95.3		3490		3.17				94.7		3330		3.15

		95.5		3460		3.17				95.4		3490		3.17				94.8		3330		3.15

		95.5		3460		3.17				95.4		3490		3.17				94.9		3330		3.15

		95.6		3460		3.17				95.5		3480		3.17				94.9		3330		3.15

		95.7		3460		3.17				95.6		3470		3.18				95		3330		3.16

		95.8		3470		3.18				95.6		3470		3.18				95.1		3340		3.16

		95.8		3470		3.18				95.7		3470		3.18				95.1		3340		3.16

		95.9		3470		3.18				95.8		3470		3.18				95.2		3340		3.16

		95.9		3470		3.18				95.8		3470		3.18				95.2		3340		3.16

		96		3470		3.18				95.9		3470		3.19				95.3		3340		3.17

		96.1		3470		3.19				95.9		3470		3.19				95.4		3340		3.17

		96.1		3480		3.19				96		3470		3.19				95.5		3350		3.17

		96.2		3480		3.19				96.1		3470		3.19				95.6		3350		3.17

		96.3		3480		3.19				96.2		3470		3.2				95.6		3350		3.18

		96.3		3480		3.19				96.2		3470		3.2				95.7		3350		3.18

		96.4		3480		3.2				96.3		3470		3.2				95.7		3350		3.18

		96.5		3480		3.2				96.3		3470		3.2				95.8		3350		3.18

		96.5		3480		3.2				96.4		3470		3.2				95.9		3350		3.18

		96.6		3480		3.2				96.5		3470		3.21				96		3360		3.19

		96.6		3480		3.21				96.6		3470		3.21				96		3360		3.19

		96.7		3480		3.21				96.7		3470		3.21				96.1		3360		3.19

		96.8		3480		3.21				96.7		3470		3.21				96.2		3360		3.19

		96.9		3480		3.21				96.8		3470		3.22				96.2		3360		3.2

		96.9		3480		3.21				96.9		3470		3.22				96.3		3370		3.2

		97		3480		3.22				96.9		3470		3.22				96.3		3370		3.2

		97		3480		3.22				97		3470		3.22				96.4		3370		3.2

		97.2		3490		3.22				97.1		3470		3.22				96.5		3370		3.2

		97.2		3490		3.22				97.1		3470		3.23				96.6		3370		3.21

		97.3		3490		3.23				97.2		3470		3.23				96.7		3380		3.21

		97.3		3490		3.23				97.3		3470		3.23				96.7		3380		3.21

		97.4		3490		3.23				97.3		3470		3.24				96.8		3380		3.22

		97.4		3500		3.23				97.4		3470		3.24				96.8		3380		3.22

		97.5		3500		3.23				97.5		3470		3.24				96.9		3380		3.22

		97.6		3500		3.24				97.5		3470		3.24				97		3380		3.22

		97.7		3500		3.24				97.6		3470		3.24				97		3380		3.22

		97.8		3500		3.24				97.7		3470		3.25				97.2		3390		3.23

		97.9		3500		3.24				97.7		3470		3.25				97.2		3390		3.23

		97.9		3500		3.25				97.8		3470		3.25				97.3		3390		3.23

		97.9		3500		3.25				97.9		3470		3.25				97.4		3390		3.23

		98		3500		3.25				97.9		3470		3.25				97.4		3390		3.24

		98.1		3500		3.25				98		3460		3.26				97.5		3400		3.24

		98.1		3500		3.26				98.1		3460		3.26				97.5		3400		3.24

		98.3		3500		3.26				98.2		3460		3.26				97.6		3400		3.24

		98.3		3500		3.26				98.2		3460		3.26				97.7		3400		3.25

		98.4		3500		3.26				98.2		3460		3.27				97.8		3400		3.25

		98.4		3500		3.26				98.3		3460		3.27				97.8		3410		3.25

		98.5		3500		3.27				98.4		3460		3.27				97.9		3410		3.25

		98.5		3500		3.27				98.5		3460		3.27				98		3410		3.25

		98.6		3500		3.27				98.6		3460		3.27				98		3410		3.26

		98.7		3500		3.27				98.6		3460		3.28				98.1		3410		3.26

		98.8		3500		3.28				98.6		3460		3.28				98.2		3410		3.26

		98.9		3500		3.28				98.7		3460		3.28				98.3		3410		3.26

		98.9		3500		3.28				98.8		3460		3.28				98.3		3420		3.27

		99		3500		3.28				98.9		3460		3.29				98.4		3420		3.27

		99		3500		3.29				98.9		3460		3.29				98.4		3420		3.27

		99.1		3500		3.29				99		3460		3.29				98.5		3420		3.27

		99.2		3500		3.29				99.1		3460		3.29				98.5		3420		3.27

		99.3		3510		3.29				99.1		3450		3.29				98.6		3420		3.28

		99.4		3500		3.3				99.2		3450		3.3				98.7		3430		3.28

		99.4		3500		3.3				99.3		3450		3.3				98.8		3430		3.28

		99.5		3500		3.3				99.3		3450		3.3				98.9		3430		3.28

		99.5		3510		3.3				99.4		3440		3.3				98.9		3430		3.29

		99.6		3510		3.3				99.5		3440		3.31				99		3430		3.29

		99.7		3500		3.31				99.5		3440		3.31				99		3440		3.29

		99.7		3500		3.31				99.6		3430		3.31				99.1		3440		3.29

		99.8		3500		3.31				99.7		3430		3.31				99.2		3440		3.3

		99.9		3500		3.31				99.7		3420		3.31				99.2		3440		3.3

		100		3500		3.32				99.8		3410		3.32				99.3		3440		3.3

		100		3500		3.32				99.8		3400		3.32				99.4		3440		3.3

		100		3490		3.32				99.9		3390		3.32				99.5		3450		3.3

		100		3490		3.32				100		3370		3.32				99.5		3450		3.31

		100		3490		3.33				100		3350		3.33				99.6		3450		3.31

		100		3490		3.33				100		3350		3.33				99.6		3450		3.31

		100		3480		3.33				100		3340		3.33				99.7		3450		3.31

		100		3480		3.33				100		3330		3.33				99.8		3450		3.32

		101		3480		3.33				100		3330		3.34				99.9		3460		3.32

		101		3480		3.34				100		3330		3.34				100		3460		3.32

		101		3480		3.34				100		3320		3.34				100		3460		3.32

		101		3470		3.34				101		3320		3.34				100		3460		3.33

		101		3470		3.34				101		3310		3.35				100		3460		3.33

		101		3470		3.34				101		3310		3.35				100		3470		3.33

		101		3470		3.35				101		3310		3.35				100		3470		3.33

		101		3470		3.35				101		3300		3.35				100		3470		3.33

		101		3460		3.35				101		3300		3.35				100		3470		3.34

		101		3460		3.36				101		3300		3.36				101		3470		3.34

		101		3460		3.36				101		3290		3.36				101		3470		3.34

		101		3460		3.36				101		3290		3.36				101		3480		3.34

		101		3460		3.36				101		3290		3.36				101		3480		3.35

		101		3460		3.36				101		3280		3.37				101		3480		3.35

		101		3460		3.37				101		3280		3.37				101		3480		3.35

		102		3460		3.37				101		3280		3.37				101		3480		3.35

		102		3460		3.37				101		3280		3.37				101		3490		3.35

		102		3460		3.37				102		3280		3.37				101		3490		3.35

		102		3460		3.38				102		3270		3.38				101		3490		3.36

		102		3460		3.38				102		3270		3.38				101		3490		3.36

		102		3460		3.38				102		3270		3.38				101		3490		3.36

		102		3460		3.38				102		3270		3.38				101		3490		3.36

		102		3460		3.38				102		3270		3.39				101		3500		3.37

		102		3460		3.39				102		3270		3.39				101		3500		3.37

		102		3460		3.39				102		3270		3.39				101		3500		3.37

		102		3460		3.39				102		3270		3.39				102		3500		3.37

		102		3460		3.39				102		3270		3.39				102		3500		3.38

		102		3460		3.4				102		3270		3.4				102		3510		3.38

		102		3460		3.4				102		3270		3.4				102		3510		3.38

		103		3460		3.4				102		3270		3.4				102		3510		3.38

		103		3460		3.4				102		3270		3.4				102		3510		3.38

		103		3460		3.41				102		3270		3.41				102		3510		3.39

		103		3460		3.41				103		3270		3.41				102		3510		3.39

		103		3460		3.41				103		3270		3.41				102		3520		3.39

		103		3460		3.41				103		3270		3.41				102		3520		3.39

		103		3460		3.42				103		3270		3.41				102		3520		3.4

		103		3460		3.42				103		3270		3.42				102		3520		3.4

		103		3460		3.42				103		3270		3.42				102		3520		3.4

		103		3460		3.42				103		3270		3.42				102		3520		3.4

		103		3460		3.42				103		3270		3.42				102		3530		3.4

		103		3460		3.43				103		3270		3.43				103		3530		3.41

		103		3460		3.43				103		3270		3.43				103		3530		3.41

		103		3460		3.43				103		3270		3.43				103		3530		3.41

		104		3460		3.43				103		3270		3.43				103		3530		3.41

		104		3460		3.44				103		3270		3.44				103		3540		3.42

		104		3460		3.44				103		3270		3.44				103		3540		3.42

		104		3460		3.44				104		3270		3.44				103		3540		3.42

		104		3460		3.44				104		3270		3.44				103		3540		3.42

		104		3460		3.44				104		3270		3.45				103		3540		3.42

		104		3460		3.45				104		3260		3.45				103		3540		3.43

		104		3460		3.45				104		3260		3.45				103		3550		3.43

		104		3460		3.45				104		3260		3.45				103		3550		3.43

		104		3470		3.45				104		3260		3.45				103		3550		3.43

		104		3460		3.46				104		3260		3.46				103		3550		3.43

		104		3460		3.46				104		3260		3.46				103		3550		3.44

		104		3460		3.46				104		3250		3.46				103		3550		3.44

		104		3460		3.46				104		3250		3.46				104		3550		3.44

		104		3470		3.47				104		3250		3.47				104		3560		3.44

		105		3470		3.47				104		3260		3.47				104		3560		3.45

		105		3470		3.47				104		3260		3.47				104		3560		3.45

		105		3470		3.47				104		3260		3.47				104		3560		3.45

		105		3470		3.47				105		3260		3.47				104		3560		3.45

		105		3470		3.48				105		3260		3.48				104		3560		3.45

		105		3470		3.48				105		3260		3.48				104		3570		3.46

		105		3470		3.48				105		3260		3.48				104		3570		3.46

		105		3470		3.48				105		3260		3.49				104		3570		3.46

		105		3470		3.49				105		3260		3.49				104		3570		3.46

		105		3470		3.49				105		3260		3.49				104		3570		3.46

		105		3470		3.49				105		3260		3.49				104		3570		3.47

		105		3480		3.49				105		3260		3.49				104		3570		3.47

		105		3480		3.49				105		3260		3.5				104		3580		3.47

		105		3480		3.5				105		3260		3.5				105		3580		3.47

		105		3480		3.5				105		3260		3.5				105		3580		3.48

		105		3480		3.5				105		3250		3.5				105		3580		3.48

		106		3480		3.5				105		3200		3.5				105		3580		3.48

		106		3480		3.51				105		3180		3.51				105		3580		3.48

		106		3480		3.51				106		3180		3.51				105		3590		3.48

		106		3480		3.51				106		3170		3.51				105		3590		3.49

		106		3480		3.51				106		3180		3.52				105		3590		3.49

		106		3480		3.51				106		3180		3.52				105		3590		3.49

		106		3490		3.52				106		3180		3.52				105		3590		3.49

		106		3490		3.52				106		3180		3.52				105		3590		3.5

		106		3490		3.52				106		3190		3.52				105		3600		3.5

		106		3490		3.52				106		3190		3.53				105		3600		3.5

		106		3490		3.53				106		3190		3.53				105		3600		3.5

		106		3490		3.53				106		3190		3.53				105		3600		3.5

		106		3490		3.53				106		3190		3.53				106		3600		3.51

		106		3490		3.53				106		3200		3.53				106		3600		3.51

		106		3490		3.53				106		3200		3.54				106		3610		3.51

		107		3500		3.54				106		3200		3.54				106		3610		3.51

		107		3500		3.54				107		3200		3.54				106		3610		3.52

		107		3500		3.54				107		3200		3.54				106		3610		3.52

		107		3500		3.54				107		3200		3.55				106		3610		3.52

		107		3500		3.55				107		3200		3.55				106		3610		3.52

		107		3500		3.55				107		3200		3.55				106		3620		3.53

		107		3500		3.55				107		3200		3.55				106		3620		3.53

		107		3500		3.55				107		3210		3.55				106		3620		3.53

		107		3510		3.55				107		3210		3.56				106		3620		3.53

		107		3510		3.56				107		3210		3.56				106		3620		3.54

		107		3510		3.56				107		3210		3.56				106		3620		3.54

		107		3510		3.56				107		3210		3.56				107		3630		3.54

		107		3510		3.56				107		3210		3.56				107		3630		3.54

		107		3510		3.57				107		3210		3.57				107		3630		3.54

		108		3510		3.57				107		3220		3.57				107		3630		3.55

		108		3510		3.57				107		3220		3.57				107		3640		3.55

		108		3510		3.57				108		3220		3.57				107		3640		3.55

		108		3510		3.57				108		3220		3.58				107		3640		3.55

		108		3510		3.58				108		3220		3.58				107		3640		3.56

		108		3520		3.58				108		3230		3.58				107		3640		3.56

		108		3520		3.58				108		3230		3.58				107		3640		3.56

		108		3520		3.58				108		3230		3.58				107		3640		3.56

		108		3520		3.58				108		3230		3.59				107		3650		3.56

		108		3520		3.59				108		3230		3.59				107		3650		3.57

		108		3520		3.59				108		3230		3.59				107		3650		3.57

		108		3520		3.59				108		3240		3.59				108		3650		3.57

		108		3520		3.59				108		3240		3.6				108		3650		3.57

		108		3520		3.59				108		3240		3.6				108		3650		3.58

		108		3530		3.6				108		3240		3.6				108		3660		3.58

		108		3530		3.6				108		3240		3.6				108		3660		3.58

		109		3530		3.6				108		3240		3.6				108		3660		3.58

		109		3530		3.6				108		3250		3.61				108		3660		3.59

		109		3530		3.61				109		3250		3.61				108		3660		3.59

		109		3530		3.61				109		3250		3.61				108		3660		3.59

		109		3530		3.61				109		3250		3.61				108		3670		3.59

		109		3530		3.61				109		3250		3.62				108		3670		3.6

		109		3540		3.61				109		3250		3.62				108		3670		3.6

		109		3540		3.62				109		3250		3.62				108		3670		3.6

		109		3540		3.62				109		3250		3.62				108		3670		3.6

		109		3540		3.62				109		3250		3.62				108		3670		3.6

		109		3540		3.62				109		3260		3.63				109		3680		3.61

		109		3540		3.62				109		3260		3.63				109		3680		3.61

		109		3540		3.63				109		3260		3.63				109		3680		3.61

		109		3540		3.63				109		3260		3.63				109		3680		3.61

		109		3540		3.63				109		3260		3.64				109		3680		3.62

		109		3550		3.63				109		3260		3.64				109		3680		3.62

		110		3550		3.64				109		3260		3.64				109		3690		3.62

		110		3550		3.64				110		3260		3.64				109		3690		3.62

		110		3540		3.64				110		3260		3.64				109		3690		3.62

		110		3540		3.64				110		3260		3.65				109		3690		3.63

		110		3540		3.65				110		3270		3.65				109		3690		3.63

		110		3540		3.65				110		3270		3.65				109		3700		3.63

		110		3550		3.65				110		3270		3.65				109		3700		3.63

		110		3550		3.65				110		3270		3.66				109		3700		3.64

		110		3550		3.65				110		3270		3.66				109		3700		3.64

		110		3550		3.66				110		3270		3.66				110		3700		3.64

		110		3550		3.66				110		3270		3.66				110		3700		3.64

		110		3550		3.66				110		3270		3.67				110		3710		3.64

		110		3550		3.66				110		3270		3.67				110		3710		3.65

		110		3560		3.67				110		3280		3.67				110		3710		3.65

		111		3560		3.67				110		3280		3.67				110		3710		3.65

		111		3560		3.67				111		3280		3.67				110		3720		3.65

		111		3560		3.67				111		3280		3.68				110		3720		3.66

		111		3560		3.68				111		3280		3.68				110		3720		3.66

		111		3560		3.68				111		3280		3.68				110		3720		3.66

		111		3560		3.68				111		3270		3.68				110		3720		3.66

		111		3560		3.68				111		3270		3.69				110		3720		3.66

		111		3560		3.68				111		3260		3.69				110		3730		3.67

		111		3570		3.69				111		3250		3.69				110		3730		3.67

		111		3570		3.69				111		3190		3.69				110		3730		3.67

		111		3570		3.69				111		3140		3.7				111		3730		3.67

		111		3570		3.69				111		3100		3.7				111		3730		3.68

		111		3570		3.7				111		3050		3.7				111		3730		3.68

		111		3570		3.7				111		2950		3.7				111		3740		3.68

		112		3570		3.7				111		2830		3.7				111		3740		3.68

		112		3570		3.7				111		2710		3.71				111		3740		3.68

		112		3580		3.7				112		2640		3.71				111		3740		3.69

		112		3580		3.71				112		2600		3.71				111		3750		3.69

		112		3580		3.71				112		2570		3.71				111		3750		3.69

		112		3580		3.71				112		2550		3.72				111		3750		3.69

		112		3580		3.71				112		2530		3.72				111		3750		3.7

		112		3580		3.72				112		2510		3.72				111		3750		3.7

		112		3580		3.72				112		2480		3.72				111		3750		3.7

		112		3580		3.72				112		2470		3.73				111		3750		3.7

		112		3590		3.72				112		2460		3.73				111		3750		3.71

		112		3590		3.72				112		2450		3.73				112		3760		3.71

		112		3590		3.73				112		2450		3.73				112		3760		3.71

		112		3590		3.73				112		2440		3.73				112		3760		3.71

		112		3590		3.73				112		2430		3.74				112		3760		3.71

		113		3590		3.74				112		2420		3.74				112		3760		3.72

		113		3590		3.74				112		2410		3.74				112		3770		3.72

		113		3590		3.74				113		2390		3.74				112		3770		3.72

		113		3590		3.74				113		2380		3.75				112		3770		3.72

		113		3590		3.74				113		2360		3.75				112		3770		3.73

		113		3600		3.75				113		2350		3.75				112		3770		3.73

		113		3600		3.75				113		2340		3.75				112		3780		3.73

		113		3600		3.75				113		2330		3.75				112		3780		3.73

		113		3600		3.75				113		2320		3.76				112		3780		3.74

		113		3600		3.76				113		2310		3.76				112		3780		3.74

		113		3600		3.76				113		2300		3.76				113		3780		3.74

		113		3600		3.76				113		2290		3.76				113		3780		3.74

		113		3610		3.76				113		2280		3.77				113		3790		3.75

		113		3600		3.76				113		2280		3.77				113		3790		3.75

		113		3610		3.77				113		2270		3.77				113		3790		3.75

		114		3610		3.77				113		2260		3.77				113		3790		3.75

		114		3610		3.77				114		2260		3.77				113		3790		3.75

		114		3610		3.77				114		2250		3.78				113		3800		3.76

		114		3610		3.78				114		2240		3.78				113		3800		3.76

		114		3610		3.78				114		2230		3.78				113		3800		3.76

		114		3610		3.78				114		2230		3.78				113		3800		3.76

		114		3620		3.78				114		2220		3.79				113		3800		3.77

		114		3610		3.78				114		2220		3.79				113		3810		3.77

		114		3620		3.79				114		2210		3.79				113		3810		3.77

		114		3620		3.79				114		2200		3.79				113		3810		3.77

		114		3620		3.79				114		2200		3.79				114		3810		3.77

		114		3620		3.79				114		2190		3.8				114		3810		3.78

		114		3620		3.8				114		2180		3.8				114		3810		3.78

		114		3620		3.8				114		2180		3.8				114		3820		3.78

		114		3620		3.8				114		2170		3.81				114		3820		3.78

		115		3620		3.8				114		2160		3.81				114		3820		3.79

		115		3620		3.8				115		2160		3.81				114		3820		3.79

		115		3630		3.81				115		2150		3.81				114		3820		3.79

		115		3620		3.81				115		2150		3.81				114		3820		3.79

		115		3630		3.81				115		2140		3.82				114		3820		3.79

		115		3630		3.81				115		2130		3.82				114		3820		3.8

		115		3630		3.81				115		2130		3.82				114		3830		3.8

		115		3630		3.82				115		2120		3.82				114		3830		3.8

		115		3630		3.82				115		2120		3.83				114		3830		3.8

		115		3630		3.82				115		2110		3.83				115		3830		3.81

		115		3630		3.82				115		2110		3.83				115		3830		3.81

		115		3630		3.82				115		2100		3.83				115		3830		3.81

		115		3640		3.83				115		2100		3.83				115		3840		3.81

		115		3640		3.83				115		2090		3.84				115		3840		3.81

		115		3640		3.83				115		2080		3.84				115		3840		3.82

		116		3640		3.83				116		2080		3.84				115		3840		3.82

		116		3640		3.84				116		2070		3.84				115		3840		3.82

		116		3640		3.84				116		2070		3.85				115		3850		3.82

		116		3640		3.84				116		2070		3.85				115		3850		3.83

		116		3640		3.84				116		2060		3.85				115		3850		3.83

		116		3650		3.85				116		2060		3.85				115		3850		3.83

		116		3650		3.85				116		2060		3.85				115		3850		3.83

		116		3650		3.85				116		2050		3.86				115		3850		3.84

		116		3650		3.85				116		2050		3.86				115		3860		3.84

		116		3650		3.85				116		2040		3.86				116		3860		3.84

		116		3650		3.86				116		2040		3.86				116		3860		3.84

		116		3650		3.86				116		2040		3.87				116		3860		3.85

		116		3660		3.86				116		2030		3.87				116		3860		3.85

		116		3660		3.86				116		2030		3.87				116		3860		3.85

		116		3660		3.87				116		2030		3.87				116		3870		3.85

		117		3660		3.87				117		2020		3.88				116		3870		3.85

		117		3660		3.87				117		2020		3.88				116		3870		3.86

		117		3660		3.87				117		2020		3.88				116		3870		3.86

		117		3660		3.87				117		2010		3.88				116		3870		3.86

		117		3670		3.88				117		2010		3.89				116		3870		3.86

		117		3670		3.88				117		2010		3.89				116		3880		3.87

		117		3670		3.88				117		2010		3.89				116		3880		3.87

		117		3670		3.88				117		2000		3.89				116		3880		3.87

		117		3670		3.89				117		2000		3.9				116		3880		3.87

		117		3670		3.89				117		2000		3.9				117		3880		3.87

		117		3680		3.89				117		1990		3.9				117		3880		3.88

		117		3680		3.89				117		1990		3.9				117		3880		3.88

		117		3680		3.89				117		1990		3.9				117		3890		3.88

		117		3680		3.9				117		1990		3.91				117		3890		3.88

		117		3680		3.9				118		1990		3.91				117		3890		3.88

		118		3680		3.9				118		1980		3.91				117		3890		3.89

		118		3690		3.9				118		1980		3.91				117		3890		3.89

		118		3690		3.91				118		1980		3.92				117		3890		3.89

		118		3690		3.91				118		1970		3.92				117		3900		3.89

		118		3690		3.91				118		1970		3.92				117		3900		3.9

		118		3690		3.91				118		1970		3.92				117		3900		3.9

		118		3690		3.91				118		1970		3.92				117		3900		3.9

		118		3690		3.92				118		1970		3.93				117		3900		3.9

		118		3690		3.92				118		1960		3.93				117		3900		3.9

		118		3700		3.92				118		1960		3.93				117		3900		3.91

		118		3700		3.92				118		1960		3.93				118		3900		3.91

		118		3700		3.93				118		1960		3.94				118		3910		3.91

		118		3700		3.93				118		1950		3.94				118		3910		3.91

		118		3700		3.93				119		1950		3.94				118		3910		3.92

		118		3710		3.93				119		1950		3.94				118		3910		3.92

		119		3710		3.93				119		1950		3.94				118		3910		3.92

		119		3710		3.94				119		1950		3.95				118		3910		3.92

		119		3710		3.94				119		1940		3.95				118		3920		3.92

		119		3710		3.94				119		1940		3.95				118		3920		3.93

		119		3710		3.94				119		1940		3.96				118		3920		3.93

		119		3710		3.95				119		1940		3.96				118		3920		3.93

		119		3720		3.95				119		1940		3.96				118		3920		3.93

		119		3720		3.95				119		1930		3.96				118		3920		3.94

		119		3720		3.95				119		1930		3.96				118		3920		3.94

		119		3720		3.95				119		1930		3.97				119		3930		3.94

		119		3720		3.96				119		1930		3.97				119		3930		3.94

		119		3720		3.96				119		1920		3.97				119		3930		3.94

		119		3720		3.96				119		1920		3.97				119		3930		3.95

		119		3730		3.96				120		1920		3.97				119		3930		3.95

		119		3730		3.97				120		1920		3.98				119		3930		3.95

		120		3730		3.97				120		1920		3.98				119		3930		3.95

		120		3730		3.97				120		1910		3.98				119		3930		3.96

		120		3730		3.97				120		1910		3.98				119		3850		3.96

		120		3730		3.97				120		1910		3.99				119		3760		3.96

		120		3730		3.98				120		1910		3.99				119		3720		3.96

		120		3730		3.98				120		1900		3.99				119		3680		3.97

		120		3740		3.98				120		1900		3.99				119		3650		3.97

		120		3740		3.98				120		1900		3.99				119		3600		3.97

		120		3740		3.99				120		1900		4				120		3570		3.97

		120		3740		3.99				120		1900		4				120		3540		3.97

		120		3740		3.99				120		1900		4				120		3510		3.98

		120		3750		3.99				120		1890		4				120		3480		3.98

		120		3750		4				120		1890		4.01				120		3450		3.98

		120		3750		4				121		1890		4.01				120		3430		3.98

		121		3750		4				121		1890		4.01				120		3410		3.98

		121		3750		4				121		1890		4.01				120		3390		3.99

		121		3750		4.01				121		1880		4.02				120		3350		3.99

		121		3750		4.01				121		1880		4.02				120		3320		3.99

		121		3750		4.01				121		1880		4.02				120		3290		3.99

		121		3750		4.01				121		1880		4.02				120		3260		4

		121		3760		4.01				121		1880		4.02				120		3240		4

		121		3760		4.02				121		1880		4.03				120		3220		4

		121		3760		4.02				121		1870		4.03				120		3200		4

		121		3740		4.02				121		1870		4.03				120		3180		4

		121		3740		4.02				121		1870		4.03				121		3160		4.01

		121		3750		4.03				121		1870		4.04				121		3140		4.01

		121		3750		4.03				121		1870		4.04				121		3130		4.01

		121		3750		4.03				121		1860		4.04				121		3120		4.01

		121		3760		4.03				122		1860		4.04				121		3110		4.02

		122		3760		4.04				122		1860		4.05				121		3100		4.02

		122		3760		4.04				122		1860		4.05				121		3090		4.02

		122		3760		4.04				122		1860		4.05				121		3080		4.02

		122		3760		4.04				122		1860		4.05				121		3070		4.02

		122		3760		4.04				122		1860		4.05				121		3050		4.03

		122		3760		4.05				122		1860		4.06				121		3040		4.03

		122		3760		4.05				122		1850		4.06				121		3030		4.03

		122		3770		4.05				122		1850		4.06				121		3020		4.03

		122		3770		4.05				122		1850		4.06				121		3010		4.04

		122		3770		4.06				122		1850		4.07				122		2990		4.04

		122		3770		4.06				122		1850		4.07				122		2980		4.04

		122		3770		4.06				122		1850		4.07				122		2970		4.04

		122		3770		4.06				122		1840		4.07				122		2960		4.05

		122		3770		4.06				123		1840		4.07				122		2940		4.05

		122		3780		4.07				123		1840		4.08				122		2930		4.05

		123		3780		4.07				123		1840		4.08				122		2910		4.05

		123		3780		4.07				123		1840		4.08				122		2900		4.05

		123		3780		4.07				123		1840		4.08				122		2890		4.06

		123		3780		4.08				123		1840		4.09				122		2880		4.06

		123		3780		4.08				123		1840		4.09				122		2860		4.06

		123		3780		4.08				123		1840		4.09				122		2850		4.06

		123		3780		4.08				123		1830		4.09				122		2840		4.06

		123		3780		4.08				123		1830		4.1				122		2820		4.07

		123		3790		4.09				123		1830		4.1				122		2800		4.07

		123		3790		4.09				123		1830		4.1				122		2790		4.07

		123		3790		4.09				123		1830		4.1				123		2780		4.07

		123		3790		4.09				123		1830		4.11				123		2760		4.08

		123		3790		4.1				124		1830		4.11				123		2750		4.08

		123		3790		4.1				124		1830		4.11				123		2740		4.08

		123		3790		4.1				124		1830		4.11				123		2730		4.08

		124		3790		4.1				124		1820		4.11				123		2720		4.08

		124		3800		4.11				124		1820		4.12				123		2700		4.09

		124		3800		4.11				124		1820		4.12				123		2690		4.09

		124		3800		4.11				124		1820		4.12				123		2680		4.09

		124		3800		4.11				124		1820		4.12				123		2670		4.09

		124		3800		4.11				124		1820		4.13				123		2660		4.1

		124		3800		4.12				124		1820		4.13				123		2650		4.1

		124		3800		4.12				124		1820		4.13				123		2640		4.1

		124		3800		4.12				124		1820		4.13				123		2630		4.1

		124		3810		4.12				124		1820		4.13				124		2630		4.11

		124		3810		4.13				124		1810		4.14				124		2610		4.11

		124		3810		4.13				124		1810		4.14				124		2610		4.11

		124		3810		4.13				125		1810		4.14				124		2600		4.11

		124		3810		4.13				125		1810		4.14				124		2590		4.12

		125		3820		4.13				125		1810		4.14				124		2590		4.12

		125		3820		4.14				125		1810		4.15				124		2580		4.12

		125		3820		4.14				125		1810		4.15				124		2570		4.12

		125		3820		4.14				125		1810		4.15				124		2570		4.12

		125		3820		4.14				125		1810		4.15				124		2560		4.13

		125		3820		4.14				125		1810		4.16				124		2550		4.13

		125		3820		4.15				125		1810		4.16				124		2550		4.13

		125		3820		4.15				125		1810		4.16				124		2540		4.13

		125		3820		4.15				125		1800		4.16				124		2540		4.14

		125		3830		4.15				125		1800		4.16				124		2530		4.14

		125		3830		4.16				125		1800		4.17				125		2530		4.14

		125		3830		4.16				125		1800		4.17				125		2520		4.14

		125		3830		4.16				125		1800		4.17				125		2520		4.14

		125		3830		4.16				126		1800		4.17				125		2510		4.15

		125		3830		4.17				126		1800		4.18				125		2510		4.15

		126		3830		4.17				126		1800		4.18				125		2500		4.15

		126		3840		4.17				126		1800		4.18				125		2500		4.15

		126		3840		4.17				126		1800		4.18				125		2490		4.16

		126		3840		4.17				126		1790		4.19				125		2490		4.16

		126		3830		4.18				126		1790		4.19				125		2480		4.16

		126		3820		4.18				126		1790		4.19				125		2480		4.16

		126		3820		4.18				126		1790		4.19				125		2470		4.16

		126		3800		4.19				126		1790		4.19				125		2470		4.17

		126		3790		4.19				126		1790		4.2				125		2460		4.17

		126		3780		4.19				126		1790		4.2				125		2460		4.17

		126		3780		4.19				126		1790		4.2				126		2450		4.17

		126		3780		4.19				126		1790		4.2				126		2450		4.18

		126		3770		4.2				127		1790		4.21				126		2440		4.18

		126		3770		4.2				127		1790		4.21				126		2440		4.18

		126		3770		4.2				127		1780		4.21				126		2440		4.18

		127		3760		4.2				127		1780		4.21				126		2430		4.18

		127		3760		4.21				127		1780		4.22				126		2430		4.19

		127		3760		4.21				127		1780		4.22				126		2420		4.19

		127		3760		4.21				127		1780		4.22				126		2420		4.19

		127		3760		4.21				127		1780		4.22				126		2420		4.19

		127		3750		4.21				127		1780		4.22				126		2410		4.19

		127		3750		4.22				127		1780		4.23				126		2410		4.2

		127		3750		4.22				127		1780		4.23				126		2400		4.2

		127		3710		4.22				127		1780		4.23				126		2400		4.2

		127		3660		4.22				127		1780		4.23				126		2390		4.2

		127		3640		4.23				127		1780		4.24				127		2390		4.21

		127		3620		4.23				127		1770		4.24				127		2380		4.21

		127		3590		4.23				128		1770		4.24				127		2380		4.21

		127		3570		4.23				128		1770		4.24				127		2380		4.21

		127		3540		4.23				128		1770		4.25				127		2370		4.21

		128		3490		4.24				128		1770		4.25				127		2370		4.22

		128		3440		4.24				128		1770		4.25				127		2360		4.22

		128		3370		4.24				128		1770		4.25				127		2360		4.22

		128		3340		4.24				128		1770		4.25				127		2350		4.22

		128		3320		4.25				128		1770		4.26				127		2350		4.23

		128		3310		4.25				128		1770		4.26				127		2350		4.23

		128		3300		4.25				128		1770		4.26				127		2340		4.23

		128		3300		4.25				128		1770		4.26				127		2340		4.23

		128		3290		4.26				128		1760		4.26				127		2340		4.23

		128		3290		4.26				128		1760		4.27				127		2330		4.24

		128		3280		4.26				128		1760		4.27				127		2330		4.24

		128		3280		4.26				128		1760		4.27				128		2320		4.24

		128		3280		4.27				129		1760		4.28				128		2320		4.24

		128		3280		4.27				129		1760		4.28				128		2310		4.25

		129		3270		4.27				129		1760		4.28				128		2310		4.25

		129		3260		4.27				129		1760		4.28				128		2300		4.25

		129		3260		4.27				129		1760		4.28				128		2300		4.25

		129		3250		4.28				129		1760		4.29				128		2300		4.26

		129		3210		4.28				129		1750		4.29				128		2290		4.26

		129		3170		4.28				129		1750		4.29				128		2290		4.26

		129		3140		4.28				129		1750		4.29				128		2280		4.26

		129		3120		4.29				129		1750		4.3				128		2280		4.26

		129		3100		4.29				129		1750		4.3				128		2280		4.27

		129		3080		4.29				129		1750		4.3				128		2280		4.27

		129		3060		4.29				129		1750		4.3				128		2270		4.27

		129		3040		4.29				129		1750		4.3				129		2270		4.27

		129		3000		4.3				130		1750		4.31				129		2270		4.27

		130		2990		4.3				130		1750		4.31				129		2260		4.28

		130		2980		4.3				130		1750		4.31				129		2260		4.28

		130		2960		4.3				130		1740		4.31				129		2260		4.28

		130		2950		4.31				130		1740		4.32				129		2250		4.28

		130		2940		4.31				130		1740		4.32				129		2250		4.29

		130		2930		4.31				130		1740		4.32				129		2250		4.29

		130		2920		4.31				130		1740		4.32				129		2240		4.29

		130		2890		4.32				130		1740		4.33				129		2240		4.29

		130		2880		4.32				130		1740		4.33				129		2240		4.29

		130		2870		4.32				130		1740		4.33				129		2230		4.3

		130		2860		4.32				130		1740		4.33				129		2230		4.3

		130		2860		4.33				130		1740		4.34				129		2220		4.3

		130		2850		4.33				130		1740		4.34				129		2220		4.31

		130		2840		4.33				130		1740		4.34				130		2220		4.31

		130		2840		4.33				131		1740		4.34				130		2210		4.31

		131		2830		4.33				131		1740		4.34				130		2210		4.31

		131		2760		4.34				131		1740		4.35				130		2210		4.31

		131		2730		4.34				131		1730		4.35				130		2200		4.32

		131		2710		4.34				131		1730		4.35				130		2200		4.32

		131		2700		4.34				131		1730		4.35				130		2200		4.32

		131		2690		4.35				131		1730		4.36				130		2190		4.32

		131		2680		4.35				131		1730		4.36				130		2190		4.33

		131		2670		4.35				131		1730		4.36				130		2190		4.33

		131		2660		4.35				131		1730		4.36				130		2180		4.33

		131		2650		4.35				131		1730		4.36				130		2180		4.33

		131		2640		4.36				131		1730		4.37				130		2180		4.33

		131		2640		4.36				131		1730		4.37				130		2170		4.34

		131		2630		4.36				131		1730		4.37				131		2170		4.34

		131		2630		4.37				132		1730		4.37				131		2170		4.34

		132		2630		4.37				132		1730		4.38				131		2170		4.34

		132		2620		4.37				132		1730		4.38				131		2160		4.35

		132		2540		4.37				132		1720		4.38				131		2160		4.35

		132		2510		4.37				132		1720		4.38				131		2160		4.35

		132		2500		4.38				132		1720		4.39				131		2160		4.35

		132		2500		4.38				132		1720		4.39				131		2150		4.36

		132		2490		4.38				132		1720		4.39				131		2150		4.36

		132		2490		4.38				132		1720		4.39				131		2150		4.36

		132		2490		4.39				132		1720		4.39				131		2150		4.36

		132		2490		4.39				132		1720		4.4				131		2140		4.36

		132		2480		4.39				132		1720		4.4				131		2140		4.37

		132		2480		4.39				132		1720		4.4				131		2140		4.37

		132		2480		4.39				132		1720		4.4				131		2130		4.37

		132		2480		4.4				132		1720		4.41				131		2130		4.37

		132		2480		4.4				133		1720		4.41				132		2130		4.38

		133		2480		4.4				133		1710		4.41				132		2130		4.38

		133		2470		4.4				133		1710		4.41				132		2120		4.38

		133		2470		4.41				133		1710		4.42				132		2120		4.38

		133		2470		4.41				133		1710		4.42				132		2120		4.39

		133		2470		4.41				133		1710		4.42				132		2120		4.39

		133		2470		4.41				133		1710		4.42				132		2120		4.39

		133		2470		4.41				133		1710		4.42				132		2110		4.39

		133		2460		4.42				133		1710		4.43				132		2110		4.39

		133		2460		4.42				133		1710		4.43				132		2110		4.4

		133		2460		4.42				133		1710		4.43				132		2110		4.4

		133		2460		4.42				133		1710		4.43				132		2110		4.4

		133		2460		4.43				133		1710		4.44				132		2100		4.4

		133		2460		4.43				133		1710		4.44				132		2100		4.41

		133		2460		4.43				134		1710		4.44				133		2100		4.41

		133		2450		4.43				134		1710		4.44				133		2100		4.41

		134		2450		4.43				134		1710		4.44				133		2100		4.41

		134		2450		4.44				134		1710		4.45				133		2100		4.41

		134		2450		4.44				134		1710		4.45				133		2090		4.42

		134		2450		4.44				134		1710		4.45				133		2090		4.42

		134		2440		4.44				134		1700		4.45				133		2090		4.42

		134		2440		4.45				134		1700		4.46				133		2090		4.42

		134		2440		4.45				134		1700		4.46				133		2090		4.43

		134		2440		4.45				134		1700		4.46				133		2090		4.43

		134		2440		4.45				134		1700		4.46				133		2080		4.43

		134		2440		4.45				134		1700		4.46				133		2080		4.43

		134		2440		4.46				134		1700		4.47				133		2080		4.44

		134		2430		4.46				134		1700		4.47				133		2080		4.44

		134		2430		4.46				134		1700		4.47				134		2080		4.44

		134		2430		4.46				134		1700		4.47				134		2080		4.44

		134		2430		4.46				135		1700		4.48				134		2080		4.44

		135		2430		4.47				135		1700		4.48				134		2080		4.45

		135		2430		4.47				135		1700		4.48				134		2080		4.45

		135		2420		4.47				135		1700		4.48				134		2070		4.45

		135		2420		4.47				135		1700		4.48				134		2070		4.45

		135		2420		4.48				135		1700		4.49				134		2070		4.46

		135		2420		4.48				135		1690		4.49				134		2070		4.46

		135		2420		4.48				135		1690		4.49				134		2070		4.46

		135		2420		4.48				135		1690		4.49				134		2070		4.46

		135		2420		4.48				135		1690		4.5				134		2070		4.47

		135		2410		4.49				135		1690		4.5				134		2070		4.47

		135		2410		4.49				135		1690		4.5				134		2060		4.47

		135		2410		4.49				135		1690		4.5				134		2060		4.47

		135		2410		4.49				135		1690		4.51				135		2060		4.47

		135		2410		4.5				136		1690		4.51				135		2060		4.48

		135		2410		4.5				136		1690		4.51				135		2060		4.48

		136		2410		4.5				136		1690		4.51				135		2060		4.48

		136		2400		4.5				136		1690		4.51				135		2060		4.48

		136		2400		4.51				136		1690		4.52				135		2060		4.49

		136		2400		4.51				136		1690		4.52				135		2060		4.49

		136		2400		4.51				136		1690		4.52				135		2050		4.49

		136		2400		4.51				136		1690		4.52				135		2050		4.49

		136		2400		4.51				136		1690		4.53				135		2050		4.49

		136		2400		4.52				136		1690		4.53				135		2050		4.5

		136		2390		4.52				136		1690		4.53				135		2050		4.5

		136		2390		4.52				136		1690		4.53				135		2050		4.5

		136		2390		4.52				136		1690		4.53				135		2050		4.51

		136		2390		4.53				136		1690		4.54				136		2050		4.51

		136		2390		4.53				136		1690		4.54				136		2040		4.51

		136		2390		4.53				137		1680		4.54				136		2040		4.51

		136		2390		4.53				137		1680		4.54				136		2040		4.51

		136		2390		4.53				137		1680		4.55				136		2040		4.52

		137		2390		4.54				137		1680		4.55				136		2040		4.52

		137		2390		4.54				137		1680		4.55				136		2040		4.52

		137		2380		4.54				137		1680		4.55				136		2040		4.52

		137		2380		4.54				137		1680		4.55				136		2040		4.52

		137		2380		4.54				137		1680		4.56				136		2040		4.53

		137		2380		4.55				137		1680		4.56				136		2040		4.53

		137		2380		4.55				137		1680		4.56				136		2040		4.53

		137		2380		4.55				137		1680		4.56				136		2030		4.53

		137		2380		4.55				137		1680		4.57				136		2030		4.54

		137		2380		4.56				137		1680		4.57				137		2030		4.54

		137		2380		4.56				137		1680		4.57				137		2030		4.54

		137		2370		4.56				137		1680		4.57				137		2030		4.54

		137		2370		4.56				138		1680		4.57				137		2030		4.55

		137		2370		4.57				138		1680		4.58				137		2030		4.55

		138		2370		4.57				138		1680		4.58				137		2030		4.55

		138		2370		4.57				138		1680		4.58				137		2030		4.55

		138		2370		4.57				138		1680		4.58				137		2030		4.55

		138		2370		4.57				138		1680		4.59				137		2020		4.56

		138		2370		4.58				138		1670		4.59				137		2020		4.56

		138		2360		4.58				138		1670		4.59				137		2020		4.56

		138		2360		4.58				138		1670		4.59				137		2020		4.56

		138		2360		4.58				138		1670		4.59				137		2020		4.57

		138		2360		4.59				138		1670		4.6				137		2020		4.57

		138		2360		4.59				138		1670		4.6				137		2020		4.57

		138		2360		4.59				138		1670		4.6				137		2020		4.57

		138		2360		4.59				138		1670		4.61				138		2020		4.57

		138		2360		4.59				138		1670		4.61				138		2020		4.58

		138		2360		4.6				139		1670		4.61				138		2010		4.58

		138		2360		4.6				139		1670		4.61				138		2010		4.58

		139		2350		4.6				139		1670		4.61				138		2010		4.58

		139		2350		4.6				139		1670		4.62				138		2010		4.59

		139		2350		4.61				139		1670		4.62				138		2010		4.59

		139		2350		4.61				139		1670		4.62				138		2010		4.59

		139		2350		4.61				139		1670		4.62				138		2010		4.59

		139		2350		4.61				139		1670		4.62				138		2010		4.6

		139		2350		4.61				139		1670		4.63				138		2010		4.6

		139		2350		4.62				139		1670		4.63				138		2010		4.6

		139		2350		4.62				139		1670		4.63				138		2010		4.6

		139		2350		4.62				139		1670		4.63				138		2000		4.6

		139		2350		4.63				139		1670		4.64				139		2000		4.61

		139		2350		4.63				139		1670		4.64				139		2000		4.61

		139		2350		4.63				140		1660		4.64				139		2000		4.61

		139		2350		4.63				140		1660		4.64				139		2000		4.61

		140		2350		4.63				140		1660		4.65				139		2000		4.62

		140		2350		4.64				140		1660		4.65				139		2000		4.62

		140		2340		4.64				140		1660		4.65				139		2000		4.62

		140		2340		4.64				140		1660		4.65				139		2000		4.62

		140		2340		4.64				140		1660		4.65				139		2000		4.62

		140		2340		4.64				140		1660		4.66				139		1990		4.63

		140		2340		4.65				140		1660		4.66				139		1990		4.63

		140		2340		4.65				140		1660		4.66				139		1990		4.63

		140		2340		4.65				140		1660		4.66				139		1990		4.63

		140		2340		4.65				140		1660		4.67				139		1990		4.64

		140		2340		4.66				140		1660		4.67				139		1990		4.64

		140		2340		4.66				140		1660		4.67				140		1990		4.64

		140		2340		4.66				140		1660		4.67				140		1990		4.64

		140		2340		4.66				140		1660		4.67				140		1990		4.65

		140		2330		4.66				141		1660		4.68				140		1980		4.65

		140		2330		4.67				141		1660		4.68				140		1980		4.65

		141		2330		4.67				141		1650		4.68				140		1980		4.65

		141		2330		4.67				141		1650		4.68				140		1980		4.65

		141		2330		4.67				141		1650		4.69				140		1980		4.66

		141		2330		4.68				141		1650		4.69				140		1980		4.66

		141		2330		4.68				141		1650		4.69				140		1980		4.66

		141		2330		4.68				141		1650		4.69				140		1980		4.66

		141		2330		4.68				141		1650		4.7				140		1980		4.67

		141		2330		4.68				141		1650		4.7				140		1980		4.67

		141		2330		4.69				141		1650		4.7				140		1970		4.67

		141		2330		4.69				141		1650		4.7				140		1970		4.67

		141		2330		4.69				141		1650		4.7				141		1970		4.67

		141		2320		4.69				141		1650		4.71				141		1970		4.68

		141		2320		4.69				142		1650		4.71				141		1970		4.68

		141		2320		4.7				142		1650		4.71				141		1970		4.68

		141		2320		4.7				142		1650		4.71				141		1970		4.68

		142		2320		4.7				142		1650		4.72				141		1970		4.68

		142		2320		4.7				142		1640		4.72				141		1970		4.69

		142		2320		4.71				142		1640		4.72				141		1970		4.69

		142		2320		4.71				142		1640		4.72				141		1970		4.69

		142		2320		4.71				142		1640		4.73				141		1970		4.69

		142		2320		4.71				142		1640		4.73				141		1960		4.7

		142		2320		4.71				142		1640		4.73				141		1960		4.7

		142		2320		4.72												141		1960		4.7

		142		2320		4.72												141		1960		4.7

		142		2310		4.72												141		1960		4.7

		142		2310		4.72												142		1960		4.71

		142		2310		4.73												142		1960		4.71

		142		2310		4.73												142		1960		4.71

		142		2310		4.73												142		1960		4.72

		142		2310		4.73												142		1960		4.72

		143		2310		4.74												142		1960		4.72

		143		2310		4.74												142		1950		4.72

		143		2310		4.74												142		1950		4.72

		143		2310		4.74												142		1950		4.73

		143		2310		4.75												142		1950		4.73

		143		2310		4.75												142		1950		4.73

		143		2300		4.75												142		1950		4.73

		143		2300		4.75												142		1950		4.74

		143		2300		4.75												142		1950		4.74

		143		2300		4.76												143		1950		4.74

		143		2300		4.76												143		1950		4.74

		143		2300		4.76												143		1940		4.74

		143		2300		4.76												143		1940		4.75

		143		2300		4.77												143		1940		4.75

		143		2300		4.77												143		1940		4.75

		144		2300		4.77												143		1940		4.75

		144		2300		4.77												143		1940		4.76

		144		2300		4.77												143		1940		4.76

		144		2300		4.78												143		1940		4.76

		144		2300		4.78												143		1940		4.76

		144		2300		4.78												143		1940		4.76

		144		2300		4.78												143		1930		4.77

		144		2290		4.79												143		1930		4.77

		144		2290		4.79												143		1930		4.77

		144		2290		4.79												144		1930		4.77

		144		2290		4.79												144		1930		4.78

		144		2290		4.79												144		1930		4.78

		144		2290		4.8												144		1930		4.78

		144		2290		4.8												144		1930		4.78

		145		2290		4.8												144		1930		4.78

		145		2290		4.8												144		1930		4.79

		145		2290		4.81												144		1930		4.79

		145		2290		4.81												144		1920		4.79

		145		2290		4.81												144		1920		4.79

		145		2280		4.81												144		1920		4.8

		145		2280		4.81												144		1920		4.8

		145		2280		4.82												144		1920		4.8

		145		2280		4.82												144		1920		4.8

		145		2280		4.82												144		1920		4.8

		145		2280		4.82												145		1920		4.81

		145		2280		4.83												145		1920		4.81

		145		2280		4.83												145		1920		4.81

		145		2280		4.83												145		1920		4.81

		145		2280		4.83												145		1910		4.82

		145		2280		4.83												145		1910		4.82

		146		2280		4.84												145		1910		4.82

		146		2280		4.84												145		1910		4.82

		146		2280		4.84												145		1910		4.82

		146		2280		4.84												145		1910		4.83

		146		2270		4.85												145		1910		4.83

		146		2270		4.85												145		1910		4.83

		146		2270		4.85												145		1910		4.83

		146		2270		4.85												145		1910		4.84

		146		2270		4.86												145		1910		4.84

		146		2270		4.86												146		1910		4.84

		146		2270		4.86												146		1900		4.84

		146		2270		4.86												146		1900		4.85

		146		2270		4.87												146		1900		4.85

		146		2270		4.87												146		1900		4.85

		147		2270		4.87												146		1900		4.85

		147		2270		4.87												146		1900		4.85

		147		2270		4.88												146		1900		4.86

		147		2270		4.88												146		1900		4.86

		147		2270		4.88												146		1900		4.86

		147		2270		4.88												146		1900		4.86

		147		2260		4.88												146		1890		4.87

		147		2260		4.89												146		1890		4.87

		147		2260		4.89												146		1890		4.87

		147		2260		4.89												147		1890		4.87

		147		2260		4.89												147		1890		4.87

		147		2260		4.9												147		1890		4.88

		147		2260		4.9												147		1890		4.88

		147		2260		4.9												147		1890		4.88

		148		2260		4.9												147		1890		4.89

		148		2260		4.9												147		1890		4.89

		148		2260		4.91												147		1890		4.89

		148		2260		4.91												147		1890		4.89

		148		2260		4.91												147		1880		4.89

		148		2260		4.91												147		1880		4.9

		148		2260		4.92												147		1880		4.9

		148		2260		4.92												147		1880		4.9

		148		2260		4.92												147		1880		4.9

		148		2260		4.92												148		1880		4.91

		148		2260		4.92												148		1880		4.91

		148		2250		4.93												148		1880		4.91

		148		2250		4.93												148		1880		4.91

		148		2250		4.93												148		1880		4.91

		148		2250		4.93												148		1880		4.92

		149		2250		4.94												148		1880		4.92

		149		2250		4.94												148		1870		4.92

		149		2250		4.94												148		1870		4.92

		149		2250		4.94												148		1870		4.93

		149		2250		4.94												148		1870		4.93

		149		2250		4.95												148		1870		4.93

		149		2250		4.95												148		1870		4.93

		149		2250		4.95												148		1870		4.93

		149		2250		4.95												148		1870		4.94

		149		2250		4.95												149		1870		4.94

		149		2250		4.96												149		1870		4.94

		149		2250		4.96												149		1870		4.94

		149		2240		4.96												149		1870		4.95

		149		2240		4.96												149		1870		4.95

		149		2240		4.97												149		1860		4.95

		150		2240		4.97												149		1860		4.95

		150		2240		4.97												149		1860		4.95

		150		2240		4.97												149		1860		4.96

		150		2240		4.98												149		1860		4.96

		150		2240		4.98												149		1860		4.96

		150		2240		4.98												149		1860		4.96

		150		2240		4.98												149		1860		4.97

		150		2240		4.99												149		1860		4.97

		150		2240		4.99												149		1860		4.97

		150		2240		4.99												149		1860		4.97

		150		2240		4.99												150		1850		4.97

		150		2240		4.99												150		1850		4.98

		150		2240		5												150		1850		4.98

		150		2240		5												150		1850		4.98

		151		2240		5												150		1850		4.99

		151		2240		5												150		1850		4.99

		151		2240		5.01												150		1850		4.99

		151		2230		5.01												150		1850		4.99

		151		2230		5.01												150		1850		4.99

		151		2230		5.01												150		1850		5

		151		2230		5.01												150		1850		5

		151		2230		5.02												150		1840		5

		151		2230		5.02												150		1840		5

		151		2230		5.02												150		1840		5

		151		2230		5.02												151		1840		5.01

		151		2230		5.03												151		1840		5.01

		151		2230		5.03												151		1840		5.01

		151		2230		5.03												151		1840		5.01

		151		2230		5.03												151		1840		5.02

		151		2230		5.03												151		1840		5.02

		152		2230		5.04												151		1840		5.02

		152		2230		5.04												151		1840		5.02

		152		2230		5.04												151		1830		5.02

		152		2230		5.04												151		1830		5.03

		152		2230		5.05												151		1830		5.03

		152		2230		5.05												151		1830		5.03

		152		2230		5.05												151		1830		5.03

		152		2220		5.05												151		1830		5.04

		152		2220		5.05												151		1830		5.04

		152		2220		5.06												152		1830		5.04

		152		2220		5.06												152		1830		5.04

		152		2220		5.06												152		1820		5.05

		152		2220		5.06												152		1820		5.05

		152		2220		5.07												152		1820		5.05

		153		2220		5.07												152		1820		5.05

		153		2220		5.07												152		1820		5.05

		153		2220		5.07												152		1820		5.06

		153		2220		5.07												152		1820		5.06

		153		2220		5.08												152		1820		5.06

		153		2220		5.08												152		1820		5.06

		153		2220		5.08												152		1820		5.07

		153		2220		5.09												152		1820		5.07

		153		2220		5.09												152		1820		5.07

		153		2220		5.09												152		1810		5.07

		153		2210		5.09												153		1810		5.07

		153		2210		5.09												153		1810		5.08

		153		2210		5.1												153		1810		5.08

		153		2210		5.1												153		1810		5.08

		153		2210		5.1												153		1810		5.09

		154		2210		5.1												153		1810		5.09

		154		2210		5.1												153		1800		5.09

		154		2210		5.11												153		1800		5.09

		154		2210		5.11												153		1800		5.09

		154		2210		5.11												153		1790		5.1

		154		2210		5.11												153		1790		5.1

		154		2210		5.11												153		1790		5.1

		154		2210		5.12												153		1790		5.1

		154		2210		5.12												153		1790		5.11

		154		2210		5.12												154		1790		5.11

		154		2210		5.12												154		1790		5.11

		154		2210		5.13												154		1790		5.11

		154		2210		5.13												154		1790		5.11

		154		2210		5.13												154		1790		5.12

		154		2210		5.13												154		1790		5.12

		155		2210		5.14												154		1780		5.12

		155		2200		5.14												154		1780		5.12

		155		2200		5.14												154		1780		5.13

		155		2200		5.14												154		1780		5.13

		155		2200		5.15												154		1780		5.13

		155		2200		5.15												154		1780		5.13

		155		2200		5.15												154		1780		5.13

		155		2200		5.15												154		1780		5.14

		155		2200		5.15												154		1780		5.14

		155		2200		5.16												155		1780		5.14

		155		2200		5.16												155		1780		5.14

		155		2200		5.16												155		1780		5.15

		155		2200		5.16												155		1780		5.15

		155		2200		5.17												155		1780		5.15

		156		2200		5.17												155		1780		5.15

		156		2200		5.17												155		1780		5.15

		156		2200		5.17												155		1770		5.16

		156		2200		5.18												155		1770		5.16

		156		2200		5.18												155		1770		5.16

		156		2200		5.18												155		1770		5.16

		156		2200		5.18												155		1770		5.17

		156		2200		5.18												155		1770		5.17

		156		2190		5.19												155		1770		5.17

		156		2190		5.19												155		1770		5.17

		156		2190		5.19												156		1770		5.18

		156		2190		5.19												156		1770		5.18

		156		2190		5.2												156		1770		5.18

		156		2190		5.2												156		1770		5.18

		156		2190		5.2												156		1770		5.18

		157		2190		5.2												156		1770		5.19

		157		2190		5.2												156		1770		5.19

		157		2190		5.21												156		1760		5.19

		157		2190		5.21												156		1760		5.19

		157		2190		5.21												156		1760		5.2

		157		2190		5.21												156		1760		5.2

		157		2190		5.22												156		1760		5.2

		157		2190		5.22												156		1760		5.2

		157		2190		5.22												156		1760		5.2

		157		2190		5.22												157		1760		5.21

		157		2190		5.23												157		1760		5.21

		157		2180		5.23												157		1760		5.21

		157		2180		5.23												157		1760		5.21

		157		2180		5.23												157		1760		5.21

		157		2180		5.23												157		1760		5.22

		158		2180		5.24												157		1760		5.22

		158		2180		5.24												157		1760		5.22

		158		2180		5.24												157		1760		5.22

		158		2180		5.24												157		1750		5.23

		158		2180		5.25												157		1750		5.23

		158		2180		5.25												157		1750		5.23

		158		2180		5.25												157		1750		5.23

		158		2180		5.25												157		1750		5.24

		158		2180		5.26												158		1750		5.24

		158		2180		5.26												158		1750		5.24

		158		2180		5.26												158		1750		5.24

		158		2180		5.26												158		1750		5.25

		158		2180		5.26												158		1750		5.25

		158		2180		5.27												158		1750		5.25

		159		2180		5.27												158		1750		5.25

		159		2180		5.27												158		1750		5.25

		159		2180		5.27												158		1750		5.26

		159		2170		5.28												158		1750		5.26

		159		2170		5.28												158		1750		5.26

		159		2170		5.28												158		1740		5.26

		159		2170		5.28												158		1740		5.27

		159		2170		5.28												158		1740		5.27

		159		2170		5.29												158		1740		5.27

		159		2170		5.29												158		1740		5.27

		159		2170		5.29												159		1740		5.28

		159		2170		5.29												159		1740		5.28

		159		2170		5.3												159		1740		5.28

		159		2170		5.3												159		1740		5.28

		160		2170		5.3												159		1740		5.28

		160		2170		5.3												159		1740		5.29

		160		2170		5.31												159		1740		5.29

		160		2170		5.31												159		1740		5.29

		160		2170		5.31												159		1740		5.29

		160		2170		5.31												159		1740		5.3

		160		2170		5.31												159		1740		5.3

		160		2160		5.32												159		1740		5.3

		160		2160		5.32												159		1740		5.3

		160		2160		5.32												159		1740		5.3

		160		2160		5.32												160		1740		5.31

		160		2160		5.33												160		1740		5.31

		160		2160		5.33												160		1740		5.31

		160		2160		5.33												160		1730		5.31

		160		2160		5.33												160		1730		5.32

		161		2160		5.33												160		1730		5.32

		161		2160		5.34												160		1730		5.32

		161		2160		5.34												160		1730		5.32

		161		2160		5.34												160		1730		5.32

		161		2160		5.34												160		1730		5.33

		161		2160		5.34												160		1730		5.33

		161		2160		5.35												160		1730		5.33

		161		2160		5.35												160		1730		5.33

		161		2160		5.35												160		1730		5.34

		161		2160		5.36												161		1730		5.34

		161		2150		5.36												161		1730		5.34

		161		2150		5.36												161		1730		5.34

		161		2150		5.36												161		1730		5.35

		161		2150		5.36												161		1730		5.35

		161		2150		5.37												161		1730		5.35

		162		2150		5.37												161		1730		5.35

		162		2150		5.37												161		1730		5.35

		162		2150		5.37												161		1720		5.36

		162		2150		5.38												161		1720		5.36

		162		2150		5.38												161		1720		5.36

		162		2150		5.38												161		1720		5.36

		162		2150		5.38												161		1720		5.37

		162		2150		5.38												161		1720		5.37

		162		2150		5.39												161		1720		5.37

		162		2150		5.39												161		1720		5.37

		162		2150		5.39												162		1720		5.37

		162		2150		5.39												162		1720		5.38

		162		2150		5.4												162		1720		5.38

		162		2140		5.4												162		1720		5.38

		163		2140		5.4												162		1720		5.38

		163		2140		5.4												162		1720		5.39

		163		2140		5.41												162		1720		5.39

		163		2140		5.41												162		1720		5.39

		163		2140		5.41												162		1720		5.39

		163		2140		5.41												162		1720		5.39

		163		2140		5.42												162		1720		5.4

		163		2140		5.42												162		1720		5.4

		163		2140		5.42												162		1720		5.4

		163		2140		5.42												162		1720		5.4

		163		2140		5.42												163		1720		5.41

		163		2140		5.43												163		1710		5.41

		163		2140		5.43												163		1710		5.41

		163		2140		5.43												163		1710		5.41

		163		2140		5.43												163		1710		5.41

		164		2140		5.44												163		1710		5.42

		164		2140		5.44												163		1710		5.42

		164		2140		5.44												163		1710		5.42

		164		2140		5.44												163		1710		5.42

		164		2130		5.44												163		1710		5.43

		164		2130		5.45												163		1710		5.43

		164		2130		5.45												163		1710		5.43

		164		2130		5.45												163		1710		5.43

		164		2130		5.45												163		1710		5.43

		164		2130		5.46												163		1710		5.44

		164		2130		5.46												164		1710		5.44

		164		2130		5.46												164		1710		5.44

		164		2130		5.46												164		1710		5.44

		164		2130		5.46												164		1710		5.45

		165		2130		5.47												164		1710		5.45

		165		2130		5.47												164		1710		5.45

		165		2130		5.47												164		1710		5.45

		165		2130		5.47												164		1700		5.45

		165		2130		5.48												164		1700		5.46

		165		2130		5.48												164		1700		5.46

		165		2130		5.48												164		1700		5.46

		165		2130		5.48												164		1700		5.46

		165		2120		5.49												164		1700		5.47

		165		2120		5.49												164		1700		5.47

		165		2120		5.49												164		1700		5.47

		165		2120		5.49												165		1700		5.47

		165		2120		5.5												165		1700		5.48

		165		2120		5.5												165		1700		5.48

		165		2120		5.5												165		1700		5.48

		166		2120		5.5												165		1700		5.48

		166		2120		5.51												165		1700		5.49

		166		2120		5.51												165		1700		5.49

		166		2120		5.51												165		1700		5.49

		166		2120		5.51												165		1700		5.49

		166		2120		5.51												165		1700		5.49

		166		2120		5.52												165		1690		5.5

		166		2120		5.52												165		1690		5.5

		166		2120		5.52												165		1690		5.5

		166		2120		5.52												165		1690		5.5

		166		2110		5.52												166		1690		5.51

		166		2110		5.53												166		1690		5.51

		166		2110		5.53												166		1690		5.51

		166		2110		5.53												166		1690		5.51

		166		2110		5.53												166		1690		5.51

		167		2110		5.54												166		1690		5.52

		167		2110		5.54												166		1690		5.52

		167		2110		5.54												166		1690		5.52

		167		2110		5.54												166		1690		5.52

		167		2110		5.55												166		1690		5.53

		167		2110		5.55												166		1690		5.53

		167		2110		5.55												166		1690		5.53

		167		2110		5.55												166		1690		5.53

		167		2110		5.55												166		1680		5.53

		167		2110		5.56												166		1680		5.54

		167		2110		5.56												167		1680		5.54

		167		2110		5.56												167		1680		5.54

		167		2110		5.56												167		1680		5.54

		167		2110		5.57												167		1680		5.55

		168		2110		5.57												167		1680		5.55

		168		2100		5.57												167		1680		5.55

		168		2100		5.57												167		1680		5.55

		168		2100		5.57												167		1680		5.56

		168		2100		5.58												167		1680		5.56

		168		2100		5.58												167		1680		5.56

		168		2100		5.58												167		1680		5.56

		168		2100		5.59												167		1680		5.57

		168		2100		5.59												167		1680		5.57

		168		2100		5.59												167		1680		5.57

		168		2100		5.59												167		1680		5.57

		168		2100		5.59												168		1670		5.57

		168		2100		5.6												168		1670		5.58

		168		2100		5.6												168		1670		5.58

		168		2100		5.6												168		1670		5.58

		169		2100		5.6												168		1670		5.58

		169		2100		5.6												168		1670		5.59

		169		2100		5.61												168		1670		5.59

		169		2100		5.61												168		1670		5.59

		169		2100		5.61												168		1670		5.59

		169		2090		5.61												168		1670		5.59

		169		2090		5.62												168		1670		5.6

		169		2090		5.62												168		1670		5.6

		169		2090		5.62												168		1670		5.6

		169		2090		5.62												168		1670		5.61

		169		2090		5.62												169		1670		5.61

		169		2090		5.63												169		1670		5.61

		169		2090		5.63												169		1670		5.61

		169		2090		5.63												169		1660		5.61

		169		2090		5.63												169		1660		5.62

		170		2090		5.64												169		1660		5.62

		170		2090		5.64												169		1660		5.62

		170		2090		5.64												169		1660		5.62

		170		2090		5.64												169		1660		5.62

		170		2090		5.65												169		1660		5.63

		170		2090		5.65												169		1660		5.63

		170		2090		5.65												169		1660		5.63

		170		2090		5.65												169		1660		5.63

		170		2090		5.65												169		1660		5.64

		170		2080		5.66												169		1660		5.64

		170		2080		5.66												170		1660		5.64

		170		2080		5.66												170		1660		5.64

		170		2080		5.66												170		1660		5.64

		170		2080		5.67												170		1660		5.65

		171		2080		5.67												170		1660		5.65

		171		2080		5.67												170		1660		5.65

		171		2080		5.67												170		1660		5.65

		171		2080		5.68												170		1650		5.66

		171		2080		5.68												170		1650		5.66

		171		2080		5.68												170		1650		5.66

		171		2080		5.68												170		1650		5.66

		171		2080		5.69												170		1650		5.67

		171		2080		5.69												170		1650		5.67

		171		2080		5.69												170		1650		5.67

		171		2080		5.69												170		1650		5.67

		171		2080		5.7												171		1650		5.67

		171		2080		5.7												171		1650		5.68

		171		2080		5.7												171		1650		5.68

		172		2080		5.7												171		1650		5.68

		172		2080		5.7												171		1650		5.68

		172		2080		5.71												171		1650		5.69

		172		2080		5.71												171		1650		5.69

		172		2080		5.71												171		1650		5.69

		172		2070		5.71												171		1650		5.69

		172		2070		5.72												171		1650		5.7

		172		2070		5.72												171		1650		5.7

		172		2070		5.72												171		1650		5.7

		172		2070		5.72												171		1640		5.7

		172		2070		5.72												171		1640		5.71

		172		2070		5.73												172		1640		5.71

		172		2070		5.73												172		1640		5.71

		172		2070		5.73												172		1640		5.71

		172		2070		5.73												172		1640		5.71

		173		2070		5.74												172		1640		5.72

		173		2070		5.74												172		1640		5.72

		173		2070		5.74												172		1640		5.72

		173		2070		5.74												172		1640		5.72

		173		2070		5.74												172		1640		5.72

		173		2070		5.75												172		1640		5.73

		173		2070		5.75												172		1640		5.73

		173		2070		5.75												172		1640		5.73

		173		2070		5.75												172		1640		5.73

		173		2070		5.76												172		1640		5.73

		173		2070		5.76												172		1640		5.74

		173		2070		5.76												172		1640		5.74

		173		2070		5.76												173		1630		5.74

		173		2060		5.76												173		1630		5.74

		173		2060		5.77												173		1630		5.74

		174		2060		5.77												173		1630		5.75

		174		2060		5.77												173		1630		5.75

		174		2060		5.77												173		1630		5.75

		174		2060		5.78												173		1630		5.75

		174		2060		5.78												173		1630		5.76

		174		2060		5.78												173		1630		5.76

		174		2060		5.78												173		1630		5.76

		174		2060		5.79												173		1630		5.76

		174		2060		5.79												173		1630		5.76

		174		2060		5.79												173		1630		5.77

		174		2060		5.79												173		1630		5.77

		174		2060		5.79												173		1630		5.77

		174		2060		5.8												174		1630		5.77

		174		2060		5.8												174		1630		5.78

		175		2060		5.8												174		1630		5.78

		175		2060		5.8												174		1630		5.78

		175		2060		5.81												174		1630		5.78

		175		2060		5.81												174		1620		5.78

		175		2050		5.81												174		1620		5.79

		175		2050		5.81												174		1620		5.79

		175		2050		5.82												174		1620		5.79

		175		2050		5.82												174		1620		5.79

		175		2050		5.82												174		1620		5.8

		175		2050		5.82

		175		2050		5.82

		175		2050		5.83

		175		2050		5.83

		175		2050		5.83

		176		2050		5.83

		176		2050		5.84

		176		2050		5.84

		176		2050		5.84

		176		2050		5.84

		176		2050		5.85

		176		2050		5.85

		176		2040		5.85

		176		2040		5.85

		176		2040		5.85

		176		2040		5.86

		176		2040		5.86

		176		2040		5.86

		176		2040		5.86

		176		2040		5.87

		177		2040		5.87





ABS 3mm PLA 10 proc

		Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)

		0.23		-5		0				0.285		0		0.001				0.266		-13.3		0				0.246		-1.67		0.001				0.278		-7.5		0

		0.324		-1.67		0.001				0.348		15.8		0.003				0.391		-10.8		0.001				0.34		12.5		0.003				0.404		-7.5		0

		0.386		13.3		0.003				0.411		35.8		0.005				0.453		4.17		0.003				0.371		34.2		0.005				0.467		-7.5		0

		0.48		32.5		0.005				0.474		55.8		0.007				0.515		23.3		0.005				0.433		53.3		0.007				0.529		2.5		0.002

		0.511		52.5		0.007				0.537		75.8		0.009				0.608		53.3		0.008				0.527		72.5		0.009				0.652		30		0.005

		0.665		90		0.011				0.633		113		0.014				0.671		71.7		0.01				0.619		103		0.013				0.715		50		0.007

		0.727		108		0.013				0.67		132		0.016				0.734		90.8		0.013				0.652		121		0.015				0.778		69.2		0.009

		0.76		127		0.016				0.762		152		0.018				0.797		108		0.015				0.745		139		0.017				0.841		86.7		0.011

		0.852		143		0.018				0.824		170		0.02				0.86		124		0.017				0.778		156		0.019				0.874		103		0.013

		0.884		157		0.02				0.916		188		0.022				0.923		139		0.019				0.871		171		0.021				0.936		120		0.015

		0.947		168		0.022				0.949		205		0.024				0.986		153		0.021				0.934		183		0.023				1.03		135		0.018

		1.01		178		0.024				1.04		222		0.027				0.994		164		0.023				0.977		196		0.025				1.09		147		0.02

		1.08		188		0.026				1.1		238		0.029				1.05		170		0.024				1.02		210		0.028				1.22		163		0.024

		1.17		203		0.03				1.23		269		0.033				1.18		190		0.028				1.1		221		0.03				1.28		172		0.026

		1.27		213		0.032				1.29		285		0.035				1.27		199		0.031				1.26		243		0.034				1.34		180		0.028

		1.33		222		0.034				1.36		298		0.037				1.33		208		0.033				1.32		253		0.036				1.41		189		0.031

		1.39		231		0.036				1.42		313		0.039				1.37		218		0.035				1.38		262		0.038				1.47		198		0.033

		1.42		239		0.038				1.48		326		0.041				1.46		227		0.037				1.41		271		0.04				1.53		207		0.035

		1.48		248		0.04				1.55		338		0.043				1.53		235		0.039				1.48		282		0.042				1.59		216		0.037

		1.58		255		0.042				1.61		349		0.046				1.59		243		0.041				1.57		291		0.044				1.66		224		0.039

		1.61		263		0.044				1.67		359		0.048				1.72		258		0.045				1.63		301		0.047				1.78		239		0.043

		1.67		270		0.046				1.8		372		0.052				1.78		265		0.048				1.69		310		0.049				1.85		246		0.045

		1.8		283		0.05				1.86		375		0.054				1.84		273		0.05				1.82		328		0.053				1.91		253		0.047

		1.89		289		0.053				1.92		378		0.056				1.9		280		0.052				1.85		337		0.055				1.97		261		0.05

		1.92		296		0.055				1.99		383		0.058				1.97		286		0.054				1.91		344		0.057				2.04		268		0.052

		2.01		302		0.057				2.05		387		0.06				2.03		291		0.056				2.01		353		0.059				2.1		275		0.054

		2.05		308		0.059				2.11		390		0.062				2.09		294		0.058				2.07		361		0.061				2.16		283		0.056

		2.11		313		0.061				2.15		395		0.064				2.16		298		0.06				2.1		368		0.063				2.22		289		0.058

		2.2		319		0.063				2.24		399		0.066				2.28		310		0.064				2.19		376		0.065				2.32		298		0.061

		2.23		324		0.065				2.37		408		0.071				2.34		317		0.067				2.22		383		0.068				2.35		305		0.063

		2.33		330		0.067				2.43		412		0.073				2.41		324		0.069				2.35		398		0.071				2.44		312		0.065

		2.45		338		0.071				2.49		415		0.075				2.47		331		0.071				2.41		404		0.074				2.51		318		0.067

		2.51		343		0.073				2.53		419		0.077				2.5		338		0.073				2.47		412		0.076				2.57		323		0.069

		2.58		348		0.076				2.59		423		0.079				2.6		343		0.075				2.57		418		0.078				2.63		329		0.071

		2.61		352		0.078				2.68		427		0.081				2.66		349		0.077				2.6		424		0.08				2.7		335		0.074

		2.7		355		0.08				2.72		431		0.083				2.72		354		0.079				2.69		431		0.082				2.76		341		0.076

		2.73		359		0.082				2.81		434		0.086				2.86		366		0.083				2.76		437		0.084				2.85		352		0.08

		2.79		362		0.084				2.94		440		0.09				2.92		370		0.086				2.79		443		0.086				2.95		357		0.082

		2.86		366		0.086				3		443		0.092				2.98		375		0.088				2.94		453		0.09				2.98		362		0.084

		3.01		373		0.09				3.03		447		0.094				3.05		379		0.09				2.97		458		0.092				3.07		366		0.086

		3.08		376		0.092				3.13		450		0.096				3.11		383		0.092				3.04		463		0.095				3.13		371		0.088

		3.11		379		0.094				3.19		453		0.098				3.17		388		0.094				3.13		468		0.097				3.2		376		0.09

		3.17		383		0.096				3.25		457		0.1				3.23		391		0.096				3.19		473		0.099				3.26		380		0.093

		3.26		386		0.098				3.31		460		0.103				3.36		398		0.1				3.25		478		0.101				3.32		384		0.095

		3.29		389		0.1				3.38		463		0.105				3.42		402		0.103				3.32		483		0.103				3.42		390		0.098

		3.36		393		0.103				3.44		467		0.107				3.49		405		0.105				3.38		487		0.105				3.45		394		0.1

		3.42		397		0.105				3.5		470		0.109				3.52		408		0.107				3.44		493		0.108				3.54		398		0.102

		3.54		402		0.108				3.57		473		0.111				3.61		412		0.109				3.5		497		0.11				3.61		403		0.104

		3.57		405		0.11				3.63		477		0.113				3.68		415		0.111				3.57		501		0.112				3.67		406		0.106

		3.67		408		0.112				3.69		480		0.115				3.74		418		0.113				3.63		505		0.114				3.73		410		0.108

		3.7		411		0.114				3.73		483		0.117				3.8		423		0.115				3.69		508		0.116				3.79		414		0.11

		3.76		415		0.116				3.79		488		0.119				3.9		429		0.119				3.75		513		0.118				3.86		418		0.112

		3.86		418		0.118				3.88		491		0.121				3.99		433		0.122				3.85		516		0.12				3.98		426		0.117

		3.92		421		0.12				4.01		498		0.126				4.05		436		0.123				3.88		519		0.122				4.05		430		0.119

		3.95		424		0.122				4.04		502		0.128				4.12		439		0.125				3.94		523		0.125				4.11		434		0.121

		4.04		428		0.124				4.14		505		0.13				4.18		443		0.128				4.07		528		0.128				4.17		438		0.123

		4.17		434		0.128				4.2		509		0.132				4.21		446		0.13				4.13		532		0.13				4.24		441		0.125

		4.2		438		0.131				4.23		513		0.134				4.3		449		0.132				4.16		535		0.132				4.3		445		0.127

		4.26		441		0.133				4.3		516		0.136				4.37		453		0.134				4.25		538		0.134				4.36		449		0.129

		4.35		443		0.135				4.39		519		0.138				4.46		461		0.138				4.28		542		0.136				4.43		453		0.131

		4.39		448		0.137				4.52		527		0.143				4.53		464		0.14				4.35		546		0.138				4.55		461		0.136

		4.45		451		0.139				4.55		531		0.145				4.62		468		0.142				4.41		549		0.14				4.61		464		0.138

		4.54		454		0.141				4.64		534		0.147				4.68		471		0.144				4.5		553		0.142				4.65		468		0.14

		4.57		458		0.143				4.71		538		0.149				4.74		475		0.147				4.6		559		0.147				4.74		473		0.142

		4.73		464		0.147				4.77		541		0.151				4.81		478		0.149				4.66		563		0.149				4.8		476		0.144

		4.79		468		0.149				4.83		544		0.153				4.87		482		0.151				4.75		566		0.151				4.87		480		0.146

		4.82		472		0.151				4.89		548		0.155				4.93		485		0.153				4.81		570		0.153				4.93		484		0.148

		4.88		475		0.154				4.96		554		0.158				5.06		492		0.157				4.85		573		0.155				5.06		492		0.152

		4.95		478		0.156				5.02		558		0.161				5.12		495		0.159				4.91		577		0.157				5.09		496		0.154

		5.01		483		0.158				5.08		561		0.162				5.19		499		0.161				4.97		580		0.159				5.18		499		0.157

		5.1		486		0.16				5.18		564		0.164				5.25		502		0.164				5.06		584		0.161				5.25		503		0.159

		5.13		489		0.162				5.21		568		0.167				5.31		505		0.166				5.13		589		0.164				5.31		507		0.161

		5.26		496		0.166				5.27		573		0.169				5.38		508		0.167				5.19		593		0.166				5.37		511		0.163

		5.35		499		0.168				5.34		576		0.171				5.44		512		0.17				5.28		597		0.168				5.44		515		0.165

		5.42		503		0.17				5.43		579		0.173				5.5		515		0.172				5.31		600		0.17				5.56		524		0.169

		5.45		507		0.172				5.56		586		0.177				5.6		520		0.175				5.41		604		0.172				5.63		528		0.171

		5.51		510		0.174				5.62		590		0.179				5.67		523		0.177				5.44		608		0.175				5.69		533		0.174

		5.57		513		0.176				5.68		594		0.181				5.73		527		0.179				5.5		612		0.177				5.75		536		0.176

		5.66		518		0.178				5.75		598		0.184				5.79		530		0.181				5.59		616		0.179				5.82		540		0.178

		5.7		521		0.181				5.81		601		0.186				5.82		533		0.184				5.69		622		0.182				5.88		544		0.18

		5.82		528		0.185				5.87		605		0.188				5.89		537		0.186				5.72		625		0.184				5.94		548		0.182

		5.91		531		0.187				5.94		608		0.19				5.98		539		0.188				5.81		628		0.186				6.04		557		0.186

		5.95		534		0.189				6.03		613		0.193				6.04		543		0.19				5.88		633		0.188				6.13		560		0.188

		6.01		538		0.191				6.09		618		0.195				6.14		548		0.193				5.94		637		0.19				6.19		564		0.19

		6.07		541		0.193				6.16		621		0.197				6.2		551		0.195				6		641		0.192				6.26		568		0.193

		6.13		545		0.195				6.22		624		0.199				6.23		554		0.197				6.06		644		0.194				6.29		573		0.194

		6.2		548		0.197				6.28		628		0.201				6.29		558		0.199				6.12		648		0.197				6.38		577		0.197

		6.29		552		0.199				6.35		631		0.203				6.35		562		0.201				6.25		655		0.201				6.45		581		0.199

		6.32		555		0.201				6.41		635		0.206				6.45		565		0.203				6.28		659		0.203				6.48		585		0.201

		6.48		562		0.206				6.47		639		0.208				6.48		568		0.206				6.37		663		0.205				6.57		588		0.203

		6.51		566		0.208				6.6		647		0.212				6.54		571		0.207				6.41		667		0.207				6.7		597		0.207

		6.57		569		0.209				6.66		650		0.214				6.6		575		0.209				6.5		670		0.209				6.76		602		0.209

		6.66		573		0.212				6.72		653		0.216				6.73		581		0.214				6.53		674		0.211				6.83		606		0.211

		6.73		576		0.214				6.79		657		0.218				6.79		585		0.216				6.62		678		0.213				6.89		609		0.213

		6.76		579		0.216				6.85		661		0.22				6.85		588		0.218				6.69		682		0.215				6.95		613		0.216

		6.85		583		0.218				6.91		664		0.222				6.92		591		0.22				6.75		686		0.217				6.99		618		0.218

		6.88		587		0.22				6.98		668		0.225				6.98		594		0.222				6.78		689		0.219				7.08		622		0.22

		7.01		592		0.223				7.04		672		0.227				7.04		598		0.224				6.87		693		0.221				7.21		630		0.224

		7.04		595		0.225				7.17		678		0.231				7.13		601		0.226				6.94		697		0.223				7.24		633		0.226

		7.13		598		0.227				7.23		683		0.233				7.16		604		0.228				7		701		0.226				7.33		638		0.228

		7.19		602		0.229				7.29		686		0.235				7.29		610		0.233				7.03		704		0.228				7.4		642		0.23

		7.22		605		0.232				7.36		689		0.237				7.35		613		0.235				7.12		708		0.23				7.46		647		0.232

		7.29		609		0.234				7.42		693		0.239				7.41		617		0.237				7.19		713		0.232				7.52		651		0.234

		7.38		612		0.236				7.48		696		0.241				7.48		621		0.239				7.25		716		0.234				7.59		656		0.237

		7.41		615		0.238				7.55		699		0.243				7.54		624		0.241				7.31		719		0.236				7.71		665		0.241

		7.47		619		0.24				7.64		705		0.247				7.6		627		0.243				7.4		725		0.239				7.78		670		0.243

		7.6		626		0.244				7.7		708		0.249				7.7		630		0.245				7.47		729		0.241				7.84		676		0.245

		7.69		630		0.246				7.73		713		0.251				7.76		633		0.247				7.53		733		0.243				7.9		682		0.247

		7.72		633		0.248				7.83		716		0.253				7.82		639		0.25				7.56		737		0.245				7.93		688		0.249

		7.79		637		0.25				7.89		719		0.255				7.88		643		0.252				7.65		741		0.247				8.03		693		0.251

		7.85		640		0.252				7.95		723		0.257				7.98		646		0.254				7.72		745		0.249				8.09		702		0.253

		7.94		644		0.254				8.02		727		0.259				8.01		649		0.256				7.78		749		0.251				8.22		721		0.258

		8		648		0.256				8.08		731		0.261				8.07		653		0.258				7.81		753		0.254				8.28		731		0.26

		8.04		652		0.258				8.21		739		0.265				8.13		657		0.26				7.87		758		0.256				8.34		742		0.262

		8.1		656		0.261				8.27		743		0.267				8.19		661		0.263				8.03		765		0.26				8.41		752		0.264

		8.19		662		0.264				8.33		748		0.269				8.26		665		0.265				8.09		770		0.262				8.44		762		0.266

		8.25		666		0.266				8.39		753		0.272				8.32		670		0.267				8.15		774		0.264				8.5		773		0.268

		8.32		671		0.268				8.46		758		0.274				8.48		683		0.271				8.22		778		0.266				8.6		783		0.27

		8.41		675		0.27				8.52		764		0.276				8.54		692		0.273				8.28		783		0.268				8.66		794		0.272

		8.47		681		0.272				8.58		771		0.278				8.6		702		0.275				8.34		788		0.27				8.72		805		0.274

		8.5		686		0.274				8.65		780		0.28				8.63		711		0.277				8.37		793		0.272				8.79		815		0.277

		8.6		693		0.276				8.77		800		0.284				8.72		723		0.279				8.46		798		0.274				8.85		825		0.279

		8.63		701		0.278				8.83		810		0.286				8.79		732		0.281				8.56		806		0.277				8.91		836		0.281

		8.72		709		0.28				8.9		821		0.288				8.85		743		0.284				8.59		814		0.279				8.98		846		0.283

		8.82		723		0.284				8.96		832		0.291				8.88		753		0.285				8.65		823		0.282				9.04		856		0.285

		8.85		733		0.286				9.02		842		0.293				8.94		763		0.287				8.75		833		0.284				9.07		866		0.287

		8.94		743		0.288				9.08		852		0.295				9.07		782		0.292				8.78		843		0.286				9.16		875		0.289

		9		754		0.29				9.15		862		0.297				9.13		792		0.294				8.87		853		0.288				9.29		893		0.294

		9.03		765		0.292				9.21		872		0.299				9.19		801		0.296				8.9		862		0.29				9.35		903		0.296

		9.1		776		0.294				9.33		892		0.303				9.29		809		0.298				8.96		871		0.292				9.39		912		0.298

		9.16		786		0.296				9.39		901		0.305				9.32		818		0.3				9.03		880		0.294				9.48		921		0.3

		9.25		797		0.298				9.46		910		0.307				9.38		827		0.302				9.18		898		0.298				9.54		928		0.302

		9.32		808		0.3				9.52		919		0.309				9.47		836		0.304				9.24		907		0.3				9.61		937		0.304

		9.35		817		0.302				9.58		928		0.311				9.54		843		0.306				9.28		915		0.302				9.64		944		0.306

		9.41		827		0.304				9.64		938		0.314				9.63		855		0.309				9.34		923		0.305				9.73		952		0.308

		9.5		837		0.306				9.7		946		0.315				9.66		863		0.312				9.43		930		0.307				9.86		967		0.313

		9.54		847		0.308				9.77		954		0.317				9.72		871		0.314				9.49		938		0.309				9.92		973		0.315

		9.6		856		0.31				9.89		972		0.322				9.82		879		0.316				9.53		944		0.311				9.98		982		0.317

		9.66		865		0.313				9.95		980		0.324				9.88		886		0.318				9.62		951		0.313				10		988		0.319

		9.75		874		0.315				10		988		0.326				9.91		893		0.32				9.71		961		0.316				10.1		996		0.321

		9.78		883		0.317				10		997		0.328				9.97		900		0.322				9.74		968		0.318				10.2		1000		0.323

		9.91		901		0.321				10.1		1000		0.33				10		907		0.324				9.84		974		0.32				10.2		1010		0.325

		10		909		0.323				10.2		1010		0.332				10.1		914		0.326				9.9		981		0.322				10.3		1020		0.327

		10		918		0.325				10.2		1020		0.334				10.2		928		0.33				9.93		987		0.324				10.4		1030		0.331

		10.1		926		0.327				10.3		1030		0.336				10.3		935		0.332				9.99		993		0.326				10.5		1040		0.333

		10.2		934		0.329				10.4		1040		0.338				10.4		942		0.334				10.1		999		0.328				10.5		1050		0.336

		10.3		943		0.331				10.5		1050		0.341				10.4		948		0.336				10.1		1010		0.33				10.6		1060		0.338

		10.3		950		0.333				10.5		1050		0.343				10.5		956		0.338				10.2		1020		0.334				10.7		1060		0.34

		10.4		958		0.336				10.6		1060		0.346				10.5		963		0.341				10.3		1020		0.336				10.8		1070		0.342

		10.5		973		0.339				10.7		1070		0.348				10.6		969		0.343				10.3		1030		0.338				10.8		1080		0.344

		10.6		981		0.342				10.7		1080		0.35				10.7		977		0.345				10.4		1030		0.34				10.9		1080		0.346

		10.6		988		0.344				10.8		1080		0.352				10.8		990		0.349				10.5		1040		0.342				10.9		1090		0.349

		10.7		996		0.346				10.8		1090		0.354				10.8		996		0.351				10.6		1050		0.344				11		1100		0.351

		10.8		1000		0.348				10.9		1100		0.356				10.9		1000		0.353				10.6		1050		0.346				11		1100		0.353

		10.8		1010		0.35				11		1110		0.359				11		1010		0.355				10.7		1060		0.348				11.1		1110		0.355

		10.9		1020		0.352				11		1110		0.361				11.1		1020		0.357				10.8		1070		0.352				11.2		1120		0.357

		10.9		1020		0.354				11.1		1120		0.363				11.1		1020		0.359				10.9		1070		0.355				11.2		1120		0.359

		11		1030		0.357				11.2		1130		0.365				11.2		1030		0.362				10.9		1080		0.357				11.3		1130		0.361

		11.1		1040		0.359				11.3		1140		0.367				11.3		1030		0.364				11		1090		0.359				11.3		1140		0.363

		11.1		1050		0.362				11.3		1140		0.369				11.3		1040		0.366				11		1090		0.36				11.4		1140		0.365

		11.2		1050		0.364				11.4		1150		0.371				11.4		1050		0.369				11.1		1100		0.363				11.5		1150		0.367

		11.2		1060		0.366				11.4		1160		0.373				11.5		1060		0.371				11.2		1100		0.365				11.5		1150		0.369

		11.3		1070		0.368				11.6		1170		0.378				11.5		1060		0.373				11.2		1110		0.367				11.6		1160		0.371

		11.4		1070		0.37				11.6		1180		0.38				11.6		1070		0.375				11.3		1120		0.37				11.7		1170		0.373

		11.4		1080		0.372				11.7		1180		0.382				11.6		1070		0.377				11.4		1120		0.372				11.7		1170		0.375

		11.5		1080		0.374				11.8		1190		0.384				11.7		1080		0.379				11.5		1130		0.374				11.8		1180		0.378

		11.6		1100		0.378				11.8		1190		0.386				11.8		1090		0.381				11.5		1140		0.376				11.8		1190		0.38

		11.7		1100		0.38				11.9		1200		0.388				11.8		1090		0.383				11.6		1140		0.378				11.9		1190		0.382

		11.7		1110		0.382				11.9		1210		0.39				11.9		1100		0.386				11.6		1150		0.38				12		1200		0.384

		11.8		1110		0.384				12		1210		0.392				12		1110		0.388				11.7		1150		0.382				12.1		1210		0.387

		11.9		1120		0.386				12.1		1230		0.396				12		1110		0.391				11.8		1160		0.385				12.1		1210		0.389

		11.9		1130		0.388				12.2		1230		0.398				12.1		1120		0.393				11.9		1170		0.389				12.2		1220		0.391

		12		1130		0.391				12.2		1240		0.4				12.2		1120		0.395				11.9		1170		0.391				12.2		1220		0.393

		12.1		1140		0.393				12.3		1250		0.402				12.3		1130		0.397				12		1180		0.393				12.3		1230		0.395

		12.1		1140		0.395				12.3		1250		0.404				12.3		1130		0.399				12.1		1190		0.395				12.4		1240		0.397

		12.2		1150		0.397				12.4		1260		0.407				12.3		1140		0.401				12.1		1190		0.397				12.5		1240		0.4

		12.3		1150		0.399				12.5		1260		0.409				12.4		1150		0.403				12.2		1200		0.399				12.5		1250		0.402

		12.3		1160		0.401				12.6		1270		0.411				12.5		1160		0.407				12.3		1200		0.401				12.6		1250		0.403

		12.4		1170		0.403				12.7		1280		0.415				12.6		1160		0.409				12.3		1210		0.403				12.7		1260		0.408

		12.4		1170		0.405				12.7		1290		0.417				12.7		1170		0.411				12.5		1220		0.407				12.8		1270		0.41

		12.5		1180		0.407				12.8		1290		0.419				12.7		1170		0.413				12.5		1220		0.409				12.8		1270		0.412

		12.6		1180		0.409				12.9		1300		0.421				12.8		1180		0.415				12.6		1230		0.412				12.9		1280		0.414

		12.7		1190		0.411				12.9		1310		0.423				12.9		1180		0.417				12.6		1240		0.414				12.9		1290		0.416

		12.8		1200		0.416				13		1310		0.425				12.9		1190		0.42				12.7		1240		0.416				13		1290		0.418

		12.8		1200		0.418				13.1		1320		0.427				13		1200		0.422				12.8		1250		0.418				13.1		1300		0.42

		12.9		1210		0.42				13.1		1330		0.43				13		1200		0.424				12.8		1250		0.42				13.1		1300		0.422

		13		1220		0.422				13.3		1340		0.434				13.2		1210		0.428				12.9		1260		0.422				13.3		1310		0.426

		13		1220		0.424				13.3		1340		0.436				13.2		1220		0.43				13		1270		0.425				13.3		1320		0.429

		13.1		1230		0.426				13.4		1350		0.438				13.3		1220		0.432				13.1		1270		0.427				13.4		1330		0.431

		13.2		1230		0.428				13.4		1360		0.44				13.4		1230		0.434				13.1		1280		0.429				13.4		1330		0.433

		13.2		1240		0.43				13.5		1360		0.442				13.4		1230		0.436				13.2		1280		0.431				13.5		1340		0.435

		13.3		1250		0.433				13.6		1370		0.444				13.5		1240		0.438				13.2		1290		0.434				13.6		1340		0.437

		13.4		1250		0.435				13.6		1370		0.446				13.6		1240		0.441				13.3		1290		0.436				13.7		1350		0.439

		13.4		1260		0.437				13.7		1380		0.448				13.6		1250		0.443				13.4		1300		0.437				13.7		1360		0.441

		13.5		1260		0.439				13.8		1390		0.452				13.7		1250		0.445				13.4		1300		0.44				13.8		1360		0.443

		13.6		1270		0.442				13.9		1400		0.455				13.8		1260		0.449				13.6		1320		0.444				13.8		1370		0.446

		13.6		1270		0.444				13.9		1400		0.457				13.9		1270		0.451				13.6		1320		0.446				13.9		1370		0.448

		13.7		1280		0.446				14		1410		0.459				13.9		1270		0.453				13.6		1330		0.448				14		1380		0.451

		13.7		1280		0.448				14.1		1410		0.461				14		1280		0.455				13.7		1330		0.45				14		1390		0.452

		13.8		1290		0.45				14.1		1420		0.463				14		1290		0.457				13.8		1340		0.452				14.1		1390		0.454

		13.9		1300		0.454				14.2		1420		0.465				14.1		1290		0.459				13.8		1340		0.454				14.2		1400		0.457

		14		1300		0.456				14.2		1430		0.467				14.2		1300		0.461				13.9		1350		0.456				14.2		1400		0.459

		14.1		1310		0.458				14.3		1440		0.469				14.2		1300		0.463				14		1360		0.458				14.3		1410		0.461

		14.1		1310		0.46				14.4		1450		0.473				14.3		1310		0.467				14.1		1370		0.463				14.4		1420		0.464

		14.2		1320		0.462				14.5		1450		0.476				14.4		1320		0.47				14.2		1370		0.465				14.5		1420		0.466

		14.2		1320		0.464				14.6		1460		0.478				14.5		1320		0.472				14.2		1380		0.467				14.5		1430		0.468

		14.3		1330		0.466				14.6		1460		0.48				14.5		1330		0.474				14.3		1380		0.469				14.6		1430		0.47

		14.3		1330		0.468				14.7		1470		0.482				14.6		1330		0.476				14.3		1390		0.471				14.7		1440		0.472

		14.4		1340		0.471				14.8		1480		0.484				14.7		1340		0.478				14.4		1400		0.473				14.7		1450		0.474

		14.5		1350		0.474				14.8		1480		0.486				14.7		1350		0.48				14.5		1400		0.475				14.7		1450		0.476

		14.6		1350		0.476				14.9		1490		0.488				14.8		1350		0.482				14.5		1410		0.477				14.8		1460		0.479

		14.6		1360		0.478				15		1500		0.492				14.9		1360		0.486				14.6		1410		0.479				14.9		1460		0.481

		14.7		1360		0.48				15.1		1500		0.494				15		1370		0.488				14.7		1420		0.484				15		1470		0.483

		14.7		1370		0.482				15.1		1510		0.496				15		1370		0.49				14.8		1430		0.486				15.1		1470		0.486

		14.8		1370		0.484				15.2		1520		0.498				15.1		1380		0.492				14.9		1430		0.487				15.1		1480		0.488

		14.9		1380		0.486				15.3		1520		0.501				15.2		1380		0.494				14.9		1440		0.49				15.2		1480		0.49

		14.9		1390		0.488				15.3		1530		0.503				15.2		1390		0.497				15		1450		0.492				15.2		1490		0.492

		15		1390		0.49				15.4		1530		0.505				15.3		1390		0.499				15		1450		0.494				15.3		1490		0.494

		15.1		1400		0.495				15.4		1530		0.507				15.4		1400		0.501				15.1		1460		0.496				15.4		1500		0.496

		15.2		1410		0.497				15.6		1540		0.511				15.5		1410		0.505				15.1		1460		0.498				15.4		1510		0.498

		15.2		1410		0.499				15.6		1550		0.513				15.6		1410		0.507				15.2		1470		0.501				15.5		1510		0.5

		15.3		1420		0.501				15.7		1550		0.515				15.6		1420		0.509				15.3		1480		0.503				15.6		1520		0.503

		15.4		1420		0.503				15.7		1560		0.517				15.7		1420		0.511				15.4		1480		0.505				15.6		1520		0.505

		15.5		1430		0.505				15.8		1570		0.519				15.7		1430		0.513				15.5		1490		0.507				15.7		1530		0.508

		15.5		1430		0.507				15.9		1570		0.521				15.8		1430		0.515				15.5		1490		0.509				15.7		1530		0.51

		15.6		1440		0.509				15.9		1580		0.523				15.9		1440		0.517				15.5		1500		0.512				15.8		1540		0.512

		15.7		1450		0.513				16		1580		0.525				15.9		1440		0.52				15.6		1510		0.514				15.9		1550		0.514

		15.7		1450		0.515				16.1		1590		0.529				16		1450		0.522				15.7		1510		0.516				16		1550		0.516

		15.8		1460		0.517				16.2		1590		0.531				16.1		1460		0.526				15.8		1520		0.52				16		1560		0.518

		15.9		1460		0.52				16.2		1600		0.533				16.2		1460		0.528				15.9		1530		0.522				16.1		1560		0.52

		15.9		1470		0.522				16.3		1600		0.535				16.2		1470		0.53				16		1530		0.524				16.2		1570		0.524

		16		1470		0.524				16.4		1610		0.537				16.3		1470		0.532				16		1540		0.526				16.3		1580		0.526

		16.1		1480		0.526				16.4		1620		0.539				16.3		1480		0.534				16.1		1540		0.528				16.3		1580		0.529

		16.1		1480		0.528				16.5		1620		0.541				16.4		1480		0.536				16.1		1550		0.53				16.4		1590		0.53

		16.3		1490		0.532				16.5		1630		0.543				16.5		1490		0.538				16.2		1560		0.532				16.4		1590		0.532

		16.3		1500		0.534				16.7		1640		0.548				16.6		1500		0.54				16.3		1560		0.534				16.5		1600		0.534

		16.4		1500		0.536				16.7		1640		0.55				16.6		1500		0.543				16.3		1570		0.537				16.6		1600		0.537

		16.4		1510		0.538				16.8		1650		0.552				16.7		1510		0.545				16.4		1570		0.539				16.6		1610		0.539

		16.5		1510		0.54				16.8		1650		0.554				16.7		1510		0.548				16.5		1580		0.542				16.7		1610		0.541

		16.6		1520		0.542				16.9		1660		0.556				16.8		1520		0.55				16.5		1590		0.544				16.7		1620		0.543

		16.6		1520		0.544				17		1660		0.558				16.9		1520		0.552				16.6		1590		0.546				16.8		1620		0.545

		16.7		1530		0.546				17		1670		0.56				16.9		1530		0.554				16.7		1600		0.548				16.9		1630		0.547

		16.7		1530		0.549				17.1		1670		0.562				17		1530		0.556				16.7		1600		0.55				16.9		1630		0.549

		16.9		1540		0.552				17.2		1690		0.567				17.1		1540		0.558				16.8		1610		0.552				17		1640		0.551

		16.9		1540		0.554				17.3		1690		0.569				17.2		1550		0.562				16.8		1610		0.554				17.1		1640		0.553

		17		1550		0.556				17.4		1700		0.571				17.3		1550		0.564				17		1620		0.558				17.1		1650		0.555

		17		1550		0.558				17.4		1700		0.573				17.3		1560		0.566				17		1630		0.56				17.2		1650		0.558

		17.1		1560		0.56				17.5		1710		0.575				17.4		1560		0.568				17.1		1640		0.563				17.3		1660		0.562

		17.2		1560		0.562				17.6		1710		0.577				17.5		1570		0.57				17.1		1640		0.564				17.4		1670		0.564

		17.2		1570		0.564				17.6		1720		0.579				17.5		1570		0.572				17.2		1650		0.566				17.4		1670		0.566

		17.3		1570		0.566				17.7		1720		0.581				17.6		1580		0.574				17.3		1650		0.569				17.5		1680		0.568

		17.4		1580		0.57				17.8		1730		0.585				17.6		1580		0.577				17.4		1660		0.571				17.6		1680		0.57

		17.5		1590		0.572				17.9		1740		0.588				17.7		1590		0.581				17.4		1660		0.573				17.6		1690		0.572

		17.5		1590		0.574				17.9		1740		0.59				17.8		1600		0.583				17.5		1670		0.577				17.7		1690		0.574

		17.6		1600		0.576				18		1750		0.592				17.9		1600		0.585				17.6		1680		0.579				17.7		1700		0.576

		17.6		1600		0.578				18.1		1750		0.594				17.9		1610		0.587				17.6		1680		0.581				17.9		1710		0.58

		17.7		1610		0.58				18.1		1760		0.596				18		1610		0.589				17.7		1690		0.583				18		1710		0.582

		17.7		1610		0.582				18.2		1760		0.598				18.1		1620		0.591				17.8		1690		0.585				18		1720		0.584

		17.8		1620		0.584				18.3		1770		0.602				18.1		1620		0.593				17.9		1700		0.587				18.1		1730		0.587

		17.9		1620		0.587				18.4		1780		0.605				18.2		1630		0.595				17.9		1700		0.589				18.1		1730		0.589

		18		1630		0.589				18.4		1780		0.606				18.3		1630		0.599				17.9		1700		0.592				18.2		1740		0.591

		18		1630		0.591				18.5		1790		0.608				18.4		1640		0.601				18.1		1710		0.596				18.3		1740		0.593

		18.1		1640		0.593				18.6		1790		0.611				18.4		1640		0.603				18.2		1720		0.598				18.3		1750		0.595

		18.2		1640		0.595				18.6		1800		0.613				18.5		1650		0.605				18.2		1720		0.6				18.4		1760		0.599

		18.2		1650		0.597				18.7		1800		0.615				18.5		1650		0.607				18.3		1730		0.602				18.5		1760		0.601

		18.3		1650		0.6				18.8		1810		0.619				18.6		1660		0.609				18.4		1730		0.604				18.6		1770		0.603

		18.3		1660		0.602				18.9		1820		0.621				18.6		1660		0.611				18.4		1740		0.606				18.6		1770		0.605

		18.4		1660		0.604				18.9		1820		0.623				18.7		1670		0.613				18.4		1740		0.608				18.7		1770		0.608

		18.6		1670		0.608				19		1830		0.625				18.8		1670		0.615				18.5		1750		0.61				18.8		1780		0.609

		18.6		1680		0.61				19		1830		0.628				18.9		1680		0.619				18.7		1760		0.614				18.8		1780		0.611

		18.7		1680		0.612				19.1		1840		0.63				19		1690		0.621				18.7		1760		0.616				18.9		1790		0.613

		18.7		1690		0.614				19.2		1840		0.632				19		1690		0.623				18.8		1770		0.619				18.9		1790		0.616

		18.8		1690		0.616				19.3		1850		0.636				19.1		1700		0.626				18.8		1770		0.621				19.1		1800		0.62

		18.8		1700		0.618				19.4		1860		0.638				19.1		1700		0.628				18.9		1780		0.623				19.1		1810		0.622

		18.9		1700		0.621				19.4		1860		0.64				19.2		1710		0.63				19		1790		0.625				19.2		1810		0.624

		19		1710		0.623				19.5		1870		0.642				19.3		1710		0.632				19		1790		0.627				19.2		1820		0.626

		19		1710		0.625				19.6		1870		0.645				19.3		1710		0.634				19.1		1800		0.629				19.3		1820		0.628

		19.1		1720		0.627				19.6		1880		0.646				19.5		1720		0.638				19.2		1800		0.632				19.4		1830		0.63

		19.2		1720		0.629				19.7		1880		0.648				19.6		1730		0.64				19.3		1810		0.634				19.4		1830		0.632

		19.2		1730		0.631				19.8		1890		0.652				19.6		1730		0.642				19.3		1810		0.636				19.5		1840		0.634

		19.3		1730		0.633				19.8		1900		0.654				19.6		1740		0.644				19.4		1820		0.638				19.6		1850		0.638

		19.3		1740		0.635				19.9		1900		0.656				19.7		1740		0.646				19.4		1820		0.641				19.7		1850		0.64

		19.4		1740		0.637				20		1910		0.658				19.8		1750		0.649				19.5		1830		0.643				19.7		1860		0.642

		19.5		1750		0.639				20		1910		0.66				19.8		1750		0.65				19.6		1830		0.644				19.8		1860		0.644

		19.5		1750		0.641				20.1		1920		0.662				19.9		1760		0.652				19.6		1840		0.647				19.8		1870		0.646

		19.6		1760		0.644				20.2		1920		0.664				20.1		1770		0.657				19.8		1850		0.651				19.9		1870		0.648

		19.7		1760		0.646				20.2		1930		0.666				20.1		1770		0.659				19.8		1850		0.653				20		1870		0.65

		19.8		1770		0.648				20.3		1930		0.669				20.1		1780		0.661				19.9		1860		0.655				20		1880		0.652

		19.8		1770		0.651				20.3		1940		0.671				20.2		1780		0.663				19.9		1860		0.657				20.1		1880		0.654

		19.9		1780		0.653				20.4		1940		0.673				20.3		1780		0.665				20		1870		0.659				20.2		1890		0.657

		19.9		1780		0.655				20.5		1950		0.675				20.3		1790		0.667				20.1		1870		0.661				20.3		1900		0.659

		20		1780		0.657				20.5		1950		0.677				20.4		1790		0.669				20.1		1880		0.663				20.3		1900		0.661

		20		1790		0.659				20.6		1960		0.679				20.5		1800		0.671				20.2		1880		0.665				20.4		1910		0.663

		20.1		1790		0.661				20.6		1960		0.681				20.5		1800		0.674				20.3		1890		0.668				20.4		1910		0.666

		20.2		1800		0.664				20.7		1970		0.683				20.6		1810		0.675				20.3		1900		0.671				20.5		1920		0.668

		20.3		1800		0.666				20.8		1970		0.685				20.7		1810		0.678				20.4		1900		0.673				20.5		1920		0.67

		20.3		1810		0.668				20.9		1980		0.689				20.7		1820		0.68				20.5		1910		0.675				20.6		1920		0.672

		20.4		1810		0.67				21		1980		0.692				20.8		1820		0.682				20.5		1910		0.677				20.7		1930		0.674

		20.5		1820		0.673				21.1		1990		0.694				20.8		1830		0.684				20.6		1920		0.679				20.8		1940		0.677

		20.5		1820		0.675				21.1		1990		0.696				20.9		1830		0.687				20.6		1920		0.681				20.9		1940		0.679

		20.6		1830		0.677				21.2		2000		0.698				21		1840		0.689				20.7		1930		0.683				20.9		1950		0.681

		20.6		1830		0.679				21.3		2000		0.7				21		1840		0.69				20.8		1930		0.686				21		1950		0.683

		20.7		1840		0.681				21.3		2010		0.703				21.1		1850		0.694				20.9		1940		0.688				21		1960		0.685

		20.8		1840		0.684				21.4		2020		0.707				21.2		1850		0.696				20.9		1940		0.691				21.1		1960		0.688

		20.9		1850		0.686				21.5		2020		0.709				21.3		1860		0.698				21		1950		0.692				21.2		1960		0.689

		20.9		1850		0.688				21.6		2030		0.711				21.3		1860		0.7				21.1		1960		0.694				21.2		1970		0.692

		21		1860		0.69				21.6		2030		0.713				21.4		1860		0.702				21.1		1960		0.696				21.3		1980		0.696

		21.1		1860		0.692				21.7		2030		0.715				21.5		1870		0.704				21.2		1970		0.699				21.4		1980		0.698

		21.1		1860		0.694				21.7		2040		0.717				21.5		1870		0.706				21.3		1970		0.701				21.5		1990		0.7

		21.2		1870		0.697				21.8		2040		0.719				21.6		1880		0.708				21.4		1980		0.704				21.5		1990		0.702

		21.3		1870		0.699				21.9		2050		0.721				21.6		1880		0.71				21.4		1980		0.706				21.6		2000		0.704

		21.4		1880		0.702				22		2060		0.725				21.8		1890		0.714				21.5		1990		0.708				21.6		2000		0.706

		21.4		1880		0.704				22.1		2060		0.727				21.8		1900		0.717				21.5		1990		0.71				21.7		2010		0.708

		21.5		1890		0.706				22.1		2070		0.729				21.9		1900		0.719				21.6		2000		0.712				21.8		2010		0.71

		21.6		1890		0.708				22.2		2070		0.732				21.9		1900		0.721				21.7		2000		0.714				21.9		2020		0.715

		21.6		1900		0.71				22.2		2080		0.734				22		1910		0.723				21.7		2010		0.716				22		2030		0.717

		21.6		1900		0.712				22.3		2080		0.736				22.1		1910		0.725				21.8		2010		0.718				22		2030		0.719

		21.7		1900		0.714				22.4		2080		0.738				22.1		1920		0.727				21.9		2020		0.722				22.1		2030		0.721

		21.8		1910		0.716				22.4		2090		0.74				22.2		1920		0.729				21.9		2020		0.724				22.1		2040		0.723

		21.9		1910		0.718				22.5		2100		0.743				22.3		1930		0.732				22		2030		0.726				22.2		2040		0.725

		22		1920		0.722				22.6		2100		0.745				22.3		1930		0.734				22.1		2030		0.728				22.3		2050		0.727

		22		1930		0.725				22.6		2100		0.747				22.4		1940		0.737				22.1		2040		0.73				22.3		2050		0.729

		22.1		1930		0.727				22.7		2110		0.749				22.5		1940		0.738				22.2		2040		0.732				22.4		2060		0.731

		22.2		1930		0.729				22.8		2110		0.751				22.5		1940		0.74				22.2		2050		0.734				22.5		2070		0.735

		22.2		1940		0.731				22.8		2120		0.754				22.6		1950		0.742				22.3		2050		0.736				22.6		2070		0.738

		22.3		1940		0.733				22.9		2120		0.756				22.7		1950		0.745				22.3		2060		0.739				22.6		2080		0.739

		22.3		1950		0.735				22.9		2130		0.758				22.7		1960		0.747				22.4		2060		0.74				22.7		2080		0.741

		22.4		1950		0.737				23		2130		0.76				22.8		1970		0.75				22.5		2070		0.742				22.8		2090		0.744

		22.5		1960		0.741				23.1		2140		0.764				22.9		1970		0.752				22.6		2070		0.744				22.8		2090		0.746

		22.6		1960		0.743				23.2		2140		0.766				22.9		1970		0.754				22.6		2080		0.746				22.9		2090		0.748

		22.6		1970		0.745				23.3		2150		0.768				23		1980		0.756				22.7		2080		0.749				23		2100		0.75

		22.7		1970		0.748				23.3		2150		0.77				23.1		1980		0.758				22.7		2090		0.751				23.1		2110		0.754

		22.8		1980		0.75				23.4		2160		0.772				23.2		1990		0.76				22.8		2090		0.753				23.1		2110		0.756

		22.8		1980		0.752				23.4		2160		0.774				23.2		1990		0.762				22.9		2100		0.755				23.2		2120		0.758

		22.9		1990		0.754				23.5		2170		0.776				23.2		2000		0.765				22.9		2100		0.758				23.3		2120		0.76

		23		1990		0.756				23.6		2170		0.778				23.3		2000		0.767				23		2110		0.76				23.3		2130		0.762

		23.1		2000		0.76				23.6		2180		0.78				23.4		2010		0.771				23.1		2110		0.762				23.4		2130		0.764

		23.2		2000		0.762				23.8		2190		0.785				23.5		2010		0.773				23.2		2120		0.764				23.4		2140		0.767

		23.2		2010		0.764				23.8		2190		0.787				23.6		2020		0.775				23.2		2120		0.766				23.5		2140		0.769

		23.3		2010		0.766				23.9		2190		0.789				23.6		2020		0.777				23.3		2130		0.768				23.7		2150		0.773

		23.4		2020		0.769				23.9		2200		0.791				23.7		2030		0.779				23.3		2130		0.771				23.7		2150		0.775

		23.4		2020		0.77				24		2200		0.793				23.8		2030		0.781				23.4		2140		0.773				23.8		2160		0.777

		23.5		2020		0.772				24.1		2210		0.795				23.8		2030		0.783				23.5		2150		0.777				23.8		2160		0.779

		23.5		2030		0.775				24.2		2210		0.797				23.9		2040		0.785				23.6		2150		0.779				23.9		2170		0.781

		23.6		2040		0.779				24.2		2220		0.799				24		2050		0.788				23.6		2160		0.781				23.9		2170		0.783

		23.7		2040		0.781				24.3		2220		0.803				24		2050		0.79				23.7		2160		0.783				24		2180		0.785

		23.8		2040		0.783				24.4		2230		0.805				24.1		2050		0.792				23.8		2170		0.785				24.1		2180		0.787

		23.8		2050		0.785				24.5		2230		0.807				24.2		2060		0.795				23.8		2170		0.787				24.2		2190		0.791

		23.9		2050		0.787				24.5		2240		0.809				24.2		2060		0.797				23.9		2180		0.789				24.3		2190		0.793

		24		2060		0.789				24.6		2240		0.812				24.3		2070		0.799				23.9		2180		0.791				24.3		2200		0.796

		24		2060		0.791				24.6		2250		0.814				24.3		2070		0.801				24		2190		0.793				24.4		2200		0.798

		24.1		2070		0.793				24.7		2250		0.816				24.4		2080		0.803				24.1		2190		0.797				24.4		2210		0.8

		24.2		2070		0.796				24.8		2260		0.818				24.5		2080		0.805				24.2		2200		0.8				24.5		2210		0.802

		24.3		2080		0.798				24.8		2260		0.82				24.6		2090		0.808				24.3		2200		0.802				24.6		2220		0.804

		24.3		2080		0.8				24.9		2270		0.823				24.6		2090		0.81				24.3		2210		0.804				24.6		2220		0.806

		24.4		2080		0.802				25		2270		0.825				24.7		2100		0.812				24.4		2210		0.806				24.8		2230		0.81

		24.4		2090		0.805				25		2280		0.827				24.7		2100		0.814				24.4		2220		0.808				24.8		2240		0.812

		24.5		2090		0.807				25.1		2280		0.829				24.8		2100		0.816				24.5		2220		0.81				24.9		2240		0.814

		24.6		2100		0.809				25.2		2280		0.832				24.9		2110		0.818				24.6		2230		0.812				24.9		2240		0.816

		24.6		2100		0.811				25.2		2290		0.834				25		2110		0.82				24.6		2230		0.814				25		2250		0.818

		24.7		2110		0.814				25.3		2290		0.836				25		2120		0.823				24.8		2240		0.817				25.1		2250		0.82

		24.8		2110		0.816				25.4		2300		0.838				25.1		2120		0.826				24.8		2250		0.819				25.2		2260		0.823

		24.8		2120		0.818				25.4		2310		0.841				25.2		2130		0.828				24.8		2250		0.821				25.2		2260		0.825

		24.9		2120		0.82				25.5		2310		0.842				25.2		2130		0.83				24.9		2250		0.823				25.3		2270		0.827

		25		2130		0.822				25.6		2310		0.844				25.3		2140		0.832				25		2260		0.825				25.4		2280		0.831

		25		2130		0.824				25.6		2320		0.846				25.3		2140		0.834				25		2270		0.828				25.4		2280		0.833

		25.1		2130		0.827				25.7		2320		0.848				25.4		2140		0.836				25.1		2270		0.83				25.5		2280		0.835

		25.1		2140		0.829				25.7		2330		0.85				25.5		2150		0.838				25.2		2270		0.832				25.6		2290		0.837

		25.2		2140		0.831				25.8		2330		0.852				25.6		2150		0.84				25.2		2280		0.834				25.6		2290		0.839

		25.3		2150		0.834				25.9		2330		0.854				25.7		2160		0.845				25.4		2290		0.838				25.7		2300		0.841

		25.4		2150		0.836				25.9		2340		0.856				25.7		2170		0.847				25.4		2290		0.84				25.8		2300		0.844

		25.5		2160		0.838				26		2350		0.859				25.8		2170		0.849				25.5		2300		0.842				25.8		2310		0.846

		25.5		2160		0.84				26.1		2350		0.862				25.8		2170		0.851				25.6		2300		0.844				25.9		2320		0.85

		25.5		2170		0.842				26.1		2350		0.864				25.9		2180		0.853				25.6		2310		0.846				26		2320		0.852

		25.6		2170		0.844				26.2		2360		0.866				26		2180		0.855				25.7		2310		0.849				26.1		2330		0.854

		25.7		2170		0.846				26.3		2360		0.868				26		2190		0.857				25.7		2320		0.851				26.1		2330		0.856

		25.7		2180		0.848				26.3		2370		0.87				26.1		2190		0.859				25.8		2320		0.853				26.2		2330		0.858

		25.8		2180		0.85				26.4		2370		0.872				26.2		2200		0.863				25.9		2330		0.857				26.3		2340		0.86

		25.9		2190		0.855				26.5		2380		0.874				26.3		2200		0.865				26		2340		0.859				26.3		2340		0.862

		26		2190		0.857				26.6		2390		0.878				26.4		2210		0.867				26.1		2340		0.861				26.4		2350		0.864

		26		2200		0.859				26.7		2390		0.88				26.4		2210		0.869				26.1		2350		0.863				26.4		2350		0.866

		26.1		2200		0.861				26.7		2400		0.883				26.5		2220		0.871				26.2		2350		0.865				26.6		2360		0.87

		26.2		2210		0.863				26.7		2400		0.885				26.6		2220		0.874				26.2		2360		0.867				26.7		2370		0.873

		26.3		2210		0.865				26.8		2410		0.887				26.6		2230		0.876				26.3		2360		0.869				26.7		2370		0.875

		26.3		2210		0.867				26.9		2410		0.889				26.6		2230		0.878				26.3		2370		0.871				26.8		2380		0.877

		26.4		2220		0.869				26.9		2420		0.891				26.8		2240		0.882				26.4		2370		0.873				26.9		2380		0.879

		26.5		2230		0.872				27		2420		0.893				26.8		2240		0.884				26.5		2380		0.878				26.9		2390		0.881

		26.5		2230		0.874				27.1		2420		0.895				26.9		2250		0.886				26.6		2390		0.88				27		2390		0.883

		26.6		2230		0.877				27.2		2430		0.898				27		2250		0.888				26.7		2390		0.882				27		2400		0.885

		26.7		2240		0.879				27.2		2430		0.9				27		2260		0.89				26.7		2390		0.884				27.1		2400		0.887

		26.7		2240		0.881				27.3		2440		0.902				27.1		2260		0.892				26.8		2400		0.886				27.2		2410		0.891

		26.8		2250		0.883				27.3		2440		0.904				27.1		2270		0.895				26.9		2400		0.888				27.3		2410		0.893

		26.9		2250		0.885				27.4		2450		0.906				27.2		2270		0.897				26.9		2410		0.89				27.3		2420		0.896

		26.9		2260		0.887				27.5		2450		0.908				27.3		2280		0.9				27		2410		0.892				27.4		2420		0.898

		27		2260		0.891				27.5		2460		0.911				27.4		2280		0.902				27.1		2420		0.896				27.4		2430		0.899

		27.1		2270		0.893				27.6		2460		0.913				27.4		2280		0.904				27.2		2430		0.898				27.5		2430		0.902

		27.2		2270		0.895				27.7		2470		0.917				27.5		2290		0.906				27.2		2430		0.9				27.6		2430		0.904

		27.2		2280		0.897				27.8		2470		0.919				27.6		2290		0.908				27.3		2440		0.902				27.7		2440		0.906

		27.3		2280		0.899				27.8		2480		0.921				27.6		2300		0.91				27.3		2440		0.905				27.8		2450		0.91

		27.3		2290		0.901				27.9		2480		0.923				27.7		2300		0.912				27.4		2450		0.907				27.8		2450		0.912

		27.4		2290		0.904				28		2490		0.925				27.8		2310		0.914				27.5		2450		0.909				27.9		2460		0.914

		27.4		2290		0.906				28.1		2490		0.927				27.9		2310		0.917				27.6		2450		0.911				28		2460		0.916

		27.6		2300		0.91				28.1		2500		0.929				27.9		2320		0.919				27.7		2460		0.914				28		2470		0.918

		27.6		2310		0.912				28.2		2500		0.931				28		2320		0.921				27.7		2470		0.916				28.1		2470		0.92

		27.7		2310		0.914				28.3		2510		0.936				28		2330		0.924				27.7		2470		0.918				28.1		2480		0.923

		27.8		2310		0.916				28.3		2510		0.938				28.1		2330		0.926				27.8		2470		0.92				28.2		2480		0.925

		27.9		2320		0.918				28.4		2520		0.94				28.2		2340		0.928				27.9		2480		0.922				28.3		2490		0.928

		27.9		2320		0.92				28.5		2520		0.942				28.2		2340		0.93				28		2480		0.924				28.3		2490		0.93

		27.9		2330		0.922				28.6		2530		0.944				28.3		2340		0.932				28		2490		0.927				28.4		2500		0.932

		28		2330		0.924				28.6		2530		0.946				28.3		2350		0.934				28.1		2490		0.929				28.5		2500		0.934

		28.2		2340		0.928				28.7		2530		0.948				28.5		2360		0.937				28.2		2500		0.931				28.5		2510		0.936

		28.2		2340		0.93				28.7		2540		0.95				28.5		2360		0.939				28.2		2500		0.934				28.6		2510		0.938

		28.3		2350		0.933				28.8		2540		0.952				28.6		2360		0.941				28.3		2510		0.936				28.7		2510		0.94

		28.4		2350		0.935				28.9		2550		0.955				28.6		2370		0.943				28.4		2510		0.938				28.7		2520		0.942

		28.4		2360		0.937				29		2550		0.957				28.7		2370		0.945				28.4		2520		0.94				28.8		2520		0.944

		28.5		2360		0.939				29		2560		0.959				28.7		2380		0.947				28.5		2520		0.942				28.9		2530		0.947

		28.5		2370		0.941				29.1		2560		0.962				28.8		2380		0.949				28.5		2530		0.944				28.9		2540		0.949

		28.6		2370		0.943				29.1		2570		0.964				28.9		2390		0.952				28.6		2530		0.946				29		2540		0.952

		28.7		2380		0.947				29.2		2570		0.966				29		2390		0.954				28.7		2540		0.948				29.1		2540		0.954

		28.8		2380		0.949				29.3		2580		0.968				29.1		2400		0.958				28.7		2540		0.95				29.2		2550		0.956

		28.9		2390		0.951				29.3		2580		0.97				29.1		2400		0.96				28.9		2550		0.955				29.2		2550		0.958

		28.9		2390		0.953				29.4		2590		0.973				29.2		2410		0.962				28.9		2550		0.957				29.3		2560		0.96

		28.9		2400		0.956				29.5		2590		0.975				29.3		2410		0.964				29		2560		0.959				29.3		2560		0.962

		29		2400		0.958				29.5		2600		0.977				29.3		2420		0.966				29.1		2560		0.961				29.4		2570		0.966

		29.1		2400		0.96				29.6		2600		0.979				29.4		2420		0.968				29.1		2570		0.963				29.5		2580		0.968

		29.1		2410		0.962				29.6		2610		0.981				29.5		2420		0.97				29.2		2570		0.965				29.6		2580		0.97

		29.3		2420		0.966				29.7		2610		0.983				29.5		2430		0.973				29.2		2580		0.967				29.7		2580		0.973

		29.4		2420		0.968				29.8		2610		0.985				29.6		2440		0.977				29.3		2580		0.969				29.7		2590		0.974

		29.4		2430		0.97				29.9		2620		0.987				29.7		2440		0.979				29.3		2590		0.971				29.8		2590		0.976

		29.4		2430		0.972				29.9		2620		0.991				29.7		2450		0.981				29.5		2600		0.975				29.8		2600		0.979

		29.5		2430		0.974				30		2630		0.993				29.8		2450		0.983				29.6		2600		0.977				29.9		2600		0.981

		29.6		2440		0.976				30.1		2630		0.995				29.9		2450		0.985				29.6		2600		0.98				29.9		2610		0.983

		29.6		2440		0.978				30.1		2640		0.997				29.9		2460		0.987				29.6		2610		0.982				30.1		2610		0.986

		29.7		2450		0.98				30.2		2640		0.999				30		2460		0.989				29.7		2610		0.984				30.1		2620		0.988

		29.8		2450		0.983				30.3		2650		1				30		2470		0.991				29.8		2620		0.986				30.2		2620		0.99

		29.9		2460		0.987				30.3		2650		1				30.2		2470		0.994				29.9		2620		0.988				30.2		2630		0.992

		29.9		2460		0.989				30.4		2660		1				30.2		2480		0.996				29.9		2630		0.99				30.3		2630		0.994

		30		2470		0.991				30.4		2660		1.01				30.3		2480		0.998				30		2630		0.993				30.3		2630		0.996

		30.1		2470		0.993				30.6		2670		1.01				30.3		2490		1				30.1		2640		0.995				30.4		2640		0.998

		30.1		2480		0.995				30.6		2670		1.01				30.4		2490		1				30.1		2640		0.997				30.5		2640		1

		30.2		2480		0.997				30.6		2680		1.01				30.5		2500		1				30.2		2650		0.999				30.5		2650		1

		30.3		2480		0.999				30.7		2680		1.02				30.5		2500		1.01				30.2		2650		1				30.7		2660		1.01

		30.3		2490		1				30.8		2690		1.02				30.6		2500		1.01				30.3		2660		1				30.7		2660		1.01

		30.4		2490		1				30.8		2690		1.02				30.7		2510		1.01				30.4		2660		1				30.8		2670		1.01

		30.5		2500		1.01				30.9		2690		1.02				30.8		2520		1.02				30.4		2670		1.01				30.8		2670		1.01

		30.6		2510		1.01				31		2700		1.03				30.8		2520		1.02				30.5		2670		1.01				30.9		2670		1.02

		30.7		2510		1.01				31.1		2700		1.03				30.9		2530		1.02				30.6		2680		1.01				31		2680		1.02

		30.7		2520		1.01				31.1		2710		1.03				31		2530		1.02				30.7		2680		1.02				31.1		2680		1.02

		30.8		2520		1.02				31.2		2710		1.03				31		2530		1.02				30.7		2690		1.02				31.1		2690		1.02

		30.8		2530		1.02				31.2		2720		1.03				31.1		2540		1.03				30.8		2690		1.02				31.2		2690		1.02

		30.9		2530		1.02				31.3		2720		1.04				31.1		2540		1.03				30.9		2700		1.02				31.2		2700		1.03

		30.9		2540		1.02				31.4		2730		1.04				31.2		2550		1.03				30.9		2700		1.02				31.3		2700		1.03

		31		2540		1.02				31.5		2730		1.04				31.4		2560		1.03				31		2710		1.03				31.4		2710		1.03

		31.1		2540		1.03				31.5		2740		1.04				31.4		2560		1.04				31.1		2710		1.03				31.5		2710		1.03

		31.2		2550		1.03				31.6		2740		1.05				31.5		2560		1.04				31.1		2720		1.03				31.5		2720		1.04

		31.2		2550		1.03				31.7		2750		1.05				31.5		2570		1.04				31.2		2720		1.03				31.6		2720		1.04

		31.3		2560		1.03				31.7		2750		1.05				31.6		2570		1.04				31.2		2730		1.04				31.6		2720		1.04

		31.3		2560		1.04				31.8		2760		1.05				31.7		2580		1.04				31.3		2730		1.04				31.7		2730		1.04

		31.4		2570		1.04				31.9		2760		1.06				31.7		2580		1.05				31.4		2730		1.04				31.8		2730		1.04

		31.4		2570		1.04				31.9		2770		1.06				31.8		2590		1.05				31.5		2740		1.04				31.9		2740		1.05

		31.5		2580		1.04				32		2770		1.06				31.8		2590		1.05				31.5		2740		1.04				31.9		2740		1.05

		31.6		2580		1.04				32		2780		1.06				32		2600		1.06				31.6		2750		1.05				32		2750		1.05

		31.7		2590		1.05				32.2		2790		1.07				32		2600		1.06				31.7		2760		1.05				32		2750		1.05

		31.8		2590		1.05				32.3		2790		1.07				32.1		2610		1.06				31.8		2760		1.05				32.1		2760		1.06

		31.8		2590		1.05				32.3		2800		1.07				32.1		2610		1.06				31.8		2770		1.05				32.2		2760		1.06

		31.8		2600		1.05				32.4		2800		1.07				32.2		2620		1.06				31.9		2770		1.06				32.2		2770		1.06

		31.9		2600		1.05				32.5		2800		1.07				32.3		2620		1.07				31.9		2780		1.06				32.3		2770		1.06

		32		2610		1.06				32.5		2810		1.08				32.3		2630		1.07				32		2780		1.06				32.4		2780		1.07

		32		2610		1.06				32.5		2810		1.08				32.4		2630		1.07				32.1		2790		1.06				32.5		2780		1.07

		32.1		2620		1.06				32.6		2820		1.08				32.5		2640		1.07				32.1		2790		1.06				32.5		2790		1.07

		32.2		2620		1.06				32.7		2830		1.08				32.6		2640		1.07				32.2		2800		1.07				32.6		2790		1.07

		32.3		2630		1.07				32.8		2830		1.09				32.6		2650		1.08				32.3		2810		1.07				32.7		2800		1.07

		32.3		2630		1.07				32.9		2840		1.09				32.7		2650		1.08				32.4		2810		1.07				32.7		2800		1.08

		32.4		2640		1.07				32.9		2840		1.09				32.8		2650		1.08				32.5		2810		1.07				32.8		2800		1.08

		32.4		2640		1.07				33		2840		1.09				32.8		2660		1.08				32.5		2820		1.08				32.8		2810		1.08

		32.5		2650		1.07				33		2850		1.1				32.9		2660		1.09				32.6		2820		1.08				32.9		2810		1.08

		32.6		2650		1.08				33.1		2850		1.1				33		2670		1.09				32.6		2830		1.08				33.1		2820		1.09

		32.6		2660		1.08				33.2		2860		1.1				33		2680		1.09				32.7		2830		1.08				33.1		2830		1.09

		32.7		2660		1.08				33.3		2870		1.1				33.1		2680		1.09				32.7		2840		1.08				33.2		2830		1.09

		32.8		2660		1.08				33.4		2870		1.11				33.2		2680		1.1				32.9		2850		1.09				33.2		2830		1.09

		32.8		2670		1.09				33.5		2880		1.11				33.2		2690		1.1				32.9		2850		1.09				33.3		2840		1.09

		32.9		2680		1.09				33.5		2880		1.11				33.3		2690		1.1				33		2860		1.09				33.4		2840		1.1

		33		2680		1.09				33.6		2880		1.11				33.4		2700		1.1				33		2860		1.1				33.4		2850		1.1

		33.1		2680		1.09				33.6		2890		1.11				33.4		2700		1.1				33.1		2860		1.1				33.5		2850		1.1

		33.1		2690		1.09				33.7		2890		1.12				33.5		2710		1.11				33.2		2870		1.1				33.6		2860		1.1

		33.2		2690		1.1				33.7		2900		1.12				33.5		2710		1.11				33.3		2870		1.1				33.7		2860		1.11

		33.2		2700		1.1				33.9		2910		1.12				33.7		2720		1.11				33.3		2880		1.1				33.7		2870		1.11

		33.3		2700		1.1				33.9		2910		1.12				33.8		2730		1.11				33.5		2890		1.11				33.7		2870		1.11

		33.4		2710		1.1				34		2920		1.13				33.8		2730		1.12				33.5		2890		1.11				33.8		2870		1.11

		33.5		2710		1.11				34.1		2920		1.13				33.9		2730		1.12				33.5		2900		1.11				33.9		2880		1.11

		33.6		2720		1.11				34.1		2930		1.13				33.9		2740		1.12				33.6		2900		1.11				33.9		2880		1.12

		33.6		2720		1.11				34.2		2930		1.13				34		2740		1.12				33.7		2910		1.12				34		2890		1.12

		33.7		2730		1.11				34.2		2940		1.13				34		2750		1.12				33.7		2910		1.12				34.1		2890		1.12

		33.8		2730		1.12				34.3		2940		1.14				34.1		2750		1.13				33.8		2910		1.12				34.2		2900		1.12

		33.8		2740		1.12				34.4		2950		1.14				34.2		2760		1.13				33.9		2920		1.12				34.2		2900		1.13

		33.9		2740		1.12				34.5		2950		1.14				34.3		2760		1.13				34		2930		1.13				34.3		2910		1.13

		33.9		2750		1.12				34.5		2960		1.14				34.4		2770		1.14				34		2930		1.13				34.3		2910		1.13

		34		2750		1.12				34.6		2960		1.15				34.4		2770		1.14				34.1		2940		1.13				34.4		2920		1.13

		34.1		2760		1.13				34.6		2970		1.15				34.5		2780		1.14				34.2		2940		1.13				34.5		2920		1.13

		34.2		2760		1.13				34.7		2970		1.15				34.5		2780		1.14				34.3		2950		1.13				34.5		2920		1.14

		34.2		2760		1.13				34.8		2970		1.15				34.6		2790		1.14				34.3		2950		1.14				34.6		2930		1.14

		34.2		2770		1.13				34.8		2980		1.15				34.7		2790		1.15				34.4		2960		1.14				34.7		2940		1.14

		34.3		2770		1.13				34.9		2980		1.16				34.8		2800		1.15				34.5		2960		1.14				34.8		2940		1.14

		34.4		2780		1.14				35		2990		1.16				34.9		2810		1.15				34.6		2970		1.15				34.8		2950		1.15

		34.5		2790		1.14				35		2990		1.16				34.9		2810		1.15				34.6		2970		1.15				34.9		2950		1.15

		34.6		2790		1.14				35.1		3000		1.16				35		2810		1.16				34.7		2980		1.15				35		2960		1.15

		34.6		2800		1.15				35.2		3000		1.17				35.1		2820		1.16				34.7		2980		1.15				35.1		2960		1.15

		34.7		2800		1.15				35.2		3010		1.17				35.1		2820		1.16				34.8		2990		1.15				35.1		2960		1.15

		34.8		2800		1.15				35.3		3010		1.17				35.2		2830		1.16				34.9		2990		1.16				35.1		2970		1.16

		34.8		2810		1.15				35.4		3020		1.17				35.2		2830		1.16				35		3000		1.16				35.3		2980		1.16

		34.9		2810		1.15				35.5		3020		1.17				35.3		2840		1.17				35		3000		1.16				35.3		2980		1.16

		35		2820		1.16				35.5		3030		1.18				35.4		2840		1.17				35.1		3010		1.16				35.4		2990		1.17

		35		2820		1.16				35.6		3030		1.18				35.5		2850		1.17				35.1		3010		1.17				35.5		2990		1.17

		35.1		2830		1.16				35.6		3040		1.18				35.5		2850		1.17				35.2		3020		1.17				35.5		2990		1.17

		35.2		2830		1.16				35.7		3040		1.18				35.6		2860		1.18				35.3		3020		1.17				35.6		3000		1.17

		35.2		2840		1.17				35.8		3050		1.19				35.7		2860		1.18				35.4		3030		1.17				35.7		3000		1.17

		35.3		2840		1.17				35.8		3050		1.19				35.8		2870		1.18				35.4		3030		1.17				35.7		3010		1.18

		35.4		2840		1.17				35.9		3060		1.19				35.8		2870		1.18				35.5		3030		1.18				35.8		3020		1.18

		35.4		2850		1.17				36		3060		1.19				35.9		2870		1.18				35.5		3040		1.18				35.9		3020		1.18

		35.5		2850		1.17				36.1		3070		1.2				35.9		2880		1.19				35.6		3050		1.18				36		3020		1.18

		35.6		2860		1.18				36.1		3070		1.2				36		2890		1.19				35.7		3050		1.18				36		3030		1.19

		35.7		2860		1.18				36.2		3080		1.2				36.1		2890		1.19				35.8		3060		1.18				36.1		3030		1.19

		35.7		2870		1.18				36.3		3080		1.2				36.2		2900		1.2				35.8		3060		1.19				36.1		3040		1.19

		35.7		2870		1.18				36.3		3090		1.2				36.3		2900		1.2				35.9		3060		1.19				36.2		3040		1.19

		35.8		2880		1.18				36.4		3090		1.21				36.3		2910		1.2				36		3070		1.19				36.3		3050		1.19

		35.9		2880		1.19				36.4		3090		1.21				36.4		2910		1.2				36		3070		1.19				36.4		3050		1.2

		36		2890		1.19				36.5		3100		1.21				36.4		2920		1.2				36.1		3080		1.2				36.4		3060		1.2

		36		2890		1.19				36.6		3100		1.21				36.5		2920		1.21				36.2		3090		1.2				36.5		3060		1.2

		36.1		2890		1.19				36.7		3110		1.22				36.6		2930		1.21				36.3		3090		1.2				36.6		3070		1.2

		36.2		2900		1.2				36.8		3120		1.22				36.7		2930		1.21				36.3		3100		1.2				36.6		3070		1.21

		36.3		2910		1.2				36.8		3120		1.22				36.8		2940		1.21				36.4		3100		1.21				36.7		3080		1.21

		36.3		2910		1.2				36.9		3130		1.22				36.8		2940		1.22				36.5		3110		1.21				36.7		3080		1.21

		36.4		2920		1.2				37		3130		1.23				36.9		2950		1.22				36.5		3110		1.21				36.8		3080		1.21

		36.5		2920		1.21				37		3130		1.23				36.9		2950		1.22				36.6		3120		1.21				36.9		3090		1.22

		36.5		2920		1.21				37.1		3140		1.23				37		2950		1.22				36.6		3120		1.21				37		3100		1.22

		36.6		2930		1.21				37.1		3140		1.23				37		2960		1.22				36.8		3130		1.22				37.1		3100		1.22

		36.7		2930		1.21				37.2		3150		1.23				37.2		2970		1.23				36.8		3130		1.22				37.1		3110		1.22

		36.7		2940		1.22				37.3		3160		1.24				37.2		2970		1.23				36.9		3140		1.22				37.2		3110		1.22

		36.8		2950		1.22				37.4		3160		1.24				37.3		2980		1.23				36.9		3140		1.22				37.3		3120		1.23

		36.9		2950		1.22				37.4		3170		1.24				37.4		2980		1.23				37		3150		1.23				37.3		3120		1.23

		36.9		2950		1.22				37.5		3170		1.24				37.4		2980		1.24				37.1		3150		1.23				37.4		3120		1.23

		37		2960		1.22				37.6		3170		1.25				37.5		2990		1.24				37.1		3160		1.23				37.4		3130		1.23

		37.1		2960		1.23				37.7		3180		1.25				37.5		2990		1.24				37.2		3160		1.23				37.6		3140		1.24

		37.2		2970		1.23				37.7		3180		1.25				37.6		3000		1.24				37.3		3170		1.24				37.6		3140		1.24

		37.2		2970		1.23				37.8		3190		1.25				37.7		3000		1.25				37.4		3180		1.24				37.7		3150		1.24

		37.3		2980		1.23				37.9		3190		1.26				37.8		3010		1.25				37.4		3180		1.24				37.8		3150		1.24

		37.3		2980		1.23				38		3200		1.26				37.8		3010		1.25				37.5		3190		1.24				37.8		3160		1.25

		37.4		2980		1.24				38		3200		1.26				37.9		3020		1.25				37.5		3190		1.25				37.9		3160		1.25

		37.4		2990		1.24				38.1		3210		1.26				38		3020		1.26				37.6		3190		1.25				38		3170		1.25

		37.5		2990		1.24				38.1		3210		1.26				38		3030		1.26				37.7		3200		1.25				38		3170		1.25

		37.6		3000		1.24				38.2		3220		1.27				38.1		3030		1.26				37.7		3200		1.25				38.1		3180		1.26

		37.6		3000		1.25				38.3		3220		1.27				38.2		3030		1.26				37.8		3210		1.25				38.2		3180		1.26

		37.7		3000		1.25				38.4		3220		1.27				38.3		3040		1.27				37.9		3220		1.26				38.3		3190		1.26

		37.7		3010		1.25				38.5		3230		1.28				38.3		3050		1.27				38		3220		1.26				38.3		3190		1.26

		37.9		3020		1.25				38.5		3240		1.28				38.4		3050		1.27				38.1		3230		1.26				38.4		3200		1.26

		38		3020		1.26				38.6		3240		1.28				38.5		3060		1.27				38.1		3230		1.26				38.4		3200		1.27

		38		3020		1.26				38.7		3250		1.28				38.5		3060		1.27				38.2		3240		1.27				38.5		3210		1.27

		38.1		3030		1.26				38.7		3250		1.28				38.6		3060		1.28				38.3		3240		1.27				38.5		3210		1.27

		38.1		3030		1.26				38.8		3250		1.29				38.7		3070		1.28				38.3		3250		1.27				38.7		3220		1.27

		38.2		3040		1.26				38.9		3260		1.29				38.8		3070		1.28				38.4		3250		1.27				38.7		3220		1.28

		38.3		3040		1.27				38.9		3260		1.29				38.8		3080		1.28				38.5		3260		1.28				38.8		3230		1.28

		38.3		3050		1.27				39		3270		1.29				38.9		3090		1.29				38.5		3260		1.28				38.8		3230		1.28

		38.4		3050		1.27				39.1		3270		1.3				39		3090		1.29				38.6		3270		1.28				38.9		3240		1.28

		38.5		3060		1.27				39.1		3280		1.3				39.1		3090		1.29				38.7		3270		1.28				39		3240		1.28

		38.6		3060		1.28				39.2		3280		1.3				39.1		3100		1.29				38.8		3280		1.28				39		3240		1.29

		38.6		3070		1.28				39.3		3290		1.3				39.2		3100		1.3				38.8		3280		1.29				39.1		3250		1.29

		38.7		3070		1.28				39.3		3290		1.3				39.3		3110		1.3				38.9		3290		1.29				39.2		3260		1.29

		38.8		3070		1.28				39.4		3300		1.31				39.3		3110		1.3				38.9		3290		1.29				39.3		3260		1.29

		38.8		3080		1.28				39.5		3300		1.31				39.4		3120		1.3				39.1		3300		1.3				39.3		3260		1.3

		38.9		3080		1.29				39.6		3310		1.31				39.5		3120		1.31				39.1		3310		1.3				39.4		3270		1.3

		39		3090		1.29				39.6		3310		1.31				39.6		3130		1.31				39.2		3310		1.3				39.4		3270		1.3

		39.1		3100		1.29				39.7		3320		1.32				39.6		3130		1.31				39.3		3310		1.3				39.5		3280		1.3

		39.1		3100		1.3				39.8		3320		1.32				39.7		3140		1.31				39.3		3320		1.3				39.6		3280		1.3

		39.2		3100		1.3				39.8		3320		1.32				39.7		3140		1.31				39.4		3320		1.31				39.6		3290		1.31

		39.3		3110		1.3				39.9		3330		1.32				39.8		3140		1.32				39.4		3330		1.31				39.7		3290		1.31

		39.3		3110		1.3				39.9		3330		1.32				39.9		3150		1.32				39.5		3330		1.31				39.8		3300		1.31

		39.4		3120		1.3				40		3340		1.33				39.9		3150		1.32				39.5		3340		1.31				39.8		3300		1.31

		39.4		3120		1.31				40.1		3350		1.33				40		3160		1.32				39.7		3350		1.32				39.9		3310		1.31

		39.5		3130		1.31				40.2		3350		1.33				40.1		3160		1.33				39.8		3350		1.32				40		3310		1.32

		39.6		3130		1.31				40.3		3350		1.33				40.1		3170		1.33				39.8		3360		1.32				40		3310		1.32

		39.6		3130		1.31				40.3		3360		1.34				40.2		3170		1.33				39.9		3360		1.32				40.1		3320		1.32

		39.7		3140		1.31				40.4		3360		1.34				40.3		3180		1.33				39.9		3370		1.32				40.1		3320		1.32

		39.8		3140		1.32				40.4		3370		1.34				40.3		3180		1.33				40		3370		1.33				40.2		3330		1.33

		39.8		3150		1.32				40.5		3370		1.34				40.4		3190		1.34				40		3370		1.33				40.3		3330		1.33

		39.9		3150		1.32				40.5		3370		1.34				40.4		3190		1.34				40.1		3380		1.33				40.4		3340		1.33

		39.9		3150		1.32				40.6		3380		1.35				40.5		3190		1.34				40.3		3390		1.33				40.4		3340		1.33

		40		3160		1.32				40.7		3390		1.35				40.6		3200		1.34				40.3		3390		1.34				40.5		3350		1.33

		40.1		3160		1.33				40.8		3390		1.35				40.7		3200		1.35				40.4		3400		1.34				40.5		3350		1.34

		40.2		3170		1.33				40.8		3390		1.35				40.7		3210		1.35				40.4		3400		1.34				40.6		3360		1.34

		40.2		3180		1.33				40.9		3400		1.36				40.8		3210		1.35				40.5		3410		1.34				40.7		3360		1.34

		40.3		3180		1.33				41		3400		1.36				40.8		3220		1.35				40.6		3410		1.34				40.8		3360		1.34

		40.4		3180		1.34				41		3410		1.36				40.9		3220		1.35				40.6		3420		1.35				40.8		3370		1.35

		40.5		3190		1.34				41.1		3410		1.36				41		3230		1.36				40.7		3420		1.35				40.9		3370		1.35

		40.5		3190		1.34				41.2		3420		1.37				41		3230		1.36				40.8		3430		1.35				41		3380		1.35

		40.6		3200		1.34				41.2		3420		1.37				41.1		3230		1.36				40.8		3430		1.35				41.1		3390		1.35

		40.6		3200		1.35				41.3		3430		1.37				41.2		3240		1.36				40.9		3440		1.36				41.1		3390		1.36

		40.7		3210		1.35				41.3		3430		1.37				41.3		3250		1.37				41		3440		1.36				41.2		3390		1.36

		40.8		3220		1.35				41.4		3430		1.37				41.3		3250		1.37				41		3450		1.36				41.3		3400		1.36

		40.9		3220		1.35				41.5		3440		1.38				41.4		3250		1.37				41.1		3450		1.36				41.3		3400		1.36

		41		3220		1.36				41.6		3440		1.38				41.5		3260		1.37				41.1		3460		1.36				41.4		3410		1.36

		41		3230		1.36				41.6		3450		1.38				41.6		3260		1.37				41.2		3460		1.37				41.5		3410		1.37

		41.1		3230		1.36				41.7		3460		1.38				41.6		3270		1.38				41.3		3470		1.37				41.5		3420		1.37

		41.1		3240		1.36				41.8		3460		1.39				41.7		3270		1.38				41.3		3470		1.37				41.6		3420		1.37

		41.2		3240		1.36				41.9		3460		1.39				41.7		3280		1.38				41.4		3480		1.37				41.7		3430		1.37

		41.3		3250		1.37				41.9		3470		1.39				41.8		3280		1.38				41.4		3480		1.38				41.7		3430		1.38

		41.3		3250		1.37				42		3470		1.39				41.9		3290		1.39				41.5		3490		1.38				41.8		3440		1.38

		41.4		3260		1.37				42.1		3480		1.39				42		3290		1.39				41.6		3490		1.38				41.9		3440		1.38

		41.5		3260		1.37				42.1		3480		1.4				42.1		3300		1.39				41.6		3500		1.38				41.9		3450		1.38

		41.5		3260		1.38				42.2		3490		1.4				42.1		3300		1.39				41.7		3500		1.38				42		3450		1.38

		41.6		3270		1.38				42.3		3490		1.4				42.2		3310		1.4				41.8		3510		1.39				42.1		3460		1.39

		41.6		3270		1.38				42.3		3500		1.4				42.2		3310		1.4				41.8		3510		1.39				42.2		3460		1.39

		41.7		3280		1.38				42.4		3500		1.41				42.3		3310		1.4				41.9		3520		1.39				42.3		3470		1.39

		41.8		3280		1.38				42.5		3510		1.41				42.4		3320		1.4				42		3520		1.39				42.3		3470		1.4

		41.9		3290		1.39				42.6		3510		1.41				42.5		3330		1.41				42.1		3530		1.39				42.4		3480		1.4

		42		3300		1.39				42.6		3510		1.41				42.5		3330		1.41				42.1		3530		1.4				42.4		3480		1.4

		42		3300		1.39				42.7		3520		1.42				42.6		3340		1.41				42.2		3540		1.4				42.5		3490		1.4

		42.1		3300		1.39				42.8		3520		1.42				42.7		3340		1.41				42.2		3540		1.4				42.5		3490		1.4

		42.2		3310		1.4				42.8		3530		1.42				42.7		3340		1.41				42.3		3550		1.4				42.6		3500		1.41

		42.2		3310		1.4				42.9		3530		1.42				42.8		3350		1.42				42.3		3550		1.41				42.7		3500		1.41

		42.3		3320		1.4				43		3540		1.42				42.8		3350		1.42				42.4		3550		1.41				42.8		3510		1.41

		42.3		3320		1.4				43		3540		1.43				42.9		3360		1.42				42.5		3560		1.41				42.8		3510		1.41

		42.5		3330		1.41				43.1		3550		1.43				43		3360		1.42				42.6		3570		1.41				42.9		3510		1.41

		42.5		3330		1.41				43.2		3550		1.43				43		3360		1.42				42.7		3570		1.41				42.9		3520		1.42

		42.6		3340		1.41				43.2		3550		1.43				43.1		3370		1.43				42.7		3580		1.42				43		3520		1.42

		42.7		3340		1.41				43.2		3560		1.44				43.2		3370		1.43				42.8		3580		1.42				43.1		3530		1.42

		42.7		3340		1.41				43.3		3560		1.44				43.2		3380		1.43				42.8		3590		1.42				43.1		3530		1.42

		42.8		3350		1.42				43.4		3570		1.44				43.3		3380		1.43				42.9		3590		1.42				43.3		3540		1.43

		42.8		3350		1.42				43.5		3570		1.44				43.4		3390		1.43				42.9		3590		1.43				43.4		3550		1.43

		42.9		3360		1.42				43.5		3580		1.44				43.4		3390		1.44				43		3600		1.43				43.4		3550		1.43

		43		3370		1.43				43.6		3580		1.45				43.5		3390		1.44				43.1		3610		1.43				43.4		3550		1.43

		43.1		3370		1.43				43.7		3590		1.45				43.6		3400		1.44				43.2		3610		1.43				43.5		3560		1.44

		43.2		3370		1.43				43.7		3590		1.45				43.7		3410		1.44				43.3		3620		1.44				43.6		3560		1.44

		43.2		3380		1.43				43.8		3590		1.45				43.7		3410		1.45				43.3		3620		1.44				43.6		3570		1.44

		43.3		3380		1.43				43.8		3600		1.45				43.8		3420		1.45				43.4		3630		1.44				43.7		3570		1.44

		43.3		3390		1.44				43.9		3600		1.46				43.8		3420		1.45				43.5		3630		1.44				43.8		3580		1.44

		43.4		3390		1.44				44		3610		1.46				43.9		3420		1.45				43.5		3640		1.44				43.9		3580		1.45

		43.5		3390		1.44				44.1		3610		1.46				44		3430		1.46				43.6		3640		1.45				43.9		3590		1.45

		43.5		3400		1.44				44.1		3620		1.46				44.1		3430		1.46				43.7		3650		1.45				44		3590		1.45

		43.7		3410		1.45				44.2		3620		1.47				44.1		3440		1.46				43.8		3650		1.45				44		3600		1.45

		43.7		3410		1.45				44.2		3630		1.47				44.2		3440		1.46				43.8		3660		1.45				44.1		3600		1.46

		43.8		3420		1.45				44.3		3630		1.47				44.2		3450		1.46				43.9		3660		1.46				44.2		3610		1.46

		43.8		3420		1.45				44.4		3640		1.47				44.3		3450		1.47				43.9		3670		1.46				44.2		3610		1.46

		43.9		3420		1.45				44.4		3640		1.47				44.4		3460		1.47				44		3670		1.46				44.3		3620		1.46

		44		3430		1.46				44.5		3640		1.48				44.4		3460		1.47				44.1		3680		1.46				44.4		3620		1.47

		44		3430		1.46				44.6		3650		1.48				44.5		3460		1.47				44.1		3680		1.46				44.5		3630		1.47

		44.1		3440		1.46				44.7		3650		1.48				44.6		3470		1.48				44.3		3690		1.47				44.6		3630		1.47

		44.2		3440		1.46				44.7		3660		1.48				44.6		3470		1.48				44.3		3690		1.47				44.6		3640		1.47

		44.3		3450		1.47				44.8		3660		1.49				44.7		3480		1.48				44.4		3700		1.47				44.7		3640		1.47

		44.3		3450		1.47				44.8		3670		1.49				44.8		3480		1.48				44.4		3700		1.48				44.7		3650		1.48

		44.4		3460		1.47				44.9		3670		1.49				44.8		3490		1.48				44.5		3710		1.48				44.8		3650		1.48

		44.5		3460		1.47				45		3680		1.49				44.9		3490		1.49				44.6		3710		1.48				44.9		3660		1.48

		44.5		3470		1.47				45		3680		1.49				45		3500		1.49				44.7		3720		1.48				45		3660		1.48

		44.6		3470		1.48				45.1		3680		1.5				45		3500		1.49				44.7		3720		1.48				45		3670		1.49

		44.6		3480		1.48				45.2		3690		1.5				45.1		3510		1.49				44.8		3730		1.49				45.1		3670		1.49

		44.8		3480		1.48				45.3		3700		1.5				45.2		3510		1.49				44.9		3740		1.49				45.2		3670		1.49

		44.9		3490		1.49				45.4		3700		1.5				45.3		3520		1.5				44.9		3740		1.49				45.2		3680		1.49

		44.9		3490		1.49				45.4		3700		1.51				45.4		3520		1.5				45		3740		1.49				45.3		3680		1.49

		45		3500		1.49				45.5		3710		1.51				45.4		3530		1.5				45.1		3750		1.5				45.3		3690		1.5

		45		3500		1.49				45.6		3710		1.51				45.5		3530		1.51				45.1		3750		1.5				45.4		3690		1.5

		45.1		3510		1.49				45.6		3720		1.51				45.6		3540		1.51				45.2		3760		1.5				45.5		3700		1.5

		45.1		3510		1.5				45.7		3720		1.52				45.6		3540		1.51				45.3		3760		1.5				45.6		3700		1.5

		45.2		3510		1.5				45.8		3730		1.52				45.6		3540		1.51				45.4		3770		1.51				45.7		3710		1.51

		45.3		3520		1.5				45.9		3730		1.52				45.7		3550		1.51				45.4		3780		1.51				45.7		3710		1.51

		45.4		3520		1.5				45.9		3740		1.52				45.8		3560		1.52				45.5		3780		1.51				45.8		3720		1.51

		45.4		3530		1.51				46		3740		1.53				45.9		3560		1.52				45.6		3790		1.51				45.8		3720		1.51

		45.5		3530		1.51				46.1		3750		1.53				46		3560		1.52				45.7		3790		1.51				45.9		3730		1.51

		45.5		3540		1.51				46.1		3750		1.53				46.1		3570		1.52				45.7		3800		1.52				45.9		3730		1.52

		45.6		3540		1.51				46.2		3760		1.53				46.1		3570		1.53				45.7		3800		1.52				46.1		3740		1.52

		45.7		3550		1.51				46.2		3760		1.53				46.1		3580		1.53				45.8		3810		1.52				46.1		3740		1.52

		45.8		3550		1.52				46.3		3770		1.54				46.2		3580		1.53				46		3820		1.52				46.2		3750		1.52

		45.9		3560		1.52				46.4		3770		1.54				46.3		3590		1.53				46		3820		1.53				46.2		3750		1.53

		45.9		3560		1.52				46.5		3770		1.54				46.3		3590		1.53				46.1		3830		1.53				46.3		3760		1.53

		45.9		3560		1.52				46.5		3780		1.54				46.5		3600		1.54				46.2		3830		1.53				46.3		3760		1.53

		46		3570		1.52				46.6		3780		1.55				46.5		3600		1.54				46.2		3830		1.53				46.4		3760		1.53

		46.1		3570		1.53				46.6		3790		1.55				46.6		3610		1.54				46.3		3840		1.54				46.5		3770		1.53

		46.1		3580		1.53				46.7		3790		1.55				46.6		3610		1.54				46.3		3840		1.54				46.5		3770		1.54

		46.2		3580		1.53				46.8		3800		1.55				46.7		3620		1.55				46.4		3850		1.54				46.7		3780		1.54

		46.3		3580		1.53				46.8		3800		1.55				46.8		3620		1.55				46.5		3860		1.54				46.8		3790		1.54

		46.3		3590		1.54				46.9		3810		1.56				46.8		3630		1.55				46.6		3860		1.55				46.8		3790		1.54

		46.4		3600		1.54				47		3810		1.56				46.9		3630		1.55				46.7		3870		1.55				46.8		3790		1.55

		46.5		3600		1.54				47.1		3810		1.56				47		3640		1.56				46.7		3870		1.55				46.9		3800		1.55

		46.6		3610		1.54				47.1		3820		1.56				47.1		3640		1.56				46.8		3880		1.55				47		3800		1.55

		46.7		3610		1.55				47.1		3820		1.57				47.1		3640		1.56				46.8		3880		1.55				47		3810		1.55

		46.7		3610		1.55				47.2		3830		1.57				47.2		3650		1.56				46.9		3880		1.56				47.1		3810		1.56

		46.8		3620		1.55				47.3		3830		1.57				47.2		3650		1.56				47		3890		1.56				47.2		3820		1.56

		46.9		3620		1.55				47.4		3840		1.57				47.3		3660		1.57				47.1		3900		1.56				47.3		3830		1.56

		46.9		3630		1.55				47.5		3840		1.57				47.4		3660		1.57				47.1		3900		1.56				47.4		3830		1.56

		47		3640		1.56				47.5		3850		1.58				47.4		3670		1.57				47.2		3910		1.57				47.4		3840		1.57

		47.1		3640		1.56				47.6		3850		1.58				47.5		3670		1.57				47.3		3910		1.57				47.5		3840		1.57

		47.1		3640		1.56				47.6		3850		1.58				47.6		3680		1.58				47.3		3920		1.57				47.5		3840		1.57

		47.2		3650		1.56				47.7		3860		1.58				47.7		3680		1.58				47.4		3920		1.57				47.6		3850		1.57

		47.3		3650		1.57				47.7		3860		1.58				47.7		3680		1.58				47.4		3930		1.57				47.7		3850		1.57

		47.4		3660		1.57				47.8		3870		1.59				47.8		3690		1.58				47.5		3930		1.58				47.8		3860		1.58

		47.4		3660		1.57				47.9		3870		1.59				47.8		3690		1.58				47.6		3940		1.58				47.8		3860		1.58

		47.4		3660		1.57				48		3880		1.59				47.9		3700		1.59				47.7		3940		1.58				47.9		3870		1.58

		47.5		3670		1.58				48.1		3880		1.6				48		3700		1.59				47.7		3950		1.58				48		3870		1.58

		47.6		3670		1.58				48.1		3890		1.6				48		3710		1.59				47.8		3950		1.59				48		3880		1.59

		47.7		3680		1.58				48.2		3890		1.6				48.1		3710		1.59				47.9		3960		1.59				48.1		3880		1.59

		47.7		3680		1.58				48.2		3900		1.6				48.2		3720		1.6				47.9		3960		1.59				48.2		3890		1.59

		47.8		3680		1.58				48.3		3900		1.6				48.3		3720		1.6				48		3970		1.59				48.2		3890		1.59

		47.9		3690		1.59				48.4		3910		1.61				48.3		3730		1.6				48		3970		1.59				48.3		3900		1.59

		47.9		3690		1.59				48.4		3910		1.61				48.4		3730		1.6				48.1		3970		1.6				48.3		3900		1.6

		48		3700		1.59				48.5		3920		1.61				48.5		3740		1.61				48.2		3980		1.6				48.5		3910		1.6

		48		3700		1.59				48.6		3920		1.61				48.5		3740		1.61				48.3		3990		1.6				48.5		3910		1.6

		48.2		3710		1.6				48.6		3930		1.62				48.6		3750		1.61				48.4		3990		1.61				48.6		3920		1.6

		48.2		3710		1.6				48.7		3930		1.62				48.6		3750		1.61				48.4		4000		1.61				48.7		3920		1.61

		48.3		3720		1.6				48.8		3930		1.62				48.8		3760		1.62				48.5		4000		1.61				48.7		3930		1.61

		48.4		3720		1.6				48.9		3940		1.62				48.9		3760		1.62				48.6		4010		1.61				48.8		3930		1.61

		48.4		3720		1.6				48.9		3940		1.62				48.9		3770		1.62				48.6		4010		1.61				48.8		3930		1.61

		48.5		3730		1.61				49		3950		1.63				49		3770		1.62				48.7		4020		1.62				48.9		3940		1.61

		48.5		3730		1.61				49.1		3960		1.63				49		3780		1.62				48.8		4020		1.62				49		3950		1.62

		48.6		3740		1.61				49.2		3960		1.63				49.1		3780		1.63				48.8		4030		1.62				49		3950		1.62

		48.7		3740		1.61				49.2		3960		1.63				49.1		3780		1.63				48.9		4030		1.62				49.1		3950		1.62

		48.8		3750		1.62				49.3		3970		1.64				49.2		3790		1.63				48.9		4030		1.62				49.2		3960		1.62

		48.8		3750		1.62				49.3		3970		1.64				49.3		3800		1.63				49		4040		1.63				49.3		3960		1.63

		48.9		3760		1.62				49.4		3980		1.64				49.4		3800		1.64				49.1		4040		1.63				49.3		3970		1.63

		48.9		3760		1.62				49.5		3980		1.64				49.5		3810		1.64				49.1		4050		1.63				49.4		3970		1.63

		49		3760		1.62				49.5		3990		1.64				49.5		3810		1.64				49.2		4050		1.63				49.4		3980		1.63

		49.1		3770		1.63				49.6		3990		1.65				49.6		3810		1.64				49.3		4060		1.64				49.5		3980		1.63

		49.1		3770		1.63				49.7		4000		1.65				49.6		3820		1.64				49.4		4070		1.64				49.6		3990		1.64

		49.2		3780		1.63				49.8		4000		1.65				49.7		3820		1.65				49.5		4070		1.64				49.7		4000		1.64

		49.3		3780		1.64				49.8		4000		1.65				49.8		3830		1.65				49.5		4080		1.64				49.7		4000		1.64

		49.4		3790		1.64				49.9		4010		1.66				49.9		3830		1.65				49.6		4080		1.65				49.8		4000		1.64

		49.4		3790		1.64				49.9		4010		1.66				50		3840		1.66				49.6		4080		1.65				49.8		4010		1.65

		49.5		3800		1.64				50		4020		1.66				50		3840		1.66				49.7		4090		1.65				49.9		4010		1.65

		49.6		3800		1.64				50.1		4020		1.66				50.1		3850		1.66				49.8		4090		1.65				50		4020		1.65

		49.7		3800		1.65				50.1		4030		1.66				50.1		3850		1.66				49.8		4100		1.66				50		4020		1.65

		49.7		3810		1.65				50.3		4040		1.67				50.2		3860		1.66				49.9		4110		1.66				50.2		4030		1.66

		49.8		3810		1.65				50.3		4040		1.67				50.3		3860		1.67				50		4110		1.66				50.2		4040		1.66

		49.9		3820		1.65				50.4		4040		1.67				50.4		3870		1.67				50.1		4110		1.66				50.3		4040		1.66

		49.9		3820		1.66				50.4		4050		1.67				50.4		3870		1.67				50.1		4120		1.66				50.3		4040		1.66

		50		3830		1.66				50.5		4050		1.68				50.5		3880		1.67				50.1		4120		1.67				50.4		4050		1.67

		50.1		3830		1.66				50.6		4060		1.68				50.6		3880		1.68				50.2		4130		1.67				50.5		4050		1.67

		50.1		3840		1.66				50.6		4060		1.68				50.6		3890		1.68				50.3		4130		1.67				50.5		4060		1.67

		50.2		3840		1.66				50.7		4070		1.68				50.7		3890		1.68				50.4		4140		1.67				50.6		4060		1.67

		50.3		3850		1.67				50.8		4070		1.68				50.8		3900		1.68				50.5		4150		1.68				50.7		4070		1.68

		50.3		3850		1.67				50.9		4080		1.69				50.9		3900		1.68				50.6		4150		1.68				50.8		4080		1.68

		50.4		3860		1.67				50.9		4080		1.69				50.9		3910		1.69				50.6		4160		1.68				50.8		4080		1.68

		50.5		3860		1.67				51		4090		1.69				51		3910		1.69				50.7		4160		1.68				50.9		4080		1.68

		50.6		3860		1.68				51		4090		1.69				51.1		3920		1.69				50.7		4170		1.68				51		4090		1.68

		50.6		3870		1.68				51.1		4090		1.7				51.2		3920		1.69				50.8		4170		1.69				51		4090		1.69

		50.7		3870		1.68				51.5		4120		1.71				51.2		3930		1.7				50.8		4170		1.69				51.1		4100		1.69

		50.7		3880		1.68				51.5		4120		1.71				51.3		3930		1.7				50.9		4180		1.69				51.2		4100		1.69

		50.8		3880		1.68				51.6		4130		1.71				51.3		3940		1.7				51		4180		1.69				51.3		4110		1.69

		50.8		3890		1.69				51.6		4130		1.71				51.4		3940		1.7				51.1		4190		1.7				51.3		4120		1.7

		50.9		3890		1.69				51.7		4140		1.72				51.5		3940		1.7				51.2		4200		1.7				51.4		4120		1.7

		51.1		3900		1.69				51.8		4140		1.72				51.5		3950		1.71				51.2		4200		1.7				51.5		4120		1.7

		51.1		3900		1.69				51.9		4150		1.72				51.6		3950		1.71				51.3		4210		1.7				51.5		4130		1.7

		51.2		3910		1.7				51.9		4150		1.72				51.7		3960		1.71				51.4		4210		1.71				51.6		4130		1.7

		51.2		3910		1.7				52		4160		1.73				51.8		3970		1.72				51.4		4220		1.71				51.7		4140		1.71

		51.3		3910		1.7				52.1		4160		1.73				51.8		3970		1.72				51.5		4220		1.71				51.7		4140		1.71

		51.4		3920		1.7				52.1		4170		1.73				51.9		3970		1.72				51.6		4220		1.71				51.9		4150		1.71

		51.4		3920		1.7				52.2		4170		1.73				52		3980		1.72				51.6		4230		1.71				51.9		4160		1.72

		51.5		3930		1.71				52.3		4180		1.74				52		3980		1.72				51.7		4240		1.72				52		4160		1.72

		51.6		3930		1.71				52.3		4180		1.74				52.1		3990		1.73				51.7		4240		1.72				52		4170		1.72

		51.7		3940		1.71				52.4		4190		1.74				52.2		3990		1.73				51.8		4250		1.72				52.1		4170		1.72

		51.7		3940		1.72				52.5		4190		1.74				52.3		4000		1.73				51.9		4250		1.72				52.2		4170		1.72

		51.8		3950		1.72				52.5		4190		1.74				52.4		4000		1.73				51.9		4250		1.72				52.2		4180		1.73

		51.8		3950		1.72				52.6		4200		1.75				52.4		4010		1.74				52		4260		1.73				52.3		4180		1.73

		51.9		3960		1.72				52.7		4210		1.75				52.5		4010		1.74				52.1		4260		1.73				52.4		4190		1.73

		52		3960		1.72				52.8		4210		1.75				52.5		4020		1.74				52.2		4270		1.73				52.5		4200		1.73

		52.1		3960		1.73				52.8		4220		1.75				52.6		4020		1.74				52.3		4280		1.74				52.5		4200		1.74

		52.1		3970		1.73				52.9		4220		1.76				52.7		4030		1.74				52.3		4280		1.74				52.6		4210		1.74

		52.2		3970		1.73				53		4230		1.76				52.7		4030		1.75				52.4		4290		1.74				52.7		4210		1.74

		52.3		3980		1.73				53		4230		1.76				52.8		4040		1.75				52.5		4290		1.74				52.7		4210		1.74

		52.3		3980		1.73				53.1		4230		1.76				52.9		4040		1.75				52.5		4300		1.74				52.8		4220		1.74

		52.4		3990		1.74				53.2		4240		1.77				52.9		4050		1.75				52.5		4300		1.75				52.8		4220		1.75

		52.4		3990		1.74				53.2		4240		1.77				53		4050		1.76				52.6		4310		1.75				52.9		4230		1.75

		52.5		4000		1.74				53.3		4250		1.77				53		4060		1.76				52.7		4310		1.75				53		4230		1.75

		52.6		4000		1.74				53.4		4250		1.77				53.1		4060		1.76				52.8		4320		1.75				53.1		4240		1.75

		52.7		4000		1.75				53.4		4260		1.77				53.2		4070		1.76				52.9		4320		1.75				53.1		4240		1.76

		52.8		4010		1.75				53.5		4260		1.78				53.2		4070		1.76				52.9		4330		1.76				53.2		4250		1.76

		52.8		4020		1.75				53.6		4270		1.78				53.3		4070		1.77				53		4330		1.76				53.2		4250		1.76

		52.9		4020		1.75				53.6		4270		1.78				53.4		4080		1.77				53		4330		1.76				53.3		4260		1.76

		53		4030		1.76				53.7		4270		1.78				53.5		4090		1.77				53.1		4340		1.76				53.4		4260		1.76

		53		4030		1.76				53.8		4280		1.79				53.5		4090		1.77				53.2		4340		1.77				53.4		4260		1.77

		53.1		4030		1.76				53.9		4290		1.79				53.6		4100		1.78				53.3		4350		1.77				53.5		4270		1.77

		53.2		4040		1.76				54		4290		1.79				53.7		4100		1.78				53.3		4360		1.77				53.5		4270		1.77

		53.2		4040		1.76				54		4300		1.79				53.7		4110		1.78				53.4		4360		1.77				53.7		4280		1.77

		53.3		4050		1.77				54		4300		1.79				53.8		4110		1.78				53.5		4370		1.78				53.7		4290		1.78

		53.3		4050		1.77				54.1		4310		1.8				53.9		4110		1.79				53.5		4370		1.78				53.8		4290		1.78

		53.4		4060		1.77				54.5		4330		1.81				54		4120		1.79				53.6		4380		1.78				53.8		4300		1.78

		53.5		4060		1.77				54.5		4330		1.81				54		4130		1.79				53.6		4380		1.78				53.9		4300		1.78

		53.5		4060		1.78				54.6		4340		1.81				54.1		4130		1.79				53.7		4390		1.78				54		4300		1.78

		53.6		4070		1.78				54.6		4340		1.81				54.2		4140		1.8				53.8		4390		1.79				54		4310		1.79

		53.7		4070		1.78				54.7		4350		1.82				54.3		4140		1.8				53.9		4400		1.79				54.1		4310		1.79

		53.7		4080		1.78				54.7		4350		1.82				54.3		4150		1.8				54		4400		1.79				54.2		4320		1.79

		53.8		4080		1.78				54.8		4350		1.82				54.4		4150		1.8				54		4410		1.79				54.3		4330		1.79

		53.9		4090		1.79				54.9		4360		1.82				54.4		4150		1.8				54.1		4410		1.8				54.3		4330		1.8

		54		4090		1.79				55		4370		1.83				54.5		4160		1.81				54.1		4420		1.8				54.4		4340		1.8

		54.1		4100		1.79				55		4370		1.83				54.6		4170		1.81				54.2		4420		1.8				54.5		4340		1.8

		54.1		4100		1.79				55.1		4370		1.83				54.7		4170		1.81				54.3		4430		1.8				54.5		4350		1.8

		54.2		4110		1.8				55.2		4380		1.83				54.7		4180		1.81				54.3		4430		1.8				54.6		4350		1.8

		54.2		4110		1.8				55.3		4380		1.83				54.8		4180		1.82				54.5		4440		1.81				54.7		4350		1.81

		54.3		4110		1.8				55.3		4390		1.84				54.9		4180		1.82				54.5		4450		1.81				54.8		4360		1.81

		54.3		4120		1.8				55.4		4390		1.84				54.9		4190		1.82				54.6		4450		1.81				54.8		4370		1.81

		54.4		4120		1.8				55.4		4400		1.84				55		4190		1.82				54.6		4450		1.82				54.9		4370		1.81

		54.5		4130		1.81				55.5		4400		1.84				55.1		4200		1.82				54.7		4460		1.82				55		4370		1.82

		54.6		4130		1.81				55.6		4410		1.85				55.1		4200		1.83				54.8		4460		1.82				55		4380		1.82

		54.6		4140		1.81				55.7		4410		1.85				55.2		4210		1.83				54.8		4470		1.82				55.1		4380		1.82

		54.7		4140		1.81				55.8		4420		1.85				55.3		4210		1.83				54.9		4470		1.82				55.1		4390		1.82

		54.7		4150		1.82				55.8		4420		1.85				55.3		4220		1.83				55		4480		1.83				55.2		4390		1.82

		54.8		4150		1.82				55.9		4430		1.86				55.4		4220		1.84				55		4480		1.83				55.2		4400		1.83

		54.9		4150		1.82				55.9		4430		1.86				55.4		4230		1.84				55.1		4490		1.83				55.3		4400		1.83

		54.9		4160		1.82				56		4440		1.86				55.5		4230		1.84				55.2		4490		1.83				55.4		4410		1.83

		55		4160		1.82				56		4440		1.86				55.6		4240		1.84				55.2		4500		1.83				55.5		4410		1.83

		55.1		4170		1.83				56.1		4440		1.86				55.6		4240		1.84				55.3		4500		1.84				55.5		4420		1.84

		55.2		4170		1.83				56.2		4450		1.87				55.8		4250		1.85				55.4		4510		1.84				55.6		4420		1.84

		55.2		4180		1.83				56.3		4460		1.87				55.9		4250		1.85				55.5		4510		1.84				55.6		4430		1.84

		55.3		4180		1.83				56.4		4460		1.87				55.9		4260		1.85				55.5		4520		1.84				55.7		4430		1.84

		55.4		4190		1.84				56.4		4470		1.87				56		4260		1.85				55.6		4520		1.85				55.8		4440		1.84

		55.4		4190		1.84				56.5		4470		1.88				56		4270		1.86				55.6		4530		1.85				55.8		4440		1.85

		55.5		4190		1.84				56.5		4470		1.88				56.1		4270		1.86				55.7		4530		1.85				56		4450		1.85

		55.6		4200		1.84				56.6		4480		1.88				56.2		4270		1.86				55.8		4540		1.85				56		4450		1.85

		55.7		4200		1.85				56.7		4480		1.88				56.2		4280		1.86				55.8		4540		1.85				56.1		4460		1.85

		55.7		4210		1.85				56.7		4490		1.88				56.3		4290		1.87				55.9		4550		1.86				56.1		4460		1.86

		55.7		4210		1.85				56.9		4500		1.89				56.4		4290		1.87				56		4550		1.86				56.2		4470		1.86

		55.8		4220		1.85				56.9		4500		1.89				56.4		4290		1.87				56		4560		1.86				56.3		4470		1.86

		55.9		4220		1.85				57		4510		1.89				56.5		4300		1.87				56.1		4560		1.86				56.3		4480		1.86

		56		4230		1.86				57		4510		1.9				56.5		4300		1.87				56.2		4570		1.87				56.4		4480		1.87

		56		4230		1.86				57.1		4510		1.9				56.6		4310		1.88				56.2		4570		1.87				56.5		4490		1.87

		56.1		4230		1.86				57.2		4520		1.9				56.7		4310		1.88				56.3		4580		1.87				56.6		4490		1.87

		56.2		4240		1.86				57.3		4520		1.9				56.7		4320		1.88				56.4		4580		1.87				56.6		4500		1.87

		56.2		4240		1.86				57.3		4530		1.9				56.8		4320		1.88				56.4		4590		1.87				56.7		4500		1.88

		56.3		4250		1.87				57.4		4540		1.91				56.9		4330		1.89				56.5		4590		1.88				56.8		4510		1.88

		56.4		4250		1.87				57.5		4540		1.91				57		4330		1.89				56.6		4590		1.88				56.9		4510		1.88

		56.4		4260		1.87				57.5		4540		1.91				57		4340		1.89				56.7		4600		1.88				56.9		4520		1.88

		56.5		4260		1.87				57.6		4550		1.91				57.1		4340		1.89				56.7		4610		1.88				57		4520		1.88

		56.5		4270		1.88				57.7		4550		1.92				57.2		4350		1.9				56.8		4610		1.89				57		4530		1.89

		56.6		4270		1.88				57.7		4560		1.92				57.2		4350		1.9				56.8		4620		1.89				57.1		4530		1.89

		56.7		4280		1.88				57.8		4560		1.92				57.3		4350		1.9				56.9		4620		1.89				57.2		4540		1.89

		56.8		4280		1.88				57.9		4570		1.92				57.3		4360		1.9				57		4630		1.89				57.3		4540		1.89

		56.9		4290		1.89				57.9		4570		1.93				57.4		4360		1.9				57		4630		1.89				57.3		4550		1.9

		56.9		4290		1.89				58		4580		1.93				57.6		4370		1.91				57.1		4630		1.9				57.4		4550		1.9

		57		4290		1.89				58.1		4580		1.93				57.6		4380		1.91				57.2		4640		1.9				57.5		4560		1.9

		57		4300		1.89				58.1		4590		1.93				57.7		4380		1.91				57.3		4650		1.9				57.5		4560		1.9

		57.1		4300		1.89				58.2		4590		1.93				57.7		4390		1.91				57.3		4650		1.9				57.6		4560		1.9

		57.1		4300		1.9				58.3		4590		1.94				57.8		4390		1.92				57.4		4660		1.91				57.6		4570		1.91

		57.3		4300		1.9				58.3		4600		1.94				57.9		4390		1.92				57.4		4660		1.91				57.7		4570		1.91

		57.4		4300		1.9				58.4		4600		1.94				57.9		4400		1.92				57.5		4670		1.91				57.7		4580		1.91

		57.4		4310		1.9				58.4		4610		1.94				58		4400		1.92				57.6		4670		1.91				57.8		4580		1.91

		57.5		4310		1.91				58.6		4620		1.95				58.1		4410		1.93				57.6		4680		1.92				57.9		4590		1.91

		57.6		4310		1.91				58.7		4620		1.95				58.1		4410		1.93				57.8		4690		1.92				57.9		4590		1.92

		57.6		4320		1.91				58.7		4620		1.95				58.2		4420		1.93				57.9		4690		1.92				58		4600		1.92

		57.7		4320		1.91				58.8		4630		1.95				58.3		4420		1.93				57.9		4700		1.92				58		4600		1.92

		57.7		4320		1.91				58.8		4630		1.95				58.3		4430		1.93				58		4700		1.93				58.1		4610		1.92

		57.9		4330		1.92				58.9		4640		1.96				58.4		4430		1.94				58		4700		1.93				58.3		4610		1.93

		57.9		4330		1.92				58.9		4640		1.96				58.5		4440		1.94				58.1		4710		1.93				58.3		4620		1.93

		58		4340		1.92				59		4650		1.96				58.5		4440		1.94				58.1		4710		1.93				58.4		4620		1.93

		58.1		4340		1.93				59.1		4650		1.96				58.6		4440		1.94				58.2		4720		1.93				58.5		4630		1.93

		58.1		4340		1.93				59.2		4660		1.97				58.7		4450		1.95				58.3		4720		1.94				58.5		4630		1.94

		58.1		4350		1.93				59.3		4660		1.97				58.7		4460		1.95				58.4		4730		1.94				58.5		4640		1.94

		58.2		4350		1.93				59.3		4670		1.97				58.8		4460		1.95				58.4		4740		1.94				58.6		4640		1.94

		58.3		4350		1.93				59.4		4670		1.97				58.9		4460		1.95				58.5		4740		1.94				58.7		4650		1.94

		58.4		4360		1.94				59.5		4680		1.98				58.9		4470		1.95				58.6		4750		1.95				58.8		4660		1.95

		58.5		4360		1.94				59.5		4680		1.98				59		4470		1.96				58.6		4750		1.95				58.9		4660		1.95

		58.5		4370		1.94				59.6		4680		1.98				59		4480		1.96				58.7		4760		1.95				59		4660		1.95

		58.6		4370		1.94				59.6		4690		1.98				59.1		4480		1.96				58.8		4760		1.95				59		4670		1.95

		58.6		4370		1.95				59.7		4700		1.98				59.2		4490		1.96				58.8		4760		1.95				59		4670		1.95

		58.7		4380		1.95				59.8		4700		1.99				59.3		4490		1.97				58.9		4770		1.96				59.1		4680		1.96

		58.8		4380		1.95				59.8		4700		1.99				59.3		4500		1.97				59		4780		1.96				59.2		4680		1.96

		58.9		4380		1.95				59.9		4710		1.99				59.4		4500		1.97				59.1		4780		1.96				59.2		4690		1.96

		59		4360		1.96				60		4710		1.99				59.4		4510		1.97				59.1		4790		1.96				59.3		4690		1.96

		59.1		4360		1.96				60		4720		1.99				59.5		4510		1.97				59.2		4790		1.97				59.4		4700		1.97

		59.1		4360		1.96				60.1		4720		2				59.6		4520		1.98				59.3		4800		1.97				59.5		4700		1.97

		59.1		4360		1.96				60.2		4730		2				59.6		4520		1.98				59.4		4800		1.97				59.5		4710		1.97

		59.2		4360		1.96				60.3		4730		2				59.7		4520		1.98				59.4		4810		1.97				59.6		4710		1.97

		59.3		4330		1.97				60.3		4740		2				59.8		4530		1.98				59.4		4810		1.98				59.7		4720		1.97

		59.3		4300		1.97				60.4		4740		2.01				59.9		4540		1.98				59.6		4820		1.98				59.7		4720		1.98

		59.4		4290		1.97				60.4		4750		2.01				59.9		4540		1.99				59.7		4830		1.98				59.8		4730		1.98

		59.5		4280		1.98				60.5		4750		2.01				60		4540		1.99				59.7		4830		1.98				59.8		4730		1.98

		59.6		4280		1.98				60.6		4760		2.01				60.1		4550		1.99				59.8		4840		1.99				60		4740		1.98

		59.7		4270		1.98				60.7		4760		2.01				60.1		4550		1.99				59.8		4840		1.99				60		4740		1.99

		59.7		4200		1.98				60.7		4760		2.02				60.2		4560		2				59.9		4840		1.99				60.1		4750		1.99

		59.8		4160		1.98				60.8		4770		2.02				60.2		4560		2				60		4850		1.99				60.1		4750		1.99

		59.9		4150		1.99				60.9		4780		2.02				60.3		4570		2				60		4850		1.99				60.2		4760		1.99

		59.9		4140		1.99				60.9		4780		2.03				60.4		4580		2				60.1		4860		2				60.3		4760		1.99

		60		4130		1.99				61		4790		2.03				60.5		4580		2.01				60.2		4870		2				60.4		4770		2

		60.1		4080		1.99				61.1		4790		2.03				60.5		4590		2.01				60.3		4870		2				60.4		4770		2

		60.2		3970		2				61.1		4800		2.03				60.6		4590		2.01				60.3		4870		2				60.5		4780		2

		60.2		3900		2				61.2		4800		2.03				60.7		4590		2.01				60.3		4880		2.01				60.6		4780		2

		60.3		3880		2				61.3		4800		2.04				60.7		4600		2.01				60.4		4880		2.01				60.6		4790		2.01

		60.3		3850		2				61.3		4810		2.04				60.8		4600		2.02				60.5		4890		2.01				60.7		4790		2.01

		60.4		3840		2				61.4		4810		2.04				60.8		4610		2.02				60.6		4890		2.01				60.7		4800		2.01

		60.5		3840		2.01				61.5		4820		2.04				61		4610		2.02				60.7		4900		2.02				60.8		4800		2.01

		60.6		3840		2.01				61.6		4820		2.04				61		4620		2.02				60.8		4910		2.02				60.9		4810		2.01

		60.6		3840		2.01				61.6		4830		2.05				61.1		4620		2.03				60.8		4910		2.02				61		4810		2.02

		60.7		3840		2.01				61.7		4830		2.05				61.2		4630		2.03				60.9		4920		2.02				61		4810		2.02

		60.8		3840		2.02				61.8		4840		2.05				61.2		4630		2.03				60.9		4920		2.02				61.1		4820		2.02

		60.9		3840		2.02				61.8		4840		2.05				61.3		4640		2.03				61		4930		2.03				61.1		4830		2.02

		60.9		3850		2.02				61.8		4850		2.06				61.3		4640		2.03				61.1		4930		2.03				61.2		4830		2.03

		61		3850		2.02				61.9		4850		2.06				61.4		4640		2.04				61.1		4930		2.03				61.3		4840		2.03

		61		3850		2.03				62		4850		2.06				61.5		4650		2.04				61.2		4940		2.03				61.4		4840		2.03

		61.1		3860		2.03				62		4860		2.06				61.5		4660		2.04				61.3		4950		2.04				61.4		4840		2.03

		61.2		3860		2.03				62.1		4860		2.06				61.6		4660		2.04				61.3		4950		2.04				61.5		4850		2.03

		61.3		3860		2.03				62.2		4870		2.07				61.7		4660		2.05				61.4		4960		2.04				61.5		4850		2.04

		61.3		3870		2.04				62.3		4870		2.07				61.7		4670		2.05				61.4		4960		2.04				61.6		4860		2.04

		61.4		3870		2.04				62.3		4880		2.07				61.8		4670		2.05				61.5		4970		2.04				61.7		4870		2.04

		61.5		3870		2.04				62.4		4880		2.07				61.8		4680		2.05				61.6		4970		2.05				61.8		4870		2.04

		61.5		3870		2.04				62.4		4880		2.07				61.9		4680		2.05				61.6		4980		2.05				61.9		4880		2.05

		61.6		3880		2.04				62.5		4890		2.08				62		4690		2.06				61.7		4980		2.05				61.9		4880		2.05

		61.7		3880		2.05				62.6		4900		2.08				62.1		4700		2.06				61.8		4990		2.05				62		4890		2.05

		61.7		3890		2.05				62.7		4900		2.08				62.2		4700		2.06				61.8		4990		2.06				62		4890		2.05

		61.8		3890		2.05				62.7		4910		2.08				62.2		4700		2.06				61.9		5000		2.06				62.1		4900		2.05

		61.9		3890		2.05				62.8		4910		2.09				62.3		4710		2.07				62		5000		2.06				62.1		4900		2.06

		62		3890		2.06				62.9		4910		2.09				62.3		4710		2.07				62.1		5010		2.06				62.3		4910		2.06

		62		3900		2.06				62.9		4920		2.09				62.4		4720		2.07				62.1		5010		2.06				62.3		4910		2.06

		62		3900		2.06				63		4920		2.09				62.5		4720		2.07				62.2		5010		2.07				62.4		4920		2.07

		62.1		3900		2.06				63		4930		2.09				62.5		4730		2.07				62.2		5020		2.07				62.4		4920		2.07

		62.2		3910		2.06				63.2		4940		2.1				62.6		4730		2.08				62.3		5020		2.07				62.5		4930		2.07

		62.3		3920		2.07				63.2		4940		2.1				62.7		4740		2.08				62.3		5030		2.07				62.6		4930		2.07

		62.4		3920		2.07				63.3		4950		2.1				62.8		4750		2.08				62.4		5030		2.07				62.6		4940		2.07

		62.4		3920		2.07				63.3		4950		2.11				62.9		4750		2.08				62.5		5040		2.08				62.7		4940		2.08

		62.5		3930		2.07				63.4		4950		2.11				62.9		4750		2.09				62.5		5040		2.08				62.8		4950		2.08

		62.5		3930		2.08				63.5		4960		2.11				63		4760		2.09				62.6		5050		2.08				62.9		4950		2.08

		62.6		3930		2.08				63.6		4960		2.11				63		4760		2.09				62.7		5050		2.08				62.9		4960		2.08

		62.7		3940		2.08				63.6		4970		2.11				63.1		4770		2.09				62.7		5060		2.08				63		4960		2.09

		62.8		3940		2.08				63.7		4970		2.12				63.2		4770		2.1				62.8		5060		2.09				63.1		4970		2.09

		62.8		3940		2.08				63.7		4980		2.12				63.3		4780		2.1				62.9		5070		2.09				63.2		4970		2.09

		62.9		3950		2.09				63.8		4980		2.12				63.3		4780		2.1				63		5070		2.09				63.2		4980		2.09

		63		3960		2.09				63.9		4990		2.12				63.4		4790		2.1				63		5080		2.09				63.3		4980		2.09

		63		3960		2.09				63.9		4990		2.12				63.5		4790		2.11				63.1		5080		2.1				63.4		4990		2.1

		63.1		3960		2.09				64		5000		2.13				63.5		4800		2.11				63.2		5090		2.1				63.4		4990		2.1

		63.2		3970		2.1				64.1		5000		2.13				63.6		4800		2.11				63.3		5090		2.1				63.5		5000		2.1

		63.3		3970		2.1				64.1		5000		2.13				63.7		4810		2.11				63.3		5100		2.1				63.5		5000		2.1

		63.3		3980		2.1				64.2		5010		2.13				63.7		4810		2.11				63.3		5100		2.11				63.6		5010		2.11

		63.4		3980		2.1				64.2		5010		2.13				63.8		4820		2.12				63.4		5110		2.11				63.7		5010		2.11

		63.4		3980		2.11				64.3		5020		2.14				63.9		4820		2.12				63.5		5120		2.11				63.8		5020		2.11

		63.5		3990		2.11				64.4		5020		2.14				64		4830		2.12				63.6		5120		2.11				63.8		5020		2.11

		63.6		3990		2.11				64.5		5030		2.14				64		4830		2.12				63.7		5130		2.11				63.9		5030		2.12

		63.7		4000		2.11				64.6		5030		2.14				64.1		4840		2.13				63.7		5130		2.12				64		5040		2.12

		63.8		4000		2.12				64.6		5040		2.15				64.2		4840		2.13				63.7		5140		2.12				64.1		5040		2.12

		63.8		4010		2.12				64.7		5040		2.15				64.2		4850		2.13				63.8		5140		2.12				64.1		5050		2.12

		63.9		4010		2.12				64.7		5050		2.15				64.3		4850		2.13				63.9		5140		2.12				64.2		5050		2.12

		64		4010		2.12				64.8		5050		2.15				64.4		4860		2.13				64		5150		2.12				64.2		5050		2.13

		64		4020		2.12				64.9		5050		2.16				64.4		4860		2.14				64		5160		2.13				64.3		5060		2.13

		64.1		4020		2.13				65		5060		2.16				64.5		4870		2.14				64.1		5160		2.13				64.4		5060		2.13

		64.1		4030		2.13				65		5070		2.16				64.6		4870		2.14				64.2		5170		2.13				64.5		5070		2.13

		64.2		4030		2.13				65.1		5070		2.16				64.6		4880		2.14				64.2		5170		2.13				64.5		5070		2.13

		64.3		4030		2.13				65.2		5080		2.17				64.7		4880		2.15				64.3		5180		2.14				64.6		5080		2.14

		64.3		4040		2.13				65.2		5080		2.17				64.7		4890		2.15				64.3		5180		2.14				64.6		5080		2.14

		64.4		4040		2.14				65.3		5080		2.17				64.8		4890		2.15				64.4		5180		2.14				64.7		5090		2.14

		64.5		4050		2.14				65.3		5090		2.17				64.9		4890		2.15				64.5		5190		2.14				64.8		5090		2.14

		64.5		4050		2.14				65.4		5090		2.17				65		4900		2.16				64.5		5190		2.14				64.9		5100		2.15

		64.6		4060		2.14				65.5		5100		2.18				65.1		4910		2.16				64.7		5200		2.15				64.9		5100		2.15

		64.7		4060		2.15				65.6		5100		2.18				65.1		4910		2.16				64.7		5210		2.15				65		5110		2.15

		64.7		4060		2.15				65.6		5110		2.18				65.1		4910		2.16				64.8		5210		2.15				65.1		5120		2.15

		64.8		4070		2.15				65.7		5110		2.18				65.2		4920		2.16				64.9		5220		2.16				65.2		5120		2.16

		64.9		4070		2.15				65.7		5120		2.19				65.3		4920		2.17				64.9		5220		2.16				65.2		5130		2.16

		64.9		4080		2.16				65.8		5120		2.19				65.4		4930		2.17				65		5230		2.16				65.3		5130		2.16

		65		4080		2.16				65.9		5130		2.19				65.4		4930		2.17				65.1		5230		2.16				65.3		5130		2.16

		65.1		4080		2.16				65.9		5130		2.19				65.6		4940		2.17				65.1		5240		2.16				65.4		5140		2.16

		65.1		4090		2.16				66		5140		2.19				65.6		4950		2.18				65.2		5240		2.17				65.4		5140		2.17

		65.2		4090		2.16				66.1		5140		2.2				65.6		4950		2.18				65.3		5250		2.17				65.6		5150		2.17

		65.3		4090		2.17				66.2		5150		2.2				65.7		4950		2.18				65.4		5260		2.17				65.6		5160		2.17

		65.3		4100		2.17				66.3		5150		2.2				65.8		4960		2.18				65.4		5260		2.17				65.7		5160		2.18

		65.4		4100		2.17				66.3		5160		2.2				65.9		4960		2.18				65.5		5270		2.18				65.8		5170		2.18

		65.4		4110		2.17				66.4		5160		2.21				65.9		4970		2.19				65.6		5270		2.18				65.8		5170		2.18

		65.5		4110		2.17				66.5		5170		2.21				66		4970		2.19				65.6		5270		2.18				65.9		5180		2.18

		65.6		4110		2.18				66.5		5170		2.21				66.1		4980		2.19				65.7		5280		2.18				65.9		5180		2.18

		65.6		4120		2.18				66.6		5180		2.21				66.1		4980		2.19				65.7		5280		2.18				66		5190		2.19

		65.8		4120		2.18				66.6		5180		2.22				66.2		4990		2.2				65.9		5290		2.19				66.1		5190		2.19

		65.8		4130		2.18				66.7		5190		2.22				66.3		4990		2.2				65.9		5300		2.19				66.2		5200		2.19

		65.9		4130		2.19				66.8		5190		2.22				66.3		5000		2.2				66		5300		2.19				66.3		5200		2.19

		65.9		4140		2.19				66.8		5200		2.22				66.4		5000		2.2				66.1		5310		2.19				66.3		5210		2.2

		66		4140		2.19				66.9		5200		2.22				66.5		5010		2.2				66.1		5310		2.2				66.4		5210		2.2

		66		4140		2.19				67		5200		2.23				66.5		5010		2.21				66.2		5320		2.2				66.4		5220		2.2

		66.1		4150		2.19				67		5210		2.23				66.6		5020		2.21				66.2		5320		2.2				66.5		5220		2.2

		66.2		4150		2.2				67.1		5210		2.23				66.6		5020		2.21				66.3		5330		2.2				66.6		5230		2.2

		66.3		4160		2.2				67.1		5220		2.23				66.7		5030		2.21				66.4		5340		2.21				66.6		5230		2.21

		66.4		4160		2.2				67.2		5220		2.24				66.8		5030		2.22				66.5		5340		2.21				66.8		5240		2.21

		66.4		4170		2.2				67.3		5230		2.24				66.9		5040		2.22				66.5		5350		2.21				66.8		5250		2.21

		66.4		4170		2.21				67.4		5230		2.24				66.9		5040		2.22				66.6		5350		2.21				66.9		5250		2.21

		66.5		4170		2.21				67.4		5240		2.24				67		5050		2.22				66.7		5350		2.22				67		5260		2.22

		66.6		4180		2.21				67.5		5240		2.24				67		5050		2.22				66.7		5360		2.22				67		5260		2.22

		66.7		4180		2.21				67.6		5250		2.25				67.1		5050		2.23				66.8		5360		2.22				67.1		5260		2.22

		66.7		4180		2.21				67.6		5250		2.25				67.2		5060		2.23				66.8		5370		2.22				67.1		5270		2.22

		66.9		4190		2.22				67.7		5250		2.25				67.2		5060		2.23				66.9		5370		2.22				67.2		5270		2.23

		66.9		4200		2.22				67.8		5260		2.25				67.3		5070		2.23				67.1		5380		2.23				67.3		5280		2.23

		66.9		4200		2.22				67.9		5270		2.26				67.4		5070		2.24				67.1		5390		2.23				67.4		5290		2.23

		67		4200		2.22				67.9		5270		2.26				67.4		5080		2.24				67.2		5390		2.23				67.4		5290		2.23

		67.1		4210		2.23				68		5280		2.26				67.5		5080		2.24				67.2		5400		2.23				67.5		5290		2.23

		67.2		4210		2.23				68		5280		2.26				67.6		5090		2.24				67.3		5400		2.24				67.5		5300		2.24

		67.2		4210		2.23				68.1		5280		2.26				67.6		5090		2.24				67.3		5410		2.24				67.6		5300		2.24

		67.3		4220		2.23				68.2		5290		2.27				67.8		5100		2.25				67.4		5410		2.24				67.7		5310		2.24

		67.4		4220		2.24				68.2		5290		2.27				67.8		5110		2.25				67.5		5410		2.24				67.8		5310		2.24

		67.4		4230		2.24				68.3		5300		2.27				67.9		5110		2.25				67.6		5420		2.25				67.8		5320		2.24

		67.5		4230		2.24				68.4		5300		2.27				67.9		5110		2.25				67.6		5430		2.25				67.8		5320		2.25

		67.5		4230		2.24				68.4		5310		2.27				68		5120		2.26				67.7		5430		2.25				68		5330		2.25

		67.6		4240		2.24				68.5		5310		2.28				68.1		5130		2.26				67.8		5440		2.25				68.1		5340		2.25

		67.7		4240		2.25				68.6		5320		2.28				68.1		5130		2.26				67.9		5440		2.25				68.1		5340		2.26

		67.7		4240		2.25				68.6		5320		2.28				68.2		5130		2.26				67.9		5450		2.26				68.2		5340		2.26

		67.8		4250		2.25				68.7		5330		2.28				68.2		5140		2.26				68		5450		2.26				68.3		5350		2.26

		67.9		4250		2.25				68.7		5330		2.29				68.4		5150		2.27				68.1		5460		2.26				68.3		5350		2.26

		67.9		4260		2.26				68.8		5340		2.29				68.4		5150		2.27				68.1		5470		2.26				68.4		5360		2.26

		68		4250		2.26				68.9		5340		2.29				68.5		5160		2.27				68.2		5470		2.27				68.4		5360		2.27

		68.1		4240		2.26				68.9		5340		2.29				68.5		5160		2.28				68.2		5470		2.27				68.5		5370		2.27

		68.1		4250		2.26				69.1		5350		2.3				68.6		5170		2.28				68.3		5480		2.27				68.6		5380		2.27

		68.2		4250		2.26				69.1		5360		2.3				68.7		5170		2.28				68.4		5480		2.27				68.7		5380		2.27

		68.3		4260		2.27				69.2		5360		2.3				68.8		5180		2.28				68.4		5490		2.27				68.8		5390		2.28

		68.4		4260		2.27				69.2		5360		2.3				68.8		5180		2.28				68.5		5490		2.28				68.8		5390		2.28

		68.4		4260		2.27				69.3		5370		2.3				68.9		5190		2.29				68.6		5500		2.28				68.9		5390		2.28

		68.5		4270		2.27				69.4		5370		2.31				69		5190		2.29				68.7		5500		2.28				68.9		5400		2.28

		68.5		4280		2.28				69.4		5380		2.31				69		5200		2.29				68.7		5510		2.28				69		5400		2.28

		68.6		4280		2.28				69.5		5380		2.31				69.1		5200		2.29				68.8		5510		2.29				69.1		5410		2.29

		68.7		4280		2.28				69.6		5390		2.31				69.1		5200		2.29				68.8		5520		2.29				69.2		5410		2.29

		68.8		4290		2.28				69.7		5390		2.32				69.2		5210		2.3				68.9		5520		2.29				69.2		5420		2.29

		68.8		4290		2.28				69.7		5400		2.32				69.3		5210		2.3				69		5530		2.29				69.3		5420		2.29

		68.8		4300		2.29				69.8		5400		2.32				69.3		5220		2.3				69		5530		2.29				69.4		5430		2.3

		68.9		4300		2.29				69.8		5410		2.32				69.4		5220		2.3				69.1		5540		2.3				69.4		5430		2.3

		69.1		4310		2.29				69.9		5410		2.32				69.5		5230		2.31				69.2		5540		2.3				69.5		5440		2.3

		69.1		4310		2.29				70		5420		2.33				69.6		5240		2.31				69.3		5550		2.3				69.5		5440		2.3

		69.2		4320		2.3				70		5420		2.33				69.6		5240		2.31				69.3		5550		2.3				69.7		5450		2.31

		69.3		4320		2.3				70.1		5420		2.33				69.7		5250		2.31				69.4		5560		2.31				69.7		5460		2.31

		69.3		4320		2.3				70.2		5430		2.33				69.8		5250		2.32				69.4		5560		2.31				69.8		5460		2.31

		69.3		4330		2.3				70.2		5440		2.33				69.8		5260		2.32				69.5		5570		2.31				69.8		5470		2.31

		69.4		4330		2.31				70.3		5440		2.34				69.9		5260		2.32				69.6		5570		2.31				69.9		5470		2.32

		69.5		4340		2.31				70.4		5440		2.34				70		5260		2.32				69.6		5580		2.31				70		5470		2.32

		69.6		4340		2.31				70.4		5450		2.34				70.1		5270		2.33				69.7		5580		2.32				70		5480		2.32

		69.6		4340		2.31				70.5		5450		2.34				70.1		5280		2.33				69.8		5590		2.32				70.1		5480		2.32

		69.7		4350		2.31				70.5		5460		2.35				70.2		5280		2.33				69.9		5600		2.32				70.2		5490		2.32

		69.7		4350		2.32				70.6		5460		2.35				70.3		5290		2.33				70		5600		2.32				70.2		5490		2.33

		69.8		4350		2.32				70.7		5470		2.35				70.3		5290		2.33				70		5610		2.33				70.3		5500		2.33

		69.8		4360		2.32				70.8		5470		2.35				70.4		5300		2.34				70.1		5610		2.33				70.4		5500		2.33

		69.9		4360		2.32				70.8		5480		2.35				70.5		5300		2.34				70.1		5610		2.33				70.4		5510		2.33

		70		4370		2.32				70.9		5480		2.36				70.5		5310		2.34				70.2		5620		2.33				70.5		5510		2.34

		70.1		4370		2.33				71		5480		2.36				70.6		5310		2.34				70.2		5620		2.34				70.6		5510		2.34

		70.1		4370		2.33				71		5490		2.36				70.7		5320		2.35				70.3		5630		2.34				70.6		5520		2.34

		70.2		4370		2.33				71.1		5490		2.36				70.8		5320		2.35				70.5		5640		2.34				70.7		5520		2.34

		70.3		4370		2.33				71.1		5500		2.36				70.8		5330		2.35				70.5		5640		2.34				70.8		5530		2.35

		70.3		4370		2.34				71.2		5500		2.37				70.9		5330		2.35				70.6		5650		2.35				70.9		5540		2.35

		70.4		4380		2.34				71.3		5510		2.37				71		5340		2.36				70.6		5650		2.35				71		5540		2.35

		70.4		4380		2.34				71.4		5520		2.37				71		5340		2.36				70.7		5660		2.35				71		5550		2.35

		70.5		4380		2.34				71.5		5520		2.38				71.1		5350		2.36				70.8		5660		2.35				71.1		5550		2.35

		70.6		4390		2.34				71.5		5520		2.38				71.1		5350		2.36				70.8		5670		2.35				71.1		5560		2.36

		70.6		4390		2.35				71.6		5530		2.38				71.3		5360		2.36				70.9		5670		2.36				71.2		5560		2.36

		70.7		4390		2.35				71.6		5530		2.38				71.3		5360		2.37				71		5680		2.36				71.2		5570		2.36

		70.8		4400		2.35				71.7		5540		2.38				71.4		5370		2.37				71.1		5690		2.36				71.3		5570		2.36

		70.9		4410		2.35				71.8		5540		2.39				71.5		5370		2.37				71.1		5690		2.36				71.4		5580		2.37

		71		4410		2.36				71.9		5550		2.39				71.5		5380		2.37				71.2		5700		2.37				71.5		5580		2.37

		71		4410		2.36				72		5560		2.39				71.5		5380		2.37				71.2		5700		2.37				71.5		5590		2.37

		71.1		4420		2.36				72		5560		2.39				71.6		5390		2.38				71.3		5700		2.37				71.6		5590		2.37

		71.1		4420		2.36				72.1		5570		2.4				71.7		5390		2.38				71.4		5710		2.37				71.7		5590		2.37

		71.2		4430		2.36				72.2		5570		2.4				71.8		5400		2.38				71.4		5710		2.37				71.7		5600		2.38

		71.3		4430		2.37				72.2		5570		2.4				71.9		5400		2.39				71.5		5720		2.38				71.8		5600		2.38

		71.4		4440		2.37				72.3		5580		2.4				71.9		5410		2.39				71.6		5730		2.38				71.9		5610		2.38

		71.4		4440		2.37				72.4		5580		2.4				72		5410		2.39				71.7		5730		2.38				71.9		5610		2.38

		71.5		4440		2.37				72.5		5590		2.41				72		5420		2.39				71.7		5740		2.38				72		5620		2.39

		71.6		4450		2.38				72.5		5600		2.41				72.1		5420		2.39				71.8		5740		2.39				72.1		5620		2.39

		71.7		4450		2.38				72.6		5600		2.41				72.2		5430		2.4				71.9		5750		2.39				72.1		5630		2.39

		71.7		4460		2.38				72.7		5610		2.41				72.2		5430		2.4				71.9		5750		2.39				72.2		5630		2.39

		71.8		4460		2.38				72.7		5610		2.42				72.3		5440		2.4				72		5750		2.39				72.2		5640		2.39

		71.8		4460		2.39				72.8		5610		2.42				72.4		5440		2.4				72		5760		2.39				72.3		5640		2.4

		71.9		4470		2.39				72.8		5620		2.42				72.5		5450		2.41				72.2		5770		2.4				72.4		5650		2.4

		72		4470		2.39				72.9		5620		2.42				72.5		5450		2.41				72.2		5770		2.4				72.5		5650		2.4

		72		4470		2.39				73		5630		2.43				72.6		5460		2.41				72.3		5780		2.4				72.5		5660		2.4

		72.1		4480		2.39				73		5630		2.43				72.7		5460		2.41				72.4		5780		2.4				72.6		5660		2.4

		72.2		4480		2.4				73.1		5640		2.43				72.8		5470		2.41				72.4		5790		2.41				72.7		5660		2.41

		72.3		4490		2.4				73.2		5640		2.43				72.8		5470		2.42				72.5		5790		2.41				72.7		5670		2.41

		72.3		4490		2.4				73.2		5650		2.43				72.9		5480		2.42				72.5		5800		2.41				72.7		5670		2.41

		72.4		4490		2.4				73.3		5650		2.44				72.9		5480		2.42				72.6		5800		2.41				72.8		5680		2.41

		72.4		4500		2.4				73.4		5660		2.44				73.1		5490		2.42				72.6		5810		2.42				72.9		5680		2.41

		72.5		4500		2.41				73.5		5660		2.44				73.1		5500		2.43				72.8		5810		2.42				73		5690		2.42

		72.6		4500		2.41				73.5		5670		2.44				73.2		5500		2.43				72.8		5820		2.42				73		5690		2.42

		72.7		4510		2.41				73.6		5670		2.45				73.2		5500		2.43				72.9		5820		2.42				73.1		5700		2.42

		72.7		4500		2.41				73.7		5680		2.45				73.3		5510		2.43				73		5830		2.43				73.1		5700		2.42

		72.8		4510		2.42				73.7		5680		2.45				73.4		5510		2.44				73		5830		2.43				73.2		5710		2.42

		72.8		4510		2.42				73.8		5690		2.45				73.4		5520		2.44				73.1		5840		2.43				73.2		5710		2.43

		72.9		4510		2.42				73.8		5690		2.45				73.5		5520		2.44				73.2		5840		2.43				73.3		5720		2.43

		72.9		4510		2.42				73.9		5690		2.46				73.5		5530		2.44				73.2		5850		2.43				73.4		5720		2.43

		73		4520		2.42				74		5700		2.46				73.7		5540		2.45				73.3		5850		2.44				73.4		5720		2.43

		73.1		4520		2.43				74		5700		2.46				73.7		5540		2.45				73.4		5860		2.44				73.5		5730		2.43

		73.2		4530		2.43				74.1		5710		2.46				73.8		5550		2.45				73.5		5870		2.44				73.6		5730		2.44

		73.2		4530		2.43				74.2		5720		2.47				73.9		5550		2.45				73.5		5870		2.44				73.7		5740		2.44

		73.3		4530		2.43				74.2		5720		2.47				73.9		5550		2.45				73.6		5880		2.45				73.7		5750		2.44

		73.3		4540		2.44				74.3		5720		2.47				74		5560		2.46				73.6		5880		2.45				73.8		5750		2.45

		73.4		4540		2.44				74.4		5730		2.47				74		5560		2.46				73.7		5890		2.45				73.9		5760		2.45

		73.5		4540		2.44				74.4		5730		2.47				74.1		5570		2.46				73.8		5890		2.45				73.9		5760		2.45

		73.6		4550		2.44				74.5		5740		2.48				74.2		5570		2.46				73.9		5900		2.45				74		5770		2.45

		73.7		4560		2.45				74.5		5740		2.48				74.3		5580		2.47				74		5910		2.46				74.1		5770		2.45

		73.7		4560		2.45				74.6		5750		2.48				74.4		5580		2.47				74		5910		2.46				74.1		5780		2.46

		73.8		4560		2.45				74.7		5750		2.48				74.4		5590		2.47				74.1		5920		2.46				74.2		5780		2.46

		73.9		4570		2.45				74.8		5760		2.49				74.4		5590		2.47				74.1		5920		2.47				74.3		5790		2.46

		73.9		4570		2.45				74.9		5760		2.49				74.5		5600		2.47				74.2		5930		2.47				74.4		5790		2.46

		74		4570		2.46				74.9		5770		2.49				74.6		5600		2.48				74.3		5930		2.47				74.4		5800		2.47

		74.1		4580		2.46				75		5770		2.49				74.6		5610		2.48				74.4		5930		2.47				74.5		5800		2.47

		74.1		4580		2.46				75		5780		2.49				74.7		5610		2.48				74.4		5940		2.47				74.5		5810		2.47

		74.2		4590		2.46				75.1		5780		2.5				74.8		5620		2.48				74.5		5950		2.48				74.6		5810		2.47

		74.3		4590		2.47				75.1		5790		2.5				74.9		5620		2.49				74.6		5950		2.48				74.6		5810		2.47

		74.3		4590		2.47				75.2		5790		2.5				74.9		5630		2.49				74.6		5960		2.48				74.7		5820		2.48

		74.4		4600		2.47				75.3		5790		2.5				75		5630		2.49				74.7		5960		2.48				74.9		5830		2.48

		74.4		4600		2.47				75.4		5800		2.51				75.1		5640		2.49				74.8		5960		2.48				74.9		5830		2.48

		74.5		4600		2.47				75.4		5810		2.51				75.1		5640		2.49				74.8		5970		2.49				75		5840		2.48

		74.6		4610		2.48				75.5		5810		2.51				75.2		5650		2.5				74.9		5970		2.49				75		5840		2.49

		74.7		4610		2.48				75.6		5820		2.51				75.3		5650		2.5				75		5980		2.49				75.1		5830		2.49

		74.7		4620		2.48				75.6		5820		2.51				75.4		5660		2.5				75		5990		2.49				75.2		5830		2.49

		74.8		4620		2.48				75.7		5830		2.52				75.4		5660		2.5				75.1		5990		2.5				75.2		5840		2.49

		74.8		4620		2.49				75.8		5830		2.52				75.5		5670		2.51				75.2		5990		2.5				75.3		5840		2.49

		74.9		4630		2.49				75.8		5830		2.52				75.6		5670		2.51				75.2		6000		2.5				75.4		5860		2.5

		75		4630		2.49				75.9		5840		2.52				75.6		5680		2.51				75.3		6000		2.5				75.5		5860		2.5

		75.1		4640		2.49				76		5850		2.53				75.7		5680		2.51				75.4		6010		2.5				75.6		5870		2.5

		75.1		4640		2.49				76		5850		2.53				75.8		5690		2.51				75.4		6010		2.51				75.6		5870		2.5

		75.2		4640		2.5				76.1		5850		2.53				75.8		5690		2.52				75.5		6020		2.51				75.7		5880		2.51

		75.3		4650		2.5				76.2		5860		2.53				75.9		5690		2.52				75.6		6020		2.51				75.7		5880		2.51

		75.3		4650		2.5				76.2		5860		2.53				76		5700		2.52				75.6		6030		2.51				75.8		5880		2.51

		75.4		4650		2.5				76.3		5870		2.54				76.1		5710		2.52				75.7		6040		2.52				75.8		5890		2.51

		75.5		4660		2.51				76.4		5870		2.54				76.1		5710		2.53				75.8		6040		2.52				76		5890		2.52

		75.5		4660		2.51				76.4		5880		2.54				76.2		5720		2.53				75.8		6050		2.52				76		5900		2.52

		75.6		4670		2.51				76.5		5880		2.54				76.3		5720		2.53				75.9		6050		2.52				76.1		5900		2.52

		75.7		4670		2.51				76.6		5890		2.55				76.3		5730		2.53				75.9		6050		2.52				76.1		5910		2.52

		75.7		4670		2.51				76.7		5890		2.55				76.3		5730		2.54				76		6060		2.53				76.2		5910		2.52

		75.7		4680		2.52				76.7		5900		2.55				76.4		5740		2.54				76.1		6060		2.53				76.2		5920		2.53

		75.8		4680		2.52				76.8		5900		2.55				76.5		5740		2.54				76.2		6070		2.53				76.3		5920		2.53

		75.9		4690		2.52				76.9		5910		2.56				76.6		5750		2.54				76.2		6080		2.53				76.4		5920		2.53

		76		4690		2.52				76.9		5910		2.56				76.7		5750		2.55				76.3		6080		2.54				76.4		5930		2.53

		76		4690		2.53				77		5920		2.56				76.8		5760		2.55				76.3		6090		2.54				76.6		5940		2.54

		76.1		4700		2.53				77.1		5930		2.56				76.8		5760		2.55				76.4		6090		2.54				76.6		5940		2.54

		76.2		4700		2.53				77.2		5930		2.57				76.9		5770		2.55				76.4		6100		2.54				76.6		5940		2.54

		76.2		4700		2.53				77.3		5930		2.57				76.9		5770		2.55				76.5		6100		2.54				76.7		5950		2.54

		76.3		4710		2.53				77.3		5940		2.57				77		5760		2.56				76.6		6110		2.55				76.8		5950		2.54

		76.4		4710		2.54				77.4		5940		2.57				77.1		5760		2.56				76.7		6110		2.55				76.9		5960		2.55

		76.4		4710		2.54				77.4		5950		2.57				77.2		5770		2.56				76.7		6120		2.55				76.9		5960		2.55

		76.5		4720		2.54				77.5		5950		2.58				77.2		5780		2.56				76.8		6120		2.55				77		5960		2.55

		76.6		4720		2.54				77.6		5960		2.58				77.3		5780		2.57				76.9		6130		2.56				77		5970		2.55

		76.6		4730		2.55				77.6		5960		2.58				77.3		5790		2.57				76.9		6130		2.56				77.1		5970		2.56

		76.7		4730		2.55				77.7		5970		2.58				77.4		5790		2.57				77		6140		2.56				77.2		5980		2.56

		76.7		4730		2.55				77.8		5970		2.59				77.5		5800		2.57				77.1		6140		2.56				77.3		5980		2.56

		76.8		4740		2.55				77.8		5970		2.59				77.6		5800		2.57				77.1		6140		2.56				77.3		5990		2.56

		76.9		4740		2.55				77.9		5980		2.59				77.6		5800		2.58				77.2		6140		2.57				77.4		5990		2.56

		77		4740		2.56				77.9		5980		2.59				77.7		5810		2.58				77.3		6150		2.57				77.5		6000		2.57

		77		4750		2.56				78		5990		2.59				77.8		5820		2.58				77.4		6160		2.57				77.5		6000		2.57

		77.1		4750		2.56				78.1		5990		2.6				77.8		5820		2.58				77.4		6160		2.57				77.6		6010		2.57

		77.2		4750		2.56				78.2		6000		2.6				77.9		5830		2.59				77.5		6170		2.58				77.6		6010		2.57

		77.2		4760		2.56				78.2		6000		2.6				78		5830		2.59				77.6		6170		2.58				77.7		6020		2.58

		77.3		4760		2.57				78.3		6010		2.6				78		5830		2.59				77.6		6180		2.58				77.8		6020		2.58

		77.4		4760		2.57				78.3		6010		2.61				78.1		5840		2.59				77.7		6180		2.58				77.8		6030		2.58

		77.5		4770		2.57				78.4		6000		2.61				78.2		5840		2.6				77.7		6190		2.58				77.9		6030		2.58

		77.6		4770		2.58				78.5		6000		2.61				78.2		5850		2.6				77.8		6190		2.59				78		6030		2.58

		77.6		4780		2.58				78.6		6000		2.61				78.3		5850		2.6				77.9		6200		2.59				78		6040		2.59

		77.6		4780		2.58				78.6		6000		2.61				78.4		5860		2.6				78		6210		2.59				78.1		6040		2.59

		77.7		4790		2.58				78.7		6000		2.62				78.5		5860		2.61				78.1		6210		2.6				78.2		6050		2.59

		77.8		4790		2.58				78.8		6000		2.62				78.6		5870		2.61				78.1		6220		2.6				78.3		6060		2.59

		77.8		4790		2.59				78.8		6000		2.62				78.6		5870		2.61				78.2		6220		2.6				78.4		6060		2.6

		77.9		4790		2.59				78.9		6010		2.62				78.7		5880		2.61				78.2		6220		2.6				78.4		6070		2.6

		78		4800		2.59				78.9		6010		2.63				78.7		5880		2.61				78.3		6230		2.6				78.5		6070		2.6

		78.1		4800		2.59				79		6010		2.63				78.8		5890		2.62				78.4		6230		2.61				78.5		6070		2.6

		78.1		4810		2.6				79.1		5990		2.63				78.8		5890		2.62				78.4		6240		2.61				78.6		6080		2.6

		78.2		4810		2.6				79.2		5970		2.63				78.9		5890		2.62				78.6		6240		2.61				78.6		6060		2.61

		78.2		4810		2.6				79.2		5830		2.63				79		5900		2.62				78.6		6250		2.61				78.7		6060		2.61

		78.3		4820		2.6				79.3		5770		2.64				79.1		5900		2.63				78.7		6240		2.62				78.8		6060		2.61

		78.4		4820		2.6				79.4		5760		2.64				79.1		5910		2.63				78.8		6240		2.62				78.9		6050		2.61

		78.4		4820		2.61				79.4		5760		2.64				79.2		5910		2.63				78.8		6250		2.62				79		6060		2.62

		78.5		4830		2.61				79.5		5760		2.64				79.3		5920		2.63				78.9		6250		2.62				79		6060		2.62

		78.6		4830		2.61				79.5		5720		2.64				79.3		5920		2.63				78.9		6260		2.62				79.1		6070		2.62

		78.7		4840		2.61				79.6		5670		2.65				79.4		5920		2.64				79		6260		2.63				79.1		6080		2.62

		78.7		4840		2.62				79.7		5660		2.65				79.4		5930		2.64				79		6270		2.63				79.2		6080		2.62

		78.8		4850		2.62				79.7		5650		2.65				79.6		5890		2.64				79.2		6280		2.63				79.2		6090		2.63

		78.9		4850		2.62				79.8		5650		2.66				79.6		5770		2.64				79.2		6280		2.63				79.4		6100		2.63

		78.9		4850		2.62				79.9		5640		2.66				79.7		5740		2.65				79.3		6280		2.64				79.4		6100		2.63

		79		4860		2.62				79.9		5630		2.66				79.7		5590		2.65				79.3		6290		2.64				79.5		6100		2.63

		79.1		4860		2.63				80		5630		2.66				79.8		5280		2.65				79.4		6290		2.64				79.5		6110		2.64

		79.1		4860		2.63				80.1		5630		2.66				79.8		5210		2.65				79.5		6300		2.64				79.6		6110		2.64

		79.2		4870		2.63				80.1		5630		2.66				79.9		5160		2.65				79.6		6300		2.65				79.7		6060		2.64

		79.3		4870		2.63				80.2		5630		2.67				80		5140		2.66				79.6		6310		2.65				79.7		6040		2.64

		79.4		4880		2.64				80.3		5620		2.67				80		5120		2.66				79.7		6310		2.65				79.8		6040		2.65

		79.4		4880		2.64				80.3		5620		2.67				80.2		5090		2.66				79.8		6320		2.65				79.9		6050		2.65

		79.5		4880		2.64				80.4		5620		2.67				80.2		5090		2.66				79.8		6330		2.66				80		6050		2.65

		79.6		4890		2.64				80.5		5620		2.68				80.3		5090		2.67				79.9		6330		2.66				80		6060		2.65

		79.6		4890		2.64				80.5		5620		2.68				80.3		5080		2.67				80		6320		2.66				80.1		6060		2.65

		79.7		4890		2.65				80.6		5620		2.68				80.4		5080		2.67				80		6320		2.66				80.1		6070		2.66

		79.8		4900		2.65				80.7		5620		2.68				80.5		5060		2.67				80.1		6320		2.66				80.2		6080		2.66

		79.8		4900		2.65				80.7		5620		2.68				80.5		5040		2.67				80.2		6330		2.67				80.3		6080		2.66

		79.9		4900		2.65				80.8		5620		2.69				80.6		5040		2.68				80.2		6330		2.67				80.3		6090		2.66

		80		4910		2.66				80.9		5580		2.69				80.7		5040		2.68				80.3		6310		2.67				80.4		6090		2.66

		80		4910		2.66				81		5560		2.69				80.8		5040		2.68				80.4		6320		2.67				80.5		6100		2.67

		80.1		4920		2.66				81		5560		2.69				80.9		5040		2.68				80.5		6320		2.68				80.6		6110		2.67

		80.1		4920		2.66				81.1		5560		2.7				80.9		5040		2.69				80.5		6320		2.68				80.7		6110		2.67

		80.2		4920		2.66				81.2		5560		2.7				81		5050		2.69				80.6		6300		2.68				80.7		6110		2.68

		80.3		4930		2.67				81.3		5560		2.7				81		5050		2.69				80.7		6310		2.68				80.8		6110		2.68

		80.3		4930		2.67				81.3		5560		2.7				81.1		5050		2.69				80.7		6310		2.68				80.8		6120		2.68

		80.4		4930		2.67				81.3		5560		2.71				81.2		5050		2.7				80.8		6310		2.69				80.9		6120		2.68

		80.5		4930		2.67				81.4		5570		2.71				81.2		5050		2.7				80.8		6290		2.69				80.9		6120		2.68

		80.5		4940		2.68				81.5		5570		2.71				81.3		5060		2.7				81		6270		2.69				81		6110		2.69

		80.6		4940		2.68				81.6		5570		2.71				81.4		5060		2.7				81		6270		2.69				81.1		6110		2.69

		80.6		4940		2.68				81.6		5570		2.71				81.5		5060		2.71				81.1		6260		2.7				81.2		6110		2.69

		80.7		4950		2.68				81.7		5570		2.72				81.5		5060		2.71				81.2		6270		2.7				81.2		6110		2.69

		80.8		4950		2.68				81.7		5570		2.72				81.6		5060		2.71				81.2		6180		2.7				81.3		6120		2.7

		80.8		4950		2.69				81.8		5570		2.72				81.7		5070		2.71				81.3		6050		2.7				81.4		6120		2.7

		81		4960		2.69				81.9		5570		2.72				81.7		5070		2.71				81.3		6050		2.7				81.4		6120		2.7

		81		4960		2.69				81.9		5570		2.72				81.8		5070		2.72				81.4		6020		2.71				81.5		6130		2.7

		81.1		4970		2.69				82		5580		2.73				81.8		5070		2.72				81.5		5900		2.71				81.5		6130		2.7

		81.2		4970		2.7				82.1		5580		2.73				81.9		5040		2.72				81.6		5770		2.71				81.6		6130		2.71

		81.2		4970		2.7				82.2		5580		2.73				82		5030		2.72				81.7		5700		2.71				81.7		6130		2.71

		81.3		4980		2.7				82.2		5580		2.73				82.1		5020		2.73				81.7		5670		2.72				81.8		6130		2.71

		81.4		4980		2.7				82.3		5590		2.74				82.1		5010		2.73				81.8		5640		2.72				81.8		6130		2.71

		81.4		4990		2.7				82.4		5580		2.74				82.2		5010		2.73				81.8		5620		2.72				81.9		6130		2.71

		81.5		4990		2.71				82.4		5550		2.74				82.2		5010		2.73				81.9		5490		2.72				81.9		6130		2.72

		81.6		4990		2.71				82.5		5520		2.74				82.3		5010		2.73				82		5440		2.73				82		6130		2.72

		81.6		5000		2.71				82.5		5510		2.74				82.4		5010		2.74				82		5430		2.73				82.1		6140		2.72

		81.7		5000		2.71				82.6		5490		2.75				82.4		5010		2.74				82.2		5380		2.73				82.2		6140		2.72

		81.8		5000		2.72				82.7		5470		2.75				82.6		5020		2.74				82.2		5380		2.73				82.3		5600		2.73

		81.8		5010		2.72				82.8		5460		2.75				82.6		5020		2.74				82.3		5370		2.74				82.3		5440		2.73

		81.9		5010		2.72				82.8		5460		2.75				82.7		5020		2.75				82.3		5370		2.74				82.4		5390		2.73

		82		5010		2.72				82.9		5450		2.76				82.8		5020		2.75				82.4		5370		2.74				82.4		5360		2.73

		82		5020		2.72				83		5440		2.76				82.8		5020		2.75				82.4		5370		2.74				82.5		5310		2.74

		82.1		5020		2.73				83		5440		2.76				82.9		5030		2.75				82.5		5380		2.74				82.6		5130		2.74

		82.2		5030		2.73				83.1		5440		2.76				82.9		5030		2.75				82.6		5380		2.75				82.6		4900		2.74

		82.2		5030		2.73				83.2		5440		2.77				83		5030		2.76				82.7		5300		2.75				82.7		3870		2.74

		82.3		5030		2.73				83.2		5430		2.77				83.1		5040		2.76				82.8		5280		2.75				82.8		-20.8		2.75

		82.4		5040		2.74				83.3		5430		2.77				83.2		5040		2.76				82.8		5270		2.75				82.9		7.5		2.75

		82.4		5040		2.74				83.4		5430		2.77				83.2		5040		2.76				82.9		5260		2.76

		82.5		5050		2.74				83.4		5430		2.77				83.3		5040		2.77				82.9		5250		2.76

		82.6		5050		2.74				83.5		5430		2.78				83.4		5040		2.77				83		5250		2.76

		82.6		5050		2.74				83.6		5430		2.78				83.4		5050		2.77				83.1		5240		2.76

		82.7		5060		2.75				83.6		5430		2.78				83.5		5050		2.77				83.1		5240		2.76

		82.8		5060		2.75				83.7		5430		2.78				83.6		5050		2.78				83.2		5240		2.77

		82.8		5060		2.75				83.8		5430		2.78				83.6		5050		2.78				83.3		5240		2.77

		82.9		5060		2.75				83.8		5430		2.79				83.7		5060		2.78				83.4		5230		2.77

		83		5060		2.76				83.9		5430		2.79				83.8		5060		2.78				83.5		5090		2.78

		83		5070		2.76				84		5430		2.79				83.9		5060		2.79				83.5		4870		2.78

		83.1		5070		2.76				84		5430		2.79				84		5070		2.79				83.6		4850		2.78

		83.1		5080		2.76				84.1		5430		2.8				84		5070		2.79				83.6		2430		2.78

		83.2		5080		2.76				84.2		5430		2.8				84.1		5070		2.79				83.7		-443		2.79

		83.3		5080		2.77				84.2		5430		2.8				84.1		5080		2.79				83.8		-432		2.79

		83.4		5090		2.77				84.3		5430		2.8				84.2		5080		2.8

		83.4		5090		2.77				84.3		5440		2.8				84.3		5090		2.8

		83.5		5090		2.77				84.4		5440		2.81				84.4		5090		2.8

		83.6		5100		2.78				84.5		5440		2.81				84.4		5090		2.8

		83.6		5100		2.78				84.6		5440		2.81				84.5		5100		2.81

		83.7		5100		2.78				84.7		5430		2.81				84.6		5100		2.81

		83.7		5110		2.78				84.7		5430		2.82				84.6		5100		2.81

		83.8		5110		2.78				84.8		5430		2.82				84.7		5110		2.81

		83.9		5120		2.79				84.8		5430		2.82				84.8		5110		2.81

		84		5120		2.79				84.9		5430		2.82				84.8		5110		2.82

		84		5130		2.79				85		5420		2.82				84.9		5120		2.82

		84.1		5130		2.79				85		5410		2.83				85		5120		2.82

		84.2		5130		2.8				85.1		5400		2.83				85.1		5130		2.83

		84.3		5140		2.8				85.2		5400		2.83				85.1		5130		2.83

		84.3		5140		2.8				85.2		5390		2.83				85.2		5130		2.83

		84.4		5140		2.8				85.3		5390		2.84				85.2		5140		2.83

		84.5		5150		2.81				85.3		5380		2.84				85.3		5140		2.83

		84.5		5150		2.81				85.4		5380		2.84				85.4		5140		2.84

		84.6		5150		2.81				85.5		5380		2.84				85.5		5150		2.84

		84.7		5130		2.81				85.5		5380		2.84				85.6		5150		2.84

		84.7		5130		2.82				85.6		5380		2.85				85.6		5160		2.84

		84.8		5130		2.82				85.7		5380		2.85				85.7		5150		2.85

		84.9		5130		2.82				85.8		5380		2.85				85.8		5150		2.85

		84.9		5130		2.82				85.8		5390		2.85				85.8		5150		2.85

		85		5140		2.82				85.9		5390		2.86				85.9		5160		2.85

		85.1		5140		2.83				86		5390		2.86				85.9		5160		2.85

		85.1		5150		2.83				86		5370		2.86				86		5170		2.86

		85.2		5150		2.83				86.1		5360		2.86				86.1		5170		2.86

		85.2		5150		2.83				86.2		5360		2.87				86.1		5170		2.86

		85.3		5160		2.83				86.2		5360		2.87				86.2		5180		2.86

		85.4		5160		2.84				86.3		5360		2.87				86.3		5180		2.87

		85.4		5150		2.84				86.4		5370		2.87				86.3		5190		2.87

		85.5		5130		2.84				86.4		5370		2.87				86.4		5190		2.87

		85.6		5130		2.84				86.5		5370		2.88				86.5		5190		2.87

		85.7		5130		2.85				86.6		5370		2.88				86.5		5190		2.87

		85.7		5130		2.85				86.6		5370		2.88				86.6		5200		2.88

		85.8		5130		2.85				86.7		5370		2.88				86.7		5210		2.88

		85.8		5140		2.85				86.8		5370		2.89				86.8		5210		2.88

		85.9		5140		2.85				86.8		5370		2.89				86.9		5210		2.88

		86		5140		2.86				86.9		5370		2.89				86.9		5210		2.89

		86		5150		2.86				87		5370		2.89				87		5220		2.89

		86.1		5150		2.86				87		5370		2.89				87		5220		2.89

		86.2		5160		2.86				87.1		5360		2.9				87.1		5220		2.89

		86.2		5160		2.87				87.1		5350		2.9				87.1		5230		2.9

		86.3		5160		2.87				87.2		5340		2.9				87.2		5230		2.9

		86.4		5170		2.87				87.4		5330		2.9				87.3		5230		2.9

		86.4		5170		2.87				87.4		5310		2.91				87.4		5240		2.9

		86.5		5170		2.87				87.5		5310		2.91				87.4		5240		2.9

		86.6		5180		2.88				87.5		5310		2.91				87.5		5240		2.91

		86.6		5180		2.88				87.6		5300		2.91				87.6		5250		2.91

		86.7		5180		2.88				87.7		5190		2.91				87.6		5250		2.91

		86.8		5190		2.88				87.7		5060		2.92				87.7		5250		2.91

		86.9		5190		2.89				87.8		4980		2.92				87.7		5240		2.91

		86.9		5200		2.89				87.8		4900		2.92				87.8		5240		2.92

		87		5200		2.89				87.9		1790		2.93				87.9		5250		2.92

		87.1		5200		2.89				88		-398		2.93				88		5250		2.92

		87.1		5200		2.9				88.1		-395		2.93				88		5230		2.92

		87.2		5210		2.9												88.1		5220		2.93

		87.2		5210		2.9												88.1		5200		2.93

		87.3		5210		2.9												88.2		5200		2.93

		87.4		5210		2.91												88.3		5180		2.93

		87.5		5210		2.91												88.4		5090		2.94

		87.6		5200		2.91												88.4		5090		2.94

		87.6		5200		2.91												88.5		5080		2.94

		87.7		5170		2.91												88.5		5080		2.94

		87.8		5110		2.92												88.6		4700		2.94

		87.8		5090		2.92												88.7		4410		2.95

		87.9		5080		2.92												88.7		-20.8		2.95

		88		5080		2.92

		88.1		5050		2.93

		88.1		5010		2.93

		88.2		4950		2.93

		88.2		1580		2.93

		88.3		-387		2.94

		88.4		-379		2.94





PETG 5 mm PC 8 proc

		Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)

		0.247		-2.5		0				0.319		-9.17		0				0.209		-8.33		0				0.343		-13.3		0				0.249		-1.67		0

		0.341		-2.5		0				0.446		-5		0.001				0.335		-5		0.001				0.471		-13.3		0				0.375		-1.67		0

		0.465		0		0.001				0.509		8.33		0.003				0.398		7.5		0.003				0.598		-10		0.001				0.5		1.67		0.001

		0.528		13.3		0.003				0.603		35.8		0.006				0.461		25		0.005				0.725		20		0.005				0.563		15.8		0.003

		0.683		47.5		0.007				0.666		51.7		0.008				0.524		41.7		0.007				0.737		36.7		0.007				0.688		52.5		0.007

		0.746		64.2		0.009				0.73		70		0.011				0.65		75		0.012				0.86		56.7		0.01				0.75		70		0.009

		0.809		80.8		0.011				0.793		86.7		0.013				0.713		90		0.014				0.923		72.5		0.012				0.812		87.5		0.012

		0.872		96.7		0.014				0.856		102		0.015				0.776		104		0.016				0.986		88.3		0.014				0.874		104		0.014

		0.935		113		0.016				0.919		117		0.017				0.84		118		0.018				1.05		103		0.016				0.906		119		0.016

		0.968		128		0.018				0.953		129		0.019				0.903		127		0.02				1.11		118		0.018				0.998		133		0.018

		1.07		143		0.02				1.05		140		0.021				0.966		135		0.022				1.21		139		0.022				1.06		144		0.02

		1.17		172		0.025				1.17		159		0.025				1.03		143		0.024				1.27		151		0.024				1.12		154		0.022

		1.27		181		0.027				1.24		167		0.028				1.16		158		0.029				1.33		163		0.026				1.19		163		0.024

		1.3		191		0.029				1.3		176		0.03				1.19		166		0.031				1.4		175		0.028				1.28		175		0.027

		1.34		201		0.031				1.36		184		0.032				1.28		174		0.033				1.46		185		0.03				1.34		184		0.029

		1.42		210		0.033				1.43		193		0.034				1.31		182		0.035				1.52		195		0.032				1.4		193		0.031

		1.48		220		0.035				1.49		202		0.036				1.41		190		0.037				1.59		206		0.034				1.47		203		0.033

		1.58		229		0.037				1.55		208		0.038				1.47		198		0.039				1.65		217		0.036				1.53		212		0.036

		1.64		238		0.04				1.68		219		0.042				1.53		205		0.041				1.78		238		0.041				1.59		219		0.038

		1.73		257		0.044				1.74		226		0.044				1.59		212		0.043				1.84		248		0.043				1.65		227		0.04

		1.83		265		0.046				1.77		232		0.047				1.72		226		0.048				1.9		258		0.045				1.71		234		0.042

		1.86		275		0.048				1.84		238		0.049				1.78		233		0.05				1.96		268		0.047				1.81		245		0.045

		1.95		283		0.05				1.93		243		0.051				1.81		239		0.052				2.03		278		0.049				1.87		251		0.047

		2.03		291		0.052				1.99		248		0.053				1.91		245		0.054				2.09		288		0.051				1.93		258		0.049

		2.06		302		0.054				2.06		253		0.055				1.97		252		0.056				2.12		297		0.053				1.99		265		0.051

		2.15		310		0.056				2.15		259		0.058				2.03		258		0.058				2.22		305		0.056				2.06		270		0.053

		2.24		326		0.061				2.21		264		0.06				2.09		263		0.06				2.34		324		0.06				2.09		277		0.055

		2.34		333		0.063				2.28		268		0.062				2.16		269		0.062				2.41		334		0.062				2.15		281		0.058

		2.37		341		0.065				2.34		273		0.065				2.25		278		0.065				2.47		343		0.064				2.24		287		0.06

		2.43		348		0.067				2.37		277		0.067				2.31		283		0.067				2.53		353		0.066				2.34		293		0.062

		2.49		356		0.069				2.48		281		0.069				2.37		288		0.07				2.6		362		0.068				2.4		298		0.065

		2.59		363		0.071				2.51		287		0.071				2.44		292		0.072				2.66		372		0.07				2.46		301		0.067

		2.62		369		0.073				2.6		292		0.074				2.5		297		0.074				2.72		381		0.072				2.49		304		0.069

		2.68		376		0.075				2.7		298		0.077				2.56		301		0.076				2.82		399		0.076				2.58		308		0.071

		2.84		389		0.079				2.73		302		0.079				2.62		305		0.078				2.91		408		0.079				2.62		312		0.073

		2.9		395		0.081				2.79		306		0.081				2.68		308		0.08				2.98		417		0.081				2.72		316		0.075

		2.96		402		0.084				2.89		310		0.083				2.81		316		0.084				3.04		426		0.083				2.78		319		0.077

		3.02		407		0.086				2.92		314		0.085				2.87		319		0.086				3.07		433		0.085				2.9		326		0.081

		3.09		412		0.088				2.98		318		0.087				2.93		323		0.088				3.17		442		0.087				2.97		329		0.084

		3.15		418		0.09				3.07		323		0.089				3		327		0.09				3.23		450		0.089				3.03		333		0.086

		3.18		422		0.092				3.13		328		0.091				3.06		330		0.092				3.35		465		0.093				3.09		337		0.088

		3.27		427		0.094				3.24		336		0.095				3.12		333		0.094				3.42		473		0.095				3.16		340		0.09

		3.34		432		0.096				3.33		340		0.098				3.18		337		0.096				3.48		479		0.098				3.22		343		0.092

		3.4		436		0.098				3.39		344		0.1				3.24		341		0.098				3.54		487		0.1				3.28		347		0.094

		3.43		440		0.1				3.42		348		0.102				3.37		348		0.103				3.61		493		0.102				3.31		351		0.096

		3.49		444		0.102				3.49		353		0.104				3.43		352		0.105				3.67		500		0.104				3.47		358		0.1

		3.55		448		0.104				3.55		357		0.106				3.49		355		0.107				3.74		506		0.106				3.53		362		0.103

		3.65		452		0.106				3.64		360		0.108				3.55		359		0.109				3.87		518		0.111				3.6		365		0.105

		3.68		455		0.108				3.71		365		0.11				3.62		363		0.111				3.93		523		0.113				3.63		369		0.107

		3.74		459		0.11				3.74		369		0.112				3.68		366		0.113				3.99		529		0.115				3.72		373		0.109

		3.8		463		0.113				3.86		377		0.116				3.74		369		0.115				4.06		535		0.117				3.78		376		0.111

		3.93		468		0.116				3.95		381		0.119				3.78		373		0.117				4.12		540		0.119				3.85		380		0.113

		3.96		471		0.118				3.99		385		0.121				3.93		380		0.121				4.18		545		0.121				3.88		383		0.115

		4.05		474		0.12				4.08		389		0.123				4		383		0.123				4.24		550		0.123				4		390		0.119

		4.12		478		0.122				4.11		393		0.125				4.06		387		0.125				4.31		556		0.125				4.1		394		0.121

		4.18		481		0.124				4.2		398		0.127				4.12		390		0.128				4.43		565		0.129				4.16		398		0.123

		4.24		484		0.126				4.27		401		0.129				4.18		393		0.13				4.5		569		0.131				4.22		401		0.125

		4.27		487		0.128				4.33		405		0.131				4.21		396		0.132				4.57		575		0.134				4.29		404		0.128

		4.36		490		0.13				4.42		411		0.134				4.31		399		0.134				4.63		580		0.136				4.35		408		0.13

		4.46		497		0.135				4.45		415		0.136				4.37		403		0.136				4.7		584		0.138				4.41		412		0.132

		4.55		500		0.137				4.55		418		0.138				4.46		408		0.139				4.76		588		0.14				4.48		415		0.134

		4.58		503		0.139				4.58		423		0.14				4.52		411		0.141				4.82		593		0.142				4.6		422		0.138

		4.68		506		0.141				4.64		426		0.142				4.59		413		0.143				4.95		601		0.146				4.63		426		0.14

		4.74		509		0.143				4.7		430		0.144				4.65		417		0.145				5.01		605		0.149				4.73		429		0.142

		4.8		513		0.145				4.77		433		0.146				4.71		420		0.147				5.07		609		0.15				4.76		433		0.144

		4.86		516		0.147				4.86		438		0.149				4.77		423		0.149				5.13		613		0.152				4.85		437		0.147

		4.93		519		0.149				4.98		445		0.153				4.84		427		0.152				5.19		618		0.155				4.92		440		0.149

		5.02		523		0.152				5.02		448		0.155				4.9		430		0.154				5.26		621		0.157				4.95		443		0.151

		5.08		526		0.154				5.08		453		0.157				5.03		437		0.158				5.32		624		0.159				5.04		448		0.153

		5.11		529		0.156				5.17		456		0.159				5.09		439		0.16				5.38		628		0.161				5.17		454		0.157

		5.18		532		0.158				5.2		459		0.161				5.15		443		0.162				5.48		633		0.164				5.23		458		0.159

		5.24		535		0.16				5.27		463		0.163				5.18		445		0.164				5.54		635		0.166				5.3		461		0.161

		5.3		538		0.163				5.33		466		0.165				5.28		448		0.166				5.6		638		0.168				5.33		464		0.164

		5.39		540		0.165				5.39		469		0.167				5.34		451		0.168				5.63		640		0.17				5.42		468		0.165

		5.46		543		0.167				5.55		477		0.171				5.4		454		0.17				5.73		643		0.172				5.48		471		0.168

		5.55		548		0.17				5.61		480		0.173				5.46		457		0.172				5.79		645		0.175				5.55		474		0.17

		5.61		551		0.172				5.64		483		0.176				5.59		463		0.177				5.85		648		0.177				5.61		477		0.172

		5.64		553		0.174				5.73		487		0.178				5.65		466		0.179				5.91		650		0.179				5.74		484		0.176

		5.71		556		0.176				5.76		490		0.18				5.71		468		0.181				6.04		655		0.183				5.77		488		0.178

		5.77		558		0.178				5.83		493		0.182				5.77		471		0.183				6.1		658		0.185				5.86		491		0.18

		5.83		561		0.18				5.92		497		0.184				5.84		473		0.185				6.16		661		0.187				5.93		494		0.182

		5.89		564		0.182				5.98		500		0.186				5.9		476		0.187				6.2		663		0.189				5.99		498		0.184

		5.99		566		0.185				6.08		507		0.19				5.96		478		0.189				6.29		667		0.192				6.05		501		0.187

		6.08		571		0.189				6.17		511		0.192				6.02		481		0.191				6.36		669		0.194				6.12		505		0.189

		6.14		573		0.191				6.23		514		0.194				6.15		486		0.195				6.42		672		0.196				6.21		510		0.192

		6.21		576		0.193				6.29		518		0.197				6.21		488		0.198				6.54		678		0.2				6.28		513		0.194

		6.3		578		0.195				6.33		521		0.199				6.28		492		0.2				6.61		682		0.202				6.34		517		0.196

		6.33		581		0.197				6.39		524		0.201				6.31		494		0.202				6.67		685		0.204				6.4		520		0.198

		6.39		583		0.199				6.45		528		0.203				6.4		498		0.204				6.7		688		0.206				6.47		524		0.2

		6.49		585		0.201				6.54		532		0.205				6.43		500		0.206				6.79		691		0.208				6.53		528		0.202

		6.52		588		0.203				6.58		535		0.207				6.52		502		0.208				6.86		694		0.21				6.59		532		0.204

		6.58		589		0.205				6.7		543		0.211				6.59		504		0.21				6.94		698		0.213				6.67		537		0.207

		6.74		594		0.209				6.76		546		0.213				6.71		510		0.214				7		702		0.215				6.79		545		0.211

		6.8		597		0.212				6.83		549		0.215				6.77		513		0.216				7.12		708		0.219				6.86		550		0.213

		6.83		599		0.214				6.89		553		0.217				6.8		515		0.218				7.19		711		0.221				6.92		555		0.215

		6.89		601		0.216				6.95		556		0.219				6.9		518		0.22				7.25		713		0.223				6.98		561		0.217

		6.95		603		0.218				7.01		560		0.221				6.96		520		0.222				7.31		717		0.225				7.05		567		0.22

		7.02		605		0.22				7.11		564		0.223				7.03		523		0.225				7.37		720		0.227				7.11		572		0.222

		7.08		608		0.222				7.17		568		0.226				7.06		526		0.227				7.44		723		0.23				7.17		578		0.224

		7.17		610		0.224				7.23		575		0.229				7.12		529		0.229				7.5		726		0.231				7.3		593		0.228

		7.27		615		0.228				7.32		579		0.231				7.24		533		0.232				7.56		728		0.233				7.36		602		0.23

		7.33		617		0.23				7.39		583		0.233				7.31		535		0.234				7.69		735		0.238				7.43		613		0.233

		7.39		619		0.232				7.42		589		0.235				7.37		538		0.236				7.75		738		0.24				7.49		623		0.235

		7.45		622		0.234				7.51		594		0.237				7.43		541		0.238				7.81		742		0.242				7.56		632		0.237

		7.55		624		0.237				7.57		600		0.239				7.5		543		0.24				7.87		745		0.244				7.62		643		0.239

		7.58		627		0.238				7.61		607		0.241				7.56		546		0.242				7.94		748		0.246				7.68		652		0.241

		7.64		629		0.241				7.7		613		0.243				7.59		548		0.244				8		751		0.248				7.81		671		0.245

		7.73		631		0.243				7.76		623		0.246				7.68		551		0.246				8.06		754		0.25				7.87		680		0.247

		7.83		637		0.247				7.85		631		0.248				7.78		557		0.25				8.12		758		0.252				7.94		688		0.249

		7.89		639		0.249				7.92		639		0.25				7.87		559		0.253				8.18		761		0.254				8		698		0.251

		7.95		642		0.251				7.98		647		0.252				7.93		562		0.255				8.28		767		0.259				8.06		707		0.253

		8.05		644		0.253				8.04		654		0.255				8		564		0.257				8.37		770		0.261				8.13		714		0.256

		8.11		646		0.255				8.07		662		0.257				8.06		567		0.259				8.43		773		0.263				8.16		721		0.258

		8.17		648		0.257				8.17		669		0.259				8.12		570		0.261				8.5		777		0.265				8.25		728		0.26

		8.2		652		0.259				8.2		678		0.261				8.18		573		0.263				8.56		780		0.267				8.38		741		0.264

		8.3		654		0.261				8.29		685		0.263				8.25		576		0.265				8.62		783		0.269				8.44		747		0.266

		8.39		659		0.265				8.39		701		0.267				8.37		583		0.269				8.68		786		0.271				8.5		753		0.268

		8.48		662		0.267				8.48		708		0.269				8.43		587		0.272				8.75		789		0.273				8.57		759		0.27

		8.51		664		0.27				8.54		715		0.271				8.5		591		0.274				8.84		794		0.276				8.63		764		0.272

		8.61		667		0.272				8.6		723		0.273				8.53		596		0.276				8.9		798		0.278				8.69		770		0.275

		8.67		669		0.274				8.63		729		0.276				8.62		602		0.278				8.96		801		0.28				8.76		775		0.276

		8.73		673		0.276				8.73		736		0.278				8.68		608		0.28				9.02		804		0.282				8.88		786		0.281

		8.8		675		0.278				8.79		743		0.28				8.75		615		0.282				9.09		807		0.284				8.92		792		0.283

		8.86		678		0.28				8.85		748		0.282				8.81		621		0.284				9.15		810		0.287				9.01		797		0.285

		8.95		683		0.284				8.98		758		0.286				8.94		633		0.288				9.21		814		0.289				9.07		802		0.287

		9.01		686		0.286				9.04		762		0.288				9		638		0.29				9.27		818		0.291				9.15		808		0.29

		9.08		689		0.288				9.1		765		0.29				9.06		644		0.292				9.37		823		0.294				9.21		813		0.292

		9.14		693		0.29				9.16		768		0.292				9.12		650		0.294				9.43		826		0.296				9.28		818		0.294

		9.23		695		0.293				9.23		772		0.294				9.16		655		0.296				9.49		829		0.298				9.4		829		0.298

		9.26		698		0.295				9.26		775		0.296				9.22		661		0.299				9.56		833		0.3				9.47		835		0.3

		9.33		703		0.297				9.35		779		0.298				9.31		667		0.301				9.62		837		0.302				9.5		840		0.302

		9.42		706		0.299				9.41		783		0.3				9.37		672		0.303				9.68		840		0.304				9.59		845		0.304

		9.51		713		0.302				9.48		788		0.302				9.5		683		0.307				9.74		843		0.307				9.65		850		0.307

		9.58		718		0.304				9.57		796		0.306				9.56		689		0.309				9.81		847		0.309				9.72		855		0.309

		9.64		723		0.306				9.63		800		0.308				9.63		695		0.311				9.93		853		0.313				9.78		860		0.311

		9.7		729		0.308				9.7		805		0.31				9.69		701		0.313				10		857		0.315				9.91		871		0.315

		9.73		735		0.31				9.76		810		0.312				9.76		707		0.316				10.1		861		0.317				9.98		876		0.317

		9.82		741		0.312				9.82		816		0.314				9.82		712		0.318				10.1		864		0.319				10		881		0.319

		9.89		746		0.315				9.88		820		0.316				9.88		718		0.32				10.2		868		0.321				10.1		886		0.322

		9.95		751		0.316				9.94		825		0.318				10		728		0.324				10.2		871		0.323				10.1		890		0.324

		10		760		0.321				10		830		0.32				10		733		0.326				10.3		874		0.325				10.2		896		0.326

		10.1		765		0.323				10.1		837		0.323				10.1		738		0.328				10.4		878		0.327				10.3		900		0.328

		10.2		770		0.325				10.1		842		0.326				10.2		744		0.33				10.5		885		0.331				10.4		906		0.33

		10.3		775		0.327				10.2		847		0.328				10.3		749		0.333				10.6		888		0.334				10.4		913		0.333

		10.3		779		0.329				10.3		851		0.33				10.3		754		0.334				10.6		892		0.336				10.5		918		0.335

		10.4		783		0.331				10.3		856		0.332				10.4		759		0.336				10.7		895		0.338				10.6		923		0.337

		10.4		788		0.333				10.4		861		0.334				10.4		764		0.338				10.7		899		0.34				10.6		928		0.339

		10.5		793		0.335				10.4		865		0.336				10.6		775		0.343				10.8		903		0.342				10.7		933		0.341

		10.6		803		0.339				10.5		870		0.338				10.6		780		0.345				10.9		906		0.344				10.8		938		0.343

		10.7		808		0.342				10.6		877		0.341				10.7		785		0.347				10.9		909		0.346				10.8		943		0.346

		10.8		813		0.344				10.7		882		0.343				10.8		790		0.349				11.1		916		0.35				10.9		948		0.348

		10.8		818		0.346				10.8		886		0.345				10.8		795		0.351				11.1		919		0.352				11		957		0.351

		10.9		823		0.348				10.8		890		0.347				10.9		800		0.353				11.2		923		0.354				11.1		961		0.353

		10.9		828		0.35				10.9		895		0.349				11		805		0.356				11.2		926		0.356				11.1		966		0.355

		11		833		0.352				10.9		899		0.351				11		812		0.359				11.3		929		0.358				11.2		971		0.357

		11.1		838		0.354				11		903		0.353				11.1		817		0.361				11.4		933		0.361				11.2		976		0.359

		11.2		847		0.358				11		908		0.356				11.2		821		0.363				11.4		936		0.363				11.3		982		0.362

		11.2		851		0.36				11.1		913		0.358				11.2		826		0.365				11.5		939		0.365				11.4		987		0.364

		11.3		855		0.362				11.2		918		0.361				11.3		830		0.367				11.6		947		0.369				11.4		992		0.366

		11.4		860		0.364				11.3		923		0.363				11.4		835		0.369				11.7		950		0.371				11.6		1000		0.37

		11.4		865		0.366				11.3		928		0.365				11.4		840		0.371				11.7		953		0.373				11.6		1010		0.372

		11.5		868		0.368				11.4		932		0.367				11.5		844		0.373				11.8		957		0.375				11.7		1010		0.374

		11.6		874		0.371				11.5		936		0.369				11.6		851		0.377				11.9		960		0.377				11.7		1020		0.376

		11.6		878		0.373				11.5		940		0.371				11.7		856		0.379				11.9		963		0.38				11.8		1020		0.378

		11.7		885		0.376				11.6		944		0.373				11.7		860		0.381				12		967		0.382				11.8		1030		0.38

		11.8		889		0.378				11.7		948		0.375				11.8		864		0.383				12.1		971		0.384				11.9		1030		0.382

		11.8		894		0.38				11.8		954		0.378				11.8		868		0.385				12.2		978		0.388				12.1		1040		0.387

		11.9		898		0.382				11.8		958		0.38				11.9		873		0.387				12.3		980		0.39				12.1		1050		0.389

		12		903		0.384				11.8		963		0.383				12		877		0.389				12.3		984		0.392				12.2		1050		0.391

		12		907		0.386				11.9		966		0.385				12		882		0.391				12.4		988		0.394				12.3		1060		0.393

		12.1		912		0.388				12		970		0.387				12.2		891		0.396				12.4		991		0.396				12.3		1060		0.395

		12.1		916		0.39				12		974		0.389				12.2		895		0.398				12.5		993		0.398				12.4		1070		0.397

		12.2		920		0.393				12.1		978		0.391				12.3		898		0.4				12.6		997		0.4				12.4		1070		0.399

		12.3		927		0.396				12.2		983		0.393				12.4		903		0.402				12.6		1000		0.402				12.5		1080		0.404

		12.4		931		0.398				12.2		987		0.395				12.4		907		0.405				12.8		1010		0.407				12.6		1090		0.406

		12.4		935		0.4				12.3		994		0.399				12.5		912		0.407				12.8		1010		0.409				12.7		1090		0.408

		12.5		939		0.402				12.4		998		0.401				12.6		916		0.409				12.9		1010		0.411				12.8		1100		0.41

		12.6		944		0.404				12.5		1000		0.404				12.7		923		0.414				12.9		1020		0.413				12.8		1100		0.412

		12.6		948		0.406				12.5		1010		0.406				12.8		928		0.416				13		1020		0.415				12.9		1110		0.414

		12.7		953		0.408				12.6		1010		0.408				12.8		932		0.418				13		1020		0.417				13		1110		0.416

		12.7		957		0.41				12.7		1010		0.41				12.9		936		0.42				13.1		1030		0.419				13.1		1120		0.421

		12.8		961		0.412				12.8		1020		0.412				13		939		0.422				13.2		1030		0.421				13.1		1130		0.423

		12.9		969		0.416				12.8		1020		0.414				13		943		0.424				13.3		1040		0.426				13.2		1130		0.425

		13		973		0.418				12.9		1030		0.418				13.1		948		0.426				13.4		1040		0.428				13.3		1140		0.427

		13		978		0.42				13		1030		0.42				13.2		955		0.43				13.4		1040		0.43				13.3		1140		0.429

		13.1		982		0.423				13.1		1040		0.422				13.3		959		0.433				13.5		1040		0.432				13.4		1150		0.431

		13.2		986		0.425				13.1		1040		0.424				13.3		963		0.435				13.6		1050		0.434				13.5		1150		0.433

		13.3		990		0.427				13.2		1050		0.426				13.4		967		0.437				13.6		1050		0.436				13.6		1160		0.438

		13.3		994		0.429				13.2		1050		0.428				13.4		972		0.439				13.7		1050		0.438				13.7		1170		0.44

		13.4		998		0.431				13.3		1050		0.43				13.5		976		0.441				13.8		1060		0.442				13.7		1170		0.442

		13.5		1010		0.435				13.4		1060		0.433				13.6		980		0.443				13.9		1060		0.444				13.7		1180		0.444

		13.6		1010		0.437				13.4		1060		0.436				13.7		988		0.447				14		1070		0.447				13.8		1180		0.446

		13.6		1020		0.439				13.5		1070		0.438				13.8		992		0.45				14		1070		0.449				13.9		1180		0.448

		13.7		1020		0.441				13.6		1070		0.44				13.8		996		0.452				14.1		1070		0.451				14		1190		0.45

		13.8		1020		0.444				13.6		1080		0.442				13.9		1000		0.454				14.1		1070		0.453				14.1		1200		0.455

		13.8		1030		0.446				13.7		1080		0.444				14		1000		0.456				14.2		1080		0.455				14.2		1200		0.457

		13.9		1030		0.447				13.8		1080		0.446				14		1010		0.458				14.3		1080		0.457				14.2		1200		0.459

		13.9		1040		0.45				13.8		1090		0.448				14.1		1010		0.46				14.4		1090		0.461				14.3		1210		0.461

		14		1040		0.453				13.9		1090		0.45				14.2		1020		0.463				14.5		1090		0.464				14.3		1210		0.463

		14.1		1050		0.455				14		1100		0.452				14.3		1020		0.465				14.5		1090		0.466				14.4		1220		0.465

		14.2		1050		0.457				14.1		1100		0.456				14.3		1030		0.468				14.6		1100		0.468				14.5		1220		0.467

		14.2		1050		0.459				14.1		1110		0.458				14.4		1030		0.47				14.6		1100		0.47				14.5		1220		0.469

		14.3		1060		0.461				14.2		1110		0.459				14.4		1030		0.472				14.7		1100		0.472				14.7		1230		0.473

		14.3		1060		0.463				14.2		1110		0.462				14.5		1040		0.474				14.8		1100		0.474				14.7		1240		0.475

		14.4		1070		0.465				14.3		1120		0.464				14.6		1040		0.476				14.9		1110		0.477				14.8		1240		0.478

		14.4		1070		0.467				14.3		1120		0.466				14.6		1040		0.478				14.9		1110		0.479				14.8		1240		0.48

		14.5		1080		0.469				14.4		1130		0.468				14.8		1050		0.482				15		1110		0.481				14.9		1250		0.482

		14.7		1080		0.474				14.5		1130		0.47				14.8		1060		0.485				15.1		1120		0.483				15		1250		0.484

		14.7		1090		0.476				14.6		1140		0.474				14.9		1060		0.486				15.1		1120		0.485				15		1260		0.486

		14.8		1090		0.478				14.7		1140		0.476				15		1060		0.489				15.2		1120		0.488				15.1		1260		0.488

		14.8		1100		0.48				14.7		1150		0.478				15		1070		0.491				15.2		1130		0.49				15.2		1270		0.491

		14.9		1100		0.482				14.8		1150		0.48				15.1		1070		0.493				15.3		1130		0.492				15.2		1270		0.493

		14.9		1100		0.484				14.9		1150		0.483				15.1		1070		0.495				15.4		1140		0.496				15.3		1280		0.495

		15		1110		0.486				14.9		1160		0.485				15.2		1080		0.497				15.5		1140		0.498				15.4		1280		0.498

		15.1		1110		0.488				15		1160		0.487				15.3		1080		0.5				15.6		1140		0.5				15.4		1290		0.5

		15.1		1120		0.49				15.1		1160		0.489				15.4		1080		0.502				15.6		1150		0.502				15.5		1290		0.502

		15.3		1120		0.494				15.1		1170		0.491				15.4		1090		0.504				15.7		1150		0.505				15.6		1300		0.504

		15.3		1130		0.497				15.2		1180		0.495				15.5		1090		0.506				15.8		1150		0.507				15.6		1300		0.506

		15.4		1130		0.498				15.3		1180		0.497				15.6		1100		0.509				15.8		1150		0.509				15.7		1310		0.51

		15.4		1140		0.501				15.3		1180		0.499				15.6		1100		0.511				15.9		1160		0.511				15.8		1310		0.512

		15.5		1140		0.503				15.4		1190		0.501				15.7		1100		0.513				16		1160		0.515				15.9		1320		0.514

		15.6		1140		0.505				15.5		1190		0.503				15.7		1110		0.515				16.1		1170		0.517				15.9		1320		0.516

		15.6		1150		0.507				15.6		1190		0.505				15.8		1110		0.518				16.1		1170		0.519				16		1320		0.518

		15.7		1150		0.509				15.6		1200		0.507				15.9		1110		0.52				16.2		1170		0.522				16.1		1330		0.521

		15.8		1160		0.511				15.7		1200		0.509				15.9		1120		0.523				16.3		1170		0.524				16.1		1330		0.523

		15.9		1160		0.515				15.8		1210		0.514				16		1120		0.525				16.3		1180		0.525				16.2		1340		0.525

		15.9		1170		0.517				15.8		1210		0.516				16.1		1120		0.527				16.4		1180		0.528				16.3		1350		0.529

		16		1170		0.519				15.9		1210		0.518				16.2		1130		0.529				16.5		1190		0.532				16.4		1350		0.531

		16.1		1180		0.521				16		1220		0.52				16.2		1130		0.531				16.6		1190		0.534				16.4		1350		0.533

		16.1		1180		0.524				16.1		1220		0.522				16.3		1130		0.533				16.6		1190		0.536				16.5		1360		0.535

		16.2		1180		0.526				16.1		1220		0.524				16.4		1140		0.537				16.7		1190		0.538				16.6		1360		0.537

		16.3		1190		0.528				16.2		1230		0.526				16.5		1140		0.539				16.8		1200		0.54				16.6		1370		0.539

		16.3		1190		0.53				16.2		1230		0.528				16.5		1150		0.541				16.8		1200		0.542				16.7		1370		0.541

		16.5		1200		0.534				16.3		1230		0.531				16.6		1150		0.544				16.9		1200		0.545				16.8		1370		0.543

		16.5		1200		0.536				16.4		1240		0.534				16.7		1150		0.546				17		1210		0.547				16.9		1380		0.547

		16.6		1210		0.538				16.5		1240		0.536				16.7		1160		0.548				17		1210		0.55				16.9		1380		0.549

		16.6		1210		0.54				16.5		1240		0.538				16.8		1160		0.55				17.1		1210		0.552				17		1390		0.551

		16.7		1210		0.542				16.6		1250		0.54				16.9		1170		0.553				17.2		1220		0.554				17.1		1390		0.553

		16.8		1220		0.544				16.7		1250		0.542				16.9		1170		0.555				17.2		1220		0.556				17.1		1400		0.555

		16.8		1220		0.546				16.7		1250		0.544				17		1170		0.557				17.3		1220		0.558				17.2		1400		0.557

		16.9		1230		0.548				16.7		1260		0.546				17.1		1180		0.559				17.4		1220		0.56				17.2		1400		0.56

		16.9		1230		0.551				16.8		1260		0.548				17.1		1180		0.562				17.4		1230		0.562				17.3		1410		0.562

		17.1		1240		0.555				17		1270		0.552				17.2		1180		0.564				17.5		1230		0.564				17.4		1420		0.566

		17.1		1240		0.557				17		1270		0.554				17.3		1190		0.565				17.5		1230		0.567				17.5		1420		0.568

		17.2		1240		0.559				17.1		1280		0.556				17.3		1190		0.568				17.6		1240		0.569				17.5		1420		0.57

		17.3		1250		0.561				17.1		1280		0.558				17.4		1190		0.57				17.7		1240		0.571				17.6		1430		0.572

		17.3		1250		0.563				17.2		1280		0.56				17.5		1200		0.572				17.7		1240		0.573				17.6		1430		0.574

		17.4		1260		0.565				17.3		1280		0.563				17.5		1200		0.574				17.8		1240		0.575				17.7		1440		0.576

		17.5		1260		0.567				17.3		1290		0.565				17.6		1200		0.576				17.9		1250		0.577				17.8		1440		0.578

		17.5		1260		0.569				17.4		1290		0.567				17.6		1210		0.578				17.9		1250		0.579				17.8		1440		0.581

		17.7		1270		0.573				17.5		1300		0.571				17.7		1210		0.581				18		1250		0.581				17.9		1450		0.584

		17.7		1270		0.575				17.6		1300		0.573				17.8		1210		0.582				18.1		1260		0.586				18		1450		0.586

		17.7		1280		0.577				17.6		1300		0.575				17.8		1220		0.585				18.2		1260		0.588				18.1		1460		0.588

		17.8		1280		0.58				17.7		1310		0.577				18		1220		0.589				18.2		1260		0.59				18.1		1460		0.59

		17.9		1290		0.582				17.7		1310		0.579				18		1220		0.591				18.3		1270		0.592				18.2		1460		0.592

		17.9		1290		0.584				17.8		1320		0.581				18.1		1230		0.593				18.4		1270		0.594				18.3		1470		0.594

		18		1290		0.586				17.9		1320		0.583				18.1		1230		0.595				18.4		1270		0.596				18.3		1470		0.596

		18.1		1300		0.588				17.9		1320		0.585				18.2		1230		0.597				18.5		1270		0.598				18.4		1470		0.598

		18.2		1300		0.592				18.1		1330		0.589				18.3		1240		0.599				18.6		1280		0.603				18.5		1480		0.6

		18.2		1310		0.594				18.1		1330		0.592				18.3		1240		0.602				18.7		1280		0.604				18.5		1480		0.602

		18.3		1310		0.596				18.2		1340		0.594				18.5		1250		0.606				18.8		1290		0.606				18.6		1490		0.604

		18.4		1310		0.598				18.2		1340		0.596				18.5		1250		0.608				18.8		1290		0.609				18.6		1490		0.606

		18.5		1310		0.601				18.3		1340		0.598				18.6		1250		0.61				18.9		1290		0.611				18.7		1490		0.609

		18.5		1320		0.603				18.4		1350		0.6				18.7		1260		0.612				18.9		1290		0.613				18.7		1500		0.611

		18.6		1320		0.605				18.4		1350		0.602				18.7		1260		0.614				19		1300		0.615				18.8		1500		0.613

		18.7		1320		0.607				18.5		1350		0.604				18.8		1260		0.616				19.1		1300		0.62				18.9		1500		0.614

		18.7		1330		0.61				18.6		1360		0.608				18.8		1260		0.618				19.2		1300		0.622				19		1510		0.617

		18.8		1330		0.612				18.7		1360		0.61				19		1270		0.623				19.3		1310		0.624				19.1		1510		0.621

		18.8		1340		0.614				18.7		1370		0.613				19		1270		0.625				19.3		1310		0.626				19.1		1520		0.623

		18.9		1340		0.616				18.8		1370		0.615				19.1		1280		0.627				19.4		1310		0.628				19.2		1520		0.625

		19		1340		0.618				18.9		1370		0.617				19.2		1280		0.629				19.4		1320		0.63				19.2		1520		0.627

		19		1350		0.62				19		1380		0.619				19.2		1280		0.631				19.5		1320		0.632				19.3		1530		0.629

		19.1		1350		0.622				19		1380		0.621				19.3		1290		0.633				19.6		1320		0.634				19.4		1530		0.631

		19.2		1350		0.624				19.1		1380		0.623				19.3		1290		0.635				19.7		1320		0.637				19.4		1540		0.633

		19.2		1360		0.626				19.2		1390		0.627				19.4		1290		0.637				19.7		1330		0.639				19.5		1540		0.635

		19.3		1360		0.631				19.2		1390		0.629				19.5		1300		0.641				19.8		1330		0.641				19.6		1540		0.639

		19.4		1370		0.633				19.3		1390		0.631				19.6		1300		0.643				19.8		1330		0.643				19.7		1550		0.641

		19.5		1370		0.635				19.4		1400		0.633				19.7		1300		0.646				19.9		1330		0.645				19.7		1550		0.643

		19.5		1370		0.637				19.5		1400		0.635				19.7		1310		0.648				20		1340		0.647				19.8		1560		0.645

		19.6		1380		0.639				19.5		1400		0.637				19.8		1310		0.65				20		1340		0.649				19.8		1560		0.647

		19.7		1380		0.641				19.6		1410		0.639				19.8		1310		0.652				20.2		1340		0.653				19.9		1560		0.649

		19.7		1380		0.643				19.6		1410		0.642				19.9		1320		0.654				20.2		1350		0.655				20		1570		0.651

		19.8		1390		0.645				19.8		1420		0.646				19.9		1320		0.656				20.3		1350		0.658				20		1570		0.653

		19.9		1390		0.647				19.8		1420		0.648				20.1		1320		0.66				20.3		1350		0.66				20.1		1570		0.655

		20		1400		0.651				19.9		1420		0.65				20.2		1330		0.662				20.4		1360		0.662				20.2		1580		0.66

		20.1		1400		0.654				19.9		1430		0.652				20.2		1330		0.665				20.5		1360		0.664				20.3		1580		0.662

		20.1		1400		0.655				20		1430		0.654				20.3		1330		0.667				20.5		1360		0.666				20.4		1590		0.664

		20.2		1410		0.658				20.1		1430		0.656				20.3		1330		0.668				20.7		1370		0.67				20.4		1590		0.666

		20.2		1410		0.66				20.1		1440		0.658				20.4		1340		0.671				20.7		1370		0.672				20.5		1590		0.668

		20.3		1410		0.662				20.2		1440		0.66				20.4		1340		0.673				20.8		1370		0.675				20.5		1600		0.67

		20.3		1420		0.664				20.3		1440		0.663				20.5		1340		0.675				20.9		1370		0.677				20.6		1600		0.672

		20.4		1420		0.666				20.4		1450		0.665				20.6		1350		0.677				20.9		1380		0.679				20.6		1600		0.674

		20.6		1430		0.67				20.4		1450		0.667				20.7		1350		0.68				21		1380		0.681				20.7		1610		0.676

		20.6		1430		0.672				20.5		1450		0.67				20.8		1350		0.682				21		1380		0.683				20.9		1610		0.68

		20.7		1430		0.674				20.6		1450		0.672				20.8		1360		0.684				21.2		1390		0.687				20.9		1620		0.682

		20.7		1440		0.676				20.6		1460		0.674				20.9		1360		0.686				21.2		1390		0.689				21		1620		0.684

		20.8		1440		0.679				20.7		1460		0.676				20.9		1360		0.688				21.3		1390		0.691				21		1620		0.686

		20.8		1440		0.681				20.7		1460		0.678				21		1360		0.69				21.4		1390		0.693				21.1		1630		0.689

		20.9		1450		0.683				20.8		1470		0.68				21.1		1370		0.692				21.4		1400		0.695				21.1		1630		0.691

		21		1450		0.685				20.9		1470		0.684				21.1		1370		0.694				21.5		1400		0.698				21.2		1630		0.693

		21.1		1450		0.688				21		1480		0.686				21.2		1380		0.699				21.5		1400		0.7				21.3		1640		0.695

		21.1		1460		0.69				21		1480		0.688				21.3		1380		0.701				21.7		1410		0.704				21.4		1640		0.698

		21.2		1460		0.692				21.1		1480		0.691				21.3		1380		0.703				21.7		1410		0.706				21.5		1640		0.7

		21.2		1460		0.694				21.2		1480		0.693				21.4		1380		0.705				21.8		1410		0.708				21.5		1650		0.702

		21.3		1470		0.696				21.2		1490		0.695				21.5		1390		0.707				21.9		1410		0.71				21.5		1650		0.704

		21.4		1470		0.698				21.3		1490		0.697				21.6		1390		0.709				21.9		1420		0.712				21.6		1650		0.706

		21.4		1470		0.7				21.3		1490		0.699				21.6		1390		0.711				22		1420		0.714				21.7		1660		0.708

		21.5		1480		0.702				21.5		1500		0.703				21.7		1390		0.713				22		1420		0.717				21.7		1660		0.711

		21.6		1480		0.704				21.5		1500		0.705				21.7		1400		0.715				22.1		1420		0.719				21.8		1660		0.712

		21.6		1480		0.708				21.6		1510		0.707				21.8		1400		0.718				22.2		1430		0.723				21.9		1670		0.715

		21.7		1490		0.71				21.6		1510		0.709				21.9		1400		0.72				22.3		1430		0.725				22		1670		0.718

		21.8		1490		0.712				21.7		1510		0.711				22		1410		0.722				22.4		1430		0.727				22		1670		0.72

		21.9		1490		0.714				21.8		1510		0.713				22		1410		0.724				22.4		1440		0.729				22.1		1680		0.722

		21.9		1500		0.716				21.8		1520		0.715				22.1		1410		0.726				22.5		1440		0.731				22.1		1680		0.724

		22		1500		0.718				21.9		1520		0.717				22.1		1410		0.729				22.5		1440		0.734				22.2		1680		0.726

		22.1		1500		0.72				22		1520		0.72				22.2		1420		0.731				22.6		1440		0.736				22.3		1690		0.728

		22.1		1510		0.722				22.1		1530		0.724				22.3		1420		0.733				22.7		1450		0.738				22.4		1690		0.73

		22.2		1510		0.725				22.1		1530		0.726				22.4		1420		0.737				22.8		1450		0.742				22.4		1690		0.732

		22.2		1510		0.728				22.2		1530		0.728				22.5		1430		0.739				22.9		1450		0.744				22.5		1700		0.735

		22.3		1520		0.73				22.3		1540		0.73				22.5		1430		0.741				22.9		1460		0.746				22.5		1700		0.737

		22.4		1520		0.732				22.3		1540		0.732				22.6		1430		0.743				23		1460		0.748				22.6		1700		0.739

		22.4		1520		0.734				22.4		1540		0.734				22.6		1430		0.745				23		1460		0.75				22.6		1710		0.741

		22.5		1530		0.736				22.5		1550		0.736				22.7		1440		0.747				23.1		1460		0.752				22.7		1710		0.743

		22.6		1530		0.738				22.5		1550		0.738				22.8		1440		0.75				23.2		1470		0.754				22.8		1710		0.745

		22.6		1530		0.74				22.6		1550		0.742				22.8		1440		0.752				23.2		1470		0.757				22.8		1720		0.747

		22.7		1540		0.742				22.7		1560		0.745				23		1450		0.755				23.3		1470		0.761				22.9		1720		0.749

		22.8		1540		0.746				22.8		1560		0.747				23		1450		0.758				23.4		1480		0.763				23		1720		0.751

		22.9		1550		0.748				22.8		1560		0.749				23.1		1450		0.76				23.5		1480		0.765				23.1		1730		0.754

		22.9		1550		0.75				22.9		1570		0.751				23.1		1450		0.762				23.6		1480		0.767				23.1		1730		0.756

		23		1550		0.752				23		1570		0.753				23.2		1460		0.764				23.6		1480		0.769				23.2		1730		0.758

		23.1		1560		0.754				23		1570		0.755				23.3		1460		0.766				23.7		1490		0.771				23.3		1740		0.76

		23.1		1560		0.757				23.1		1570		0.757				23.3		1460		0.768				23.7		1490		0.773				23.3		1740		0.763

		23.2		1560		0.759				23.2		1580		0.759				23.4		1460		0.77				23.8		1490		0.775				23.4		1740		0.765

		23.2		1560		0.761				23.2		1580		0.762				23.5		1470		0.774				23.9		1500		0.779				23.4		1740		0.767

		23.3		1570		0.763				23.3		1580		0.764				23.6		1470		0.776				24		1500		0.781				23.5		1750		0.769

		23.4		1570		0.766				23.4		1590		0.766				23.6		1470		0.778				24.1		1500		0.783				23.6		1750		0.772

		23.5		1580		0.768				23.5		1590		0.769				23.7		1480		0.781				24.1		1500		0.786				23.6		1760		0.774

		23.5		1580		0.77				23.5		1590		0.771				23.8		1480		0.783				24.2		1510		0.788				23.7		1760		0.776

		23.6		1580		0.772				23.6		1600		0.773				23.8		1480		0.785				24.2		1510		0.79				23.8		1760		0.778

		23.6		1580		0.774				23.6		1600		0.775				23.9		1480		0.787				24.3		1510		0.792				23.8		1760		0.78

		23.7		1590		0.776				23.7		1600		0.777				24		1490		0.789				24.3		1510		0.794				23.9		1770		0.782

		23.8		1590		0.779				23.8		1610		0.781				24		1490		0.791				24.5		1520		0.798				24		1770		0.785

		23.8		1590		0.781				23.9		1610		0.783				24.1		1490		0.794				24.6		1520		0.8				24		1770		0.787

		23.9		1600		0.782				24		1610		0.785				24.2		1490		0.796				24.6		1520		0.802				24.1		1780		0.789

		24		1600		0.786				24		1610		0.787				24.2		1500		0.798				24.7		1530		0.804				24.2		1780		0.793

		24.1		1600		0.788				24.1		1620		0.789				24.3		1500		0.8				24.7		1530		0.806				24.3		1780		0.795

		24.1		1610		0.79				24.1		1620		0.791				24.3		1500		0.803				24.8		1530		0.808				24.4		1790		0.797

		24.2		1610		0.792				24.2		1620		0.793				24.4		1500		0.805				24.8		1530		0.81				24.4		1790		0.799

		24.3		1610		0.794				24.3		1630		0.795				24.5		1510		0.807				24.9		1530		0.813				24.5		1790		0.801

		24.3		1620		0.796				24.4		1630		0.8				24.5		1510		0.809				25.1		1540		0.817				24.5		1800		0.803

		24.4		1620		0.798				24.4		1630		0.802				24.6		1510		0.812				25.1		1540		0.819				24.6		1800		0.805

		24.5		1620		0.8				24.5		1640		0.804				24.7		1510		0.814				25.2		1540		0.821				24.7		1800		0.807

		24.5		1630		0.803				24.6		1640		0.806				24.8		1520		0.816				25.2		1550		0.823				24.8		1810		0.811

		24.6		1630		0.805				24.6		1640		0.808				24.8		1520		0.818				25.3		1550		0.825				24.8		1810		0.813

		24.6		1630		0.808				24.7		1640		0.81				24.9		1520		0.82				25.3		1550		0.827				24.9		1820		0.816

		24.7		1640		0.81				24.8		1650		0.812				24.9		1520		0.822				25.4		1550		0.829				25		1820		0.817

		24.8		1640		0.812				24.8		1650		0.814				25		1530		0.824				25.5		1560		0.831				25		1820		0.82

		24.9		1640		0.814				24.9		1650		0.818				25.1		1530		0.826				25.6		1560		0.836				25.1		1820		0.822

		24.9		1640		0.816				25		1660		0.82				25.2		1530		0.829				25.6		1560		0.838				25.1		1830		0.824

		25		1650		0.818				25		1660		0.822				25.2		1530		0.832				25.7		1570		0.84				25.2		1830		0.826

		25.1		1650		0.822				25.1		1660		0.824				25.3		1540		0.834				25.8		1570		0.842				25.3		1830		0.828

		25.2		1660		0.824				25.2		1670		0.827				25.3		1540		0.836				25.8		1570		0.844				25.4		1840		0.831

		25.2		1660		0.826				25.3		1670		0.829				25.4		1540		0.838				25.9		1570		0.846				25.4		1840		0.833

		25.3		1660		0.828				25.3		1670		0.831				25.5		1540		0.84				26		1580		0.848				25.5		1840		0.835

		25.3		1660		0.83				25.4		1670		0.833				25.5		1550		0.842				26.1		1580		0.85				25.6		1850		0.837

		25.4		1670		0.832				25.5		1680		0.836				25.6		1550		0.844				26.1		1580		0.854				25.6		1850		0.839

		25.5		1670		0.834				25.5		1680		0.838				25.7		1550		0.847				26.2		1580		0.856				25.7		1850		0.842

		25.5		1670		0.837				25.6		1680		0.84				25.8		1550		0.849				26.3		1590		0.858				25.8		1860		0.844

		25.6		1680		0.84				25.7		1690		0.842				25.8		1560		0.852				26.3		1590		0.86				25.8		1860		0.846

		25.7		1680		0.842				25.7		1690		0.844				25.9		1560		0.854				26.4		1590		0.863				25.9		1860		0.848

		25.7		1680		0.844				25.8		1690		0.846				25.9		1560		0.856				26.5		1590		0.865				26		1870		0.851

		25.8		1690		0.846				25.8		1690		0.849				26		1560		0.858				26.6		1600		0.867				26		1870		0.853

		25.9		1690		0.848				25.9		1700		0.851				26.1		1570		0.86				26.6		1600		0.869				26.1		1870		0.855

		25.9		1690		0.85				26		1700		0.853				26.1		1570		0.862				26.7		1600		0.873				26.1		1880		0.857

		26		1690		0.852				26.1		1700		0.857				26.2		1570		0.864				26.8		1610		0.875				26.2		1880		0.859

		26.1		1700		0.854				26.2		1710		0.859				26.2		1570		0.866				26.8		1610		0.877				26.3		1880		0.861

		26.2		1700		0.858				26.2		1710		0.861				26.3		1570		0.868				26.9		1610		0.879				26.4		1880		0.864

		26.2		1700		0.86				26.3		1710		0.863				26.4		1580		0.87				27		1610		0.881				26.4		1890		0.866

		26.3		1710		0.862				26.3		1720		0.865				26.4		1580		0.872				27.1		1610		0.883				26.5		1890		0.868

		26.3		1710		0.863				26.4		1720		0.867				26.5		1580		0.875				27.1		1620		0.886				26.6		1900		0.872

		26.4		1710		0.866				26.4		1720		0.869				26.6		1580		0.877				27.1		1620		0.887				26.7		1900		0.874

		26.5		1720		0.868				26.5		1720		0.872				26.6		1590		0.879				27.2		1620		0.89				26.7		1900		0.876

		26.5		1720		0.87				26.6		1730		0.874				26.7		1590		0.881				27.4		1630		0.894				26.8		1910		0.878

		26.6		1720		0.872				26.7		1730		0.877				26.8		1590		0.884				27.4		1630		0.896				26.8		1910		0.88

		26.7		1720		0.874				26.8		1730		0.879				26.9		1590		0.886				27.5		1630		0.898				26.9		1910		0.882

		26.7		1730		0.877				26.8		1730		0.881				26.9		1600		0.888				27.6		1630		0.9				27		1910		0.884

		26.8		1730		0.879				26.9		1740		0.883				27		1600		0.89				27.6		1640		0.902				27		1920		0.886

		26.9		1730		0.881				26.9		1740		0.885				27		1600		0.892				27.6		1640		0.904				27.1		1920		0.889

		26.9		1740		0.883				27		1740		0.887				27.1		1600		0.894				27.7		1640		0.906				27.2		1920		0.892

		27		1740		0.885				27.1		1740		0.889				27.2		1610		0.896				27.8		1640		0.908				27.2		1930		0.894

		27.1		1740		0.888				27.1		1750		0.892				27.2		1610		0.898				27.9		1650		0.913				27.3		1930		0.896

		27.1		1740		0.89				27.2		1750		0.894				27.3		1610		0.9				28		1650		0.915				27.4		1930		0.898

		27.2		1750		0.892				27.3		1750		0.896				27.4		1610		0.904				28		1650		0.917				27.5		1940		0.9

		27.2		1750		0.894				27.3		1760		0.899				27.4		1620		0.906				28.1		1650		0.919				27.5		1940		0.902

		27.4		1760		0.898				27.4		1760		0.901				27.5		1620		0.908				28.2		1660		0.921				27.5		1940		0.904

		27.4		1760		0.9				27.5		1760		0.903				27.6		1620		0.91				28.2		1660		0.923				27.6		1950		0.906

		27.5		1760		0.902				27.5		1760		0.905				27.6		1620		0.912				28.3		1660		0.925				27.7		1950		0.91

		27.6		1760		0.904				27.6		1770		0.907				27.7		1630		0.914				28.3		1660		0.927				27.8		1950		0.913

		27.6		1770		0.906				27.7		1770		0.911				27.8		1630		0.916				28.4		1670		0.93				27.9		1960		0.915

		27.7		1770		0.909				27.8		1770		0.913				27.8		1630		0.918				28.5		1670		0.932				27.9		1960		0.917

		27.7		1770		0.911				27.9		1780		0.915				27.9		1630		0.92				28.6		1670		0.934				28		1960		0.919

		27.8		1770		0.913				27.9		1780		0.917				28		1640		0.924				28.6		1670		0.936				28.1		1970		0.921

		27.9		1780		0.915				27.9		1780		0.919				28.1		1640		0.926				28.7		1680		0.938				28.1		1970		0.923

		28		1780		0.919				28		1790		0.921				28.1		1650		0.928				28.7		1680		0.94				28.2		1970		0.925

		28		1780		0.921				28.1		1790		0.923				28.2		1650		0.931				28.8		1680		0.943				28.2		1970		0.927

		28.1		1790		0.923				28.1		1790		0.925				28.2		1650		0.933				28.9		1680		0.945				28.3		1980		0.93

		28.2		1790		0.925				28.3		1790		0.929				28.3		1650		0.935				28.9		1690		0.947				28.4		1980		0.932

		28.3		1790		0.927				28.3		1800		0.931				28.4		1660		0.937				29.1		1690		0.95				28.5		1980		0.934

		28.3		1790		0.929				28.4		1800		0.933				28.4		1660		0.939				29.1		1690		0.952				28.5		1990		0.936

		28.4		1800		0.931				28.4		1800		0.935				28.6		1660		0.943				29.1		1690		0.954				28.6		1990		0.938

		28.4		1800		0.933				28.5		1810		0.937				28.6		1670		0.945				29.2		1700		0.956				28.6		1990		0.94

		28.5		1800		0.938				28.6		1810		0.939				28.7		1670		0.947				29.3		1700		0.958				28.7		2000		0.943

		28.6		1810		0.94				28.6		1810		0.941				28.8		1670		0.949				29.4		1700		0.96				28.8		2000		0.945

		28.7		1810		0.942				28.7		1810		0.943				28.8		1670		0.951				29.4		1700		0.963				28.9		2000		0.947

		28.7		1810		0.944				28.8		1820		0.945				28.9		1670		0.954				29.5		1710		0.965				28.9		2010		0.95

		28.8		1810		0.946				28.9		1820		0.95				28.9		1680		0.956				29.5		1710		0.967				29		2010		0.952

		28.9		1820		0.948				28.9		1820		0.952				29		1680		0.957				29.7		1710		0.971				29		2010		0.954

		28.9		1820		0.95				29		1830		0.954				29		1680		0.96				29.7		1710		0.973				29.1		2020		0.956

		29		1820		0.952				29.1		1830		0.956				29.1		1680		0.962				29.8		1720		0.975				29.2		2020		0.958

		29.1		1830		0.955				29.1		1830		0.958				29.2		1690		0.964				29.9		1720		0.977				29.2		2020		0.96

		29.1		1830		0.957				29.2		1830		0.96				29.2		1690		0.966				29.9		1720		0.979				29.3		2020		0.962

		29.2		1830		0.959				29.3		1840		0.962				29.3		1690		0.968				30		1720		0.981				29.4		2030		0.964

		29.3		1840		0.962				29.3		1840		0.964				29.4		1690		0.97				30		1720		0.983				29.5		2030		0.967

		29.3		1840		0.963				29.4		1840		0.968				29.4		1690		0.972				30.1		1730		0.985				29.5		2030		0.97

		29.4		1840		0.966				29.5		1850		0.97				29.5		1700		0.974				30.2		1730		0.988				29.6		2040		0.972

		29.5		1840		0.968				29.6		1850		0.972				29.6		1700		0.976				30.2		1730		0.99				29.7		2040		0.974

		29.5		1840		0.97				29.6		1850		0.974				29.6		1700		0.979				30.3		1730		0.993				29.7		2040		0.976

		29.6		1850		0.972				29.7		1860		0.976				29.7		1710		0.982				30.4		1740		0.995				29.8		2050		0.978

		29.7		1850		0.975				29.7		1860		0.979				29.8		1710		0.984				30.4		1740		0.997				29.8		2050		0.98

		29.7		1850		0.977				29.8		1860		0.981				29.9		1710		0.986				30.5		1740		0.999				29.9		2050		0.982

		29.8		1860		0.979				29.9		1860		0.983				29.9		1710		0.988				30.5		1740		1				30		2060		0.986

		29.9		1860		0.981				30		1870		0.987				30		1710		0.99				30.6		1750		1				30.1		2060		0.988

		29.9		1860		0.983				30		1870		0.989				30		1710		0.992				30.7		1750		1				30.1		2060		0.99

		30		1860		0.985				30.1		1870		0.991				30.1		1720		0.994				30.8		1750		1.01				30.2		2070		0.993

		30		1870		0.988				30.2		1880		0.993				30.2		1720		0.997				30.9		1750		1.01				30.3		2070		0.994

		30.1		1870		0.99				30.3		1880		0.995				30.2		1720		0.999				30.9		1760		1.01				30.4		2070		0.996

		30.2		1870		0.991				30.3		1880		0.997				30.3		1720		1				31		1760		1.02				30.4		2070		0.999

		30.3		1870		0.995				30.3		1880		1				30.4		1730		1				31		1760		1.02				30.4		2080		1

		30.3		1880		0.997				30.4		1890		1				30.4		1730		1				31.1		1760		1.02				30.6		2080		1

		30.4		1880		0.999				30.5		1890		1				30.5		1730		1.01				31.2		1760		1.02				30.6		2080		1.01

		30.5		1880		1				30.6		1890		1.01				30.6		1730		1.01				31.3		1770		1.02				30.7		2090		1.01

		30.5		1880		1				30.7		1890		1.01				30.6		1730		1.01				31.4		1770		1.03				30.8		2090		1.01

		30.6		1890		1				30.7		1900		1.01				30.8		1740		1.02				31.4		1770		1.03				30.8		2090		1.01

		30.6		1890		1.01				30.8		1900		1.01				30.8		1740		1.02				31.5		1770		1.03				30.9		2100		1.02

		30.7		1890		1.01				30.8		1900		1.02				30.9		1740		1.02				31.5		1780		1.03				30.9		2100		1.02

		30.8		1890		1.01				30.9		1910		1.02				31		1740		1.02				31.6		1780		1.04				31		2100		1.02

		30.9		1900		1.01				30.9		1910		1.02				31		1750		1.02				31.6		1780		1.04				31.1		2100		1.02

		30.9		1900		1.02				31		1910		1.02				31.1		1750		1.03				31.7		1780		1.04				31.1		2110		1.02

		31		1900		1.02				31.1		1910		1.02				31.1		1750		1.03				31.8		1790		1.04				31.2		2110		1.03

		31.1		1910		1.02				31.2		1920		1.03				31.2		1750		1.03				31.9		1790		1.05				31.3		2110		1.03

		31.1		1910		1.02				31.3		1920		1.03				31.3		1760		1.04				32		1790		1.05				31.3		2120		1.03

		31.2		1910		1.03				31.3		1920		1.03				31.4		1760		1.04				32		1790		1.05				31.4		2120		1.03

		31.3		1910		1.03				31.3		1920		1.03				31.4		1760		1.04				32.1		1800		1.05				31.4		2120		1.03

		31.3		1910		1.03				31.4		1930		1.04				31.5		1760		1.04				32.2		1800		1.05				31.5		2120		1.04

		31.4		1920		1.03				31.5		1930		1.04				31.5		1760		1.04				32.2		1800		1.06				31.6		2130		1.04

		31.4		1920		1.03				31.6		1930		1.04				31.6		1770		1.05				32.3		1800		1.06				31.7		2130		1.04

		31.5		1920		1.04				31.7		1940		1.04				31.7		1770		1.05				32.3		1800		1.06				31.8		2140		1.05

		31.6		1930		1.04				31.7		1940		1.05				31.8		1770		1.05				32.4		1810		1.06				31.8		2140		1.05

		31.6		1930		1.04				31.8		1940		1.05				31.9		1780		1.05				32.5		1810		1.07				31.9		2140		1.05

		31.7		1930		1.04				31.8		1940		1.05				31.9		1780		1.06				32.5		1810		1.07				32		2140		1.05

		31.8		1940		1.05				31.9		1950		1.05				32		1780		1.06				32.6		1810		1.07				32		2150		1.05

		31.8		1940		1.05				32		1950		1.05				32.1		1780		1.06				32.7		1820		1.07				32.1		2150		1.06

		31.9		1940		1.05				32		1950		1.06				32.1		1780		1.06				32.7		1820		1.07				32.1		2150		1.06

		32		1950		1.05				32.1		1950		1.06				32.2		1790		1.06				32.8		1820		1.08				32.2		2150		1.06

		32.1		1950		1.06				32.2		1960		1.06				32.3		1790		1.07				32.9		1820		1.08				32.3		2160		1.06

		32.1		1950		1.06				32.3		1960		1.06				32.3		1790		1.07				32.9		1820		1.08				32.4		2160		1.07

		32.2		1960		1.06				32.3		1960		1.07				32.4		1790		1.07				33		1830		1.08				32.5		2170		1.07

		32.3		1960		1.06				32.4		1960		1.07				32.5		1800		1.07				33.1		1830		1.09				32.5		2170		1.07

		32.3		1960		1.06				32.4		1970		1.07				32.6		1800		1.08				33.2		1830		1.09				32.6		2170		1.07

		32.4		1960		1.07				32.5		1970		1.07				32.6		1800		1.08				33.2		1840		1.09				32.6		2180		1.07

		32.4		1960		1.07				32.6		1970		1.07				32.7		1800		1.08				33.3		1840		1.09				32.7		2180		1.08

		32.6		1970		1.07				32.6		1970		1.08				32.7		1800		1.08				33.4		1840		1.1				32.8		2180		1.08

		32.6		1970		1.07				32.7		1980		1.08				32.8		1810		1.08				33.4		1840		1.1				32.8		2190		1.08

		32.7		1970		1.08				32.8		1980		1.08				32.9		1810		1.09				33.5		1840		1.1				32.9		2190		1.08

		32.8		1980		1.08				32.8		1980		1.08				32.9		1810		1.09				33.6		1850		1.1				33		2190		1.09

		32.8		1980		1.08				32.9		1980		1.09				33		1810		1.09				33.6		1850		1.1				33		2190		1.09

		32.9		1980		1.08				33		1990		1.09				33.1		1820		1.1				33.7		1850		1.11				33.1		2200		1.09

		32.9		1980		1.08				33		1990		1.09				33.2		1820		1.1				33.8		1850		1.11				33.2		2200		1.09

		33		1990		1.09				33.1		1990		1.09				33.3		1820		1.1				33.8		1860		1.11				33.3		2200		1.09

		33.1		1990		1.09				33.2		2000		1.09				33.3		1820		1.1				33.9		1860		1.11				33.3		2200		1.1

		33.2		1990		1.09				33.3		2000		1.1				33.4		1820		1.1				33.9		1860		1.11				33.4		2210		1.1

		33.3		2000		1.09				33.3		2000		1.1				33.4		1830		1.11				34		1860		1.12				33.5		2210		1.1

		33.3		2000		1.1				33.4		2010		1.1				33.5		1830		1.11				34.1		1860		1.12				33.5		2220		1.1

		33.4		2000		1.1				33.5		2010		1.1				33.6		1830		1.11				34.1		1870		1.12				33.6		2220		1.11

		33.4		2000		1.1				33.5		2010		1.1				33.7		1830		1.11				34.2		1870		1.12				33.7		2220		1.11

		33.5		2010		1.1				33.6		2010		1.11				33.7		1840		1.12				34.3		1870		1.13				33.7		2220		1.11

		33.6		2010		1.1				33.6		2010		1.11				33.8		1840		1.12				34.3		1870		1.13				33.8		2230		1.11

		33.6		2010		1.11				33.7		2020		1.11				33.9		1840		1.12				34.4		1880		1.13				33.8		2230		1.11

		33.7		2010		1.11				33.8		2020		1.11				33.9		1840		1.12				34.5		1880		1.13				33.9		2230		1.12

		33.8		2020		1.11				33.8		2020		1.12				34		1850		1.12				34.5		1880		1.13				34		2240		1.12

		33.8		2020		1.11				33.9		2020		1.12				34		1850		1.13				34.6		1880		1.14				34.1		2240		1.12

		33.9		2020		1.12				34		2030		1.12				34.2		1850		1.13				34.7		1890		1.14				34.1		2240		1.12

		33.9		2020		1.12				34		2030		1.12				34.3		1860		1.13				34.8		1890		1.14				34.2		2240		1.13

		34		2030		1.12				34.1		2030		1.12				34.3		1860		1.13				34.9		1890		1.14				34.3		2250		1.13

		34.1		2030		1.12				34.2		2030		1.13				34.4		1860		1.14				34.9		1890		1.15				34.3		2250		1.13

		34.1		2030		1.12				34.2		2040		1.13				34.4		1860		1.14				35		1890		1.15				34.4		2250		1.13

		34.2		2030		1.13				34.3		2040		1.13				34.5		1860		1.14				35		1900		1.15				34.5		2250		1.13

		34.3		2040		1.13				34.4		2040		1.13				34.5		1870		1.14				35.1		1900		1.15				34.5		2260		1.14

		34.4		2040		1.13				34.5		2050		1.14				34.6		1870		1.15				35.1		1900		1.15				34.6		2260		1.14

		34.4		2040		1.13				34.5		2050		1.14				34.8		1870		1.15				35.2		1900		1.16				34.7		2260		1.14

		34.5		2050		1.14				34.6		2050		1.14				34.8		1870		1.15				35.3		1910		1.16				34.7		2270		1.14

		34.6		2050		1.14				34.7		2050		1.14				34.9		1880		1.15				35.4		1910		1.16				34.8		2270		1.14

		34.6		2050		1.14				34.7		2060		1.15				34.9		1880		1.16				35.4		1910		1.16				34.8		2270		1.15

		34.7		2050		1.14				34.8		2060		1.15				35		1880		1.16				35.5		1910		1.17				34.9		2270		1.15

		34.8		2050		1.15				34.8		2060		1.15				35.1		1880		1.16				35.5		1910		1.17				35		2280		1.15

		34.8		2060		1.15				34.9		2060		1.15				35.1		1890		1.16				35.6		1920		1.17				35		2280		1.15

		34.9		2060		1.15				35		2070		1.15				35.2		1890		1.16				35.7		1920		1.17				35.1		2280		1.16

		35		2060		1.15				35		2070		1.16				35.3		1890		1.17				35.8		1920		1.17				35.2		2290		1.16

		35		2070		1.15				35.1		2070		1.16				35.3		1890		1.17				35.9		1920		1.18				35.3		2290		1.16

		35.1		2070		1.16				35.2		2070		1.16				35.4		1890		1.17				35.9		1930		1.18				35.3		2290		1.16

		35.2		2070		1.16				35.2		2070		1.16				35.5		1900		1.17				36		1930		1.18				35.4		2300		1.17

		35.3		2070		1.16				35.3		2080		1.16				35.5		1900		1.18				36		1930		1.18				35.4		2300		1.17

		35.3		2080		1.16				35.4		2080		1.17				35.6		1900		1.18				36.1		1930		1.19				35.5		2300		1.17

		35.4		2080		1.16				35.4		2080		1.17				35.7		1900		1.18				36.1		1930		1.19				35.6		2300		1.17

		35.4		2080		1.17				35.5		2080		1.17				35.7		1910		1.18				36.2		1940		1.19				35.6		2310		1.17

		35.5		2080		1.17				35.6		2090		1.17				35.8		1910		1.18				36.3		1940		1.19				35.8		2310		1.18

		35.6		2090		1.17				35.7		2090		1.18				35.9		1910		1.19				36.3		1940		1.19				35.8		2320		1.18

		35.6		2090		1.17				35.7		2090		1.18				35.9		1910		1.19				36.4		1940		1.2				35.9		2320		1.18

		35.7		2090		1.18				35.7		2090		1.18				36		1920		1.19				36.5		1950		1.2				36		2320		1.18

		35.8		2090		1.18				35.8		2100		1.18				36.1		1920		1.19				36.6		1950		1.2				36		2320		1.19

		35.8		2100		1.18				35.9		2100		1.18				36.2		1920		1.2				36.6		1950		1.2				36.1		2330		1.19

		35.9		2100		1.18				35.9		2100		1.19				36.2		1920		1.2				36.7		1950		1.21				36.2		2330		1.19

		35.9		2100		1.18				36		2100		1.19				36.3		1920		1.2				36.8		1960		1.21				36.2		2330		1.19

		36.1		2110		1.19				36.1		2110		1.19				36.3		1930		1.2				36.8		1960		1.21				36.3		2330		1.19

		36.2		2110		1.19				36.2		2110		1.19				36.5		1930		1.21				36.9		1960		1.21				36.3		2340		1.2

		36.2		2110		1.19				36.2		2110		1.2				36.5		1930		1.21				37		1960		1.22				36.4		2340		1.2

		36.3		2110		1.19				36.3		2120		1.2				36.6		1940		1.21				37.1		1970		1.22				36.5		2340		1.2

		36.3		2120		1.2				36.4		2120		1.2				36.6		1940		1.21				37.2		1970		1.22				36.5		2340		1.2

		36.4		2120		1.2				36.4		2120		1.2				36.7		1940		1.21				37.2		1970		1.22				36.6		2350		1.2

		36.5		2120		1.2				36.5		2120		1.2				36.8		1940		1.22				37.3		1970		1.23				36.6		2350		1.21

		36.5		2120		1.2				36.5		2130		1.21				36.8		1940		1.22				37.3		1970		1.23				36.7		2350		1.21

		36.6		2130		1.21				36.6		2130		1.21				36.9		1950		1.22				37.4		1980		1.23				36.7		2360		1.21

		36.7		2130		1.21				36.7		2130		1.21				37		1950		1.23				37.5		1980		1.23				36.9		2360		1.22

		36.8		2130		1.21				36.8		2140		1.21				37.1		1950		1.23				37.6		1980		1.24				37		2360		1.22

		36.8		2140		1.21				36.8		2140		1.22				37.2		1950		1.23				37.6		1990		1.24				37		2370		1.22

		36.9		2140		1.22				36.9		2140		1.22				37.2		1960		1.23				37.7		1990		1.24				37.1		2370		1.22

		37		2140		1.22				37		2140		1.22				37.3		1960		1.23				37.8		1990		1.24				37.1		2370		1.22

		37		2140		1.22				37		2150		1.22				37.3		1960		1.24				37.8		1990		1.24				37.2		2370		1.23

		37.1		2150		1.22				37.1		2150		1.22				37.4		1960		1.24				37.9		1990		1.25				37.3		2380		1.23

		37.2		2150		1.23				37.2		2150		1.23				37.5		1970		1.24				38		2000		1.25				37.3		2380		1.23

		37.2		2150		1.23				37.2		2150		1.23				37.6		1970		1.24				38		2000		1.25				37.4		2380		1.23

		37.3		2150		1.23				37.3		2160		1.23				37.6		1970		1.25				38.2		2000		1.25				37.5		2390		1.24

		37.4		2160		1.23				37.4		2160		1.23				37.7		1970		1.25				38.2		2000		1.26				37.5		2390		1.24

		37.4		2160		1.23				37.4		2160		1.24				37.8		1980		1.25				38.3		2010		1.26				37.6		2390		1.24

		37.5		2160		1.24				37.5		2160		1.24				37.8		1980		1.25				38.3		2010		1.26				37.7		2390		1.24

		37.6		2160		1.24				37.6		2160		1.24				37.9		1980		1.25				38.4		2010		1.26				37.7		2400		1.24

		37.6		2170		1.24				37.7		2170		1.24				37.9		1980		1.26				38.4		2010		1.26				37.8		2400		1.25

		37.7		2170		1.24				37.7		2170		1.24				38		1980		1.26				38.5		2010		1.27				37.8		2400		1.25

		37.8		2170		1.25				37.7		2170		1.25				38.1		1990		1.26				38.6		2020		1.27				37.9		2410		1.25

		37.9		2180		1.25				37.8		2180		1.25				38.2		1990		1.26				38.6		2020		1.27				38		2410		1.25

		37.9		2180		1.25				38		2180		1.25				38.3		1990		1.27				38.8		2020		1.27				38.1		2410		1.25

		38		2180		1.25				38		2180		1.25				38.3		1990		1.27				38.8		2020		1.28				38.1		2410		1.26

		38		2180		1.25				38.1		2190		1.26				38.4		2000		1.27				38.8		2030		1.28				38.2		2420		1.26

		38.1		2190		1.26				38.1		2190		1.26				38.5		2000		1.27				38.9		2030		1.28				38.3		2420		1.26

		38.2		2190		1.26				38.2		2190		1.26				38.5		2000		1.28				39		2030		1.28				38.3		2420		1.26

		38.2		2190		1.26				38.3		2190		1.26				38.6		2000		1.28				39.1		2030		1.28				38.4		2420		1.27

		38.3		2200		1.26				38.3		2200		1.27				38.6		2000		1.28				39.1		2030		1.29				38.4		2430		1.27

		38.4		2200		1.27				38.4		2200		1.27				38.8		2010		1.28				39.2		2040		1.29				38.5		2430		1.27

		38.5		2200		1.27				38.5		2200		1.27				38.8		2010		1.29				39.3		2040		1.29				38.6		2440		1.27

		38.5		2200		1.27				38.6		2210		1.27				38.9		2010		1.29				39.4		2040		1.29				38.7		2440		1.28

		38.6		2210		1.27				38.6		2210		1.28				39		2010		1.29				39.4		2050		1.3				38.7		2440		1.28

		38.7		2210		1.28				38.7		2210		1.28				39		2020		1.29				39.5		2050		1.3				38.8		2440		1.28

		38.7		2210		1.28				38.8		2210		1.28				39.1		2020		1.29				39.5		2050		1.3				38.9		2450		1.28

		38.8		2210		1.28				38.8		2210		1.28				39.1		2020		1.3				39.6		2050		1.3				39		2450		1.28

		38.8		2220		1.28				38.9		2220		1.28				39.2		2020		1.3				39.7		2060		1.31				39		2450		1.29

		39		2220		1.29				39		2220		1.29				39.3		2030		1.3				39.8		2060		1.31				39.1		2460		1.29

		39.1		2220		1.29				39		2220		1.29				39.3		2030		1.3				39.9		2060		1.31				39.2		2460		1.29

		39.1		2230		1.29				39.1		2220		1.29				39.4		2030		1.31				39.9		2060		1.31				39.2		2460		1.29

		39.2		2230		1.29				39.1		2230		1.29				39.5		2030		1.31				40		2070		1.32				39.3		2470		1.3

		39.2		2230		1.29				39.2		2230		1.3				39.5		2040		1.31				40		2070		1.32				39.3		2470		1.3

		39.3		2230		1.3				39.3		2230		1.3				39.6		2040		1.31				40.1		2070		1.32				39.4		2470		1.3

		39.4		2230		1.3				39.4		2230		1.3				39.7		2040		1.31				40.2		2070		1.32				39.5		2480		1.3

		39.4		2240		1.3				39.4		2240		1.3				39.7		2040		1.32				40.2		2080		1.32				39.5		2480		1.3

		39.5		2240		1.3				39.5		2240		1.3				39.8		2040		1.32				40.3		2080		1.33				39.6		2480		1.31

		39.6		2250		1.31				39.5		2240		1.31				39.8		2050		1.32				40.4		2080		1.33				39.7		2490		1.31

		39.7		2250		1.31				39.6		2240		1.31				40		2050		1.32				40.5		2080		1.33				39.8		2490		1.31

		39.7		2250		1.31				39.7		2250		1.31				40		2050		1.33				40.5		2080		1.33				39.8		2500		1.31

		39.8		2250		1.31				39.8		2250		1.31				40.1		2050		1.33				40.6		2090		1.34				39.9		2500		1.32

		39.8		2250		1.31				39.9		2250		1.32				40.2		2060		1.33				40.6		2090		1.34				40		2500		1.32

		39.9		2260		1.32				39.9		2260		1.32				40.2		2060		1.33				40.7		2090		1.34				40		2510		1.32

		40		2260		1.32				40		2260		1.32				40.3		2060		1.33				40.8		2090		1.34				40.1		2510		1.32

		40.1		2260		1.32				40.1		2260		1.32				40.3		2060		1.34				40.8		2090		1.34				40.2		2510		1.32

		40.1		2260		1.32				40.1		2260		1.32				40.4		2060		1.34				40.9		2100		1.35				40.3		2520		1.33

		40.2		2270		1.33				40.1		2270		1.33				40.6		2070		1.34				41		2100		1.35				40.3		2520		1.33

		40.3		2270		1.33				40.3		2270		1.33				40.6		2070		1.34				41		2100		1.35				40.4		2520		1.33

		40.3		2270		1.33				40.3		2270		1.33				40.7		2070		1.35				41.1		2100		1.35				40.4		2520		1.33

		40.4		2280		1.33				40.4		2280		1.33				40.7		2080		1.35				41.2		2110		1.35				40.5		2530		1.34

		40.4		2280		1.33				40.5		2280		1.34				40.8		2080		1.35				41.2		2110		1.36				40.6		2530		1.34

		40.5		2280		1.34				40.6		2280		1.34				40.8		2080		1.35				41.3		2110		1.36				40.6		2530		1.34

		40.6		2280		1.34				40.6		2290		1.34				40.9		2080		1.36				41.4		2110		1.36				40.7		2530		1.34

		40.7		2290		1.34				40.6		2290		1.34				41		2080		1.36				41.4		2110		1.36				40.8		2540		1.35

		40.7		2290		1.34				40.7		2290		1.35				41.1		2090		1.36				41.5		2120		1.37				40.9		2540		1.35

		40.8		2290		1.35				40.8		2300		1.35				41.2		2090		1.36				41.6		2120		1.37				40.9		2540		1.35

		40.9		2300		1.35				40.9		2300		1.35				41.2		2090		1.37				41.7		2120		1.37				41		2550		1.35

		41		2300		1.35				41		2300		1.35				41.3		2100		1.37				41.7		2120		1.37				41		2550		1.35

		41		2300		1.35				41.1		2310		1.36				41.3		2100		1.37				41.8		2130		1.38				41.1		2550		1.36

		41.1		2300		1.36				41.1		2310		1.36				41.4		2100		1.37				41.9		2130		1.38				41.1		2550		1.36

		41.2		2310		1.36				41.2		2310		1.36				41.5		2100		1.37				41.9		2130		1.38				41.2		2560		1.36

		41.2		2310		1.36				41.2		2310		1.36				41.6		2100		1.38				42		2130		1.38				41.3		2560		1.36

		41.3		2310		1.36				41.3		2320		1.36				41.6		2110		1.38				42		2130		1.38				41.4		2560		1.37

		41.4		2320		1.36				41.4		2320		1.37				41.7		2110		1.38				42.2		2140		1.39				41.5		2570		1.37

		41.4		2320		1.37				41.5		2330		1.37				41.8		2110		1.38				42.2		2140		1.39				41.5		2570		1.37

		41.5		2320		1.37				41.5		2330		1.37				41.9		2110		1.39				42.3		2140		1.39				41.6		2570		1.37

		41.5		2320		1.37				41.6		2330		1.37				41.9		2120		1.39				42.4		2140		1.39				41.6		2570		1.37

		41.6		2330		1.37				41.6		2330		1.38				42		2120		1.39				42.4		2150		1.4				41.7		2580		1.38

		41.7		2330		1.37				41.7		2330		1.38				42		2120		1.39				42.5		2150		1.4				41.8		2580		1.38

		41.7		2330		1.38				41.8		2340		1.38				42.1		2120		1.39				42.6		2150		1.4				41.9		2580		1.38

		41.8		2330		1.38				41.8		2340		1.38				42.2		2120		1.4				42.6		2150		1.4				41.9		2590		1.38

		41.9		2340		1.38				41.9		2340		1.38				42.2		2130		1.4				42.7		2160		1.41				42		2590		1.39

		41.9		2340		1.38				42		2350		1.39				42.3		2130		1.4				42.8		2160		1.41				42.1		2590		1.39

		42		2340		1.39				42		2350		1.39				42.4		2130		1.4				42.8		2160		1.41				42.1		2590		1.39

		42.1		2340		1.39				42.1		2350		1.39				42.4		2130		1.41				42.9		2160		1.41				42.2		2600		1.39

		42.1		2350		1.39				42.2		2350		1.39				42.5		2140		1.41				43		2160		1.42				42.2		2600		1.39

		42.2		2350		1.39				42.3		2350		1.4				42.6		2140		1.41				43.1		2160		1.42				42.3		2600		1.4

		42.2		2350		1.39				42.3		2360		1.4				42.6		2140		1.41				43.1		2170		1.42				42.5		2610		1.4

		42.3		2350		1.4				42.4		2360		1.4				42.7		2140		1.41				43.2		2170		1.42				42.5		2610		1.4

		42.4		2360		1.4				42.5		2360		1.4				42.8		2140		1.42				43.3		2170		1.43				42.6		2610		1.4

		42.5		2360		1.4				42.5		2360		1.41				42.9		2150		1.42				43.3		2170		1.43				42.6		2620		1.41

		42.6		2360		1.41				42.6		2370		1.41				42.9		2150		1.42				43.4		2180		1.43				42.7		2620		1.41

		42.6		2360		1.41				42.7		2370		1.41				43		2150		1.42				43.5		2180		1.43				42.7		2620		1.41

		42.7		2370		1.41				42.7		2370		1.41				43.1		2150		1.43				43.6		2180		1.43				42.8		2620		1.41

		42.7		2370		1.41				42.8		2370		1.41				43.1		2160		1.43				43.6		2180		1.44				42.9		2630		1.42

		42.8		2370		1.41				42.9		2370		1.42				43.2		2160		1.43				43.7		2180		1.44				43		2630		1.42

		42.9		2370		1.42				42.9		2380		1.42				43.3		2160		1.43				43.7		2190		1.44				43.1		2630		1.42

		42.9		2380		1.42				43		2380		1.42				43.3		2160		1.44				43.8		2190		1.44				43.1		2640		1.42

		43		2380		1.42				43.1		2380		1.42				43.4		2170		1.44				43.9		2190		1.45				43.2		2640		1.43

		43.1		2380		1.42				43.2		2390		1.43				43.5		2170		1.44				44		2190		1.45				43.2		2640		1.43

		43.2		2380		1.42				43.2		2390		1.43				43.5		2170		1.44				44		2190		1.45				43.3		2650		1.43

		43.2		2390		1.43				43.3		2390		1.43				43.6		2170		1.44				44.1		2200		1.45				43.4		2650		1.43

		43.3		2390		1.43				43.3		2390		1.43				43.7		2170		1.45				44.2		2200		1.45				43.4		2650		1.43

		43.4		2390		1.43				43.4		2390		1.43				43.7		2180		1.45				44.2		2200		1.46				43.5		2650		1.44

		43.4		2390		1.43				43.5		2400		1.44				43.8		2180		1.45				44.3		2200		1.46				43.6		2660		1.44

		43.5		2400		1.44				43.5		2400		1.44				43.9		2180		1.45				44.3		2210		1.46				43.7		2660		1.44

		43.6		2400		1.44				43.6		2400		1.44				43.9		2180		1.46				44.4		2210		1.46				43.8		2660		1.44

		43.6		2400		1.44				43.7		2400		1.44				44		2180		1.46				44.5		2210		1.47				43.8		2670		1.45

		43.7		2400		1.44				43.7		2410		1.45				44.1		2190		1.46				44.5		2210		1.47				43.9		2670		1.45

		43.8		2410		1.44				43.8		2410		1.45				44.1		2190		1.46				44.6		2210		1.47				44		2670		1.45

		43.8		2410		1.45				43.9		2410		1.45				44.2		2190		1.46				44.6		2220		1.47				44		2670		1.45

		43.9		2410		1.45				43.9		2410		1.45				44.2		2190		1.47				44.7		2220		1.47				44.1		2680		1.45

		43.9		2410		1.45				44		2420		1.45				44.3		2190		1.47				44.8		2220		1.48				44.1		2680		1.46

		44		2420		1.45				44.1		2420		1.46				44.4		2200		1.47				44.8		2220		1.48				44.2		2680		1.46

		44.1		2420		1.45				44.2		2420		1.46				44.5		2200		1.47				45		2230		1.48				44.3		2690		1.46

		44.1		2420		1.46				44.2		2430		1.46				44.6		2200		1.48				45		2230		1.48				44.3		2690		1.46

		44.2		2430		1.46				44.3		2430		1.46				44.6		2200		1.48				45.1		2230		1.49				44.4		2690		1.47

		44.3		2430		1.46				44.4		2430		1.47				44.7		2210		1.48				45.2		2230		1.49				44.5		2690		1.47

		44.3		2430		1.46				44.5		2430		1.47				44.7		2210		1.48				45.2		2240		1.49				44.5		2700		1.47

		44.4		2430		1.47				44.5		2430		1.47				44.8		2210		1.49				45.3		2240		1.49				44.6		2700		1.47

		44.5		2440		1.47				44.6		2440		1.47				44.9		2210		1.49				45.3		2240		1.49				44.7		2700		1.47

		44.6		2440		1.47				44.6		2440		1.48				44.9		2210		1.49				45.4		2240		1.5				44.8		2710		1.48

		44.6		2440		1.47				44.7		2440		1.48				45.1		2220		1.49				45.5		2250		1.5				44.8		2710		1.48

		44.7		2440		1.47				44.8		2450		1.48				45.1		2220		1.5				45.6		2250		1.5				44.9		2710		1.48

		44.7		2450		1.48				44.8		2450		1.48				45.2		2220		1.5				45.6		2250		1.5				45		2720		1.48

		44.8		2450		1.48				44.9		2450		1.48				45.3		2220		1.5				45.7		2250		1.51				45		2720		1.49

		44.9		2450		1.48				45		2450		1.49				45.3		2230		1.5				45.8		2250		1.51				45.1		2720		1.49

		45		2460		1.48				45		2450		1.49				45.4		2230		1.5				45.9		2260		1.51				45.1		2730		1.49

		45		2460		1.49				45.1		2460		1.49				45.4		2230		1.51				45.9		2260		1.51				45.2		2730		1.49

		45.1		2460		1.49				45.1		2460		1.49				45.5		2230		1.51				46		2260		1.52				45.3		2730		1.5

		45.1		2460		1.49				45.2		2460		1.5				45.6		2230		1.51				46		2260		1.52				45.4		2730		1.5

		45.2		2470		1.49				45.3		2470		1.5				45.7		2240		1.51				46.1		2260		1.52				45.4		2740		1.5

		45.2		2470		1.49				45.4		2470		1.5				45.7		2240		1.52				46.2		2270		1.52				45.5		2740		1.5

		45.4		2470		1.5				45.5		2470		1.5				45.8		2240		1.52				46.3		2270		1.53				45.6		2740		1.5

		45.4		2470		1.5				45.5		2470		1.51				45.9		2240		1.52				46.3		2270		1.53				45.6		2750		1.51

		45.5		2480		1.5				45.6		2480		1.51				45.9		2250		1.52				46.4		2270		1.53				45.7		2750		1.51

		45.5		2480		1.5				45.6		2480		1.51				46		2250		1.52				46.5		2270		1.53				45.7		2750		1.51

		45.6		2480		1.51				45.7		2480		1.51				46.1		2250		1.53				46.5		2280		1.53				45.8		2750		1.51

		45.7		2480		1.51				45.8		2480		1.51				46.1		2250		1.53				46.6		2280		1.54				45.9		2760		1.52

		45.7		2490		1.51				45.9		2490		1.52				46.2		2250		1.53				46.6		2280		1.54				46		2760		1.52

		45.8		2490		1.51				45.9		2490		1.52				46.3		2260		1.54				46.8		2280		1.54				46		2760		1.52

		45.9		2490		1.51				46		2490		1.52				46.4		2260		1.54				46.9		2280		1.54				46.1		2760		1.52

		46		2500		1.52				46.1		2490		1.52				46.4		2260		1.54				46.9		2290		1.55				46.1		2770		1.52

		46.1		2500		1.52				46.1		2500		1.53				46.5		2270		1.54				47		2290		1.55				46.2		2770		1.53

		46.1		2500		1.52				46.2		2500		1.53				46.6		2270		1.54				47		2290		1.55				46.3		2770		1.53

		46.2		2500		1.52				46.2		2500		1.53				46.6		2270		1.55				47.1		2290		1.55				46.3		2780		1.53

		46.2		2510		1.53				46.3		2500		1.53				46.7		2270		1.55				47.1		2290		1.55				46.4		2780		1.53

		46.3		2510		1.53				46.4		2510		1.53				46.8		2270		1.55				47.2		2290		1.56				46.5		2780		1.54

		46.3		2510		1.53				46.4		2510		1.54				46.9		2280		1.55				47.3		2300		1.56				46.5		2790		1.54

		46.4		2510		1.53				46.5		2510		1.54				46.9		2280		1.56				47.4		2300		1.56				46.6		2790		1.54

		46.5		2520		1.54				46.6		2510		1.54				47		2280		1.56				47.5		2300		1.56				46.7		2790		1.54

		46.6		2520		1.54				46.7		2510		1.54				47.1		2290		1.56				47.6		2300		1.57				46.7		2790		1.54

		46.6		2520		1.54				46.7		2520		1.54				47.1		2290		1.56				47.6		2310		1.57				46.8		2800		1.55

		46.7		2530		1.54				46.8		2520		1.55				47.2		2290		1.56				47.7		2310		1.57				46.9		2800		1.55

		46.8		2530		1.55				46.8		2520		1.55				47.2		2290		1.57				47.7		2310		1.57				46.9		2800		1.55

		46.8		2530		1.55				46.9		2520		1.55				47.3		2290		1.57				47.8		2310		1.58				47		2800		1.55

		46.9		2530		1.55				47		2530		1.55				47.4		2300		1.57				47.8		2310		1.58				47.1		2810		1.56

		47		2540		1.55				47.1		2530		1.56				47.5		2300		1.57				47.9		2310		1.58				47.2		2810		1.56

		47.1		2540		1.56				47.1		2530		1.56				47.6		2300		1.58				48		2320		1.58				47.2		2810		1.56

		47.2		2540		1.56				47.2		2530		1.56				47.6		2300		1.58				48.1		2320		1.58				47.3		2820		1.56

		47.2		2550		1.56				47.3		2540		1.56				47.6		2300		1.58				48.1		2320		1.59				47.4		2820		1.56

		47.3		2550		1.56				47.3		2540		1.56				47.7		2300		1.58				48.2		2320		1.59				47.4		2820		1.57

		47.4		2550		1.56				47.4		2540		1.57				47.8		2310		1.58				48.2		2320		1.59				47.5		2820		1.57

		47.4		2550		1.57				47.4		2540		1.57				47.8		2310		1.59				48.3		2330		1.59				47.5		2830		1.57

		47.5		2550		1.57				47.5		2550		1.57				47.9		2310		1.59				48.4		2330		1.6				47.7		2830		1.57

		47.5		2560		1.57				47.6		2550		1.58				48		2320		1.59				48.5		2330		1.6				47.7		2830		1.58

		47.6		2560		1.57				47.7		2550		1.58				48.1		2320		1.59				48.5		2330		1.6				47.8		2830		1.58

		47.7		2560		1.58				47.7		2550		1.58				48.1		2320		1.6				48.6		2330		1.6				47.9		2840		1.58

		47.7		2570		1.58				47.8		2560		1.58				48.2		2320		1.6				48.6		2340		1.6				47.9		2840		1.58

		47.8		2570		1.58				47.9		2560		1.58				48.3		2320		1.6				48.7		2340		1.61				48		2840		1.58

		47.9		2570		1.58				47.9		2560		1.59				48.3		2330		1.6				48.8		2340		1.61				48		2840		1.59

		47.9		2570		1.58				48		2560		1.59				48.4		2330		1.6				48.8		2340		1.61				48.1		2850		1.59

		48		2580		1.59				48		2570		1.59				48.5		2330		1.61				48.9		2340		1.61				48.1		2850		1.59

		48.1		2580		1.59				48.2		2570		1.59				48.6		2330		1.61				49		2340		1.61				48.2		2850		1.59

		48.1		2580		1.59				48.2		2570		1.6				48.6		2330		1.61				49		2350		1.62				48.3		2860		1.6

		48.2		2580		1.59				48.3		2580		1.6				48.7		2340		1.62				49.1		2350		1.62				48.4		2860		1.6

		48.3		2590		1.6				48.4		2580		1.6				48.8		2340		1.62				49.2		2350		1.62				48.4		2860		1.6

		48.4		2590		1.6				48.4		2580		1.6				48.9		2340		1.62				49.3		2350		1.62				48.5		2860		1.6

		48.4		2590		1.6				48.5		2580		1.6				48.9		2340		1.62				49.3		2350		1.63				48.5		2870		1.6

		48.5		2590		1.6				48.6		2580		1.61				49		2340		1.62				49.4		2360		1.63				48.6		2870		1.61

		48.5		2600		1.6				48.6		2590		1.61				49		2350		1.63				49.4		2360		1.63				48.7		2870		1.61

		48.6		2600		1.61				48.7		2590		1.61				49.1		2350		1.63				49.5		2360		1.63				48.7		2870		1.61

		48.7		2600		1.61				48.8		2590		1.61				49.2		2350		1.63				49.5		2360		1.63				48.9		2880		1.61

		48.7		2600		1.61				48.8		2600		1.62				49.3		2350		1.63				49.6		2360		1.64				48.9		2880		1.62

		48.8		2610		1.61				48.9		2600		1.62				49.4		2360		1.64				49.8		2370		1.64				49		2880		1.62

		48.9		2610		1.62				49		2600		1.62				49.4		2360		1.64				49.8		2370		1.64				49		2890		1.62

		49		2610		1.62				49		2600		1.62				49.5		2360		1.64				49.9		2370		1.64				49.1		2890		1.62

		49		2610		1.62				49.1		2600		1.62				49.5		2360		1.64				49.9		2370		1.65				49.2		2890		1.63

		49.1		2620		1.62				49.2		2610		1.63				49.6		2360		1.64				50		2370		1.65				49.3		2890		1.63

		49.1		2620		1.62				49.3		2610		1.63				49.6		2370		1.65				50		2380		1.65				49.3		2900		1.63

		49.2		2620		1.63				49.3		2610		1.63				49.8		2370		1.65				50.1		2380		1.65				49.4		2900		1.63

		49.3		2620		1.63				49.3		2610		1.63				49.9		2370		1.65				50.2		2380		1.66				49.5		2900		1.64

		49.3		2630		1.63				49.4		2620		1.64				49.9		2370		1.65				50.3		2380		1.66				49.6		2910		1.64

		49.5		2630		1.63				49.5		2620		1.64				50		2370		1.66				50.4		2380		1.66				49.6		2910		1.64

		49.5		2630		1.64				49.6		2620		1.64				50		2380		1.66				50.4		2390		1.66				49.7		2910		1.64

		49.6		2640		1.64				49.6		2620		1.64				50.1		2380		1.66				50.5		2390		1.67				49.7		2910		1.64

		49.7		2640		1.64				49.7		2630		1.64				50.2		2380		1.66				50.5		2390		1.67				49.8		2920		1.65

		49.7		2640		1.64				49.7		2630		1.65				50.2		2380		1.67				50.6		2390		1.67				49.9		2920		1.65

		49.8		2640		1.65				49.8		2630		1.65				50.3		2390		1.67				50.7		2390		1.67				50		2920		1.65

		49.8		2640		1.65				49.9		2640		1.65				50.4		2390		1.67				50.8		2390		1.67				50		2930		1.65

		49.9		2650		1.65				50		2640		1.65				50.4		2390		1.67				50.9		2400		1.68				50.1		2930		1.66

		50		2650		1.65				50.1		2640		1.66				50.5		2390		1.67				51		2400		1.68				50.2		2930		1.66

		50.1		2650		1.66				50.1		2640		1.66				50.5		2390		1.68				51		2400		1.68				50.2		2930		1.66

		50.1		2660		1.66				50.2		2650		1.66				50.6		2390		1.68				51		2400		1.68				50.3		2940		1.66

		50.2		2660		1.66				50.2		2650		1.66				50.7		2400		1.68				51.1		2410		1.69				50.4		2940		1.66

		50.3		2660		1.66				50.3		2650		1.66				50.7		2400		1.68				51.2		2410		1.69				50.4		2940		1.67

		50.4		2660		1.66				50.4		2660		1.67				50.8		2400		1.68				51.3		2410		1.69				50.5		2950		1.67

		50.4		2670		1.67				50.5		2660		1.67				50.9		2400		1.69				51.3		2410		1.69				50.6		2950		1.67

		50.4		2670		1.67				50.5		2660		1.67				51		2410		1.69				51.4		2410		1.69				50.7		2950		1.68

		50.5		2670		1.67				50.6		2660		1.67				51		2410		1.69				51.5		2420		1.7				50.7		2950		1.68

		50.6		2670		1.67				50.7		2660		1.68				51.1		2410		1.69				51.5		2420		1.7				50.8		2960		1.68

		50.7		2680		1.68				50.7		2670		1.68				51.2		2410		1.7				51.6		2420		1.7				50.9		2960		1.68

		50.7		2680		1.68				50.8		2670		1.68				51.2		2410		1.7				51.7		2420		1.71				50.9		2960		1.68

		50.8		2680		1.68				50.9		2670		1.68				51.3		2420		1.7				51.7		2430		1.71				51		2960		1.69

		50.9		2680		1.68				51		2680		1.69				51.4		2420		1.7				51.8		2430		1.71				51		2970		1.69

		50.9		2690		1.68				51		2680		1.69				51.5		2420		1.71				51.9		2430		1.71				51.2		2970		1.69

		51		2690		1.69				51.1		2680		1.69				51.5		2420		1.71				51.9		2430		1.71				51.2		2970		1.69

		51.1		2690		1.69				51.2		2680		1.69				51.5		2420		1.71				52		2430		1.72				51.3		2980		1.7

		51.2		2690		1.69				51.2		2690		1.7				51.6		2430		1.71				52.1		2430		1.72				51.4		2980		1.7

		51.2		2700		1.69				51.3		2690		1.7				51.7		2430		1.71				52.2		2440		1.72				51.4		2980		1.7

		51.3		2700		1.7				51.4		2690		1.7				51.7		2430		1.72				52.2		2440		1.72				51.5		2980		1.7

		51.3		2700		1.7				51.4		2690		1.7				51.8		2430		1.72				52.3		2440		1.73				51.5		2990		1.7

		51.4		2700		1.7				51.5		2700		1.71				51.9		2430		1.72				52.3		2440		1.73				51.6		2990		1.71

		51.4		2710		1.7				51.6		2700		1.71				51.9		2440		1.72				52.4		2440		1.73				51.7		2990		1.71

		51.5		2710		1.7				51.7		2700		1.71				52		2440		1.73				52.4		2450		1.73				51.8		3000		1.71

		51.6		2710		1.71				51.7		2700		1.71				52.1		2440		1.73				52.5		2450		1.73				51.8		3000		1.71

		51.6		2710		1.71				51.8		2710		1.71				52.2		2440		1.73				52.6		2450		1.74				51.9		3000		1.72

		51.8		2720		1.71				51.8		2710		1.72				52.2		2450		1.73				52.7		2450		1.74				52		3000		1.72

		51.8		2720		1.71				51.9		2710		1.72				52.3		2450		1.74				52.7		2450		1.74				52		3010		1.72

		51.9		2720		1.72				51.9		2710		1.72				52.4		2450		1.74				52.8		2460		1.74				52.1		3010		1.72

		52		2720		1.72				52		2710		1.72				52.4		2450		1.74				52.9		2460		1.74				52.2		3010		1.72

		52		2730		1.72				52.1		2720		1.73				52.5		2450		1.74				52.9		2460		1.75				52.2		3010		1.73

		52.1		2730		1.72				52.2		2720		1.73				52.6		2460		1.75				53		2460		1.75				52.3		3020		1.73

		52.1		2730		1.72				52.3		2730		1.73				52.7		2460		1.75				53		2460		1.75				52.4		3020		1.73

		52.2		2730		1.73				52.3		2730		1.73				52.7		2460		1.75				53.1		2460		1.75				52.4		3020		1.73

		52.4		2740		1.73				52.4		2730		1.73				52.8		2460		1.75				53.2		2470		1.76				52.5		3020		1.74

		52.4		2740		1.73				52.4		2730		1.74				52.9		2470		1.75				53.3		2470		1.76				52.6		3030		1.74

		52.4		2740		1.73				52.5		2740		1.74				52.9		2470		1.76				53.3		2470		1.76				52.6		3030		1.74

		52.5		2740		1.74				52.6		2740		1.74				53		2470		1.76				53.4		2470		1.76				52.7		3030		1.74

		52.6		2750		1.74				52.7		2740		1.74				53		2470		1.76				53.4		2480		1.76				52.8		3040		1.75

		52.7		2750		1.74				52.8		2750		1.75				53.2		2470		1.76				53.5		2480		1.77				52.8		3040		1.75

		52.7		2750		1.74				52.8		2750		1.75				53.2		2480		1.77				53.6		2480		1.77				52.9		3040		1.75

		52.8		2750		1.74				52.9		2750		1.75				53.3		2480		1.77				53.6		2480		1.77				53		3050		1.75

		52.9		2760		1.75				52.9		2750		1.75				53.4		2480		1.77				53.7		2480		1.77				53.1		3050		1.76

		52.9		2760		1.75				53		2760		1.76				53.4		2480		1.77				53.8		2490		1.78				53.1		3050		1.76

		53		2760		1.75				53.1		2760		1.76				53.5		2490		1.77				53.9		2490		1.78				53.2		3050		1.76

		53		2760		1.75				53.2		2760		1.76				53.5		2490		1.78				53.9		2490		1.78				53.3		3060		1.76

		53.1		2770		1.76				53.3		2760		1.76				53.6		2490		1.78				54		2490		1.78				53.3		3060		1.76

		53.2		2770		1.76				53.3		2770		1.77				53.7		2490		1.78				54		2490		1.78				53.4		3060		1.77

		53.3		2770		1.76				53.4		2770		1.77				53.8		2490		1.78				54.1		2490		1.79				53.4		3060		1.77

		53.3		2770		1.76				53.4		2770		1.77				53.9		2500		1.79				54.2		2500		1.79				53.5		3070		1.77

		53.4		2780		1.76				53.5		2770		1.77				53.9		2500		1.79				54.2		2500		1.79				53.6		3070		1.77

		53.5		2780		1.77				53.6		2770		1.77				54		2500		1.79				54.3		2500		1.79				53.7		3070		1.78

		53.5		2780		1.77				53.6		2780		1.78				54		2500		1.79				54.4		2500		1.8				53.7		3070		1.78

		53.6		2780		1.77				53.7		2780		1.78				54.1		2510		1.8				54.5		2510		1.8				53.8		3080		1.78

		53.6		2790		1.77				53.8		2780		1.78				54.2		2510		1.8				54.5		2510		1.8				53.9		3080		1.78

		53.7		2790		1.78				53.9		2780		1.78				54.3		2510		1.8				54.6		2510		1.8				53.9		3080		1.78

		53.8		2790		1.78				53.9		2790		1.78				54.3		2510		1.8				54.7		2510		1.81				54		3080		1.79

		53.8		2790		1.78				54		2790		1.79				54.4		2510		1.8				54.8		2510		1.81				54		3090		1.79

		53.9		2790		1.78				54.1		2790		1.79				54.5		2520		1.81				54.8		2520		1.81				54.1		3090		1.79

		54		2800		1.78				54.1		2790		1.79				54.5		2520		1.81				54.9		2520		1.81				54.2		3090		1.79

		54		2800		1.79				54.2		2800		1.79				54.6		2520		1.81				54.9		2520		1.81				54.3		3100		1.79

		54.1		2800		1.79				54.2		2800		1.8				54.6		2520		1.81				55		2520		1.82				54.3		3100		1.8

		54.1		2800		1.79				54.3		2800		1.8				54.7		2520		1.82				55.1		2520		1.82				54.4		3100		1.8

		54.2		2810		1.79				54.3		2800		1.8				54.8		2530		1.82				55.2		2530		1.82				54.5		3100		1.8

		54.3		2810		1.79				54.5		2810		1.8				54.9		2530		1.82				55.3		2530		1.82				54.5		3110		1.8

		54.3		2810		1.8				54.6		2810		1.81				54.9		2530		1.82				55.3		2530		1.83				54.6		3110		1.81

		54.4		2810		1.8				54.6		2810		1.81				55		2530		1.82				55.4		2530		1.83				54.6		3110		1.81

		54.4		2820		1.8				54.7		2810		1.81				55		2530		1.83				55.4		2530		1.83				54.7		3110		1.81

		54.5		2820		1.8				54.7		2820		1.81				55.1		2540		1.83				55.5		2540		1.83				54.8		3120		1.81

		54.6		2820		1.81				54.8		2820		1.81				55.2		2540		1.83				55.6		2540		1.84				54.9		3120		1.82

		54.7		2820		1.81				54.9		2820		1.82				55.3		2540		1.83				55.6		2540		1.84				54.9		3120		1.82

		54.7		2830		1.81				54.9		2820		1.82				55.3		2540		1.83				55.7		2540		1.84				55		3130		1.82

		54.8		2830		1.81				55		2830		1.82				55.4		2540		1.84				55.8		2550		1.84				55.1		3130		1.82

		54.8		2830		1.81				55.1		2830		1.82				55.5		2550		1.84				55.8		2550		1.84				55.1		3130		1.82

		54.9		2830		1.82				55.2		2830		1.83				55.5		2550		1.84				55.9		2550		1.85				55.2		3130		1.83

		55		2830		1.82				55.2		2830		1.83				55.6		2550		1.85				56		2550		1.85				55.3		3140		1.83

		55.1		2840		1.82				55.2		2840		1.83				55.7		2550		1.85				56		2550		1.85				55.3		3140		1.83

		55.1		2840		1.82				55.3		2840		1.83				55.7		2550		1.85				56.1		2560		1.85				55.4		3140		1.83

		55.2		2840		1.83				55.4		2840		1.83				55.8		2560		1.85				56.2		2560		1.86				55.5		3150		1.84

		55.3		2850		1.83				55.4		2840		1.84				55.8		2560		1.85				56.3		2560		1.86				55.5		3150		1.84

		55.3		2850		1.83				55.5		2840		1.84				55.9		2560		1.86				56.3		2560		1.86				55.6		3150		1.84

		55.4		2850		1.83				55.7		2850		1.84				56		2560		1.86				56.4		2560		1.86				55.7		3150		1.84

		55.4		2850		1.83				55.7		2850		1.84				56.1		2570		1.86				56.4		2570		1.86				55.7		3160		1.84

		55.5		2850		1.84				55.7		2850		1.85				56.2		2570		1.86				56.5		2570		1.87				55.8		3160		1.85

		55.6		2860		1.84				55.8		2860		1.85				56.2		2570		1.87				56.6		2570		1.87				55.9		3160		1.85

		55.7		2860		1.84				55.9		2860		1.85				56.3		2570		1.87				56.7		2570		1.87				55.9		3160		1.85

		55.8		2860		1.84				55.9		2860		1.85				56.3		2570		1.87				56.8		2580		1.87				56		3170		1.85

		55.8		2860		1.85				56		2860		1.85				56.4		2580		1.87				56.8		2580		1.88				56.1		3170		1.86

		55.9		2870		1.85				56.1		2870		1.86				56.4		2580		1.87				56.9		2580		1.88				56.1		3170		1.86

		55.9		2870		1.85				56.2		2870		1.86				56.5		2580		1.88				56.9		2580		1.88				56.2		3170		1.86

		56		2870		1.85				56.2		2870		1.86				56.7		2580		1.88				57		2580		1.88				56.2		3180		1.86

		56		2880		1.85				56.3		2870		1.87				56.7		2590		1.88				57.1		2590		1.88				56.3		3180		1.86

		56.1		2880		1.86				56.4		2880		1.87				56.8		2590		1.88				57.1		2590		1.89				56.4		3180		1.87

		56.2		2880		1.86				56.4		2880		1.87				56.8		2590		1.89				57.2		2590		1.89				56.5		3180		1.87

		56.2		2880		1.86				56.5		2880		1.87				56.9		2590		1.89				57.2		2590		1.89				56.5		3190		1.87

		56.3		2890		1.86				56.6		2880		1.87				57		2590		1.89				57.3		2590		1.89				56.6		3190		1.87

		56.4		2890		1.87				56.6		2890		1.88				57		2600		1.89				57.3		2600		1.89				56.7		3190		1.87

		56.5		2890		1.87				56.7		2890		1.88				57.1		2600		1.89				57.4		2600		1.9				56.7		3190		1.88

		56.5		2890		1.87				56.8		2890		1.88				57.2		2600		1.9				57.5		2600		1.9				56.8		3200		1.88

		56.6		2900		1.87				56.8		2890		1.88				57.3		2600		1.9				57.5		2600		1.9				56.8		3200		1.88

		56.7		2900		1.87				56.9		2900		1.88				57.3		2600		1.9				57.6		2600		1.9				56.9		3200		1.88

		56.7		2900		1.88				57		2900		1.89				57.3		2610		1.9				57.7		2610		1.91				57		3200		1.89

		56.8		2900		1.88				57.1		2900		1.89				57.4		2610		1.91				57.7		2610		1.91				57.1		3210		1.89

		56.8		2910		1.88				57.1		2900		1.89				57.5		2610		1.91				57.8		2610		1.91				57.2		3210		1.89

		57		2910		1.89				57.2		2900		1.89				57.5		2610		1.91				57.9		2610		1.91				57.2		3210		1.89

		57		2910		1.89				57.2		2910		1.9				57.6		2610		1.91				58		2610		1.91				57.3		3220		1.9

		57.1		2910		1.89				57.3		2910		1.9				57.7		2620		1.91				58		2620		1.92				57.4		3220		1.9

		57.2		2920		1.89				57.4		2910		1.9				57.7		2620		1.92				58.1		2620		1.92				57.4		3220		1.9

		57.3		2920		1.89				57.5		2910		1.9				57.8		2620		1.92				58.2		2620		1.92				57.5		3220		1.9

		57.3		2920		1.9				57.5		2920		1.9				57.9		2620		1.92				58.2		2620		1.92				57.6		3230		1.9

		57.4		2920		1.9				57.6		2920		1.91				58		2630		1.92				58.3		2620		1.93				57.7		3230		1.91

		57.4		2930		1.9				57.6		2920		1.91				58		2630		1.93				58.3		2630		1.93				57.7		3230		1.91

		57.5		2930		1.9				57.7		2920		1.91				58.1		2630		1.93				58.4		2630		1.93				57.8		3240		1.91

		57.6		2930		1.91				57.7		2930		1.91				58.2		2630		1.93				58.5		2630		1.93				57.9		3240		1.91

		57.6		2930		1.91				57.8		2930		1.91				58.3		2630		1.93				58.5		2630		1.93				57.9		3240		1.92

		57.7		2940		1.91				57.9		2930		1.92				58.3		2640		1.93				58.6		2640		1.94				58		3240		1.92

		57.7		2940		1.91				58		2930		1.92				58.3		2640		1.94				58.7		2640		1.94				58.1		3250		1.92

		57.8		2940		1.91				58		2940		1.92				58.5		2640		1.94				58.7		2640		1.94				58.1		3250		1.92

		57.9		2940		1.92				58.1		2940		1.92				58.5		2640		1.94				58.8		2640		1.94				58.2		3250		1.93

		58		2950		1.92				58.2		2940		1.93				58.6		2650		1.95				58.8		2640		1.94				58.3		3260		1.93

		58		2950		1.92				58.2		2940		1.93				58.7		2650		1.95				59		2650		1.95				58.4		3260		1.93

		58.1		2950		1.92				58.3		2950		1.93				58.7		2650		1.95				59.1		2650		1.95				58.4		3260		1.93

		58.2		2960		1.93				58.3		2950		1.93				58.8		2650		1.95				59.1		2650		1.95				58.5		3260		1.94

		58.3		2960		1.93				58.4		2950		1.93				58.8		2650		1.95				59.2		2650		1.96				58.5		3270		1.94

		58.3		2960		1.93				58.5		2950		1.94				58.9		2660		1.96				59.2		2660		1.96				58.6		3270		1.94

		58.4		2960		1.93				58.6		2960		1.94				59		2660		1.96				59.3		2660		1.96				58.7		3270		1.94

		58.5		2960		1.93				58.7		2960		1.94				59.1		2660		1.96				59.3		2660		1.96				58.8		3270		1.94

		58.5		2970		1.94				58.7		2960		1.95				59.2		2660		1.96				59.4		2660		1.96				58.8		3280		1.95

		58.6		2970		1.94				58.8		2960		1.95				59.2		2670		1.97				59.5		2660		1.97				58.9		3280		1.95

		58.7		2970		1.94				58.8		2970		1.95				59.3		2670		1.97				59.6		2670		1.97				58.9		3280		1.95

		58.7		2980		1.94				58.9		2970		1.95				59.3		2670		1.97				59.6		2670		1.97				59		3280		1.95

		58.8		2980		1.95				59		2970		1.95				59.4		2670		1.97				59.7		2670		1.97				59.1		3290		1.95

		58.8		2980		1.95				59		2970		1.96				59.5		2670		1.97				59.8		2670		1.97				59.2		3290		1.96

		58.9		2980		1.95				59.1		2980		1.96				59.6		2670		1.98				59.8		2670		1.98				59.2		3290		1.96

		59		2980		1.95				59.2		2980		1.96				59.7		2680		1.98				59.9		2680		1.98				59.3		3290		1.96

		59		2990		1.95				59.3		2980		1.96				59.7		2680		1.98				59.9		2680		1.98				59.3		3300		1.96

		59.1		2990		1.96				59.3		2980		1.96				59.8		2680		1.98				60		2680		1.98				59.4		3300		1.97

		59.2		2990		1.96				59.4		2990		1.97				59.8		2690		1.99				60.1		2690		1.99				59.4		3300		1.97

		59.3		3000		1.96				59.5		2990		1.97				59.9		2690		1.99				60.2		2690		1.99				59.5		3300		1.97

		59.3		3000		1.96				59.5		2990		1.97				60		2690		1.99				60.2		2690		1.99				59.6		3310		1.97

		59.4		3000		1.97				59.6		2990		1.97				60		2690		1.99				60.3		2690		1.99				59.6		3310		1.97

		59.4		3000		1.97				59.6		2990		1.98				60.1		2690		2				60.4		2690		1.99				59.7		3310		1.98

		59.5		3000		1.97				59.7		3000		1.98				60.2		2700		2				60.4		2700		2				59.8		3310		1.98

		59.6		3010		1.97				59.8		3000		1.98				60.2		2700		2				60.5		2700		2				59.9		3320		1.98

		59.6		3010		1.97				59.9		3000		1.98				60.3		2700		2				60.6		2700		2				59.9		3320		1.98

		59.7		3010		1.98				59.9		3010		1.98				60.4		2700		2				60.6		2700		2				60		3320		1.99

		59.7		3010		1.98				60		3010		1.99				60.4		2700		2.01				60.7		2700		2.01				60.1		3330		1.99

		59.9		3020		1.98				60		3010		1.99				60.5		2710		2.01				60.7		2710		2.01				60.1		3330		1.99

		59.9		3020		1.98				60.1		3010		1.99				60.6		2710		2.01				60.8		2710		2.01				60.1		3330		1.99

		60		3020		1.99				60.1		3010		1.99				60.7		2710		2.01				60.9		2710		2.01				60.2		3330		1.99

		60.1		3030		1.99				60.2		3020		1.99				60.7		2710		2.01				60.9		2710		2.01				60.3		3340		2

		60.2		3030		1.99				60.3		3020		2				60.8		2710		2.02				61		2710		2.02				60.4		3340		2

		60.2		3030		1.99				60.4		3020		2				60.9		2720		2.02				61.1		2720		2.02				60.4		3340		2

		60.2		3030		1.99				60.4		3030		2				61		2720		2.02				61.1		2720		2.02				60.5		3340		2

		60.3		3030		2				60.5		3030		2				61		2720		2.03				61.2		2720		2.02				60.6		3350		2

		60.4		3040		2				60.6		3030		2.01				61.1		2720		2.03				61.3		2730		2.03				60.6		3350		2.01

		60.5		3040		2				60.6		3030		2.01				61.2		2730		2.03				61.4		2730		2.03				60.7		3350		2.01

		60.6		3040		2				60.7		3030		2.01				61.2		2730		2.03				61.4		2730		2.03				60.8		3350		2.01

		60.6		3050		2.01				60.7		3040		2.01				61.2		2730		2.03				61.5		2730		2.03				60.8		3360		2.01

		60.7		3050		2.01				60.8		3040		2.01				61.3		2730		2.04				61.6		2730		2.04				60.9		3360		2.02

		60.7		3050		2.01				60.9		3040		2.02				61.4		2730		2.04				61.6		2740		2.04				60.9		3360		2.02

		60.8		3050		2.01				61		3040		2.02				61.4		2740		2.04				61.7		2740		2.04				61.1		3370		2.02

		60.8		3050		2.01				61		3050		2.02				61.5		2740		2.04				61.8		2740		2.04				61.1		3370		2.02

		60.9		3060		2.02				61.1		3050		2.02				61.6		2740		2.04				61.9		2740		2.04				61.2		3370		2.03

		61		3060		2.02				61.1		3050		2.03				61.7		2740		2.05				61.9		2750		2.05				61.2		3370		2.03

		61.1		3060		2.02				61.2		3050		2.03				61.7		2740		2.05				62		2750		2.05				61.3		3380		2.03

		61.2		3070		2.02				61.3		3060		2.03				61.7		2750		2.05				62.1		2750		2.05				61.4		3380		2.03

		61.2		3070		2.03				61.4		3060		2.03				61.8		2750		2.05				62.1		2750		2.05				61.4		3380		2.03

		61.3		3070		2.03				61.4		3060		2.04				61.9		2750		2.05				62.2		2750		2.06				61.5		3380		2.04

		61.4		3070		2.03				61.5		3060		2.04				62		2750		2.06				62.2		2760		2.06				61.6		3390		2.04

		61.4		3080		2.03				61.6		3070		2.04				62		2750		2.06				62.3		2760		2.06				61.6		3390		2.04

		61.5		3080		2.04				61.6		3070		2.04				62.1		2760		2.06				62.4		2760		2.06				61.7		3390		2.04

		61.5		3080		2.04				61.7		3070		2.04				62.2		2760		2.06				62.4		2760		2.06				61.8		3390		2.05

		61.6		3080		2.04				61.7		3070		2.05				62.2		2760		2.07				62.5		2770		2.07				61.8		3400		2.05

		61.7		3090		2.04				61.8		3080		2.05				62.3		2760		2.07				62.6		2770		2.07				61.9		3400		2.05

		61.7		3090		2.04				61.9		3080		2.05				62.3		2760		2.07				62.6		2770		2.07				62		3400		2.05

		61.8		3090		2.05				61.9		3080		2.05				62.4		2770		2.07				62.7		2770		2.07				62		3400		2.05

		61.9		3090		2.05				62		3080		2.06				62.5		2770		2.07				62.8		2770		2.07				62.1		3410		2.06

		61.9		3100		2.05				62.1		3090		2.06				62.6		2770		2.08				62.9		2780		2.08				62.1		3410		2.06

		62		3100		2.05				62.2		3090		2.06				62.6		2770		2.08				63		2780		2.08				62.3		3410		2.06

		62.1		3100		2.06				62.2		3090		2.06				62.7		2770		2.08				63		2780		2.08				62.3		3420		2.06

		62.1		3100		2.06				62.3		3090		2.06				62.7		2780		2.08				63.1		2780		2.09				62.4		3420		2.07

		62.2		3110		2.06				62.4		3100		2.07				62.8		2780		2.09				63.1		2790		2.09				62.5		3420		2.07

		62.3		3110		2.06				62.4		3100		2.07				62.9		2780		2.09				63.2		2790		2.09				62.5		3420		2.07

		62.3		3110		2.06				62.5		3100		2.07				62.9		2780		2.09				63.3		2790		2.09				62.6		3430		2.07

		62.4		3110		2.07				62.5		3100		2.07				63		2780		2.09				63.3		2790		2.09				62.7		3430		2.07

		62.5		3120		2.07				62.7		3110		2.08				63.1		2790		2.09				63.4		2790		2.1				62.7		3430		2.08

		62.5		3120		2.07				62.7		3110		2.08				63.2		2790		2.1				63.5		2800		2.1				62.8		3430		2.08

		62.6		3120		2.07				62.8		3110		2.08				63.3		2790		2.1				63.6		2800		2.1				62.9		3440		2.08

		62.7		3120		2.07				62.8		3110		2.08				63.3		2790		2.1				63.6		2800		2.1				63		3440		2.08

		62.8		3130		2.08				62.9		3120		2.08				63.4		2800		2.1				63.7		2800		2.11				63		3440		2.09

		62.8		3130		2.08				63		3120		2.09				63.4		2800		2.11				63.7		2810		2.11				63.1		3450		2.09

		62.9		3130		2.08				63		3120		2.09				63.5		2800		2.11				63.8		2810		2.11				63.1		3450		2.09

		62.9		3130		2.08				63.1		3120		2.09				63.6		2800		2.11				63.9		2810		2.11				63.2		3450		2.09

		63		3130		2.09				63.2		3130		2.09				63.6		2800		2.11				63.9		2810		2.11				63.2		3450		2.09

		63.1		3140		2.09				63.3		3130		2.1				63.7		2810		2.12				64		2810		2.12				63.3		3460		2.1

		63.1		3140		2.09				63.4		3130		2.1				63.8		2810		2.12				64.1		2820		2.12				63.4		3460		2.1

		63.2		3140		2.09				63.4		3130		2.1				63.9		2810		2.12				64.1		2820		2.12				63.5		3460		2.1

		63.3		3150		2.1				63.5		3140		2.1				63.9		2810		2.12				64.1		2820		2.12				63.5		3460		2.1

		63.3		3150		2.1				63.5		3140		2.11				64		2820		2.12				64.2		2820		2.12				63.6		3470		2.11

		63.4		3150		2.1				63.6		3140		2.11				64		2820		2.13				64.3		2820		2.13				63.7		3470		2.11

		63.5		3150		2.1				63.6		3140		2.11				64.1		2820		2.13				64.4		2830		2.13				63.7		3470		2.11

		63.5		3150		2.1				63.8		3150		2.11				64.1		2820		2.13				64.4		2830		2.13				63.8		3480		2.11

		63.6		3160		2.11				63.8		3150		2.12				64.2		2820		2.13				64.5		2830		2.13				63.9		3480		2.12

		63.6		3160		2.11				63.9		3150		2.12				64.3		2830		2.14				64.6		2830		2.13				63.9		3480		2.12

		63.7		3160		2.11				64		3150		2.12				64.4		2830		2.14				64.6		2840		2.14				64		3480		2.12

		63.8		3160		2.11				64		3160		2.12				64.5		2830		2.14				64.7		2840		2.14				64.1		3490		2.12

		63.9		3170		2.12				64.1		3160		2.12				64.5		2830		2.14				64.8		2840		2.14				64.1		3490		2.12

		63.9		3170		2.12				64.1		3160		2.13				64.6		2840		2.14				64.8		2840		2.14				64.2		3490		2.13

		64		3170		2.12				64.2		3160		2.13				64.7		2840		2.15				64.9		2840		2.15				64.3		3490		2.13

		64.1		3170		2.12				64.3		3170		2.13				64.7		2840		2.15				65		2850		2.15				64.3		3500		2.13

		64.1		3180		2.12				64.4		3170		2.13				64.8		2840		2.15				65		2850		2.15				64.4		3500		2.13

		64.2		3180		2.13				64.5		3170		2.14				64.9		2840		2.15				65.1		2850		2.15				64.5		3500		2.13

		64.3		3180		2.13				64.5		3170		2.14				65		2850		2.16				65.2		2860		2.16				64.5		3500		2.14

		64.3		3180		2.13				64.6		3180		2.14				65		2850		2.16				65.3		2860		2.16				64.6		3510		2.14

		64.4		3190		2.13				64.7		3180		2.14				65.1		2850		2.16				65.3		2860		2.16				64.7		3510		2.14

		64.5		3190		2.14				64.7		3180		2.14				65.1		2850		2.16				65.4		2860		2.16				64.8		3510		2.15

		64.6		3190		2.14				64.8		3180		2.15				65.2		2850		2.16				65.5		2860		2.17				64.8		3520		2.15

		64.6		3190		2.14				64.8		3190		2.15				65.2		2860		2.17				65.5		2870		2.17				64.9		3520		2.15

		64.7		3200		2.14				64.9		3190		2.15				65.3		2860		2.17				65.6		2870		2.17				65		3520		2.15

		64.7		3200		2.14				65		3190		2.15				65.4		2860		2.17				65.7		2870		2.17				65		3520		2.15

		64.8		3200		2.15				65.1		3190		2.16				65.5		2860		2.17				65.8		2870		2.18				65.1		3520		2.16

		64.9		3200		2.15				65.1		3200		2.16				65.6		2870		2.18				65.8		2880		2.18				65.2		3530		2.16

		65		3210		2.15				65.2		3200		2.16				65.6		2870		2.18				65.9		2880		2.18				65.2		3530		2.16

		65.1		3210		2.15				65.3		3200		2.16				65.6		2870		2.18				66		2880		2.18				65.3		3530		2.16

		65.1		3210		2.16				65.3		3200		2.16				65.7		2870		2.18				66		2880		2.18				65.4		3530		2.16

		65.2		3220		2.16				65.4		3200		2.17				65.8		2870		2.18				66.1		2880		2.19				65.4		3540		2.17

		65.3		3220		2.16				65.4		3210		2.17				65.8		2880		2.19				66.1		2890		2.19				65.5		3540		2.17

		65.3		3220		2.16				65.5		3210		2.17				65.9		2880		2.19				66.2		2890		2.19				65.5		3540		2.17

		65.4		3220		2.17				65.6		3210		2.18				66		2880		2.19				66.3		2890		2.19				65.6		3540		2.17

		65.4		3230		2.17				65.7		3220		2.18				66.1		2880		2.19				66.4		2890		2.2				65.7		3550		2.17

		65.5		3230		2.17				65.8		3220		2.18				66.1		2880		2.2				66.4		2890		2.2				65.7		3550		2.18

		65.5		3230		2.17				65.8		3220		2.18				66.2		2890		2.2				66.5		2900		2.2				65.8		3550		2.18

		65.6		3230		2.17				65.9		3220		2.18				66.3		2890		2.2				66.6		2900		2.2				65.9		3560		2.18

		65.7		3240		2.18				65.9		3220		2.19				66.3		2890		2.2				66.6		2900		2.2				66		3560		2.18

		65.8		3240		2.18				66		3230		2.19				66.4		2890		2.2				66.7		2900		2.21				66		3560		2.19

		65.8		3240		2.18				66.1		3230		2.19				66.4		2890		2.21				66.8		2900		2.21				66.1		3560		2.19

		65.9		3240		2.18				66.1		3230		2.19				66.5		2900		2.21				66.9		2910		2.21				66.1		3570		2.19

		66		3250		2.19				66.3		3240		2.2				66.6		2900		2.21				67		2910		2.21				66.2		3570		2.19

		66		3250		2.19				66.3		3240		2.2				66.7		2900		2.21				67		2910		2.22				66.3		3570		2.2

		66.1		3250		2.19				66.4		3240		2.2				66.8		2900		2.22				67.1		2910		2.22				66.4		3580		2.2

		66.1		3250		2.19				66.4		3240		2.2				66.8		2910		2.22				67.1		2920		2.22				66.5		3580		2.2

		66.2		3260		2.19				66.5		3250		2.2				66.9		2910		2.22				67.2		2920		2.22				66.5		3580		2.2

		66.3		3260		2.2				66.5		3250		2.21				66.9		2910		2.22				67.2		2920		2.22				66.6		3580		2.21

		66.4		3260		2.2				66.6		3250		2.21				67		2910		2.22				67.3		2920		2.23				66.6		3590		2.21

		66.5		3260		2.2				66.7		3250		2.21				67.1		2910		2.23				67.5		2930		2.23				66.7		3590		2.21

		66.5		3270		2.2				66.8		3260		2.21				67.2		2920		2.23				67.5		2930		2.23				66.8		3590		2.21

		66.6		3270		2.2				66.9		3260		2.22				67.3		2920		2.23				67.6		2930		2.23				66.8		3590		2.21

		66.6		3270		2.21				66.9		3260		2.22				67.3		2920		2.24				67.6		2930		2.24				66.9		3600		2.22

		66.7		3270		2.21				67		3260		2.22				67.4		2920		2.24				67.7		2930		2.24				67		3600		2.22

		66.8		3280		2.21				67		3260		2.22				67.4		2930		2.24				67.7		2940		2.24				67		3600		2.22

		66.8		3280		2.21				67.1		3270		2.22				67.5		2930		2.24				67.8		2940		2.24				67.1		3600		2.22

		66.9		3280		2.22				67.2		3270		2.23				67.5		2930		2.24				67.9		2940		2.25				67.2		3610		2.23

		67		3280		2.22				67.2		3270		2.23				67.6		2930		2.25				67.9		2940		2.25				67.2		3610		2.23

		67		3290		2.22				67.3		3270		2.23				67.7		2930		2.25				68		2950		2.25				67.3		3610		2.23

		67.1		3290		2.22				67.4		3280		2.23				67.8		2940		2.25				68.1		2950		2.25				67.4		3610		2.23

		67.1		3290		2.22				67.5		3280		2.24				67.8		2940		2.25				68.1		2950		2.25				67.4		3620		2.23

		67.2		3290		2.23				67.5		3280		2.24				67.9		2940		2.25				68.2		2950		2.26				67.5		3620		2.24

		67.4		3300		2.23				67.6		3280		2.24				68		2940		2.26				68.3		2950		2.26				67.6		3620		2.24

		67.4		3300		2.23				67.7		3280		2.24				68		2950		2.26				68.3		2960		2.26				67.7		3620		2.24

		67.5		3300		2.24				67.7		3290		2.24				68.1		2950		2.26				68.4		2960		2.26				67.7		3630		2.24

		67.5		3300		2.24				67.8		3290		2.25				68.1		2950		2.26				68.5		2960		2.27				67.8		3630		2.25

		67.6		3310		2.24				67.8		3290		2.25				68.2		2950		2.27				68.5		2960		2.27				67.9		3630		2.25

		67.6		3310		2.24				67.9		3290		2.25				68.3		2950		2.27				68.6		2970		2.27				67.9		3630		2.25

		67.7		3310		2.24				68		3300		2.26				68.4		2960		2.27				68.7		2970		2.27				67.9		3640		2.25

		67.8		3310		2.25				68.1		3300		2.26				68.5		2960		2.27				68.8		2970		2.28				68		3640		2.25

		67.8		3320		2.25				68.1		3300		2.26				68.5		2960		2.28				68.9		2970		2.28				68.1		3640		2.26

		68		3320		2.25				68.2		3300		2.26				68.6		2960		2.28				68.9		2970		2.28				68.2		3650		2.26

		68		3320		2.25				68.3		3310		2.26				68.6		2970		2.28				69		2970		2.28				68.3		3650		2.26

		68.1		3330		2.26				68.4		3310		2.27				68.7		2970		2.28				69		2980		2.28				68.4		3650		2.26

		68.1		3330		2.26				68.4		3310		2.27				68.8		2970		2.28				69.1		2980		2.29				68.4		3650		2.27

		68.2		3330		2.26				68.5		3310		2.27				68.9		2970		2.29				69.2		2980		2.29				68.5		3660		2.27

		68.3		3330		2.26				68.6		3280		2.27				68.9		2970		2.29				69.3		2990		2.29				68.5		3660		2.27

		68.3		3330		2.26				68.6		3270		2.28				69		2980		2.29				69.3		2990		2.29				68.6		3660		2.27

		68.4		3340		2.27				68.7		3270		2.28				69		2980		2.29				69.4		2990		2.3				68.7		3660		2.28

		68.5		3340		2.27				68.7		3280		2.28				69.1		2980		2.29				69.5		2990		2.3				68.8		3670		2.28

		68.5		3340		2.27				68.8		3280		2.28				69.1		2980		2.3				69.5		2990		2.3				68.8		3670		2.28

		68.6		3350		2.27				68.9		3290		2.28				69.2		2980		2.3				69.6		3000		2.3				68.9		3670		2.28

		68.7		3350		2.28				68.9		3290		2.29				69.3		2990		2.3				69.6		3000		2.3				69		3670		2.28

		68.8		3350		2.28				69		3290		2.29				69.3		2990		2.3				69.8		3000		2.31				69		3680		2.29

		68.8		3350		2.28				69		3300		2.29				69.4		2990		2.3				69.8		3000		2.31				69.1		3680		2.29

		68.9		3360		2.28				69.2		3300		2.29				69.5		2990		2.31				69.9		3010		2.31				69.1		3680		2.29

		69		3360		2.28				69.3		3300		2.3				69.6		3000		2.31				70		3010		2.32				69.2		3680		2.29

		69		3360		2.29				69.3		3300		2.3				69.7		3000		2.31				70		3010		2.32				69.3		3680		2.3

		69.1		3360		2.29				69.4		3300		2.3				69.7		3000		2.32				70.1		3010		2.32				69.4		3690		2.3

		69.2		3370		2.29				69.4		3310		2.3				69.8		3000		2.32				70.2		3010		2.32				69.4		3690		2.3

		69.3		3370		2.29				69.5		3310		2.3				69.9		3000		2.32				70.2		3020		2.32				69.5		3690		2.3

		69.3		3370		2.3				69.6		3310		2.31				69.9		3010		2.32				70.4		3020		2.33				69.5		3690		2.3

		69.4		3370		2.3				69.6		3310		2.31				70		3010		2.32				70.4		3020		2.33				69.6		3700		2.31

		69.4		3380		2.3				69.7		3320		2.31				70		3010		2.33				70.5		3020		2.33				69.7		3700		2.31

		69.5		3380		2.3				69.8		3320		2.31				70.1		3010		2.33				70.5		3030		2.33				69.8		3700		2.31

		69.6		3380		2.31				69.8		3320		2.32				70.2		3020		2.33				70.6		3030		2.34				69.9		3700		2.31

		69.7		3390		2.31				69.9		3320		2.32				70.3		3020		2.33				70.7		3030		2.34				69.9		3710		2.32

		69.8		3390		2.31				70		3320		2.32				70.3		3020		2.33				70.7		3030		2.34				70		3710		2.32

		69.8		3390		2.31				70		3330		2.32				70.4		3020		2.34				70.8		3030		2.34				70.1		3710		2.32

		69.9		3390		2.32				70.1		3330		2.32				70.4		3020		2.34				70.9		3040		2.34				70.1		3710		2.32

		69.9		3390		2.32				70.2		3330		2.33				70.5		3030		2.34				70.9		3040		2.35				70.2		3720		2.33

		70		3400		2.32				70.2		3330		2.33				70.5		3030		2.34				71		3040		2.35				70.2		3720		2.33

		70		3400		2.32				70.3		3340		2.33				70.6		3030		2.35				71		3040		2.35				70.3		3720		2.33

		70.1		3400		2.32				70.4		3340		2.33				70.8		3030		2.35				71.1		3040		2.35				70.4		3720		2.33

		70.2		3410		2.33				70.4		3340		2.34				70.8		3040		2.35				71.2		3050		2.36				70.5		3730		2.34

		70.3		3410		2.33				70.5		3340		2.34				70.9		3040		2.35				71.3		3050		2.36				70.6		3730		2.34

		70.4		3410		2.33				70.5		3340		2.34				71		3040		2.36				71.3		3050		2.36				70.6		3730		2.34

		70.4		3410		2.33				70.6		3350		2.34				71		3040		2.36				71.4		3050		2.36				70.7		3730		2.34

		70.4		3410		2.33				70.7		3350		2.34				71.1		3040		2.36				71.5		3060		2.37				70.8		3740		2.34

		70.5		3420		2.34				70.8		3350		2.35				71.1		3050		2.36				71.5		3060		2.37				70.8		3740		2.35

		70.6		3420		2.34				70.8		3360		2.35				71.2		3050		2.36				71.6		3060		2.37				70.9		3740		2.35

		70.7		3420		2.34				70.9		3360		2.35				71.3		3050		2.37				71.7		3060		2.37				70.9		3740		2.35

		70.7		3430		2.34				71		3360		2.35				71.4		3050		2.37				71.7		3060		2.37				71		3750		2.35

		70.8		3430		2.35				71		3360		2.36				71.4		3050		2.37				71.8		3070		2.38				71.1		3750		2.36

		70.9		3430		2.35				71.1		3360		2.36				71.4		3060		2.37				71.9		3070		2.38				71.2		3750		2.36

		70.9		3430		2.35				71.2		3370		2.36				71.5		3060		2.38				71.9		3070		2.38				71.3		3750		2.36

		71		3430		2.35				71.3		3370		2.36				71.6		3060		2.38				72		3080		2.38				71.3		3760		2.36

		71		3440		2.35				71.3		3370		2.37				71.6		3060		2.38				72.1		3080		2.39				71.3		3760		2.36

		71.1		3440		2.36				71.4		3370		2.37				71.7		3070		2.38				72.2		3080		2.39				71.4		3760		2.37

		71.2		3440		2.36				71.5		3370		2.37				71.8		3070		2.38				72.3		3080		2.39				71.5		3760		2.37

		71.3		3450		2.36				71.5		3380		2.37				71.9		3070		2.39				72.3		3080		2.39				71.6		3770		2.37

		71.4		3450		2.36				71.6		3380		2.37				71.9		3070		2.39				72.4		3090		2.39				71.7		3770		2.37

		71.4		3450		2.37				71.7		3380		2.38				72		3080		2.39				72.4		3090		2.4				71.7		3770		2.38

		71.5		3450		2.37				71.7		3380		2.38				72.1		3080		2.39				72.5		3090		2.4				71.8		3770		2.38

		71.6		3460		2.37				71.8		3390		2.38				72.2		3080		2.4				72.6		3090		2.4				71.8		3780		2.38

		71.6		3460		2.37				71.8		3390		2.38				72.2		3080		2.4				72.7		3090		2.4				71.9		3780		2.38

		71.7		3460		2.38				71.9		3390		2.39				72.3		3080		2.4				72.7		3100		2.41				71.9		3780		2.38

		71.8		3460		2.38				72		3390		2.39				72.4		3090		2.4				72.8		3100		2.41				72		3780		2.39

		71.8		3470		2.38				72.1		3400		2.39				72.4		3090		2.41				72.9		3100		2.41				72.1		3790		2.39

		71.9		3470		2.38				72.1		3400		2.39				72.5		3090		2.41				72.9		3100		2.41				72.2		3790		2.39

		71.9		3470		2.38				72.2		3400		2.39				72.6		3090		2.41				73		3100		2.41				72.3		3790		2.39

		72		3470		2.39				72.2		3400		2.4				72.6		3100		2.41				73		3110		2.42				72.3		3800		2.4

		72.1		3480		2.39				72.3		3400		2.4				72.7		3100		2.41				73.1		3110		2.42				72.4		3800		2.4

		72.1		3480		2.39				72.3		3410		2.4				72.7		3100		2.42				73.1		3110		2.42				72.4		3800		2.4

		72.2		3480		2.39				72.4		3410		2.4				72.8		3100		2.42				73.2		3110		2.42				72.5		3800		2.4

		72.3		3480		2.4				72.5		3410		2.41				72.9		3100		2.42				73.3		3110		2.43				72.6		3810		2.41

		72.4		3490		2.4				72.6		3410		2.41				72.9		3110		2.42				73.3		3120		2.43				72.7		3810		2.41

		72.4		3490		2.4				72.7		3420		2.41				73		3110		2.43				73.4		3120		2.43				72.8		3810		2.41

		72.5		3490		2.4				72.7		3420		2.41				73.1		3110		2.43				73.5		3120		2.43				72.8		3810		2.41

		72.6		3490		2.41				72.8		3420		2.41				73.2		3110		2.43				73.5		3120		2.43				72.9		3820		2.42

		72.6		3500		2.41				72.8		3420		2.42				73.3		3120		2.43				73.6		3120		2.44				72.9		3820		2.42

		72.7		3500		2.41				72.9		3430		2.42				73.3		3120		2.43				73.6		3130		2.44				73		3820		2.42

		72.8		3500		2.41				73		3430		2.42				73.4		3120		2.44				73.8		3130		2.44				73.1		3820		2.42

		72.8		3510		2.41				73.1		3430		2.42				73.4		3120		2.44				73.9		3130		2.44				73.1		3830		2.42

		72.9		3510		2.42				73.2		3440		2.43				73.5		3120		2.44				73.9		3140		2.45				73.2		3830		2.43

		73		3510		2.42				73.2		3440		2.43				73.6		3130		2.45				73.9		3140		2.45				73.3		3820		2.43

		73.1		3510		2.42				73.3		3440		2.43				73.7		3130		2.45				74		3140		2.45				73.4		3830		2.43

		73.1		3520		2.42				73.4		3440		2.43				73.7		3130		2.45				74.1		3140		2.45				73.5		3830		2.43

		73.2		3520		2.43				73.4		3440		2.44				73.8		3130		2.45				74.2		3140		2.45				73.5		3840		2.44

		73.3		3520		2.43				73.5		3450		2.44				73.9		3140		2.45				74.2		3150		2.46				73.6		3840		2.44

		73.3		3520		2.43				73.6		3450		2.44				73.9		3140		2.46				74.3		3150		2.46				73.6		3840		2.44

		73.4		3530		2.43				73.6		3450		2.44				74		3140		2.46				74.4		3150		2.46				73.7		3840		2.44

		73.5		3530		2.43				73.7		3460		2.44				74		3140		2.46				74.4		3150		2.46				73.8		3850		2.44

		73.5		3530		2.44				73.7		3460		2.45				74.1		3140		2.46				74.5		3150		2.47				73.8		3850		2.45

		73.7		3540		2.44				73.8		3460		2.45				74.2		3150		2.46				74.5		3160		2.47				73.9		3850		2.45

		73.7		3540		2.44				73.9		3460		2.45				74.3		3150		2.47				74.6		3160		2.47				74		3850		2.45

		73.8		3540		2.44				73.9		3460		2.45				74.3		3150		2.47				74.7		3160		2.47				74.1		3860		2.46

		73.8		3540		2.45				74		3470		2.45				74.4		3150		2.47				74.8		3160		2.47				74.2		3860		2.46

		73.9		3540		2.45				74.1		3470		2.46				74.4		3150		2.47				74.9		3170		2.48				74.2		3860		2.46

		74		3550		2.45				74.1		3470		2.46				74.5		3160		2.48				74.9		3170		2.48				74.3		3860		2.46

		74		3550		2.45				74.2		3470		2.46				74.6		3160		2.48				75		3170		2.48				74.3		3860		2.46

		74.1		3550		2.46				74.3		3480		2.46				74.6		3160		2.48				75		3170		2.48				74.4		3860		2.47

		74.1		3550		2.46				74.3		3480		2.47				74.7		3160		2.48				75.1		3170		2.49				74.4		3870		2.47

		74.3		3560		2.46				74.4		3480		2.47				74.8		3170		2.49				75.2		3180		2.49				74.6		3870		2.47

		74.3		3560		2.46				74.5		3480		2.47				74.9		3170		2.49				75.3		3180		2.49				74.6		3870		2.47

		74.4		3560		2.47				74.6		3490		2.47				75		3170		2.49				75.3		3180		2.49				74.7		3870		2.47

		74.4		3570		2.47				74.6		3490		2.47				75		3170		2.49				75.4		3180		2.49				74.7		3880		2.48

		74.5		3570		2.47				74.7		3490		2.48				75.1		3180		2.49				75.5		3190		2.5				74.8		3880		2.48

		74.6		3570		2.47				74.7		3490		2.48				75.1		3180		2.5				75.5		3190		2.5				74.8		3880		2.48

		74.6		3570		2.47				74.8		3490		2.48				75.2		3180		2.5				75.6		3190		2.5				74.9		3880		2.48

		74.7		3580		2.48				74.9		3500		2.48				75.3		3180		2.5				75.6		3190		2.5				75		3880		2.49

		74.8		3580		2.48				75		3500		2.49				75.4		3180		2.5				75.7		3190		2.51				75		3890		2.49

		74.8		3580		2.48				75		3500		2.49				75.4		3190		2.51				75.8		3200		2.51				75.2		3890		2.49

		74.9		3580		2.48				75.1		3500		2.49				75.5		3190		2.51				75.8		3200		2.51				75.2		3890		2.49

		75		3590		2.49				75.1		3510		2.49				75.6		3190		2.51				75.9		3200		2.51				75.3		3900		2.5

		75.1		3590		2.49				75.2		3510		2.49				75.6		3190		2.51				76		3200		2.51				75.3		3900		2.5

		75.1		3590		2.49				75.2		3510		2.5				75.7		3190		2.51				76		3210		2.52				75.4		3900		2.5

		75.2		3590		2.49				75.3		3510		2.5				75.8		3200		2.52				76.1		3210		2.52				75.5		3900		2.5

		75.3		3600		2.49				75.4		3510		2.5				75.8		3200		2.52				76.1		3210		2.52				75.6		3910		2.5

		75.3		3600		2.5				75.5		3510		2.5				75.9		3200		2.52				76.2		3210		2.52				75.6		3910		2.51

		75.4		3600		2.5				75.6		3510		2.51				75.9		3200		2.52				76.3		3210		2.52				75.7		3910		2.51

		75.5		3610		2.5				75.7		3520		2.51				76		3210		2.53				76.3		3220		2.53				75.8		3910		2.51

		75.5		3610		2.5				75.7		3520		2.51				76.1		3210		2.53				76.4		3220		2.53				75.8		3920		2.51

		75.6		3610		2.51				75.7		3520		2.51				76.1		3210		2.53				76.5		3220		2.53				75.9		3920		2.52

		75.7		3610		2.51				75.8		3530		2.51				76.2		3210		2.53				76.5		3220		2.53				76		3920		2.52

		75.8		3610		2.51				75.9		3530		2.52				76.3		3210		2.53				76.6		3220		2.54				76		3920		2.52

		75.8		3620		2.51				76		3530		2.52				76.3		3220		2.54				76.7		3230		2.54				76.1		3930		2.52

		75.9		3620		2.51				76.1		3530		2.52				76.4		3220		2.54				76.7		3230		2.54				76.2		3930		2.52

		76		3620		2.52				76.1		3540		2.53				76.5		3220		2.54				76.8		3230		2.54				76.2		3930		2.53

		76		3630		2.52				76.2		3540		2.53				76.6		3220		2.54				76.8		3230		2.54				76.3		3930		2.53

		76.1		3630		2.52				76.3		3540		2.53				76.7		3230		2.55				76.9		3230		2.55				76.4		3940		2.53

		76.1		3630		2.52				76.3		3540		2.53				76.7		3230		2.55				77		3240		2.55				76.4		3940		2.53

		76.2		3630		2.53				76.4		3540		2.53				76.8		3230		2.55				77		3240		2.55				76.5		3940		2.54

		76.3		3640		2.53				76.4		3550		2.54				76.8		3230		2.55				77.2		3240		2.56				76.6		3940		2.54

		76.3		3640		2.53				76.6		3550		2.54				76.9		3230		2.55				77.2		3250		2.56				76.6		3950		2.54

		76.4		3640		2.53				76.6		3550		2.54				77		3240		2.56				77.3		3250		2.56				76.7		3950		2.54

		76.4		3640		2.53				76.7		3550		2.54				77.1		3240		2.56				77.3		3250		2.56				76.7		3950		2.54

		76.6		3650		2.54				76.7		3560		2.55				77.1		3240		2.56				77.4		3250		2.56				76.8		3950		2.55

		76.7		3650		2.54				76.8		3560		2.55				77.2		3240		2.56				77.5		3250		2.57				76.9		3960		2.55

		76.7		3650		2.54				76.9		3560		2.55				77.3		3250		2.57				77.5		3260		2.57				77		3960		2.55

		76.8		3650		2.54				77		3560		2.55				77.3		3250		2.57				77.6		3260		2.57				77		3960		2.55

		76.8		3660		2.55				77		3570		2.55				77.4		3250		2.57				77.8		3260		2.57				77.1		3960		2.56

		76.9		3660		2.55				77.1		3570		2.56				77.4		3250		2.57				77.8		3260		2.58				77.2		3970		2.56

		76.9		3660		2.55				77.2		3570		2.56				77.5		3250		2.57				77.8		3270		2.58				77.2		3970		2.56

		77		3660		2.55				77.2		3570		2.56				77.6		3260		2.58				77.9		3270		2.58				77.3		3970		2.56

		77.1		3670		2.56				77.3		3580		2.57				77.7		3260		2.58				78		3270		2.58				77.4		3970		2.56

		77.2		3670		2.56				77.4		3580		2.57				77.7		3260		2.58				78		3270		2.58				77.5		3980		2.57

		77.2		3670		2.56				77.4		3580		2.57				77.8		3260		2.58				78.1		3270		2.59				77.5		3980		2.57

		77.3		3670		2.56				77.5		3580		2.57				77.8		3270		2.59				78.2		3280		2.59				77.6		3980		2.57

		77.4		3680		2.56				77.6		3580		2.57				77.9		3270		2.59				78.3		3280		2.59				77.7		3980		2.57

		77.4		3680		2.57				77.6		3590		2.58				78		3270		2.59				78.3		3280		2.59				77.7		3980		2.58

		77.5		3680		2.57				77.7		3590		2.58				78.1		3270		2.59				78.4		3280		2.59				77.7		3990		2.58

		77.6		3680		2.57				77.8		3590		2.58				78.1		3270		2.6				78.4		3290		2.6				77.8		3990		2.58

		77.6		3690		2.57				77.9		3600		2.58				78.2		3280		2.6				78.5		3290		2.6				77.9		3990		2.58

		77.7		3690		2.58				78		3600		2.59				78.3		3280		2.6				78.5		3290		2.6				78		3990		2.58

		77.7		3690		2.58				78		3600		2.59				78.3		3280		2.6				78.6		3290		2.6				78		4000		2.59

		77.8		3690		2.58				78.1		3600		2.59				78.4		3280		2.6				78.7		3290		2.61				78.1		4000		2.59

		77.9		3690		2.58				78.1		3600		2.59				78.5		3290		2.61				78.7		3300		2.61				78.2		4000		2.59

		77.9		3700		2.58				78.2		3610		2.59				78.5		3290		2.61				78.8		3300		2.61				78.2		4000		2.59

		78		3700		2.59				78.3		3610		2.6				78.6		3290		2.61				78.9		3300		2.61				78.3		4000		2.6

		78		3700		2.59				78.3		3610		2.6				78.6		3290		2.61				79		3300		2.61				78.3		4010		2.6

		78.1		3700		2.59				78.4		3610		2.6				78.7		3290		2.61				79		3300		2.62				78.4		4010		2.6

		78.2		3710		2.59				78.5		3620		2.6				78.7		3290		2.62				79.1		3310		2.62				78.5		4010		2.6

		78.3		3710		2.6				78.5		3620		2.61				78.8		3300		2.62				79.1		3310		2.62				78.6		4010		2.6

		78.3		3710		2.6				78.6		3620		2.61				78.9		3300		2.62				79.2		3310		2.62				78.6		4020		2.61

		78.4		3720		2.6				78.6		3620		2.61				79		3300		2.62				79.3		3310		2.62				78.7		4020		2.61

		78.5		3720		2.6				78.7		3620		2.61				79		3300		2.63				79.4		3320		2.63				78.8		4020		2.61

		78.5		3720		2.6				78.8		3630		2.62				79.1		3310		2.63				79.5		3320		2.63				78.8		4020		2.61

		78.6		3720		2.61				78.9		3630		2.62				79.2		3310		2.63				79.5		3320		2.63				78.9		4020		2.62

		78.7		3730		2.61				79		3630		2.62				79.2		3310		2.63				79.6		3320		2.64				79		4020		2.62

		78.7		3730		2.61				79		3630		2.62				79.3		3310		2.63				79.6		3330		2.64				79		4030		2.62

		78.8		3730		2.61				79.1		3630		2.62				79.4		3310		2.64				79.7		3330		2.64				79.1		4030		2.62

		78.9		3740		2.62				79.1		3640		2.63				79.4		3320		2.64				79.8		3330		2.64				79.1		4030		2.62

		79		3740		2.62				79.2		3640		2.63				79.5		3320		2.64				79.8		3330		2.64				79.2		4030		2.63

		79.1		3740		2.62				79.3		3640		2.63				79.6		3320		2.64				80		3340		2.65				79.3		4040		2.63

		79.1		3740		2.62				79.4		3640		2.63				79.7		3320		2.65				80		3340		2.65				79.3		4040		2.63

		79.2		3750		2.62				79.4		3650		2.63				79.7		3330		2.65				80.1		3340		2.65				79.4		4040		2.63

		79.2		3750		2.63				79.5		3650		2.64				79.7		3330		2.65				80.1		3340		2.65				79.5		4040		2.64

		79.3		3750		2.63				79.6		3650		2.64				79.8		3330		2.65				80.2		3340		2.66				79.5		4050		2.64

		79.4		3750		2.63				79.6		3650		2.64				79.9		3330		2.65				80.2		3350		2.66				79.6		4050		2.64

		79.4		3750		2.63				79.7		3650		2.64				80		3330		2.66				80.3		3350		2.66				79.7		4050		2.64

		79.5		3760		2.64				79.7		3650		2.64				80.1		3330		2.66				80.4		3350		2.66				79.7		4050		2.64

		79.6		3760		2.64				79.8		3650		2.65				80.1		3340		2.66				80.5		3350		2.67				79.8		4060		2.65

		79.7		3760		2.64				79.8		3660		2.65				80.2		3340		2.66				80.5		3360		2.67				79.9		4060		2.65

		79.7		3770		2.64				80		3660		2.65				80.2		3340		2.67				80.6		3360		2.67				79.9		4060		2.65

		79.8		3770		2.65				80		3660		2.66				80.3		3340		2.67				80.7		3360		2.67				80		4060		2.65

		79.8		3770		2.65				80.1		3660		2.66				80.4		3340		2.67				80.7		3360		2.67				80.1		4060		2.65

		79.9		3770		2.65				80.2		3660		2.66				80.4		3350		2.67				80.8		3360		2.68				80.1		4070		2.66

		80		3780		2.65				80.2		3660		2.66				80.6		3350		2.68				80.8		3370		2.68				80.2		4070		2.66

		80.1		3780		2.65				80.3		3670		2.66				80.7		3350		2.68				80.9		3370		2.68				80.3		4070		2.66

		80.1		3780		2.66				80.3		3670		2.67				80.7		3350		2.68				81		3370		2.68				80.4		4070		2.67

		80.2		3780		2.66				80.4		3670		2.67				80.7		3360		2.68				81.1		3380		2.69				80.4		4080		2.67

		80.2		3790		2.66				80.5		3670		2.67				80.8		3360		2.69				81.2		3380		2.69				80.5		4080		2.67

		80.3		3790		2.66				80.6		3650		2.67				80.9		3360		2.69				81.2		3380		2.69				80.6		4080		2.67

		80.4		3790		2.67				80.6		3650		2.68				81		3360		2.69				81.3		3380		2.69				80.6		4080		2.67

		80.4		3790		2.67				80.7		3660		2.68				81		3360		2.69				81.3		3380		2.69				80.7		4090		2.68

		80.5		3800		2.67				80.8		3660		2.68				81.1		3370		2.7				81.4		3390		2.7				80.8		4090		2.68

		80.6		3800		2.67				80.9		3660		2.68				81.2		3370		2.7				81.5		3390		2.7				80.9		4090		2.68

		80.7		3800		2.67				80.9		3670		2.68				81.3		3370		2.7				81.5		3390		2.7				80.9		4100		2.68

		80.7		3800		2.68				81		3670		2.69				81.3		3370		2.7				81.7		3390		2.7				81		4100		2.69

		80.8		3810		2.68				81.1		3680		2.69				81.4		3380		2.7				81.7		3400		2.71				81.1		4100		2.69

		80.9		3810		2.68				81.1		3680		2.69				81.4		3380		2.71				81.8		3400		2.71				81.1		4100		2.69

		80.9		3810		2.68				81.2		3680		2.7				81.5		3380		2.71				81.9		3400		2.71				81.2		4100		2.69

		81		3810		2.69				81.3		3680		2.7				81.6		3380		2.71				81.9		3400		2.71				81.2		4110		2.69

		81.1		3820		2.69				81.3		3680		2.7				81.6		3380		2.71				82		3400		2.72				81.4		4110		2.7

		81.1		3820		2.69				81.4		3680		2.7				81.7		3390		2.72				82		3410		2.72				81.4		4110		2.7

		81.2		3820		2.69				81.5		3690		2.7				81.8		3390		2.72				82.1		3410		2.72				81.5		4120		2.7

		81.3		3830		2.7				81.5		3690		2.71				81.9		3390		2.72				82.2		3410		2.72				81.6		4120		2.7

		81.3		3830		2.7				81.6		3690		2.71				81.9		3390		2.72				82.3		3420		2.73				81.6		4120		2.71

		81.4		3830		2.7				81.7		3690		2.71				82		3390		2.72				82.3		3420		2.73				81.7		4110		2.71

		81.5		3830		2.7				81.7		3690		2.71				82		3400		2.73				82.4		3420		2.73				81.8		4120		2.71

		81.5		3840		2.7				81.8		3700		2.71				82.1		3400		2.73				82.5		3420		2.73				81.8		4120		2.71

		81.6		3840		2.71				81.9		3700		2.72				82.2		3400		2.73				82.5		3420		2.73				81.9		4120		2.72

		81.7		3840		2.71				81.9		3700		2.72				82.3		3400		2.73				82.6		3430		2.74				82		4130		2.72

		81.7		3840		2.71				82		3700		2.72				82.4		3410		2.74				82.7		3430		2.74				82.1		4130		2.72

		81.8		3850		2.71				82		3710		2.72				82.4		3410		2.74				82.7		3430		2.74				82.1		4130		2.72

		81.9		3850		2.72				82.1		3710		2.73				82.5		3410		2.74				82.8		3430		2.74				82.2		4130		2.73

		82		3850		2.72				82.2		3700		2.73				82.6		3410		2.74				82.9		3430		2.75				82.3		4130		2.73

		82		3850		2.72				82.3		3710		2.73				82.6		3420		2.74				83		3440		2.75				82.3		4140		2.73

		82.1		3860		2.72				82.3		3710		2.73				82.6		3420		2.75				83		3440		2.75				82.4		4140		2.73

		82.2		3860		2.72				82.4		3710		2.73				82.7		3420		2.75				83.1		3440		2.75				82.5		4140		2.73

		82.2		3860		2.73				82.5		3710		2.74				82.8		3420		2.75				83.1		3440		2.75				82.5		4140		2.74

		82.3		3860		2.73				82.5		3720		2.74				82.9		3430		2.76				83.2		3450		2.76				82.6		4140		2.74

		82.4		3870		2.73				82.6		3720		2.74				83		3430		2.76				83.3		3450		2.76				82.6		4150		2.74

		82.4		3870		2.73				82.6		3720		2.74				83.1		3430		2.76				83.3		3450		2.76				82.7		4150		2.74

		82.5		3870		2.74				82.7		3720		2.74				83.1		3430		2.76				83.5		3450		2.77				82.8		4150		2.75

		82.6		3880		2.74				82.8		3730		2.75				83.2		3430		2.76				83.5		3460		2.77				82.8		4150		2.75

		82.6		3880		2.74				82.9		3730		2.75				83.2		3430		2.77				83.6		3460		2.77				82.9		4160		2.75

		82.7		3880		2.74				82.9		3730		2.75				83.3		3430		2.77				83.7		3460		2.77				83		4160		2.75

		82.7		3880		2.74				83		3730		2.75				83.4		3430		2.77				83.7		3460		2.77				83		4160		2.75

		82.8		3880		2.75				83		3730		2.76				83.5		3440		2.77				83.8		3460		2.78				83.1		4160		2.76

		82.9		3890		2.75				83.1		3740		2.76				83.5		3440		2.78				83.8		3470		2.78				83.2		4160		2.76

		83		3890		2.75				83.2		3740		2.76				83.6		3440		2.78				83.9		3470		2.78				83.2		4170		2.76

		83.1		3890		2.75				83.3		3740		2.76				83.6		3450		2.78				84		3470		2.78				83.3		4170		2.76

		83.1		3900		2.76				83.4		3740		2.77				83.7		3450		2.78				84.1		3470		2.78				83.4		4170		2.76

		83.1		3900		2.76				83.5		3750		2.77				83.8		3450		2.78				84.1		3480		2.79				83.4		4170		2.77

		83.2		3900		2.76				83.5		3750		2.77				83.9		3450		2.79				84.2		3480		2.79				83.5		4170		2.77

		83.3		3900		2.76				83.5		3750		2.77				83.9		3450		2.79				84.3		3480		2.79				83.6		4180		2.77

		83.3		3910		2.76				83.6		3750		2.77				84		3460		2.79				84.3		3480		2.79				83.6		4180		2.77

		83.4		3910		2.77				83.7		3750		2.78				84.1		3460		2.79				84.4		3490		2.8				83.7		4180		2.78

		83.5		3910		2.77				83.8		3760		2.78				84.1		3460		2.8				84.4		3490		2.8				83.8		4180		2.78

		83.6		3910		2.77				83.8		3760		2.78				84.2		3460		2.8				84.5		3490		2.8				83.9		4190		2.78

		83.6		3920		2.77				83.9		3760		2.78				84.2		3460		2.8				84.6		3490		2.8				83.9		4190		2.78

		83.7		3920		2.78				84		3750		2.79				84.3		3470		2.8				84.7		3500		2.81				84		4190		2.78

		83.8		3920		2.78				84.1		3760		2.79				84.4		3470		2.8				84.8		3500		2.81				84		4190		2.79

		83.8		3920		2.78				84.1		3760		2.79				84.4		3470		2.81				84.8		3500		2.81				84.1		4190		2.79

		83.9		3930		2.78				84.2		3760		2.79				84.5		3470		2.81				84.9		3500		2.81				84.1		4190		2.79

		83.9		3930		2.78				84.2		3770		2.8				84.5		3470		2.81				84.9		3500		2.81				84.3		4200		2.8

		84		3930		2.79				84.3		3770		2.8				84.7		3480		2.81				85		3510		2.82				84.3		4200		2.8

		84.1		3930		2.79				84.4		3770		2.8				84.7		3480		2.82				85.1		3510		2.82				84.4		4200		2.8

		84.2		3940		2.79				84.4		3770		2.8				84.8		3480		2.82				85.1		3510		2.82				84.5		4210		2.8

		84.2		3940		2.79				84.5		3770		2.8				84.8		3480		2.82				85.2		3510		2.82				84.5		4210		2.8

		84.3		3940		2.8				84.6		3780		2.81				84.9		3490		2.82				85.3		3510		2.83				84.6		4210		2.81

		84.4		3940		2.8				84.6		3780		2.81				85		3490		2.82				85.3		3520		2.83				84.6		4210		2.81

		84.4		3940		2.8				84.7		3780		2.81				85		3490		2.83				85.4		3520		2.83				84.7		4210		2.81

		84.5		3950		2.8				84.7		3780		2.81				85.1		3490		2.83				85.5		3520		2.83				84.8		4210		2.81

		84.5		3950		2.8				84.8		3780		2.81				85.2		3490		2.83				85.5		3520		2.83				84.9		4220		2.82

		84.6		3950		2.81				84.9		3780		2.82				85.2		3500		2.83				85.6		3530		2.84				85		4220		2.82

		84.7		3950		2.81				84.9		3790		2.82				85.3		3500		2.83				85.7		3530		2.84				85		4220		2.82

		84.8		3960		2.81				85		3790		2.82				85.4		3500		2.84				85.8		3530		2.84				85		4220		2.82

		84.8		3960		2.81				85.1		3790		2.82				85.4		3500		2.84				85.8		3530		2.84				85.1		4220		2.82

		84.9		3960		2.82				85.2		3790		2.83				85.5		3500		2.84				85.9		3540		2.85				85.2		4220		2.83

		85		3960		2.82				85.3		3800		2.83				85.5		3510		2.84				86		3540		2.85				85.2		4220		2.83

		85		3970		2.82				85.3		3800		2.83				85.6		3510		2.84				86		3540		2.85				85.3		4220		2.83

		85		3970		2.82				85.4		3800		2.83				85.7		3510		2.85				86.1		3540		2.85				85.4		4230		2.83

		85.1		3970		2.82				85.4		3800		2.84				85.7		3510		2.85				86.1		3540		2.85				85.5		4230		2.84

		85.2		3970		2.83				85.5		3810		2.84				85.9		3520		2.85				86.2		3550		2.86				85.5		4230		2.84

		85.3		3980		2.83				85.5		3810		2.84				85.9		3520		2.86				86.3		3550		2.86				85.6		4230		2.84

		85.4		3980		2.83				85.7		3810		2.84				86		3520		2.86				86.4		3550		2.86				85.7		4240		2.84

		85.4		3980		2.83				85.7		3810		2.85				86.1		3520		2.86				86.4		3550		2.86				85.8		4240		2.84

		85.5		3980		2.84				85.8		3820		2.85				86.1		3530		2.86				86.5		3550		2.87				85.8		4240		2.85

		85.5		3990		2.84				85.9		3820		2.85				86.2		3530		2.86				86.6		3560		2.87				85.9		4240		2.85

		85.6		3990		2.84				85.9		3820		2.85				86.2		3530		2.87				86.6		3560		2.87				86		4240		2.85

		85.7		3990		2.84				86		3820		2.85				86.3		3530		2.87				86.7		3560		2.87				86		4250		2.85

		85.7		3990		2.84				86		3820		2.86				86.4		3530		2.87				86.8		3560		2.87				86.1		4250		2.86

		85.9		4000		2.85				86.1		3830		2.86				86.4		3540		2.87				86.9		3570		2.88				86.2		4250		2.86

		85.9		4000		2.85				86.3		3830		2.86				86.5		3540		2.88				86.9		3570		2.88				86.2		4250		2.86

		86		4000		2.85				86.3		3830		2.86				86.6		3540		2.88				87		3570		2.88				86.3		4250		2.86

		86		4010		2.85				86.4		3830		2.87				86.6		3540		2.88				87.1		3570		2.88				86.4		4260		2.86

		86.1		4010		2.86				86.4		3840		2.87				86.7		3540		2.88				87.1		3580		2.89				86.4		4260		2.87

		86.2		4010		2.86				86.5		3840		2.87				86.7		3550		2.88				87.2		3580		2.89				86.5		4260		2.87

		86.2		4010		2.86				86.5		3840		2.87				86.8		3550		2.89				87.3		3580		2.89				86.6		4260		2.87

		86.3		4020		2.86				86.6		3840		2.87				86.9		3550		2.89				87.3		3580		2.89				86.7		4270		2.88

		86.4		4020		2.87				86.7		3840		2.88				87		3560		2.89				87.4		3580		2.9				86.7		4270		2.88

		86.5		4020		2.87				86.8		3840		2.88				87		3560		2.89				87.5		3590		2.9				86.8		4270		2.88

		86.5		4020		2.87				86.8		3850		2.88				87.1		3560		2.9				87.5		3590		2.9				86.9		4270		2.88

		86.6		4030		2.87				86.9		3850		2.88				87.2		3560		2.9				87.6		3590		2.9				86.9		4270		2.88

		86.6		4030		2.87				87		3850		2.89				87.2		3560		2.9				87.6		3590		2.9				87		4280		2.89

		86.7		4030		2.88				87		3850		2.89				87.3		3570		2.9				87.7		3600		2.91				87.1		4280		2.89

		86.8		4030		2.88				87.1		3850		2.89				87.4		3570		2.9				87.8		3600		2.91				87.1		4280		2.89

		86.8		4040		2.88				87.2		3860		2.89				87.4		3570		2.91				87.8		3600		2.91				87.2		4280		2.89

		86.9		4040		2.88				87.2		3860		2.89				87.5		3570		2.91				87.9		3600		2.91				87.3		4290		2.9

		87		4040		2.89				87.3		3860		2.9				87.6		3580		2.91				88		3600		2.92				87.4		4290		2.9

		87.1		4040		2.89				87.4		3860		2.9				87.7		3580		2.91				88		3610		2.92				87.4		4290		2.9

		87.1		4050		2.89				87.4		3860		2.9				87.7		3580		2.92				88.1		3610		2.92				87.4		4290		2.9

		87.2		4050		2.89				87.5		3870		2.9				87.8		3580		2.92				88.2		3610		2.92				87.5		4290		2.9

		87.3		4050		2.89				87.5		3870		2.91				87.9		3580		2.92				88.3		3610		2.92				87.6		4300		2.91

		87.3		4050		2.9				87.6		3870		2.91				87.9		3590		2.92				88.3		3620		2.93				87.7		4300		2.91

		87.4		4060		2.9				87.7		3870		2.91				88		3590		2.92				88.4		3620		2.93				87.8		4300		2.91

		87.4		4060		2.9				87.7		3870		2.91				88		3590		2.93				88.4		3620		2.93				87.8		4300		2.91

		87.5		4060		2.9				87.8		3880		2.91				88.1		3590		2.93				88.5		3620		2.93				87.9		4300		2.91

		87.6		4070		2.91				87.9		3880		2.92				88.2		3600		2.93				88.5		3620		2.93				87.9		4310		2.92

		87.7		4070		2.91				88		3880		2.92				88.3		3600		2.93				88.7		3630		2.94				88		4310		2.92

		87.8		4070		2.91				88.1		3890		2.92				88.3		3600		2.94				88.7		3630		2.94				88.1		4310		2.92

		87.8		4070		2.91				88.1		3890		2.92				88.4		3600		2.94				88.8		3630		2.94				88.1		4310		2.92

		87.9		4070		2.92				88.2		3890		2.93				88.5		3600		2.94				88.8		3630		2.94				88.2		4320		2.93

		88		4070		2.92				88.2		3890		2.93				88.5		3610		2.94				88.9		3640		2.95				88.2		4320		2.93

		88		4080		2.92				88.3		3890		2.93				88.6		3610		2.94				89		3640		2.95				88.3		4320		2.93

		88.1		4080		2.92				88.4		3900		2.93				88.7		3610		2.95				89		3640		2.95				88.4		4320		2.93

		88.2		4080		2.92				88.4		3900		2.94				88.7		3610		2.95				89.1		3640		2.95				88.4		4320		2.93

		88.2		4090		2.93				88.5		3900		2.94				88.8		3610		2.95				89.1		3640		2.95				88.5		4330		2.94

		88.3		4090		2.93				88.6		3900		2.94				88.9		3620		2.95				89.3		3650		2.96				88.6		4330		2.94

		88.4		4090		2.93				88.7		3900		2.94				89		3620		2.96				89.3		3650		2.96				88.6		4330		2.94

		88.4		4080		2.93				88.7		3910		2.94				89		3620		2.96				89.4		3650		2.96				88.7		4330		2.94

		88.4		4080		2.93				88.8		3910		2.95				89		3620		2.96				89.5		3660		2.96				88.8		4340		2.95

		88.5		4080		2.94				88.8		3910		2.95				89.1		3630		2.96				89.5		3660		2.97				88.9		4340		2.95

		88.6		4090		2.94				88.9		3910		2.95				89.2		3630		2.96				89.6		3660		2.97				89		4340		2.95

		88.7		4090		2.94				89		3910		2.95				89.2		3630		2.97				89.6		3660		2.97				89		4340		2.95

		88.7		4090		2.94				89.1		3920		2.96				89.4		3630		2.97				89.7		3660		2.97				89.1		4350		2.96

		88.8		4100		2.95				89.1		3920		2.96				89.5		3640		2.97				89.8		3670		2.98				89.2		4350		2.96

		88.9		4100		2.95				89.2		3920		2.96				89.5		3640		2.97				89.9		3670		2.98				89.2		4350		2.96

		88.9		4100		2.95				89.3		3920		2.96				89.5		3640		2.98				90		3670		2.98				89.3		4350		2.96

		89		4100		2.95				89.3		3930		2.96				89.6		3640		2.98				90		3670		2.98				89.3		4350		2.96

		89		4110		2.95				89.4		3930		2.97				89.7		3640		2.98				90.1		3680		2.99				89.4		4360		2.97

		89.1		4110		2.96				89.4		3930		2.97				89.8		3650		2.98				90.1		3680		2.99				89.4		4360		2.97

		89.2		4110		2.96				89.5		3930		2.97				89.8		3650		2.99				90.2		3680		2.99				89.6		4360		2.97

		89.3		4110		2.96				89.6		3930		2.97				89.9		3650		2.99				90.3		3680		2.99				89.6		4370		2.97

		89.3		4110		2.96				89.6		3940		2.98				90		3650		2.99				90.3		3680		2.99				89.7		4370		2.98

		89.4		4120		2.97				89.7		3940		2.98				90.1		3660		2.99				90.5		3690		3				89.8		4370		2.98

		89.5		4120		2.97				89.8		3940		2.98				90.1		3660		3				90.5		3690		3				89.9		4370		2.98

		89.5		4120		2.97				89.8		3940		2.98				90.2		3660		3				90.6		3690		3				89.9		4370		2.98

		89.6		4130		2.97				89.9		3940		2.98				90.3		3660		3				90.6		3700		3				90		4380		2.98

		89.7		4130		2.97				89.9		3950		2.99				90.3		3660		3				90.7		3700		3.01				90		4380		2.99

		89.7		4130		2.98				90		3950		2.99				90.4		3670		3				90.8		3700		3.01				90.1		4380		2.99

		89.8		4130		2.98				90.1		3950		2.99				90.4		3670		3.01				90.8		3700		3.01				90.2		4390		2.99

		89.9		4140		2.98				90.2		3950		2.99				90.5		3670		3.01				90.9		3700		3.01				90.3		4390		2.99

		89.9		4140		2.98				90.2		3960		3				90.5		3670		3.01				91		3710		3.02				90.3		4390		3

		90		4140		2.99				90.3		3960		3				90.6		3670		3.01				91.1		3710		3.02				90.4		4390		3

		90		4140		2.99				90.3		3960		3				90.7		3680		3.01				91.2		3710		3.02				90.4		4390		3

		90.1		4140		2.99				90.4		3960		3				90.7		3680		3.02				91.2		3710		3.02				90.5		4400		3

		90.2		4150		2.99				90.5		3960		3				90.8		3680		3.02				91.3		3720		3.03				90.6		4400		3.01

		90.2		4150		2.99				90.6		3970		3.01				90.9		3680		3.02				91.3		3720		3.03				90.6		4400		3.01

		90.3		4150		3				90.7		3970		3.01				90.9		3680		3.02				91.4		3720		3.03				90.7		4400		3.01

		90.4		4150		3				90.7		3970		3.01				91		3690		3.03				91.4		3720		3.03				90.8		4410		3.01

		90.5		4160		3				90.8		3970		3.01				91.1		3690		3.03				91.6		3730		3.03				90.9		4410		3.02

		90.5		4160		3				90.9		3980		3.02				91.2		3690		3.03				91.6		3730		3.04				91		4410		3.02

		90.6		4160		3.01				90.9		3980		3.02				91.2		3690		3.03				91.7		3730		3.04				91		4410		3.02

		90.7		4170		3.01				91		3980		3.02				91.3		3700		3.03				91.7		3730		3.04				91.1		4420		3.02

		90.7		4170		3.01				91.1		3980		3.02				91.4		3700		3.04				91.8		3730		3.04				91.1		4420		3.02

		90.8		4170		3.01				91.1		3980		3.02				91.4		3700		3.04				91.9		3740		3.05				91.2		4420		3.03

		90.9		4170		3.02				91.2		3990		3.03				91.5		3700		3.04				91.9		3740		3.05				91.3		4420		3.03

		90.9		4180		3.02				91.3		3990		3.03				91.5		3520		3.04				92		3740		3.05				91.3		4430		3.03

		91		4180		3.02				91.3		3990		3.03				91.6		3350		3.05				92.1		3740		3.05				91.4		4430		3.03

		91.1		4180		3.02				91.4		3990		3.04				91.7		3350		3.05				92.1		3750		3.05				91.5		4430		3.04

		91.1		4190		3.02				91.5		4000		3.04				91.7		3350		3.05				92.2		3750		3.06				91.6		4430		3.04

		91.2		4190		3.03				91.5		4000		3.04				91.8		3360		3.05				92.3		3750		3.06				91.6		4430		3.04

		91.3		4190		3.03				91.6		4000		3.04				91.9		3360		3.05				92.3		3750		3.06				91.7		4440		3.04

		91.3		4190		3.03				91.7		4000		3.04				91.9		3360		3.06				92.4		3750		3.06				91.7		4440		3.04

		91.4		4190		3.03				91.7		4000		3.05				92		3370		3.06				92.5		3760		3.06				91.8		4440		3.05

		91.4		4200		3.03				91.8		4010		3.05				92.1		3380		3.06				92.5		3760		3.07				91.9		4440		3.05

		91.5		4200		3.04				91.9		4010		3.05				92.1		3380		3.06				92.6		3760		3.07				91.9		4450		3.05

		91.6		4200		3.04				91.9		4010		3.05				92.2		3390		3.07				92.6		3760		3.07				92		4450		3.05

		91.7		4200		3.04				92		4010		3.05				92.3		3400		3.07				92.8		3770		3.08				92.1		4450		3.06

		91.7		4210		3.04				92.1		4020		3.06				92.4		3400		3.07				92.8		3770		3.08				92.1		4450		3.06

		91.8		4210		3.05				92.1		4020		3.06				92.4		3410		3.07				92.9		3770		3.08				92.2		4450		3.06

		91.9		4210		3.05				92.2		4020		3.06				92.5		3410		3.07				93		3770		3.08				92.3		4460		3.06

		91.9		4210		3.05				92.2		4020		3.06				92.5		3420		3.08				93		3780		3.08				92.3		4460		3.06

		92		4220		3.05				92.3		4020		3.07				92.6		3430		3.08				93.1		3780		3.09				92.4		4460		3.07

		92		4220		3.05				92.4		4030		3.07				92.7		3430		3.08				93.2		3780		3.09				92.4		4460		3.07

		92.1		4220		3.06				92.5		4030		3.07				92.7		3430		3.08				93.2		3780		3.09				92.6		4470		3.07

		92.2		4220		3.06				92.6		4030		3.07				92.8		3440		3.08				93.3		3790		3.09				92.7		4470		3.07

		92.3		4230		3.06				92.6		4030		3.07				92.9		3440		3.09				93.4		3790		3.1				92.7		4470		3.08

		92.3		4230		3.06				92.7		4030		3.08				92.9		3450		3.09				93.4		3790		3.1				92.8		4470		3.08

		92.4		4230		3.07				92.7		4040		3.08				93		3450		3.09				93.5		3790		3.1				92.8		4480		3.08

		92.4		4230		3.07				92.8		4040		3.08				93		3460		3.09				93.6		3800		3.1				92.9		4480		3.08

		92.5		4240		3.07				92.8		4040		3.08				93.1		3460		3.1				93.6		3800		3.1				92.9		4480		3.08

		92.6		4240		3.07				92.9		4040		3.08				93.2		3460		3.1				93.7		3800		3.11				93		4480		3.09

		92.6		4240		3.07				93		4040		3.09				93.3		3460		3.1				93.8		3800		3.11				93.1		4490		3.09

		92.7		4240		3.08				93.1		4050		3.09				93.4		3470		3.1				93.9		3800		3.11				93.2		4490		3.09

		92.8		4250		3.08				93.2		4050		3.09				93.4		3470		3.11				93.9		3810		3.11				93.3		4490		3.09

		92.9		4250		3.08				93.2		4050		3.1				93.5		3470		3.11				94		3810		3.12				93.3		4490		3.1

		93		4250		3.08				93.3		4050		3.1				93.5		3480		3.11				94.1		3810		3.12				93.4		4490		3.1

		93		4250		3.09				93.4		4050		3.1				93.6		3480		3.11				94.1		3810		3.12				93.4		4490		3.1

		93.1		4260		3.09				93.4		4060		3.1				93.7		3480		3.11				94.2		3810		3.12				93.5		4500		3.1

		93.1		4260		3.09				93.5		4060		3.1				93.8		3490		3.12				94.3		3820		3.12				93.6		4500		3.11

		93.2		4260		3.09				93.6		4060		3.11				93.9		3490		3.12				94.3		3820		3.13				93.7		4500		3.11

		93.3		4260		3.1				93.7		4060		3.11				93.9		3500		3.12				94.4		3820		3.13				93.7		4500		3.11

		93.3		4270		3.1				93.7		4070		3.11				94		3500		3.12				94.5		3820		3.13				93.8		4510		3.11

		93.5		4270		3.1				93.7		4070		3.11				94		3500		3.13				94.5		3830		3.13				93.9		4510		3.11

		93.5		4270		3.1				93.8		4070		3.12				94.1		3510		3.13				94.6		3830		3.14				93.9		4510		3.12

		93.6		4280		3.11				93.9		4070		3.12				94.2		3510		3.13				94.6		3830		3.14				94		4510		3.12

		93.6		4280		3.11				93.9		4070		3.12				94.2		3510		3.13				94.7		3830		3.14				94		4510		3.12

		93.7		4280		3.11				94		4080		3.12				94.3		3510		3.14				94.8		3840		3.14				94.1		4520		3.12

		93.8		4280		3.11				94.1		4080		3.12				94.4		3510		3.14				94.8		3840		3.14				94.2		4520		3.12

		93.8		4290		3.11				94.2		4080		3.13				94.4		3510		3.14				94.9		3840		3.15				94.2		4520		3.13

		93.9		4290		3.12				94.3		4080		3.13				94.5		3510		3.14				95		3840		3.15				94.3		4520		3.13

		94		4290		3.12				94.3		4090		3.13				94.6		3510		3.14				95.1		3850		3.15				94.4		4520		3.13

		94		4290		3.12				94.4		4090		3.13				94.7		3520		3.15				95.1		3850		3.15				94.4		4520		3.13

		94.1		4300		3.12				94.5		4090		3.14				94.7		3520		3.15				95.2		3850		3.16				94.5		4530		3.14

		94.2		4300		3.13				94.5		4090		3.14				94.8		3520		3.15				95.3		3850		3.16				94.6		4530		3.14

		94.3		4300		3.13				94.6		4090		3.14				94.8		3520		3.15				95.3		3850		3.16				94.6		4530		3.14

		94.3		4300		3.13				94.6		4080		3.14				94.9		3530		3.16				95.4		3860		3.16				94.7		4530		3.14

		94.3		4310		3.13				94.8		4070		3.15				95		3530		3.16				95.4		3860		3.16				94.7		4530		3.14

		94.4		4310		3.13				94.8		4080		3.15				95		3530		3.16				95.6		3860		3.17				94.9		4540		3.15

		94.5		4310		3.14				94.9		4080		3.15				95.1		3530		3.16				95.7		3860		3.17				94.9		4540		3.15

		94.6		4320		3.14				95		4080		3.15				95.2		3530		3.16				95.7		3870		3.17				95		4540		3.15

		94.7		4320		3.14				95		4090		3.15				95.2		3540		3.17				95.8		3870		3.18				95.1		4540		3.16

		94.8		4320		3.14				95.1		4090		3.16				95.3		3540		3.17				95.8		3870		3.18				95.1		4540		3.16

		94.8		4320		3.15				95.2		4090		3.16				95.4		3540		3.17				95.9		3870		3.18				95.2		4540		3.16

		94.8		4330		3.15				95.2		4090		3.16				95.5		3530		3.17				95.9		3880		3.18				95.2		4540		3.16

		94.9		4330		3.15				95.3		4100		3.16				95.5		3540		3.18				96		3880		3.18				95.3		4550		3.16

		95		4330		3.15				95.3		4100		3.17				95.6		3540		3.18				96.1		3880		3.19				95.4		4550		3.17

		95.1		4330		3.16				95.4		4100		3.17				95.7		3540		3.18				96.2		3880		3.19				95.5		4550		3.17

		95.2		4340		3.16				95.5		4100		3.17				95.7		3540		3.18				96.3		3890		3.19				95.6		4550		3.17

		95.2		4340		3.16				95.6		4100		3.17				95.8		3540		3.18				96.3		3890		3.19				95.6		4560		3.17

		95.3		4340		3.16				95.6		4100		3.17				95.8		3540		3.19				96.4		3890		3.2				95.7		4560		3.18

		95.3		4340		3.16				95.7		4100		3.18				95.9		3540		3.19				96.4		3890		3.2				95.8		4560		3.18

		95.4		4350		3.17				95.7		4110		3.18				96		3540		3.19				96.5		3890		3.2				95.8		4560		3.18

		95.5		4350		3.17				95.8		4110		3.18				96		3540		3.19				96.6		3900		3.2				95.9		4570		3.18

		95.5		4350		3.17				95.9		4110		3.18				96.1		3550		3.2				96.6		3900		3.2				96		4570		3.18

		95.6		4350		3.17				96		4110		3.19				96.2		3550		3.2				96.7		3900		3.21				96.1		4570		3.19

		95.7		4360		3.18				96		4110		3.19				96.3		3550		3.2				96.8		3900		3.21				96.1		4570		3.19

		95.8		4360		3.18				96.1		4110		3.19				96.3		3550		3.2				96.9		3910		3.21				96.2		4570		3.19

		95.8		4360		3.18				96.1		4110		3.19				96.3		3550		3.2				96.9		3910		3.21				96.2		4570		3.19

		95.9		4360		3.18				96.2		4120		3.19				96.4		3550		3.21				97		3910		3.22				96.3		4580		3.2

		95.9		4370		3.18				96.2		4120		3.2				96.5		3550		3.21				97.1		3910		3.22				96.4		4580		3.2

		96		4370		3.19				96.3		4120		3.2				96.6		3550		3.21				97.1		3920		3.22				96.4		4580		3.2

		96.1		4370		3.19				96.4		4120		3.2				96.7		3560		3.21				97.2		3920		3.22				96.5		4580		3.2

		96.1		4370		3.19				96.5		4120		3.2				96.7		3560		3.21				97.3		3920		3.22				96.5		4580		3.2

		96.2		4380		3.19				96.5		4130		3.21				96.8		3560		3.22				97.3		3920		3.23				96.7		4590		3.21

		96.2		4380		3.19				96.6		4130		3.21				96.8		3560		3.22				97.4		3930		3.23				96.7		4590		3.21

		96.3		4380		3.2				96.6		4130		3.21				96.9		3560		3.22				97.5		3930		3.23				96.8		4590		3.21

		96.4		4380		3.2				96.7		4130		3.21				97		3560		3.22				97.5		3930		3.23				96.9		4590		3.21

		96.4		4390		3.2				96.8		4130		3.21				97		3560		3.23				97.6		3930		3.24				96.9		4600		3.22

		96.5		4390		3.2				96.9		4130		3.22				97.2		3570		3.23				97.7		3930		3.24				97		4600		3.22

		96.6		4390		3.21				96.9		4140		3.22				97.2		3570		3.23				97.7		3940		3.24				97.1		4600		3.22

		96.6		4390		3.21				97		4140		3.22				97.3		3570		3.23				97.8		3940		3.24				97.1		4600		3.22

		96.7		4400		3.21				97.1		4140		3.22				97.3		3570		3.24				97.9		3940		3.24				97.2		4610		3.23

		96.7		4400		3.21				97.1		4140		3.23				97.4		3570		3.24				98		3940		3.25				97.3		4610		3.23

		96.8		4400		3.21				97.2		4140		3.23				97.4		3580		3.24				98.1		3950		3.25				97.4		4610		3.23

		96.9		4400		3.22				97.2		4150		3.23				97.5		3580		3.24				98.1		3950		3.25				97.4		4610		3.23

		97		4410		3.22				97.3		4150		3.23				97.6		3580		3.24				98.2		3950		3.26				97.5		4620		3.24

		97		4410		3.22				97.4		4150		3.23				97.6		3580		3.25				98.2		3950		3.26				97.6		4620		3.24

		97.1		4410		3.22				97.4		4150		3.24				97.7		3580		3.25				98.3		3950		3.26				97.6		4620		3.24

		97.2		4410		3.22				97.6		4160		3.24				97.8		3580		3.25				98.3		3960		3.26				97.7		4620		3.24

		97.2		4420		3.23				97.6		4160		3.24				97.8		3580		3.25				98.4		3960		3.26				97.8		4630		3.25

		97.3		4420		3.23				97.7		4160		3.24				97.9		3590		3.25				98.5		3960		3.27				97.8		4630		3.25

		97.4		4420		3.23				97.7		4160		3.25				97.9		3590		3.26				98.5		3960		3.27				97.9		4630		3.25

		97.5		4430		3.24				97.8		4160		3.25				98		3590		3.26				98.6		3960		3.27				98		4630		3.25

		97.5		4430		3.24				97.9		4160		3.25				98.1		3590		3.26				98.7		3970		3.27				98		4630		3.25

		97.6		4430		3.24				97.9		4170		3.25				98.1		3590		3.26				98.7		3970		3.27				98.1		4630		3.26

		97.7		4430		3.24				98		4170		3.25				98.3		3590		3.27				98.8		3970		3.28				98.1		4640		3.26

		97.7		4430		3.24				98.1		4170		3.26				98.3		3590		3.27				98.8		3970		3.28				98.2		4640		3.26

		97.8		4440		3.25				98.2		4180		3.26				98.4		3590		3.27				98.9		3970		3.28				98.4		4640		3.26

		97.8		4440		3.25				98.3		4180		3.26				98.5		3590		3.27				99		3980		3.28				98.4		4640		3.27

		97.9		4440		3.25				98.3		4180		3.26				98.5		3600		3.28				99.1		3980		3.29				98.5		4650		3.27

		98		4450		3.25				98.4		4180		3.27				98.6		3600		3.28				99.2		3980		3.29				98.5		4650		3.27

		98.1		4450		3.26				98.4		4180		3.27				98.7		3600		3.28				99.2		3980		3.29				98.6		4650		3.27

		98.1		4450		3.26				98.5		4190		3.27				98.7		3600		3.28				99.3		3980		3.29				98.7		4650		3.27

		98.2		4450		3.26				98.6		4190		3.27				98.8		3600		3.29				99.3		3990		3.29				98.7		4650		3.28

		98.2		4460		3.26				98.7		4190		3.28				98.9		3600		3.29				99.4		3990		3.3				98.8		4640		3.28

		98.3		4460		3.26				98.7		4190		3.28				99		3600		3.29				99.5		3990		3.3				98.9		4640		3.28

		98.4		4460		3.27				98.8		4200		3.28				99		3600		3.29				99.5		3990		3.3				99		4640		3.29

		98.4		4460		3.27				98.8		4200		3.28				99.1		3610		3.29				99.6		4000		3.3				99.1		4650		3.29

		98.5		4460		3.27				98.9		4200		3.28				99.1		3610		3.3				99.7		4000		3.31				99.1		4650		3.29

		98.6		4470		3.27				99		4200		3.29				99.2		3610		3.3				99.7		4000		3.31				99.1		4650		3.29

		98.6		4470		3.27				99.1		4200		3.29				99.2		3610		3.3				99.8		4000		3.31				99.2		4650		3.29

		98.7		4470		3.28				99.1		4210		3.29				99.4		3610		3.3				99.9		4000		3.31				99.3		4650		3.3

		98.7		4470		3.28				99.2		4210		3.3				99.5		3610		3.31				99.9		4010		3.31				99.4		4650		3.3

		98.8		4480		3.28				99.3		4210		3.3				99.5		3610		3.31				100		4010		3.32				99.4		4650		3.3

		98.9		4480		3.28				99.3		4210		3.3				99.6		3610		3.31				100		4010		3.32				99.5		4660		3.3

		98.9		4480		3.28				99.4		4210		3.3				99.6		3620		3.31				100		4020		3.32				99.6		4660		3.3

		99.1		4480		3.29				99.5		4220		3.3				99.7		3620		3.31				100		4020		3.32				99.6		4660		3.31

		99.2		4490		3.29				99.5		4220		3.31				99.8		3620		3.32				100		4020		3.33				99.7		4660		3.31

		99.2		4490		3.29				99.6		4220		3.31				99.8		3620		3.32				100		4020		3.33				99.7		4660		3.31

		99.2		4490		3.29				99.6		4220		3.31				99.9		3620		3.32				100		4020		3.33				99.8		4660		3.31

		99.3		4490		3.3				99.8		4230		3.31				100		3620		3.33				100		4030		3.33				99.9		4660		3.32

		99.4		4500		3.3				99.9		4230		3.32				100		3620		3.33				101		4030		3.33				100		4660		3.32

		99.5		4500		3.3				99.9		4230		3.32				100		3610		3.33				101		4030		3.34				100		4660		3.32

		99.5		4500		3.3				100		4230		3.32				100		3610		3.33				101		4030		3.34				100		4670		3.32

		99.7		4500		3.31				100		4230		3.32				100		3610		3.33				101		4040		3.34				100		4670		3.32

		99.7		4510		3.31				100		4240		3.32				100		3610		3.34				101		4040		3.34				100		4670		3.33

		99.7		4510		3.31				100		4240		3.33				100		3610		3.34				101		4040		3.35				100		4670		3.33

		99.8		4510		3.31				100		4240		3.33				100		3620		3.34				101		4040		3.35				100		4670		3.33

		99.9		4510		3.32				100		4240		3.33				101		3620		3.34				101		4040		3.35				100		4670		3.33

		100		4520		3.32				100		4240		3.33				101		3620		3.34				101		4050		3.35				100		4670		3.34

		100		4520		3.32				100		4240		3.34				101		3620		3.35				101		4050		3.35				101		4670		3.34

		100		4520		3.32				101		4250		3.34				101		3620		3.35				101		4050		3.36				101		4680		3.34

		100		4520		3.32				101		4250		3.34				101		3620		3.35				101		4060		3.36				101		4680		3.34

		100		4530		3.33				101		4250		3.34				101		3620		3.35				101		4060		3.36				101		4680		3.34

		100		4530		3.33				101		4250		3.35				101		3620		3.36				101		4060		3.37				101		4680		3.35

		100		4530		3.33				101		4260		3.35				101		3630		3.36				102		4060		3.37				101		4680		3.35

		100		4530		3.33				101		4260		3.35				101		3630		3.36				102		4060		3.37				101		4680		3.35

		100		4540		3.34				101		4260		3.35				101		3630		3.36				102		4070		3.37				101		4680		3.35

		101		4540		3.34				101		4260		3.35				101		3630		3.36				102		4070		3.37				101		4690		3.35

		101		4540		3.34				101		4260		3.36				101		3630		3.37				102		4070		3.38				101		4690		3.36

		101		4540		3.34				101		4270		3.36				101		3630		3.37				102		4070		3.38				101		4690		3.36

		101		4550		3.34				101		4270		3.36				101		3630		3.37				102		4080		3.38				101		4690		3.36

		101		4550		3.35				101		4270		3.36				101		3630		3.37				102		4080		3.38				101		4690		3.36

		101		4540		3.35				101		4270		3.36				101		3630		3.37				102		4080		3.39				101		4690		3.37

		101		4330		3.35				101		4270		3.37				102		3630		3.38				102		4080		3.39				101		4700		3.37

		101		4280		3.35				101		4280		3.37				102		3640		3.38				102		4080		3.39				102		4690		3.37

		101		4290		3.36				102		4280		3.37				102		3640		3.38				102		4090		3.39				102		4690		3.37

		101		4290		3.36				102		4280		3.37				102		3640		3.38				102		4090		3.39				102		4690		3.38

		101		4290		3.36				102		4280		3.38				102		3640		3.39				102		4090		3.4				102		4700		3.38

		101		4280		3.36				102		4280		3.38				102		3640		3.39				102		4090		3.4				102		4700		3.38

		101		4230		3.37				102		4290		3.38				102		3640		3.39				103		4100		3.4				102		4700		3.38

		101		4170		3.37				102		4290		3.38				102		3640		3.39				103		4100		3.4				102		4700		3.38

		101		4180		3.37				102		4290		3.38				102		3640		3.4				103		4100		3.41				102		4700		3.39

		102		4190		3.37				102		4280		3.39				102		3640		3.4				103		4100		3.41				102		4710		3.39

		102		4200		3.37				102		4270		3.39				102		3640		3.4				103		4100		3.41				102		4710		3.39

		102		4170		3.38				102		4270		3.39				102		3640		3.4				103		4110		3.41				102		4710		3.39

		102		4140		3.38				102		4270		3.4				102		3650		3.4				103		4110		3.41				102		4710		3.4

		102		4150		3.38				102		4280		3.4				102		3650		3.41				103		4110		3.42				102		4710		3.4

		102		4160		3.38				102		4280		3.4				102		3650		3.41				103		4110		3.42				102		4710		3.4

		102		4170		3.39				102		4280		3.4				103		3650		3.41				103		4120		3.42				102		4710		3.4

		102		4180		3.39				102		4280		3.4				103		3650		3.41				103		4120		3.42				103		4710		3.4

		102		4190		3.39				103		4290		3.41				103		3650		3.42				103		4120		3.43				103		4720		3.41

		102		4200		3.39				103		4290		3.41				103		3650		3.42				103		4120		3.43				103		4720		3.41

		102		4210		3.39				103		4290		3.41				103		3660		3.42				103		4120		3.43				103		4720		3.41

		102		4220		3.4				103		4290		3.41				103		3660		3.42				103		4130		3.43				103		4720		3.41

		102		4230		3.4				103		4290		3.41				103		3660		3.42				104		4130		3.44				103		4720		3.42

		102		4250		3.4				103		4290		3.42				103		3650		3.43				104		4130		3.44				103		4720		3.42

		102		4260		3.4				103		4290		3.42				103		3660		3.43				104		4130		3.44				103		4730		3.42

		103		4260		3.4				103		4300		3.42				103		3660		3.43				104		4140		3.44				103		4730		3.42

		103		4180		3.41				103		4300		3.43				103		3660		3.43				104		4140		3.44				103		4730		3.42

		103		4000		3.41				103		4300		3.43				103		3660		3.44				104		4140		3.45				103		4730		3.43

		103		4000		3.41				103		4300		3.43				103		3670		3.44				104		4140		3.45				103		4730		3.43

		103		4000		3.41				103		4300		3.43				103		3670		3.44				104		4140		3.45				103		4730		3.43

		103		4010		3.42				103		4300		3.43				103		3670		3.44				104		4150		3.45				103		4740		3.43

		103		4020		3.42				103		4310		3.44				104		3670		3.44				104		4150		3.46				104		4740		3.44

		103		4020		3.42				104		4310		3.44				104		3670		3.45				104		4150		3.46				104		4740		3.44

		103		4010		3.42				104		4310		3.44				104		3670		3.45				104		4150		3.46				104		4740		3.44

		103		4020		3.43				104		4310		3.44				104		3670		3.45				104		4160		3.46				104		4740		3.44

		103		4020		3.43				104		4310		3.45				104		3680		3.45				104		4160		3.46				104		4740		3.45

		103		4030		3.43				104		4320		3.45				104		3680		3.46				104		4160		3.47				104		4740		3.45

		103		4040		3.43				104		4320		3.45				104		3680		3.46				105		4160		3.47				104		4750		3.45

		103		4050		3.43				104		4320		3.45				104		3680		3.46				105		4160		3.47				104		4750		3.45

		104		4060		3.44				104		4320		3.45				104		3680		3.46				105		4170		3.47				104		4730		3.45

		104		4060		3.44				104		4320		3.46				104		3680		3.46				105		4170		3.48				104		4610		3.46

		104		4070		3.44				104		4320		3.46				104		3690		3.47				105		4170		3.48				104		4620		3.46

		104		4070		3.44				104		4330		3.46				104		3690		3.47				105		4170		3.48				104		4630		3.46

		104		4080		3.45				104		4330		3.46				104		3690		3.47				105		4180		3.48				104		4630		3.46

		104		4070		3.45				104		4330		3.47				104		3690		3.47				105		4180		3.48				104		4640		3.47

		104		4080		3.45				104		4330		3.47				105		3690		3.48				105		4180		3.49				104		4650		3.47

		104		4080		3.45				105		4330		3.47				105		3690		3.48				105		4180		3.49				105		4660		3.47

		104		4090		3.45				105		4340		3.47				105		3690		3.48				105		4170		3.49				105		4670		3.47

		104		4100		3.46				105		4340		3.48				105		3690		3.48				105		4180		3.49				105		4680		3.48

		104		4100		3.46				105		4340		3.48				105		3690		3.48				105		4180		3.5				105		4650		3.48

		104		4100		3.46				105		4340		3.48				105		3690		3.49				105		4180		3.5				105		4640		3.48

		104		4110		3.46				105		4340		3.48				105		3690		3.49				106		4190		3.5				105		4640		3.48

		104		4110		3.47				105		4340		3.48				105		3700		3.49				106		4190		3.5				105		4630		3.48

		104		4120		3.47				105		4350		3.49				105		3700		3.49				106		4190		3.5				105		4630		3.49

		105		4120		3.47				105		4350		3.49				105		3700		3.5				106		4190		3.51				105		4630		3.49

		105		4120		3.47				105		4350		3.49				105		3700		3.5				106		4190		3.51				105		4630		3.49

		105		4130		3.48				105		4350		3.49				105		3700		3.5				106		4190		3.51				105		4640		3.5

		105		4130		3.48				105		4350		3.49				105		3700		3.5				106		4190		3.51				105		4650		3.5

		105		4130		3.48				105		4350		3.5				105		3700		3.5				106		4200		3.52				105		4650		3.5

		105		4140		3.48				105		4360		3.5				105		3710		3.51				106		4190		3.52				105		4650		3.5

		105		4140		3.48				105		4360		3.5				106		3700		3.51				106		4190		3.52				106		4650		3.5

		105		4110		3.49				106		4360		3.51				106		3700		3.51				106		4190		3.52				106		4660		3.51

		105		4100		3.49				106		4360		3.51				106		3700		3.51				106		4200		3.52				106		4660		3.51

		105		4110		3.49				106		4360		3.51				106		3710		3.52				106		4200		3.53				106		4660		3.51

		105		4110		3.49				106		4370		3.51				106		3710		3.52				106		4200		3.53				106		4650		3.51

		105		4110		3.5				106		4370		3.51				106		3710		3.52				106		4210		3.53				106		4640		3.51

		105		4110		3.5				106		4370		3.52				106		3710		3.52				107		4210		3.53				106		4640		3.52

		105		4120		3.5				106		4370		3.52				106		3710		3.52				107		4210		3.54				106		4640		3.52

		105		4120		3.5				106		4370		3.52				106		3720		3.53				107		4210		3.54				106		4650		3.52

		106		4110		3.5				106		4380		3.52				106		3720		3.53				107		4210		3.54				106		4650		3.52

		106		4110		3.51				106		4380		3.52				106		3720		3.53				107		4210		3.54				106		4650		3.53

		106		4110		3.51				106		4380		3.53				106		3720		3.54				107		4220		3.54				106		4650		3.53

		106		4110		3.51				106		4380		3.53				106		3720		3.54				107		4220		3.55				106		4650		3.53

		106		4120		3.51				106		4380		3.53				106		3730		3.54				107		4220		3.55				106		4650		3.53

		106		4110		3.52				106		4380		3.53				106		3730		3.54				107		4220		3.55				106		4650		3.53

		106		4120		3.52				106		4390		3.54				107		3730		3.54				107		4220		3.55				107		4650		3.54

		106		4120		3.52				106		4390		3.54				107		3730		3.55				107		4220		3.56				107		4660		3.54

		106		4120		3.52				107		4390		3.54				107		3730		3.55				107		4230		3.56				107		4660		3.54

		106		4120		3.52				107		4390		3.54				107		3730		3.55				107		4230		3.56				107		4660		3.54

		106		4130		3.53				107		4400		3.55				107		3740		3.55				107		4230		3.56				107		4660		3.55

		106		4130		3.53				107		4400		3.55				107		3690		3.55				107		4230		3.56				107		4660		3.55

		106		4130		3.53				107		4400		3.55				107		3620		3.56				107		4230		3.57				107		4660		3.55

		106		4130		3.53				107		4400		3.55				107		3620		3.56				108		4240		3.57				107		4660		3.55

		106		4140		3.54				107		4400		3.55				107		3630		3.56				108		4240		3.57				107		4670		3.55

		107		4140		3.54				107		4400		3.56				107		3640		3.56				108		4240		3.57				107		4670		3.56

		107		4150		3.54				107		4410		3.56				107		3650		3.57				108		4240		3.58				107		4670		3.56

		107		4150		3.54				107		4410		3.56				107		3660		3.57				108		4250		3.58				107		4670		3.56

		107		4150		3.54				107		4410		3.56				107		3670		3.57				108		4250		3.58				107		4670		3.56

		107		4150		3.55				107		4410		3.57				107		3670		3.57				108		4250		3.58				107		4680		3.56

		107		4150		3.55				107		4410		3.57				108		3680		3.58				108		4250		3.58				107		4640		3.57

		107		4150		3.55				107		4420		3.57				108		3690		3.58				108		4250		3.59				108		4640		3.57

		107		4150		3.55				108		4420		3.57				108		3690		3.58				108		4260		3.59				108		4630		3.57

		107		4150		3.56				108		4420		3.57				108		3690		3.58				108		4260		3.59				108		4540		3.58

		107		4150		3.56				108		4420		3.58				108		3700		3.59				108		4260		3.59				108		4510		3.58

		107		4140		3.56				108		4420		3.58				108		3700		3.59				108		4260		3.6				108		4510		3.58

		107		4140		3.56				108		4430		3.58				108		3700		3.59				108		4270		3.6				108		4510		3.58

		107		4150		3.57				108		4420		3.58				108		3700		3.59				108		4270		3.6				108		4520		3.58

		107		4150		3.57				108		4430		3.59				108		3700		3.59				109		4270		3.6				108		4530		3.59

		107		4150		3.57				108		4430		3.59				108		3700		3.6				109		4270		3.6				108		4530		3.59

		108		4150		3.57				108		4430		3.59				108		3710		3.6				109		4270		3.61				108		4540		3.59

		108		4150		3.57				108		4430		3.59				108		3710		3.6				109		4280		3.61				108		4540		3.59

		108		4150		3.58				108		4440		3.59				108		3710		3.6				109		4280		3.61				108		4550		3.6

		108		4160		3.58				108		4440		3.6				108		3710		3.61				109		4280		3.61				108		4550		3.6

		108		4160		3.58				108		4440		3.6				108		3710		3.61				109		4280		3.61				108		4550		3.6

		108		4160		3.58				108		4440		3.6				109		3710		3.61				109		4280		3.62				108		4560		3.6

		108		4160		3.58				109		4450		3.61				109		3720		3.61				109		4290		3.62				109		4550		3.6

		108		4160		3.59				109		4450		3.61				109		3720		3.61				109		4290		3.62				109		4560		3.61

		108		4160		3.59				109		4450		3.61				109		3720		3.62				109		4290		3.62				109		4570		3.61

		108		4160		3.59				109		4440		3.61				109		3720		3.62				109		4290		3.63				109		4570		3.61

		108		4160		3.6				109		4450		3.61				109		3720		3.62				109		4300		3.63				109		4580		3.61

		108		4170		3.6				109		4450		3.62				109		3710		3.62				109		4300		3.63				109		4580		3.62

		108		4170		3.6				109		4450		3.62				109		3680		3.63				110		4300		3.63				109		4590		3.62

		108		4170		3.6				109		4460		3.62				109		3690		3.63				110		4300		3.63				109		4580		3.62

		109		4170		3.6				109		4460		3.62				109		3690		3.63				110		4300		3.64				109		4580		3.62

		109		4170		3.61				109		4460		3.63				109		3700		3.63				110		4310		3.64				109		4580		3.63

		109		4180		3.61				109		4460		3.63				109		3700		3.63				110		4310		3.64				109		4580		3.63

		109		4180		3.61				109		4460		3.63				109		3700		3.64				110		4310		3.64				109		4580		3.63

		109		4180		3.61				109		4460		3.63				109		3710		3.64				110		4310		3.65				109		4580		3.63

		109		4190		3.61				109		4470		3.64				109		3710		3.64				110		4320		3.65				109		4590		3.63

		109		4190		3.62				110		4470		3.64				110		3710		3.64				110		4320		3.65				110		4590		3.64

		109		4190		3.62				110		4470		3.64				110		3710		3.65				110		4320		3.65				110		4590		3.64

		109		4190		3.62				110		4470		3.64				110		3710		3.65				110		4320		3.65				110		4590		3.64

		109		4190		3.62				110		4480		3.64				110		3710		3.65				110		4320		3.66				110		4590		3.64

		109		4190		3.63				110		4480		3.65				110		3710		3.65				110		4330		3.66				110		4590		3.65

		109		4190		3.63				110		4480		3.65				110		3710		3.65				110		4330		3.66				110		4600		3.65

		109		4200		3.63				110		4480		3.65				110		3720		3.66				110		4330		3.66				110		4600		3.65

		109		4200		3.63				110		4480		3.65				110		3720		3.66				111		4330		3.67				110		4600		3.65

		110		4200		3.64				110		4490		3.66				110		3720		3.66				111		4340		3.67				110		4600		3.66

		110		4200		3.64				110		4490		3.66				110		3720		3.66				111		4340		3.67				110		4600		3.66

		110		4210		3.64				110		4490		3.66				110		3710		3.67				111		4340		3.67				110		4600		3.66

		110		4210		3.64				110		4490		3.66				110		3710		3.67				111		4340		3.68				110		4600		3.66

		110		4110		3.64				110		4490		3.67				110		3720		3.67				111		4340		3.68				110		4610		3.66

		110		85.8		3.65				110		4490		3.67				110		3720		3.67				111		4350		3.68				110		4610		3.67

		110		-394		3.65				110		4500		3.67				110		3720		3.67				111		4350		3.68				111		4610		3.67

										111		4500		3.67				111		3720		3.68				111		4350		3.68				111		4610		3.67

										111		4500		3.67				111		3720		3.68				111		4350		3.69				111		4620		3.67

										111		4500		3.68				111		3720		3.68				111		4350		3.69				111		4620		3.68

										111		4500		3.68				111		3710		3.68				111		4360		3.69				111		4620		3.68

										111		4500		3.68				111		3720		3.69				111		4360		3.69				111		4620		3.68

										111		4510		3.68				111		3720		3.69				111		4360		3.69				111		4620		3.68

										111		4510		3.69				111		3720		3.69				111		4360		3.7				111		4630		3.69

										111		4510		3.69				111		3720		3.69				112		4360		3.7				111		4630		3.69

										111		4510		3.69				111		3720		3.69				112		4360		3.7				111		4630		3.69

										111		4510		3.69				111		3720		3.7				112		4370		3.71				111		4630		3.69

										111		4510		3.7				111		3720		3.7				112		4370		3.71				111		4640		3.69

										111		4520		3.7				111		3720		3.7				112		4370		3.71				111		4640		3.7

										111		4520		3.7				111		3720		3.7				112		4370		3.71				111		4640		3.7

										111		4520		3.7				111		3730		3.71				112		4370		3.71				111		4640		3.7

										111		4520		3.7				112		3730		3.71				112		4380		3.72				111		4650		3.7

										112		4520		3.71				112		3730		3.71				112		4380		3.72				112		4650		3.71

										112		4530		3.71				112		3730		3.71				112		4380		3.72				112		4650		3.71

										112		4530		3.71				112		3730		3.71				112		4380		3.72				112		4650		3.71

										112		4530		3.71				112		3730		3.72				112		4390		3.73				112		4660		3.71

										112		4530		3.72				112		3730		3.72				112		4390		3.73				112		4660		3.71

										112		4530		3.72				112		3740		3.72				112		4390		3.73				112		4660		3.72

										112		4530		3.72				112		3740		3.72				112		4390		3.73				112		4660		3.72

										112		4540		3.72				112		3740		3.73				113		4390		3.73				112		4660		3.72

										112		4540		3.72				112		3740		3.73				113		4390		3.74				112		4660		3.72

										112		4540		3.73				112		3740		3.73				113		4390		3.74				112		4660		3.73

										112		4540		3.73				112		3740		3.73				113		4400		3.74				112		4660		3.73

										112		4540		3.73				112		3740		3.73				113		4400		3.74				112		4650		3.73

										112		4540		3.73				112		3740		3.74				113		4400		3.74				112		4650		3.73

										112		4540		3.74				112		3750		3.74				113		4400		3.75				112		4650		3.74

										112		4540		3.74				113		3750		3.74				113		4400		3.75				113		4660		3.74

										113		4540		3.74				113		3750		3.74				113		4410		3.75				113		4660		3.74

										113		4540		3.74				113		3750		3.75				113		4410		3.75				113		4650		3.74

										113		4550		3.74				113		3750		3.75				113		4410		3.76				113		4650		3.74

										113		4550		3.75				113		3750		3.75				113		4410		3.76				113		4650		3.75

										113		4550		3.75				113		3750		3.75				113		4420		3.76				113		4650		3.75

										113		4550		3.75				113		3750		3.75				113		4420		3.76				113		4660		3.75

										113		4540		3.75				113		3750		3.76				113		4420		3.76				113		4660		3.75

										113		4530		3.76				113		3760		3.76				114		4420		3.77				113		4660		3.76

										113		4540		3.76				113		3760		3.76				114		4420		3.77				113		4660		3.76

										113		4540		3.76				113		3760		3.76				114		4430		3.77				113		4660		3.76

										113		4540		3.76				113		3760		3.77				114		4430		3.77				113		4670		3.76

										113		4540		3.77				113		3760		3.77				114		4430		3.78				113		4670		3.77

										113		4540		3.77				113		3760		3.77				114		4440		3.78				113		4670		3.77

										113		4540		3.77				113		3760		3.77				114		4440		3.78				113		4670		3.77

										114		4550		3.77				113		3770		3.77				114		4440		3.78				114		4670		3.77

										114		4550		3.78				114		3770		3.78				114		4440		3.79				114		4670		3.77

										114		4550		3.78				114		3770		3.78				114		4440		3.79				114		4670		3.78

										114		4550		3.78				114		3770		3.78				114		4450		3.79				114		4670		3.78

										114		4550		3.78				114		3770		3.78				114		4450		3.79				114		4670		3.78

										114		4550		3.78				114		3770		3.79				114		4450		3.79				114		4670		3.78

										114		4550		3.79				114		3780		3.79				114		4450		3.8				114		4660		3.79

										114		4560		3.79				114		3780		3.79				114		4450		3.8				114		4660		3.79

										114		4560		3.79				114		3780		3.79				115		4460		3.8				114		4670		3.79

										114		4560		3.79				114		3780		3.8				115		4460		3.8				114		4670		3.79

										114		4560		3.8				114		3780		3.8				115		4460		3.81				114		4670		3.79

										114		4560		3.8				114		3780		3.8				115		4460		3.81				114		4670		3.8

										114		4560		3.8				114		3790		3.8				115		4470		3.81				114		4670		3.8

										114		4560		3.8				114		3780		3.8				115		4470		3.81				114		4670		3.8

										114		4560		3.8				114		3780		3.81				115		4470		3.81				115		4670		3.8

										115		4570		3.81				115		3790		3.81				115		4470		3.82				115		4680		3.81

										115		4570		3.81				115		3790		3.81				115		4470		3.82				115		4680		3.81

										115		4570		3.81				115		3790		3.81				115		4480		3.82				115		4680		3.81

										115		4570		3.81				115		3790		3.82				115		4480		3.82				115		4680		3.81

										115		4570		3.82				115		3790		3.82				115		4480		3.82				115		4680		3.82

										115		4570		3.82				115		3800		3.82				115		4480		3.83				115		4670		3.82

										115		4570		3.82				115		3800		3.82				115		4480		3.83				115		4650		3.82

										115		4580		3.82				115		3800		3.82				115		4490		3.83				115		4630		3.82

										115		4580		3.82				115		3800		3.83				116		4490		3.84				115		2520		3.83

										115		4580		3.83				115		3800		3.83				116		4490		3.84				115		-433		3.83

										115		4580		3.83				115		3800		3.83				116		4490		3.84				115		-437		3.83

										115		4580		3.83				115		3800		3.83				116		4500		3.84

										115		4580		3.83				115		3810		3.84				116		4500		3.84

										115		4520		3.84				115		3810		3.84				116		4500		3.85

										116		4510		3.84				116		3810		3.84				116		4500		3.85

										116		4510		3.84				116		3810		3.84				116		4500		3.85

										116		4510		3.84				116		3810		3.85				116		4510		3.85

										116		4520		3.84				116		3810		3.85				116		4510		3.86

										116		4520		3.85				116		3810		3.85				116		4510		3.86

										116		4530		3.85				116		3820		3.85				116		4510		3.86

										116		4530		3.85				116		3820		3.85				116		4520		3.86

										116		4530		3.85				116		3820		3.86				116		4520		3.86

										116		4540		3.86				116		3820		3.86				117		4520		3.87

										116		4540		3.86				116		3820		3.86				117		4520		3.87

										116		4540		3.86				116		3820		3.86				117		4520		3.87

										116		4550		3.86				116		3820		3.86				117		4530		3.87

										116		4550		3.86				116		3820		3.87				117		4530		3.88

										116		4550		3.87				116		3830		3.87				117		4530		3.88

										116		4560		3.87				116		3830		3.87				117		4530		3.88

										117		4560		3.87				116		3830		3.87				117		4530		3.88

										117		4560		3.87				117		3830		3.88				117		4540		3.88

										117		4560		3.88				117		3830		3.88				117		4540		3.89

										117		4560		3.88				117		3830		3.88				117		4540		3.89

										117		4560		3.88				117		3830		3.88				117		4540		3.89

										117		4560		3.88				117		3840		3.88				117		4550		3.89

										117		4570		3.89				117		3840		3.89				117		4550		3.9

										117		4570		3.89				117		3840		3.89				117		4550		3.9

										117		4570		3.89				117		3840		3.89				118		4550		3.9

										117		4570		3.89				117		3840		3.89				118		4550		3.9

										117		4570		3.9				117		3840		3.9				118		4560		3.9

										117		4580		3.9				117		3840		3.9				118		4560		3.91

										117		4580		3.9				117		3840		3.9				118		4560		3.91

										117		4580		3.9				117		3850		3.9				118		4560		3.91

										118		4580		3.91				117		3850		3.9				118		4560		3.91

										118		4580		3.91				117		3850		3.91				118		4570		3.91

										118		4590		3.91				117		3850		3.91				118		4570		3.92

										118		4590		3.91				118		3850		3.91				118		4570		3.92

										118		4590		3.91				118		3850		3.91				118		4570		3.92

										118		4590		3.92				118		3850		3.91				118		4570		3.92

										118		4590		3.92				118		3860		3.92				118		4580		3.92

										118		4590		3.92				118		3860		3.92				118		4580		3.93

										118		4590		3.92				118		3860		3.92				118		4580		3.93

										118		4590		3.93				118		3860		3.92				118		4580		3.93

										118		4600		3.93				118		3860		3.93				119		4590		3.93

										118		4600		3.93				118		3860		3.93				119		4590		3.94

										118		4600		3.93				118		3870		3.93				119		4590		3.94

										118		4600		3.93				118		3870		3.93				119		4590		3.94

										118		4600		3.94				118		3870		3.93				119		4590		3.94

										118		4600		3.94				118		3870		3.94				119		4590		3.94

										119		4600		3.94				118		3870		3.94				119		4600		3.95

										119		4610		3.94				118		3870		3.94				119		4600		3.95

										119		4610		3.95				119		3870		3.94				119		4600		3.95

										119		4610		3.95				119		3870		3.95				119		4600		3.95

										119		4610		3.95				119		3870		3.95				119		4610		3.96

										119		4610		3.95				119		3870		3.95				119		4610		3.96

										119		4610		3.95				119		3880		3.95				119		4610		3.96

										119		4610		3.96				119		3880		3.96				119		4610		3.96

										119		4610		3.96				119		3880		3.96				119		4610		3.96

										119		4610		3.96				119		3880		3.96				120		4620		3.97

										119		4620		3.96				119		3880		3.96				120		4620		3.97

										119		4620		3.97				119		3880		3.96				120		4620		3.97

										119		4620		3.97				119		3880		3.97				120		4620		3.97

										119		4620		3.97				119		3890		3.97				120		4620		3.98

										120		4620		3.97				119		3890		3.97				120		4630		3.98

										120		4620		3.97				119		3890		3.97				120		4630		3.98

										120		4620		3.98				119		3890		3.98				120		4630		3.98

										120		4600		3.98				120		3890		3.98				120		4630		3.98

										120		4600		3.98				120		3890		3.98				120		4630		3.99

										120		4580		3.98				120		3890		3.98				120		4640		3.99

										120		4590		3.99				120		3900		3.98				120		4640		3.99

										120		4590		3.99				120		3900		3.99				120		4640		3.99

										120		4600		3.99				120		3900		3.99				120		4640		4

										120		4600		3.99				120		3900		3.99				120		4640		4

										120		4610		3.99				120		3900		3.99				121		4650		4

										120		4600		4				120		3900		4				121		4650		4

										120		4600		4				120		3900		4				121		4650		4.01

										120		4600		4				120		3890		4				121		4660		4.01

										120		4610		4				120		3890		4				121		4660		4.01

										121		4610		4.01				120		3890		4				121		4660		4.01

										121		4610		4.01				120		3900		4.01				121		4660		4.01

										121		4610		4.01				120		3900		4.01				121		4660		4.02

										121		4610		4.01				121		3900		4.01				121		4670		4.02

										121		4610		4.01				121		3900		4.01				121		4670		4.02

										121		4610		4.02				121		3900		4.01				121		4670		4.02

										121		4610		4.02				121		3900		4.02				121		4670		4.03

										121		4610		4.02				121		3910		4.02				121		4680		4.03

										121		4610		4.02				121		3910		4.02				121		4680		4.03

										121		4620		4.03				121		3910		4.02				121		4680		4.03

										121		4620		4.03				121		3910		4.03				122		4680		4.04

										121		4620		4.03				121		3910		4.03				122		4680		4.04

										121		4620		4.03				121		3920		4.03				122		4690		4.04

										121		4620		4.03				121		3920		4.03				122		4690		4.04

										122		4630		4.04				121		3920		4.03				122		4690		4.05

										122		4630		4.04				121		3920		4.04				122		4690		4.05

										122		4630		4.04				121		3920		4.04				122		4700		4.05

										122		4630		4.04				121		3920		4.04				122		4700		4.05

										122		4630		4.05				122		3920		4.04				122		4700		4.05

										122		4630		4.05				122		3930		4.05				122		4700		4.06

										122		4630		4.05				122		3930		4.05				122		4700		4.06

										122		4640		4.05				122		3930		4.05				122		4710		4.06

										122		4640		4.06				122		3930		4.05				122		4710		4.06

										122		4640		4.06				122		3930		4.06				122		4710		4.07

										122		4640		4.06				122		3930		4.06				123		4710		4.07

										122		4640		4.06				122		3930		4.06				123		4720		4.07

										122		4640		4.06				122		3930		4.06				123		4720		4.07

										122		4640		4.07				122		3930		4.06				123		4720		4.07

										122		4650		4.07				122		3940		4.07				123		4720		4.08

										122		4650		4.07				122		3940		4.07				123		4720		4.08

										123		4650		4.07				122		3940		4.07				123		4730		4.08

										123		4650		4.08				122		3940		4.07				123		4730		4.08

										123		4650		4.08				123		3940		4.08				123		4730		4.09

										123		4650		4.08				123		3940		4.08				123		4730		4.09

										123		4650		4.08				123		3940		4.08				123		4730		4.09

										123		4650		4.08				123		3940		4.08				123		4740		4.09

										123		4660		4.09				123		3950		4.08				123		4740		4.09

										123		4660		4.09				123		3950		4.09				123		4740		4.1

										123		4660		4.09				123		3950		4.09				123		4740		4.1

										123		4660		4.09				123		3950		4.09				124		4750		4.1

										123		4650		4.1				123		3950		4.09				124		4750		4.1

										123		4630		4.1				123		3950		4.1				124		4750		4.11

										123		4620		4.1				123		3950		4.1				124		4750		4.11

										123		4630		4.1				123		3960		4.1				124		4760		4.11

										123		4630		4.1				123		3960		4.1				124		4760		4.11

										124		4640		4.11				123		3960		4.1				124		4760		4.11

										124		4640		4.11				123		3960		4.11				124		4760		4.12

										124		4640		4.11				123		3960		4.11				124		4760		4.12

										124		4640		4.11				124		3960		4.11				124		4770		4.12

										124		4650		4.12				124		3960		4.11				124		4770		4.12

										124		4650		4.12				124		3960		4.12				124		4770		4.13

										124		4650		4.12				124		3960		4.12				124		4770		4.13

										124		4650		4.12				124		3960		4.12				124		4770		4.13

										124		4650		4.13				124		3970		4.12				124		4780		4.13

										124		4650		4.13				124		3970		4.12				125		4780		4.13

										124		4660		4.13				124		3970		4.13				125		4780		4.14

										124		4660		4.13				124		3970		4.13				125		4780		4.14

										124		4650		4.14				124		3970		4.13				125		4780		4.14

										124		4650		4.14				124		3970		4.13				125		4790		4.14

										125		4660		4.14				124		3970		4.14				125		4790		4.14

										125		4660		4.14				124		3970		4.14				125		4790		4.15

										125		4660		4.14				124		3970		4.14				125		4790		4.15

										125		4660		4.14				124		3970		4.14				125		4790		4.15

										125		4660		4.15				125		3970		4.14				125		4800		4.15

										125		4660		4.15				125		3980		4.14				125		4800		4.16

										125		4660		4.15				125		3980		4.15				125		4800		4.16

										125		4670		4.16				125		3980		4.15				125		4810		4.16

										125		4670		4.16				125		3980		4.15				125		4810		4.16

										125		4670		4.16				125		3980		4.16				125		4810		4.16

										125		4670		4.16				125		3980		4.16				126		4810		4.17

										125		4670		4.16				125		3980		4.16				126		4810		4.17

										125		4670		4.16				125		3980		4.16				126		4810		4.17

										125		4670		4.17				125		3980		4.16				126		4820		4.17

										125		4670		4.17				125		3980		4.16				126		4820		4.18

										126		4680		4.17				125		3980		4.17				126		4820		4.18

										126		4680		4.17				125		3980		4.17				126		4820		4.18

										126		4680		4.18				125		3980		4.17				126		4830		4.18

										126		4680		4.18				126		3990		4.18				126		4830		4.18

										126		4680		4.18				126		3990		4.18				126		4830		4.19

										126		4680		4.18				126		3990		4.18				126		4830		4.19

										126		4680		4.19				126		3990		4.18				126		4830		4.19

										126		4680		4.19				126		3990		4.18				126		4840		4.2

										126		4680		4.19				126		3990		4.19				126		4840		4.2

										126		4690		4.19				126		3990		4.19				126		4840		4.2

										126		4690		4.2				126		3990		4.19				127		4840		4.2

										126		4690		4.2				126		3990		4.19				127		4840		4.2

										126		4690		4.2				126		3990		4.19				127		4840		4.21

										126		4690		4.2				126		3990		4.2				127		4850		4.21

										126		4690		4.2				126		3990		4.2				127		4850		4.21

										127		4690		4.21				126		3990		4.2				127		4850		4.21

										127		4700		4.21				126		3990		4.2				127		4850		4.22

										127		4700		4.21				126		3990		4.21				127		4860		4.22

										127		4700		4.21				127		3990		4.21				127		4860		4.22

										127		4700		4.22				127		4000		4.21				127		4860		4.22

										127		4700		4.22				127		4000		4.21				127		4860		4.22

										127		4700		4.22				127		4000		4.22				127		4860		4.23

										127		4700		4.22				127		3990		4.22				127		4870		4.23

										127		4710		4.22				127		4000		4.22				127		4870		4.23

										127		4710		4.23				127		4000		4.22				128		4870		4.23

										127		4700		4.23				127		4000		4.22				128		4870		4.24

										127		4700		4.23				127		4000		4.23				128		4880		4.24

										127		4700		4.23				127		4000		4.23				128		4880		4.24

										127		4710		4.24				127		4000		4.23				128		4880		4.24

										127		4700		4.24				127		4000		4.23				128		4870		4.24

										128		4700		4.24				127		4000		4.24				128		4830		4.25

										128		4700		4.24				127		4000		4.24				128		4820		4.25

										128		4700		4.24				127		4010		4.24				128		4780		4.25

										128		4700		4.25				128		4010		4.24				128		4670		4.25

										128		4710		4.25				128		4010		4.25				128		4670		4.26

										128		4710		4.25				128		4010		4.25				128		4680		4.26

										128		4710		4.25				128		4010		4.25				128		4680		4.26

										128		4710		4.26				128		4010		4.25				128		4690		4.26

										128		4720		4.26				128		4010		4.25				128		4690		4.26

										128		4720		4.26				128		4010		4.26				129		4690		4.27

										128		4720		4.26				128		4020		4.26				129		4670		4.27

										128		4700		4.26				128		4020		4.26				129		4620		4.27

										128		4670		4.27				128		4020		4.26				129		4530		4.27

										129		-366		4.27				128		4020		4.27				129		4530		4.28

										129		-369		4.27				128		4020		4.27				129		4530		4.28

																		128		4020		4.27				129		4530		4.28

																		128		4020		4.27				129		4540		4.28

																		129		4020		4.27				129		4540		4.28

																		129		4020		4.28				129		4540		4.29

																		129		4020		4.28				129		4550		4.29

																		129		4030		4.28				129		4550		4.29

																		129		4030		4.28				129		4550		4.29

																		129		4010		4.29				129		4560		4.3

																		129		4010		4.29				129		4560		4.3

																		129		4010		4.29				130		4570		4.3

																		129		4020		4.29				130		4570		4.3

																		129		4020		4.29				130		4570		4.3

																		129		4020		4.3				130		4580		4.31

																		129		4020		4.3				130		4570		4.31

																		129		4020		4.3				130		4560		4.31

																		129		4030		4.3				130		4560		4.31

																		129		4030		4.31				130		4560		4.32

																		130		4030		4.31				130		4250		4.32

																		130		4030		4.31				130		-263		4.32

																		130		4030		4.31				130		-302		4.32

																		130		4030		4.32

																		130		4030		4.32

																		130		4030		4.32

																		130		4030		4.32

																		130		4030		4.32

																		130		4030		4.33

																		130		4030		4.33

																		130		4040		4.33

																		130		4040		4.33

																		130		4040		4.34

																		130		4040		4.34

																		130		4040		4.34

																		131		4040		4.34

																		131		4040		4.35

																		131		4040		4.35

																		131		4050		4.35

																		131		4050		4.35

																		131		4050		4.35

																		131		4050		4.36

																		131		4050		4.36

																		131		4050		4.36

																		131		4050		4.36

																		131		4050		4.37

																		131		4050		4.37

																		131		4060		4.37

																		131		4060		4.37

																		131		4060		4.37

																		132		4060		4.38

																		132		4060		4.38

																		132		4060		4.38

																		132		4060		4.38

																		132		4070		4.39

																		132		4070		4.39

																		132		4070		4.39

																		132		4070		4.39

																		132		4070		4.39

																		132		4070		4.4

																		132		4070		4.4

																		132		4080		4.4

																		132		4080		4.4

																		132		4080		4.41

																		133		4080		4.41

																		133		4080		4.41

																		133		4080		4.41

																		133		4080		4.42

																		133		4080		4.42

																		133		4080		4.42

																		133		4090		4.42

																		133		4090		4.42

																		133		4090		4.43

																		133		4090		4.43

																		133		4090		4.43

																		133		4090		4.43

																		133		4090		4.43

																		133		4090		4.44

																		133		4090		4.44

																		134		4100		4.44

																		134		4100		4.44

																		134		4100		4.45

																		134		4100		4.45

																		134		4100		4.45

																		134		4100		4.45

																		134		4100		4.45

																		134		4100		4.46

																		134		4110		4.46

																		134		4110		4.46

																		134		4110		4.47

																		134		4110		4.47

																		134		4110		4.47

																		134		4110		4.47

																		134		4110		4.47

																		135		4110		4.48

																		135		4110		4.48

																		135		4120		4.48

																		135		4120		4.48

																		135		4120		4.49

																		135		4120		4.49

																		135		4120		4.49

																		135		4120		4.49

																		135		4120		4.5

																		135		4120		4.5

																		135		4130		4.5

																		135		4130		4.5

																		135		4130		4.5

																		135		4130		4.51

																		135		4130		4.51

																		136		4130		4.51

																		136		4130		4.51

																		136		4130		4.52

																		136		4130		4.52

																		136		4130		4.52

																		136		4130		4.52

																		136		4130		4.52

																		136		4130		4.53

																		136		4140		4.53

																		136		4140		4.53

																		136		4140		4.53

																		136		4140		4.54

																		136		4140		4.54

																		136		4140		4.54

																		136		4140		4.54

																		137		4140		4.54

																		137		4140		4.55

																		137		4150		4.55

																		137		4150		4.55

																		137		4150		4.55

																		137		4150		4.56

																		137		4150		4.56

																		137		4150		4.56

																		137		4150		4.56

																		137		4150		4.56

																		137		4150		4.57

																		137		4150		4.57

																		137		4150		4.57

																		137		4150		4.58

																		138		4160		4.58

																		138		4160		4.58

																		138		4160		4.58

																		138		4160		4.58

																		138		4160		4.59

																		138		4160		4.59

																		138		4160		4.59

																		138		4160		4.59

																		138		4160		4.59

																		138		4170		4.6

																		138		4170		4.6

																		138		4170		4.6

																		138		4170		4.6

																		138		4170		4.6

																		138		4170		4.61

																		139		4170		4.61

																		139		4170		4.61

																		139		4170		4.61

																		139		4170		4.62

																		139		4170		4.62

																		139		4170		4.62

																		139		4170		4.62

																		139		4170		4.62

																		139		4180		4.63

																		139		4180		4.63

																		139		4180		4.63

																		139		4180		4.63

																		139		4180		4.64

																		139		4180		4.64

																		139		4180		4.64

																		139		4180		4.64

																		140		4180		4.64

																		140		4190		4.65

																		140		4190		4.65

																		140		4190		4.65

																		140		4190		4.65

																		140		4190		4.66

																		140		4190		4.66

																		140		4190		4.66

																		140		4190		4.66

																		140		4190		4.66

																		140		4200		4.67

																		140		4200		4.67

																		140		4200		4.67

																		140		4200		4.67

																		141		4200		4.68

																		141		4200		4.68

																		141		4200		4.68

																		141		4200		4.68

																		141		4200		4.68

																		141		4210		4.69

																		141		4210		4.69

																		141		4210		4.69

																		141		4210		4.69

																		141		4210		4.7

																		141		4210		4.7

																		141		4210		4.7

																		141		4210		4.7

																		141		4210		4.7

																		142		4210		4.71

																		142		4210		4.71

																		142		4210		4.71

																		142		4220		4.71

																		142		4220		4.72

																		142		4220		4.72

																		142		4220		4.72

																		142		4220		4.72

																		142		4220		4.73

																		142		4220		4.73

																		142		4220		4.73

																		142		4220		4.73

																		142		4220		4.73

																		142		4220		4.74

																		142		4220		4.74

																		142		4220		4.74

																		143		4220		4.74

																		143		4220		4.74

																		143		4220		4.75

																		143		4220		4.75

																		143		4220		4.75

																		143		4220		4.75

																		143		4220		4.76

																		143		4220		4.76

																		143		4220		4.76

																		143		4220		4.76

																		143		4220		4.77

																		143		4220		4.77

																		143		4220		4.77

																		143		4220		4.77

																		143		4220		4.77

																		144		4220		4.78

																		144		4220		4.78

																		144		4220		4.78

																		144		4220		4.78

																		144		4220		4.79

																		144		4220		4.79

																		144		4220		4.79

																		144		4220		4.79

																		144		4220		4.79

																		144		4090		4.8

																		144		-128		4.8





PETG 3mm PLA 10 proc

		Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)

		0.143		-2.5		0				0.242		-5.83		0				0.251		-5.83		0				0.265		-8.33		0				0.184		-8.33		0				0.256		-8.33		0				0.194		-5.83		0

		0.293		-2.5		0				0.369		-2.5		0.001				0.378		-2.5		0.001				0.359		-6.67		0.001				0.308		-8.33		0				0.381		-4.17		0.001				0.319		-1.67		0.001

		0.418		0.833		0.001				0.432		11.7		0.003				0.411		12.5		0.003				0.421		8.33		0.003				0.402		-8.33		0				0.443		12.5		0.003				0.382		17.5		0.003

		0.48		15.8		0.003				0.495		29.2		0.005				0.504		31.7		0.005				0.513		27.5		0.005				0.496		0.833		0.002				0.505		34.2		0.005				0.445		41.7		0.005

		0.542		35		0.005				0.558		47.5		0.007				0.598		60		0.008				0.608		65.8		0.009				0.527		18.3		0.004				0.63		76.7		0.009				0.508		67.5		0.007

		0.636		65		0.008				0.622		75.8		0.011				0.661		78.3		0.01				0.7		84.2		0.011				0.682		56.7		0.008				0.693		97.5		0.011				0.634		115		0.012

		0.699		84.2		0.01				0.715		92.5		0.013				0.724		94.2		0.013				0.763		103		0.013				0.748		74.2		0.01				0.756		118		0.013				0.643		138		0.014

		0.762		102		0.012				0.781		109		0.015				0.787		109		0.015				0.826		120		0.016				0.811		92.5		0.013				0.788		138		0.016				0.766		162		0.016

		0.825		118		0.014				0.844		126		0.017				0.82		123		0.017				0.864		138		0.018				0.873		109		0.015				0.88		158		0.018				0.829		184		0.018

		0.889		134		0.017				0.877		141		0.019				0.883		130		0.019				0.956		155		0.02				0.936		125		0.017				0.943		176		0.02				0.862		205		0.02

		0.951		148		0.019				0.94		153		0.021				0.976		136		0.021				0.989		170		0.022				1.01		139		0.019				1.01		193		0.022				0.954		225		0.022

		0.993		161		0.021				1.03		164		0.023				1.04		143		0.023				1.07		188		0.025				1.04		153		0.021				1.04		211		0.024				1.02		244		0.024

		1.09		171		0.024				1.1		174		0.025				1.13		154		0.027				1.13		202		0.027				1.1		163		0.023				1.19		243		0.028				1.14		281		0.029

		1.15		181		0.027				1.19		187		0.029				1.2		161		0.029				1.25		228		0.031				1.26		184		0.028				1.23		260		0.031				1.21		295		0.031

		1.21		188		0.029				1.25		194		0.031				1.26		168		0.031				1.32		240		0.033				1.32		194		0.03				1.32		276		0.033				1.27		309		0.033

		1.3		195		0.031				1.32		203		0.033				1.32		176		0.033				1.41		251		0.035				1.35		204		0.032				1.35		292		0.035				1.3		326		0.035

		1.34		202		0.033				1.38		210		0.035				1.33		183		0.035				1.47		263		0.037				1.41		213		0.034				1.45		307		0.037				1.4		342		0.037

		1.41		210		0.035				1.44		219		0.037				1.45		190		0.037				1.53		274		0.039				1.51		220		0.036				1.51		320		0.039				1.46		358		0.039

		1.47		217		0.037				1.51		227		0.039				1.52		197		0.04				1.56		286		0.041				1.57		226		0.038				1.57		333		0.041				1.49		373		0.041

		1.56		223		0.04				1.57		234		0.041				1.58		203		0.042				1.66		298		0.044				1.6		232		0.04				1.64		345		0.043				1.55		387		0.043

		1.6		230		0.042				1.63		243		0.044				1.71		215		0.046				1.69		309		0.046				1.67		238		0.042				1.76		370		0.047				1.69		409		0.047

		1.69		242		0.045				1.76		257		0.048				1.77		221		0.048				1.78		324		0.049				1.79		249		0.047				1.82		382		0.049				1.75		421		0.049

		1.75		248		0.047				1.82		263		0.05				1.83		226		0.05				1.85		335		0.051				1.85		255		0.049				1.83		393		0.051				1.81		433		0.051

		1.81		255		0.049				1.86		269		0.052				1.87		231		0.052				1.91		344		0.053				1.92		260		0.051				1.95		404		0.054				1.87		445		0.053

		1.88		263		0.051				1.95		276		0.054				1.96		236		0.054				1.97		353		0.055				2.01		265		0.053				2.02		413		0.056				1.94		458		0.055

		1.97		268		0.053				2.01		282		0.056				2.02		241		0.056				2.03		362		0.057				2.07		270		0.055				2.08		423		0.058				2		468		0.057

		2.03		275		0.055				2.07		288		0.058				2.08		245		0.058				2.13		370		0.059				2.1		275		0.057				2.14		433		0.06				2.06		480		0.06

		2.09		282		0.057				2.14		294		0.06				2.19		254		0.063				2.16		378		0.061				2.2		280		0.059				2.27		453		0.064				2.13		491		0.062

		2.16		288		0.06				2.26		307		0.065				2.28		258		0.065				2.22		388		0.063				2.26		285		0.061				2.33		462		0.066				2.22		507		0.065

		2.25		297		0.063				2.33		313		0.067				2.34		263		0.067				2.28		397		0.066				2.35		292		0.064				2.39		471		0.068				2.28		519		0.067

		2.31		303		0.065				2.39		318		0.069				2.38		266		0.069				2.44		414		0.07				2.42		296		0.067				2.46		479		0.071				2.35		529		0.069

		2.38		308		0.067				2.45		324		0.071				2.44		269		0.071				2.47		423		0.072				2.48		301		0.069				2.52		488		0.073				2.41		539		0.071

		2.41		313		0.069				2.52		329		0.073				2.53		273		0.073				2.53		431		0.074				2.54		305		0.071				2.58		497		0.075				2.47		550		0.073

		2.47		318		0.071				2.58		335		0.075				2.6		277		0.075				2.59		438		0.076				2.6		308		0.073				2.62		505		0.077				2.54		560		0.075

		2.53		323		0.073				2.61		341		0.077				2.69		282		0.079				2.69		447		0.078				2.63		313		0.075				2.71		513		0.079				2.6		570		0.078

		2.62		328		0.075				2.71		345		0.079				2.75		286		0.081				2.75		454		0.08				2.7		316		0.077				2.84		530		0.083				2.66		581		0.079

		2.69		333		0.077				2.83		355		0.083				2.82		289		0.083				2.78		462		0.082				2.79		319		0.079				2.9		538		0.085				2.79		600		0.084

		2.78		339		0.08				2.9		359		0.086				2.88		293		0.085				2.88		469		0.084				2.85		324		0.082				2.96		546		0.088				2.85		609		0.086

		2.81		343		0.082				2.93		363		0.088				2.94		297		0.087				2.94		479		0.087				2.92		327		0.084				3.02		553		0.09				2.91		619		0.088

		2.91		348		0.084				3.02		368		0.09				3.01		301		0.089				3		486		0.089				2.98		331		0.086				3.09		561		0.092				2.98		628		0.09

		2.97		352		0.086				3.08		372		0.092				3.07		305		0.091				3.06		493		0.091				3.04		333		0.088				3.15		568		0.094				3.04		638		0.092

		3.03		355		0.088				3.15		375		0.094				3.13		309		0.093				3.16		499		0.094				3.13		336		0.09				3.21		574		0.096				3.1		646		0.094

		3.06		359		0.091				3.21		379		0.096				3.26		316		0.097				3.19		506		0.096				3.2		339		0.092				3.28		581		0.098				3.17		654		0.096

		3.16		363		0.093				3.34		387		0.1				3.32		320		0.1				3.28		512		0.098				3.23		343		0.095				3.4		593		0.102				3.29		671		0.101

		3.19		366		0.095				3.4		390		0.103				3.35		323		0.102				3.34		518		0.1				3.32		345		0.097				3.47		598		0.104				3.36		679		0.103

		3.28		370		0.097				3.46		394		0.105				3.45		328		0.104				3.37		523		0.102				3.45		351		0.101				3.53		603		0.106				3.42		687		0.105

		3.34		373		0.099				3.52		397		0.107				3.51		331		0.106				3.44		529		0.104				3.51		353		0.103				3.59		609		0.108				3.48		694		0.107

		3.37		377		0.101				3.59		401		0.109				3.57		334		0.108				3.59		539		0.108				3.54		357		0.105				3.66		614		0.111				3.54		701		0.109

		3.47		380		0.103				3.65		405		0.111				3.64		338		0.11				3.65		544		0.11				3.63		360		0.107				3.72		619		0.113				3.61		708		0.111

		3.53		383		0.105				3.71		408		0.113				3.7		341		0.112				3.72		548		0.112				3.66		363		0.109				3.78		624		0.115				3.67		717		0.113

		3.59		387		0.107				3.77		413		0.115				3.83		348		0.116				3.75		553		0.114				3.73		366		0.111				3.91		634		0.119				3.73		723		0.115

		3.62		389		0.109				3.9		420		0.119				3.89		353		0.119				3.84		557		0.117				3.82		369		0.113				3.97		639		0.121				3.86		736		0.119

		3.69		393		0.112				3.93		423		0.121				3.95		357		0.121				3.9		562		0.119				3.85		372		0.115				4.03		644		0.123				3.89		742		0.121

		3.75		396		0.114				3.99		428		0.123				4.02		360		0.123				3.94		566		0.121				3.91		375		0.118				4.1		649		0.125				3.96		748		0.124

		3.81		399		0.116				4.09		432		0.125				4.08		364		0.125				4.03		570		0.123				4.01		380		0.121				4.16		655		0.128				4.05		754		0.126

		3.94		405		0.12				4.15		435		0.127				4.14		368		0.127				4.09		575		0.126				4.07		383		0.123				4.22		660		0.13				4.11		761		0.128

		4		408		0.122				4.21		438		0.129				4.21		373		0.129				4.15		580		0.128				4.13		386		0.125				4.29		664		0.131				4.15		767		0.13

		4.06		412		0.124				4.27		442		0.132				4.33		380		0.133				4.22		584		0.13				4.23		388		0.127				4.41		675		0.136				4.24		773		0.132

		4.12		415		0.126				4.34		446		0.134				4.4		383		0.135				4.28		588		0.132				4.29		392		0.129				4.45		680		0.138				4.3		778		0.134

		4.18		418		0.128				4.46		453		0.138				4.46		388		0.137				4.34		593		0.134				4.32		395		0.131				4.54		686		0.14				4.4		786		0.137

		4.25		421		0.13				4.52		458		0.14				4.52		392		0.14				4.4		597		0.136				4.38		398		0.133				4.6		691		0.142				4.46		792		0.139

		4.34		424		0.132				4.58		461		0.142				4.59		396		0.142				4.5		600		0.138				4.44		401		0.135				4.67		696		0.144				4.52		798		0.142

		4.37		428		0.134				4.65		464		0.144				4.65		400		0.144				4.53		605		0.14				4.54		405		0.137				4.73		701		0.146				4.58		803		0.144

		4.53		434		0.138				4.71		468		0.146				4.68		403		0.146				4.59		609		0.142				4.63		409		0.14				4.76		706		0.148				4.65		808		0.146

		4.56		437		0.141				4.77		472		0.148				4.77		407		0.148				4.72		616		0.146				4.66		413		0.142				4.86		712		0.151				4.71		813		0.148

		4.62		441		0.143				4.83		475		0.15				4.9		414		0.152				4.78		620		0.148				4.76		415		0.144				4.98		722		0.155				4.77		818		0.15

		4.72		444		0.145				4.9		479		0.152				4.96		418		0.154				4.84		623		0.15				4.79		419		0.147				5.05		727		0.157				4.84		823		0.152

		4.75		448		0.147				4.96		483		0.155				5.03		422		0.157				4.87		628		0.152				4.85		422		0.149				5.11		732		0.159				4.96		834		0.156

		4.84		451		0.149				5.08		490		0.159				5.09		426		0.159				4.97		632		0.154				4.91		425		0.151				5.17		738		0.161				5.03		839		0.158

		4.87		454		0.151				5.14		493		0.161				5.15		428		0.161				5		636		0.156				4.97		428		0.153				5.23		743		0.163				5.09		844		0.16

		4.96		458		0.153				5.18		497		0.163				5.22		432		0.163				5.06		640		0.158				5.07		431		0.155				5.3		748		0.165				5.15		849		0.162

		5.06		463		0.156				5.27		500		0.165				5.28		435		0.165				5.12		645		0.16				5.16		438		0.159				5.33		753		0.167				5.19		855		0.165

		5.12		467		0.158				5.33		504		0.167				5.41		443		0.169				5.18		648		0.162				5.26		441		0.161				5.39		758		0.17				5.28		860		0.167

		5.15		470		0.16				5.39		507		0.169				5.47		446		0.171				5.31		657		0.167				5.32		444		0.163				5.55		768		0.174				5.34		866		0.169

		5.25		474		0.162				5.45		510		0.171				5.53		449		0.173				5.4		661		0.169				5.38		447		0.166				5.61		773		0.176				5.4		871		0.171

		5.28		478		0.164				5.52		513		0.173				5.6		453		0.176				5.43		664		0.171				5.45		450		0.168				5.68		778		0.178				5.53		880		0.175

		5.37		480		0.166				5.64		520		0.177				5.66		456		0.178				5.53		669		0.173				5.48		453		0.169				5.74		783		0.18				5.59		885		0.177

		5.43		484		0.169				5.71		523		0.179				5.72		459		0.179				5.59		673		0.175				5.54		457		0.172				5.8		788		0.182				5.66		890		0.179

		5.5		488		0.171				5.77		527		0.181				5.79		463		0.182				5.62		677		0.177				5.63		459		0.174				5.86		793		0.184				5.69		895		0.181

		5.59		493		0.174				5.83		529		0.184				5.85		467		0.184				5.68		681		0.179				5.76		466		0.178				5.93		798		0.186				5.79		900		0.184

		5.65		498		0.176				5.89		533		0.186				5.98		473		0.188				5.75		684		0.181				5.77		468		0.18				5.99		803		0.188				5.86		904		0.186

		5.68		501		0.178				5.95		537		0.188				6.04		477		0.19				5.9		693		0.185				5.85		472		0.182				6.12		813		0.193				5.89		908		0.188

		5.74		503		0.18				6.02		539		0.19				6.1		481		0.192				5.96		697		0.187				5.91		475		0.184				6.18		817		0.195				5.95		913		0.19

		5.84		507		0.182				6.08		543		0.192				6.17		484		0.194				6.03		700		0.189				6.01		479		0.186				6.24		821		0.197				6.07		923		0.194

		5.9		511		0.184				6.2		549		0.196				6.23		488		0.197				6.09		704		0.191				6.04		483		0.188				6.31		826		0.199				6.17		926		0.197

		5.96		514		0.186				6.26		553		0.198				6.26		491		0.199				6.12		708		0.193				6.13		485		0.19				6.37		830		0.201				6.23		931		0.199

		5.99		518		0.188				6.33		556		0.2				6.35		495		0.201				6.21		712		0.196				6.19		488		0.192				6.43		835		0.203				6.26		935		0.201

		6.09		522		0.191				6.36		560		0.202				6.42		498		0.203				6.28		716		0.198				6.26		492		0.195				6.5		840		0.205				6.32		939		0.203

		6.18		528		0.194				6.45		563		0.204				6.54		506		0.207				6.34		719		0.2				6.35		497		0.198				6.56		844		0.207				6.39		943		0.205

		6.21		531		0.196				6.51		567		0.206				6.61		510		0.209				6.43		725		0.203				6.38		500		0.2				6.69		853		0.212				6.48		948		0.207

		6.28		534		0.198				6.57		570		0.208				6.67		513		0.211				6.46		728		0.205				6.48		503		0.202				6.75		858		0.214				6.54		952		0.209

		6.37		538		0.2				6.64		573		0.21				6.73		517		0.213				6.56		733		0.207				6.51		507		0.204				6.81		863		0.216				6.64		958		0.212

		6.43		542		0.202				6.76		580		0.215				6.79		520		0.215				6.62		736		0.209				6.57		509		0.206				6.88		867		0.218				6.67		963		0.214

		6.49		545		0.204				6.82		583		0.217				6.86		524		0.217				6.65		739		0.211				6.66		513		0.208				6.94		871		0.22				6.76		967		0.216

		6.56		548		0.206				6.89		587		0.219				6.92		528		0.22				6.71		743		0.213				6.69		516		0.21				7		876		0.222				6.82		971		0.218

		6.62		553		0.208				6.95		590		0.221				6.98		531		0.221				6.81		747		0.215				6.79		520		0.212				7.07		880		0.224				6.89		975		0.22

		6.68		558		0.211				7.01		593		0.223				7.11		538		0.226				6.87		750		0.217				6.91		526		0.217				7.19		889		0.228				6.95		979		0.222

		6.77		562		0.213				7.07		597		0.225				7.17		542		0.228				6.93		756		0.22				6.94		529		0.219				7.26		894		0.23				7.01		983		0.224

		6.84		565		0.215				7.13		600		0.227				7.23		546		0.23				7.02		759		0.223				7.04		533		0.22				7.29		898		0.233				7.07		988		0.227

		6.9		568		0.217				7.2		604		0.229				7.29		549		0.232				7.06		763		0.225				7.07		537		0.223				7.38		902		0.235				7.17		994		0.23

		6.93		572		0.22				7.32		610		0.233				7.36		553		0.234				7.15		767		0.227				7.13		540		0.225				7.44		907		0.237				7.2		999		0.232

		6.99		576		0.222				7.38		614		0.235				7.42		557		0.236				7.21		770		0.229				7.22		543		0.227				7.51		911		0.239				7.29		1000		0.234

		7.06		580		0.224				7.45		618		0.238				7.48		560		0.238				7.27		773		0.231				7.29		547		0.229				7.57		915		0.241				7.32		1010		0.236

		7.12		583		0.226				7.51		620		0.24				7.54		563		0.24				7.34		778		0.233				7.32		551		0.231				7.63		920		0.243				7.38		1010		0.238

		7.21		587		0.228				7.57		623		0.242				7.67		571		0.245				7.4		781		0.235				7.38		555		0.233				7.73		926		0.246				7.48		1020		0.24

		7.27		593		0.231				7.63		628		0.244				7.73		575		0.247				7.49		788		0.239				7.54		563		0.237				7.79		930		0.248				7.51		1020		0.242

		7.34		596		0.233				7.69		630		0.245				7.79		579		0.248				7.59		792		0.241				7.57		567		0.239				7.85		935		0.251				7.6		1020		0.244

		7.43		600		0.235				7.76		633		0.248				7.82		583		0.251				7.65		795		0.243				7.63		571		0.241				7.92		939		0.253				7.73		1030		0.248

		7.49		604		0.237				7.88		641		0.252				7.92		587		0.253				7.71		798		0.246				7.72		575		0.243				7.98		944		0.255				7.76		1040		0.25

		7.52		608		0.239				7.94		644		0.254				7.98		592		0.255				7.77		803		0.248				7.75		581		0.246				8.04		948		0.257				7.82		1040		0.252

		7.62		612		0.241				8		648		0.256				8.04		598		0.257				7.8		807		0.25				7.82		586		0.247				8.11		953		0.259				7.91		1050		0.255

		7.65		616		0.243				8.07		651		0.258				8.1		604		0.259				7.87		809		0.252				7.91		592		0.249				8.17		957		0.261				7.95		1050		0.257

		7.71		620		0.245				8.1		654		0.26				8.16		613		0.261				7.96		813		0.254				7.94		598		0.252				8.3		966		0.265				8.04		1050		0.259

		7.77		625		0.248				8.19		658		0.262				8.29		632		0.265				8.02		818		0.257				8.1		610		0.256				8.36		970		0.268				8.1		1060		0.261

		7.87		635		0.251				8.25		661		0.264				8.35		642		0.267				8.12		823		0.259				8.13		617		0.258				8.42		974		0.27				8.13		1060		0.263

		7.93		643		0.253				8.32		664		0.266				8.41		653		0.269				8.15		827		0.261				8.19		624		0.26				8.49		978		0.271				8.2		1070		0.265

		7.99		653		0.255				8.44		671		0.27				8.48		663		0.271				8.21		830		0.263				8.25		632		0.262				8.55		983		0.274				8.32		1070		0.269

		8.05		664		0.257				8.5		674		0.273				8.54		673		0.273				8.27		833		0.265				8.32		641		0.264				8.61		987		0.276				8.38		1080		0.271

		8.15		675		0.259				8.57		678		0.275				8.6		683		0.276				8.33		838		0.267				8.41		650		0.266				8.68		991		0.278				8.48		1080		0.273

		8.18		685		0.261				8.63		681		0.277				8.66		693		0.278				8.43		841		0.269				8.47		658		0.268				8.71		996		0.28				8.54		1090		0.276

		8.24		696		0.263				8.69		684		0.279				8.72		704		0.28				8.49		844		0.271				8.53		668		0.27				8.8		1000		0.282				8.57		1090		0.278

		8.3		707		0.265				8.73		688		0.281				8.85		725		0.284				8.58		853		0.276				8.6		681		0.274				8.93		1010		0.286				8.63		1090		0.28

		8.4		717		0.267				8.82		692		0.283				8.91		735		0.286				8.65		856		0.278				8.66		690		0.276				8.96		1010		0.288				8.69		1100		0.282

		8.43		728		0.27				8.88		695		0.285				8.97		744		0.288				8.74		859		0.28				8.72		698		0.278				9.05		1020		0.291				8.76		1100		0.284

		8.52		738		0.271				9		704		0.289				9.03		754		0.29				8.77		863		0.282				8.82		707		0.28				9.12		1020		0.293				8.91		1110		0.288

		8.58		748		0.273				9.07		708		0.291				9.1		764		0.292				8.87		867		0.284				8.85		714		0.282				9.18		1030		0.295				8.98		1110		0.29

		8.62		758		0.276				9.13		713		0.293				9.16		773		0.294				8.93		871		0.286				8.94		723		0.284				9.24		1030		0.297				9.01		1120		0.292

		8.71		769		0.278				9.19		719		0.296				9.22		783		0.296				8.96		875		0.288				8.97		729		0.286				9.31		1030		0.299				9.07		1120		0.294

		8.77		778		0.28				9.22		727		0.298				9.28		793		0.299				9.05		878		0.29				9.03		736		0.288				9.4		1040		0.302				9.13		1130		0.296

		8.8		788		0.282				9.32		736		0.3				9.41		810		0.302				9.11		883		0.292				9.1		742		0.29				9.46		1040		0.304				9.19		1130		0.298

		8.86		798		0.284				9.38		744		0.302				9.47		819		0.304				9.21		889		0.295				9.22		753		0.295				9.53		1050		0.306				9.26		1130		0.3

		8.96		808		0.286				9.44		753		0.304				9.53		828		0.307				9.27		893		0.298				9.31		758		0.297				9.59		1050		0.309				9.35		1140		0.302

		9.05		823		0.289				9.51		763		0.306				9.59		837		0.309				9.33		898		0.3				9.38		763		0.299				9.65		1060		0.311				9.47		1150		0.307

		9.11		832		0.291				9.63		779		0.31				9.66		845		0.311				9.36		902		0.302				9.44		768		0.3				9.72		1060		0.312				9.54		1150		0.309

		9.15		841		0.293				9.69		787		0.312				9.69		853		0.313				9.43		906		0.304				9.47		775		0.303				9.78		1060		0.315				9.57		1150		0.311

		9.24		851		0.295				9.76		794		0.314				9.78		861		0.315				9.52		912		0.306				9.53		781		0.305				9.85		1070		0.317				9.66		1160		0.313

		9.27		860		0.298				9.82		801		0.317				9.84		869		0.317				9.55		919		0.308				9.6		786		0.307				9.97		1080		0.321				9.72		1160		0.315

		9.36		869		0.3				9.88		807		0.319				9.9		877		0.319				9.61		927		0.31				9.7		793		0.309				10		1080		0.323				9.79		1160		0.317

		9.43		878		0.302				9.95		812		0.321				10		893		0.323				9.68		936		0.312				9.82		804		0.313				10.1		1080		0.325				9.85		1170		0.319

		9.49		888		0.304				9.98		816		0.323				10.1		900		0.325				9.83		953		0.316				9.89		811		0.315				10.2		1090		0.327				9.92		1170		0.321

		9.55		896		0.306				10		822		0.325				10.2		908		0.327				9.89		963		0.318				9.95		817		0.318				10.2		1090		0.33				10		1180		0.326

		9.61		904		0.308				10.1		826		0.327				10.2		915		0.329				9.93		972		0.32				9.98		822		0.32				10.3		1100		0.332				10.1		1180		0.328

		9.68		913		0.31				10.2		834		0.33				10.3		923		0.331				10		981		0.322				10		828		0.322				10.4		1100		0.334				10.2		1190		0.33

		9.74		922		0.312				10.3		840		0.332				10.3		929		0.333				10.1		989		0.324				10.1		834		0.324				10.4		1100		0.336				10.2		1190		0.332

		9.77		930		0.314				10.3		845		0.334				10.4		937		0.335				10.1		998		0.327				10.2		840		0.326				10.5		1110		0.339				10.3		1190		0.334

		9.86		939		0.316				10.4		851		0.336				10.5		943		0.338				10.2		1010		0.329				10.2		846		0.328				10.6		1120		0.341				10.3		1200		0.336

		9.89		947		0.318				10.5		857		0.339				10.6		956		0.342				10.3		1010		0.331				10.3		852		0.33				10.6		1120		0.343				10.4		1200		0.338

		9.99		955		0.321				10.5		863		0.341				10.7		963		0.344				10.3		1020		0.333				10.4		862		0.334				10.7		1120		0.345				10.5		1200		0.34

		10.1		963		0.323				10.6		869		0.343				10.7		968		0.346				10.5		1040		0.337				10.5		868		0.336				10.8		1130		0.347				10.5		1210		0.343

		10.1		975		0.326				10.6		875		0.345				10.8		974		0.348				10.5		1040		0.339				10.5		873		0.339				10.8		1130		0.35				10.6		1210		0.346

		10.2		983		0.328				10.7		881		0.347				10.8		979		0.35				10.6		1050		0.341				10.6		878		0.341				10.9		1140		0.352				10.7		1220		0.348

		10.2		991		0.33				10.8		890		0.35				10.9		984		0.352				10.6		1060		0.343				10.7		884		0.343				10.9		1140		0.354				10.7		1220		0.35

		10.3		998		0.332				10.9		896		0.352				11		990		0.354				10.7		1070		0.345				10.7		889		0.344				11.1		1150		0.358				10.8		1220		0.352

		10.4		1010		0.334				10.9		902		0.354				11		996		0.356				10.7		1070		0.348				10.8		894		0.347				11.1		1160		0.36				10.9		1230		0.354

		10.5		1010		0.336				11		908		0.356				11.1		1000		0.36				10.8		1080		0.35				10.9		900		0.349				11.2		1160		0.362				10.9		1230		0.356

		10.5		1020		0.338				11.1		913		0.359				11.1		1010		0.362				10.9		1090		0.352				11		908		0.352				11.3		1170		0.364				11		1240		0.358

		10.5		1030		0.34				11.1		918		0.361				11.2		1010		0.364				11		1100		0.355				11		913		0.354				11.3		1170		0.366				11		1240		0.36

		10.6		1040		0.342				11.2		924		0.362				11.3		1020		0.366				11		1110		0.357				11.1		918		0.356				11.4		1180		0.368				11.2		1260		0.364

		10.7		1050		0.345				11.3		929		0.365				11.4		1020		0.368				11.1		1110		0.359				11.1		923		0.358				11.4		1190		0.371				11.3		1260		0.366

		10.8		1050		0.348				11.4		938		0.368				11.4		1030		0.37				11.1		1120		0.361				11.2		929		0.36				11.5		1190		0.373				11.3		1270		0.368

		10.9		1060		0.35				11.4		943		0.37				11.5		1040		0.372				11.2		1130		0.363				11.3		934		0.362				11.6		1200		0.376				11.4		1280		0.37

		10.9		1070		0.352				11.5		949		0.372				11.6		1040		0.374				11.3		1140		0.365				11.3		939		0.364				11.7		1210		0.378				11.5		1290		0.373

		11		1070		0.354				11.5		954		0.374				11.7		1050		0.378				11.4		1140		0.367				11.4		945		0.366				11.7		1210		0.38				11.5		1300		0.375

		11		1080		0.356				11.6		959		0.376				11.7		1060		0.38				11.4		1150		0.369				11.4		950		0.369				11.8		1220		0.382				11.6		1310		0.377

		11.1		1090		0.358				11.7		965		0.378				11.8		1060		0.382				11.5		1160		0.372				11.5		958		0.372				11.8		1230		0.384				11.6		1310		0.379

		11.2		1090		0.36				11.7		971		0.38				11.9		1070		0.384				11.5		1170		0.374				11.6		963		0.374				11.9		1230		0.386				11.7		1320		0.381

		11.3		1100		0.363				11.8		976		0.382				11.9		1070		0.386				11.6		1180		0.377				11.7		968		0.376				12		1240		0.388				11.8		1340		0.384

		11.3		1110		0.365				11.9		986		0.386				12		1080		0.389				11.7		1180		0.378				11.7		973		0.378				12.1		1250		0.391				11.8		1340		0.386

		11.4		1120		0.367				11.9		992		0.389				12.1		1090		0.391				11.7		1190		0.381				11.8		978		0.38				12.1		1260		0.394				11.9		1350		0.388

		11.5		1120		0.369				12		997		0.391				12.1		1090		0.393				11.8		1200		0.383				11.9		983		0.382				12.2		1260		0.396				12		1360		0.39

		11.5		1130		0.371				12.1		1000		0.393				12.2		1100		0.397				11.9		1200		0.385				11.9		988		0.384				12.3		1270		0.398				12		1370		0.392

		11.6		1140		0.373				12.1		1010		0.395				12.3		1110		0.399				11.9		1210		0.387				12		994		0.386				12.3		1280		0.4				12.1		1370		0.395

		11.6		1140		0.375				12.2		1010		0.397				12.4		1110		0.401				12		1220		0.389				12		999		0.388				12.4		1280		0.402				12.1		1380		0.397

		11.7		1150		0.378				12.3		1020		0.399				12.4		1120		0.403				12.1		1230		0.393				12.2		1010		0.392				12.5		1290		0.404				12.2		1390		0.399

		11.8		1160		0.38				12.3		1020		0.401				12.5		1120		0.405				12.2		1240		0.395				12.2		1020		0.394				12.5		1300		0.406				12.3		1400		0.402

		11.9		1170		0.384				12.4		1030		0.403				12.6		1130		0.408				12.3		1240		0.397				12.3		1020		0.397				12.6		1310		0.408				12.4		1410		0.404

		12		1180		0.386				12.5		1040		0.406				12.6		1140		0.41				12.3		1250		0.399				12.4		1030		0.399				12.6		1310		0.41				12.5		1420		0.406

		12		1180		0.388				12.5		1040		0.408				12.7		1140		0.412				12.4		1260		0.401				12.4		1030		0.401				12.7		1330		0.413				12.5		1420		0.408

		12.1		1190		0.39				12.6		1050		0.41				12.8		1150		0.416				12.5		1270		0.403				12.5		1040		0.403				12.8		1330		0.415				12.6		1430		0.41

		12.1		1200		0.392				12.7		1050		0.412				12.9		1160		0.418				12.5		1270		0.406				12.6		1040		0.405				12.9		1340		0.418				12.6		1440		0.412

		12.2		1200		0.394				12.8		1060		0.414				12.9		1160		0.42				12.5		1280		0.408				12.6		1050		0.407				12.9		1350		0.42				12.7		1450		0.414

		12.2		1210		0.396				12.8		1060		0.417				13		1160		0.422				12.6		1290		0.41				12.7		1050		0.409				13		1360		0.422				12.7		1450		0.416

		12.3		1210		0.399				12.9		1070		0.419				13.1		1170		0.424				12.7		1300		0.414				12.8		1060		0.413				13		1360		0.424				12.8		1460		0.418

		12.5		1230		0.403				12.9		1070		0.421				13.1		1180		0.426				12.8		1300		0.416				12.9		1070		0.415				13.1		1370		0.426				12.9		1470		0.421

		12.5		1230		0.405				13		1080		0.423				13.2		1180		0.428				12.9		1310		0.418				12.9		1070		0.417				13.2		1380		0.428				12.9		1470		0.422

		12.6		1240		0.407				13.1		1090		0.427				13.2		1190		0.43				13		1320		0.42				13		1080		0.42				13.2		1390		0.43				13		1480		0.425

		12.6		1240		0.409				13.2		1090		0.429				13.4		1200		0.435				13		1320		0.422				13		1080		0.422				13.3		1390		0.432				13.1		1490		0.427

		12.7		1250		0.411				13.2		1100		0.431				13.4		1200		0.437				13.1		1330		0.424				13.1		1090		0.424				13.4		1400		0.434				13.1		1500		0.429

		12.7		1250		0.413				13.3		1100		0.433				13.5		1210		0.439				13.1		1340		0.427				13.2		1090		0.426				13.4		1410		0.436				13.2		1500		0.431

		12.8		1260		0.415				13.4		1110		0.435				13.6		1210		0.441				13.2		1340		0.428				13.2		1100		0.428				13.5		1420		0.438				13.3		1510		0.433

		12.9		1260		0.417				13.4		1110		0.438				13.6		1220		0.443				13.3		1350		0.433				13.3		1100		0.43				13.5		1420		0.44				13.3		1520		0.435

		13		1270		0.42				13.5		1120		0.44				13.7		1220		0.445				13.4		1360		0.435				13.4		1110		0.433				13.6		1430		0.442				13.4		1520		0.437

		13		1270		0.422				13.5		1120		0.442				13.7		1230		0.447				13.4		1370		0.437				13.4		1120		0.435				13.6		1440		0.444				13.5		1540		0.441

		13.1		1280		0.424				13.6		1130		0.445				13.8		1230		0.449				13.5		1370		0.439				13.5		1120		0.437				13.7		1450		0.446				13.6		1540		0.443

		13.1		1280		0.426				13.7		1140		0.447				13.9		1240		0.452				13.5		1380		0.441				13.6		1130		0.439				13.8		1460		0.451				13.6		1550		0.446

		13.2		1290		0.429				13.8		1140		0.449				14		1250		0.454				13.6		1380		0.443				13.6		1130		0.441				13.9		1470		0.453				13.7		1560		0.448

		13.3		1290		0.431				13.9		1140		0.451				14		1250		0.456				13.7		1390		0.445				13.7		1140		0.443				14		1470		0.455				13.7		1560		0.449

		13.3		1300		0.433				13.9		1150		0.453				14.1		1260		0.458				13.7		1400		0.447				13.8		1140		0.445				14		1480		0.457				13.8		1570		0.451

		13.4		1300		0.435				14		1150		0.455				14.2		1260		0.46				13.9		1410		0.451				13.8		1150		0.448				14.1		1490		0.459				13.9		1570		0.454

		13.5		1310		0.437				14		1160		0.457				14.2		1270		0.463				13.9		1410		0.453				13.9		1160		0.452				14.2		1500		0.461				13.9		1580		0.456

		13.6		1320		0.441				14.1		1160		0.459				14.3		1270		0.465				14		1420		0.456				14		1160		0.454				14.2		1500		0.463				14		1590		0.459

		13.7		1330		0.443				14.2		1170		0.461				14.3		1280		0.467				14.1		1430		0.458				14.1		1170		0.456				14.3		1510		0.465				14.1		1600		0.461

		13.7		1330		0.445				14.2		1180		0.464				14.5		1290		0.471				14.1		1430		0.459				14.2		1170		0.458				14.4		1520		0.467				14.1		1600		0.463

		13.8		1340		0.447				14.3		1180		0.467				14.5		1300		0.473				14.2		1440		0.462				14.2		1170		0.46				14.5		1530		0.472				14.2		1610		0.465

		13.8		1340		0.45				14.4		1190		0.469				14.6		1300		0.475				14.3		1440		0.464				14.3		1180		0.462				14.5		1540		0.474				14.3		1610		0.467

		13.9		1350		0.452				14.4		1190		0.471				14.7		1310		0.477				14.3		1450		0.466				14.3		1190		0.464				14.6		1540		0.476				14.3		1620		0.469

		14		1350		0.454				14.5		1200		0.473				14.7		1310		0.48				14.4		1460		0.47				14.4		1190		0.466				14.6		1550		0.478				14.4		1630		0.471

		14		1360		0.456				14.6		1200		0.475				14.8		1320		0.482				14.5		1470		0.472				14.5		1200		0.469				14.7		1560		0.48				14.4		1630		0.474

		14.1		1370		0.46				14.6		1210		0.477				14.8		1320		0.484				14.5		1470		0.474				14.5		1200		0.471				14.8		1560		0.482				14.5		1640		0.476

		14.2		1370		0.462				14.7		1210		0.479				14.9		1330		0.486				14.6		1480		0.476				14.6		1210		0.473				14.9		1570		0.484				14.6		1650		0.48

		14.3		1380		0.464				14.7		1220		0.481				15		1340		0.49				14.7		1490		0.478				14.7		1210		0.476				14.9		1580		0.486				14.7		1660		0.482

		14.3		1380		0.466				14.9		1230		0.485				15.1		1340		0.492				14.8		1490		0.48				14.8		1220		0.478				15		1590		0.49				14.8		1660		0.484

		14.4		1390		0.468				14.9		1230		0.487				15.2		1350		0.494				14.8		1500		0.483				14.8		1220		0.48				15.1		1600		0.492				14.8		1670		0.486

		14.5		1390		0.47				15		1240		0.489				15.2		1350		0.496				14.9		1500		0.485				14.8		1230		0.482				15.2		1600		0.494				14.9		1670		0.488

		14.5		1400		0.472				15.1		1240		0.491				15.3		1360		0.499				15		1520		0.489				14.9		1230		0.484				15.2		1610		0.496				14.9		1680		0.49

		14.6		1400		0.474				15.1		1250		0.493				15.3		1360		0.501				15.1		1520		0.491				15		1240		0.486				15.3		1620		0.499				15		1680		0.492

		14.7		1410		0.477				15.2		1250		0.496				15.4		1370		0.503				15.1		1530		0.493				15.1		1240		0.488				15.4		1620		0.501				15.1		1690		0.494

		14.7		1410		0.479				15.2		1260		0.498				15.5		1370		0.505				15.2		1530		0.495				15.2		1250		0.492				15.4		1630		0.503				15.2		1700		0.497

		14.8		1420		0.481				15.3		1260		0.5				15.6		1380		0.509				15.3		1540		0.497				15.2		1250		0.494				15.5		1640		0.505				15.3		1710		0.499

		14.9		1430		0.483				15.4		1270		0.502				15.7		1390		0.511				15.3		1540		0.499				15.3		1260		0.496				15.5		1640		0.507				15.3		1710		0.501

		14.9		1430		0.484				15.5		1270		0.506				15.7		1390		0.513				15.4		1550		0.501				15.4		1260		0.499				15.6		1650		0.51				15.4		1720		0.504

		14.9		1430		0.487				15.5		1280		0.508				15.8		1400		0.515				15.4		1560		0.504				15.4		1270		0.501				15.7		1660		0.512				15.4		1720		0.506

		15		1440		0.489				15.6		1280		0.51				15.8		1400		0.517				15.5		1570		0.508				15.5		1270		0.503				15.8		1660		0.514				15.5		1730		0.508

		15.1		1450		0.491				15.7		1290		0.512				15.9		1410		0.519				15.6		1570		0.509				15.5		1280		0.505				15.8		1670		0.516				15.6		1730		0.51

		15.1		1450		0.493				15.7		1290		0.514				16		1410		0.522				15.7		1580		0.512				15.6		1280		0.507				15.9		1680		0.518				15.6		1740		0.512

		15.3		1460		0.497				15.8		1300		0.517				16		1420		0.524				15.7		1580		0.514				15.7		1290		0.51				15.9		1680		0.521				15.7		1750		0.515

		15.4		1470		0.499				15.8		1300		0.519				16.2		1430		0.528				15.8		1590		0.516				15.8		1290		0.512				16		1690		0.523				15.8		1750		0.517

		15.4		1470		0.501				15.9		1300		0.521				16.2		1430		0.53				15.9		1600		0.518				15.8		1300		0.514				16		1700		0.524				15.8		1760		0.519

		15.4		1480		0.503				16		1310		0.523				16.3		1440		0.532				15.9		1600		0.52				15.9		1300		0.516				16.1		1700		0.527				15.9		1770		0.521

		15.5		1480		0.505				16.1		1310		0.526				16.4		1440		0.534				16		1610		0.522				15.9		1310		0.518				16.2		1710		0.53				15.9		1770		0.523

		15.6		1490		0.508				16.1		1320		0.528				16.4		1450		0.536				16.1		1610		0.524				16		1310		0.52				16.3		1720		0.532				16		1780		0.526

		15.6		1490		0.51				16.2		1320		0.53				16.5		1450		0.538				16.1		1620		0.527				16.1		1320		0.522				16.4		1720		0.534				16.1		1780		0.528

		15.7		1500		0.512				16.3		1330		0.532				16.5		1460		0.54				16.2		1630		0.529				16.1		1320		0.524				16.4		1730		0.536				16.1		1790		0.53

		15.8		1500		0.514				16.3		1330		0.534				16.6		1460		0.542				16.3		1630		0.531				16.2		1330		0.527				16.5		1730		0.538				16.2		1790		0.532

		15.9		1510		0.517				16.4		1340		0.536				16.7		1470		0.546				16.3		1640		0.534				16.3		1330		0.53				16.5		1740		0.54				16.3		1800		0.535

		15.9		1510		0.519				16.4		1340		0.538				16.8		1480		0.548				16.4		1650		0.536				16.3		1340		0.532				16.6		1750		0.542				16.4		1810		0.537

		16		1520		0.521				16.5		1350		0.54				16.8		1480		0.55				16.5		1650		0.538				16.4		1340		0.534				16.6		1750		0.544				16.4		1810		0.539

		16.1		1520		0.523				16.6		1350		0.543				16.9		1490		0.552				16.5		1660		0.54				16.5		1350		0.536				16.7		1760		0.546				16.5		1820		0.541

		16.1		1530		0.525				16.7		1360		0.546				17		1490		0.554				16.6		1660		0.542				16.5		1350		0.538				16.8		1770		0.55				16.5		1820		0.543

		16.2		1530		0.527				16.7		1360		0.548				17		1490		0.556				16.6		1670		0.544				16.6		1360		0.54				16.9		1770		0.552				16.6		1830		0.545

		16.2		1540		0.53				16.8		1370		0.55				17.1		1500		0.558				16.8		1680		0.547				16.7		1360		0.542				16.9		1780		0.554				16.7		1840		0.547

		16.3		1540		0.532				16.9		1370		0.552				17.1		1500		0.56				16.8		1680		0.549				16.7		1360		0.544				17		1780		0.556				16.8		1840		0.549

		16.4		1550		0.534				16.9		1380		0.554				17.3		1510		0.565				16.9		1690		0.551				16.8		1370		0.549				17		1790		0.558				16.9		1850		0.554

		16.4		1550		0.536				17		1380		0.556				17.3		1520		0.567				16.9		1700		0.553				16.9		1380		0.55				17.1		1800		0.56				16.9		1860		0.556

		16.5		1560		0.538				17.1		1380		0.558				17.4		1520		0.569				17		1700		0.555				17		1380		0.552				17.2		1800		0.562				17		1860		0.558

		16.5		1560		0.54				17.1		1390		0.561				17.5		1530		0.571				17.1		1710		0.557				17.1		1390		0.555				17.3		1810		0.564				17		1870		0.56

		16.6		1570		0.542				17.2		1400		0.563				17.5		1530		0.573				17.1		1710		0.559				17.1		1390		0.557				17.4		1820		0.567				17.1		1870		0.562

		16.7		1570		0.544				17.3		1400		0.565				17.6		1540		0.575				17.2		1720		0.562				17.2		1400		0.559				17.4		1820		0.569				17.2		1880		0.564

		16.7		1580		0.546				17.3		1400		0.568				17.6		1540		0.577				17.3		1720		0.564				17.2		1400		0.561				17.5		1830		0.571				17.2		1880		0.566

		16.8		1580		0.548				17.4		1410		0.57				17.7		1550		0.579				17.4		1740		0.568				17.3		1400		0.563				17.5		1830		0.573				17.3		1890		0.568

		16.9		1590		0.55				17.5		1410		0.572				17.8		1560		0.583				17.4		1740		0.57				17.4		1410		0.566				17.6		1840		0.575				17.4		1900		0.571

		16.9		1590		0.552				17.5		1420		0.574				17.9		1560		0.585				17.5		1750		0.572				17.4		1420		0.568				17.7		1840		0.578				17.5		1910		0.573

		17		1600		0.556				17.6		1420		0.576				18		1570		0.588				17.6		1750		0.574				17.5		1420		0.57				17.7		1850		0.58				17.5		1910		0.576

		17.1		1610		0.559				17.7		1430		0.58				18		1570		0.59				17.6		1760		0.576				17.6		1420		0.572				17.8		1860		0.582				17.6		1920		0.577

		17.2		1610		0.561				17.8		1430		0.582				18.1		1580		0.592				17.7		1760		0.578				17.7		1430		0.575				17.8		1860		0.584				17.7		1920		0.579

		17.3		1620		0.563				17.8		1440		0.584				18.2		1580		0.594				17.8		1770		0.58				17.7		1430		0.577				17.9		1870		0.587				17.7		1930		0.582

		17.3		1620		0.565				17.9		1440		0.586				18.2		1590		0.596				17.8		1780		0.583				17.8		1440		0.579				18		1880		0.589				17.8		1930		0.584

		17.4		1630		0.567				18		1450		0.588				18.3		1590		0.599				17.9		1780		0.585				17.8		1440		0.581				18		1880		0.591				17.8		1940		0.586

		17.4		1630		0.569				18		1450		0.59				18.4		1600		0.601				18		1790		0.588				17.9		1450		0.584				18.1		1890		0.593				17.9		1940		0.588

		17.5		1640		0.571				18.1		1460		0.592				18.4		1600		0.603				18		1800		0.591				18		1450		0.586				18.2		1890		0.595				18		1950		0.592

		17.6		1650		0.575				18.2		1460		0.595				18.5		1610		0.606				18.1		1800		0.593				18		1460		0.588				18.3		1900		0.597				18.1		1960		0.594

		17.7		1650		0.577				18.2		1470		0.598				18.6		1610		0.608				18.2		1810		0.595				18.1		1460		0.59				18.3		1900		0.6				18.2		1970		0.596

		17.8		1660		0.58				18.3		1470		0.6				18.6		1620		0.61				18.3		1810		0.597				18.2		1470		0.592				18.4		1910		0.602				18.2		1970		0.598

		17.8		1660		0.582				18.4		1480		0.602				18.7		1620		0.612				18.3		1820		0.599				18.2		1470		0.594				18.5		1920		0.605				18.3		1980		0.6

		17.9		1670		0.584				18.4		1480		0.604				18.8		1630		0.614				18.3		1830		0.601				18.3		1480		0.596				18.5		1920		0.607				18.3		1980		0.602

		17.9		1670		0.586				18.5		1490		0.606				18.9		1640		0.618				18.4		1830		0.603				18.3		1480		0.598				18.6		1930		0.609				18.4		1990		0.605

		18		1680		0.588				18.6		1490		0.608				18.9		1640		0.62				18.5		1840		0.607				18.4		1480		0.6				18.6		1940		0.611				18.5		1990		0.607

		18.1		1680		0.59				18.6		1490		0.61				19		1640		0.623				18.6		1850		0.609				18.5		1490		0.604				18.7		1940		0.613				18.6		2000		0.61

		18.2		1690		0.594				18.7		1500		0.612				19.1		1650		0.625				18.7		1850		0.611				18.6		1500		0.606				18.8		1950		0.615				18.6		2010		0.612

		18.3		1700		0.596				18.8		1500		0.614				19.1		1650		0.627				18.7		1860		0.614				18.7		1500		0.608				18.8		1950		0.617				18.7		2010		0.614

		18.3		1700		0.598				18.8		1510		0.618				19.2		1660		0.629				18.8		1860		0.616				18.7		1500		0.61				18.9		1960		0.619				18.7		2020		0.616

		18.4		1710		0.6				18.9		1520		0.62				19.3		1660		0.631				18.9		1870		0.618				18.8		1510		0.612				19		1970		0.623				18.8		2020		0.618

		18.4		1710		0.602				19		1520		0.622				19.3		1670		0.633				18.9		1870		0.62				18.8		1510		0.614				19.1		1980		0.625				18.9		2030		0.62

		18.5		1720		0.604				19.1		1520		0.625				19.4		1680		0.637				19		1880		0.622				18.9		1520		0.616				19.2		1980		0.628				18.9		2030		0.622

		18.5		1720		0.607				19.1		1530		0.627				19.5		1680		0.639				19.1		1890		0.626				18.9		1520		0.618				19.2		1990		0.63				19		2040		0.624

		18.6		1730		0.609				19.2		1530		0.629				19.6		1690		0.641				19.2		1890		0.628				19		1530		0.62				19.3		1990		0.632				19.1		2040		0.626

		18.7		1730		0.611				19.2		1540		0.631				19.6		1690		0.643				19.3		1900		0.63				19.1		1530		0.625				19.4		2000		0.634				19.2		2050		0.63

		18.8		1740		0.614				19.3		1540		0.633				19.7		1700		0.646				19.3		1900		0.632				19.2		1540		0.626				19.4		2010		0.636				19.2		2060		0.633

		18.8		1740		0.616				19.4		1550		0.636				19.8		1700		0.648				19.4		1910		0.635				19.3		1540		0.629				19.4		2010		0.638				19.3		2070		0.635

		18.9		1750		0.618				19.5		1550		0.638				19.8		1710		0.65				19.4		1910		0.636				19.3		1550		0.63				19.5		2020		0.64				19.3		2070		0.637

		19		1750		0.62				19.5		1560		0.64				20		1720		0.654				19.5		1920		0.639				19.4		1550		0.633				19.6		2030		0.644				19.4		2080		0.639

		19		1760		0.622				19.6		1560		0.642				20		1720		0.656				19.6		1920		0.641				19.5		1560		0.635				19.7		2030		0.646				19.5		2080		0.641

		19.1		1760		0.624				19.7		1560		0.644				20.1		1730		0.658				19.6		1930		0.643				19.5		1560		0.637				19.8		2040		0.649				19.5		2090		0.643

		19.2		1770		0.626				19.7		1570		0.647				20.1		1730		0.66				19.7		1940		0.647				19.6		1560		0.639				19.9		2050		0.651				19.6		2090		0.645

		19.2		1770		0.628				19.7		1570		0.649				20.2		1730		0.662				19.8		1940		0.649				19.7		1570		0.642				19.9		2050		0.652				19.8		2100		0.649

		19.3		1780		0.63				19.8		1580		0.651				20.3		1740		0.664				19.9		1950		0.651				19.7		1570		0.644				19.9		2060		0.654				19.8		2110		0.651

		19.4		1790		0.634				19.9		1580		0.653				20.3		1740		0.666				19.9		1950		0.653				19.8		1580		0.646				20		2060		0.657				19.8		2110		0.654

		19.4		1790		0.637				20		1590		0.656				20.4		1750		0.67				20		1960		0.655				19.9		1580		0.648				20.1		2070		0.659				19.9		2120		0.656

		19.5		1800		0.639				20.1		1590		0.658				20.5		1760		0.672				20		1960		0.657				19.9		1590		0.65				20.2		2080		0.662				20		2130		0.658

		19.6		1800		0.641				20.1		1590		0.66				20.5		1760		0.674				20.1		1970		0.659				20		1590		0.652				20.3		2080		0.664				20		2130		0.66

		19.7		1810		0.643				20.2		1600		0.662				20.6		1770		0.676				20.2		1970		0.661				20		1590		0.655				20.3		2090		0.666				20.1		2140		0.662

		19.7		1810		0.645				20.2		1600		0.664				20.7		1770		0.678				20.3		1980		0.666				20.1		1600		0.657				20.4		2090		0.668				20.2		2140		0.664

		19.8		1820		0.647				20.3		1610		0.666				20.7		1770		0.68				20.4		1990		0.668				20.2		1610		0.66				20.4		2100		0.67				20.3		2150		0.668

		19.8		1820		0.649				20.3		1610		0.668				20.8		1780		0.682				20.4		1990		0.67				20.3		1610		0.662				20.5		2110		0.672				20.3		2160		0.67

		19.9		1830		0.652				20.4		1620		0.67				20.8		1780		0.684				20.5		2000		0.672				20.3		1610		0.664				20.5		2110		0.674				20.4		2160		0.672

		20		1830		0.654				20.5		1620		0.672				21		1790		0.689				20.6		2000		0.674				20.4		1620		0.666				20.6		2120		0.676				20.5		2170		0.674

		20		1840		0.656				20.6		1630		0.677				21.1		1800		0.691				20.6		2010		0.676				20.5		1620		0.668				20.7		2120		0.679				20.5		2170		0.676

		20.1		1840		0.659				20.7		1630		0.679				21.1		1800		0.693				20.7		2010		0.678				20.5		1620		0.67				20.8		2130		0.683				20.6		2180		0.678

		20.2		1850		0.661				20.7		1640		0.681				21.2		1810		0.695				20.8		2020		0.682				20.6		1630		0.672				20.9		2140		0.685				20.7		2180		0.68

		20.2		1850		0.662				20.8		1640		0.683				21.2		1810		0.697				20.9		2030		0.685				20.6		1630		0.674				20.9		2150		0.687				20.7		2190		0.683

		20.3		1860		0.665				20.8		1640		0.685				21.3		1820		0.699				20.9		2030		0.687				20.7		1640		0.676				21		2150		0.689				20.8		2200		0.687

		20.4		1860		0.667				20.9		1650		0.687				21.4		1820		0.701				21		2040		0.689				20.8		1640		0.68				21.1		2160		0.691				20.9		2210		0.689

		20.4		1870		0.67				21		1650		0.689				21.5		1830		0.705				21		2040		0.691				20.9		1650		0.683				21.1		2160		0.693				21		2210		0.691

		20.5		1870		0.672				21		1660		0.691				21.5		1830		0.706				21.1		2050		0.693				21		1650		0.685				21.2		2170		0.695				21		2220		0.693

		20.6		1880		0.674				21.1		1660		0.694				21.6		1840		0.708				21.2		2050		0.695				21		1660		0.687				21.2		2170		0.697				21.1		2220		0.695

		20.7		1880		0.676				21.2		1670		0.697				21.7		1840		0.71				21.3		2050		0.697				21.1		1660		0.689				21.3		2180		0.7				21.2		2230		0.697

		20.7		1890		0.678				21.2		1670		0.699				21.7		1840		0.713				21.3		2060		0.7				21.1		1660		0.691				21.4		2190		0.702				21.3		2230		0.699

		20.8		1890		0.68				21.3		1680		0.701				21.8		1850		0.715				21.4		2070		0.702				21.2		1670		0.693				21.4		2190		0.704				21.3		2240		0.701

		20.8		1900		0.682				21.4		1680		0.703				21.8		1850		0.717				21.5		2070		0.704				21.3		1670		0.695				21.5		2200		0.707				21.4		2250		0.704

		20.9		1900		0.684				21.5		1680		0.705				21.9		1860		0.719				21.5		2080		0.707				21.3		1680		0.697				21.6		2200		0.709				21.4		2250		0.706

		21		1910		0.689				21.5		1690		0.707				22		1870		0.723				21.6		2080		0.709				21.4		1680		0.699				21.6		2210		0.711				21.5		2260		0.708

		21.1		1910		0.691				21.6		1690		0.709				22.1		1870		0.725				21.7		2090		0.711				21.5		1680		0.701				21.7		2210		0.713				21.6		2270		0.711

		21.1		1920		0.693				21.7		1700		0.713				22.2		1870		0.727				21.7		2090		0.713				21.5		1690		0.703				21.8		2220		0.715				21.6		2270		0.713

		21.2		1920		0.695				21.7		1700		0.715				22.2		1880		0.73				21.8		2100		0.715				21.6		1690		0.705				21.8		2220		0.717				21.7		2280		0.715

		21.3		1930		0.697				21.8		1710		0.717				22.3		1880		0.732				21.9		2100		0.717				21.6		1690		0.707				21.9		2240		0.721				21.7		2280		0.717

		21.3		1930		0.699				21.9		1710		0.719				22.3		1890		0.734				21.9		2110		0.72				21.7		1700		0.709				22		2240		0.723				21.8		2290		0.719

		21.4		1940		0.701				21.9		1720		0.721				22.4		1890		0.736				22		2110		0.722				21.7		1700		0.712				22.1		2250		0.725				21.9		2300		0.723

		21.4		1940		0.703				22		1720		0.723				22.5		1900		0.74				22		2120		0.724				21.8		1710		0.714				22.1		2250		0.728				22		2300		0.725

		21.5		1950		0.705				22.1		1720		0.726				22.6		1910		0.742				22.1		2120		0.726				21.9		1710		0.717				22.2		2260		0.73				22.1		2310		0.727

		21.6		1960		0.709				22.1		1730		0.728				22.7		1910		0.744				22.2		2130		0.728				22		1720		0.719				22.3		2260		0.732				22.2		2320		0.729

		21.7		1960		0.711				22.2		1730		0.73				22.7		1910		0.747				22.3		2130		0.73				22.1		1720		0.721				22.3		2270		0.734				22.2		2320		0.732

		21.8		1960		0.713				22.3		1740		0.734				22.8		1920		0.748				22.3		2140		0.732				22.1		1720		0.723				22.4		2270		0.736				22.3		2330		0.734

		21.8		1970		0.716				22.4		1740		0.736				22.9		1920		0.75				22.4		2140		0.734				22.2		1730		0.725				22.5		2280		0.74				22.3		2330		0.736

		21.9		1970		0.718				22.5		1750		0.738				22.9		1930		0.753				22.5		2150		0.739				22.2		1730		0.727				22.6		2290		0.742				22.4		2340		0.738

		21.9		1980		0.72				22.5		1750		0.74				23		1940		0.757				22.5		2150		0.741				22.3		1730		0.729				22.7		2290		0.744				22.4		2340		0.74

		22		1980		0.722				22.6		1760		0.742				23.1		1940		0.759				22.6		2160		0.743				22.3		1740		0.732				22.7		2300		0.746				22.6		2350		0.743

		22.1		1990		0.724				22.6		1760		0.744				23.2		1940		0.761				22.7		2160		0.745				22.4		1740		0.734				22.8		2300		0.748				22.6		2360		0.745

		22.2		2000		0.728				22.7		1760		0.746				23.2		1950		0.763				22.8		2170		0.747				22.5		1750		0.738				22.8		2310		0.75				22.7		2360		0.747

		22.2		2000		0.73				22.8		1770		0.748				23.3		1950		0.765				22.8		2170		0.749				22.6		1750		0.74				22.9		2310		0.752				22.7		2370		0.749

		22.3		2010		0.732				22.9		1780		0.753				23.4		1960		0.767				22.9		2180		0.751				22.6		1760		0.742				22.9		2320		0.754				22.8		2370		0.751

		22.4		2010		0.734				22.9		1780		0.755				23.4		1960		0.77				22.9		2180		0.753				22.7		1760		0.744				23		2330		0.757				22.9		2380		0.753

		22.5		2020		0.737				23		1790		0.757				23.5		1970		0.774				23		2190		0.755				22.8		1770		0.746				23.1		2330		0.76				22.9		2380		0.755

		22.5		2020		0.739				23.1		1790		0.759				23.6		1970		0.776				23.1		2190		0.758				22.8		1770		0.748				23.2		2340		0.762				23		2390		0.757

		22.6		2020		0.74				23.1		1790		0.761				23.7		1980		0.778				23.1		2200		0.761				22.9		1770		0.75				23.2		2340		0.764				23.1		2400		0.761

		22.7		2030		0.743				23.2		1800		0.763				23.7		1980		0.78				23.2		2200		0.762				23		1780		0.753				23.3		2350		0.766				23.1		2400		0.763

		22.7		2040		0.747				23.2		1800		0.765				23.8		1980		0.782				23.3		2210		0.765				23		1780		0.754				23.3		2360		0.768				23.2		2410		0.765

		22.8		2040		0.749				23.3		1800		0.767				23.9		1990		0.784				23.3		2210		0.767				23.1		1780		0.756				23.4		2360		0.77				23.2		2410		0.767

		22.9		2050		0.751				23.4		1810		0.77				23.9		1990		0.786				23.4		2220		0.769				23.1		1790		0.758				23.5		2370		0.772				23.3		2420		0.769

		22.9		2050		0.753				23.5		1810		0.772				24		2000		0.788				23.4		2220		0.771				23.2		1790		0.761				23.5		2370		0.774				23.4		2420		0.771

		23		2060		0.755				23.5		1820		0.775				24.1		2000		0.793				23.5		2230		0.773				23.3		1800		0.763				23.6		2380		0.776				23.4		2430		0.773

		23.1		2060		0.757				23.6		1820		0.777				24.2		2010		0.795				23.7		2230		0.777				23.3		1800		0.765				23.7		2380		0.779				23.5		2430		0.775

		23.2		2070		0.759				23.6		1830		0.779				24.2		2010		0.797				23.7		2240		0.779				23.4		1800		0.767				23.8		2390		0.781				23.6		2440		0.777

		23.2		2070		0.761				23.7		1830		0.781				24.3		2020		0.799				23.8		2240		0.781				23.5		1810		0.769				23.8		2400		0.783				23.7		2450		0.781

		23.3		2080		0.766				23.8		1830		0.783				24.3		2020		0.801				23.8		2250		0.783				23.5		1810		0.771				23.9		2400		0.786				23.7		2450		0.783

		23.4		2080		0.768				23.8		1840		0.785				24.4		2030		0.803				23.9		2250		0.786				23.6		1810		0.773				24		2410		0.788				23.8		2460		0.785

		23.5		2090		0.77				23.9		1840		0.787				24.5		2030		0.805				23.9		2260		0.788				23.7		1820		0.777				24		2410		0.79				23.9		2460		0.787

		23.5		2090		0.772				24		1850		0.791				24.6		2030		0.807				24		2260		0.79				23.8		1820		0.779				24.1		2420		0.792				23.9		2470		0.79

		23.6		2100		0.774				24.1		1850		0.793				24.7		2040		0.812				24.1		2270		0.792				23.8		1830		0.782				24.1		2420		0.794				24		2470		0.792

		23.6		2100		0.776				24.2		1860		0.795				24.7		2050		0.814				24.2		2280		0.796				23.9		1830		0.784				24.2		2430		0.796				24.1		2480		0.794

		23.7		2110		0.778				24.2		1860		0.797				24.8		2050		0.816				24.3		2280		0.798				24		1840		0.786				24.3		2440		0.8				24.2		2480		0.796

		23.7		2110		0.78				24.3		1870		0.799				24.9		2050		0.818				24.3		2280		0.8				24		1840		0.787				24.4		2450		0.802				24.2		2490		0.799

		23.8		2110		0.782				24.3		1870		0.801				24.9		2060		0.82				24.4		2290		0.802				24.1		1840		0.79				24.4		2460		0.804				24.3		2500		0.801

		23.9		2120		0.787				24.4		1870		0.804				25		2060		0.822				24.5		2290		0.804				24.2		1850		0.792				24.5		2460		0.806				24.4		2500		0.803

		24		2130		0.788				24.5		1880		0.806				25.1		2070		0.824				24.5		2300		0.806				24.3		1850		0.796				24.6		2470		0.809				24.4		2510		0.805

		24.1		2130		0.79				24.6		1880		0.808				25.1		2070		0.826				24.6		2300		0.808				24.4		1860		0.798				24.6		2470		0.811				24.5		2510		0.807

		24.1		2140		0.793				24.6		1890		0.811				25.2		2080		0.83				24.6		2310		0.81				24.4		1860		0.8				24.7		2480		0.813				24.6		2520		0.809

		24.2		2140		0.795				24.7		1890		0.813				25.3		2080		0.833				24.8		2310		0.814				24.5		1870		0.802				24.8		2490		0.815				24.6		2520		0.812

		24.2		2140		0.797				24.8		1890		0.815				25.4		2090		0.834				24.8		2320		0.816				24.5		1870		0.804				24.8		2490		0.818				24.7		2530		0.814

		24.3		2150		0.799				24.8		1900		0.817				25.4		2090		0.836				24.9		2320		0.818				24.6		1870		0.806				24.9		2500		0.82				24.7		2540		0.816

		24.4		2150		0.801				24.9		1900		0.819				25.5		2100		0.839				24.9		2330		0.82				24.7		1880		0.808				25		2500		0.822				24.8		2540		0.819

		24.4		2160		0.803				24.9		1910		0.821				25.6		2100		0.841				25		2330		0.822				24.7		1880		0.811				25		2510		0.824				24.9		2550		0.821

		24.6		2170		0.807				25		1910		0.823				25.6		2110		0.843				25		2340		0.824				24.8		1890		0.814				25.1		2510		0.826				24.9		2550		0.823

		24.6		2170		0.809				25.1		1910		0.825				25.7		2110		0.845				25.1		2340		0.826				24.9		1890		0.816				25.2		2520		0.828				25		2560		0.825

		24.7		2170		0.811				25.2		1920		0.828				25.7		2110		0.847				25.2		2340		0.828				25		1890		0.818				25.2		2520		0.83				25.1		2560		0.827

		24.7		2180		0.813				25.2		1920		0.83				25.9		2120		0.851				25.3		2350		0.831				25		1900		0.82				25.3		2530		0.832				25.2		2570		0.829

		24.8		2180		0.815				25.3		1930		0.833				25.9		2130		0.853				25.3		2360		0.833				25		1900		0.822				25.4		2540		0.834				25.2		2570		0.831

		24.9		2190		0.817				25.3		1930		0.835				26		2130		0.855				25.4		2360		0.836				25.1		1910		0.824				25.5		2550		0.839				25.2		2580		0.833

		24.9		2190		0.819				25.4		1930		0.837				26.1		2130		0.857				25.5		2370		0.838				25.2		1910		0.826				25.5		2550		0.841				25.3		2590		0.835

		25		2200		0.822				25.5		1940		0.839				26.1		2140		0.859				25.5		2370		0.839				25.3		1910		0.828				25.6		2560		0.843				25.4		2590		0.838

		25.2		2200		0.826				25.5		1940		0.841				26.2		2140		0.862				25.6		2370		0.842				25.4		1920		0.832				25.7		2560		0.845				25.5		2600		0.841

		25.2		2210		0.828				25.6		1940		0.843				26.2		2150		0.864				25.7		2380		0.844				25.5		1920		0.834				25.7		2570		0.847				25.6		2600		0.843

		25.3		2210		0.83				25.7		1950		0.845				26.3		2150		0.866				25.7		2380		0.846				25.5		1930		0.836				25.8		2570		0.849				25.6		2610		0.845

		25.3		2220		0.832				25.8		1960		0.849				26.4		2160		0.87				25.8		2390		0.849				25.6		1930		0.838				25.9		2580		0.851				25.7		2620		0.847

		25.4		2220		0.834				25.8		1960		0.851				26.5		2160		0.872				25.9		2390		0.851				25.6		1940		0.841				25.9		2580		0.853				25.7		2620		0.849

		25.5		2230		0.836				25.9		1960		0.854				26.6		2170		0.874				25.9		2400		0.853				25.7		1940		0.843				26		2590		0.856				25.8		2630		0.851

		25.5		2230		0.838				26		1970		0.856				26.6		2170		0.876				26		2400		0.855				25.8		1940		0.845				26.1		2600		0.859				25.9		2630		0.853

		25.6		2230		0.84				26		1970		0.858				26.6		2170		0.878				26		2410		0.857				25.8		1950		0.847				26.1		2600		0.861				25.9		2640		0.856

		25.7		2240		0.844				26.1		1970		0.86				26.7		2180		0.88				26.1		2410		0.859				25.9		1950		0.85				26.2		2610		0.863				26		2640		0.858

		25.7		2250		0.846				26.1		1980		0.862				26.8		2180		0.882				26.2		2410		0.862				26		1960		0.852				26.3		2610		0.865				26.1		2650		0.861

		25.8		2250		0.848				26.2		1980		0.864				26.9		2190		0.884				26.3		2420		0.864				26		1960		0.854				26.3		2620		0.867				26.1		2650		0.863

		25.9		2250		0.85				26.3		1990		0.866				27		2190		0.887				26.3		2430		0.867				26.1		1960		0.856				26.4		2620		0.869				26.2		2660		0.865

		25.9		2260		0.852				26.4		1990		0.869				27		2200		0.889				26.4		2430		0.869				26.1		1970		0.858				26.4		2630		0.871				26.2		2670		0.867

		26		2260		0.854				26.5		1990		0.871				27.1		2200		0.892				26.4		2430		0.871				26.2		1970		0.861				26.5		2640		0.873				26.3		2670		0.869

		26.1		2270		0.856				26.5		2000		0.873				27.1		2210		0.894				26.5		2440		0.873				26.3		1980		0.863				26.6		2640		0.876				26.4		2680		0.871

		26.1		2270		0.858				26.6		2000		0.875				27.2		2210		0.896				26.6		2440		0.875				26.4		1980		0.865				26.7		2650		0.878				26.4		2680		0.873

		26.2		2280		0.862				26.6		2000		0.877				27.3		2210		0.898				26.7		2450		0.877				26.4		1980		0.868				26.7		2650		0.88				26.6		2690		0.876

		26.3		2280		0.864				26.7		2010		0.879				27.3		2220		0.9				26.7		2450		0.879				26.5		1990		0.87				26.8		2660		0.882				26.6		2690		0.878

		26.3		2290		0.867				26.8		2010		0.881				27.4		2220		0.902				26.8		2460		0.881				26.6		1990		0.872				26.9		2660		0.884				26.6		2700		0.88

		26.4		2290		0.869				26.8		2020		0.884				27.5		2230		0.904				26.8		2460		0.883				26.6		2000		0.874				26.9		2670		0.887				26.7		2700		0.882

		26.5		2300		0.871				26.9		2020		0.886				27.5		2230		0.906				26.9		2470		0.888				26.7		2000		0.876				27		2680		0.889				26.8		2710		0.884

		26.6		2300		0.873				27		2030		0.89				27.6		2230		0.908				27		2470		0.889				26.8		2000		0.878				27		2680		0.891				26.8		2720		0.886

		26.6		2310		0.875				27		2030		0.892				27.6		2240		0.91				27.1		2480		0.892				26.8		2010		0.88				27.1		2690		0.893				26.9		2720		0.888

		26.6		2310		0.877				27.1		2030		0.894				27.7		2240		0.912				27.1		2480		0.894				26.9		2010		0.883				27.2		2690		0.896				27		2730		0.891

		26.7		2310		0.879				27.2		2040		0.896				27.8		2250		0.914				27.2		2490		0.896				27		2010		0.884				27.2		2700		0.898				27		2730		0.893

		26.8		2320		0.882				27.3		2040		0.898				27.8		2250		0.917				27.3		2490		0.898				27		2020		0.887				27.3		2710		0.9				27.1		2740		0.896

		26.9		2330		0.884				27.3		2050		0.9				27.9		2250		0.919				27.3		2490		0.9				27.1		2020		0.89				27.4		2710		0.902				27.2		2740		0.898

		26.9		2330		0.886				27.4		2050		0.902				27.9		2260		0.921				27.4		2500		0.902				27.2		2030		0.892				27.5		2720		0.904				27.3		2750		0.9

		27		2330		0.888				27.4		2050		0.905				28		2270		0.925				27.5		2500		0.905				27.2		2030		0.894				27.5		2720		0.906				27.3		2750		0.902

		27.1		2340		0.89				27.5		2060		0.906				28.1		2270		0.927				27.6		2510		0.907				27.3		2040		0.896				27.6		2730		0.909				27.4		2760		0.904

		27.1		2340		0.892				27.6		2060		0.911				28.2		2280		0.929				27.6		2510		0.909				27.4		2040		0.898				27.6		2730		0.91				27.4		2770		0.906

		27.2		2350		0.895				27.7		2070		0.913				28.3		2280		0.931				27.7		2520		0.911				27.4		2050		0.9				27.7		2740		0.912				27.5		2770		0.908

		27.2		2350		0.897				27.8		2070		0.915				28.3		2280		0.933				27.7		2520		0.914				27.5		2050		0.902				27.8		2750		0.916				27.6		2780		0.91

		27.3		2360		0.899				27.8		2070		0.917				28.4		2290		0.935				27.8		2530		0.916				27.6		2050		0.905				27.8		2750		0.918				27.6		2780		0.913

		27.5		2360		0.903				27.9		2080		0.919				28.4		2290		0.937				27.9		2530		0.918				27.6		2060		0.907				27.9		2760		0.92				27.7		2790		0.915

		27.5		2370		0.905				27.9		2080		0.921				28.5		2300		0.939				27.9		2530		0.92				27.7		2060		0.909				28		2760		0.922				27.8		2790		0.918

		27.6		2370		0.907				28		2080		0.923				28.6		2310		0.943				28		2540		0.923				27.8		2070		0.912				28		2770		0.924				27.8		2800		0.92

		27.6		2380		0.909				28		2090		0.925				28.7		2310		0.945				28.1		2540		0.925				27.8		2070		0.913				28.1		2770		0.926				27.9		2800		0.922

		27.7		2380		0.911				28.2		2090		0.929				28.8		2310		0.948				28.1		2550		0.927				27.9		2070		0.915				28.2		2780		0.928				28		2810		0.924

		27.8		2390		0.913				28.3		2100		0.931				28.8		2320		0.95				28.2		2550		0.929				27.9		2080		0.918				28.2		2780		0.93				28.1		2820		0.926

		27.8		2390		0.915				28.3		2100		0.934				28.9		2320		0.952				28.3		2560		0.931				28		2080		0.92				28.3		2790		0.932				28.1		2820		0.928

		27.9		2390		0.918				28.4		2100		0.936				28.9		2330		0.954				28.3		2560		0.933				28.1		2090		0.923				28.4		2800		0.935				28.2		2830		0.931

		28		2400		0.922				28.5		2110		0.938				29		2330		0.956				28.4		2570		0.935				28.2		2090		0.925				28.5		2800		0.938				28.2		2830		0.933

		28.1		2410		0.924				28.5		2110		0.94				29.1		2330		0.958				28.5		2570		0.937				28.2		2100		0.927				28.5		2810		0.94				28.3		2840		0.935

		28.1		2410		0.926				28.5		2120		0.942				29.2		2340		0.962				28.6		2580		0.942				28.3		2100		0.929				28.6		2810		0.942				28.4		2840		0.937

		28.2		2420		0.928				28.6		2120		0.944				29.2		2350		0.964				28.6		2580		0.944				28.3		2100		0.931				28.6		2820		0.944				28.4		2850		0.94

		28.2		2420		0.93				28.8		2130		0.948				29.3		2350		0.966				28.7		2580		0.946				28.4		2110		0.933				28.7		2820		0.946				28.5		2860		0.942

		28.3		2420		0.932				28.8		2130		0.95				29.4		2350		0.968				28.8		2590		0.948				28.4		2110		0.935				28.8		2820		0.948				28.6		2860		0.944

		28.4		2430		0.934				28.9		2130		0.952				29.4		2360		0.97				28.8		2590		0.95				28.5		2110		0.937				28.8		2830		0.95				28.6		2870		0.945

		28.5		2430		0.936				28.9		2140		0.955				29.5		2360		0.972				28.9		2600		0.952				28.6		2120		0.94				28.9		2840		0.953				28.7		2880		0.949

		28.5		2440		0.938				29		2140		0.956				29.6		2370		0.974				28.9		2600		0.954				28.7		2120		0.942				29		2840		0.955				28.8		2880		0.951

		28.6		2450		0.942				29		2140		0.958				29.6		2370		0.977				29		2610		0.956				28.7		2130		0.944				29		2850		0.957				28.8		2890		0.953

		28.7		2450		0.945				29.1		2150		0.96				29.8		2380		0.981				29.1		2610		0.959				28.8		2130		0.946				29.1		2850		0.959				28.9		2900		0.955

		28.8		2460		0.947				29.2		2150		0.963				29.8		2380		0.983				29.2		2620		0.961				28.8		2130		0.948				29.2		2860		0.961				29		2900		0.957

		28.8		2460		0.948				29.3		2160		0.967				29.8		2390		0.985				29.2		2620		0.963				28.9		2140		0.95				29.2		2860		0.963				29		2910		0.959

		28.9		2460		0.951				29.4		2160		0.969				29.9		2390		0.987				29.3		2620		0.965				28.9		2140		0.952				29.3		2870		0.966				29.1		2910		0.961

		28.9		2470		0.953				29.4		2170		0.971				30		2400		0.989				29.4		2630		0.967				29		2140		0.954				29.4		2870		0.968				29.1		2920		0.963

		29		2470		0.955				29.5		2170		0.973				30.1		2400		0.991				29.4		2630		0.969				29.1		2150		0.956				29.5		2880		0.972				29.2		2920		0.965

		29.1		2480		0.957				29.5		2170		0.975				30.1		2400		0.993				29.5		2640		0.972				29.1		2150		0.958				29.5		2890		0.974				29.3		2930		0.969

		29.2		2480		0.96				29.6		2180		0.977				30.2		2410		0.995				29.6		2640		0.974				29.2		2160		0.961				29.6		2890		0.976				29.4		2940		0.971

		29.2		2490		0.962				29.7		2180		0.979				30.3		2420		0.999				29.7		2650		0.978				29.3		2160		0.963				29.6		2900		0.978				29.4		2940		0.973

		29.3		2490		0.964				29.8		2180		0.981				30.4		2420		1				29.7		2650		0.98				29.4		2160		0.965				29.7		2910		0.98				29.5		2950		0.975

		29.4		2500		0.966				29.9		2190		0.985				30.4		2420		1				29.8		2660		0.982				29.4		2170		0.968				29.8		2910		0.982				29.5		2950		0.977

		29.4		2500		0.968				29.9		2190		0.987				30.5		2430		1				29.8		2660		0.984				29.5		2170		0.97				29.8		2910		0.984				29.6		2960		0.979

		29.5		2500		0.97				30		2200		0.989				30.6		2430		1.01				29.9		2660		0.986				29.6		2170		0.972				29.9		2920		0.987				29.7		2970		0.981

		29.5		2510		0.973				30		2200		0.991				30.6		2440		1.01				30		2670		0.988				29.6		2180		0.974				30		2930		0.989				29.7		2970		0.983

		29.6		2510		0.975				30.1		2200		0.993				30.7		2440		1.01				30.1		2670		0.99				29.7		2180		0.976				30.1		2930		0.991				29.8		2980		0.985

		29.6		2520		0.977				30.1		2210		0.995				30.7		2440		1.01				30.1		2680		0.993				29.7		2190		0.978				30.1		2940		0.994				29.9		2990		0.989

		29.8		2520		0.98				30.2		2210		0.997				30.9		2450		1.02				30.2		2680		0.997				29.8		2190		0.981				30.2		2940		0.996				30		2990		0.991

		29.8		2530		0.982				30.3		2210		0.999				30.9		2460		1.02				30.3		2690		0.999				29.9		2200		0.983				30.2		2950		0.998				30		3000		0.993

		29.9		2530		0.984				30.4		2220		1				31		2460		1.02				30.4		2690		1				29.9		2200		0.985				30.3		2950		1				30.1		3000		0.996

		30		2540		0.986				30.4		2220		1				31.1		2460		1.02				30.4		2700		1				30		2200		0.987				30.4		2960		1				30.2		3010		0.998

		30		2540		0.988				30.5		2230		1.01				31.1		2470		1.03				30.5		2700		1				30.1		2210		0.99				30.4		2960		1				30.2		3010		1

		30.1		2540		0.99				30.6		2230		1.01				31.2		2470		1.03				30.6		2700		1.01				30.1		2210		0.991				30.5		2970		1.01				30.3		3020		1

		30.1		2550		0.992				30.6		2230		1.01				31.2		2480		1.03				30.6		2710		1.01				30.2		2210		0.993				30.6		2980		1.01				30.4		3020		1

		30.2		2550		0.994				30.7		2240		1.01				31.3		2480		1.03				30.7		2710		1.01				30.3		2220		0.996				30.7		2990		1.01				30.5		3030		1.01

		30.3		2560		0.997				30.8		2240		1.02				31.4		2490		1.04				30.8		2720		1.01				30.4		2230		1				30.7		2990		1.01				30.5		3040		1.01

		30.4		2560		0.999				30.8		2240		1.02				31.5		2490		1.04				30.8		2720		1.02				30.4		2230		1				30.8		3000		1.02				30.6		3050		1.01

		30.4		2570		1				30.9		2250		1.02				31.5		2500		1.04				30.9		2730		1.02				30.5		2230		1				30.9		3000		1.02				30.7		3050		1.01

		30.5		2570		1				30.9		2250		1.02				31.6		2500		1.04				31		2730		1.02				30.6		2240		1.01				31		3010		1.02				30.7		3060		1.02

		30.5		2580		1.01				31		2260		1.02				31.7		2500		1.04				31		2730		1.02				30.6		2240		1.01				31		3010		1.02				30.8		3060		1.02

		30.6		2580		1.01				31.1		2260		1.03				31.7		2510		1.05				31.1		2740		1.03				30.7		2240		1.01				31.1		3020		1.03				30.9		3070		1.02

		30.6		2580		1.01				31.2		2260		1.03				31.8		2510		1.05				31.1		2740		1.03				30.8		2250		1.01				31.1		3020		1.03				30.9		3070		1.02

		30.7		2590		1.01				31.2		2270		1.03				32		2530		1.06				31.2		2750		1.03				30.8		2250		1.01				31.2		3030		1.03				31		3080		1.03

		30.9		2600		1.02				31.3		2270		1.03				32.1		2530		1.06				31.3		2750		1.03				31		2260		1.02				31.3		3030		1.03				31.1		3090		1.03

		30.9		2600		1.02				31.4		2280		1.04				32.1		2540		1.06				31.3		2760		1.03				31		2260		1.02				31.3		3040		1.03				31.2		3090		1.03

		31		2610		1.02				31.4		2280		1.04				32.2		2540		1.06				31.4		2760		1.04				31.1		2270		1.02				31.4		3040		1.04				31.2		3100		1.03

		31		2610		1.02				31.5		2290		1.04				32.3		2540		1.06				31.5		2760		1.04				31.1		2270		1.03				31.5		3050		1.04				31.3		3100		1.03

		31.1		2610		1.03				31.5		2290		1.04				32.3		2550		1.07				31.6		2770		1.04				31.2		2270		1.03				31.5		3050		1.04				31.3		3110		1.04

		31.2		2620		1.03				31.6		2290		1.04				32.4		2550		1.07				31.6		2770		1.04				31.3		2280		1.03				31.6		3060		1.04				31.4		3110		1.04

		31.2		2620		1.03				31.7		2300		1.05				32.4		2560		1.07				31.7		2780		1.05				31.4		2280		1.03				31.6		3070		1.05				31.5		3120		1.04

		31.3		2630		1.03				31.7		2300		1.05				32.5		2560		1.07				31.7		2780		1.05				31.4		2290		1.03				31.8		3080		1.05				31.5		3120		1.04

		31.4		2640		1.04				31.8		2300		1.05				32.6		2570		1.08				31.8		2780		1.05				31.5		2290		1.04				31.8		3080		1.05				31.6		3130		1.05

		31.5		2640		1.04				31.9		2310		1.05				32.7		2570		1.08				31.9		2790		1.05				31.6		2290		1.04				31.9		3090		1.05				31.7		3140		1.05

		31.5		2640		1.04				31.9		2310		1.05				32.7		2570		1.08				31.9		2790		1.05				31.6		2300		1.04				32		3090		1.06				31.7		3140		1.05

		31.6		2650		1.04				32		2320		1.06				32.8		2580		1.08				32		2800		1.06				31.7		2300		1.04				32		3100		1.06				31.8		3150		1.05

		31.7		2650		1.04				32.1		2320		1.06				32.8		2580		1.08				32.1		2800		1.06				31.8		2310		1.04				32.1		3100		1.06				31.9		3150		1.05

		31.7		2660		1.05				32.2		2320		1.06				32.9		2590		1.09				32.1		2810		1.06				31.8		2310		1.05				32.1		3110		1.06				31.9		3160		1.06

		31.8		2660		1.05				32.2		2330		1.06				33		2590		1.09				32.2		2810		1.06				31.9		2310		1.05				32.2		3110		1.06				32		3160		1.06

		31.9		2670		1.05				32.3		2330		1.07				33		2600		1.09				32.3		2810		1.06				31.9		2320		1.05				32.3		3120		1.07				32		3170		1.06

		31.9		2670		1.05				32.4		2340		1.07				33.1		2600		1.09				32.3		2820		1.07				32.1		2320		1.06				32.4		3130		1.07				32.1		3180		1.06

		32		2680		1.06				32.4		2340		1.07				33.2		2610		1.1				32.4		2820		1.07				32.1		2330		1.06				32.5		3130		1.07				32.2		3180		1.07

		32.1		2680		1.06				32.5		2340		1.07				33.3		2610		1.1				32.5		2830		1.07				32.2		2330		1.06				32.5		3140		1.07				32.3		3190		1.07

		32.1		2680		1.06				32.6		2350		1.08				33.3		2610		1.1				32.5		2830		1.07				32.2		2340		1.06				32.6		3140		1.08				32.4		3190		1.07

		32.2		2690		1.06				32.6		2350		1.08				33.4		2620		1.1				32.6		2830		1.08				32.3		2340		1.06				32.6		3150		1.08				32.4		3200		1.07

		32.2		2690		1.06				32.7		2360		1.08				33.5		2620		1.1				32.7		2840		1.08				32.3		2340		1.07				32.7		3150		1.08				32.5		3200		1.07

		32.3		2700		1.07				32.8		2360		1.08				33.5		2630		1.11				32.7		2840		1.08				32.4		2350		1.07				32.8		3160		1.08				32.5		3210		1.08

		32.4		2700		1.07				32.9		2360		1.08				33.6		2630		1.11				32.8		2850		1.08				32.5		2350		1.07				32.9		3160		1.08				32.6		3220		1.08

		32.5		2700		1.07				32.9		2370		1.09				33.7		2640		1.11				32.8		2850		1.08				32.6		2360		1.07				32.9		3170		1.09				32.6		3220		1.08

		32.5		2710		1.07				32.9		2370		1.09				33.7		2640		1.11				32.9		2850		1.09				32.7		2360		1.08				33		3180		1.09				32.7		3230		1.08

		32.6		2720		1.08				33		2380		1.09				33.8		2650		1.12				33		2860		1.09				32.7		2370		1.08				33		3180		1.09				32.8		3230		1.09

		32.6		2720		1.08				33.1		2380		1.09				33.9		2650		1.12				33.1		2860		1.09				32.8		2370		1.08				33.1		3190		1.09				32.9		3240		1.09

		32.7		2720		1.08				33.2		2380		1.1				33.9		2660		1.12				33.1		2870		1.09				32.8		2370		1.08				33.2		3190		1.1				32.9		3250		1.09

		32.8		2730		1.08				33.2		2390		1.1				34		2660		1.12				33.2		2870		1.1				32.9		2380		1.08				33.3		3200		1.1				33		3250		1.09

		32.9		2730		1.08				33.3		2390		1.1				34.1		2660		1.12				33.2		2880		1.1				33		2380		1.09				33.3		3200		1.1				33		3260		1.09

		32.9		2740		1.09				33.4		2390		1.1				34.1		2670		1.13				33.3		2880		1.1				33		2380		1.09				33.4		3210		1.1				33.1		3260		1.1

		33		2740		1.09				33.4		2400		1.1				34.2		2680		1.13				33.4		2880		1.1				33.1		2390		1.09				33.4		3210		1.1				33.2		3270		1.1

		33		2740		1.09				33.5		2400		1.11				34.2		2680		1.13				33.5		2890		1.1				33.3		2390		1.09				33.5		3220		1.11				33.2		3270		1.1

		33.2		2750		1.09				33.5		2410		1.11				34.3		2680		1.13				33.5		2890		1.11				33.3		2400		1.1				33.6		3230		1.11				33.3		3280		1.1

		33.2		2760		1.1				33.6		2410		1.11				34.4		2690		1.14				33.6		2900		1.11				33.3		2400		1.1				33.7		3230		1.11				33.4		3290		1.11

		33.3		2760		1.1				33.7		2420		1.12				34.4		2690		1.14				33.7		2900		1.11				33.4		2410		1.1				33.8		3240		1.11				33.5		3290		1.11

		33.3		2770		1.1				33.8		2420		1.12				34.5		2700		1.14				33.8		2910		1.11				33.5		2410		1.1				33.8		3240		1.12				33.5		3300		1.11

		33.4		2770		1.1				33.9		2420		1.12				34.6		2700		1.14				33.8		2910		1.12				33.6		2410		1.11				33.9		3250		1.12				33.6		3300		1.11

		33.5		2770		1.1				33.9		2430		1.12				34.7		2710		1.14				33.9		2920		1.12				33.6		2420		1.11				34		3250		1.12				33.7		3310		1.11

		33.5		2780		1.11				34		2430		1.12				34.8		2720		1.15				33.9		2920		1.12				33.7		2420		1.11				34		3260		1.12				33.7		3310		1.12

		33.6		2780		1.11				34.1		2430		1.13				34.8		2720		1.15				34		2920		1.12				33.8		2430		1.11				34		3260		1.13				33.8		3320		1.12

		33.7		2790		1.11				34.1		2440		1.13				34.9		2720		1.15				34.1		2930		1.13				33.8		2430		1.11				34.1		3270		1.13				33.8		3320		1.12

		33.8		2790		1.11				34.2		2440		1.13				34.9		2730		1.15				34.2		2930		1.13				33.9		2430		1.12				34.2		3280		1.13				33.9		3330		1.12

		33.8		2800		1.12				34.3		2450		1.13				35		2730		1.16				34.2		2940		1.13				34		2440		1.12				34.3		3280		1.13				34		3340		1.12

		33.9		2800		1.12				34.3		2450		1.13				35.1		2740		1.16				34.3		2940		1.13				34		2440		1.12				34.3		3290		1.13				34.1		3340		1.13

		34		2810		1.12				34.4		2450		1.14				35.1		2740		1.16				34.4		2950		1.14				34.1		2450		1.12				34.4		3290		1.14				34.1		3350		1.13

		34		2810		1.12				34.4		2460		1.14				35.2		2740		1.16				34.5		2950		1.14				34.1		2450		1.12				34.5		3290		1.14				34.2		3350		1.13

		34.1		2820		1.12				34.5		2460		1.14				35.3		2750		1.17				34.5		2960		1.14				34.2		2450		1.13				34.5		3300		1.14				34.2		3360		1.13

		34.2		2820		1.13				34.6		2470		1.14				35.3		2750		1.17				34.6		2960		1.14				34.3		2460		1.13				34.6		3310		1.14				34.3		3360		1.14

		34.2		2820		1.13				34.7		2470		1.15				35.4		2760		1.17				34.6		2960		1.14				34.4		2470		1.13				34.7		3310		1.15				34.4		3370		1.14

		34.3		2830		1.13				34.7		2470		1.15				35.5		2760		1.17				34.7		2970		1.15				34.4		2470		1.14				34.7		3320		1.15				34.4		3370		1.14

		34.4		2840		1.14				34.8		2480		1.15				35.5		2770		1.17				34.8		2970		1.15				34.5		2470		1.14				34.8		3320		1.15				34.5		3380		1.14

		34.5		2840		1.14				34.8		2480		1.15				35.6		2770		1.18				34.9		2980		1.15				34.6		2480		1.14				34.9		3330		1.15				34.6		3390		1.15

		34.5		2850		1.14				34.9		2490		1.15				35.6		2780		1.18				34.9		2980		1.15				34.7		2480		1.14				35		3330		1.15				34.7		3400		1.15

		34.6		2850		1.14				35		2490		1.16				35.7		2780		1.18				35		2990		1.16				34.7		2490		1.14				35		3340		1.16				34.7		3400		1.15

		34.7		2860		1.14				35		2490		1.16				35.8		2790		1.18				35.1		2990		1.16				34.8		2490		1.15				35		3340		1.16				34.8		3410		1.15

		34.7		2860		1.15				35.1		2500		1.16				35.9		2790		1.19				35.1		2990		1.16				34.8		2490		1.15				35.1		3350		1.16				34.9		3410		1.15

		34.8		2860		1.15				35.2		2500		1.16				35.9		2790		1.19				35.2		3000		1.16				34.9		2500		1.15				35.2		3350		1.16				34.9		3420		1.16

		34.9		2870		1.15				35.2		2500		1.17				36		2800		1.19				35.2		3000		1.16				35		2510		1.15				35.2		3360		1.16				35		3420		1.16

		34.9		2880		1.15				35.3		2510		1.17				36.1		2800		1.19				35.3		3010		1.17				35.1		2510		1.16				35.4		3370		1.17				35		3430		1.16

		35		2880		1.16				35.4		2510		1.17				36.1		2810		1.19				35.4		3010		1.17				35.2		2510		1.16				35.5		3370		1.17				35.2		3440		1.16

		35.1		2890		1.16				35.4		2520		1.17				36.2		2810		1.2				35.5		3020		1.17				35.2		2520		1.16				35.5		3380		1.17				35.2		3440		1.17

		35.2		2890		1.16				35.5		2520		1.17				36.3		2810		1.2				35.5		3020		1.17				35.3		2520		1.16				35.5		3380		1.18				35.3		3450		1.17

		35.2		2900		1.16				35.6		2520		1.18				36.4		2820		1.2				35.6		3020		1.18				35.3		2520		1.16				35.6		3390		1.18				35.4		3460		1.17

		35.3		2900		1.16				35.6		2530		1.18				36.4		2830		1.2				35.7		3030		1.18				35.4		2530		1.17				35.7		3390		1.18				35.4		3460		1.17

		35.3		2910		1.17				35.7		2530		1.18				36.5		2830		1.21				35.7		3030		1.18				35.4		2530		1.17				35.7		3400		1.18				35.5		3470		1.17

		35.4		2910		1.17				35.8		2530		1.18				36.6		2830		1.21				35.8		3040		1.18				35.6		2540		1.17				35.8		3400		1.18				35.6		3470		1.18

		35.5		2920		1.17				35.8		2540		1.18				36.6		2840		1.21				35.9		3040		1.18				35.6		2540		1.17				35.9		3410		1.19				35.6		3480		1.18

		35.6		2920		1.17				35.9		2540		1.19				36.7		2840		1.21				35.9		3040		1.19				35.7		2550		1.18				35.9		3410		1.19				35.7		3480		1.18

		35.7		2930		1.18				35.9		2540		1.19				36.7		2850		1.22				36		3050		1.19				35.7		2550		1.18				36		3420		1.19				35.8		3490		1.18

		35.7		2930		1.18				36		2550		1.19				36.8		2850		1.22				36		3050		1.19				35.8		2550		1.18				36.1		3420		1.19				35.8		3500		1.19

		35.8		2940		1.18				36.1		2550		1.19				36.9		2860		1.22				36.1		3060		1.19				35.8		2560		1.18				36.1		3430		1.2				35.9		3500		1.19

		35.9		2940		1.18				36.2		2560		1.2				37		2860		1.22				36.2		3060		1.19				35.9		2560		1.18				36.2		3430		1.2				35.9		3510		1.19

		35.9		2940		1.19				36.3		2560		1.2				37.1		2870		1.23				36.2		3060		1.2				36		2560		1.19				36.3		3440		1.2				36		3510		1.19

		36		2950		1.19				36.3		2560		1.2				37.1		2870		1.23				36.3		3070		1.2				36.1		2570		1.19				36.3		3440		1.2				36.1		3520		1.19

		36		2960		1.19				36.3		2570		1.2				37.2		2880		1.23				36.4		3070		1.2				36.2		2570		1.19				36.4		3450		1.2				36.1		3520		1.2

		36.1		2960		1.19				36.4		2570		1.2				37.3		2880		1.23				36.4		3080		1.2				36.2		2580		1.19				36.5		3450		1.21				36.2		3530		1.2

		36.2		2960		1.19				36.5		2580		1.21				37.3		2880		1.23				36.5		3080		1.21				36.3		2580		1.2				36.6		3460		1.21				36.3		3540		1.2

		36.3		2970		1.2				36.6		2580		1.21				37.4		2890		1.24				36.6		3090		1.21				36.3		2590		1.2				36.6		3460		1.21				36.4		3540		1.21

		36.3		2970		1.2				36.7		2590		1.21				37.5		2900		1.24				36.7		3090		1.21				36.4		2590		1.2				36.7		3470		1.21				36.4		3550		1.21

		36.4		2980		1.2				36.8		2590		1.21				37.6		2900		1.24				36.7		3100		1.21				36.5		2590		1.2				36.8		3470		1.21				36.5		3550		1.21

		36.4		2980		1.2				36.8		2590		1.22				37.6		2900		1.24				36.8		3100		1.22				36.5		2600		1.2				36.8		3480		1.22				36.6		3560		1.21

		36.5		2990		1.21				36.8		2600		1.22				37.7		2910		1.25				36.8		3100		1.22				36.6		2600		1.21				36.9		3480		1.22				36.7		3560		1.21

		36.5		2990		1.21				36.9		2600		1.22				37.7		2910		1.25				36.9		3110		1.22				36.7		2610		1.21				36.9		3490		1.22				36.7		3570		1.22

		36.7		3000		1.21				37		2600		1.22				37.8		2920		1.25				37		3110		1.22				36.8		2610		1.21				37		3490		1.22				36.8		3570		1.22

		36.7		3000		1.21				37		2610		1.23				37.9		2920		1.25				37.1		3120		1.23				36.8		2620		1.21				37.1		3500		1.23				36.9		3580		1.22

		36.8		3010		1.22				37.2		2610		1.23				38		2920		1.25				37.2		3120		1.23				36.9		2620		1.22				37.2		3510		1.23				36.9		3590		1.22

		36.9		3010		1.22				37.2		2620		1.23				38.1		2930		1.26				37.2		3130		1.23				36.9		2630		1.22				37.3		3510		1.23				37		3590		1.23

		36.9		3020		1.22				37.3		2620		1.23				38.1		2930		1.26				37.3		3130		1.23				37		2630		1.22				37.3		3520		1.23				37.1		3600		1.23

		37		3020		1.22				37.3		2620		1.23				38.1		2940		1.26				37.3		3130		1.23				37.1		2630		1.22				37.4		3520		1.24				37.2		3610		1.23

		37.1		3020		1.22				37.4		2630		1.24				38.2		2940		1.26				37.4		3140		1.24				37.2		2640		1.23				37.4		3530		1.24				37.2		3610		1.23

		37.1		3030		1.23				37.4		2630		1.24				38.3		2950		1.27				37.5		3140		1.24				37.2		2640		1.23				37.5		3530		1.24				37.3		3620		1.23

		37.2		3030		1.23				37.5		2640		1.24				38.3		2950		1.27				37.5		3150		1.24				37.3		2650		1.23				37.5		3540		1.24				37.3		3620		1.24

		37.3		3040		1.23				37.6		2640		1.24				38.4		2950		1.27				37.7		3150		1.24				37.3		2650		1.23				37.6		3540		1.24				37.4		3630		1.24

		37.3		3040		1.23				37.7		2640		1.25				38.5		2960		1.27				37.7		3160		1.25				37.4		2660		1.23				37.7		3550		1.25				37.5		3630		1.24

		37.4		3050		1.24				37.7		2650		1.25				38.6		2960		1.28				37.8		3160		1.25				37.5		2660		1.24				37.8		3550		1.25				37.5		3640		1.24

		37.4		3050		1.24				37.8		2650		1.25				38.6		2970		1.28				37.9		3170		1.25				37.5		2660		1.24				37.8		3560		1.25				37.6		3650		1.25

		37.5		3060		1.24				37.8		2650		1.25				38.7		2970		1.28				37.9		3170		1.25				37.6		2670		1.24				37.9		3560		1.25				37.7		3650		1.25

		37.6		3060		1.24				37.9		2660		1.25				38.8		2980		1.28				38		3170		1.25				37.7		2670		1.24				37.9		3570		1.25				37.8		3660		1.25

		37.7		3060		1.24				38		2660		1.26				38.8		2980		1.28				38		3180		1.26				37.8		2680		1.25				38		3570		1.26				37.8		3660		1.25

		37.7		3070		1.25				38		2670		1.26				38.9		2980		1.29				38.1		3180		1.26				37.9		2680		1.25				38		3580		1.26				37.9		3670		1.25

		37.8		3070		1.25				38.1		2670		1.26				38.9		2990		1.29				38.2		3190		1.26				37.9		2690		1.25				38.1		3580		1.26				38		3680		1.26

		37.9		3080		1.25				38.2		2670		1.26				39		2990		1.29				38.2		3190		1.26				38		2690		1.25				38.2		3590		1.26				38		3680		1.26

		37.9		3080		1.25				38.2		2680		1.26				39.1		3000		1.29				38.3		3200		1.27				38		2690		1.26				38.3		3600		1.27				38.1		3690		1.26

		38		3090		1.25				38.3		2680		1.27				39.1		3000		1.3				38.4		3200		1.27				38.1		2700		1.26				38.4		3600		1.27				38.1		3690		1.26

		38.1		3090		1.26				38.4		2690		1.27				39.2		3010		1.3				38.5		3210		1.27				38.2		2700		1.26				38.4		3610		1.27				38.2		3700		1.27

		38.1		3100		1.26				38.5		2690		1.27				39.3		3010		1.3				38.5		3210		1.27				38.2		2700		1.26				38.5		3610		1.27				38.3		3700		1.27

		38.2		3100		1.26				38.5		2690		1.27				39.4		3010		1.3				38.6		3210		1.27				38.3		2710		1.27				38.5		3620		1.28				38.3		3710		1.27

		38.2		3100		1.26				38.6		2700		1.28				39.4		3020		1.3				38.6		3220		1.28				38.4		2720		1.27				38.6		3620		1.28				38.4		3710		1.27

		38.3		3110		1.27				38.7		2700		1.28				39.5		3020		1.31				38.7		3220		1.28				38.5		2720		1.27				38.7		3630		1.28				38.4		3720		1.27

		38.4		3110		1.27				38.7		2700		1.28				39.5		3030		1.31				38.8		3230		1.28				38.6		2720		1.27				38.8		3640		1.28				38.5		3730		1.28

		38.5		3120		1.27				38.7		2710		1.28				39.6		3030		1.31				38.9		3230		1.29				38.6		2730		1.27				38.9		3640		1.29				38.6		3730		1.28

		38.5		3120		1.27				38.8		2710		1.28				39.7		3040		1.31				38.9		3240		1.29				38.7		2730		1.28				38.9		3650		1.29				38.7		3740		1.28

		38.6		3130		1.27				38.9		2720		1.29				39.7		3040		1.32				39		3240		1.29				38.7		2730		1.28				39		3650		1.29				38.7		3740		1.28

		38.6		3130		1.28				39		2720		1.29				39.8		3040		1.32				39		3250		1.29				38.8		2740		1.28				39		3660		1.29				38.8		3750		1.29

		38.7		3130		1.28				39		2720		1.29				39.9		3050		1.32				39.1		3250		1.29				38.9		2750		1.28				39.1		3660		1.29				38.8		3750		1.29

		38.8		3140		1.28				39.1		2730		1.29				40		3050		1.32				39.2		3250		1.3				39		2750		1.29				39.2		3670		1.3				38.9		3760		1.29

		38.8		3140		1.28				39.2		2730		1.3				40		3060		1.32				39.2		3260		1.3				39.1		2750		1.29				39.2		3670		1.3				39		3760		1.29

		38.9		3150		1.28				39.2		2740		1.3				40.1		3060		1.33				39.3		3260		1.3				39.1		2760		1.29				39.4		3680		1.3				39		3770		1.29

		39		3150		1.29				39.3		2740		1.3				40.2		3070		1.33				39.4		3270		1.3				39.1		2760		1.29				39.4		3690		1.3				39.2		3780		1.3

		39.1		3160		1.29				39.3		2740		1.3				40.2		3070		1.33				39.4		3270		1.3				39.2		2760		1.29				39.5		3690		1.31				39.2		3790		1.3

		39.1		3160		1.29				39.4		2750		1.3				40.3		3080		1.33				39.5		3280		1.31				39.3		2770		1.3				39.5		3700		1.31				39.3		3790		1.3

		39.2		3170		1.3				39.5		2750		1.31				40.4		3080		1.33				39.6		3280		1.31				39.3		2770		1.3				39.6		3700		1.31				39.3		3800		1.3

		39.3		3170		1.3				39.6		2760		1.31				40.4		3080		1.34				39.7		3280		1.31				39.4		2780		1.3				39.7		3710		1.31				39.4		3800		1.31

		39.3		3180		1.3				39.6		2760		1.31				40.5		3090		1.34				39.7		3290		1.31				39.5		2780		1.31				39.8		3710		1.31				39.5		3810		1.31

		39.4		3180		1.3				39.7		2760		1.31				40.5		3090		1.34				39.8		3290		1.32				39.6		2790		1.31				39.8		3720		1.32				39.5		3810		1.31

		39.5		3180		1.3				39.7		2770		1.32				40.6		3100		1.34				39.9		3300		1.32				39.7		2790		1.31				39.9		3720		1.32				39.6		3820		1.31

		39.6		3190		1.31				39.8		2770		1.32				40.7		3100		1.35				39.9		3300		1.32				39.7		2790		1.31				39.9		3730		1.32				39.7		3820		1.31

		39.7		3200		1.31				39.9		2770		1.32				40.8		3110		1.35				40		3310		1.32				39.8		2800		1.31				40		3730		1.32				39.8		3830		1.32

		39.7		3200		1.31				40		2780		1.32				40.8		3110		1.35				40.1		3310		1.32				39.8		2800		1.32				40.1		3740		1.33				39.8		3840		1.32

		39.8		3210		1.31				40		2780		1.33				40.9		3120		1.35				40.1		3310		1.33				39.9		2800		1.32				40.1		3740		1.33				39.9		3840		1.32

		39.8		3210		1.32				40.1		2790		1.33				41		3120		1.36				40.2		3320		1.33				40		2810		1.32				40.2		3750		1.33				40		3850		1.32

		39.9		3210		1.32				40.2		2790		1.33				41		3120		1.36				40.2		3320		1.33				40.1		2810		1.32				40.3		3750		1.33				40		3850		1.33

		39.9		3220		1.32				40.2		2790		1.33				41.1		3130		1.36				40.3		3330		1.33				40.1		2820		1.32				40.3		3760		1.33				40.1		3860		1.33

		40		3220		1.32				40.3		2800		1.33				41.2		3130		1.36				40.4		3330		1.34				40.2		2820		1.33				40.4		3760		1.34				40.1		3860		1.33

		40.1		3230		1.33				40.4		2800		1.34				41.3		3140		1.37				40.5		3340		1.34				40.2		2830		1.33				40.5		3770		1.34				40.2		3870		1.33

		40.2		3230		1.33				40.4		2810		1.34				41.3		3140		1.37				40.5		3340		1.34				40.3		2830		1.33				40.6		3780		1.34				40.3		3880		1.34

		40.2		3240		1.33				40.5		2810		1.34				41.4		3150		1.37				40.6		3340		1.34				40.4		2830		1.33				40.6		3780		1.34				40.4		3880		1.34

		40.3		3240		1.33				40.6		2820		1.34				41.5		3150		1.37				40.7		3350		1.34				40.5		2840		1.34				40.7		3790		1.35				40.4		3890		1.34

		40.4		3240		1.33				40.7		2820		1.34				41.5		3160		1.37				40.7		3350		1.35				40.5		2840		1.34				40.7		3790		1.35				40.5		3900		1.34

		40.4		3250		1.34				40.7		2820		1.35				41.6		3160		1.38				40.8		3360		1.35				40.6		2840		1.34				40.8		3800		1.35				40.6		3900		1.34

		40.5		3250		1.34				40.7		2830		1.35				41.7		3160		1.38				40.8		3360		1.35				40.7		2850		1.34				40.8		3800		1.35				40.6		3910		1.35

		40.6		3260		1.34				40.8		2830		1.35				41.7		3170		1.38				40.9		3360		1.35				40.8		2860		1.35				40.9		3810		1.35				40.7		3910		1.35

		40.7		3260		1.34				40.9		2830		1.35				41.8		3170		1.38				41		3370		1.36				40.8		2860		1.35				41		3810		1.36				40.7		3920		1.35

		40.7		3270		1.35				41		2840		1.36				41.9		3180		1.39				41.1		3370		1.36				40.9		2860		1.35				41		3820		1.36				40.9		3930		1.35

		40.8		3270		1.35				41		2840		1.36				41.9		3180		1.39				41.1		3380		1.36				41		2870		1.35				41.1		3820		1.36				41		3930		1.36

		40.9		3280		1.35				41.1		2850		1.36				42		3190		1.39				41.2		3380		1.36				41		2870		1.35				41.2		3830		1.36				41		3940		1.36

		40.9		3280		1.35				41.2		2850		1.36				42.1		3190		1.39				41.2		3390		1.36				41.1		2870		1.36				41.3		3830		1.36				41.1		3940		1.36

		41		3280		1.35				41.2		2850		1.36				42.1		3200		1.39				41.3		3390		1.37				41.1		2880		1.36				41.3		3840		1.37				41.1		3950		1.36

		41.1		3290		1.36				41.3		2860		1.37				42.2		3200		1.4				41.4		3390		1.37				41.2		2880		1.36				41.3		3840		1.37				41.2		3960		1.37

		41.1		3290		1.36				41.3		2860		1.37				42.2		3200		1.4				41.4		3400		1.37				41.3		2890		1.36				41.4		3850		1.37				41.2		3960		1.37

		41.2		3300		1.36				41.4		2870		1.37				42.3		3210		1.4				41.5		3410		1.37				41.3		2890		1.37				41.5		3850		1.37				41.3		3970		1.37

		41.3		3300		1.36				41.5		2870		1.37				42.4		3210		1.4				41.6		3410		1.38				41.4		2890		1.37				41.6		3860		1.38				41.5		3980		1.37

		41.4		3310		1.37				41.6		2870		1.37				42.4		3220		1.41				41.7		3410		1.38				41.5		2900		1.37				41.7		3870		1.38				41.5		3980		1.38

		41.4		3310		1.37				41.6		2880		1.38				42.5		3220		1.41				41.7		3420		1.38				41.6		2900		1.37				41.7		3870		1.38				41.6		3990		1.38

		41.5		3320		1.37				41.7		2880		1.38				42.6		3230		1.41				41.8		3420		1.38				41.6		2900		1.37				41.8		3880		1.38				41.6		3990		1.38

		41.6		3320		1.37				41.8		2880		1.38				42.6		3230		1.41				41.9		3430		1.38				41.7		2910		1.38				41.8		3880		1.39				41.7		4000		1.38

		41.6		3320		1.38				41.8		2890		1.38				42.7		3230		1.41				41.9		3430		1.39				41.7		2910		1.38				41.9		3890		1.39				41.7		4010		1.38

		41.7		3330		1.38				41.9		2890		1.39				42.8		3240		1.42				42		3440		1.39				41.8		2920		1.38				42		3890		1.39				41.8		4010		1.39

		41.7		3330		1.38				41.9		2900		1.39				42.8		3240		1.42				42.1		3440		1.39				41.9		2920		1.38				42		3900		1.39				41.9		4020		1.39

		41.9		3340		1.38				42		2900		1.39				42.9		3250		1.42				42.2		3450		1.39				41.9		2920		1.39				42.2		3910		1.4				42		4030		1.39

		41.9		3340		1.39				42.1		2900		1.39				43		3250		1.42				42.2		3450		1.4				42		2930		1.39				42.2		3910		1.4				42.1		4030		1.39

		42		3350		1.39				42.2		2910		1.4				43.1		3260		1.43				42.3		3460		1.4				42.1		2930		1.39				42.3		3920		1.4				42.1		4040		1.4

		42		3350		1.39				42.2		2910		1.4				43.1		3260		1.43				42.4		3460		1.4				42.1		2930		1.39				42.4		3920		1.4				42.2		4040		1.4

		42.1		3360		1.39				42.3		2920		1.4				43.2		3270		1.43				42.4		3470		1.4				42.2		2940		1.39				42.4		3930		1.4				42.2		4050		1.4

		42.2		3360		1.39				42.4		2920		1.4				43.3		3270		1.43				42.4		3470		1.4				42.2		2940		1.4				42.5		3930		1.41				42.3		4050		1.4

		42.2		3360		1.4				42.5		2920		1.41				43.3		3270		1.43				42.5		3470		1.41				42.3		2950		1.4				42.5		3940		1.41				42.4		4060		1.4

		42.3		3370		1.4				42.5		2930		1.41				43.4		3280		1.44				42.6		3480		1.41				42.5		2950		1.4				42.6		3940		1.41				42.4		4060		1.41

		42.4		3380		1.4				42.6		2930		1.41				43.5		3280		1.44				42.7		3490		1.41				42.5		2960		1.4				42.7		3950		1.41				42.5		4070		1.41

		42.5		3380		1.4				42.6		2940		1.41				43.5		3290		1.44				42.8		3490		1.42				42.6		2960		1.41				42.8		3950		1.42				42.6		4080		1.41

		42.6		3380		1.41				42.7		2940		1.41				43.7		3290		1.45				42.9		3500		1.42				42.6		2960		1.41				42.8		3960		1.42				42.7		4080		1.41

		42.6		3390		1.41				42.8		2940		1.42				43.7		3300		1.45				42.9		3500		1.42				42.7		2970		1.41				42.9		3960		1.42				42.7		4090		1.42

		42.7		3390		1.41				42.8		2950		1.42				43.8		3300		1.45				42.9		3500		1.42				42.8		2970		1.41				42.9		3970		1.42				42.8		4090		1.42

		42.7		3400		1.41				42.9		2950		1.42				43.8		3310		1.45				43		3510		1.42				42.8		2970		1.41				43		3970		1.42				42.8		4100		1.42

		42.8		3400		1.41				43		2960		1.42				43.9		3310		1.45				43.1		3510		1.43				42.9		2980		1.42				43.1		3980		1.43				42.9		4100		1.42

		42.8		3400		1.42				43		2960		1.42				44		3310		1.46				43.2		3520		1.43				43		2980		1.42				43.2		3980		1.43				42.9		4110		1.42

		43		3410		1.42				43.1		2960		1.43				44		3320		1.46				43.3		3530		1.43				43		2990		1.42				43.3		3990		1.43				43		4110		1.43

		43		3420		1.42				43.2		2970		1.43				44.1		3320		1.46				43.3		3530		1.43				43.1		2990		1.42				43.3		4000		1.43				43.1		4120		1.43

		43.1		3420		1.43				43.3		2970		1.43				44.2		3330		1.46				43.4		3530		1.44				43.2		3000		1.43				43.4		4000		1.44				43.2		4130		1.43

		43.2		3420		1.43				43.3		2970		1.43				44.3		3330		1.47				43.4		3540		1.44				43.3		3000		1.43				43.5		4010		1.44				43.2		4130		1.43

		43.2		3430		1.43				43.4		2980		1.44				44.3		3340		1.47				43.5		3540		1.44				43.3		3000		1.43				43.5		4010		1.44				43.3		4140		1.44

		43.3		3430		1.43				43.5		2980		1.44				44.4		3340		1.47				43.6		3550		1.44				43.4		3010		1.43				43.6		4020		1.44				43.4		4140		1.44

		43.4		3440		1.43				43.5		2990		1.44				44.5		3340		1.47				43.7		3550		1.44				43.4		3010		1.44				43.6		4020		1.44				43.4		4150		1.44

		43.4		3440		1.44				43.6		2990		1.44				44.5		3350		1.47				43.7		3550		1.45				43.5		3020		1.44				43.7		4030		1.45				43.5		4150		1.44

		43.5		3450		1.44				43.6		2990		1.44				44.6		3350		1.48				43.8		3560		1.45				43.6		3020		1.44				43.8		4030		1.45				43.5		4160		1.44

		43.6		3450		1.44				43.7		3000		1.45				44.6		3360		1.48				43.9		3570		1.45				43.7		3030		1.44				43.9		4040		1.45				43.6		4170		1.45

		43.7		3460		1.44				43.8		3000		1.45				44.7		3360		1.48				43.9		3570		1.45				43.7		3030		1.45				43.9		4050		1.45				43.7		4170		1.45

		43.7		3460		1.45				43.8		3000		1.45				44.8		3370		1.48				44		3570		1.46				43.8		3030		1.45				44		4060		1.46				43.8		4180		1.45

		43.7		3460		1.45				43.9		3010		1.45				44.9		3370		1.49				44.1		3580		1.46				43.9		3040		1.45				44.1		4060		1.46				43.8		4190		1.45

		43.8		3470		1.45				43.9		3010		1.45				44.9		3380		1.49				44.1		3580		1.46				44		3040		1.45				44.1		4070		1.46				43.9		4190		1.45

		43.9		3470		1.45				44		3010		1.46				45		3380		1.49				44.2		3590		1.46				44		3040		1.45				44.2		4070		1.46				43.9		4200		1.46

		43.9		3470		1.45				44.1		3020		1.46				45		3380		1.49				44.3		3590		1.47				44.1		3050		1.46				44.2		4080		1.47				44		4200		1.46

		44		3480		1.46				44.1		3020		1.46				45.1		3390		1.49				44.3		3600		1.47				44.2		3050		1.46				44.3		4080		1.47				44.1		4210		1.46

		44.1		3490		1.46				44.2		3020		1.46				45.2		3390		1.5				44.4		3600		1.47				44.2		3060		1.46				44.4		4090		1.47				44.1		4210		1.46

		44.2		3490		1.46				44.2		3030		1.47				45.2		3400		1.5				44.5		3600		1.47				44.3		3060		1.46				44.5		4090		1.47				44.2		4220		1.47

		44.2		3490		1.46				44.3		3030		1.47				45.3		3400		1.5				44.5		3610		1.47				44.4		3070		1.47				44.6		4100		1.47				44.3		4220		1.47

		44.3		3500		1.46				44.4		3040		1.47				45.4		3410		1.5				44.6		3610		1.48				44.4		3070		1.47				44.6		4100		1.48				44.3		4230		1.47

		44.3		3500		1.47				44.5		3040		1.47				45.5		3410		1.51				44.7		3620		1.48				44.5		3070		1.47				44.7		4110		1.48				44.4		4240		1.47

		44.4		3510		1.47				44.6		3050		1.48				45.5		3410		1.51				44.7		3620		1.48				44.6		3080		1.47				44.7		4110		1.48				44.5		4240		1.47

		44.5		3510		1.47				44.6		3050		1.48				45.6		3420		1.51				44.8		3630		1.48				44.7		3090		1.48				44.8		4120		1.48				44.5		4250		1.48

		44.6		3510		1.47				44.7		3050		1.48				45.6		3420		1.51				44.9		3630		1.49				44.7		3090		1.48				44.8		4120		1.49				44.6		4250		1.48

		44.7		3520		1.48				44.8		3060		1.48				45.7		3430		1.51				45		3640		1.49				44.8		3100		1.48				44.9		4130		1.49				44.6		4260		1.48

		44.7		3530		1.48				44.8		3060		1.48				45.8		3430		1.52				45		3640		1.49				44.9		3100		1.48				45.1		4140		1.49				44.7		4260		1.48

		44.8		3530		1.48				44.9		3070		1.49				45.8		3440		1.52				45.1		3640		1.49				45		3100		1.49				45.1		4140		1.49				44.8		4270		1.48

		44.9		3530		1.48				45		3070		1.49				45.9		3440		1.52				45.1		3650		1.49				45		3110		1.49				45.2		4150		1.5				44.9		4280		1.49

		44.9		3540		1.49				45		3080		1.49				46		3450		1.52				45.2		3650		1.5				45		3110		1.49				45.2		4150		1.5				45		4290		1.49

		45		3540		1.49				45.1		3080		1.49				46.1		3450		1.53				45.3		3660		1.5				45.1		3120		1.49				45.3		4160		1.5				45		4290		1.49

		45.1		3550		1.49				45.2		3080		1.5				46.2		3460		1.53				45.3		3660		1.5				45.2		3120		1.49				45.4		4160		1.5				45.1		4300		1.5

		45.1		3550		1.49				45.2		3090		1.5				46.2		3460		1.53				45.4		3670		1.5				45.3		3120		1.5				45.4		4170		1.5				45.1		4300		1.5

		45.2		3560		1.49				45.3		3090		1.5				46.3		3460		1.53				45.5		3670		1.51				45.3		3130		1.5				45.5		4170		1.51				45.2		4310		1.5

		45.3		3560		1.5				45.4		3090		1.5				46.3		3470		1.53				45.6		3680		1.51				45.4		3130		1.5				45.6		4180		1.51				45.3		4310		1.5

		45.3		3560		1.5				45.4		3100		1.5				46.4		3470		1.54				45.6		3680		1.51				45.5		3140		1.5				45.6		4180		1.51				45.3		4320		1.5

		45.4		3570		1.5				45.5		3100		1.51				46.4		3480		1.54				45.7		3680		1.51				45.5		3140		1.5				45.7		4190		1.51				45.5		4330		1.51

		45.5		3570		1.5				45.5		3100		1.51				46.6		3480		1.54				45.7		3690		1.51				45.6		3140		1.51				45.7		4190		1.51				45.5		4340		1.51

		45.5		3580		1.51				45.6		3110		1.51				46.6		3490		1.54				45.8		3690		1.52				45.7		3150		1.51				45.8		4200		1.52				45.6		4340		1.51

		45.6		3580		1.51				45.7		3110		1.51				46.7		3490		1.55				45.8		3700		1.52				45.8		3150		1.51				45.9		4200		1.52				45.6		4350		1.51

		45.6		3590		1.51				45.7		3120		1.52				46.8		3500		1.55				45.9		3700		1.52				45.8		3160		1.52				45.9		4210		1.52				45.7		4350		1.52

		45.8		3590		1.51				45.8		3120		1.52				46.8		3500		1.55				46		3710		1.52				45.9		3160		1.52				46		4210		1.52				45.8		4360		1.52

		45.8		3600		1.52				45.9		3120		1.52				46.9		3510		1.55				46.1		3710		1.53				46		3170		1.52				46.1		4220		1.52				45.9		4360		1.52

		45.9		3600		1.52				46		3130		1.52				47		3510		1.56				46.2		3720		1.53				46		3170		1.52				46.1		4220		1.53				45.9		4370		1.52

		45.9		3610		1.52				46		3130		1.52				47		3510		1.56				46.2		3720		1.53				46.1		3170		1.52				46.2		4230		1.53				46		4380		1.53

		46		3610		1.52				46.1		3130		1.53				47.1		3520		1.56				46.3		3730		1.53				46.1		3180		1.53				46.2		4230		1.53				46.1		4380		1.53

		46.1		3610		1.52				46.2		3140		1.53				47.2		3530		1.56				46.4		3730		1.53				46.2		3180		1.53				46.3		4240		1.53				46.1		4390		1.53

		46.1		3620		1.53				46.2		3140		1.53				47.3		3530		1.57				46.4		3730		1.54				46.3		3190		1.53				46.4		4240		1.54				46.2		4400		1.53

		46.2		3620		1.53				46.3		3150		1.53				47.3		3540		1.57				46.5		3740		1.54				46.4		3190		1.53				46.4		4250		1.54				46.2		4400		1.53

		46.3		3630		1.53				46.3		3150		1.53				47.4		3540		1.57				46.6		3750		1.54				46.4		3190		1.54				46.5		4250		1.54				46.3		4410		1.54

		46.3		3630		1.53				46.4		3150		1.54				47.4		3540		1.57				46.7		3750		1.55				46.5		3200		1.54				46.6		4260		1.54				46.4		4410		1.54

		46.4		3640		1.54				46.5		3160		1.54				47.5		3550		1.57				46.8		3750		1.55				46.6		3200		1.54				46.6		4260		1.54				46.5		4420		1.54

		46.5		3640		1.54				46.5		3160		1.54				47.6		3550		1.58				46.8		3760		1.55				46.6		3210		1.54				46.8		4270		1.55				46.6		4430		1.54

		46.6		3640		1.54				46.6		3160		1.54				47.7		3560		1.58				46.8		3760		1.55				46.7		3210		1.54				46.8		4280		1.55				46.6		4440		1.55

		46.6		3650		1.54				46.6		3170		1.55				47.8		3560		1.58				46.9		3770		1.55				46.7		3210		1.55				46.9		4280		1.55				46.7		4440		1.55

		46.7		3650		1.54				46.7		3170		1.55				47.8		3570		1.58				47		3770		1.56				46.8		3220		1.55				46.9		4290		1.55				46.8		4450		1.55

		46.7		3660		1.55				46.8		3180		1.55				47.9		3570		1.59				47		3770		1.56				46.9		3220		1.55				47		4290		1.56				46.8		4450		1.55

		46.8		3660		1.55				46.8		3180		1.55				47.9		3580		1.59				47.2		3780		1.56				46.9		3230		1.55				47.1		4300		1.56				46.9		4460		1.55

		46.9		3660		1.55				46.9		3180		1.55				48		3580		1.59				47.2		3780		1.56				47		3230		1.55				47.1		4300		1.56				47		4460		1.56

		47		3670		1.55				47		3190		1.56				48.1		3580		1.59				47.3		3790		1.57				47.1		3230		1.56				47.2		4310		1.56				47		4470		1.56

		47.1		3680		1.56				47		3190		1.56				48.1		3590		1.59				47.3		3790		1.57				47.2		3240		1.56				47.3		4310		1.57				47.1		4480		1.56

		47.1		3680		1.56				47.1		3190		1.56				48.2		3590		1.6				47.4		3800		1.57				47.2		3240		1.56				47.4		4320		1.57				47.1		4480		1.56

		47.2		3680		1.56				47.1		3200		1.56				48.3		3600		1.6				47.4		3800		1.57				47.3		3250		1.56				47.5		4330		1.57				47.2		4490		1.57

		47.2		3690		1.56				47.2		3200		1.56				48.4		3610		1.6				47.5		3810		1.57				47.3		3250		1.57				47.5		4330		1.57				47.3		4500		1.57

		47.3		3690		1.56				47.4		3210		1.57				48.5		3610		1.61				47.6		3810		1.58				47.4		3250		1.57				47.6		4340		1.58				47.3		4500		1.57

		47.4		3700		1.57				47.4		3210		1.57				48.5		3610		1.61				47.7		3810		1.58				47.5		3260		1.57				47.6		4340		1.58				47.4		4510		1.57

		47.4		3700		1.57				47.5		3210		1.57				48.6		3620		1.61				47.7		3820		1.58				47.6		3260		1.57				47.7		4350		1.58				47.5		4510		1.57

		47.5		3700		1.57				47.5		3220		1.57				48.6		3620		1.61				47.8		3820		1.58				47.6		3270		1.58				47.8		4350		1.58				47.5		4520		1.58

		47.6		3710		1.58				47.6		3220		1.58				48.7		3630		1.61				47.9		3830		1.58				47.7		3270		1.58				47.8		4360		1.58				47.6		4520		1.58

		47.7		3720		1.58				47.6		3230		1.58				48.8		3630		1.62				47.9		3830		1.59				47.8		3280		1.58				47.9		4370		1.59				47.7		4530		1.58

		47.7		3720		1.58				47.7		3230		1.58				48.8		3640		1.62				48		3840		1.59				47.8		3280		1.58				48		4370		1.59				47.8		4540		1.58

		47.8		3720		1.58				47.8		3230		1.58				48.9		3640		1.62				48.1		3840		1.59				47.9		3280		1.58				48.1		4380		1.59				47.8		4540		1.59

		47.8		3730		1.58				47.9		3240		1.59				49		3650		1.62				48.1		3840		1.59				47.9		3290		1.59				48.1		4380		1.59				47.9		4550		1.59

		47.9		3730		1.59				48		3240		1.59				49.1		3650		1.62				48.2		3850		1.6				48		3290		1.59				48.2		4390		1.6				48		4560		1.59

		48		3740		1.59				48		3250		1.59				49.1		3650		1.63				48.3		3850		1.6				48.1		3300		1.59				48.3		4390		1.6				48		4560		1.59

		48.1		3740		1.59				48.1		3250		1.59				49.2		3660		1.63				48.3		3860		1.6				48.2		3300		1.59				48.3		4400		1.6				48.1		4570		1.59

		48.1		3750		1.59				48.1		3250		1.6				49.3		3660		1.63				48.4		3860		1.6				48.3		3310		1.6				48.4		4400		1.6				48.1		4570		1.6

		48.2		3750		1.6				48.2		3260		1.6				49.3		3670		1.63				48.5		3870		1.6				48.4		3310		1.6				48.5		4410		1.61				48.2		4580		1.6

		48.3		3760		1.6				48.3		3260		1.6				49.3		3670		1.64				48.5		3870		1.61				48.4		3310		1.6				48.6		4420		1.61				48.3		4590		1.6

		48.4		3760		1.6				48.3		3260		1.6				49.5		3680		1.64				48.6		3880		1.61				48.4		3320		1.6				48.6		4420		1.61				48.3		4590		1.6

		48.4		3770		1.6				48.5		3270		1.61				49.5		3680		1.64				48.7		3880		1.61				48.5		3320		1.6				48.7		4430		1.61				48.4		4600		1.61

		48.5		3770		1.6				48.5		3270		1.61				49.6		3680		1.64				48.8		3890		1.61				48.6		3330		1.61				48.7		4430		1.61				48.5		4600		1.61

		48.6		3780		1.61				48.6		3280		1.61				49.6		3690		1.64				48.8		3890		1.62				48.7		3330		1.61				48.8		4440		1.62				48.5		4610		1.61

		48.6		3780		1.61				48.6		3280		1.61				49.7		3690		1.65				48.9		3900		1.62				48.8		3340		1.61				48.8		4440		1.62				48.6		4610		1.61

		48.6		3780		1.61				48.7		3290		1.61				49.8		3700		1.65				49		3900		1.62				48.8		3340		1.61				48.9		4450		1.62				48.7		4620		1.61

		48.7		3790		1.61				48.8		3290		1.62				49.8		3700		1.65				49		3900		1.62				48.9		3340		1.62				49		4450		1.62				48.7		4620		1.62

		48.8		3790		1.62				48.8		3290		1.62				49.9		3710		1.65				49.1		3910		1.63				48.9		3350		1.62				49.1		4460		1.63				48.8		4630		1.62

		48.9		3800		1.62				48.9		3300		1.62				50		3710		1.66				49.2		3910		1.63				49		3350		1.62				49.1		4460		1.63				48.9		4640		1.62

		48.9		3800		1.62				49		3300		1.62				50		3720		1.66				49.2		3920		1.63				49.1		3350		1.62				49.2		4470		1.63				48.9		4640		1.62

		49		3810		1.62				49.1		3310		1.63				50.1		3720		1.66				49.3		3920		1.63				49.1		3360		1.62				49.2		4470		1.63				49		4650		1.63

		49		3810		1.62				49.1		3310		1.63				50.2		3720		1.66				49.4		3930		1.64				49.2		3360		1.63				49.3		4480		1.63				49		4650		1.63

		49.1		3820		1.63				49.2		3310		1.63				50.2		3730		1.66				49.5		3930		1.64				49.3		3370		1.63				49.4		4480		1.64				49.1		4660		1.63

		49.2		3820		1.63				49.3		3320		1.63				50.3		3730		1.67				49.5		3940		1.64				49.3		3370		1.63				49.4		4490		1.64				49.2		4670		1.63

		49.3		3830		1.63				49.4		3320		1.64				50.4		3740		1.67				49.6		3940		1.64				49.4		3370		1.63				49.5		4490		1.64				49.2		4670		1.63

		49.4		3830		1.63				49.4		3320		1.64				50.4		3740		1.67				49.7		3940		1.64				49.4		3380		1.63				49.6		4500		1.64				49.3		4680		1.64

		49.5		3840		1.64				49.5		3330		1.64				50.5		3740		1.67				49.7		3950		1.65				49.5		3380		1.64				49.7		4510		1.65				49.4		4680		1.64

		49.5		3840		1.64				49.6		3340		1.64				50.6		3750		1.68				49.8		3950		1.65				49.5		3390		1.64				49.7		4510		1.65				49.5		4690		1.64

		49.6		3850		1.64				49.6		3340		1.65				50.7		3760		1.68				49.8		3960		1.65				49.6		3390		1.64				49.8		4520		1.65				49.5		4700		1.64

		49.6		3850		1.64				49.7		3340		1.65				50.7		3760		1.68				50		3960		1.65				49.7		3390		1.64				49.9		4520		1.65				49.6		4700		1.65

		49.7		3860		1.64				49.8		3350		1.65				50.8		3770		1.68				50		3970		1.66				49.7		3400		1.65				50		4530		1.65				49.6		4710		1.65

		49.8		3860		1.65				49.8		3350		1.65				50.8		3770		1.69				50.1		3970		1.66				49.9		3400		1.65				50		4530		1.66				49.7		4710		1.65

		49.9		3870		1.65				49.9		3350		1.65				50.9		3770		1.69				50.2		3980		1.66				49.9		3410		1.65				50.1		4540		1.66				49.8		4720		1.65

		49.9		3870		1.65				50		3360		1.66				51		3780		1.69				50.2		3980		1.66				50		3410		1.65				50.1		4540		1.66				49.8		4720		1.65

		50		3870		1.65				50		3360		1.66				51.1		3780		1.69				50.3		3990		1.66				50		3420		1.66				50.2		4550		1.66				49.9		4730		1.66

		50		3880		1.66				50.2		3370		1.66				51.1		3790		1.69				50.3		3990		1.67				50.1		3420		1.66				50.3		4550		1.67				50		4740		1.66

		50.1		3880		1.66				50.2		3370		1.66				51.2		3790		1.7				50.4		3990		1.67				50.2		3420		1.66				50.3		4560		1.67				50.1		4750		1.66

		50.2		3890		1.66				50.3		3380		1.67				51.3		3800		1.7				50.5		4000		1.67				50.2		3430		1.66				50.4		4560		1.67				50.1		4750		1.66

		50.2		3890		1.66				50.3		3380		1.67				51.3		3800		1.7				50.6		4010		1.68				50.3		3430		1.66				50.5		4570		1.67				50.2		4760		1.67

		50.3		3900		1.66				50.4		3380		1.67				51.4		3800		1.7				50.7		4010		1.68				50.4		3440		1.67				50.6		4570		1.67				50.3		4770		1.67

		50.4		3900		1.67				50.4		3390		1.67				51.5		3810		1.7				50.7		4010		1.68				50.5		3440		1.67				50.6		4580		1.68				50.3		4770		1.67

		50.5		3910		1.67				50.5		3390		1.67				51.5		3810		1.71				50.7		4020		1.68				50.5		3440		1.67				50.6		4580		1.68				50.4		4780		1.67

		50.5		3910		1.67				50.6		3390		1.68				51.6		3820		1.71				50.8		4020		1.68				50.6		3450		1.67				50.7		4590		1.68				50.5		4780		1.67

		50.6		3910		1.67				50.7		3400		1.68				51.6		3820		1.71				50.9		4030		1.69				50.6		3450		1.68				50.8		4600		1.68				50.5		4790		1.68

		50.6		3920		1.68				50.8		3400		1.68				51.8		3830		1.72				51		4030		1.69				50.7		3460		1.68				50.9		4600		1.69				50.7		4800		1.68

		50.7		3920		1.68				50.8		3410		1.68				51.8		3830		1.72				51.1		4040		1.69				50.8		3460		1.68				50.9		4610		1.69				50.7		4800		1.68

		50.8		3930		1.68				50.9		3410		1.69				51.9		3840		1.72				51.1		4040		1.69				50.8		3460		1.68				51		4610		1.69				50.8		4810		1.68

		50.8		3930		1.68				50.9		3410		1.69				52		3840		1.72				51.2		4050		1.7				50.9		3470		1.68				51.1		4620		1.69				50.8		4820		1.69

		51		3940		1.69				51		3420		1.69				52		3850		1.72				51.2		4050		1.7				51		3470		1.69				51.1		4620		1.69				50.9		4820		1.69

		51		3940		1.69				51.1		3420		1.69				52.1		3850		1.73				51.3		4050		1.7				51.1		3480		1.69				51.2		4630		1.7				51		4830		1.69

		51		3950		1.69				51.1		3420		1.69				52.1		3850		1.73				51.4		4060		1.7				51.1		3480		1.69				51.2		4630		1.7				51		4830		1.69

		51.1		3950		1.69				51.2		3430		1.7				52.2		3860		1.73				51.5		4060		1.7				51.2		3490		1.69				51.3		4640		1.7				51.1		4840		1.69

		51.2		3950		1.69				51.3		3430		1.7				52.3		3870		1.73				51.5		4070		1.71				51.3		3490		1.7				51.4		4640		1.7				51.1		4840		1.7

		51.3		3960		1.7				51.3		3440		1.7				52.3		3870		1.73				51.6		4080		1.71				51.3		3490		1.7				51.5		4650		1.71				51.3		4860		1.7

		51.3		3960		1.7				51.4		3440		1.7				52.4		3870		1.74				51.7		4080		1.71				51.4		3500		1.7				51.5		4650		1.71				51.3		4860		1.7

		51.4		3970		1.7				51.5		3440		1.71				52.5		3880		1.74				51.7		4080		1.71				51.4		3500		1.7				51.6		4660		1.71				51.4		4870		1.71

		51.5		3970		1.71				51.5		3450		1.71				52.6		3880		1.74				51.8		4090		1.72				51.5		3510		1.7				51.7		4660		1.71				51.5		4870		1.71

		51.5		3980		1.71				51.6		3450		1.71				52.6		3890		1.74				51.9		4090		1.72				51.6		3510		1.71				51.7		4670		1.71				51.5		4880		1.71

		51.6		3980		1.71				51.6		3460		1.71				52.7		3890		1.75				52		4090		1.72				51.7		3520		1.71				51.8		4670		1.72				51.6		4880		1.71

		51.7		3990		1.71				51.7		3460		1.71				52.7		3890		1.75				52		4100		1.72				51.7		3520		1.71				51.9		4680		1.72				51.6		4890		1.71

		51.8		3990		1.71				51.8		3470		1.72				52.8		3900		1.75				52.1		4100		1.73				51.8		3520		1.71				52		4690		1.72				51.7		4900		1.72

		51.8		4000		1.72				51.9		3470		1.72				52.9		3910		1.75				52.2		4110		1.73				51.8		3530		1.72				52		4690		1.72				51.8		4910		1.72

		51.9		4000		1.72				51.9		3470		1.72				53		3910		1.76				52.2		4110		1.73				51.9		3530		1.72				52.1		4700		1.73				51.9		4910		1.72

		52		4000		1.72				52		3480		1.72				53		3910		1.76				52.3		4120		1.73				52		3540		1.72				52.1		4700		1.73				52		4920		1.72

		52		4010		1.72				52.1		3480		1.73				53.1		3920		1.76				52.3		4120		1.73				52.1		3540		1.72				52.2		4710		1.73				52		4920		1.73

		52.1		4020		1.73				52.2		3490		1.73				53.2		3920		1.76				52.4		4130		1.74				52.2		3550		1.73				52.3		4710		1.73				52.1		4930		1.73

		52.2		4020		1.73				52.2		3490		1.73				53.2		3930		1.76				52.5		4130		1.74				52.2		3550		1.73				52.4		4720		1.73				52.1		4940		1.73

		52.3		4020		1.73				52.3		3490		1.73				53.3		3930		1.77				52.6		4130		1.74				52.3		3550		1.73				52.4		4720		1.74				52.2		4940		1.73

		52.3		4030		1.73				52.4		3500		1.74				53.3		3940		1.77				52.6		4140		1.74				52.3		3560		1.73				52.5		4730		1.74				52.3		4950		1.73

		52.4		4030		1.73				52.4		3500		1.74				53.5		3950		1.77				52.6		4140		1.75				52.4		3560		1.73				52.5		4740		1.74				52.4		4960		1.74

		52.5		4040		1.74				52.5		3510		1.74				53.5		3950		1.77				52.7		4140		1.75				52.5		3560		1.74				52.6		4740		1.74				52.4		4960		1.74

		52.5		4040		1.74				52.6		3510		1.74				53.6		3950		1.78				52.8		4150		1.75				52.5		3570		1.74				52.7		4740		1.75				52.5		4970		1.74

		52.6		4040		1.74				52.7		3520		1.75				53.7		3960		1.78				52.9		4150		1.75				52.6		3570		1.74				52.8		4750		1.75				52.5		4970		1.74

		52.6		4050		1.74				52.7		3520		1.75				53.7		3960		1.78				52.9		4160		1.75				52.7		3580		1.74				52.8		4750		1.75				52.6		4980		1.75

		52.8		4060		1.75				52.8		3520		1.75				53.8		3960		1.78				53		4160		1.76				52.8		3580		1.75				52.9		4760		1.75				52.7		4980		1.75

		52.8		4060		1.75				52.9		3530		1.75				53.9		3970		1.78				53.1		4170		1.76				52.8		3590		1.75				52.9		4760		1.75				52.8		4990		1.75

		52.9		4060		1.75				52.9		3530		1.75				53.9		3970		1.79				53.1		4170		1.76				52.8		3590		1.75				53		4770		1.76				52.8		4990		1.75

		52.9		4070		1.75				53		3540		1.76				54		3980		1.79				53.1		4170		1.76				52.9		3590		1.75				53		4770		1.76				52.9		5000		1.75

		53		4070		1.76				53		3540		1.76				54.1		3990		1.79				53.3		4180		1.77				53		3600		1.75				53.2		4780		1.76				53		5010		1.76

		53		4080		1.76				53.1		3540		1.76				54.2		3990		1.8				53.3		4190		1.77				53.1		3600		1.76				53.2		4790		1.76				53		5020		1.76

		53.1		4080		1.76				53.2		3550		1.76				54.2		3990		1.8				53.4		4190		1.77				53.1		3610		1.76				53.3		4790		1.77				53.1		5020		1.76

		53.2		4090		1.76				53.2		3550		1.77				54.3		4000		1.8				53.5		4190		1.77				53.2		3610		1.76				53.3		4800		1.77				53.2		5030		1.76

		53.3		4090		1.77				53.3		3550		1.77				54.4		4000		1.8				53.5		4200		1.77				53.3		3620		1.76				53.4		4800		1.77				53.3		5030		1.77

		53.4		4100		1.77				53.4		3560		1.77				54.4		4010		1.8				53.6		4200		1.78				53.3		3620		1.76				53.5		4810		1.77				53.3		5040		1.77

		53.4		4100		1.77				53.4		3560		1.77				54.5		4010		1.81				53.7		4200		1.78				53.4		3620		1.77				53.5		4810		1.77				53.4		5050		1.77

		53.5		4110		1.77				53.5		3570		1.77				54.6		4020		1.81				53.7		4210		1.78				53.4		3630		1.77				53.6		4820		1.78				53.4		5050		1.77

		53.6		4110		1.77				53.6		3570		1.78				54.6		4020		1.81				53.8		4210		1.78				53.5		3630		1.77				53.6		4820		1.78				53.5		5060		1.78

		53.6		4110		1.78				53.7		3570		1.78				54.7		4030		1.81				53.9		4220		1.79				53.6		3630		1.77				53.7		4830		1.78				53.6		5070		1.78

		53.7		4120		1.78				53.7		3580		1.78				54.8		4030		1.82				54		4230		1.79				53.6		3640		1.77				53.8		4830		1.78				53.6		5070		1.78

		53.7		4120		1.78				53.8		3580		1.78				54.8		4040		1.82				54		4230		1.79				53.7		3640		1.78				53.9		4840		1.79				53.7		5080		1.78

		53.8		4130		1.78				53.8		3580		1.78				54.9		4040		1.82				54.1		4230		1.79				53.8		3650		1.78				53.9		4840		1.79				53.8		5080		1.78

		53.9		4130		1.79				53.9		3590		1.79				54.9		4040		1.82				54.1		4240		1.79				53.9		3660		1.78				54		4850		1.79				53.8		5090		1.79

		53.9		4140		1.79				53.9		3590		1.79				55		4050		1.82				54.2		4240		1.8				53.9		3660		1.79				54.1		4850		1.79				53.9		5100		1.79

		54		4140		1.79				54		3600		1.79				55.1		4050		1.83				54.3		4250		1.8				54		3660		1.79				54.1		4860		1.79				53.9		5100		1.79

		54.1		4140		1.79				54.1		3600		1.8				55.1		4060		1.83				54.3		4250		1.8				54.1		3670		1.79				54.2		4860		1.8				54		5110		1.79

		54.1		4150		1.79				54.2		3610		1.8				55.2		4060		1.83				54.5		4260		1.81				54.2		3670		1.79				54.3		4870		1.8				54.1		5120		1.8

		54.2		4150		1.8				54.3		3610		1.8				55.3		4070		1.83				54.5		4260		1.81				54.2		3680		1.79				54.4		4870		1.8				54.2		5130		1.8

		54.3		4160		1.8				54.3		3610		1.8				55.3		4070		1.83				54.6		4270		1.81				54.3		3680		1.8				54.4		4880		1.8				54.3		5130		1.8

		54.3		4160		1.8				54.4		3620		1.8				55.4		4080		1.84				54.6		4270		1.81				54.3		3680		1.8				54.5		4880		1.81				54.4		5140		1.8

		54.4		4170		1.8				54.4		3620		1.81				55.5		4080		1.84				54.7		4270		1.81				54.4		3690		1.8				54.5		4890		1.81				54.4		5140		1.81

		54.5		4170		1.8				54.5		3620		1.81				55.5		4080		1.84				54.8		4280		1.82				54.5		3690		1.8				54.6		4890		1.81				54.4		5150		1.81

		54.5		4170		1.81				54.6		3630		1.81				55.6		4090		1.84				54.8		4280		1.82				54.6		3700		1.81				54.6		4900		1.81				54.5		5160		1.81

		54.6		4180		1.81				54.7		3630		1.81				55.7		4100		1.85				54.9		4290		1.82				54.6		3700		1.81				54.7		4900		1.81				54.6		5160		1.81

		54.7		4180		1.81				54.7		3640		1.81				55.8		4100		1.85				55		4290		1.82				54.7		3700		1.81				54.9		4910		1.82				54.6		5170		1.81

		54.8		4190		1.81				54.8		3640		1.82				55.9		4100		1.85				55.1		4300		1.83				54.7		3710		1.81				54.9		4920		1.82				54.7		5180		1.82

		54.8		4190		1.82				54.9		3640		1.82				55.9		4110		1.85				55.1		4300		1.83				54.8		3710		1.81				55		4920		1.82				54.8		5180		1.82

		54.9		4200		1.82				54.9		3650		1.82				56		4110		1.86				55.2		4310		1.83				54.9		3720		1.82				55		4930		1.82				54.9		5190		1.82

		54.9		4200		1.82				55		3650		1.82				56.1		4120		1.86				55.3		4310		1.83				55		3720		1.82				55.1		4930		1.83				54.9		5190		1.82

		55		4200		1.82				55		3660		1.83				56.1		4120		1.86				55.3		4310		1.83				55		3730		1.82				55.2		4940		1.83				55		5200		1.82

		55		4210		1.82				55.1		3660		1.83				56.2		4130		1.86				55.4		4320		1.84				55.1		3730		1.82				55.2		4940		1.83				55.1		5200		1.83

		55.1		4210		1.83				55.2		3660		1.83				56.3		4140		1.87				55.5		4320		1.84				55.2		3740		1.83				55.3		4950		1.83				55.1		5210		1.83

		55.2		4220		1.83				55.3		3670		1.83				56.4		4140		1.87				55.5		4330		1.84				55.2		3740		1.83				55.4		4950		1.84				55.2		5220		1.83

		55.3		4220		1.83				55.3		3670		1.84				56.4		4140		1.87				55.6		4330		1.84				55.3		3740		1.83				55.4		4960		1.84				55.2		5220		1.83

		55.3		4220		1.83				55.4		3680		1.84				56.5		4150		1.87				55.7		4340		1.85				55.4		3750		1.83				55.5		4960		1.84				55.3		5230		1.84

		55.4		4230		1.83				55.5		3680		1.84				56.6		4150		1.87				55.8		4340		1.85				55.4		3750		1.83				55.5		4970		1.84				55.4		5240		1.84

		55.4		4230		1.84				55.6		3680		1.84				56.6		4160		1.88				55.8		4350		1.85				55.5		3760		1.84				55.6		4970		1.84				55.4		5240		1.84

		55.5		4240		1.84				55.6		3690		1.84				56.7		4160		1.88				55.9		4350		1.85				55.6		3760		1.84				55.7		4980		1.85				55.5		5250		1.84

		55.6		4250		1.84				55.7		3690		1.85				56.7		4160		1.88				56		4350		1.85				55.7		3770		1.84				55.8		4980		1.85				55.6		5250		1.84

		55.7		4250		1.84				55.7		3700		1.85				56.8		4170		1.88				56		4360		1.86				55.7		3770		1.84				55.8		4990		1.85				55.6		5260		1.85

		55.8		4250		1.85				55.8		3700		1.85				56.9		4180		1.89				56.1		4360		1.86				55.8		3780		1.85				55.9		5000		1.85				55.7		5260		1.85

		55.8		4260		1.85				55.9		3710		1.85				57		4180		1.89				56.2		4370		1.86				55.9		3780		1.85				56		5000		1.86				55.8		5270		1.85

		55.9		4260		1.85				56		3710		1.86				57		4180		1.89				56.2		4370		1.86				55.9		3780		1.85				56		5010		1.86				55.8		5280		1.85

		55.9		4270		1.85				56.1		3710		1.86				57.1		4190		1.89				56.3		4380		1.87				56		3790		1.85				56.1		5010		1.86				56		5290		1.86

		56		4270		1.85				56.1		3720		1.86				57.1		4190		1.89				56.4		4380		1.87				56		3790		1.86				56.1		5010		1.86				56		5290		1.86

		56.1		4270		1.86				56.2		3720		1.86				57.2		4200		1.9				56.5		4390		1.87				56.2		3800		1.86				56.2		5020		1.86				56.1		5300		1.86

		56.1		4280		1.86				56.2		3720		1.86				57.2		4200		1.9				56.5		4390		1.87				56.2		3800		1.86				56.3		5020		1.87				56.1		5300		1.86

		56.2		4280		1.86				56.3		3730		1.87				57.3		4200		1.9				56.6		4390		1.88				56.3		3810		1.86				56.4		5030		1.87				56.2		5310		1.87

		56.3		4290		1.86				56.3		3730		1.87				57.4		4210		1.9				56.6		4400		1.88				56.3		3810		1.87				56.5		5040		1.87				56.3		5320		1.87

		56.3		4290		1.87				56.5		3740		1.87				57.5		4220		1.91				56.7		4410		1.88				56.4		3820		1.87				56.5		5040		1.87				56.3		5320		1.87

		56.4		4300		1.87				56.6		3740		1.88				57.6		4220		1.91				56.8		4410		1.88				56.5		3820		1.87				56.6		5050		1.88				56.4		5330		1.87

		56.5		4300		1.87				56.6		3750		1.88				57.6		4220		1.91				56.9		4410		1.89				56.6		3820		1.87				56.6		5050		1.88				56.5		5340		1.88

		56.5		4300		1.87				56.7		3750		1.88				57.7		4230		1.91				56.9		4420		1.89				56.6		3830		1.87				56.7		5060		1.88				56.6		5340		1.88

		56.6		4310		1.87				56.8		3750		1.88				57.7		4230		1.91				57		4420		1.89				56.7		3840		1.88				56.8		5060		1.88				56.6		5350		1.88

		56.6		4310		1.88				56.8		3760		1.88				57.8		4240		1.92				57		4430		1.89				56.8		3840		1.88				56.9		5070		1.88				56.7		5360		1.88

		56.8		4320		1.88				56.9		3760		1.89				57.9		4240		1.92				57.1		4430		1.89				56.9		3840		1.88				56.9		5070		1.89				56.8		5360		1.88

		56.8		4320		1.88				56.9		3760		1.89				58		4250		1.92				57.2		4430		1.9				56.9		3850		1.88				57		5080		1.89				56.8		5370		1.89

		56.9		4330		1.89				57.1		3770		1.89				58.1		4250		1.93				57.3		4440		1.9				57		3850		1.89				57.1		5090		1.89				56.9		5370		1.89

		56.9		4330		1.89				57.1		3780		1.89				58.1		4260		1.93				57.3		4450		1.9				57		3860		1.89				57.1		5090		1.89				56.9		5380		1.89

		57		4340		1.89				57.2		3780		1.9				58.2		4260		1.93				57.4		4450		1.9				57.1		3860		1.89				57.2		5100		1.9				57		5380		1.89

		57.1		4340		1.89				57.2		3780		1.9				58.3		4270		1.93				57.5		4450		1.91				57.2		3860		1.89				57.2		5100		1.9				57.1		5390		1.9

		57.1		4350		1.89				57.3		3790		1.9				58.3		4270		1.93				57.5		4460		1.91				57.2		3870		1.9				57.3		5110		1.9				57.2		5400		1.9

		57.2		4350		1.9				57.4		3790		1.9				58.4		4270		1.94				57.6		4460		1.91				57.3		3870		1.9				57.4		5110		1.9				57.3		5400		1.9

		57.3		4360		1.9				57.4		3790		1.9				58.4		4280		1.94				57.7		4460		1.91				57.4		3880		1.9				57.4		5120		1.9				57.3		5410		1.9

		57.3		4360		1.9				57.5		3800		1.91				58.5		4280		1.94				57.7		4470		1.91				57.5		3880		1.9				57.5		5120		1.91				57.3		5410		1.9

		57.4		4360		1.9				57.5		3800		1.91				58.6		4290		1.94				57.8		4470		1.92				57.5		3880		1.9				57.5		5130		1.91				57.4		5420		1.91

		57.5		4370		1.9				57.7		3810		1.91				58.6		4290		1.95				57.8		4480		1.92				57.6		3890		1.91				57.6		5130		1.91				57.5		5430		1.91

		57.6		4370		1.91				57.7		3810		1.91				58.7		4300		1.95				58		4480		1.92				57.7		3890		1.91				57.7		5140		1.91				57.5		5430		1.91

		57.6		4380		1.91				57.7		3810		1.92				58.8		4300		1.95				58		4490		1.92				57.7		3900		1.91				57.7		5140		1.91				57.6		5440		1.91

		57.7		4380		1.91				57.8		3820		1.92				58.8		4310		1.95				58.1		4490		1.92				57.8		3900		1.91				57.8		5150		1.92				57.7		5440		1.91

		57.8		4390		1.91				57.9		3820		1.92				58.9		4310		1.95				58.1		4500		1.93				57.8		3910		1.92				57.9		5150		1.92				57.8		5450		1.92

		57.9		4390		1.92				57.9		3830		1.92				59		4310		1.96				58.2		4500		1.93				57.9		3910		1.92				57.9		5160		1.92				57.8		5460		1.92

		57.9		4400		1.92				58		3830		1.92				59.1		4320		1.96				58.3		4500		1.93				58		3910		1.92				58		5160		1.92				57.8		5460		1.92

		58		4400		1.92				58.1		3830		1.93				59.1		4330		1.96				58.3		4510		1.93				58		3920		1.92				58		5170		1.92				57.9		5470		1.92

		58		4410		1.92				58.2		3840		1.93				59.2		4330		1.96				58.4		4510		1.94				58.1		3920		1.92				58.2		5180		1.93				58		5470		1.92

		58.1		4410		1.93				58.2		3840		1.93				59.3		4340		1.97				58.5		4520		1.94				58.2		3930		1.93				58.3		5180		1.93				58		5480		1.93

		58.2		4410		1.93				58.3		3840		1.93				59.3		4340		1.97				58.5		4520		1.94				58.2		3930		1.93				58.3		5190		1.93				58.1		5480		1.93

		58.3		4420		1.93				58.4		3850		1.94				59.4		4340		1.97				58.6		4530		1.94				58.3		3940		1.93				58.4		5190		1.94				58.2		5490		1.93

		58.3		4420		1.93				58.4		3850		1.94				59.5		4350		1.97				58.7		4530		1.95				58.4		3940		1.93				58.4		5200		1.94				58.3		5500		1.93

		58.4		4430		1.94				58.5		3850		1.94				59.5		4350		1.97				58.7		4540		1.95				58.4		3940		1.94				58.5		5200		1.94				58.3		5510		1.94

		58.5		4430		1.94				58.5		3860		1.94				59.6		4360		1.98				58.8		4540		1.95				58.5		3950		1.94				58.6		5210		1.94				58.4		5510		1.94

		58.5		4440		1.94				58.6		3860		1.94				59.7		4360		1.98				58.9		4540		1.95				58.6		3950		1.94				58.6		5210		1.94				58.4		5520		1.94

		58.6		4440		1.94				58.7		3860		1.95				59.8		4370		1.98				58.9		4550		1.95				58.6		3950		1.94				58.7		5220		1.95				58.5		5520		1.94

		58.7		4450		1.94				58.8		3870		1.95				59.8		4370		1.98				59		4550		1.96				58.7		3960		1.94				58.8		5220		1.95				58.6		5530		1.94

		58.8		4450		1.95				58.8		3880		1.95				59.9		4380		1.99				59.1		4560		1.96				58.7		3960		1.95				58.9		5230		1.95				58.6		5530		1.95

		58.8		4460		1.95				58.9		3880		1.95				60		4380		1.99				59.2		4560		1.96				58.8		3970		1.95				58.9		5230		1.95				58.7		5540		1.95

		58.9		4460		1.95				59		3880		1.96				60		4390		1.99				59.2		4570		1.96				58.9		3970		1.95				59		5240		1.96				58.8		5540		1.95

		58.9		4460		1.95				59		3890		1.96				60.1		4390		1.99				59.3		4570		1.97				59		3980		1.95				59		5240		1.96				58.9		5560		1.95

		59		4470		1.96				59.1		3890		1.96				60.1		4390		1.99				59.3		4580		1.97				59		3980		1.96				59.1		5250		1.96				59		5560		1.96

		59.1		4480		1.96				59.2		3890		1.96				60.3		4400		2				59.4		4580		1.97				59.1		3980		1.96				59.1		5250		1.96				59		5570		1.96

		59.2		4480		1.96				59.2		3900		1.96				60.4		4410		2				59.4		4580		1.97				59.2		3990		1.96				59.2		5260		1.96				59.1		5570		1.96

		59.3		4480		1.96				59.3		3900		1.97				60.4		4410		2				59.5		4590		1.97				59.2		3990		1.96				59.3		5260		1.97				59.1		5580		1.96

		59.3		4490		1.97				59.4		3910		1.97				60.5		4420		2.01				59.6		4600		1.98				59.3		4000		1.96				59.3		5270		1.97				59.2		5590		1.97

		59.4		4490		1.97				59.4		3910		1.97				60.5		4420		2.01				59.7		4600		1.98				59.3		4000		1.97				59.4		5270		1.97				59.3		5590		1.97

		59.4		4500		1.97				59.5		3910		1.97				60.6		4420		2.01				59.8		4600		1.98				59.4		4000		1.97				59.5		5280		1.97				59.3		5600		1.97

		59.5		4500		1.97				59.6		3920		1.98				60.7		4430		2.01				59.9		4610		1.98				59.5		4010		1.97				59.5		5280		1.97				59.4		5610		1.97

		59.6		4510		1.98				59.6		3920		1.98				60.7		4430		2.01				59.9		4610		1.99				59.6		4010		1.97				59.6		5290		1.98				59.5		5610		1.98

		59.7		4510		1.98				59.7		3930		1.98				60.9		4440		2.02				59.9		4620		1.99				59.6		4020		1.97				59.7		5290		1.98				59.6		5620		1.98

		59.7		4520		1.98				59.7		3930		1.98				60.9		4450		2.02				60		4620		1.99				59.7		4020		1.98				59.7		5300		1.98				59.6		5630		1.98

		59.8		4520		1.98				59.8		3930		1.98				61		4450		2.02				60.1		4620		1.99				59.7		4030		1.98				59.8		5300		1.98				59.7		5630		1.98

		59.9		4530		1.98				59.9		3940		1.99				61		4450		2.02				60.1		4630		1.99				59.8		4030		1.98				59.8		5310		1.99				59.8		5640		1.98

		59.9		4530		1.99				60		3940		1.99				61.1		4460		2.03				60.2		4630		2				59.9		4030		1.98				60		5320		1.99				59.8		5640		1.99

		60		4530		1.99				60		3940		1.99				61.1		4460		2.03				60.3		4640		2				60		4040		1.98				60		5320		1.99				59.9		5650		1.99

		60.1		4540		1.99				60.1		3950		1.99				61.2		4470		2.03				60.4		4640		2				60.1		4050		1.99				60.1		5330		1.99				60		5660		1.99

		60.2		4550		1.99				60.2		3950		2				61.3		4470		2.03				60.4		4650		2				60.1		4050		1.99				60.2		5330		2				60		5660		1.99

		60.2		4550		2				60.2		3960		2				61.3		4480		2.03				60.5		4650		2.01				60.2		4050		1.99				60.2		5340		2				60.1		5670		2

		60.3		4550		2				60.3		3960		2				61.4		4480		2.04				60.6		4650		2.01				60.2		4060		2				60.3		5340		2				60.2		5680		2

		60.3		4560		2				60.4		3960		2				61.5		4490		2.04				60.6		4660		2.01				60.3		4060		2				60.3		5350		2				60.2		5680		2

		60.4		4560		2				60.5		3970		2.01				61.5		4490		2.04				60.7		4660		2.01				60.4		4070		2				60.4		5350		2				60.3		5690		2

		60.5		4570		2				60.5		3970		2.01				61.6		4490		2.04				60.8		4670		2.01				60.4		4070		2				60.5		5360		2.01				60.3		5690		2

		60.5		4570		2.01				60.6		3980		2.01				61.7		4500		2.05				60.8		4670		2.02				60.5		4070		2				60.6		5370		2.01				60.4		5700		2.01

		60.6		4570		2.01				60.6		3980		2.01				61.8		4500		2.05				60.9		4680		2.02				60.6		4080		2.01				60.7		5370		2.01				60.5		5700		2.01

		60.7		4580		2.01				60.7		3980		2.01				61.8		4510		2.05				60.9		4680		2.02				60.7		4090		2.01				60.7		5380		2.01				60.6		5710		2.01

		60.8		4590		2.02				60.8		3990		2.02				61.9		4510		2.05				61		4680		2.02				60.7		4090		2.01				60.8		5380		2.02				60.6		5720		2.01

		60.9		4590		2.02				60.8		3990		2.02				61.9		4520		2.05				61.1		4690		2.02				60.8		4090		2.01				60.9		5390		2.02				60.7		5730		2.02

		60.9		4600		2.02				60.9		4000		2.02				62		4520		2.06				61.1		4690		2.03				60.9		4100		2.02				60.9		5390		2.02				60.7		5730		2.02

		61		4600		2.02				61		4000		2.02				62.1		4530		2.06				61.2		4700		2.03				61		4100		2.02				61		5400		2.02				60.8		5740		2.02

		61.1		4600		2.02				61.1		4010		2.03				62.1		4530		2.06				61.3		4700		2.03				61		4110		2.02				61.1		5410		2.03				60.9		5740		2.02

		61.1		4610		2.03				61.2		4010		2.03				62.2		4540		2.06				61.4		4710		2.03				61.1		4110		2.02				61.2		5410		2.03				61		5750		2.02

		61.2		4610		2.03				61.2		4010		2.03				62.3		4540		2.07				61.4		4710		2.04				61.1		4110		2.02				61.2		5420		2.03				61		5750		2.03

		61.3		4620		2.03				61.2		4020		2.03				62.3		4540		2.07				61.4		4710		2.04				61.2		4120		2.03				61.3		5420		2.03				61.1		5760		2.03

		61.4		4630		2.03				61.3		4020		2.03				62.4		4550		2.07				61.5		4720		2.04				61.3		4120		2.03				61.3		5430		2.04				61.2		5770		2.03

		61.4		4630		2.04				61.4		4020		2.04				62.4		4550		2.07				61.6		4720		2.04				61.4		4130		2.03				61.4		5430		2.04				61.2		5780		2.03

		61.5		4630		2.04				61.4		4030		2.04				62.5		4560		2.07				61.6		4730		2.04				61.4		4130		2.03				61.5		5440		2.04				61.3		5780		2.04

		61.6		4640		2.04				61.5		4030		2.04				62.6		4570		2.08				61.7		4730		2.05				61.5		4130		2.04				61.5		5440		2.04				61.4		5790		2.04

		61.6		4640		2.04				61.6		4040		2.04				62.7		4570		2.08				61.8		4740		2.05				61.6		4140		2.04				61.6		5450		2.04				61.5		5790		2.04

		61.7		4650		2.04				61.7		4040		2.05				62.8		4570		2.08				61.8		4740		2.05				61.6		4140		2.04				61.7		5450		2.05				61.5		5800		2.04

		61.7		4650		2.05				61.8		4050		2.05				62.8		4580		2.08				61.9		4750		2.05				61.6		4150		2.04				61.7		5460		2.05				61.6		5810		2.04

		61.8		4650		2.05				61.8		4050		2.05				62.9		4580		2.09				62		4750		2.06				61.7		4150		2.04				61.8		5460		2.05				61.6		5810		2.05

		61.9		4660		2.05				61.9		4050		2.05				62.9		4590		2.09				62.1		4760		2.06				61.8		4160		2.05				61.8		5470		2.05				61.7		5820		2.05

		61.9		4660		2.05				61.9		4060		2.06				63		4590		2.09				62.1		4760		2.06				61.9		4160		2.05				61.9		5470		2.05				61.8		5830		2.05

		62		4670		2.06				62		4060		2.06				63.1		4590		2.09				62.2		4760		2.06				62		4170		2.05				62		5480		2.06				61.9		5830		2.05

		62.1		4670		2.06				62.1		4060		2.06				63.2		4600		2.1				62.3		4770		2.07				62.1		4170		2.05				62		5480		2.06				61.9		5840		2.06

		62.2		4680		2.06				62.1		4070		2.06				63.3		4610		2.1				62.3		4770		2.07				62.1		4180		2.06				62.1		5490		2.06				62		5850		2.06

		62.2		4680		2.06				62.2		4070		2.06				63.3		4610		2.1				62.4		4780		2.07				62.1		4180		2.06				62.2		5490		2.06				62.1		5850		2.06

		62.3		4680		2.06				62.3		4080		2.07				63.4		4620		2.1				62.5		4780		2.07				62.2		4180		2.06				62.3		5500		2.07				62.1		5860		2.06

		62.3		4690		2.07				62.3		4080		2.07				63.4		4620		2.11				62.6		4790		2.08				62.3		4190		2.06				62.3		5500		2.07				62.2		5860		2.06

		62.4		4700		2.07				62.4		4080		2.07				63.5		4630		2.11				62.6		4790		2.08				62.4		4190		2.07				62.4		5510		2.07				62.2		5870		2.07

		62.5		4700		2.07				62.5		4090		2.07				63.6		4630		2.11				62.7		4800		2.08				62.4		4200		2.07				62.4		5510		2.07				62.3		5880		2.07

		62.6		4700		2.07				62.5		4090		2.07				63.6		4630		2.11				62.8		4800		2.08				62.5		4200		2.07				62.5		5520		2.07				62.4		5880		2.07

		62.6		4710		2.08				62.6		4090		2.08				63.8		4640		2.12				62.8		4810		2.08				62.5		4210		2.07				62.6		5520		2.08				62.5		5890		2.07

		62.7		4710		2.08				62.7		4100		2.08				63.9		4650		2.12				62.9		4810		2.09				62.6		4210		2.07				62.6		5530		2.08				62.5		5890		2.08

		62.7		4720		2.08				62.7		4100		2.08				63.9		4650		2.12				62.9		4810		2.09				62.7		4210		2.08				62.7		5530		2.08				62.6		5900		2.08

		62.8		4720		2.08				62.8		4110		2.08				63.9		4650		2.12				63.1		4820		2.09				62.8		4220		2.08				62.8		5540		2.08				62.7		5910		2.08

		62.9		4720		2.08				62.9		4110		2.09				64		4660		2.12				63.1		4830		2.09				62.8		4220		2.08				62.9		5550		2.09				62.7		5910		2.08

		62.9		4730		2.09				63		4120		2.09				64.1		4660		2.13				63.2		4830		2.1				62.9		4230		2.08				63		5550		2.09				62.7		5920		2.08

		63		4730		2.09				63		4120		2.09				64.1		4670		2.13				63.3		4830		2.1				63		4230		2.08				63		5560		2.09				62.8		5920		2.09

		63.1		4740		2.09				63.1		4120		2.09				64.2		4670		2.13				63.3		4840		2.1				63		4240		2.09				63.1		5560		2.09				62.9		5930		2.09

		63.2		4740		2.09				63.1		4130		2.09				64.3		4680		2.13				63.4		4840		2.1				63.1		4240		2.09				63.1		5570		2.09				63		5940		2.09

		63.2		4750		2.1				63.2		4130		2.1				64.4		4680		2.13				63.5		4850		2.1				63.1		4240		2.09				63.2		5570		2.1				63.1		5940		2.09

		63.2		4750		2.1				63.3		4130		2.1				64.4		4690		2.14				63.5		4850		2.11				63.2		4250		2.09				63.2		5580		2.1				63.1		5950		2.1

		63.3		4760		2.1				63.4		4140		2.1				64.5		4690		2.14				63.6		4860		2.11				63.3		4250		2.1				63.3		5580		2.1				63.2		5960		2.1

		63.4		4760		2.1				63.4		4140		2.1				64.5		4690		2.14				63.7		4860		2.11				63.3		4250		2.1				63.4		5590		2.1				63.2		5960		2.1

		63.5		4770		2.1				63.5		4150		2.11				64.6		4700		2.14				63.8		4870		2.12				63.4		4260		2.1				63.5		5590		2.11				63.3		5970		2.1

		63.5		4770		2.11				63.5		4150		2.11				64.7		4700		2.15				63.8		4870		2.12				63.5		4260		2.1				63.6		5600		2.11				63.4		5970		2.1

		63.6		4770		2.11				63.6		4150		2.11				64.7		4710		2.15				63.9		4870		2.12				63.5		4270		2.1				63.6		5610		2.11				63.4		5980		2.11

		63.7		4780		2.11				63.6		4160		2.11				64.8		4710		2.15				63.9		4880		2.12				63.7		4280		2.11				63.7		5610		2.11				63.5		5990		2.11

		63.7		4780		2.11				63.7		4160		2.11				64.9		4720		2.15				64		4880		2.12				63.7		4280		2.11				63.7		5620		2.12				63.6		5990		2.11

		63.8		4790		2.12				63.9		4170		2.12				65		4720		2.16				64.1		4890		2.13				63.8		4280		2.11				63.8		5620		2.12				63.6		6000		2.11

		63.8		4790		2.12				63.9		4170		2.12				65.1		4730		2.16				64.2		4890		2.13				63.8		4290		2.11				63.9		5630		2.12				63.7		6000		2.12

		63.9		4800		2.12				64		4180		2.12				65.1		4730		2.16				64.3		4900		2.13				63.9		4290		2.12				64		5640		2.12				63.7		6010		2.12

		64		4800		2.12				64		4180		2.12				65.2		4740		2.16				64.3		4900		2.13				64		4290		2.12				64.1		5640		2.13				63.8		6020		2.12

		64.1		4810		2.12				64.1		4180		2.13				65.3		4740		2.16				64.3		4910		2.13				64		4300		2.12				64.1		5650		2.13				63.9		6020		2.12

		64.1		4810		2.13				64.1		4190		2.13				65.3		4750		2.17				64.4		4910		2.14				64.1		4300		2.12				64.2		5650		2.13				63.9		6030		2.12

		64.2		4810		2.13				64.2		4190		2.13				65.4		4750		2.17				64.5		4910		2.14				64.1		4310		2.13				64.2		5660		2.13				64		6040		2.13

		64.2		4820		2.13				64.3		4190		2.13				65.5		4760		2.17				64.6		4920		2.14				64.3		4310		2.13				64.3		5660		2.13				64.1		6040		2.13

		64.3		4820		2.13				64.4		4200		2.14				65.6		4760		2.18				64.6		4920		2.14				64.3		4320		2.13				64.4		5670		2.14				64.2		6050		2.13

		64.4		4830		2.13				64.5		4200		2.14				65.6		4770		2.18				64.7		4930		2.15				64.4		4320		2.13				64.4		5670		2.14				64.2		6060		2.13

		64.5		4830		2.14				64.5		4210		2.14				65.7		4770		2.18				64.8		4930		2.15				64.5		4330		2.13				64.5		5680		2.14				64.3		6060		2.13

		64.6		4840		2.14				64.6		4210		2.14				65.7		4780		2.18				64.8		4930		2.15				64.5		4330		2.14				64.6		5690		2.14				64.4		6070		2.14

		64.6		4840		2.14				64.6		4220		2.15				65.8		4780		2.18				64.9		4910		2.15				64.5		4330		2.14				64.7		5690		2.15				64.4		6070		2.14

		64.6		4850		2.14				64.7		4220		2.15				65.9		4780		2.19				64.9		4910		2.15				64.6		4340		2.14				64.8		5700		2.15				64.5		6080		2.14

		64.7		4850		2.15				64.8		4220		2.15				65.9		4790		2.19				65		4920		2.16				64.7		4340		2.14				64.8		5700		2.15				64.6		6090		2.14

		64.8		4850		2.15				64.8		4230		2.15				66		4800		2.19				65.1		4930		2.16				64.8		4340		2.15				64.9		5700		2.15				64.6		6090		2.15

		64.8		4860		2.15				64.9		4230		2.15				66.1		4800		2.19				65.1		4930		2.16				64.9		4350		2.15				65		5710		2.15				64.6		6100		2.15

		64.9		4860		2.15				65		4240		2.16				66.2		4810		2.2				65.2		4940		2.16				64.9		4360		2.15				65		5710		2.16				64.7		6100		2.15

		65		4870		2.15				65.1		4240		2.16				66.2		4810		2.2				65.3		4940		2.17				65		4360		2.15				65.1		5720		2.16				64.8		6110		2.15

		65.1		4880		2.16				65.1		4240		2.16				66.3		4810		2.2				65.4		4950		2.17				65		4360		2.16				65.1		5720		2.16				64.8		6110		2.15

		65.2		4880		2.16				65.2		4250		2.16				66.4		4820		2.2				65.4		4950		2.17				65.1		4370		2.16				65.3		5730		2.17				64.9		6120		2.16

		65.2		4880		2.16				65.3		4250		2.17				66.4		4820		2.2				65.5		4950		2.17				65.2		4370		2.16				65.3		5740		2.17				65		6130		2.16

		65.3		4890		2.16				65.3		4260		2.17				66.5		4830		2.21				65.6		4960		2.18				65.2		4380		2.16				65.4		5740		2.17				65		6130		2.16

		65.3		4890		2.17				65.4		4260		2.17				66.6		4840		2.21				65.7		4960		2.18				65.3		4380		2.16				65.4		5750		2.17				65.2		6140		2.16

		65.4		4900		2.17				65.4		4260		2.17				66.7		4840		2.21				65.7		4960		2.18				65.4		4390		2.17				65.5		5750		2.17				65.2		6150		2.17

		65.5		4900		2.17				65.5		4270		2.17				66.8		4840		2.21				65.8		4970		2.18				65.5		4390		2.17				65.6		5760		2.18				65.3		6160		2.17

		65.5		4900		2.17				65.6		4270		2.18				66.8		4850		2.22				65.8		4970		2.18				65.6		4400		2.17				65.6		5760		2.18				65.3		6160		2.17

		65.7		4910		2.18				65.7		4280		2.18				66.8		4850		2.22				65.9		4980		2.19				65.6		4400		2.17				65.7		5770		2.18				65.4		6170		2.17

		65.7		4920		2.18				65.7		4280		2.18				66.9		4860		2.22				66		4980		2.19				65.7		4410		2.18				65.8		5780		2.18				65.5		6170		2.17

		65.8		4920		2.18				65.8		4290		2.18				67		4860		2.22				66.1		4980		2.19				65.8		4410		2.18				65.9		5780		2.19				65.5		6180		2.18

		65.8		4930		2.18				65.9		4290		2.19				67		4870		2.23				66.1		4990		2.19				65.8		4410		2.18				66		5790		2.19				65.6		6180		2.18

		65.9		4930		2.19				65.9		4290		2.19				67.2		4880		2.23				66.2		4990		2.2				65.9		4420		2.18				66		5790		2.19				65.7		6200		2.18

		66		4930		2.19				66		4300		2.19				67.3		4880		2.23				66.2		4990		2.2				66		4420		2.18				66.1		5800		2.19				65.8		6200		2.18

		66.1		4940		2.19				66		4300		2.19				67.3		4880		2.23				66.3		5000		2.2				66		4430		2.19				66.1		5800		2.19				65.8		6210		2.19

		66.1		4940		2.19				66.1		4300		2.19				67.4		4890		2.24				66.4		5000		2.2				66.1		4430		2.19				66.2		5810		2.2				65.9		6210		2.19

		66.2		4950		2.2				66.2		4310		2.2				67.4		4890		2.24				66.5		5010		2.2				66.2		4440		2.19				66.3		5810		2.2				66		6220		2.19

		66.3		4950		2.2				66.3		4310		2.2				67.5		4900		2.24				66.5		5010		2.21				66.3		4440		2.2				66.3		5820		2.2				66.1		6230		2.19

		66.3		4960		2.2				66.3		4320		2.2				67.5		4900		2.24				66.6		5010		2.21				66.3		4450		2.2				66.4		5820		2.2				66.1		6230		2.2

		66.4		4960		2.2				66.4		4320		2.2				67.6		4910		2.24				66.6		5020		2.21				66.4		4450		2.2				66.5		5830		2.21				66.1		6240		2.2

		66.5		4960		2.2				66.4		4320		2.2				67.7		4910		2.25				66.7		5020		2.21				66.4		4450		2.2				66.5		5830		2.21				66.3		6250		2.2

		66.5		4970		2.21				66.5		4330		2.21				67.8		4920		2.25				66.7		5030		2.21				66.5		4460		2.2				66.6		5840		2.21				66.4		6260		2.2

		66.6		4970		2.21				66.5		4330		2.21				67.8		4920		2.25				66.8		5030		2.22				66.5		4460		2.21				66.6		5840		2.21				66.4		6260		2.21

		66.6		4980		2.21				66.6		4330		2.21				67.9		4920		2.25				66.9		5040		2.22				66.6		4470		2.21				66.7		5850		2.21				66.5		6270		2.21

		66.7		4980		2.21				66.7		4340		2.21				67.9		4930		2.26				67		5040		2.22				66.7		4470		2.21				66.8		5850		2.22				66.6		6270		2.21

		66.8		4990		2.21				66.8		4340		2.22				68		4930		2.26				67		5040		2.22				66.8		4480		2.21				66.8		5860		2.22				66.6		6280		2.21

		66.9		4990		2.22				66.9		4350		2.22				68.3		4950		2.27				67.1		5050		2.23				66.9		4480		2.21				67		5870		2.22				66.6		6280		2.21

		66.9		5000		2.22				66.9		4350		2.22				68.3		4960		2.27				67.2		5050		2.23				66.9		4480		2.22				67		5870		2.22				66.7		6290		2.22

		67		5000		2.22				67		4350		2.22				68.4		4960		2.27				67.2		5050		2.23				66.9		4490		2.22				67.1		5880		2.23				66.8		6300		2.22

		67		5000		2.22				67		4360		2.22				68.5		4970		2.27				67.2		5060		2.23				67		4490		2.22				67.2		5880		2.23				66.9		6300		2.22

		67.1		5010		2.23				67.1		4360		2.23				68.6		4970		2.27				67.3		5060		2.23				67.1		4500		2.22				67.2		5890		2.23				66.9		6310		2.22

		67.1		5010		2.23				67.1		4370		2.23				68.6		4970		2.28				67.4		5070		2.24				67.1		4500		2.23				67.3		5890		2.23				67		6320		2.23

		67.2		5020		2.23				67.2		4370		2.23				68.7		4980		2.28				67.4		5070		2.24				67.2		4500		2.23				67.3		5900		2.23				67.1		6320		2.23

		67.3		5020		2.23				67.4		4380		2.24				68.8		4980		2.28				67.6		5080		2.24				67.3		4510		2.23				67.4		5900		2.24				67.1		6330		2.23

		67.4		5030		2.23				67.4		4380		2.24				68.8		4990		2.29				67.7		5080		2.24				67.4		4510		2.23				67.6		5910		2.24				67.2		6330		2.23

		67.5		5030		2.24				67.5		4380		2.24				68.9		4990		2.29				67.7		5090		2.25				67.4		4520		2.23				67.6		5920		2.24				67.2		6340		2.23

		67.5		5030		2.24				67.5		4390		2.24				69		5000		2.29				67.7		5090		2.25				67.5		4520		2.24				67.6		5920		2.25				67.3		6350		2.24

		67.6		5040		2.24				67.6		4390		2.24				69.1		5000		2.29				67.8		5090		2.25				67.6		4530		2.24				67.7		5930		2.25				67.4		6350		2.24

		67.6		5040		2.24				67.6		4390		2.25				69.1		5010		2.29				67.9		5100		2.25				67.6		4530		2.24				67.8		5930		2.25				67.5		6360		2.24

		67.7		5050		2.25				67.7		4400		2.25				69.2		5010		2.3				67.9		5100		2.25				67.7		4530		2.24				67.8		5940		2.25				67.6		6370		2.24

		67.7		5050		2.25				67.8		4400		2.25				69.2		5010		2.3				68		5110		2.26				67.7		4540		2.25				67.9		5940		2.25				67.6		6370		2.25

		67.8		5060		2.25				67.9		4410		2.25				69.3		5020		2.3				68.1		5110		2.26				67.8		4540		2.25				68		5950		2.26				67.6		6380		2.25

		67.9		5060		2.25				68		4410		2.26				69.3		5020		2.3				68.2		5120		2.26				67.9		4550		2.25				68		5950		2.26				67.7		6380		2.25

		68		5070		2.26				68		4420		2.26				69.5		5030		2.31				68.2		5120		2.26				68		4550		2.25				68.1		5960		2.26				67.8		6390		2.25

		68.1		5070		2.26				68.1		4420		2.26				69.5		5040		2.31				68.3		5120		2.27				68.1		4560		2.26				68.2		5970		2.26				67.9		6400		2.25

		68.1		5080		2.26				68.2		4430		2.26				69.6		5040		2.31				68.3		5130		2.27				68.1		4560		2.26				68.3		5970		2.26				67.9		6400		2.26

		68.2		5080		2.26				68.2		4430		2.26				69.7		5040		2.31				68.4		5130		2.27				68.2		4570		2.26				68.3		5970		2.27				68		6410		2.26

		68.3		5080		2.26				68.3		4430		2.27				69.7		5050		2.31				68.5		5130		2.27				68.2		4570		2.26				68.4		5980		2.27				68		6420		2.26

		68.3		5090		2.27				68.4		4440		2.27				69.8		5050		2.32				68.6		5140		2.27				68.3		4570		2.26				68.5		5980		2.27				68.1		6420		2.26

		68.4		5090		2.27				68.4		4440		2.27				69.8		5060		2.32				68.7		5140		2.28				68.4		4580		2.27				68.5		5990		2.27				68.2		6430		2.26

		68.5		5100		2.27				68.5		4450		2.27				69.9		5060		2.32				68.7		5140		2.28				68.5		4590		2.27				68.6		6000		2.28				68.2		6430		2.27

		68.6		5110		2.27				68.6		4450		2.28				70		5070		2.32				68.8		5140		2.28				68.5		4590		2.27				68.6		6000		2.28				68.3		6440		2.27

		68.6		5110		2.28				68.6		4450		2.28				70.1		5070		2.33				68.9		5150		2.28				68.6		4600		2.27				68.8		6010		2.28				68.4		6450		2.27

		68.7		5110		2.28				68.7		4460		2.28				70.2		5080		2.33				68.9		5150		2.29				68.7		4600		2.28				68.8		6010		2.28				68.4		6450		2.27

		68.8		5120		2.28				68.7		4460		2.28				70.2		5080		2.33				69		5150		2.29				68.8		4600		2.28				68.9		6020		2.29				68.5		6460		2.28

		68.8		5120		2.28				68.8		4460		2.28				70.3		5090		2.33				69.1		5160		2.29				68.8		4610		2.28				69		6020		2.29				68.6		6470		2.28

		68.9		5130		2.28				68.9		4470		2.29				70.4		5090		2.34				69.1		5160		2.29				68.9		4610		2.28				69		6030		2.29				68.6		6470		2.28

		68.9		5130		2.29				69		4470		2.29				70.4		5100		2.34				69.2		5170		2.3				68.9		4620		2.28				69.1		6030		2.29				68.7		6480		2.28

		69		5140		2.29				69		4480		2.29				70.5		5100		2.34				69.3		5170		2.3				69.1		4620		2.29				69.1		6040		2.29				68.8		6480		2.28

		69.1		5140		2.29				69.1		4480		2.29				70.6		5110		2.34				69.4		5180		2.3				69.1		4630		2.29				69.2		6040		2.3				68.8		6490		2.29

		69.2		5150		2.29				69.2		4490		2.3				70.7		5110		2.35				69.4		5180		2.3				69.2		4630		2.29				69.3		6050		2.3				68.9		6500		2.29

		69.2		5150		2.3				69.3		4490		2.3				70.7		5120		2.35				69.5		5180		2.31				69.3		4640		2.29				69.4		6060		2.3				69		6500		2.29

		69.3		5160		2.3				69.3		4490		2.3				70.8		5120		2.35				69.6		5190		2.31				69.3		4640		2.3				69.4		6060		2.3				69		6510		2.29

		69.4		5160		2.3				69.4		4500		2.3				70.8		5130		2.35				69.6		5190		2.31				69.4		4650		2.3				69.5		6070		2.31				69.1		6510		2.29

		69.5		5170		2.3				69.4		4500		2.3				70.9		5130		2.35				69.7		5190		2.31				69.4		4650		2.3				69.6		6070		2.31				69.2		6530		2.3

		69.5		5170		2.31				69.5		4510		2.31				71		5140		2.36				69.7		5200		2.31				69.5		4650		2.3				69.6		6080		2.31				69.3		6530		2.3

		69.6		5180		2.31				69.5		4510		2.31				71.1		5140		2.36				69.9		5200		2.32				69.6		4660		2.31				69.7		6080		2.31				69.3		6540		2.3

		69.7		5180		2.31				69.7		4520		2.31				71.1		5140		2.36				69.9		5210		2.32				69.7		4660		2.31				69.8		6090		2.31				69.4		6540		2.31

		69.7		5190		2.31				69.7		4520		2.31				71.2		5150		2.36				70		5210		2.32				69.7		4670		2.31				69.9		6100		2.32				69.5		6550		2.31

		69.8		5190		2.31				69.8		4520		2.32				71.3		5160		2.37				70		5210		2.32				69.8		4670		2.31				70		6100		2.32				69.5		6560		2.31

		69.8		5190		2.32				69.9		4530		2.32				71.3		5160		2.37				70.1		5220		2.33				69.9		4680		2.32				70		6110		2.32				69.6		6560		2.31

		69.9		5200		2.32				69.9		4530		2.32				71.4		5170		2.37				70.2		5220		2.33				69.9		4680		2.32				70.1		6110		2.33				69.6		6570		2.31

		70		5200		2.32				70		4530		2.32				71.5		5170		2.37				70.2		5220		2.33				70		4690		2.32				70.1		6120		2.33				69.8		6580		2.32

		70		5210		2.32				70		4540		2.32				71.6		5170		2.37				70.3		5230		2.33				70.1		4690		2.32				70.2		6120		2.33				69.9		6590		2.32

		70.1		5210		2.33				70.1		4540		2.33				71.6		5180		2.38				70.4		5230		2.34				70.2		4700		2.33				70.2		6130		2.33				69.9		6590		2.32

		70.2		5220		2.33				70.2		4550		2.33				71.7		5180		2.38				70.5		5240		2.34				70.2		4700		2.33				70.3		6130		2.33				70		6600		2.32

		70.3		5220		2.33				70.3		4550		2.33				71.7		5190		2.38				70.6		5240		2.34				70.3		4710		2.33				70.4		6140		2.34				70		6600		2.33

		70.3		5230		2.33				70.3		4560		2.33				71.8		5190		2.38				70.6		5250		2.34				70.4		4710		2.33				70.5		6140		2.34				70.1		6610		2.33

		70.4		5230		2.34				70.4		4560		2.34				71.9		5200		2.39				70.7		5250		2.35				70.4		4710		2.33				70.5		6150		2.34				70.1		6620		2.33

		70.5		5230		2.34				70.4		4560		2.34				72		5200		2.39				70.7		5250		2.35				70.5		4720		2.34				70.6		6150		2.34				70.2		6620		2.33

		70.5		5240		2.34				70.5		4570		2.34				72		5210		2.39				70.8		5260		2.35				70.5		4720		2.34				70.7		6160		2.34				70.3		6630		2.33

		70.6		5240		2.34				70.5		4570		2.34				72.1		5210		2.39				70.8		5260		2.35				70.6		4730		2.34				70.7		6160		2.35				70.4		6640		2.34

		70.6		5250		2.34				70.6		4570		2.34				72.1		5220		2.39				71		5270		2.36				70.8		4730		2.34				70.8		6170		2.35				70.5		6650		2.34

		70.8		5260		2.35				70.7		4580		2.35				72.2		5220		2.4				71.1		5270		2.36				70.8		4740		2.35				70.8		6170		2.35				70.5		6650		2.34

		70.9		5260		2.35				70.8		4580		2.35				72.2		5220		2.4				71.1		5270		2.36				70.9		4740		2.35				70.9		6180		2.35				70.6		6660		2.34

		70.9		5260		2.35				70.9		4590		2.35				72.3		5230		2.4				71.1		5280		2.36				70.9		4750		2.35				71		6190		2.36				70.7		6660		2.35

		71		5270		2.35				70.9		4590		2.35				72.4		5240		2.4				71.2		5280		2.36				71		4750		2.35				71.1		6190		2.36				70.7		6670		2.35

		71		5270		2.36				70.9		4590		2.36				72.5		5240		2.41				71.3		5280		2.37				71.1		4760		2.36				71.1		6200		2.36				70.8		6670		2.35

		71.1		5280		2.36				71		4600		2.36				72.5		5240		2.41				71.3		5290		2.37				71.1		4760		2.36				71.2		6200		2.36				70.9		6680		2.35

		71.2		5280		2.36				71.1		4600		2.36				72.6		5250		2.41				71.4		5290		2.37				71.2		4760		2.36				71.3		6210		2.37				70.9		6690		2.36

		71.2		5290		2.36				71.2		4610		2.36				72.7		5250		2.41				71.5		5300		2.37				71.3		4770		2.36				71.3		6210		2.37				71		6690		2.36

		71.4		5290		2.37				71.2		4610		2.36				72.7		5260		2.41				71.6		5300		2.38				71.3		4770		2.36				71.4		6220		2.37				71		6700		2.36

		71.4		5300		2.37				71.3		4610		2.37				72.8		5260		2.42				71.7		5310		2.38				71.4		4780		2.37				71.5		6220		2.37				71.1		6700		2.36

		71.5		5300		2.37				71.4		4620		2.37				72.9		5270		2.42				71.7		5310		2.38				71.5		4780		2.37				71.5		6230		2.38				71.2		6710		2.36

		71.5		5300		2.37				71.4		4620		2.37				73		5270		2.42				71.8		5310		2.38				71.5		4790		2.37				71.6		6240		2.38				71.2		6720		2.37

		71.6		5310		2.38				71.5		4630		2.37				73.1		5280		2.42				71.9		5320		2.38				71.6		4790		2.37				71.7		6240		2.38				71.3		6720		2.37

		71.6		5310		2.38				71.6		4630		2.38				73.1		5280		2.43				71.9		5320		2.39				71.6		4790		2.38				71.8		6250		2.38				71.3		6730		2.37

		71.7		5320		2.38				71.6		4630		2.38				73.2		5290		2.43				72		5330		2.39				71.7		4800		2.38				71.8		6250		2.38				71.4		6730		2.37

		71.8		5320		2.38				71.7		4640		2.38				73.2		5290		2.43				72		5330		2.39				71.8		4800		2.38				71.9		6260		2.39				71.5		6740		2.38

		71.8		5330		2.38				71.7		4640		2.38				73.3		5300		2.43				72.1		5340		2.39				71.9		4810		2.38				71.9		6260		2.39				71.5		6750		2.38

		71.9		5330		2.39				71.8		4650		2.38				73.4		5300		2.44				72.2		5340		2.4				71.9		4810		2.38				72		6270		2.39				71.6		6760		2.38

		72		5340		2.39				71.9		4650		2.39				73.5		5310		2.44				72.3		5340		2.4				72		4820		2.39				72.1		6280		2.39				71.7		6760		2.38

		72.1		5340		2.39				71.9		4650		2.39				73.5		5310		2.44				72.4		5350		2.4				72		4820		2.39				72.2		6280		2.4				71.7		6770		2.38

		72.1		5340		2.39				72		4660		2.39				73.6		5320		2.44				72.4		5350		2.4				72.1		4830		2.39				72.3		6290		2.4				71.8		6770		2.39

		72.2		5350		2.39				72.1		4660		2.39				73.6		5320		2.45				72.5		5360		2.41				72.2		4830		2.39				72.3		6290		2.4				71.9		6780		2.39

		72.2		5350		2.4				72.2		4670		2.4				73.7		5330		2.45				72.5		5360		2.41				72.2		4830		2.39				72.4		6300		2.4				71.9		6790		2.39

		72.3		5360		2.4				72.2		4670		2.4				73.8		5330		2.45				72.6		5360		2.41				72.3		4840		2.4				72.4		6300		2.4				72		6800		2.39

		72.4		5360		2.4				72.3		4680		2.4				73.8		5340		2.45				72.7		5370		2.41				72.3		4840		2.4				72.5		6310		2.41				72.1		6800		2.4

		72.5		5370		2.4				72.4		4680		2.4				73.9		5340		2.45				72.8		5370		2.41				72.5		4850		2.4				72.5		6310		2.41				72.2		6810		2.4

		72.5		5370		2.41				72.4		4680		2.4				74.1		5350		2.46				72.8		5380		2.42				72.6		4850		2.41				72.7		6320		2.41				72.2		6820		2.4

		72.6		5380		2.41				72.5		4690		2.41				74.1		5350		2.46				72.9		5380		2.42				72.6		4860		2.41				72.8		6330		2.41				72.3		6820		2.4

		72.7		5380		2.41				72.6		4690		2.41				74.1		5360		2.46				73		5390		2.42				72.7		4860		2.41				72.8		6330		2.42				72.4		6830		2.4

		72.7		5380		2.41				72.6		4700		2.41				74.2		5360		2.46				73		5390		2.42				72.7		4870		2.41				72.9		6330		2.42				72.4		6830		2.41

		72.8		5390		2.41				72.7		4700		2.41				74.3		5360		2.47				73.1		5390		2.43				72.8		4870		2.41				72.9		6340		2.42				72.5		6840		2.41

		72.8		5390		2.42				72.8		4700		2.42				74.4		5370		2.47				73.1		5400		2.43				72.9		4870		2.42				73		6340		2.42				72.6		6850		2.41

		72.9		5400		2.42				72.8		4710		2.42				74.4		5370		2.47				73.2		5400		2.43				72.9		4880		2.42				73.1		6350		2.43				72.6		6850		2.41

		73		5400		2.42				72.9		4710		2.42				74.5		5380		2.47				73.3		5410		2.43				73		4880		2.42				73.1		6350		2.43				72.7		6860		2.42

		73.1		5410		2.42				73		4710		2.42				74.6		5380		2.48				73.4		5410		2.43				73.1		4890		2.42				73.3		6360		2.43				72.8		6870		2.42

		73.1		5410		2.43				73		4720		2.42				74.6		5390		2.48				73.4		5420		2.44				73.2		4900		2.43				73.3		6370		2.43				72.8		6870		2.42

		73.2		5420		2.43				73.1		4720		2.43				74.7		5390		2.48				73.5		5420		2.44				73.2		4900		2.43				73.4		6370		2.44				72.9		6880		2.42

		73.2		5420		2.43				73.2		4730		2.43				74.8		5400		2.48				73.5		5420		2.44				73.3		4900		2.43				73.5		6380		2.44				73		6880		2.42

		73.3		5420		2.43				73.3		4730		2.43				74.9		5400		2.49				73.6		5430		2.44				73.3		4910		2.43				73.5		6380		2.44				73		6890		2.43

		73.4		5430		2.43				73.3		4740		2.43				74.9		5410		2.49				73.7		5430		2.44				73.4		4910		2.43				73.5		6390		2.44				73.1		6900		2.43

		73.4		5430		2.44				73.4		4740		2.44				75		5410		2.49				73.7		5440		2.45				73.5		4920		2.44				73.6		6390		2.44				73.2		6910		2.43

		73.5		5440		2.44				73.4		4740		2.44				75.1		5420		2.49				73.8		5440		2.45				73.5		4920		2.44				73.7		6400		2.45				73.3		6910		2.43

		73.6		5450		2.44				73.5		4750		2.44				75.2		5420		2.5				73.9		5440		2.45				73.6		4920		2.44				73.8		6410		2.45				73.3		6920		2.44

		73.7		5450		2.44				73.5		4750		2.44				75.2		5430		2.5				74		5440		2.45				73.7		4930		2.44				73.9		6410		2.45				73.4		6930		2.44

		73.7		5450		2.45				73.6		4750		2.44				75.3		5430		2.5				74		5450		2.46				73.8		4940		2.45				73.9		6420		2.45				73.4		6930		2.44

		73.8		5460		2.45				73.7		4760		2.45				75.3		5440		2.5				74		5450		2.46				73.8		4940		2.45				74		6420		2.46				73.5		6940		2.44

		73.9		5460		2.45				73.8		4760		2.45				75.4		5440		2.5				74.1		5450		2.46				73.9		4950		2.45				74		6430		2.46				73.6		6940		2.44

		73.9		5470		2.45				73.8		4770		2.45				75.5		5450		2.51				74.2		5460		2.46				74		4950		2.45				74.1		6430		2.46				73.6		6950		2.45

		74		5470		2.46				73.9		4770		2.45				75.5		5450		2.51				74.3		5470		2.47				74.1		4950		2.46				74.1		6440		2.46				73.7		6960		2.45

		74.1		5480		2.46				74		4780		2.46				75.6		5450		2.51				74.4		5470		2.47				74.1		4960		2.46				74.2		6440		2.46				73.8		6960		2.45

		74.1		5480		2.46				74		4780		2.46				75.7		5460		2.51				74.4		5470		2.47				74.2		4960		2.46				74.3		6450		2.47				73.9		6970		2.45

		74.2		5490		2.46				74.1		4780		2.46				75.8		5460		2.52				74.5		5480		2.47				74.2		4970		2.46				74.4		6460		2.47				73.9		6980		2.46

		74.3		5490		2.46				74.1		4790		2.46				75.9		5470		2.52				74.5		5480		2.47				74.3		4970		2.46				74.4		6460		2.47				74		6980		2.46

		74.3		5490		2.47				74.2		4790		2.46				75.9		5470		2.52				74.6		5480		2.48				74.4		4980		2.47				74.5		6470		2.47				74		6990		2.46

		74.4		5500		2.47				74.3		4790		2.47				76		5480		2.52				74.7		5490		2.48				74.4		4980		2.47				74.6		6470		2.48				74.1		6990		2.46

		74.4		5500		2.47				74.3		4800		2.47				76.1		5480		2.52				74.7		5490		2.48				74.5		4980		2.47				74.7		6480		2.48				74.2		7000		2.46

		74.5		5510		2.47				74.4		4800		2.47				76.1		5490		2.53				74.8		5490		2.48				74.6		4990		2.47				74.7		6480		2.48				74.3		7010		2.47

		74.6		5520		2.48				74.5		4810		2.47				76.2		5490		2.53				74.9		5500		2.49				74.7		4990		2.48				74.8		6480		2.48				74.4		7020		2.47

		74.7		5520		2.48				74.5		4810		2.48				76.2		5490		2.53				75		5500		2.49				74.7		5000		2.48				74.9		6490		2.48				74.4		7020		2.47

		74.8		5530		2.48				74.6		4810		2.48				76.3		5490		2.53				75		5510		2.49				74.8		5000		2.48				74.9		6500		2.49				74.5		7030		2.48

		74.9		5530		2.48				74.7		4820		2.48				76.4		5500		2.54				75.1		5510		2.49				74.9		5010		2.48				75		6510		2.49				74.5		7040		2.48

		74.9		5530		2.49				74.7		4820		2.48				76.4		5500		2.54				75.2		5510		2.49				75		5010		2.49				75.1		6510		2.49				74.6		7040		2.48

		75		5540		2.49				74.8		4830		2.48				76.5		5510		2.54				75.2		5520		2.5				75		5020		2.49				75.1		6510		2.49				74.7		7050		2.48

		75		5540		2.49				74.8		4830		2.49				76.6		5510		2.54				75.3		5520		2.5				75.1		5020		2.49				75.2		6520		2.5				74.7		7050		2.48

		75.1		5550		2.49				75		4840		2.49				76.6		5520		2.54				75.4		5520		2.5				75.1		5030		2.49				75.3		6520		2.5				74.8		7060		2.49

		75.2		5550		2.49				75.1		4840		2.49				76.7		5520		2.55				75.5		5530		2.51				75.2		5030		2.49				75.3		6530		2.5				74.9		7070		2.49

		75.2		5550		2.5				75.1		4850		2.49				76.7		5530		2.55				75.5		5540		2.51				75.3		5030		2.5				75.4		6530		2.5				75		7080		2.49

		75.3		5560		2.5				75.2		4850		2.5				76.9		5530		2.55				75.6		5540		2.51				75.3		5040		2.5				75.5		6540		2.51				75		7080		2.49

		75.3		5560		2.5				75.2		4850		2.5				76.9		5540		2.55				75.6		5540		2.51				75.4		5040		2.5				75.5		6540		2.51				75.1		7090		2.5

		75.4		5570		2.5				75.3		4860		2.5				77		5540		2.56				75.7		5550		2.51				75.5		5050		2.5				75.7		6550		2.51				75.2		7090		2.5

		75.4		5570		2.5				75.3		4860		2.5				77.1		5550		2.56				75.8		5550		2.52				75.6		5050		2.5				75.7		6560		2.51				75.2		7100		2.5

		75.5		5580		2.51				75.4		4860		2.5				77.1		5550		2.56				75.8		5560		2.52				75.6		5060		2.51				75.8		6560		2.52				75.3		7110		2.5

		75.6		5580		2.51				75.5		4870		2.51				77.2		5550		2.56				75.9		5560		2.52				75.7		5060		2.51				75.8		6570		2.52				75.4		7110		2.5

		75.6		5590		2.51				75.6		4870		2.51				77.2		5560		2.57				76		5560		2.52				75.7		5060		2.51				75.9		6570		2.52				75.4		7120		2.51

		75.8		5590		2.51				75.6		4880		2.51				77.3		5560		2.57				76		5570		2.52				75.8		5070		2.51				75.9		6580		2.52				75.5		7130		2.51

		75.8		5600		2.52				75.7		4880		2.51				77.5		5570		2.57				76.1		5570		2.53				75.9		5070		2.52				76		6580		2.52				75.6		7130		2.51

		75.9		5600		2.52				75.8		4880		2.52				77.5		5580		2.57				76.2		5580		2.53				76		5080		2.52				76.1		6590		2.53				75.6		7140		2.51

		76		5610		2.52				75.8		4890		2.52				77.6		5580		2.58				76.2		5580		2.53				76		5090		2.52				76.2		6600		2.53				75.7		7140		2.52

		76		5610		2.52				75.9		4890		2.52				77.6		5580		2.58				76.3		5580		2.53				76.1		5090		2.52				76.3		6600		2.53				75.8		7150		2.52

		76.1		5620		2.52				75.9		4900		2.52				77.7		5590		2.58				76.4		5590		2.54				76.2		5090		2.53				76.3		6600		2.53				75.8		7160		2.52

		76.2		5620		2.53				76		4900		2.52				77.8		5560		2.58				76.4		5590		2.54				76.2		5100		2.53				76.4		6610		2.54				75.9		7160		2.52

		76.2		5620		2.53				76.1		4910		2.53				77.8		5540		2.58				76.5		5600		2.54				76.3		5100		2.53				76.4		6610		2.54				75.9		7170		2.52

		76.3		5630		2.53				76.2		4910		2.53				77.9		5550		2.59				76.6		5600		2.54				76.4		5110		2.53				76.5		6620		2.54				76.1		7180		2.53

		76.3		5640		2.53				76.2		4910		2.53				78		5560		2.59				76.6		5610		2.54				76.4		5110		2.53				76.6		6620		2.54				76.1		7190		2.53

		76.4		5640		2.54				76.3		4920		2.53				78.1		5570		2.59				76.7		5610		2.55				76.5		5110		2.54				76.6		6630		2.54				76.2		7190		2.53

		76.5		5640		2.54				76.3		4920		2.54				78.1		5570		2.59				76.8		5620		2.55				76.6		5120		2.54				76.7		6630		2.55				76.3		7200		2.53

		76.6		5650		2.54				76.4		4920		2.54				78.2		5580		2.6				76.8		5620		2.55				76.7		5130		2.54				76.8		6640		2.55				76.3		7200		2.54

		76.6		5650		2.54				76.5		4930		2.54				78.3		5580		2.6				76.9		5620		2.55				76.7		5130		2.54				76.9		6650		2.55				76.4		7210		2.54

		76.7		5650		2.54				76.5		4930		2.54				78.3		5590		2.6				77		5630		2.55				76.8		5140		2.55				76.9		6650		2.55				76.4		7220		2.54

		76.8		5660		2.55				76.6		4930		2.54				78.4		5590		2.6				77		5630		2.56				76.9		5140		2.55				76.9		6660		2.56				76.5		7220		2.54

		76.8		5670		2.55				76.7		4940		2.55				78.4		5590		2.6				77.1		5640		2.56				76.9		5140		2.55				77		6660		2.56				76.6		7230		2.54

		76.9		5670		2.55				76.8		4950		2.55				78.6		5600		2.61				77.2		5640		2.56				77		5150		2.55				77.1		6670		2.56				76.7		7240		2.55

		77		5670		2.55				76.8		4950		2.55				78.6		5610		2.61				77.3		5640		2.56				77.1		5150		2.55				77.1		6670		2.56				76.7		7240		2.55

		77		5680		2.56				76.9		4950		2.55				78.7		5610		2.61				77.3		5640		2.57				77.2		5160		2.56				77.2		6680		2.56				76.8		7250		2.55

		77.1		5680		2.56				77		4960		2.56				78.7		5610		2.61				77.4		5640		2.57				77.2		5170		2.56				77.3		6680		2.57				76.9		7260		2.55

		77.2		5690		2.56				77.1		4960		2.56				78.8		5610		2.62				77.4		5640		2.57				77.3		5170		2.56				77.4		6690		2.57				76.9		7260		2.56

		77.2		5690		2.56				77.1		4960		2.56				78.9		5610		2.62				77.5		5640		2.57				77.4		5170		2.57				77.5		6700		2.57				77		7270		2.56

		77.3		5700		2.56				77.2		4970		2.56				78.9		5610		2.62				77.5		5650		2.57				77.4		5180		2.57				77.5		6700		2.57				77		7270		2.56

		77.3		5690		2.57				77.3		4980		2.57				79		5620		2.62				77.6		5650		2.58				77.5		5180		2.57				77.6		6700		2.58				77.1		7280		2.56

		77.4		5690		2.57				77.3		4980		2.57				79.1		5630		2.63				77.7		5660		2.58				77.6		5190		2.57				77.7		6710		2.58				77.2		7290		2.56

		77.5		5700		2.57				77.4		4980		2.57				79.2		5630		2.63				77.8		5660		2.58				77.6		5190		2.57				77.7		6720		2.58				77.3		7300		2.57

		77.6		5700		2.57				77.5		4990		2.57				79.3		5640		2.63				77.9		5670		2.59				77.6		5190		2.58				77.8		6720		2.58				77.3		7300		2.57

		77.6		5710		2.58				77.5		4990		2.58				79.3		5640		2.63				77.9		5670		2.59				77.8		5200		2.58				77.9		6720		2.58				77.4		7310		2.57

		77.7		5710		2.58				77.6		4990		2.58				79.4		5640		2.64				78		5670		2.59				77.8		5210		2.58				77.9		6730		2.59				77.5		7310		2.57

		77.8		5720		2.58				77.7		5000		2.58				79.4		5650		2.64				78.1		5680		2.59				77.9		5210		2.58				78		6740		2.59				77.5		7320		2.58

		77.8		5720		2.58				77.7		5000		2.58				79.5		5650		2.64				78.1		5680		2.59				78		5220		2.59				78		6740		2.59				77.6		7320		2.58

		77.9		5720		2.58				77.8		5010		2.58				79.6		5660		2.64				78.2		5680		2.6				78		5220		2.59				78.1		6750		2.59				77.6		7330		2.58

		78		5730		2.59				77.9		5010		2.59				79.7		5660		2.65				78.3		5690		2.6				78.1		5220		2.59				78.2		6750		2.6				77.7		7340		2.58

		78		5740		2.59				77.9		5010		2.59				79.7		5660		2.65				78.4		5690		2.6				78.2		5230		2.59				78.2		6760		2.6				77.8		7340		2.59

		78.1		5740		2.59				78		5020		2.59				79.8		5670		2.65				78.4		5700		2.6				78.2		5230		2.59				78.3		6760		2.6				77.8		7350		2.59

		78.2		5740		2.59				78.1		5020		2.59				79.8		5670		2.65				78.5		5700		2.61				78.3		5240		2.6				78.3		6770		2.6				77.9		7360		2.59

		78.3		5750		2.6				78.2		5030		2.59				79.9		5680		2.65				78.5		5700		2.61				78.4		5240		2.6				78.4		6770		2.6				78		7360		2.59

		78.3		5750		2.6				78.2		5030		2.6				80		5680		2.66				78.6		5710		2.61				78.5		5250		2.6				78.5		6780		2.61				78		7370		2.59

		78.4		5760		2.6				78.2		5030		2.6				80		5680		2.66				78.7		5710		2.61				78.6		5250		2.6				78.6		6780		2.61				78.1		7370		2.6

		78.4		5760		2.6				78.3		5040		2.6				80.1		5690		2.66				78.8		5720		2.61				78.6		5260		2.61				78.7		6790		2.61				78.2		7380		2.6

		78.5		5770		2.61				78.4		5040		2.6				80.1		5690		2.66				78.8		5720		2.62				78.7		5260		2.61				78.7		6790		2.61				78.2		7390		2.6

		78.6		5770		2.61				78.5		5050		2.61				80.3		5700		2.67				78.9		5730		2.62				78.7		5270		2.61				78.8		6800		2.62				78.3		7390		2.6

		78.7		5780		2.61				78.6		5050		2.61				80.3		5710		2.67				79		5730		2.62				78.8		5270		2.61				78.8		6800		2.62				78.4		7400		2.61

		78.7		5780		2.61				78.7		5060		2.61				80.4		5710		2.67				79.1		5730		2.62				78.8		5270		2.62				78.9		6810		2.62				78.4		7410		2.61

		78.8		5790		2.62				78.7		5060		2.61				80.5		5710		2.67				79.1		5740		2.63				78.9		5280		2.62				79		6810		2.62				78.5		7410		2.61

		78.9		5790		2.62				78.7		5060		2.62				80.5		5720		2.67				79.2		5740		2.63				79.1		5290		2.62				79		6820		2.62				78.6		7420		2.61

		78.9		5780		2.62				78.8		5070		2.62				80.6		5720		2.68				79.2		5750		2.63				79.1		5290		2.62				79.1		6820		2.63				78.6		7420		2.61

		79		5780		2.62				78.9		5070		2.62				80.6		5730		2.68				79.3		5750		2.63				79.2		5300		2.63				79.2		6830		2.63				78.7		7430		2.62

		79.1		5790		2.62				79		5080		2.62				80.7		5730		2.68				79.4		5750		2.64				79.2		5300		2.63				79.3		6830		2.63				78.8		7440		2.62

		79.2		5800		2.63				79.1		5080		2.63				80.8		5740		2.68				79.4		5760		2.64				79.3		5300		2.63				79.3		6840		2.63				78.8		7440		2.62

		79.3		5810		2.63				79.2		5090		2.63				80.9		5740		2.69				79.5		5760		2.64				79.3		5310		2.63				79.3		6840		2.64				78.9		7450		2.62

		79.3		5810		2.63				79.2		5090		2.63				80.9		5750		2.69				79.6		5770		2.64				79.4		5310		2.63				79.4		6850		2.64				79		7460		2.63

		79.4		5810		2.63				79.3		5090		2.63				81		5750		2.69				79.7		5770		2.64				79.5		5320		2.64				79.5		6850		2.64				79.1		7470		2.63

		79.4		5820		2.64				79.3		5100		2.63				81		5750		2.69				79.7		5740		2.65				79.6		5330		2.64				79.6		6860		2.64				79.2		7470		2.63

		79.5		5820		2.64				79.4		5100		2.64				81.1		5760		2.69				79.8		5740		2.65				79.7		5330		2.64				79.6		6860		2.64				79.2		7480		2.63

		79.5		5830		2.64				79.4		5110		2.64				81.2		5760		2.7				79.9		5750		2.65				79.7		5330		2.64				79.7		6870		2.65				79.2		7480		2.63

		79.6		5830		2.64				79.5		5110		2.64				81.2		5770		2.7				79.9		5750		2.65				79.8		5340		2.65				79.8		6880		2.65				79.3		7490		2.64

		79.7		5840		2.65				79.6		5110		2.64				81.3		5770		2.7				80		5760		2.65				79.8		5340		2.65				79.8		6880		2.65				79.4		7490		2.64

		79.8		5840		2.65				79.7		5120		2.65				81.4		5780		2.7				80		5760		2.66				79.9		5350		2.65				79.9		6890		2.65				79.4		7500		2.64

		79.8		5850		2.65				79.7		5120		2.65				81.5		5780		2.71				80.1		5770		2.66				80		5350		2.65				80		6890		2.66				79.5		7510		2.64

		79.9		5850		2.65				79.8		5120		2.65				81.5		5790		2.71				80.2		5770		2.66				80		5350		2.65				80.1		6900		2.66				79.6		7520		2.65

		80		5850		2.65				79.8		5120		2.65				81.6		5790		2.71				80.2		5780		2.66				80.1		5360		2.66				80.1		6900		2.66				79.7		7520		2.65

		80		5860		2.66				79.9		5120		2.65				81.7		5800		2.71				80.3		5760		2.67				80.2		5360		2.66				80.2		6910		2.66				79.7		7530		2.65

		80.1		5860		2.66				80		5120		2.66				81.7		5800		2.71				80.4		5760		2.67				80.3		5370		2.66				80.3		6910		2.66				79.8		7530		2.65

		80.2		5870		2.66				80		5130		2.66				81.8		5800		2.72				80.4		5760		2.67				80.3		5370		2.66				80.4		6920		2.67				79.8		7540		2.65

		80.2		5880		2.66				80.1		5130		2.66				81.9		5810		2.72				80.4		5760		2.67				80.4		5380		2.67				80.4		6920		2.67				79.9		7550		2.66

		80.3		5880		2.67				80.2		5140		2.66				82		5820		2.72				80.5		5770		2.67				80.4		5380		2.67				80.5		6930		2.67				80		7550		2.66

		80.4		5880		2.67				80.3		5150		2.67				82.1		5820		2.73				80.7		5770		2.68				80.5		5390		2.67				80.6		6930		2.67				80		7560		2.66

		80.5		5890		2.67				80.3		5150		2.67				82.1		5830		2.73				80.7		5780		2.68				80.6		5390		2.67				80.6		6940		2.68				80.1		7560		2.66

		80.5		5890		2.67				80.4		5150		2.67				82.2		5830		2.73				80.8		5780		2.68				80.6		5390		2.67				80.7		6940		2.68				80.2		7570		2.67

		80.6		5890		2.67				80.5		5160		2.67				82.2		5830		2.73				80.9		5780		2.68				80.7		5400		2.68				80.7		6950		2.68				80.3		7580		2.67

		80.7		5900		2.68				80.6		5160		2.68				82.3		5840		2.73				80.9		5780		2.69				80.8		5410		2.68				80.8		6950		2.68				80.3		7590		2.67

		80.7		5900		2.68				80.6		5160		2.68				82.4		5840		2.74				80.9		5790		2.69				80.9		5410		2.68				80.9		6960		2.69				80.4		7590		2.67

		80.8		5910		2.68				80.7		5170		2.68				82.4		5850		2.74				81		5790		2.69				80.9		5410		2.68				81		6970		2.69				80.4		7600		2.67

		80.9		5920		2.68				80.8		5170		2.68				82.5		5860		2.74				81.1		5790		2.69				81		5420		2.69				81		6970		2.69				80.5		7600		2.68

		80.9		5920		2.69				80.9		5180		2.69				82.6		5860		2.74				81.2		5800		2.7				81		5420		2.69				81.1		6980		2.69				80.6		7610		2.68

		81		5920		2.69				80.9		5180		2.69				82.7		5860		2.75				81.3		5800		2.7				81.1		5430		2.69				81.2		6980		2.7				80.7		7620		2.68

		81.1		5930		2.69				81		5190		2.69				82.7		5870		2.75				81.4		5800		2.7				81.2		5430		2.69				81.3		6990		2.7				80.7		7630		2.68

		81.1		5930		2.69				81.1		5190		2.69				82.8		5870		2.75				81.4		5810		2.7				81.2		5430		2.69				81.3		6990		2.7				80.8		7630		2.69

		81.2		5940		2.7				81.1		5190		2.69				82.9		5880		2.75				81.5		5810		2.7				81.4		5440		2.7				81.4		7000		2.7				80.9		7640		2.69

		81.3		5940		2.7				81.1		5190		2.7				82.9		5880		2.75				81.5		5810		2.71				81.4		5450		2.7				81.4		7000		2.7				80.9		7640		2.69

		81.4		5950		2.7				81.2		5200		2.7				83		5890		2.76				81.6		5810		2.71				81.5		5450		2.7				81.5		7010		2.71				81		7650		2.69

		81.4		5950		2.7				81.3		5200		2.7				83.1		5890		2.76				81.7		5820		2.71				81.5		5460		2.7				81.6		7020		2.71				81.1		7650		2.69

		81.5		5960		2.71				81.4		5210		2.7				83.2		5900		2.76				81.7		5820		2.71				81.6		5460		2.71				81.7		7020		2.71				81.1		7660		2.7

		81.6		5960		2.71				81.5		5210		2.71				83.2		5900		2.76				81.8		5830		2.72				81.7		5460		2.71				81.7		7030		2.71				81.2		7670		2.7

		81.6		5970		2.71				81.5		5210		2.71				83.3		5910		2.77				81.8		5820		2.72				81.7		5470		2.71				81.8		7030		2.72				81.2		7670		2.7

		81.7		5970		2.71				81.6		5220		2.71				83.4		5910		2.77				81.9		5830		2.72				81.8		5470		2.71				81.9		7040		2.72				81.3		7680		2.7

		81.8		5970		2.71				81.6		5220		2.71				83.4		5920		2.77				82		5830		2.72				81.9		5480		2.72				81.9		7040		2.72				81.4		7690		2.7

		81.8		5980		2.72				81.7		5230		2.71				83.5		5920		2.77				82		5830		2.72				82		5480		2.72				82		7040		2.72				81.4		7690		2.71

		81.9		5980		2.72				81.7		5230		2.72				83.6		5930		2.78				82.1		5830		2.73				82		5490		2.72				82		7050		2.72				81.5		7700		2.71

		82		5990		2.72				81.8		5230		2.72				83.6		5930		2.78				82.2		5840		2.73				82.1		5490		2.72				82.2		7060		2.73				81.6		7700		2.71

		82		5990		2.72				81.9		5240		2.72				83.7		5940		2.78				82.3		5840		2.73				82.2		5500		2.73				82.2		7070		2.73				81.6		7710		2.71

		82.1		6000		2.72				82		5240		2.72				83.8		5940		2.78				82.3		5850		2.73				82.2		5500		2.73				82.3		7070		2.73				81.7		7720		2.72

		82.2		6000		2.73				82.1		5240		2.72				83.9		5950		2.79				82.4		5850		2.74				82.3		5510		2.73				82.3		7070		2.74				81.8		7720		2.72

		82.2		6000		2.73				82.1		5250		2.73				83.9		5950		2.79				82.4		5850		2.74				82.3		5510		2.73				82.4		7080		2.74				81.8		7730		2.72

		82.2		6010		2.73				82.1		5250		2.73				84		5960		2.79				82.5		5860		2.74				82.4		5510		2.73				82.5		7080		2.74				81.9		7740		2.72

		82.3		6010		2.73				82.2		5260		2.73				84		5960		2.79				82.6		5860		2.74				82.5		5520		2.74				82.5		7090		2.74				82		7740		2.72

		82.4		6020		2.73				82.3		5260		2.73				84.1		5960		2.79				82.7		5860		2.74				82.6		5530		2.74				82.6		7090		2.74				82		7750		2.73

		82.5		6020		2.74				82.4		5260		2.74				84.2		5970		2.8				82.7		5860		2.75				82.7		5530		2.74				82.7		7100		2.75				82.1		7750		2.73

		82.6		6030		2.74				82.5		5270		2.74				84.2		5970		2.8				82.8		5860		2.75				82.7		5540		2.74				82.7		7110		2.75				82.1		7760		2.73

		82.6		6030		2.74				82.5		5270		2.74				84.4		5980		2.8				82.8		5870		2.75				82.8		5540		2.75				82.8		7110		2.75				82.2		7770		2.73

		82.7		6040		2.75				82.6		5280		2.74				84.4		5980		2.8				83		5870		2.75				82.9		5540		2.75				82.9		7120		2.75				82.2		7770		2.73

		82.7		6040		2.75				82.6		5280		2.75				84.5		5990		2.81				83		5870		2.76				82.9		5550		2.75				83		7120		2.75				82.3		7780		2.74

		82.8		6050		2.75				82.7		5290		2.75				84.5		5990		2.81				83.1		5870		2.76				83		5550		2.75				83		7120		2.76				82.4		7780		2.74

		82.9		6050		2.75				82.8		5290		2.75				84.6		6000		2.81				83.1		5880		2.76				83.1		5560		2.76				83.1		7130		2.76				82.5		7790		2.74

		82.9		6050		2.75				82.8		5290		2.75				84.7		6000		2.81				83.2		5870		2.76				83.2		5570		2.76				83.1		7130		2.76				82.5		7800		2.74

		83		6060		2.76				82.9		5300		2.75				84.7		6010		2.81				83.3		5880		2.77				83.2		5570		2.76				83.2		7140		2.76				82.6		7800		2.75

		83.1		6060		2.76				83		5300		2.76				84.8		6010		2.82				83.3		5880		2.77				83.3		5570		2.76				83.3		7150		2.77				82.7		7810		2.75

		83.2		6070		2.76				83.1		5310		2.76				84.9		6020		2.82				83.4		5880		2.77				83.4		5580		2.77				83.4		7150		2.77				82.7		7810		2.75

		83.2		6070		2.76				83.1		5310		2.76				85		6020		2.82				83.5		5880		2.77				83.4		5580		2.77				83.4		7160		2.77				82.8		7820		2.75

		83.3		6080		2.76				83.2		5310		2.76				85		6030		2.83				83.6		5880		2.78				83.5		5590		2.77				83.5		7160		2.77				82.9		7830		2.75

		83.4		6080		2.77				83.2		5320		2.77				85.1		6030		2.83				83.6		5890		2.78				83.5		5590		2.77				83.6		7170		2.78				83		7840		2.76

		83.4		6090		2.77				83.3		5320		2.77				85.2		6040		2.83				83.7		5890		2.78				83.6		5590		2.77				83.6		7170		2.78				83		7840		2.76

		83.5		6090		2.77				83.4		5330		2.77				85.3		6040		2.83				83.8		5890		2.78				83.7		5600		2.78				83.7		7180		2.78				83.1		7850		2.76

		83.6		6090		2.77				83.4		5330		2.77				85.3		6050		2.83				83.8		5890		2.78				83.7		5600		2.78				83.7		7180		2.78				83.1		7850		2.76

		83.7		6100		2.78				83.5		5330		2.77				85.4		6050		2.84				83.9		5890		2.79				83.8		5610		2.78				83.8		7190		2.79				83.2		7860		2.77

		83.7		6110		2.78				83.6		5340		2.78				85.4		6050		2.84				83.9		5890		2.79				83.9		5610		2.78				83.9		7190		2.79				83.2		7870		2.77

		83.8		6110		2.78				83.7		5340		2.78				85.5		6060		2.84				84		5900		2.79				83.9		5620		2.78				84		7200		2.79				83.3		7870		2.77

		83.8		6110		2.78				83.7		5350		2.78				85.6		6060		2.84				84.1		5900		2.79				84		5620		2.79				84.1		7200		2.79				83.4		7880		2.77

		83.9		6120		2.79				83.8		5350		2.78				85.7		6060		2.85				84.2		5900		2.8				84.1		5620		2.79				84.1		7210		2.79				83.5		7890		2.77

		84		6120		2.79				83.9		5360		2.79				85.8		6070		2.85				84.3		5900		2.8				84.1		5630		2.79				84.2		7210		2.8				83.6		7890		2.78

		84		6130		2.79				83.9		5360		2.79				85.8		6070		2.85				84.3		5900		2.8				84.2		5630		2.79				84.2		7220		2.8				83.6		7900		2.78

		84.1		6130		2.79				84		5360		2.79				85.8		6080		2.85				84.4		5900		2.8				84.3		5640		2.8				84.3		7220		2.8				83.6		7900		2.78

		84.1		6130		2.79				84.1		5370		2.79				85.9		6080		2.85				84.4		5900		2.8				84.4		5640		2.8				84.3		7230		2.8				83.7		7910		2.78

		84.3		6140		2.8				84.2		5370		2.8				86		6090		2.86				84.5		5900		2.81				84.4		5650		2.8				84.5		7240		2.81				83.8		7920		2.78

		84.3		6150		2.8				84.3		5380		2.8				86		6090		2.86				84.6		5900		2.81				84.5		5650		2.8				84.5		7240		2.81				83.9		7920		2.79

		84.4		6150		2.8				84.3		5380		2.8				86.2		6100		2.86				84.6		5900		2.81				84.5		5650		2.8				84.6		7250		2.81				83.9		7930		2.79

		84.5		6150		2.8				84.4		5390		2.8				86.2		6100		2.86				84.7		5900		2.81				84.6		5660		2.81				84.7		7250		2.81				84		7930		2.79

		84.5		6160		2.81				84.4		5390		2.81				86.3		6110		2.87				84.7		5900		2.81				84.6		5660		2.81				84.7		7250		2.81				84.1		7950		2.8

		84.6		6160		2.81				84.5		5390		2.81				86.3		6110		2.87				84.8		5900		2.82				84.7		5670		2.81				84.8		7260		2.82				84.1		7950		2.8

		84.6		6160		2.81				84.6		5400		2.81				86.4		6120		2.87				84.8		5900		2.82				84.8		5650		2.81				84.9		7260		2.82				84.2		7960		2.8

		84.7		6170		2.81				84.6		5400		2.81				86.4		6120		2.87				84.9		5910		2.82				84.9		5660		2.82				84.9		7270		2.82				84.3		7960		2.8

		84.8		6170		2.82				84.8		5410		2.82				86.5		6120		2.87				85		5910		2.82				85		5670		2.82				85		7270		2.82				84.3		7970		2.8

		84.9		6160		2.82				84.8		5410		2.82				86.6		6130		2.88				85.1		5910		2.82				85		5670		2.82				85.1		7280		2.83				84.4		7980		2.81

		85		6170		2.82				84.9		5420		2.82				86.7		6130		2.88				85.2		5920		2.83				85		5680		2.82				85.1		7280		2.83				84.5		7980		2.81

		85.1		6170		2.82				84.9		5420		2.82				86.8		6140		2.88				85.2		5910		2.83				85.1		5680		2.82				85.2		7290		2.83				84.6		7990		2.81

		85.1		6180		2.83				85		5420		2.82				86.8		6140		2.88				85.3		5920		2.83				85.2		5690		2.83				85.2		7290		2.83				84.6		8000		2.81

		85.1		6180		2.83				85		5430		2.83				86.9		6150		2.89				85.3		5920		2.83				85.2		5690		2.83				85.3		7300		2.83				84.7		8000		2.81

		85.2		6190		2.83				85.1		5430		2.83				86.9		6150		2.89				85.4		5920		2.84				85.3		5690		2.83				85.4		7300		2.84				84.8		8010		2.82

		85.3		6190		2.83				85.2		5430		2.83				87		6150		2.89				85.5		5920		2.84				85.4		5700		2.83				85.4		7310		2.84				84.8		8010		2.82

		85.4		6200		2.83				85.3		5440		2.83				87.1		6160		2.89				85.6		5930		2.84				85.5		5700		2.84				85.5		7310		2.84				84.9		8020		2.82

		85.4		6200		2.84				85.3		5440		2.84				87.1		6160		2.89				85.6		5930		2.84				85.5		5710		2.84				85.6		7320		2.84				84.9		8030		2.82

		85.5		6210		2.84				85.4		5450		2.84				87.2		6170		2.9				85.7		5930		2.85				85.6		5710		2.84				85.7		7330		2.85				85		8030		2.83

		85.6		6210		2.84				85.5		5450		2.84				87.3		6170		2.9				85.8		5940		2.85				85.7		5710		2.84				85.7		7330		2.85				85.1		8040		2.83

		85.6		6220		2.84				85.5		5450		2.84				87.4		6180		2.9				85.8		5940		2.85				85.7		5720		2.85				85.8		7340		2.85				85.1		8040		2.83

		85.7		6220		2.84				85.6		5460		2.84				87.5		6180		2.91				85.9		5940		2.85				85.8		5720		2.85				85.9		7340		2.85				85.2		8050		2.83

		85.8		6220		2.85				85.6		5460		2.85				87.5		6180		2.91				86		5950		2.85				85.9		5730		2.85				85.9		7350		2.85				85.3		8060		2.83

		85.8		6230		2.85				85.7		5470		2.85				87.6		6190		2.91				86		5950		2.86				86		5730		2.85				86		7350		2.86				85.4		8060		2.84

		85.9		6230		2.85				85.8		5470		2.85				87.7		6190		2.91				86.1		5950		2.86				86		5740		2.85				86.1		7360		2.86				85.4		8070		2.84

		86		6240		2.86				85.9		5480		2.85				87.7		6200		2.91				86.2		5960		2.86				86.1		5740		2.86				86.2		7070		2.86				85.5		8080		2.84

		86.1		6240		2.86				85.9		5480		2.85				87.8		6200		2.92				86.2		5960		2.86				86.2		5750		2.86				86.2		6830		2.87				85.6		8080		2.84

		86.1		6240		2.86				86		5480		2.86				87.8		6200		2.92				86.3		5960		2.86				86.2		5750		2.86				86.3		6810		2.87				85.6		8090		2.85

		86.2		6240		2.86				86		5490		2.86				87.9		6200		2.92				86.3		5970		2.87				86.3		5750		2.86				86.4		6810		2.87				85.6		8090		2.85

		86.3		6240		2.86				86.1		5490		2.86				88		6210		2.92				86.4		5970		2.87				86.4		5760		2.86				86.5		6810		2.87				85.7		8100		2.85

		86.3		6250		2.87				86.2		5490		2.86				88.1		6210		2.92				86.5		5970		2.87				86.4		5760		2.87				86.5		6810		2.87				85.8		8110		2.85

		86.4		6250		2.87				86.2		5500		2.87				88.1		6220		2.93				86.5		5970		2.87				86.4		5770		2.87				86.6		6810		2.88				85.9		8120		2.86

		86.4		6260		2.87				86.3		5500		2.87				88.2		6220		2.93				86.6		5970		2.88				86.5		5770		2.87				86.6		6810		2.88				86		8120		2.86

		86.6		6260		2.87				86.4		5500		2.87				88.3		6230		2.93				86.7		5980		2.88				86.6		5770		2.87				86.7		6810		2.88				86.1		8130		2.86

		86.6		6260		2.88				86.5		5510		2.87				88.3		6230		2.93				86.7		5970		2.88				86.6		5780		2.88				86.8		6820		2.88				86.1		8140		2.86

		86.7		6270		2.88				86.5		5520		2.88				88.4		6240		2.94				86.8		5960		2.88				86.7		5780		2.88				86.8		6830		2.89				86.2		8140		2.86

		86.8		6270		2.88				86.6		5520		2.88				88.4		6240		2.94				86.8		5960		2.88				86.8		5780		2.88				86.9		6830		2.89				86.2		8150		2.87

		86.8		6280		2.88				86.7		5520		2.88				88.6		6250		2.94				86.9		5960		2.89				86.8		5790		2.88				87		6840		2.89				86.3		8150		2.87

		86.9		6280		2.88				86.7		5530		2.88				88.6		6250		2.94				87		5220		2.89				86.9		5790		2.88				87		6840		2.89				86.4		8170		2.87

		87		6280		2.89				86.8		5530		2.88				88.7		6260		2.95				87.1		-512		2.89				87		5800		2.89				87.1		6850		2.89				86.5		8170		2.87

		87		6280		2.89				86.9		5530		2.89				88.7		6260		2.95				87.2		-511		2.9				87		5800		2.89				87.1		6850		2.9				86.5		8180		2.88

		87.1		6290		2.89				87		5540		2.89				88.8		6270		2.95												87.2		5810		2.89				87.2		6860		2.9				86.6		8180		2.88

		87.2		6300		2.89				87		5540		2.89				88.8		6270		2.95												87.2		5810		2.89				87.3		6860		2.9				86.6		8190		2.88

		87.2		6300		2.9				87.1		5550		2.89				88.9		6270		2.95												87.3		5820		2.9				87.4		6870		2.9				86.7		8190		2.88

		87.3		6300		2.9				87.1		5550		2.89				89		6280		2.96												87.3		5820		2.9				87.4		6880		2.9				86.8		8200		2.88

		87.4		6310		2.9				87.2		5550		2.9				89.1		6290		2.96												87.4		5820		2.9				87.5		6870		2.91				86.8		8210		2.89

		87.5		6310		2.9				87.3		5560		2.9				89.1		6290		2.96												87.4		5820		2.9				87.6		6850		2.91				86.9		8210		2.89

		87.5		6310		2.91				87.3		5560		2.9				89.2		6290		2.96												87.5		5830		2.9				87.6		6850		2.91				87		8220		2.89

		87.6		6300		2.91				87.4		5560		2.9				89.2		6300		2.97												87.6		5830		2.91				87.7		6850		2.91				87		8220		2.89

		87.7		6280		2.91				87.4		5570		2.9				89.3		6300		2.97												87.7		5830		2.91				87.8		6850		2.92				87.1		8230		2.9

		87.8		6280		2.91				87.5		5570		2.91				89.4		6310		2.97												87.8		5840		2.91				87.8		6850		2.92				87.2		8240		2.9

		87.8		6280		2.92				87.6		5580		2.91				89.4		6310		2.97												87.8		5840		2.92				87.9		6860		2.92				87.2		8240		2.9

		87.9		6280		2.92				87.7		5580		2.91				89.5		6320		2.97												87.9		5840		2.92				88		6860		2.92				87.3		8250		2.9

		88		5790		2.92				87.7		5590		2.92				89.6		6320		2.98												88		5850		2.92				88		6860		2.92				87.4		8250		2.9

		88		2200		2.93				87.8		5590		2.92				89.7		6330		2.98												88		5850		2.92				88.1		6860		2.93				87.4		8260		2.91

		88.1		-438		2.93				87.9		5590		2.92				89.7		6330		2.98												88.1		5850		2.92				88.1		6870		2.93				87.5		8270		2.91

		88.1		-437		2.93				88		5600		2.92				89.8		6330		2.98												88.2		5860		2.93				88.2		6870		2.93				87.6		8280		2.91

										88		5600		2.92				89.9		6330		2.99												88.3		5860		2.93				88.3		6880		2.93				87.7		8280		2.91

										88.1		5600		2.93				89.9		6340		2.99												88.3		5850		2.93				88.4		6880		2.93				87.7		8290		2.92

										88.1		5610		2.93				90		6340		2.99												88.4		5850		2.93				88.5		6890		2.94				87.8		8290		2.92

										88.2		5610		2.93				90		6350		2.99												88.5		5860		2.94				88.5		6900		2.94				87.8		8300		2.92

										88.3		5610		2.93				90.1		6350		2.99												88.5		5860		2.94				88.6		6900		2.94				87.9		8310		2.92

										88.4		5620		2.94				90.2		6360		3												88.6		5870		2.94				88.6		6910		2.94				88		8310		2.92

										88.4		5620		2.94				90.3		6360		3												88.6		5870		2.94				88.7		6910		2.95				88		8320		2.93

										88.5		5630		2.94				90.3		6370		3												88.7		5870		2.94				88.8		6920		2.95				88.1		8330		2.93

										88.5		5630		2.94				90.4		6370		3												88.8		5880		2.95				88.8		6930		2.95				88.2		8330		2.93

										88.6		5630		2.94				90.5		6380		3.01												88.9		5880		2.95				88.9		6930		2.95				88.2		8340		2.93

										88.7		5640		2.95				90.5		6380		3.01												88.9		5890		2.95				88.9		6940		2.95				88.3		8350		2.94

										88.8		5640		2.95				90.6		6390		3.01												89		5890		2.95				89		6940		2.96				88.4		8350		2.94

										88.9		5650		2.95				90.7		6390		3.01												89		5890		2.96				89.1		6950		2.96				88.4		8360		2.94

										88.9		5650		2.95				90.8		6400		3.02												89.1		5900		2.96				89.2		6950		2.96				88.5		8360		2.94

										89		5660		2.96				90.8		6400		3.02												89.2		5900		2.96				89.2		6950		2.96				88.6		8370		2.94

										89		5660		2.96				90.9		6410		3.02												89.2		5900		2.96				89.3		3430		2.97				88.7		8380		2.95

										89.1		5660		2.96				91		6410		3.02												89.3		5900		2.96				89.3		-441		2.97				88.7		8380		2.95

										89.1		5670		2.96				91		6420		3.02												89.4		5900		2.97				89.4		-438		2.97				88.8		8390		2.95

										89.2		5670		2.96				91.1		6420		3.03												89.4		5900		2.97												88.8		8390		2.95

										89.3		5670		2.97				91.2		6420		3.03												89.5		5900		2.97												88.9		8400		2.96

										89.4		5680		2.97				91.2		6430		3.03												89.6		5900		2.97												89		8410		2.96

										89.5		5690		2.97				91.3		6430		3.03												89.7		5910		2.98												89		8410		2.96

										89.5		5690		2.97				91.4		6440		3.04												89.7		5910		2.98												89.1		8420		2.96

										89.6		5690		2.98				91.5		6440		3.04												89.8		5920		2.98												89.1		8420		2.96

										89.6		5700		2.98				91.5		6450		3.04												89.8		5920		2.98												89.3		8430		2.97

										89.7		5700		2.98				91.6		6450		3.04												89.9		5820		2.98												89.3		8440		2.97

										89.8		5710		2.98				91.6		6460		3.04												89.9		5790		2.99												89.4		8450		2.97

										89.8		5710		2.99				91.7		6460		3.05												90		5790		2.99												89.5		8450		2.97

										90		5720		2.99				91.8		6460		3.05												90.1		5790		2.99												89.5		8460		2.98

										90		5720		2.99				91.9		6470		3.05												90.1		5780		2.99												89.5		8460		2.98

										90.1		5720		2.99				91.9		6480		3.05												90.2		5770		2.99												89.6		8470		2.98

										90.1		5730		3				92		6480		3.06												90.3		5750		3												89.7		8480		2.98

										90.2		5730		3				92.1		6480		3.06												90.3		5750		3												89.7		8480		2.98

										90.3		5740		3				92.1		6490		3.06												90.4		5730		3												89.8		8490		2.99

										90.4		5740		3				92.2		6490		3.06												90.5		5530		3												89.9		8490		2.99

										90.4		5740		3				92.3		6500		3.07												90.5		5210		3.01												89.9		8500		2.99

										90.5		5750		3.01				92.3		6500		3.07												90.6		5160		3.01												90		8500		2.99

										90.6		5750		3.01				92.4		6510		3.07												90.7		5140		3.01												90.1		8510		2.99

										90.6		5760		3.01				92.5		6510		3.07												90.8		5110		3.01												90.1		8520		3

										90.7		5760		3.01				92.6		6520		3.08												90.8		5100		3.01												90.2		8520		3

										90.8		5770		3.02				92.6		6520		3.08												90.8		5080		3.02												90.3		8530		3

										90.8		5770		3.02				92.7		6530		3.08												90.9		1840		3.02												90.3		8530		3

										90.9		5770		3.02				92.8		6530		3.08												91		-381		3.02												90.4		8540		3.01

										90.9		5780		3.02				92.8		6540		3.08																												90.5		8550		3.01

										91		5780		3.02				92.9		6540		3.09																												90.5		8550		3.01

										91.2		5790		3.03				93		6550		3.09																												90.6		8560		3.01

										91.2		5790		3.03				93.1		6550		3.09																												90.6		8570		3.01

										91.3		5800		3.03				93.1		6560		3.09																												90.7		8570		3.02

										91.3		5800		3.04				93.2		6560		3.1																												90.8		8580		3.02

										91.4		5800		3.04				93.2		6570		3.1																												90.8		8580		3.02

										91.4		5800		3.04				93.3		6570		3.1																												90.9		8590		3.02

										91.5		5810		3.04				93.4		6570		3.1																												91		8600		3.03

										91.6		5810		3.04				93.4		6580		3.1																												91.1		8600		3.03

										91.7		5820		3.05				93.5		6580		3.11																												91.1		8610		3.03

										91.8		5820		3.05				93.6		6590		3.11																												91.2		8610		3.03

										91.8		5820		3.05				93.7		6600		3.11																												91.3		8620		3.03

										91.9		5830		3.05				93.7		6600		3.12																												91.3		8630		3.04

										91.9		5830		3.05				93.8		6600		3.12																												91.4		8630		3.04

										92		5830		3.06				93.9		6610		3.12																												91.4		8640		3.04

										92		5730		3.06				93.9		6610		3.12																												91.5		8650		3.04

										92.1		5210		3.06				94		6610		3.12																												91.6		8650		3.04

										92.2		5160		3.06				94.1		6620		3.13																												91.6		8660		3.05

										92.3		5150		3.07				94.2		6620		3.13																												91.7		8670		3.05

										92.3		5140		3.07				94.2		6630		3.13																												91.8		8670		3.05

										92.4		5140		3.07				94.3		6630		3.13																												91.8		8680		3.05

										92.5		5140		3.07				94.3		6640		3.13																												91.9		8680		3.06

										92.5		5140		3.07				94.4		6640		3.14																												91.9		8690		3.06

										92.6		5130		3.08				94.5		6650		3.14																												92		8690		3.06

										92.7		5130		3.08				94.5		6650		3.14																												92.1		8710		3.06

										92.7		5110		3.08				94.6		6650		3.14																												92.2		8710		3.07

										92.8		2830		3.09				94.7		6660		3.15																												92.3		8720		3.07

										92.9		-346		3.09				94.8		6660		3.15																												92.3		8720		3.07

										92.9		-344		3.09				94.9		6670		3.15																												92.4		8730		3.07

																		94.9		6670		3.15																												92.4		8730		3.07

																		95		6680		3.16																												92.5		8740		3.08

																		95		6680		3.16																												92.6		8750		3.08

																		95.1		6680		3.16																												92.7		8760		3.08

																		95.1		6690		3.16																												92.8		8760		3.08

																		95.2		6690		3.16																												92.8		8770		3.09

																		95.4		6700		3.17																												92.9		8780		3.09

																		95.4		6700		3.17																												92.9		8780		3.09

																		95.5		6710		3.17																												93		8790		3.09

																		95.6		6710		3.17																												93.1		8790		3.09

																		95.6		6700		3.18																												93.2		8800		3.1

																		95.6		6640		3.18																												93.3		8810		3.1

																		95.7		3380		3.18																												93.3		8810		3.1

																		95.8		-437		3.19																												93.4		8820		3.1

																		95.8		-436		3.19																												93.4		8830		3.11

																																																		93.5		8830		3.11

																																																		93.5		8840		3.11

																																																		93.6		8840		3.11

																																																		93.7		8850		3.11

																																																		93.7		8850		3.12

																																																		93.8		8860		3.12

																																																		93.9		8870		3.12

																																																		93.9		8870		3.12

																																																		94		8880		3.12

																																																		94		8890		3.13

																																																		94.1		8890		3.13

																																																		94.2		8900		3.13

																																																		94.3		8900		3.13

																																																		94.3		8910		3.14

																																																		94.4		8920		3.14

																																																		94.4		8920		3.14

																																																		94.5		8930		3.14

																																																		94.6		8930		3.14

																																																		94.7		8940		3.15

																																																		94.7		8950		3.15

																																																		94.8		8950		3.15

																																																		94.8		8960		3.15

																																																		94.9		8960		3.16

																																																		95		8970		3.16

																																																		95		8980		3.16

																																																		95.1		8980		3.16

																																																		95.2		8990		3.16

																																																		95.3		8990		3.17

																																																		95.3		9000		3.17

																																																		95.4		9010		3.17

																																																		95.4		9010		3.17

																																																		95.5		9020		3.18

																																																		95.6		9030		3.18

																																																		95.6		9030		3.18

																																																		95.7		9040		3.18

																																																		95.8		9040		3.18

																																																		95.8		9050		3.19

																																																		95.9		9060		3.19

																																																		95.9		9060		3.19

																																																		96		9070		3.19

																																																		96.1		9080		3.2

																																																		96.2		9080		3.2

																																																		96.2		9090		3.2

																																																		96.3		9090		3.2

																																																		96.3		9100		3.2

																																																		96.4		9100		3.21

																																																		96.5		9110		3.21

																																																		96.5		9120		3.21

																																																		96.6		9120		3.21

																																																		96.7		9130		3.22

																																																		96.8		9140		3.22

																																																		96.8		9140		3.22

																																																		96.9		9150		3.22

																																																		97		9150		3.22

																																																		97		9160		3.23

																																																		97.1		9170		3.23

																																																		97.2		9170		3.23

																																																		97.2		9180		3.23

																																																		97.3		9180		3.24

																																																		97.3		9190		3.24

																																																		97.4		9200		3.24

																																																		97.5		9200		3.24

																																																		97.6		9210		3.24

																																																		97.6		9210		3.25

																																																		97.7		9220		3.25

																																																		97.8		9230		3.25

																																																		97.8		9230		3.25

																																																		97.9		9240		3.25

																																																		97.9		9240		3.26

																																																		98		9250		3.26

																																																		98.1		9260		3.26

																																																		98.2		9260		3.26

																																																		98.2		9270		3.27

																																																		98.3		9270		3.27

																																																		98.3		9280		3.27

																																																		98.4		9290		3.27

																																																		98.5		9290		3.27

																																																		98.5		9300		3.28

																																																		98.6		9300		3.28

																																																		98.7		9310		3.28

																																																		98.7		9310		3.28

																																																		98.8		9320		3.28

																																																		98.9		9330		3.29

																																																		98.9		9340		3.29

																																																		99		9340		3.29

																																																		99.1		9350		3.29

																																																		99.2		9350		3.3

																																																		99.2		9360		3.3

																																																		99.2		9360		3.3

																																																		99.3		9370		3.3

																																																		99.4		9370		3.3

																																																		99.5		9390		3.31

																																																		99.6		9390		3.31

																																																		99.7		9400		3.31

																																																		99.7		9400		3.32

																																																		99.8		9410		3.32

																																																		99.8		9410		3.32

																																																		99.9		9420		3.32

																																																		100		9420		3.32

																																																		100		9430		3.33

																																																		100		9440		3.33

																																																		100		9440		3.33

																																																		100		9450		3.33

																																																		100		9450		3.34

																																																		100		9460		3.34

																																																		100		9470		3.34

																																																		101		9470		3.34

																																																		101		9480		3.35

																																																		101		9480		3.35

																																																		101		9490		3.35

																																																		101		9500		3.35

																																																		101		9500		3.35

																																																		101		9510		3.36

																																																		101		9510		3.36

																																																		101		9520		3.36

																																																		101		9520		3.36

																																																		101		9530		3.37

																																																		101		9540		3.37

																																																		101		9540		3.37

																																																		101		9550		3.37

																																																		101		9550		3.37

																																																		102		9560		3.38

																																																		102		9560		3.38

																																																		102		9570		3.38

																																																		102		9580		3.38

																																																		102		9580		3.38

																																																		102		9590		3.39

																																																		102		9600		3.39

																																																		102		9600		3.39

																																																		102		9610		3.39

																																																		102		9610		3.4

																																																		102		9620		3.4

																																																		102		9620		3.4

																																																		102		9630		3.4

																																																		102		9630		3.4

																																																		102		9640		3.41

																																																		102		9640		3.41

																																																		103		9650		3.41

																																																		103		9660		3.41

																																																		103		9660		3.41

																																																		103		9670		3.42

																																																		103		9670		3.42

																																																		103		9680		3.42

																																																		103		9690		3.42

																																																		103		9690		3.43

																																																		103		9700		3.43

																																																		103		9710		3.43

																																																		103		9710		3.43

																																																		103		9720		3.43

																																																		103		9720		3.44

																																																		103		9730		3.44

																																																		103		9730		3.44

																																																		104		9740		3.45

																																																		104		9750		3.45

																																																		104		9750		3.45

																																																		104		9760		3.45

																																																		104		9760		3.45

																																																		104		9760		3.46

																																																		104		9760		3.46

																																																		104		9760		3.46

																																																		104		9770		3.46

																																																		104		9780		3.47

																																																		104		9770		3.47

																																																		104		9770		3.47

																																																		104		9770		3.47

																																																		104		9780		3.47

																																																		105		9790		3.48

																																																		105		9800		3.48

																																																		105		9800		3.48

																																																		105		9790		3.48

																																																		105		9760		3.49

																																																		105		9750		3.49

																																																		105		9720		3.49

																																																		105		9720		3.49

																																																		105		9730		3.49

																																																		105		9720		3.5

																																																		105		9670		3.5

																																																		105		9680		3.5

																																																		105		9690		3.5

																																																		105		9690		3.51

																																																		105		9690		3.51

																																																		106		9700		3.51

																																																		106		9700		3.51

																																																		106		9700		3.52

																																																		106		9710		3.52

																																																		106		9710		3.52

																																																		106		9720		3.52

																																																		106		9720		3.53

																																																		106		9730		3.53

																																																		106		9730		3.53

																																																		106		9730		3.53

																																																		106		9730		3.53

																																																		106		9730		3.54

																																																		106		9730		3.54

																																																		106		9740		3.54

																																																		107		9740		3.54

																																																		107		9740		3.55

																																																		107		9730		3.55

																																																		107		9710		3.55

																																																		107		9690		3.55

																																																		107		9690		3.55

																																																		107		9690		3.56

																																																		107		9700		3.56

																																																		107		9700		3.56

																																																		107		9700		3.56

																																																		107		9700		3.57

																																																		107		9700		3.57

																																																		107		9710		3.57

																																																		107		9710		3.57

																																																		107		9720		3.57

																																																		108		9720		3.58

																																																		108		9730		3.58

																																																		108		9730		3.58

																																																		108		9740		3.58

																																																		108		9740		3.59

																																																		108		9740		3.59

																																																		108		9750		3.59

																																																		108		9750		3.59

																																																		108		9760		3.6

																																																		108		9760		3.6

																																																		108		9760		3.6

																																																		108		9760		3.6

																																																		108		9770		3.61

																																																		108		9770		3.61

																																																		109		9770		3.61

																																																		109		9770		3.61

																																																		109		9780		3.62

																																																		109		9780		3.62

																																																		109		9780		3.62

																																																		109		9780		3.62

																																																		109		9780		3.62

																																																		109		9790		3.63

																																																		109		9790		3.63

																																																		109		9790		3.63

																																																		109		9800		3.63

																																																		109		9800		3.64

																																																		109		9800		3.64

																																																		109		9810		3.64

																																																		110		9810		3.64

																																																		110		9810		3.64

																																																		110		9820		3.65

																																																		110		9820		3.65

																																																		110		9830		3.65

																																																		110		9830		3.66

																																																		110		9830		3.66

																																																		110		9830		3.66

																																																		110		9830		3.66

																																																		110		9820		3.66

																																																		110		9820		3.67

																																																		110		9820		3.67

																																																		110		9750		3.67

																																																		110		4670		3.68

																																																		111		-379		3.68

																																																		111		-372		3.68





PLA 3 mm PLA 10 proc

		Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)				Time (sec)		Force (N)		Position (mm)

		0.325		0.833		0				0.312		-2.5		0				0.154		-5		0				0.173		-8.33		0				0.31		-10		0				0.194		-9.17		0				0.242		-7.5		0				0.198		-6.67		0

		0.511		0		0				0.437		-2.5		0				0.247		-5.83		0				0.298		-8.33		0				0.438		-10.8		0				0.35		-9.17		0				0.368		-7.5		0				0.324		-6.67		0

		0.699		16.7		0.003				0.593		0.833		0.001				0.373		-5.83		0				0.454		-8.33		0				0.565		-7.5		0.001				0.475		-5.83		0.001				0.493		-5		0.001				0.449		-4.17		0.001

		0.761		34.2		0.005				0.719		36.7		0.005				0.499		-2.5		0.001				0.58		-5		0.001				0.698		30.8		0.005				0.537		10		0.003				0.556		6.67		0.003				0.511		13.3		0.003

		0.823		54.2		0.007				0.782		57.5		0.007				0.591		13.3		0.003				0.675		30.8		0.005				0.761		50		0.007				0.632		50.8		0.007				0.681		38.3		0.007				0.643		57.5		0.007

		0.885		73.3		0.009				0.815		77.5		0.009				0.685		43.3		0.006				0.767		48.3		0.007				0.824		68.3		0.01				0.724		70.8		0.009				0.744		53.3		0.009				0.705		77.5		0.01

		0.947		91.7		0.011				0.877		96.7		0.012				0.748		62.5		0.008				0.83		67.5		0.009				0.887		85.8		0.012				0.786		90		0.011				0.807		68.3		0.011				0.767		95.8		0.012

		1.02		110		0.013				0.97		113		0.014				0.811		81.7		0.011				0.893		85.8		0.011				0.95		103		0.014				0.819		108		0.014				0.87		83.3		0.013				0.829		113		0.014

		1.05		132		0.016				1.05		133		0.016				0.848		101		0.013				0.925		104		0.013				1.01		121		0.016				0.911		127		0.016				0.903		99.2		0.016				0.891		132		0.016

		1.15		149		0.018				1.05		153		0.018				0.94		121		0.015				1.02		121		0.016				1.08		137		0.018				0.974		145		0.018				0.995		113		0.018				0.953		149		0.018

		1.24		182		0.022				1.11		162		0.02				1		138		0.017				1.05		138		0.018				1.14		152		0.02				1.04		163		0.02				1.06		126		0.02				1.02		167		0.02

		1.3		197		0.024				1.23		193		0.024				1.07		155		0.019				1.14		153		0.02				1.23		172		0.023				1.1		179		0.022				1.12		140		0.022				1.08		183		0.022

		1.37		212		0.027				1.33		207		0.026				1.13		172		0.021				1.24		183		0.024				1.3		184		0.025				1.16		195		0.024				1.21		160		0.025				1.17		215		0.026

		1.46		226		0.029				1.39		218		0.028				1.26		204		0.025				1.33		199		0.026				1.36		198		0.028				1.22		218		0.027				1.28		171		0.027				1.26		230		0.029

		1.49		240		0.031				1.42		228		0.03				1.32		219		0.028				1.39		214		0.028				1.42		211		0.03				1.32		232		0.029				1.34		183		0.03				1.33		244		0.031

		1.59		253		0.033				1.48		238		0.032				1.38		233		0.03				1.46		228		0.031				1.49		225		0.032				1.38		245		0.031				1.37		194		0.032				1.39		258		0.033

		1.62		267		0.035				1.54		248		0.034				1.44		248		0.032				1.52		243		0.033				1.55		238		0.034				1.44		257		0.033				1.47		206		0.034				1.45		270		0.035

		1.68		280		0.037				1.61		258		0.036				1.51		262		0.034				1.58		258		0.035				1.62		250		0.037				1.47		268		0.035				1.53		216		0.036				1.51		283		0.037

		1.77		293		0.039				1.67		268		0.038				1.57		276		0.036				1.64		272		0.037				1.68		263		0.039				1.56		278		0.038				1.59		228		0.038				1.58		293		0.039

		1.83		312		0.042				1.76		280		0.042				1.6		290		0.038				1.71		286		0.039				1.78		288		0.043				1.63		288		0.04				1.65		237		0.04				1.64		304		0.041

		1.9		324		0.044				1.83		289		0.044				1.7		305		0.04				1.83		313		0.043				1.87		299		0.045				1.69		298		0.042				1.78		258		0.044				1.76		328		0.045

		1.99		336		0.046				1.92		298		0.046				1.82		332		0.045				1.86		323		0.045				1.93		311		0.047				1.82		318		0.046				1.84		268		0.046				1.83		337		0.047

		2.02		348		0.049				1.95		307		0.048				1.89		345		0.047				1.96		335		0.047				2		323		0.049				1.88		328		0.048				1.9		277		0.049				1.86		348		0.049

		2.08		359		0.051				2.01		316		0.05				1.95		359		0.049				2.02		344		0.049				2.06		333		0.051				1.94		337		0.05				1.98		289		0.051				1.95		358		0.051

		2.15		370		0.053				2.07		323		0.052				2.01		372		0.051				2.08		354		0.052				2.07		343		0.053				2		346		0.052				2.05		300		0.054				1.98		368		0.053

		2.24		382		0.055				2.14		331		0.054				2.08		385		0.053				2.14		363		0.054				2.19		355		0.056				2.06		356		0.054				2.12		309		0.055				2.08		378		0.056

		2.25		393		0.057				2.23		339		0.056				2.14		398		0.055				2.21		372		0.056				2.25		365		0.058				2.13		365		0.056				2.18		319		0.057				2.14		388		0.058

		2.33		398		0.058				2.32		354		0.06				2.2		412		0.057				2.27		380		0.058				2.38		383		0.062				2.19		374		0.059				2.24		328		0.06				2.17		398		0.06

		2.4		414		0.061				2.39		363		0.062				2.26		423		0.059				2.39		396		0.062				2.44		392		0.064				2.25		383		0.061				2.34		347		0.064				2.23		406		0.062

		2.46		425		0.063				2.48		373		0.064				2.39		449		0.064				2.43		404		0.064				2.5		401		0.066				2.31		392		0.063				2.43		355		0.066				2.39		423		0.066

		2.52		435		0.065				2.54		384		0.066				2.45		462		0.066				2.52		413		0.066				2.57		409		0.068				2.41		408		0.067				2.49		364		0.068				2.45		432		0.068

		2.61		445		0.067				2.57		398		0.068				2.52		473		0.068				2.59		420		0.068				2.63		418		0.07				2.5		418		0.069				2.55		372		0.07				2.48		440		0.07

		2.68		453		0.07				2.64		411		0.071				2.58		486		0.07				2.66		429		0.071				2.69		426		0.072				2.56		426		0.071				2.61		380		0.072				2.55		448		0.072

		2.71		463		0.072				2.7		424		0.073				2.64		498		0.072				2.72		436		0.073				2.76		434		0.074				2.62		434		0.073				2.68		388		0.074				2.64		456		0.074

		2.77		471		0.074				2.79		438		0.075				2.68		509		0.074				2.79		443		0.075				2.82		442		0.077				2.66		442		0.075				2.74		396		0.076				2.7		463		0.077

		2.86		478		0.076				2.85		455		0.078				2.77		521		0.076				2.88		458		0.079				2.92		457		0.081				2.75		450		0.077				2.8		403		0.078				2.76		471		0.079

		2.93		488		0.079				2.92		466		0.08				2.83		532		0.078				2.98		464		0.081				3.01		464		0.083				2.81		458		0.079				2.93		418		0.083				2.82		478		0.081

		2.99		494		0.081				3.01		478		0.082				2.93		554		0.082				3.04		470		0.083				3.07		472		0.085				2.84		465		0.081				2.99		424		0.085				2.93		490		0.084

		3.05		499		0.083				3.04		488		0.084				3.02		564		0.084				3.1		477		0.086				3.14		478		0.087				2.9		473		0.083				3.05		431		0.087				2.99		497		0.086

		3.15		506		0.085				3.14		499		0.086				3.08		576		0.087				3.16		483		0.088				3.2		484		0.089				3.06		488		0.087				3.12		437		0.089				3.07		505		0.089

		3.21		512		0.087				3.2		509		0.088				3.15		588		0.089				3.23		490		0.09				3.23		491		0.091				3.12		496		0.09				3.18		443		0.091				3.13		511		0.091

		3.24		519		0.089				3.23		520		0.09				3.21		598		0.091				3.29		496		0.092				3.32		497		0.094				3.18		502		0.092				3.24		448		0.093				3.19		518		0.093

		3.3		525		0.092				3.32		529		0.093				3.27		608		0.093				3.35		502		0.094				3.45		508		0.097				3.25		510		0.094				3.28		453		0.095				3.25		523		0.095

		3.39		532		0.093				3.42		548		0.097				3.34		619		0.095				3.45		514		0.098				3.48		514		0.1				3.31		518		0.096				3.34		458		0.097				3.32		529		0.097

		3.43		538		0.095				3.48		558		0.099				3.46		641		0.099				3.51		520		0.1				3.55		519		0.102				3.37		525		0.098				3.49		468		0.102				3.35		535		0.099

		3.49		544		0.097				3.57		568		0.101				3.53		653		0.101				3.6		526		0.102				3.61		524		0.104				3.44		532		0.1				3.53		473		0.103				3.5		548		0.103

		3.55		551		0.1				3.6		577		0.103				3.59		664		0.104				3.68		533		0.105				3.7		529		0.106				3.5		538		0.102				3.62		478		0.105				3.54		553		0.105

		3.61		557		0.102				3.67		586		0.105				3.65		674		0.105				3.74		539		0.107				3.74		534		0.108				3.62		552		0.106				3.68		482		0.108				3.63		560		0.107

		3.68		563		0.104				3.73		595		0.107				3.72		685		0.107				3.77		545		0.109				3.83		539		0.11				3.66		560		0.109				3.74		486		0.11				3.69		566		0.11

		3.74		570		0.106				3.79		604		0.109				3.78		696		0.11				3.86		551		0.111				3.96		548		0.114				3.75		570		0.111				3.81		490		0.112				3.75		571		0.112

		3.8		576		0.108				3.85		613		0.111				3.84		707		0.112				3.93		557		0.113				4.02		553		0.117				3.81		582		0.113				3.87		494		0.114				3.82		577		0.114

		3.86		582		0.11				3.98		627		0.114				3.97		729		0.116				4.02		565		0.116				4.08		558		0.119				3.87		593		0.115				3.93		499		0.116				3.85		583		0.116

		3.93		588		0.112				4.01		635		0.116				4.03		740		0.118				4.05		570		0.118				4.15		562		0.121				3.94		604		0.117				4.06		508		0.12				3.94		588		0.118

		4.02		598		0.115				4.07		643		0.118				4.09		750		0.12				4.15		575		0.12				4.21		566		0.123				4		616		0.119				4.12		512		0.122				4.04		600		0.122

		4.08		604		0.117				4.13		651		0.121				4.16		761		0.122				4.21		581		0.122				4.27		570		0.125				4.06		627		0.121				4.18		517		0.125				4.13		606		0.124

		4.17		610		0.119				4.2		660		0.123				4.2		772		0.125				4.24		586		0.125				4.34		575		0.127				4.12		638		0.123				4.25		522		0.127				4.19		611		0.126

		4.21		616		0.122				4.26		668		0.125				4.29		783		0.127				4.34		592		0.127				4.46		583		0.131				4.25		660		0.127				4.31		527		0.129				4.25		617		0.128

		4.27		622		0.124				4.35		676		0.127				4.32		793		0.129				4.4		597		0.129				4.53		588		0.134				4.31		670		0.129				4.37		531		0.131				4.32		623		0.13

		4.36		628		0.126				4.41		683		0.129				4.41		803		0.131				4.47		602		0.131				4.59		592		0.136				4.37		682		0.131				4.44		535		0.133				4.38		628		0.132

		4.42		634		0.128				4.51		699		0.133				4.54		823		0.135				4.56		609		0.134				4.65		597		0.138				4.43		692		0.133				4.56		544		0.137				4.44		634		0.135

		4.46		640		0.13				4.57		708		0.135				4.6		834		0.137				4.62		614		0.136				4.71		601		0.14				4.5		703		0.135				4.63		548		0.139				4.51		639		0.137

		4.55		646		0.132				4.66		715		0.137				4.64		844		0.139				4.69		619		0.138				4.78		606		0.142				4.53		713		0.138				4.69		553		0.141				4.6		648		0.14

		4.67		658		0.136				4.7		723		0.139				4.73		854		0.142				4.75		626		0.141				4.81		611		0.144				4.62		724		0.14				4.75		557		0.143				4.63		653		0.142

		4.71		663		0.138				4.79		729		0.141				4.77		865		0.144				4.81		634		0.143				4.9		615		0.146				4.68		733		0.142				4.81		562		0.145				4.73		658		0.144

		4.77		670		0.14				4.82		737		0.144				4.86		875		0.146				4.88		642		0.145				4.97		623		0.149				4.81		755		0.146				4.88		566		0.147				4.79		663		0.146

		4.86		676		0.143				4.88		744		0.145				4.93		883		0.148				4.94		650		0.147				5.03		628		0.151				4.87		766		0.148				4.94		571		0.15				4.85		669		0.148

		4.89		682		0.144				4.95		751		0.147				5.05		903		0.152				4.97		658		0.149				5.09		633		0.153				4.94		776		0.15				5.07		579		0.154				4.88		673		0.15

		4.95		688		0.146				5.01		758		0.15				5.12		913		0.155				5.13		673		0.153				5.16		638		0.155				5		786		0.152				5.13		583		0.156				4.97		679		0.152

		5.02		694		0.148				5.13		771		0.154				5.18		921		0.156				5.19		680		0.155				5.25		643		0.158				5.03		796		0.154				5.17		588		0.158				5.04		685		0.154

		5.08		700		0.151				5.23		778		0.156				5.24		930		0.159				5.25		687		0.157				5.31		648		0.16				5.12		806		0.156				5.26		592		0.16				5.13		694		0.158

		5.17		706		0.153				5.26		784		0.158				5.31		939		0.161				5.32		693		0.159				5.38		653		0.162				5.16		816		0.159				5.32		596		0.162				5.19		701		0.16

		5.27		718		0.157				5.32		790		0.16				5.37		948		0.163				5.35		699		0.161				5.44		658		0.164				5.25		826		0.161				5.35		600		0.165				5.26		706		0.162

		5.33		723		0.159				5.38		797		0.162				5.4		957		0.165				5.44		706		0.163				5.53		666		0.167				5.31		836		0.163				5.42		604		0.167				5.32		712		0.164

		5.42		730		0.161				5.48		803		0.164				5.5		965		0.167				5.51		713		0.166				5.57		671		0.169				5.43		854		0.167				5.51		608		0.169				5.38		718		0.166

		5.45		736		0.163				5.51		808		0.166				5.63		983		0.171				5.61		725		0.17				5.66		676		0.171				5.5		864		0.169				5.61		618		0.173				5.45		724		0.168

		5.52		742		0.165				5.6		813		0.168				5.66		990		0.174				5.7		731		0.172				5.72		680		0.173				5.56		873		0.171				5.7		622		0.175				5.51		730		0.17

		5.58		748		0.167				5.66		822		0.172				5.75		998		0.176				5.76		738		0.174				5.76		685		0.176				5.62		883		0.173				5.76		626		0.177				5.57		736		0.172

		5.67		754		0.169				5.73		828		0.174				5.82		1010		0.178				5.84		745		0.177				5.82		690		0.178				5.68		891		0.175				5.82		630		0.179				5.63		744		0.175

		5.7		760		0.171				5.82		833		0.176				5.88		1020		0.18				5.9		752		0.179				5.91		695		0.18				5.75		900		0.177				5.89		634		0.181				5.73		750		0.177

		5.8		766		0.173				5.85		839		0.178				5.94		1020		0.182				5.94		758		0.181				5.98		700		0.182				5.81		909		0.179				5.95		638		0.183				5.79		756		0.179

		5.89		774		0.176				5.91		844		0.18				6.01		1030		0.184				6.03		763		0.183				6.1		709		0.186				5.87		918		0.181				6.01		643		0.185				5.85		762		0.181

		5.92		781		0.179				6.01		849		0.182				6.1		1040		0.187				6.09		768		0.185				6.17		714		0.188				5.94		932		0.184				6.08		648		0.187				5.92		768		0.184

		6.02		787		0.181				6.04		854		0.184				6.16		1050		0.189				6.19		778		0.189				6.24		720		0.191				6.03		939		0.186				6.2		656		0.192				5.98		773		0.186

		6.05		793		0.183				6.1		860		0.186				6.23		1060		0.192				6.25		783		0.191				6.3		725		0.193				6.09		948		0.189				6.27		660		0.194				6.04		779		0.188

		6.11		798		0.185				6.19		865		0.188				6.29		1070		0.193				6.31		789		0.192				6.37		730		0.195				6.15		956		0.191				6.33		664		0.196				6.1		784		0.19

		6.17		805		0.187				6.29		875		0.192				6.35		1070		0.195				6.37		795		0.195				6.43		735		0.197				6.22		964		0.193				6.39		668		0.198				6.2		793		0.193

		6.23		811		0.189				6.35		880		0.194				6.42		1080		0.198				6.44		800		0.197				6.49		739		0.199				6.28		973		0.195				6.45		673		0.2				6.26		799		0.195

		6.3		818		0.191				6.44		886		0.196				6.48		1090		0.2				6.47		806		0.199				6.59		747		0.202				6.35		982		0.197				6.52		678		0.202				6.32		805		0.197

		6.36		823		0.193				6.51		891		0.198				6.54		1100		0.202				6.56		812		0.201				6.65		751		0.204				6.41		990		0.199				6.58		682		0.204				6.39		810		0.199

		6.48		833		0.196				6.54		896		0.201				6.67		1110		0.206				6.63		818		0.203				6.68		756		0.206				6.54		1010		0.204				6.64		685		0.206				6.45		815		0.202

		6.55		838		0.198				6.63		901		0.203				6.74		1120		0.208				6.75		829		0.207				6.78		761		0.208				6.6		1010		0.205				6.77		694		0.211				6.51		821		0.203

		6.58		845		0.201				6.66		906		0.205				6.8		1120		0.21				6.82		834		0.209				6.84		766		0.211				6.66		1020		0.208				6.83		698		0.213				6.58		827		0.205

		6.67		851		0.203				6.75		911		0.207				6.86		1130		0.213				6.88		840		0.211				6.9		770		0.213				6.7		1030		0.21				6.87		702		0.215				6.64		833		0.208

		6.7		857		0.205				6.85		921		0.211				6.92		1140		0.215				6.91		846		0.214				6.96		775		0.215				6.76		1040		0.212				6.96		706		0.217				6.73		841		0.211

		6.76		863		0.207				6.94		926		0.213				6.99		1140		0.217				7.01		852		0.216				7.03		779		0.217				6.82		1040		0.214				7.02		710		0.219				6.79		846		0.213

		6.83		869		0.209				6.97		931		0.215				7.05		1150		0.219				7.07		858		0.218				7.15		789		0.221				6.88		1050		0.216				7.09		713		0.221				6.86		851		0.215

		6.92		875		0.211				7.04		936		0.217				7.11		1160		0.221				7.13		864		0.22				7.22		794		0.223				6.97		1060		0.218				7.15		718		0.223				6.92		857		0.217

		7.01		884		0.214				7.13		940		0.219				7.21		1170		0.225				7.19		871		0.222				7.28		799		0.225				7.07		1070		0.221				7.21		723		0.225				6.98		863		0.219

		7.08		890		0.216				7.19		945		0.222				7.3		1180		0.227				7.32		888		0.226				7.34		805		0.227				7.13		1080		0.223				7.34		730		0.229				7.05		868		0.221

		7.11		897		0.218				7.25		950		0.224				7.37		1180		0.229				7.38		899		0.228				7.41		812		0.229				7.17		1080		0.226				7.4		734		0.232				7.11		873		0.223

		7.17		903		0.22				7.29		955		0.226				7.4		1190		0.232				7.45		910		0.231				7.47		818		0.231				7.27		1090		0.228				7.46		738		0.234				7.17		878		0.226

		7.23		908		0.223				7.35		960		0.228				7.49		1200		0.233				7.51		921		0.232				7.53		827		0.234				7.33		1100		0.23				7.53		743		0.236				7.3		889		0.23

		7.29		914		0.224				7.44		967		0.231				7.56		1200		0.236				7.57		931		0.234				7.56		836		0.236				7.39		1100		0.232				7.59		747		0.238				7.36		895		0.232

		7.39		921		0.226				7.53		972		0.233				7.62		1210		0.238				7.61		942		0.237				7.69		850		0.239				7.43		1110		0.234				7.65		752		0.24				7.43		901		0.234

		7.42		927		0.229				7.57		977		0.235				7.68		1220		0.24				7.7		953		0.239				7.75		859		0.241				7.52		1120		0.236				7.72		756		0.242				7.49		906		0.236

		7.48		933		0.231				7.66		982		0.237				7.78		1230		0.244				7.76		964		0.241				7.81		870		0.243				7.58		1130		0.238				7.78		763		0.245				7.52		911		0.238

		7.64		945		0.235				7.72		986		0.239				7.87		1240		0.246				7.89		987		0.245				7.88		879		0.245				7.62		1130		0.24				7.87		767		0.247				7.62		916		0.24

		7.67		952		0.237				7.75		991		0.241				7.93		1240		0.248				7.95		997		0.247				7.94		889		0.247				7.71		1140		0.243				7.94		771		0.25				7.68		922		0.243

		7.73		958		0.239				7.82		995		0.243				8.01		1250		0.251				7.99		1010		0.249				8		899		0.249				7.77		1140		0.245				8		777		0.252				7.74		928		0.245

		7.79		963		0.241				7.88		1000		0.245				8.07		1260		0.253				8.08		1020		0.251				8.06		908		0.251				7.83		1150		0.247				8.03		783		0.254				7.84		936		0.248

		7.86		970		0.243				7.94		1000		0.247				8.14		1260		0.255				8.14		1030		0.254				8.13		918		0.254				7.9		1160		0.249				8.13		789		0.256				7.9		941		0.25

		7.92		976		0.245				8.07		1010		0.251				8.2		1270		0.257				8.18		1040		0.256				8.19		933		0.257				7.93		1160		0.251				8.19		796		0.258				7.96		946		0.252

		8.01		983		0.247				8.13		1020		0.253				8.23		1270		0.259				8.27		1050		0.258				8.28		941		0.259				7.99		1170		0.253				8.25		804		0.26				8		951		0.254

		8.04		988		0.249				8.16		1020		0.255				8.36		1290		0.264				8.4		1070		0.262				8.34		951		0.261				8.09		1180		0.255				8.35		823		0.264				8.06		956		0.256

		8.14		995		0.252				8.25		1030		0.257				8.45		1290		0.266				8.43		1080		0.264				8.41		959		0.263				8.21		1190		0.259				8.44		831		0.266				8.15		962		0.258

		8.17		1000		0.254				8.28		1030		0.259				8.49		1300		0.268				8.5		1090		0.266				8.47		968		0.265				8.28		1190		0.262				8.51		840		0.268				8.21		968		0.26

		8.23		1010		0.256				8.35		1040		0.261				8.58		1300		0.27				8.59		1100		0.269				8.5		977		0.267				8.34		1200		0.263				8.57		848		0.271				8.28		973		0.262

		8.29		1010		0.258				8.41		1040		0.263				8.64		1310		0.272				8.65		1110		0.271				8.56		986		0.269				8.4		1210		0.266				8.63		858		0.273				8.4		983		0.266

		8.36		1020		0.26				8.47		1050		0.265				8.7		1320		0.274				8.72		1120		0.273				8.66		994		0.271				8.46		1210		0.268				8.7		867		0.275				8.47		988		0.269

		8.45		1030		0.262				8.53		1050		0.267				8.74		1320		0.276				8.78		1130		0.275				8.78		1010		0.275				8.53		1220		0.27				8.73		876		0.277				8.53		993		0.271

		8.48		1030		0.264				8.69		1060		0.271				8.8		1330		0.278				8.84		1140		0.277				8.84		1020		0.277				8.59		1220		0.272				8.82		884		0.279				8.59		998		0.273

		8.54		1040		0.266				8.72		1070		0.274				8.92		1340		0.281				8.97		1160		0.281				8.9		1030		0.279				8.69		1240		0.276				8.95		901		0.283				8.63		1000		0.275

		8.61		1040		0.268				8.78		1080		0.275				8.99		1340		0.283				9.03		1170		0.283				8.94		1040		0.281				8.78		1240		0.278				9.01		910		0.285				8.72		1010		0.277

		8.67		1050		0.27				8.85		1080		0.278				9.05		1350		0.286				9.1		1170		0.285				9.03		1040		0.284				8.84		1250		0.28				9.04		918		0.287				8.78		1010		0.279

		8.76		1060		0.273				8.91		1090		0.28				9.11		1350		0.288				9.16		1180		0.287				9.06		1050		0.286				8.91		1250		0.282				9.14		926		0.29				8.84		1020		0.281

		8.82		1070		0.275				8.97		1100		0.282				9.18		1360		0.29				9.22		1190		0.289				9.13		1060		0.288				8.97		1260		0.285				9.2		934		0.292				8.97		1030		0.286

		8.89		1070		0.277				9.03		1100		0.284				9.21		1370		0.292				9.28		1200		0.292				9.19		1070		0.29				9.03		1270		0.287				9.26		942		0.294				9.03		1030		0.288

		8.95		1080		0.279				9.09		1110		0.286				9.27		1370		0.294				9.32		1210		0.294				9.28		1070		0.292				9.1		1270		0.289				9.34		951		0.296				9.1		1040		0.29

		9.01		1090		0.282				9.16		1120		0.288				9.36		1380		0.296				9.41		1220		0.296				9.38		1090		0.296				9.13		1280		0.291				9.4		958		0.298				9.16		1040		0.292

		9.07		1090		0.284				9.31		1130		0.292				9.49		1390		0.3				9.51		1240		0.3				9.44		1100		0.298				9.22		1290		0.294				9.5		973		0.303				9.22		1050		0.294

		9.17		1100		0.286				9.34		1140		0.294				9.55		1390		0.302				9.6		1240		0.302				9.5		1100		0.3				9.31		1290		0.296				9.59		981		0.305				9.29		1050		0.296

		9.23		1100		0.288				9.41		1140		0.296				9.61		1400		0.304				9.66		1250		0.304				9.56		1110		0.302				9.38		1300		0.298				9.65		988		0.307				9.35		1060		0.298

		9.32		1110		0.291				9.5		1150		0.298				9.67		1400		0.306				9.73		1260		0.306				9.62		1120		0.305				9.44		1300		0.3				9.73		996		0.309				9.41		1060		0.3

		9.39		1120		0.293				9.56		1160		0.301				9.71		1410		0.308				9.76		1270		0.309				9.72		1120		0.307				9.48		1310		0.303				9.79		1000		0.312				9.54		1080		0.304

		9.45		1130		0.295				9.63		1160		0.303				9.8		1410		0.31				9.82		1280		0.31				9.78		1130		0.309				9.55		1320		0.305				9.85		1010		0.313				9.57		1090		0.306

		9.51		1130		0.297				9.69		1170		0.305				9.86		1420		0.312				9.92		1290		0.313				9.84		1140		0.311				9.61		1320		0.307				9.92		1020		0.315				9.66		1100		0.309

		9.57		1140		0.299				9.72		1180		0.307				9.93		1430		0.315				9.98		1290		0.315				9.9		1140		0.313				9.7		1330		0.309				10		1030		0.32				9.73		1110		0.311

		9.6		1140		0.302				9.78		1180		0.309				10.1		1440		0.319				10.1		1310		0.319				10		1160		0.317				9.83		1340		0.313				10.1		1040		0.322				9.76		1120		0.313

		9.67		1150		0.304				9.94		1200		0.313				10.1		1440		0.321				10.2		1320		0.321				10.1		1160		0.319				9.9		1350		0.316				10.2		1050		0.324				9.85		1130		0.315

		9.73		1160		0.306				10		1200		0.315				10.2		1450		0.323				10.2		1330		0.323				10.2		1170		0.321				9.96		1360		0.318				10.2		1050		0.326				9.92		1140		0.317

		9.79		1160		0.308				10		1210		0.317				10.2		1450		0.325				10.3		1340		0.325				10.2		1180		0.323				10		1360		0.32				10.3		1060		0.328				10		1170		0.321

		9.92		1180		0.312				10.1		1210		0.319				10.3		1460		0.327				10.4		1340		0.327				10.3		1180		0.325				10.1		1370		0.322				10.4		1070		0.33				10.1		1180		0.323

		9.98		1180		0.314				10.2		1220		0.321				10.3		1460		0.329				10.4		1350		0.329				10.3		1190		0.327				10.2		1370		0.324				10.4		1070		0.332				10.2		1190		0.326

		10		1190		0.316				10.2		1230		0.323				10.4		1470		0.332				10.5		1360		0.332				10.4		1200		0.329				10.2		1380		0.327				10.5		1080		0.336				10.2		1200		0.328

		10.1		1190		0.318				10.3		1230		0.325				10.5		1480		0.334				10.5		1370		0.334				10.5		1200		0.331				10.3		1390		0.331				10.6		1090		0.338				10.2		1210		0.33

		10.2		1200		0.32				10.3		1240		0.327				10.6		1490		0.338				10.6		1380		0.338				10.5		1210		0.333				10.4		1400		0.333				10.6		1090		0.34				10.3		1220		0.332

		10.2		1210		0.322				10.5		1250		0.332				10.7		1490		0.34				10.7		1390		0.34				10.6		1220		0.338				10.5		1410		0.335				10.7		1100		0.342				10.4		1240		0.334

		10.3		1210		0.324				10.5		1260		0.334				10.7		1500		0.342				10.8		1400		0.342				10.7		1230		0.34				10.6		1410		0.338				10.8		1110		0.344				10.5		1250		0.336

		10.4		1220		0.326				10.6		1260		0.336				10.8		1500		0.344				10.8		1400		0.344				10.8		1230		0.342				10.6		1420		0.34				10.8		1110		0.346				10.6		1260		0.339

		10.5		1230		0.33				10.7		1270		0.338				10.9		1510		0.346				10.9		1410		0.346				10.8		1240		0.344				10.7		1420		0.341				10.9		1120		0.348				10.6		1270		0.341

		10.5		1230		0.332				10.7		1280		0.34				10.9		1510		0.348				11		1420		0.349				10.9		1250		0.346				10.7		1430		0.344				10.9		1130		0.35				10.7		1290		0.343

		10.6		1240		0.334				10.8		1280		0.342				11		1520		0.35				11.1		1430		0.351				11		1250		0.348				10.9		1440		0.348				11.1		1140		0.355				10.8		1300		0.345

		10.6		1250		0.336				10.9		1290		0.344				11.1		1530		0.352				11.1		1430		0.352				11		1260		0.35				10.9		1450		0.35				11.2		1140		0.357				10.8		1310		0.348

		10.7		1250		0.338				10.9		1290		0.346				11.1		1530		0.356				11.2		1450		0.357				11.1		1260		0.352				11		1460		0.352				11.2		1150		0.359				10.9		1320		0.35

		10.8		1260		0.34				11		1310		0.35				11.2		1540		0.357				11.3		1450		0.359				11.2		1270		0.355				11.1		1460		0.354				11.3		1160		0.361				11		1330		0.352

		10.8		1270		0.342				11.1		1310		0.353				11.3		1550		0.359				11.3		1460		0.361				11.2		1280		0.357				11.1		1470		0.356				11.3		1160		0.363				11		1340		0.354

		10.9		1270		0.344				11.2		1320		0.355				11.3		1550		0.361				11.4		1470		0.363				11.3		1280		0.359				11.2		1470		0.358				11.4		1170		0.365				11.2		1360		0.358

		10.9		1280		0.346				11.2		1320		0.357				11.4		1560		0.364				11.5		1480		0.365				11.4		1290		0.362				11.2		1480		0.361				11.5		1170		0.367				11.2		1370		0.36

		11		1280		0.348				11.3		1330		0.359				11.5		1560		0.366				11.6		1480		0.367				11.4		1300		0.364				11.3		1490		0.363				11.5		1180		0.369				11.3		1380		0.362

		11.1		1290		0.35				11.4		1340		0.361				11.5		1570		0.368				11.6		1490		0.369				11.5		1300		0.366				11.4		1500		0.367				11.6		1190		0.372				11.3		1390		0.365

		11.1		1300		0.352				11.4		1340		0.363				11.5		1580		0.37				11.7		1500		0.371				11.6		1310		0.368				11.5		1510		0.369				11.7		1190		0.375				11.4		1400		0.367

		11.2		1300		0.354				11.5		1350		0.365				11.6		1580		0.372				11.8		1510		0.376				11.6		1310		0.37				11.6		1510		0.371				11.7		1200		0.377				11.4		1410		0.369

		11.3		1310		0.356				11.6		1350		0.367				11.7		1590		0.375				11.9		1520		0.378				11.7		1320		0.372				11.6		1520		0.373				11.8		1200		0.379				11.5		1420		0.371

		11.4		1320		0.358				11.7		1360		0.37				11.8		1600		0.377				11.9		1530		0.38				11.8		1330		0.376				11.7		1530		0.375				11.8		1210		0.381				11.6		1430		0.373

		11.4		1320		0.361				11.7		1370		0.372				11.9		1600		0.379				12		1530		0.382				11.9		1340		0.378				11.7		1530		0.378				11.9		1210		0.383				11.7		1450		0.377

		11.4		1330		0.363				11.7		1370		0.374				11.9		1610		0.381				12.1		1540		0.384				11.9		1340		0.38				11.8		1540		0.38				12		1220		0.385				11.8		1450		0.379

		11.6		1340		0.367				11.8		1380		0.376				12		1610		0.383				12.1		1550		0.386				12		1350		0.382				11.9		1550		0.384				12		1220		0.387				11.8		1460		0.381

		11.6		1350		0.369				11.9		1380		0.378				12.1		1620		0.386				12.2		1550		0.389				12.1		1350		0.385				12		1560		0.386				12.1		1230		0.389				11.9		1470		0.383

		11.7		1350		0.371				11.9		1390		0.381				12.1		1630		0.388				12.3		1560		0.391				12.1		1360		0.387				12.1		1570		0.388				12.2		1240		0.392				12		1480		0.385

		11.8		1360		0.373				12		1400		0.383				12.2		1630		0.39				12.3		1570		0.394				12.2		1360		0.389				12.1		1570		0.39				12.2		1240		0.394				12		1490		0.388

		11.8		1360		0.375				12.1		1400		0.385				12.3		1640		0.394				12.4		1580		0.396				12.2		1370		0.391				12.2		1580		0.392				12.3		1250		0.396				12.1		1500		0.39

		11.9		1370		0.377				12.1		1410		0.387				12.3		1650		0.396				12.5		1580		0.398				12.4		1380		0.395				12.2		1590		0.394				12.4		1250		0.399				12.2		1510		0.392

		11.9		1380		0.379				12.2		1410		0.39				12.4		1660		0.398				12.5		1590		0.4				12.4		1390		0.397				12.3		1590		0.396				12.5		1260		0.4				12.3		1530		0.396

		12		1380		0.382				12.3		1420		0.392				12.5		1660		0.4				12.6		1590		0.402				12.5		1390		0.399				12.4		1600		0.399				12.5		1260		0.402				12.3		1540		0.398

		12.1		1390		0.384				12.4		1430		0.394				12.6		1670		0.402				12.7		1600		0.404				12.6		1400		0.401				12.5		1610		0.401				12.6		1270		0.405				12.4		1540		0.4

		12.2		1400		0.387				12.4		1430		0.396				12.6		1670		0.404				12.7		1610		0.406				12.6		1400		0.403				12.5		1610		0.404				12.7		1270		0.407				12.5		1550		0.402

		12.3		1400		0.389				12.5		1440		0.398				12.7		1680		0.406				12.8		1610		0.409				12.7		1410		0.405				12.6		1620		0.406				12.7		1280		0.411				12.5		1560		0.404

		12.3		1410		0.391				12.6		1440		0.4				12.7		1690		0.408				12.9		1630		0.413				12.7		1410		0.407				12.7		1630		0.408				12.8		1290		0.413				12.6		1570		0.407

		12.3		1420		0.393				12.6		1450		0.402				12.8		1690		0.412				13		1630		0.415				12.8		1420		0.409				12.7		1630		0.41				12.9		1290		0.415				12.6		1580		0.409

		12.4		1420		0.395				12.7		1450		0.404				12.9		1700		0.414				13		1640		0.417				12.8		1430		0.412				12.8		1640		0.412				12.9		1300		0.417				12.7		1590		0.411

		12.5		1430		0.397				12.7		1460		0.407				13		1700		0.416				13.1		1640		0.419				12.9		1430		0.414				12.9		1650		0.414				13		1300		0.419				12.8		1600		0.414

		12.5		1430		0.399				12.8		1470		0.41				13		1710		0.418				13.2		1650		0.421				13		1440		0.416				13		1660		0.419				13.1		1310		0.421				12.9		1610		0.416

		12.6		1440		0.401				12.9		1470		0.412				13.1		1720		0.42				13.2		1660		0.423				13.1		1440		0.418				13.1		1670		0.421				13.1		1310		0.423				12.9		1620		0.418

		12.7		1450		0.403				12.9		1480		0.414				13.1		1720		0.422				13.3		1660		0.425				13.1		1450		0.42				13.1		1670		0.423				13.2		1320		0.426				13		1620		0.42

		12.8		1460		0.407				13		1480		0.416				13.2		1730		0.424				13.4		1670		0.427				13.2		1450		0.422				13.2		1680		0.425				13.3		1330		0.43				13.1		1630		0.422

		12.9		1470		0.41				13.1		1490		0.418				13.3		1730		0.426				13.5		1680		0.431				13.2		1460		0.424				13.2		1690		0.427				13.4		1340		0.432				13.1		1640		0.425

		12.9		1470		0.412				13.2		1500		0.42				13.4		1750		0.43				13.5		1690		0.434				13.3		1470		0.426				13.3		1700		0.429				13.4		1340		0.434				13.2		1650		0.427

		13		1480		0.414				13.2		1500		0.422				13.5		1750		0.433				13.6		1690		0.436				13.4		1470		0.428				13.4		1700		0.432				13.5		1350		0.436				13.2		1660		0.428

		13		1480		0.416				13.2		1510		0.424				13.5		1760		0.435				13.7		1700		0.437				13.5		1480		0.431				13.5		1720		0.435				13.6		1350		0.438				13.3		1670		0.431

		13.1		1490		0.418				13.3		1510		0.426				13.6		1760		0.436				13.7		1710		0.439				13.5		1490		0.433				13.6		1720		0.438				13.6		1360		0.44				13.4		1670		0.433

		13.2		1490		0.42				13.4		1520		0.431				13.6		1770		0.439				13.8		1710		0.442				13.6		1490		0.435				13.6		1730		0.44				13.7		1360		0.442				13.5		1680		0.435

		13.2		1500		0.422				13.5		1530		0.433				13.7		1770		0.441				13.8		1720		0.444				13.6		1500		0.437				13.7		1740		0.442				13.8		1370		0.444				13.5		1690		0.437

		13.3		1510		0.426				13.6		1530		0.435				13.8		1780		0.443				13.9		1720		0.446				13.7		1500		0.44				13.8		1740		0.444				13.8		1370		0.446				13.6		1700		0.439

		13.4		1520		0.428				13.6		1540		0.437				13.8		1780		0.445				14		1730		0.448				13.8		1510		0.442				13.8		1750		0.446				14		1380		0.45				13.6		1710		0.441

		13.5		1520		0.431				13.7		1540		0.439				14		1800		0.449				14.1		1740		0.452				13.8		1510		0.444				13.9		1750		0.448				14		1390		0.452				13.7		1710		0.443

		13.5		1530		0.433				13.7		1550		0.441				14		1800		0.451				14.2		1750		0.454				13.9		1520		0.446				13.9		1760		0.45				14.1		1390		0.455				13.8		1720		0.445

		13.6		1540		0.434				13.8		1550		0.443				14.1		1810		0.453				14.2		1750		0.456				14		1530		0.449				14		1770		0.454				14.1		1400		0.457				13.9		1740		0.45

		13.7		1540		0.436				13.9		1560		0.445				14.1		1810		0.455				14.3		1760		0.458				14.1		1540		0.451				14.1		1780		0.456				14.2		1400		0.459				14		1750		0.452

		13.8		1550		0.439				14		1560		0.448				14.2		1820		0.458				14.4		1770		0.461				14.1		1540		0.453				14.1		1780		0.458				14.3		1410		0.461				14		1760		0.454

		13.8		1550		0.441				14.1		1570		0.45				14.3		1820		0.46				14.4		1770		0.463				14.2		1550		0.455				14.2		1790		0.46				14.3		1410		0.463				14.1		1760		0.456

		13.9		1560		0.444				14.1		1570		0.452				14.3		1830		0.462				14.5		1780		0.465				14.2		1550		0.457				14.3		1800		0.462				14.4		1420		0.465				14.1		1770		0.458

		13.9		1570		0.446				14.1		1580		0.454				14.4		1830		0.464				14.5		1780		0.467				14.3		1560		0.46				14.4		1800		0.464				14.5		1430		0.468				14.2		1780		0.46

		14		1570		0.448				14.2		1590		0.456				14.5		1840		0.467				14.7		1800		0.471				14.4		1560		0.462				14.4		1810		0.466				14.6		1430		0.47				14.3		1790		0.462

		14.1		1580		0.45				14.3		1590		0.458				14.6		1850		0.469				14.7		1800		0.473				14.4		1570		0.464				14.4		1820		0.468				14.6		1440		0.472				14.3		1800		0.465

		14.2		1580		0.452				14.4		1590		0.461				14.6		1850		0.471				14.8		1810		0.475				14.5		1580		0.468				14.6		1830		0.472				14.7		1440		0.474				14.4		1810		0.467

		14.2		1590		0.454				14.4		1600		0.463				14.6		1860		0.473				14.8		1810		0.477				14.6		1590		0.47				14.7		1830		0.475				14.7		1450		0.477				14.5		1820		0.469

		14.3		1600		0.456				14.5		1610		0.465				14.7		1860		0.475				14.9		1820		0.479				14.7		1600		0.472				14.7		1840		0.476				14.8		1460		0.478				14.5		1820		0.472

		14.3		1600		0.458				14.6		1610		0.468				14.8		1870		0.477				15		1820		0.481				14.7		1600		0.474				14.8		1850		0.479				14.9		1460		0.48				14.6		1830		0.474

		14.4		1610		0.461				14.6		1620		0.47				14.8		1870		0.479				15		1830		0.484				14.8		1610		0.476				14.9		1850		0.481				14.9		1470		0.483				14.7		1840		0.476

		14.4		1610		0.463				14.7		1620		0.472				14.9		1880		0.481				15.1		1840		0.485				14.9		1610		0.478				14.9		1860		0.483				15		1480		0.487				14.7		1850		0.478

		14.5		1620		0.465				14.7		1630		0.474				15.1		1890		0.486				15.2		1850		0.488				14.9		1620		0.48				15		1860		0.485				15.1		1480		0.489				14.8		1860		0.48

		14.6		1620		0.467				14.8		1630		0.476				15.1		1890		0.488				15.3		1850		0.49				15		1630		0.482				15		1870		0.487				15.1		1490		0.491				14.9		1870		0.482

		14.6		1630		0.469				14.9		1640		0.478				15.2		1900		0.49				15.3		1860		0.493				15.1		1640		0.487				15.2		1880		0.491				15.2		1500		0.493				15		1880		0.486

		14.7		1640		0.471				14.9		1640		0.48				15.3		1900		0.492				15.4		1860		0.495				15.2		1650		0.489				15.2		1890		0.493				15.3		1500		0.495				15.1		1890		0.488

		14.8		1640		0.473				15		1650		0.483				15.3		1910		0.494				15.4		1870		0.497				15.2		1650		0.491				15.3		1900		0.496				15.3		1510		0.497				15.1		1900		0.491

		14.8		1650		0.475				15.1		1650		0.484				15.3		1920		0.496				15.5		1870		0.499				15.3		1660		0.493				15.4		1900		0.498				15.4		1510		0.499				15.2		1910		0.493

		14.9		1650		0.477				15.1		1660		0.486				15.4		1920		0.499				15.6		1880		0.501				15.3		1670		0.495				15.4		1910		0.5				15.5		1520		0.501				15.2		1910		0.495

		15		1660		0.481				15.2		1660		0.489				15.5		1930		0.501				15.6		1890		0.503				15.4		1670		0.497				15.5		1910		0.502				15.6		1530		0.504				15.3		1920		0.497

		15.1		1670		0.483				15.3		1670		0.491				15.6		1940		0.505				15.8		1900		0.508				15.5		1680		0.499				15.6		1920		0.504				15.6		1530		0.507				15.4		1930		0.499

		15.1		1680		0.485				15.3		1670		0.493				15.7		1940		0.507				15.8		1900		0.51				15.6		1690		0.501				15.6		1930		0.507				15.7		1540		0.509				15.4		1940		0.501

		15.2		1680		0.487				15.4		1680		0.495				15.8		1950		0.509				15.9		1910		0.512				15.7		1700		0.506				15.7		1940		0.509				15.7		1550		0.511				15.5		1950		0.504

		15.3		1690		0.49				15.5		1680		0.497				15.8		1950		0.511				15.9		1910		0.514				15.7		1700		0.508				15.8		1940		0.511				15.8		1550		0.513				15.6		1960		0.506

		15.3		1690		0.492				15.5		1690		0.499				15.9		1960		0.513				16		1920		0.516				15.8		1710		0.51				15.8		1950		0.514				15.9		1560		0.515				15.7		1960		0.508

		15.4		1700		0.494				15.6		1690		0.501				15.9		1960		0.515				16.1		1930		0.518				15.8		1720		0.512				15.9		1950		0.516				15.9		1560		0.517				15.7		1970		0.51

		15.5		1700		0.496				15.6		1700		0.503				16		1970		0.517				16.1		1930		0.52				15.9		1720		0.514				15.9		1960		0.518				16		1570		0.519				15.7		1980		0.512

		15.5		1710		0.498				15.7		1700		0.505				16.1		1970		0.519				16.2		1940		0.522				16		1730		0.516				16		1970		0.52				16.1		1580		0.523				15.8		1990		0.514

		15.6		1710		0.5				15.7		1710		0.507				16.2		1980		0.523				16.3		1950		0.527				16		1740		0.518				16.1		1970		0.522				16.2		1590		0.525				15.9		2000		0.517

		15.7		1720		0.502				15.8		1710		0.51				16.3		1990		0.526				16.4		1950		0.529				16.1		1740		0.52				16.2		1980		0.526				16.3		1600		0.527				16		2000		0.519

		15.7		1730		0.504				15.9		1720		0.512				16.3		2000		0.528				16.5		1960		0.531				16.2		1760		0.524				16.3		1990		0.528				16.3		1600		0.529				16.1		2020		0.523

		15.7		1730		0.506				15.9		1720		0.514				16.4		2000		0.53				16.5		1960		0.533				16.3		1760		0.526				16.3		2000		0.53				16.4		1610		0.531				16.2		2030		0.525

		15.8		1740		0.508				16		1730		0.516				16.4		2010		0.532				16.6		1970		0.535				16.4		1770		0.528				16.4		2000		0.532				16.4		1620		0.534				16.2		2030		0.527

		15.9		1740		0.511				16.1		1730		0.518				16.5		2010		0.534				16.6		1980		0.537				16.4		1780		0.531				16.5		2010		0.534				16.5		1620		0.536				16.3		2040		0.529

		15.9		1750		0.513				16.1		1740		0.52				16.6		2020		0.536				16.7		1980		0.539				16.5		1780		0.533				16.5		2010		0.537				16.6		1630		0.538				16.3		2050		0.531

		16		1750		0.514				16.3		1750		0.524				16.6		2020		0.538				16.8		1990		0.541				16.6		1790		0.535				16.6		2020		0.539				16.6		1630		0.54				16.4		2060		0.533

		16.1		1760		0.518				16.3		1750		0.526				16.7		2030		0.542				16.9		2000		0.545				16.6		1800		0.537				16.7		2030		0.541				16.7		1640		0.543				16.5		2060		0.535

		16.2		1770		0.52				16.4		1760		0.528				16.8		2040		0.545				16.9		2000		0.547				16.7		1800		0.539				16.8		2040		0.545				16.8		1650		0.545				16.5		2070		0.537

		16.2		1770		0.522				16.5		1760		0.53				16.8		2040		0.547				17		2010		0.55				16.8		1820		0.543				16.8		2040		0.547				16.8		1660		0.547				16.6		2080		0.54

		16.3		1780		0.524				16.5		1770		0.532				16.9		2050		0.549				17.1		2010		0.552				16.9		1820		0.545				16.9		2050		0.549				16.9		1660		0.549				16.7		2090		0.543

		16.4		1780		0.526				16.6		1770		0.534				17		2050		0.55				17.1		2020		0.554				16.9		1830		0.547				17		2060		0.551				17		1670		0.551				16.8		2100		0.545

		16.4		1790		0.528				16.6		1780		0.536				17		2060		0.553				17.2		2020		0.556				17		1840		0.55				17		2060		0.554				17.1		1680		0.553				16.8		2110		0.548

		16.5		1800		0.53				16.7		1780		0.539				17.1		2060		0.555				17.2		2030		0.558				17.1		1840		0.552				17.1		2070		0.556				17.1		1680		0.556				16.9		2120		0.55

		16.5		1800		0.532				16.8		1790		0.543				17.2		2070		0.557				17.3		2030		0.56				17.1		1850		0.554				17.1		2070		0.557				17.2		1690		0.558				17		2120		0.552

		16.6		1810		0.534				16.9		1800		0.545				17.3		2080		0.561				17.5		2040		0.564				17.2		1860		0.556				17.2		2080		0.56				17.3		1700		0.562				17		2130		0.554

		16.7		1820		0.537				16.9		1800		0.547				17.4		2090		0.563				17.5		2050		0.566				17.3		1870		0.56				17.4		2090		0.564				17.4		1710		0.564				17.1		2140		0.556

		16.7		1820		0.54				17		1800		0.549				17.4		2090		0.565				17.6		2050		0.568				17.4		1880		0.562				17.4		2100		0.566				17.4		1710		0.566				17.1		2140		0.558

		16.8		1830		0.542				17.1		1810		0.551				17.5		2100		0.567				17.7		2060		0.57				17.4		1880		0.564				17.4		2100		0.568				17.5		1720		0.568				17.2		2160		0.562

		16.9		1830		0.544				17.1		1810		0.553				17.6		2100		0.57				17.7		2060		0.573				17.5		1890		0.566				17.5		2110		0.57				17.5		1730		0.57				17.3		2170		0.564

		17		1840		0.546				17.2		1820		0.555				17.6		2110		0.572				17.7		2070		0.575				17.6		1900		0.569				17.6		2120		0.572				17.6		1730		0.571				17.4		2170		0.566

		17		1840		0.548				17.3		1820		0.557				17.7		2110		0.574				17.8		2070		0.577				17.6		1900		0.571				17.6		2120		0.574				17.6		1740		0.573				17.4		2180		0.568

		17.1		1850		0.55				17.3		1830		0.56				17.7		2120		0.576				17.9		2080		0.579				17.7		1910		0.573				17.7		2130		0.576				17.7		1740		0.575				17.5		2190		0.571

		17.2		1850		0.552				17.4		1830		0.563				17.9		2120		0.579				18		2090		0.582				17.8		1920		0.575				17.8		2130		0.579				17.8		1750		0.578				17.6		2190		0.573

		17.3		1870		0.556				17.5		1840		0.565				17.9		2130		0.581				18.1		2090		0.584				17.9		1930		0.579				17.9		2150		0.583				17.9		1760		0.58				17.6		2200		0.575

		17.3		1870		0.558				17.5		1840		0.567				18		2140		0.583				18.1		2100		0.586				18		1930		0.581				18		2150		0.585				17.9		1760		0.582				17.7		2210		0.577

		17.4		1880		0.56				17.6		1850		0.569				18		2140		0.585				18.2		2100		0.588				18		1940		0.583				18		2160		0.587				18		1770		0.585				17.8		2220		0.581

		17.4		1880		0.563				17.7		1850		0.571				18.1		2150		0.587				18.2		2110		0.59				18.1		1940		0.585				18.1		2160		0.589				18		1780		0.587				17.9		2230		0.583

		17.5		1890		0.564				17.7		1860		0.573				18.2		2150		0.59				18.3		2110		0.592				18.1		1950		0.588				18.2		2170		0.591				18.1		1780		0.589				17.9		2240		0.585

		17.6		1890		0.566				17.8		1860		0.575				18.2		2160		0.591				18.4		2120		0.595				18.2		1960		0.59				18.2		2180		0.593				18.2		1790		0.591				18		2250		0.587

		17.6		1900		0.569				17.9		1870		0.577				18.3		2160		0.594				18.4		2120		0.597				18.2		1960		0.592				18.3		2180		0.595				18.2		1800		0.593				18.1		2250		0.589

		17.7		1900		0.571				17.9		1870		0.58				18.4		2170		0.597				18.6		2130		0.601				18.3		1970		0.594				18.4		2190		0.597				18.3		1800		0.595				18.1		2260		0.591

		17.8		1910		0.575				18		1880		0.582				18.4		2170		0.599				18.6		2130		0.603				18.4		1970		0.597				18.4		2190		0.6				18.4		1810		0.599				18.2		2270		0.593

		17.9		1920		0.577				18		1880		0.584				18.5		2180		0.601				18.7		2140		0.605				18.5		1980		0.599				18.4		2200		0.602				18.5		1820		0.601				18.2		2270		0.595

		18		1920		0.579				18.1		1890		0.586				18.6		2180		0.603				18.7		2140		0.607				18.6		1980		0.601				18.5		2200		0.604				18.5		1830		0.603				18.4		2290		0.599

		18		1930		0.581				18.2		1890		0.589				18.6		2190		0.605				18.8		2150		0.609				18.6		1990		0.603				18.6		2210		0.606				18.6		1830		0.605				18.5		2300		0.602

		18.1		1940		0.583				18.2		1900		0.591				18.7		2200		0.607				18.8		2150		0.611				18.7		2000		0.605				18.7		2220		0.608				18.6		1840		0.607				18.5		2300		0.604

		18.1		1940		0.585				18.3		1900		0.593				18.8		2200		0.61				18.9		2160		0.613				18.7		2000		0.607				18.7		2220		0.61				18.7		1840		0.609				18.5		2310		0.606

		18.2		1950		0.587				18.4		1910		0.595				18.8		2210		0.611				19		2160		0.616				18.8		2010		0.609				18.8		2230		0.612				18.8		1850		0.611				18.6		2320		0.608

		18.3		1950		0.59				18.5		1910		0.598				18.9		2210		0.615				19.1		2170		0.619				18.8		2010		0.611				18.9		2230		0.614				18.8		1860		0.614				18.7		2320		0.61

		18.4		1960		0.594				18.5		1920		0.6				19		2220		0.617				19.2		2180		0.622				18.9		2020		0.614				18.9		2240		0.616				18.9		1860		0.616				18.7		2330		0.612

		18.4		1970		0.596				18.6		1920		0.602				19		2220		0.619				19.2		2180		0.624				19.1		2030		0.618				19		2250		0.618				19		1870		0.62				18.8		2340		0.614

		18.5		1970		0.598				18.6		1930		0.604				19.1		2230		0.621				19.3		2190		0.626				19.1		2030		0.62				19.1		2260		0.622				19.1		1880		0.622				19		2350		0.618

		18.6		1980		0.6				18.7		1930		0.606				19.2		2230		0.623				19.4		2190		0.628				19.2		2040		0.622				19.2		2260		0.624				19.2		1880		0.624				19		2360		0.62

		18.7		1980		0.602				18.8		1940		0.608				19.2		2240		0.625				19.4		2200		0.63				19.2		2050		0.624				19.2		2270		0.626				19.2		1890		0.626				19.1		2370		0.622

		18.7		1990		0.604				18.8		1940		0.611				19.3		2240		0.627				19.5		2200		0.632				19.3		2050		0.627				19.3		2270		0.628				19.3		1890		0.628				19.1		2380		0.625

		18.7		1990		0.606				18.9		1950		0.612				19.4		2250		0.629				19.6		2210		0.634				19.4		2060		0.629				19.3		2280		0.631				19.4		1900		0.63				19.2		2380		0.627

		18.8		2000		0.608				19		1950		0.615				19.5		2260		0.634				19.7		2220		0.639				19.4		2060		0.631				19.4		2290		0.633				19.4		1910		0.632				19.3		2390		0.629

		19		2010		0.613				19.1		1960		0.619				19.6		2260		0.636				19.8		2220		0.641				19.6		2070		0.635				19.5		2290		0.635				19.5		1910		0.635				19.3		2400		0.631

		19		2010		0.615				19.1		1970		0.621				19.6		2270		0.638				19.8		2230		0.643				19.6		2080		0.637				19.5		2300		0.637				19.5		1920		0.638				19.4		2400		0.633

		19.1		2020		0.616				19.2		1970		0.623				19.7		2270		0.64				19.9		2230		0.645				19.7		2090		0.639				19.7		2310		0.641				19.6		1920		0.64				19.5		2420		0.637

		19.2		2020		0.619				19.3		1980		0.625				19.7		2280		0.642				19.9		2230		0.647				19.8		2090		0.641				19.7		2320		0.643				19.7		1930		0.642				19.5		2420		0.639

		19.2		2030		0.621				19.4		1980		0.627				19.8		2280		0.644				20		2240		0.649				19.8		2100		0.643				19.8		2320		0.645				19.7		1940		0.644				19.6		2430		0.641

		19.2		2030		0.623				19.4		1980		0.629				19.9		2290		0.646				20.1		2240		0.651				19.9		2100		0.645				19.8		2330		0.647				19.8		1940		0.646				19.7		2440		0.643

		19.3		2040		0.625				19.5		1990		0.631				19.9		2290		0.648				20.1		2250		0.653				19.9		2110		0.647				19.9		2330		0.649				19.9		1950		0.648				19.8		2440		0.645

		19.4		2040		0.627				19.5		1990		0.633				20		2300		0.651				20.2		2260		0.657				20		2110		0.65				20		2340		0.651				19.9		1950		0.65				19.8		2450		0.647

		19.5		2050		0.631				19.6		2000		0.638				20.1		2310		0.653				20.3		2260		0.66				20.1		2120		0.653				20		2340		0.654				20		1960		0.652				19.9		2460		0.649

		19.6		2060		0.633				19.7		2010		0.64				20.1		2310		0.655				20.4		2270		0.662				20.2		2130		0.655				20.1		2350		0.656				20.1		1970		0.656				19.9		2470		0.651

		19.6		2060		0.635				19.8		2010		0.642				20.2		2320		0.658				20.4		2270		0.664				20.2		2130		0.657				20.2		2360		0.658				20.2		1970		0.658				20		2480		0.656

		19.7		2070		0.637				19.8		2020		0.644				20.2		2320		0.66				20.5		2280		0.666				20.3		2140		0.659				20.2		2360		0.66				20.2		1980		0.66				20.1		2490		0.658

		19.8		2070		0.64				19.9		2020		0.646				20.3		2330		0.662				20.5		2280		0.668				20.4		2150		0.661				20.3		2370		0.663				20.3		1980		0.663				20.2		2490		0.66

		19.8		2070		0.641				20		2030		0.648				20.4		2330		0.664				20.6		2290		0.67				20.4		2150		0.663				20.4		2380		0.665				20.4		1990		0.665				20.3		2500		0.662

		19.9		2080		0.643				20		2030		0.65				20.4		2340		0.666				20.7		2290		0.672				20.5		2160		0.665				20.4		2380		0.667				20.5		1990		0.667				20.3		2510		0.664

		19.9		2080		0.645				20.1		2040		0.652				20.5		2340		0.668				20.8		2300		0.676				20.5		2160		0.668				20.5		2390		0.669				20.5		2000		0.669				20.4		2510		0.666

		20.1		2090		0.65				20.2		2050		0.656				20.6		2350		0.67				20.9		2300		0.678				20.7		2170		0.672				20.6		2390		0.671				20.6		2010		0.671				20.4		2520		0.668

		20.1		2100		0.652				20.3		2050		0.658				20.7		2350		0.672				20.9		2310		0.68				20.7		2180		0.674				20.6		2400		0.673				20.7		2010		0.674				20.5		2530		0.67

		20.2		2100		0.654				20.4		2060		0.66				20.7		2360		0.675				21		2310		0.683				20.8		2180		0.676				20.7		2410		0.677				20.7		2020		0.677				20.6		2540		0.673

		20.2		2110		0.656				20.4		2060		0.662				20.8		2360		0.677				21.1		2320		0.685				20.9		2190		0.678				20.8		2420		0.679				20.8		2030		0.679				20.7		2540		0.675

		20.3		2110		0.658				20.5		2060		0.664				20.8		2370		0.679				21.1		2320		0.687				20.9		2200		0.68				20.9		2420		0.681				20.8		2030		0.681				20.7		2550		0.677

		20.4		2120		0.66				20.5		2070		0.666				20.9		2370		0.681				21.2		2330		0.689				21		2200		0.682				20.9		2430		0.684				20.9		2040		0.683				20.8		2560		0.679

		20.5		2120		0.662				20.6		2070		0.669				21		2380		0.683				21.3		2330		0.691				21		2210		0.684				21		2430		0.685				21		2040		0.685				20.8		2560		0.681

		20.5		2130		0.664				20.7		2080		0.671				21.1		2390		0.687				21.4		2340		0.694				21.2		2220		0.688				21		2440		0.687				21.1		2050		0.687				20.9		2570		0.684

		20.6		2140		0.669				20.8		2090		0.675				21.2		2390		0.689				21.4		2340		0.696				21.2		2220		0.691				21.1		2440		0.689				21.1		2050		0.689				20.9		2580		0.686

		20.7		2140		0.671				20.9		2090		0.677				21.2		2400		0.691				21.5		2350		0.698				21.3		2230		0.693				21.2		2450		0.692				21.2		2060		0.693				21		2580		0.688

		20.8		2150		0.673				20.9		2100		0.679				21.3		2400		0.693				21.5		2350		0.7				21.4		2230		0.695				21.3		2460		0.696				21.3		2070		0.695				21.1		2590		0.691

		20.8		2150		0.675				21		2100		0.681				21.3		2410		0.695				21.6		2360		0.702				21.4		2240		0.697				21.4		2470		0.698				21.4		2070		0.697				21.2		2600		0.693

		20.9		2160		0.677				21		2110		0.683				21.4		2410		0.698				21.7		2360		0.704				21.5		2240		0.699				21.4		2470		0.7				21.4		2080		0.699				21.3		2610		0.695

		20.9		2160		0.679				21.1		2110		0.685				21.5		2420		0.7				21.7		2370		0.707				21.6		2250		0.701				21.5		2480		0.702				21.5		2080		0.702				21.3		2610		0.697

		21		2170		0.681				21.2		2120		0.688				21.6		2430		0.704				21.8		2370		0.709				21.7		2260		0.705				21.5		2490		0.704				21.5		2090		0.704				21.3		2620		0.699

		21.2		2180		0.685				21.2		2120		0.69				21.7		2430		0.706				21.9		2380		0.712				21.7		2270		0.708				21.6		2490		0.706				21.6		2090		0.706				21.4		2630		0.701

		21.2		2180		0.688				21.3		2130		0.692				21.7		2440		0.708				22		2380		0.714				21.8		2270		0.71				21.7		2500		0.708				21.7		2100		0.708				21.5		2630		0.703

		21.2		2190		0.689				21.4		2140		0.696				21.8		2440		0.71				22		2390		0.716				21.9		2280		0.712				21.7		2500		0.71				21.7		2110		0.711				21.6		2640		0.705

		21.3		2190		0.691				21.5		2140		0.698				21.9		2450		0.712				22.1		2390		0.718				21.9		2280		0.714				21.8		2510		0.715				21.8		2110		0.713				21.7		2650		0.709

		21.4		2200		0.694				21.5		2150		0.7				21.9		2450		0.715				22.1		2400		0.72				22		2290		0.716				21.9		2520		0.717				21.9		2120		0.715				21.8		2660		0.711

		21.4		2200		0.696				21.6		2150		0.702				22		2460		0.717				22.2		2400		0.722				22		2290		0.718				22		2530		0.719				21.9		2120		0.717				21.8		2670		0.714

		21.5		2210		0.698				21.6		2160		0.704				22		2460		0.718				22.2		2410		0.724				22.1		2300		0.72				22.1		2530		0.721				22		2130		0.719				21.9		2670		0.716

		21.6		2210		0.7				21.7		2160		0.706				22.1		2470		0.721				22.3		2410		0.727				22.2		2310		0.724				22.1		2540		0.723				22.1		2130		0.722				21.9		2680		0.718

		21.7		2220		0.703				21.8		2160		0.708				22.2		2480		0.725				22.4		2420		0.73				22.3		2310		0.727				22.2		2540		0.725				22.1		2140		0.724				22		2690		0.72

		21.7		2230		0.705				21.9		2170		0.71				22.3		2480		0.727				22.5		2420		0.732				22.4		2320		0.728				22.2		2550		0.727				22.2		2140		0.726				22		2690		0.722

		21.8		2230		0.707				22		2180		0.715				22.4		2490		0.729				22.6		2430		0.734				22.4		2320		0.731				22.3		2550		0.729				22.3		2150		0.727				22.1		2700		0.724

		21.8		2230		0.709				22		2180		0.717				22.4		2490		0.731				22.6		2430		0.736				22.5		2330		0.733				22.4		2570		0.733				22.3		2150		0.73				22.3		2710		0.728

		21.9		2240		0.711				22.1		2190		0.719				22.5		2500		0.733				22.7		2440		0.738				22.6		2330		0.735				22.5		2570		0.735				22.4		2160		0.732				22.3		2720		0.73

		22		2240		0.713				22.2		2190		0.721				22.5		2500		0.735				22.7		2440		0.74				22.6		2340		0.737				22.6		2580		0.737				22.4		2170		0.734				22.4		2730		0.732

		22.1		2250		0.716				22.2		2200		0.723				22.6		2510		0.738				22.8		2450		0.742				22.7		2340		0.739				22.6		2580		0.739				22.5		2170		0.736				22.4		2730		0.735

		22.1		2250		0.717				22.3		2200		0.725				22.7		2520		0.742				22.9		2450		0.744				22.8		2350		0.742				22.6		2590		0.741				22.6		2180		0.738				22.5		2740		0.737

		22.2		2260		0.72				22.3		2210		0.727				22.8		2520		0.744				23		2460		0.748				22.8		2360		0.744				22.7		2590		0.744				22.6		2180		0.74				22.5		2740		0.739

		22.3		2270		0.724				22.4		2210		0.729				22.9		2530		0.746				23.1		2460		0.751				22.9		2360		0.746				22.8		2600		0.746				22.7		2190		0.742				22.6		2750		0.741

		22.3		2270		0.726				22.5		2220		0.732				22.9		2530		0.748				23.1		2470		0.753				22.9		2370		0.749				22.9		2610		0.748				22.7		2190		0.744				22.7		2760		0.743

		22.4		2280		0.728				22.5		2220		0.734				23		2540		0.75				23.2		2470		0.755				23		2370		0.751				23		2620		0.752				22.8		2200		0.746				22.8		2770		0.745

		22.5		2290		0.73				22.6		2230		0.736				23.1		2540		0.752				23.2		2480		0.757				23.1		2380		0.753				23.1		2620		0.754				22.9		2200		0.749				22.9		2780		0.749

		22.6		2290		0.732				22.7		2230		0.738				23.1		2540		0.755				23.3		2480		0.759				23.2		2380		0.755				23.1		2630		0.756				23		2210		0.752				22.9		2780		0.751

		22.6		2290		0.734				22.7		2240		0.74				23.2		2550		0.759				23.4		2490		0.761				23.2		2390		0.757				23.2		2640		0.758				23.1		2220		0.754				23		2790		0.753

		22.6		2300		0.736				22.8		2240		0.742				23.3		2560		0.761				23.4		2490		0.763				23.3		2390		0.76				23.2		2640		0.76				23.1		2220		0.756				23.1		2800		0.756

		22.7		2310		0.738				22.9		2250		0.745				23.3		2560		0.763				23.5		2500		0.767				23.4		2400		0.762				23.3		2650		0.762				23.2		2230		0.758				23.1		2800		0.758

		22.8		2310		0.742				23		2250		0.747				23.4		2570		0.765				23.6		2500		0.77				23.4		2400		0.764				23.4		2650		0.764				23.2		2230		0.76				23.2		2810		0.759

		22.9		2320		0.745				23		2260		0.749				23.5		2570		0.767				23.7		2510		0.772				23.5		2410		0.767				23.4		2660		0.767				23.3		2240		0.762				23.3		2820		0.762

		23		2320		0.747				23		2260		0.751				23.6		2580		0.769				23.7		2510		0.774				23.6		2410		0.769				23.6		2670		0.771				23.4		2240		0.764				23.3		2820		0.764

		23.1		2330		0.749				23.1		2260		0.753				23.6		2580		0.772				23.8		2520		0.776				23.6		2420		0.771				23.6		2680		0.773				23.4		2250		0.767				23.4		2830		0.766

		23.1		2330		0.751				23.2		2270		0.755				23.7		2590		0.773				23.9		2520		0.778				23.7		2420		0.773				23.7		2680		0.775				23.5		2250		0.769				23.5		2840		0.77

		23.2		2340		0.753				23.3		2270		0.757				23.8		2600		0.777				23.9		2530		0.78				23.8		2430		0.775				23.7		2690		0.777				23.6		2260		0.771				23.6		2850		0.772

		23.2		2340		0.755				23.3		2280		0.759				23.8		2600		0.779				24		2530		0.782				23.9		2440		0.779				23.8		2690		0.779				23.6		2270		0.774				23.6		2850		0.774

		23.3		2350		0.757				23.4		2280		0.761				23.9		2600		0.781				24.1		2540		0.786				24		2440		0.781				23.9		2700		0.781				23.7		2270		0.776				23.7		2860		0.776

		23.3		2350		0.759				23.4		2290		0.763				24		2610		0.783				24.2		2540		0.789				24		2450		0.783				23.9		2710		0.783				23.7		2280		0.777				23.8		2870		0.778

		23.5		2360		0.763				23.5		2290		0.766				24		2610		0.785				24.3		2550		0.791				24.1		2450		0.785				24		2710		0.785				23.8		2280		0.78				23.8		2870		0.78

		23.6		2370		0.766				23.6		2300		0.769				24.1		2620		0.787				24.3		2550		0.793				24.1		2460		0.787				24.1		2720		0.787				23.9		2290		0.782				23.9		2880		0.783

		23.6		2370		0.768				23.7		2300		0.771				24.2		2620		0.789				24.4		2560		0.795				24.2		2460		0.79				24.1		2730		0.791				24		2290		0.785				23.9		2890		0.785

		23.6		2380		0.769				23.7		2310		0.773				24.2		2630		0.791				24.4		2560		0.797				24.2		2470		0.792				24.2		2730		0.794				24		2300		0.787				24		2900		0.789

		23.7		2380		0.772				23.8		2310		0.775				24.4		2640		0.796				24.5		2570		0.799				24.3		2470		0.794				24.3		2740		0.796				24.1		2300		0.789				24.1		2900		0.791

		23.8		2390		0.774				23.9		2320		0.777				24.4		2640		0.798				24.6		2570		0.802				24.5		2480		0.798				24.4		2750		0.798				24.2		2310		0.791				24.2		2910		0.793

		23.8		2390		0.776				23.9		2320		0.779				24.4		2650		0.8				24.6		2580		0.804				24.5		2490		0.8				24.4		2750		0.8				24.2		2310		0.793				24.2		2920		0.795

		23.9		2400		0.778				24		2330		0.781				24.5		2650		0.802				24.7		2580		0.806				24.6		2490		0.802				24.5		2760		0.802				24.3		2320		0.795				24.3		2920		0.797

		24		2400		0.78				24		2330		0.783				24.6		2660		0.804				24.8		2580		0.808				24.7		2500		0.804				24.6		2760		0.804				24.3		2320		0.797				24.4		2930		0.799

		24.1		2410		0.782				24.1		2340		0.786				24.7		2660		0.806				24.9		2590		0.811				24.7		2500		0.807				24.6		2770		0.806				24.4		2330		0.799				24.4		2940		0.801

		24.1		2410		0.784				24.2		2340		0.788				24.7		2670		0.808				24.9		2590		0.813				24.7		2510		0.809				24.7		2780		0.81				24.5		2330		0.802				24.5		2940		0.803

		24.2		2420		0.786				24.3		2340		0.79				24.9		2680		0.813				25		2600		0.815				24.8		2510		0.81				24.8		2790		0.812				24.6		2340		0.806				24.6		2960		0.808

		24.2		2420		0.788				24.3		2350		0.793				24.9		2680		0.815				25		2600		0.817				25		2520		0.815				24.9		2790		0.814				24.7		2350		0.808				24.7		2960		0.81

		24.3		2430		0.79				24.4		2350		0.795				25		2690		0.816				25.1		2610		0.821				25		2530		0.817				24.9		2800		0.816				24.7		2350		0.81				24.7		2970		0.812

		24.4		2430		0.792				24.4		2360		0.797				25		2690		0.819				25.2		2620		0.823				25.1		2530		0.819				25		2800		0.819				24.8		2360		0.812				24.8		2970		0.814

		24.4		2440		0.795				24.5		2360		0.799				25.1		2700		0.821				25.3		2620		0.825				25.2		2540		0.821				25.1		2810		0.821				24.8		2360		0.814				24.9		2980		0.816

		24.5		2440		0.797				24.5		2370		0.801				25.2		2700		0.823				25.3		2620		0.827				25.2		2540		0.823				25.1		2820		0.823				24.9		2370		0.816				24.9		2990		0.818

		24.6		2450		0.801				24.6		2370		0.803				25.2		2710		0.825				25.4		2630		0.829				25.3		2550		0.825				25.2		2820		0.825				25		2370		0.818				25		2990		0.82

		24.7		2460		0.803				24.7		2380		0.807				25.4		2720		0.829				25.5		2630		0.831				25.3		2550		0.827				25.3		2830		0.829				25		2380		0.82				25.1		3000		0.822

		24.7		2460		0.805				24.8		2380		0.809				25.4		2720		0.831				25.5		2640		0.834				25.4		2560		0.832				25.4		2840		0.831				25.1		2390		0.823				25.2		3010		0.827

		24.8		2470		0.807				24.9		2390		0.811				25.5		2730		0.833				25.6		2640		0.837				25.5		2570		0.834				25.4		2850		0.833				25.2		2390		0.825				25.2		3020		0.829

		24.8		2470		0.809				24.9		2390		0.813				25.6		2730		0.836				25.7		2650		0.839				25.6		2570		0.836				25.5		2850		0.835				25.3		2400		0.827				25.3		3030		0.831

		24.9		2480		0.811				25		2400		0.816				25.6		2730		0.838				25.7		2650		0.841				25.7		2580		0.838				25.6		2860		0.838				25.3		2400		0.83				25.4		3030		0.833

		25		2480		0.813				25.1		2400		0.818				25.7		2740		0.84				25.8		2660		0.843				25.7		2580		0.84				25.6		2860		0.84				25.4		2410		0.832				25.5		3040		0.835

		25		2490		0.816				25.1		2410		0.82				25.7		2740		0.842				25.9		2660		0.845				25.8		2590		0.842				25.7		2870		0.842				25.4		2410		0.834				25.5		3050		0.837

		25.1		2500		0.819				25.2		2410		0.821				25.8		2750		0.844				26		2660		0.847				25.8		2590		0.844				25.8		2870		0.844				25.5		2420		0.836				25.6		3050		0.839

		25.2		2500		0.822				25.3		2420		0.826				25.9		2760		0.848				26		2670		0.849				25.9		2590		0.846				25.9		2890		0.848				25.6		2420		0.838				25.6		3060		0.841

		25.3		2510		0.824				25.4		2420		0.828				26		2760		0.85				26		2670		0.851				26		2600		0.85				25.9		2890		0.85				25.6		2430		0.84				25.8		3070		0.845

		25.3		2510		0.826				25.4		2430		0.83				26.1		2770		0.852				26.2		2680		0.856				26.1		2610		0.852				26		2900		0.852				25.7		2440		0.844				25.8		3080		0.847

		25.4		2520		0.828				25.5		2430		0.832				26.1		2770		0.854				26.3		2690		0.858				26.2		2610		0.855				26.1		2900		0.854				25.8		2440		0.846				25.9		3080		0.85

		25.5		2520		0.83				25.5		2440		0.834				26.2		2780		0.856				26.3		2690		0.86				26.2		2620		0.857				26.1		2910		0.857				25.9		2450		0.848				26		3090		0.852

		25.6		2530		0.832				25.6		2440		0.836				26.2		2780		0.859				26.4		2700		0.862				26.3		2620		0.859				26.2		2920		0.859				26		2450		0.85				26		3100		0.854

		25.6		2530		0.834				25.7		2450		0.838				26.3		2790		0.861				26.5		2700		0.864				26.3		2630		0.861				26.3		2920		0.861				26		2460		0.852				26.1		3100		0.856

		25.7		2540		0.837				25.8		2450		0.84				26.3		2790		0.863				26.5		2700		0.866				26.4		2630		0.863				26.3		2930		0.863				26.1		2460		0.854				26.1		3110		0.858

		25.7		2540		0.839				25.9		2460		0.845				26.5		2800		0.867				26.6		2710		0.868				26.5		2640		0.865				26.4		2940		0.867				26.1		2470		0.857				26.2		3120		0.86

		25.8		2550		0.841				25.9		2460		0.847				26.5		2810		0.869				26.6		2710		0.87				26.5		2640		0.867				26.5		2940		0.869				26.2		2470		0.859				26.3		3130		0.864

		25.9		2550		0.843				26		2470		0.849				26.6		2810		0.871				26.8		2720		0.875				26.6		2650		0.869				26.6		2950		0.871				26.3		2480		0.863				26.4		3140		0.866

		25.9		2560		0.846				26		2470		0.851				26.7		2820		0.873				26.8		2730		0.877				26.7		2650		0.871				26.6		2960		0.873				26.4		2490		0.865				26.5		3140		0.868

		26		2560		0.848				26.1		2480		0.853				26.7		2820		0.875				26.9		2730		0.879				26.7		2660		0.873				26.7		2960		0.875				26.4		2490		0.867				26.5		3150		0.87

		26.1		2570		0.85				26.2		2480		0.855				26.8		2830		0.878				27		2730		0.881				26.8		2660		0.875				26.8		2970		0.877				26.5		2500		0.869				26.6		3160		0.872

		26.1		2570		0.852				26.3		2480		0.857				26.9		2830		0.88				27		2740		0.883				26.8		2670		0.878				26.8		2970		0.879				26.6		2500		0.871				26.6		3160		0.875

		26.2		2580		0.856				26.3		2490		0.859				26.9		2830		0.882				27.1		2740		0.885				26.9		2670		0.88				26.9		2980		0.882				26.6		2510		0.873				26.7		3170		0.877

		26.3		2590		0.858				26.4		2500		0.863				27.1		2840		0.886				27.2		2750		0.887				27		2680		0.882				27		2990		0.886				26.7		2510		0.875				26.7		3180		0.879

		26.4		2590		0.86				26.5		2500		0.865				27.1		2850		0.888				27.2		2750		0.889				27		2680		0.884				27.1		3000		0.888				26.7		2520		0.877				26.9		3190		0.883

		26.5		2600		0.862				26.5		2510		0.867				27.2		2850		0.89				27.3		2760		0.892				27.2		2690		0.888				27.1		3000		0.89				26.8		2520		0.879				27		3200		0.885

		26.5		2600		0.864				26.6		2510		0.869				27.2		2860		0.892				27.3		2760		0.894				27.2		2690		0.89				27.2		3010		0.892				26.9		2530		0.883				27		3200		0.887

		26.6		2610		0.867				26.7		2520		0.871				27.3		2860		0.894				27.4		2760		0.896				27.3		2700		0.892				27.3		3020		0.894				27		2540		0.886				27.1		3210		0.889

		26.6		2610		0.868				26.8		2520		0.874				27.4		2870		0.896				27.5		2770		0.898				27.3		2700		0.894				27.3		3020		0.896				27.1		2540		0.888				27.1		3220		0.892

		26.7		2620		0.87				26.8		2520		0.876				27.4		2870		0.898				27.5		2770		0.9				27.4		2710		0.896				27.4		3030		0.899				27.1		2550		0.89				27.2		3220		0.894

		26.8		2620		0.873				26.9		2530		0.878				27.5		2880		0.9				27.6		2780		0.902				27.5		2710		0.898				27.4		3030		0.901				27.2		2550		0.892				27.3		3230		0.896

		26.8		2630		0.875				26.9		2530		0.88				27.6		2890		0.905				27.6		2780		0.904				27.5		2720		0.9				27.6		3040		0.905				27.3		2560		0.894				27.4		3240		0.9

		26.9		2630		0.877				27		2540		0.884				27.7		2890		0.907				27.7		2790		0.906				27.6		2720		0.902				27.6		3050		0.907				27.3		2560		0.896				27.5		3250		0.902

		27		2640		0.879				27.1		2550		0.886				27.8		2900		0.909				27.8		2790		0.908				27.7		2730		0.905				27.7		3060		0.909				27.4		2570		0.898				27.5		3250		0.904

		27		2640		0.881				27.2		2550		0.888				27.8		2900		0.911				27.9		2800		0.912				27.7		2730		0.907				27.8		3060		0.911				27.5		2580		0.902				27.6		3260		0.906

		27		2650		0.883				27.2		2550		0.89				27.9		2910		0.913				28		2800		0.915				27.8		2740		0.91				27.8		3070		0.913				27.6		2580		0.904				27.7		3270		0.908

		27.1		2650		0.885				27.3		2560		0.892				27.9		2910		0.915				28		2810		0.917				27.8		2740		0.912				27.9		3080		0.915				27.6		2590		0.907				27.7		3270		0.911

		27.2		2660		0.887				27.4		2560		0.895				28		2920		0.917				28.1		2810		0.919				27.9		2750		0.914				28		3080		0.917				27.7		2590		0.909				27.8		3280		0.913

		27.2		2660		0.889				27.4		2570		0.897				28.1		2920		0.919				28.2		2810		0.921				28		2750		0.916				28.1		3090		0.921				27.8		2600		0.911				27.9		3290		0.916

		27.4		2670		0.893				27.5		2570		0.899				28.1		2920		0.921				28.2		2820		0.923				28.1		2760		0.918				28.1		3100		0.924				27.8		2600		0.913				27.9		3300		0.918

		27.4		2680		0.895				27.6		2580		0.901				28.2		2930		0.926				28.3		2820		0.925				28.1		2760		0.92				28.2		3100		0.926				27.9		2610		0.915				28		3300		0.92

		27.5		2680		0.897				27.7		2580		0.904				28.3		2940		0.928				28.4		2830		0.927				28.2		2770		0.924				28.3		3110		0.928				27.9		2610		0.917				28		3310		0.922

		27.5		2690		0.899				27.7		2590		0.906				28.4		2940		0.93				28.5		2840		0.932				28.3		2770		0.926				28.3		3120		0.93				28.1		2620		0.92				28.1		3320		0.924

		27.6		2690		0.902				27.8		2590		0.908				28.4		2950		0.932				28.5		2840		0.934				28.4		2780		0.928				28.4		3120		0.932				28.1		2620		0.922				28.2		3320		0.926

		27.7		2700		0.904				27.8		2600		0.91				28.5		2950		0.934				28.6		2840		0.936				28.4		2780		0.93				28.5		3130		0.934				28.1		2630		0.924				28.2		3330		0.928

		27.7		2700		0.906				27.9		2600		0.912				28.6		2960		0.936				28.6		2850		0.938				28.5		2790		0.933				28.5		3130		0.936				28.2		2630		0.926				28.3		3340		0.93

		27.8		2710		0.908				27.9		2600		0.914				28.6		2960		0.938				28.7		2850		0.94				28.6		2790		0.934				28.6		3150		0.94				28.3		2640		0.928				28.4		3350		0.935

		27.9		2710		0.912				28		2610		0.916				28.7		2970		0.94				28.8		2860		0.942				28.6		2800		0.936				28.7		3150		0.943				28.3		2640		0.93				28.5		3350		0.937

		28		2720		0.914				28.1		2610		0.918				28.8		2980		0.944				28.9		2860		0.944				28.6		2800		0.938				28.8		3160		0.945				28.4		2650		0.932				28.6		3360		0.939

		28		2720		0.916				28.2		2620		0.921				28.9		2980		0.946				29		2870		0.948				28.8		2810		0.943				28.8		3160		0.947				28.5		2650		0.934				28.6		3370		0.941

		28.1		2730		0.918				28.2		2620		0.924				28.9		2980		0.948				29		2870		0.951				28.8		2820		0.945				28.9		3170		0.949				28.5		2660		0.938				28.7		3370		0.943

		28.2		2730		0.92				28.3		2630		0.926				29		2990		0.95				29.1		2880		0.953				28.9		2820		0.947				28.9		3180		0.951				28.6		2670		0.94				28.7		3380		0.945

		28.3		2740		0.922				28.3		2630		0.928				29.1		2990		0.952				29.1		2880		0.955				29		2820		0.949				29		3180		0.953				28.7		2670		0.942				28.8		3390		0.947

		28.3		2740		0.925				28.4		2640		0.93				29.1		3000		0.954				29.2		2890		0.957				29		2830		0.951				29.1		3190		0.955				28.7		2670		0.944				28.9		3390		0.949

		28.4		2750		0.927				28.5		2640		0.932				29.2		3000		0.957				29.3		2890		0.959				29.1		2830		0.953				29.2		3200		0.96				28.8		2680		0.946				29		3410		0.954

		28.4		2750		0.929				28.5		2640		0.934				29.2		3010		0.959				29.4		2900		0.961				29.2		2840		0.955				29.2		3210		0.961				28.9		2680		0.948				29.1		3410		0.956

		28.5		2760		0.933				28.6		2650		0.936				29.3		3010		0.962				29.5		2900		0.965				29.2		2840		0.957				29.3		3210		0.963				28.9		2690		0.95				29.1		3420		0.958

		28.6		2770		0.935				28.7		2650		0.938				29.4		3020		0.964				29.5		2910		0.967				29.3		2850		0.959				29.4		3220		0.966				29		2690		0.952				29.2		3430		0.96

		28.7		2770		0.937				28.8		2660		0.941				29.4		3020		0.966				29.6		2910		0.969				29.4		2850		0.962				29.5		3220		0.968				29		2700		0.954				29.3		3430		0.962

		28.8		2780		0.939				28.8		2660		0.943				29.5		3030		0.968				29.7		2920		0.972				29.4		2860		0.964				29.5		3230		0.97				29.2		2710		0.958				29.3		3440		0.964

		28.8		2780		0.941				28.9		2670		0.946				29.6		3030		0.97				29.7		2920		0.974				29.5		2860		0.966				29.6		3240		0.972				29.2		2710		0.96				29.4		3450		0.966

		28.9		2790		0.943				28.9		2670		0.948				29.6		3040		0.972				29.8		2920		0.976				29.6		2870		0.968				29.7		3240		0.974				29.3		2720		0.962				29.5		3450		0.968

		28.9		2790		0.946				29		2680		0.95				29.7		3040		0.974				29.9		2930		0.978				29.6		2870		0.971				29.8		3250		0.978				29.4		2720		0.964				29.6		3470		0.973

		29		2800		0.947				29.1		2680		0.952				29.8		3050		0.976				30		2940		0.982				29.7		2880		0.973				29.8		3260		0.98				29.4		2730		0.966				29.6		3470		0.975

		29		2800		0.949				29.1		2690		0.954				29.9		3060		0.98				30		2940		0.984				29.7		2880		0.975				29.9		3270		0.983				29.5		2730		0.968				29.7		3480		0.977

		29.2		2810		0.953				29.2		2690		0.956				30		3060		0.982				30.1		2950		0.986				29.8		2880		0.977				30		3270		0.985				29.5		2730		0.97				29.8		3490		0.979

		29.2		2810		0.955				29.3		2700		0.959				30		3060		0.984				30.2		2950		0.988				30		2890		0.981				30		3280		0.987				29.6		2740		0.972				29.8		3490		0.981

		29.3		2820		0.957				29.3		2700		0.961				30.1		3070		0.986				30.2		2950		0.991				30		2900		0.983				30.1		3280		0.989				29.7		2750		0.975				29.9		3500		0.983

		29.4		2820		0.959				29.4		2710		0.963				30.1		3070		0.989				30.3		2960		0.993				30.1		2900		0.985				30.2		3290		0.991				29.7		2750		0.977				30		3510		0.985

		29.4		2830		0.961				29.5		2710		0.965				30.2		3080		0.991				30.4		2960		0.995				30.1		2910		0.987				30.3		3300		0.995				29.8		2760		0.979				30.1		3520		0.988

		29.5		2830		0.963				29.5		2720		0.967				30.3		3080		0.993				30.4		2970		0.997				30.2		2910		0.989				30.4		3310		0.997				29.9		2760		0.981				30.1		3520		0.99

		29.5		2840		0.965				29.6		2720		0.969				30.3		3090		0.995				30.5		2970		0.999				30.2		2920		0.991				30.4		3310		1				29.9		2770		0.983				30.2		3530		0.992

		29.6		2840		0.967				29.7		2730		0.971				30.4		3100		0.999				30.5		2970		1				30.3		2920		0.994				30.5		3320		1				30		2770		0.985				30.2		3540		0.994

		29.6		2850		0.969				29.8		2730		0.974				30.5		3100		1				30.6		2980		1				30.4		2930		0.996				30.5		3330		1				30.1		2780		0.988				30.3		3540		0.997

		29.7		2850		0.972				29.9		2740		0.978				30.5		3110		1				30.7		2980		1				30.5		2940		1				30.6		3330		1.01				30.1		2780		0.99				30.3		3550		0.999

		29.8		2860		0.975				29.9		2740		0.98				30.6		3110		1				30.7		2990		1.01				30.6		2940		1				30.7		3340		1.01				30.2		2790		0.993				30.4		3560		1

		29.9		2860		0.976				30		2750		0.982				30.7		3120		1.01				30.8		2990		1.01				30.6		2940		1				30.7		3340		1.01				30.3		2790		0.995				30.5		3560		1

		29.9		2870		0.979				30.1		2750		0.984				30.8		3120		1.01				30.9		3000		1.01				30.7		2950		1.01				30.8		3350		1.01				30.3		2800		0.997				30.6		3580		1.01

		30		2870		0.981				30.1		2760		0.986				30.8		3120		1.01				30.9		3000		1.01				30.8		2950		1.01				30.9		3360		1.02				30.4		2800		0.999				30.7		3580		1.01

		30.1		2880		0.983				30.2		2760		0.988				30.9		3130		1.01				31		3000		1.02				30.8		2960		1.01				31		3370		1.02				30.5		2810		1				30.7		3590		1.01

		30.1		2880		0.985				30.3		2770		0.99				31		3140		1.02				31.1		3010		1.02				30.9		2960		1.01				31		3370		1.02				30.5		2810		1				30.8		3600		1.01

		30.2		2890		0.987				30.3		2770		0.992				31.1		3140		1.02				31.2		3020		1.02				30.9		2970		1.01				31.1		3380		1.02				30.6		2820		1				30.9		3600		1.02

		30.3		2900		0.991				30.3		2780		0.994				31.1		3150		1.02				31.2		3020		1.02				31.1		2980		1.02				31.1		3390		1.03				30.6		2820		1.01				30.9		3610		1.02

		30.4		2900		0.993				30.4		2780		0.997				31.2		3150		1.02				31.3		3020		1.03				31.1		2980		1.02				31.2		3390		1.03				30.7		2830		1.01				31		3620		1.02

		30.4		2900		0.995				30.5		2790		0.999				31.3		3160		1.03				31.4		3030		1.03				31.2		2990		1.02				31.3		3400		1.03				30.8		2830		1.01				31.1		3620		1.02

		30.5		2910		0.997				30.6		2790		1				31.3		3160		1.03				31.4		3030		1.03				31.3		2990		1.03				31.4		3410		1.03				30.8		2840		1.01				31.1		3630		1.02

		30.6		2910		0.999				30.7		2800		1				31.4		3170		1.03				31.5		3040		1.03				31.3		2990		1.03				31.5		3420		1.04				30.9		2840		1.02				31.2		3640		1.03

		30.6		2920		1				30.7		2800		1.01				31.5		3170		1.03				31.5		3040		1.03				31.4		3000		1.03				31.6		3420		1.04				31		2850		1.02				31.3		3640		1.03

		30.7		2920		1				30.8		2810		1.01				31.5		3180		1.03				31.7		3050		1.04				31.5		3000		1.03				31.6		3430		1.04				31		2850		1.02				31.3		3650		1.03

		30.7		2930		1.01				30.8		2810		1.01				31.6		3180		1.04				31.8		3050		1.04				31.5		3010		1.03				31.7		3430		1.04				31.1		2850		1.02				31.3		3660		1.03

		30.8		2930		1.01				30.9		2810		1.01				31.7		3190		1.04				31.8		3060		1.04				31.6		3020		1.04				31.7		3440		1.04				31.1		2860		1.02				31.4		3660		1.04

		30.9		2940		1.01				31		2820		1.01				31.8		3190		1.04				31.9		3060		1.05				31.7		3020		1.04				31.8		3450		1.05				31.2		2860		1.03				31.5		3670		1.04

		31		2950		1.01				31.1		2830		1.02				31.8		3200		1.05				31.9		3070		1.05				31.8		3030		1.04				31.8		3450		1.05				31.3		2870		1.03				31.6		3680		1.04

		31		2950		1.02				31.1		2830		1.02				31.9		3200		1.05				32		3070		1.05				31.8		3030		1.04				32		3470		1.05				31.4		2880		1.03				31.6		3680		1.04

		31.1		2960		1.02				31.2		2840		1.02				32		3210		1.05				32.1		3070		1.05				31.9		3040		1.05				32.1		3470		1.05				31.5		2880		1.03				31.7		3690		1.04

		31.2		2960		1.02				31.3		2840		1.02				32		3210		1.05				32.1		3080		1.05				32		3040		1.05				32.1		3480		1.06				31.5		2890		1.04				31.7		3700		1.05

		31.2		2960		1.02				31.3		2840		1.03				32.1		3220		1.05				32.2		3080		1.06				32		3040		1.05				32.2		3480		1.06				31.6		2890		1.04				31.8		3700		1.05

		31.3		2970		1.02				31.4		2850		1.03				32.2		3230		1.06				32.3		3090		1.06				32.1		3050		1.05				32.2		3490		1.06				31.7		2900		1.04				31.9		3710		1.05

		31.4		2970		1.03				31.4		2850		1.03				32.3		3230		1.06				32.4		3090		1.06				32.2		3060		1.06				32.3		3500		1.06				31.7		2900		1.04				31.9		3720		1.05

		31.4		2980		1.03				31.5		2860		1.03				32.3		3230		1.06				32.4		3100		1.06				32.2		3060		1.06				32.4		3500		1.07				31.8		2910		1.05				32		3720		1.05

		31.5		2990		1.03				31.6		2860		1.04				32.4		3240		1.06				32.5		3100		1.07				32.3		3070		1.06				32.5		3510		1.07				31.9		2910		1.05				32		3730		1.06

		31.6		2990		1.04				31.7		2870		1.04				32.4		3240		1.07				32.6		3110		1.07				32.4		3070		1.06				32.6		3520		1.07				31.9		2920		1.05				32.1		3740		1.06

		31.7		3000		1.04				31.8		2870		1.04				32.5		3250		1.07				32.6		3110		1.07				32.4		3080		1.06				32.6		3520		1.07				32		2920		1.05				32.2		3750		1.06

		31.8		3000		1.04				31.8		2880		1.04				32.6		3250		1.07				32.7		3120		1.07				32.5		3080		1.07				32.7		3530		1.08				32		2930		1.05				32.3		3760		1.06

		31.8		3010		1.04				31.8		2880		1.04				32.6		3260		1.07				32.8		3120		1.07				32.6		3090		1.07				32.8		3540		1.08				32.1		2930		1.06				32.4		3760		1.07

		31.9		3010		1.04				31.9		2880		1.05				32.7		3260		1.08				32.9		3130		1.08				32.6		3090		1.07				32.8		3540		1.08				32.2		2940		1.06				32.5		3770		1.07

		31.9		3010		1.05				32		2890		1.05				32.8		3270		1.08				32.9		3130		1.08				32.7		3100		1.07				32.8		3550		1.08				32.2		2940		1.06				32.5		3780		1.07

		32		3020		1.05				32.1		2890		1.05				32.9		3270		1.08				33		3140		1.08				32.8		3100		1.08				32.9		3550		1.08				32.3		2950		1.06				32.5		3780		1.07

		32.1		3030		1.05				32.1		2900		1.05				32.9		3280		1.08				33		3140		1.08				32.8		3110		1.08				33.1		3570		1.09				32.4		2950		1.06				32.6		3790		1.08

		32.2		3030		1.05				32.2		2900		1.06				33		3280		1.08				33.1		3140		1.09				32.9		3110		1.08				33.1		3570		1.09				32.4		2960		1.07				32.8		3800		1.08

		32.2		3040		1.06				32.3		2910		1.06				33		3290		1.09				33.2		3150		1.09				33		3120		1.08				33.2		3580		1.09				32.5		2960		1.07				32.8		3810		1.08

		32.3		3040		1.06				32.3		2910		1.06				33.1		3290		1.09				33.2		3150		1.09				33		3120		1.08				33.3		3590		1.09				32.6		2970		1.07				32.9		3820		1.08

		32.3		3040		1.06				32.4		2920		1.06				33.2		3290		1.09				33.3		3160		1.09				33.1		3130		1.09				33.3		3590		1.1				32.6		2970		1.07				33		3820		1.09

		32.4		3050		1.06				32.4		2920		1.06				33.3		3300		1.09				33.4		3160		1.1				33.2		3130		1.09				33.4		3600		1.1				32.7		2980		1.08				33		3830		1.09

		32.4		3050		1.06				32.5		2930		1.07				33.3		3310		1.1				33.5		3170		1.1				33.3		3140		1.09				33.4		3600		1.1				32.8		2980		1.08				33.1		3840		1.09

		32.5		3060		1.07				32.6		2930		1.07				33.4		3310		1.1				33.6		3170		1.1				33.4		3140		1.1				33.5		3610		1.1				32.9		2990		1.08				33.1		3840		1.09

		32.6		3060		1.07				32.7		2940		1.07				33.4		3310		1.1				33.6		3180		1.1				33.4		3150		1.1				33.6		3620		1.11				32.9		2990		1.08				33.2		3850		1.09

		32.7		3070		1.07				32.7		2940		1.08				33.5		3320		1.1				33.7		3180		1.11				33.5		3150		1.1				33.6		3620		1.11				32.9		3000		1.08				33.3		3860		1.1

		32.7		3080		1.07				32.8		2950		1.08				33.5		3320		1.1				33.7		3180		1.11				33.5		3160		1.1				33.7		3630		1.11				33		3000		1.09				33.4		3870		1.1

		32.8		3080		1.07				32.9		2950		1.08				33.6		3330		1.11				33.8		3190		1.11				33.6		3160		1.1				33.8		3640		1.11				33.1		3010		1.09				33.4		3880		1.1

		32.9		3080		1.08				32.9		2960		1.08				33.7		3330		1.11				33.8		3190		1.11				33.7		3170		1.11				33.9		3640		1.11				33.2		3010		1.09				33.5		3880		1.1

		32.9		3090		1.08				33		2960		1.08				33.8		3340		1.11				33.9		3200		1.11				33.7		3170		1.11				33.9		3650		1.12				33.2		3020		1.09				33.6		3890		1.11

		33		3090		1.08				33.1		2960		1.09				33.9		3350		1.11				34		3200		1.12				33.9		3180		1.11				34		3650		1.12				33.3		3020		1.1				33.6		3900		1.11

		33		3100		1.08				33.1		2970		1.09				33.9		3350		1.12				34.1		3210		1.12				33.9		3180		1.11				34		3660		1.12				33.4		3030		1.1				33.7		3900		1.11

		33.1		3100		1.09				33.2		2980		1.09				34		3350		1.12				34.2		3210		1.12				34		3190		1.12				34.1		3670		1.13				33.4		3030		1.1				33.8		3910		1.11

		33.2		3110		1.09				33.3		2980		1.09				34.1		3360		1.12				34.2		3220		1.12				34		3190		1.12				34.2		3680		1.13				33.5		3040		1.1				33.9		3920		1.12

		33.3		3120		1.09				33.4		2980		1.1				34.1		3360		1.12				34.2		3220		1.13				34.1		3200		1.12				34.3		3690		1.13				33.5		3040		1.1				33.9		3930		1.12

		33.3		3120		1.09				33.4		2990		1.1				34.2		3370		1.12				34.3		3220		1.13				34.2		3200		1.12				34.4		3690		1.13				33.6		3050		1.11				34		3940		1.12

		33.4		3120		1.09				33.5		2990		1.1				34.3		3370		1.13				34.4		3230		1.13				34.2		3210		1.12				34.4		3700		1.13				33.7		3050		1.11				34.1		3940		1.12

		33.4		3130		1.1				33.6		3000		1.1				34.4		3380		1.13				34.5		3240		1.13				34.3		3210		1.13				34.5		3700		1.14				33.8		3060		1.11				34.1		3950		1.13

		33.5		3130		1.1				33.6		3000		1.1				34.5		3390		1.13				34.6		3240		1.14				34.4		3220		1.13				34.5		3710		1.14				33.9		3060		1.11				34.2		3960		1.13

		33.6		3140		1.1				33.7		3010		1.11				34.5		3390		1.13				34.6		3240		1.14				34.5		3230		1.13				34.6		3720		1.14				33.9		3070		1.12				34.3		3960		1.13

		33.7		3140		1.1				33.8		3010		1.11				34.5		3400		1.14				34.7		3250		1.14				34.6		3230		1.14				34.7		3720		1.14				34		3070		1.12				34.3		3970		1.13

		33.7		3150		1.11				33.8		3010		1.11				34.6		3400		1.14				34.8		3250		1.14				34.6		3230		1.14				34.8		3730		1.15				34		3080		1.12				34.5		3980		1.14

		33.8		3150		1.11				33.9		3020		1.11				34.7		3410		1.14				34.8		3260		1.14				34.7		3240		1.14				34.8		3740		1.15				34.1		3080		1.12				34.5		3990		1.14

		33.9		3160		1.11				34		3020		1.12				34.8		3410		1.14				34.9		3260		1.15				34.7		3240		1.14				34.9		3740		1.15				34.1		3090		1.12				34.6		4000		1.14

		33.9		3170		1.11				34.1		3030		1.12				34.8		3410		1.15				35		3260		1.15				34.8		3250		1.14				35		3750		1.15				34.2		3090		1.13				34.6		4000		1.14

		34		3170		1.12				34.1		3030		1.12				34.9		3420		1.15				35.1		3270		1.15				34.8		3250		1.15				35		3760		1.15				34.3		3100		1.13				34.7		4010		1.14

		34.1		3180		1.12				34.2		3040		1.12				35		3430		1.15				35.1		3280		1.15				35		3260		1.15				35.1		3760		1.16				34.4		3100		1.13				34.8		4020		1.15

		34.2		3180		1.12				34.2		3040		1.12				35		3430		1.15				35.2		3280		1.16				35		3260		1.15				35.1		3770		1.16				34.4		3110		1.13				34.8		4020		1.15

		34.2		3180		1.12				34.3		3050		1.13				35.1		3440		1.15				35.3		3290		1.16				35.1		3270		1.15				35.3		3780		1.16				34.5		3110		1.14				34.9		4030		1.15

		34.3		3190		1.12				34.4		3050		1.13				35.2		3440		1.16				35.3		3290		1.16				35.1		3270		1.15				35.3		3790		1.16				34.6		3120		1.14				35		4040		1.15

		34.3		3190		1.13				34.4		3060		1.13				35.2		3440		1.16				35.4		3290		1.16				35.2		3280		1.16				35.4		3790		1.17				34.6		3120		1.14				35.1		4050		1.16

		34.4		3200		1.13				34.5		3060		1.13				35.3		3450		1.16				35.5		3300		1.16				35.3		3280		1.16				35.5		3800		1.17				34.7		3130		1.14				35.1		4060		1.16

		34.4		3200		1.13				34.6		3060		1.14				35.4		3450		1.16				35.5		3300		1.17				35.3		3290		1.16				35.5		3800		1.17				34.8		3130		1.14				35.2		4060		1.16

		34.5		3210		1.13				34.7		3070		1.14				35.5		3460		1.17				35.6		3310		1.17				35.4		3290		1.16				35.6		3810		1.17				34.9		3140		1.15				35.3		4070		1.16

		34.6		3210		1.13				34.7		3070		1.14				35.5		3470		1.17				35.7		3310		1.17				35.5		3300		1.17				35.6		3820		1.17				34.9		3150		1.15				35.3		4080		1.16

		34.6		3220		1.14				34.8		3080		1.14				35.6		3470		1.17				35.7		3320		1.17				35.6		3300		1.17				35.7		3820		1.18				35		3150		1.15				35.4		4080		1.17

		34.7		3220		1.14				34.8		3080		1.14				35.7		3480		1.17				35.8		3320		1.18				35.7		3310		1.17				35.8		3830		1.18				35		3150		1.15				35.5		4090		1.17

		34.8		3220		1.14				34.9		3090		1.15				35.7		3480		1.18				35.9		3330		1.18				35.7		3310		1.17				35.9		3840		1.18				35.1		3160		1.16				35.6		4100		1.17

		34.8		3230		1.14				35		3090		1.15				35.8		3490		1.18				35.9		3330		1.18				35.8		3320		1.18				35.9		3850		1.18				35.2		3160		1.16				35.6		4110		1.18

		34.9		3230		1.14				35		3100		1.15				35.9		3490		1.18				36		3330		1.18				35.8		3320		1.18				36		3850		1.19				35.3		3170		1.16				35.7		4120		1.18

		35		3240		1.15				35.1		3100		1.15				36		3500		1.18				36.1		3340		1.18				35.9		3330		1.18				36.1		3860		1.19				35.3		3170		1.16				35.7		4120		1.18

		35		3240		1.15				35.2		3100		1.16				36		3500		1.18				36.1		3340		1.19				36		3330		1.18				36.1		3870		1.19				35.4		3180		1.16				35.8		4130		1.18

		35.1		3250		1.15				35.2		3110		1.16				36.1		3510		1.19				36.2		3350		1.19				36		3340		1.18				36.2		3870		1.19				35.5		3190		1.17				35.9		4140		1.18

		35.1		3250		1.15				35.3		3110		1.16				36.1		3510		1.19				36.2		3350		1.19				36.2		3340		1.19				36.3		3880		1.2				35.5		3190		1.17				36		4140		1.19

		35.2		3250		1.15				35.4		3120		1.16				36.2		3520		1.19				36.3		3360		1.19				36.2		3350		1.19				36.3		3880		1.2				35.6		3200		1.17				36		4150		1.19

		35.3		3260		1.16				35.5		3130		1.17				36.3		3520		1.19				36.4		3360		1.2				36.3		3350		1.19				36.5		3900		1.2				35.7		3200		1.18				36.1		4160		1.19

		35.3		3260		1.16				35.6		3130		1.17				36.3		3530		1.2				36.5		3370		1.2				36.3		3360		1.19				36.5		3900		1.2				35.8		3210		1.18				36.2		4170		1.19

		35.4		3270		1.16				35.6		3130		1.17				36.4		3530		1.2				36.5		3370		1.2				36.4		3360		1.2				36.6		3910		1.21				35.8		3210		1.18				36.2		4180		1.2

		35.4		3270		1.16				35.7		3140		1.17				36.5		3540		1.2				36.6		3380		1.2				36.5		3370		1.2				36.6		3910		1.21				35.9		3220		1.18				36.3		4180		1.2

		35.5		3280		1.17				35.7		3140		1.17				36.6		3540		1.2				36.6		3380		1.2				36.5		3370		1.2				36.7		3920		1.21				35.9		3220		1.18				36.4		4190		1.2

		35.6		3290		1.17				35.8		3150		1.18				36.6		3550		1.21				36.7		3390		1.21				36.6		3380		1.2				36.8		3930		1.21				36		3230		1.19				36.4		4200		1.2

		35.7		3290		1.17				35.8		3150		1.18				36.7		3550		1.21				36.7		3390		1.21				36.7		3380		1.21				36.8		3930		1.21				36.1		3230		1.19				36.5		4200		1.2

		35.8		3290		1.17				35.9		3150		1.18				36.7		3560		1.21				36.8		3400		1.21				36.7		3380		1.21				36.9		3940		1.22				36.1		3240		1.19				36.5		4210		1.21

		35.8		3300		1.18				36		3160		1.18				36.8		3560		1.21				36.9		3400		1.21				36.8		3390		1.21				37		3950		1.22				36.2		3240		1.19				36.6		4220		1.21

		35.9		3300		1.18				36.1		3160		1.19				36.9		3560		1.21				36.9		3400		1.21				36.8		3390		1.21				37.1		3960		1.22				36.3		3250		1.19				36.7		4230		1.21

		35.9		3310		1.18				36.1		3170		1.19				36.9		3570		1.22				37		3410		1.22				36.9		3400		1.21				37.1		3960		1.22				36.3		3250		1.2				36.8		4240		1.21

		36		3310		1.18				36.2		3170		1.19				37		3570		1.22				37.1		3410		1.22				37		3400		1.22				37.2		3970		1.23				36.4		3260		1.2				36.9		4240		1.22

		36.1		3320		1.18				36.2		3180		1.19				37.1		3580		1.22				37.2		3420		1.22				37		3410		1.22				37.2		3980		1.23				36.5		3260		1.2				36.9		4250		1.22

		36.1		3320		1.19				36.3		3180		1.19				37.1		3580		1.22				37.2		3420		1.22				37.1		3410		1.22				37.3		3980		1.23				36.5		3270		1.2				37		4260		1.22

		36.3		3330		1.19				36.4		3190		1.2				37.2		3590		1.22				37.3		3420		1.23				37.2		3420		1.22				37.4		3990		1.23				36.6		3270		1.21				37		4260		1.22

		36.3		3330		1.19				36.4		3190		1.2				37.3		3590		1.23				37.3		3430		1.23				37.3		3420		1.23				37.5		3990		1.23				36.7		3280		1.21				37.1		4270		1.22

		36.3		3340		1.19				36.5		3190		1.2				37.3		3600		1.23				37.4		3430		1.23				37.4		3430		1.23				37.5		4000		1.24				36.7		3280		1.21				37.2		4280		1.23

		36.4		3340		1.2				36.6		3200		1.2				37.4		3600		1.23				37.4		3440		1.23				37.4		3430		1.23				37.6		4010		1.24				36.8		3290		1.21				37.3		4290		1.23

		36.5		3350		1.2				36.7		3210		1.21				37.4		3610		1.23				37.5		3440		1.23				37.5		3440		1.23				37.7		4020		1.24				36.8		3290		1.21				37.4		4300		1.23

		36.6		3350		1.2				36.7		3210		1.21				37.5		3610		1.23				37.6		3450		1.24				37.5		3440		1.23				37.8		4020		1.24				36.9		3300		1.22				37.4		4300		1.24

		36.6		3350		1.2				36.8		3220		1.21				37.6		3620		1.24				37.7		3450		1.24				37.6		3450		1.24				37.8		4030		1.25				37		3300		1.22				37.5		4310		1.24

		36.7		3360		1.2				36.9		3220		1.21				37.7		3620		1.24				37.7		3450		1.24				37.6		3450		1.24				37.9		4040		1.25				37		3310		1.22				37.6		4320		1.24

		36.7		3360		1.21				37		3220		1.21				37.7		3630		1.24				37.8		3460		1.24				37.7		3460		1.24				38		4040		1.25				37.2		3310		1.23				37.6		4320		1.24

		36.8		3370		1.21				37		3230		1.22				37.8		3630		1.24				37.9		3470		1.25				37.8		3460		1.24				38		4050		1.25				37.2		3320		1.23				37.7		4330		1.24

		36.9		3380		1.21				37.1		3230		1.22				37.8		3640		1.25				37.9		3470		1.25				37.8		3470		1.25				38.1		4050		1.26				37.3		3320		1.23				37.8		4340		1.25

		37		3380		1.21				37.2		3240		1.22				37.9		3640		1.25				38		3470		1.25				37.9		3470		1.25				38.2		4070		1.26				37.3		3330		1.23				37.8		4350		1.25

		37.1		3380		1.22				37.2		3240		1.22				38		3640		1.25				38.1		3480		1.25				38		3470		1.25				38.3		4070		1.26				37.4		3330		1.23				37.9		4350		1.25

		37.1		3390		1.22				37.3		3250		1.23				38		3650		1.25				38.2		3480		1.25				38.1		3480		1.25				38.3		4080		1.26				37.5		3340		1.24				38		4360		1.25

		37.2		3390		1.22				37.4		3250		1.23				38.1		3660		1.26				38.2		3490		1.26				38.1		3480		1.25				38.4		4090		1.27				37.5		3340		1.24				38		4370		1.25

		37.2		3400		1.22				37.4		3260		1.23				38.2		3660		1.26				38.3		3490		1.26				38.2		3490		1.26				38.4		4090		1.27				37.6		3350		1.24				38.1		4370		1.26

		37.3		3400		1.22				37.5		3260		1.23				38.3		3670		1.26				38.3		3500		1.26				38.3		3500		1.26				38.5		4100		1.27				37.7		3350		1.24				38.2		4380		1.26

		37.4		3410		1.23				37.5		3260		1.23				38.3		3670		1.26				38.4		3500		1.26				38.4		3500		1.26				38.6		4100		1.27				37.8		3360		1.24				38.2		4390		1.26

		37.5		3420		1.23				37.6		3270		1.24				38.4		3680		1.26				38.5		3510		1.27				38.4		3510		1.26				38.6		4110		1.27				37.8		3370		1.25				38.3		4390		1.26

		37.5		3420		1.23				37.6		3270		1.24				38.4		3680		1.27				38.5		3510		1.27				38.5		3510		1.27				38.7		4120		1.28				37.9		3370		1.25				38.4		4410		1.27

		37.6		3420		1.24				37.8		3280		1.24				38.5		3690		1.27				38.6		3510		1.27				38.6		3510		1.27				38.8		4120		1.28				37.9		3370		1.25				38.5		4410		1.27

		37.7		3430		1.24				37.8		3280		1.24				38.6		3690		1.27				38.7		3520		1.27				38.6		3520		1.27				38.9		4130		1.28				38		3380		1.25				38.5		4420		1.27

		37.7		3430		1.24				37.9		3290		1.25				38.7		3700		1.27				38.7		3520		1.27				38.7		3520		1.27				38.9		4140		1.28				38.1		3380		1.26				38.6		4430		1.27

		37.8		3440		1.24				38		3290		1.25				38.8		3700		1.28				38.8		3530		1.28				38.7		3530		1.27				39		4140		1.29				38.1		3390		1.26				38.7		4430		1.28

		37.9		3440		1.24				38		3300		1.25				38.8		3710		1.28				38.8		3530		1.28				38.8		3530		1.28				39		4150		1.29				38.2		3390		1.26				38.7		4440		1.28

		38		3450		1.25				38.1		3300		1.25				38.9		3710		1.28				38.9		3530		1.28				38.9		3540		1.28				39.1		4160		1.29				38.3		3400		1.26				38.8		4450		1.28

		38		3460		1.25				38.1		3310		1.25				39		3720		1.28				39		3540		1.28				39		3550		1.28				39.2		4160		1.29				38.3		3410		1.26				38.8		4450		1.28

		38.1		3460		1.25				38.2		3310		1.26				39		3720		1.28				39.1		3540		1.29				39.1		3550		1.29				39.2		4170		1.29				38.4		3410		1.27				39		4470		1.29

		38.2		3460		1.25				38.3		3320		1.26				39.1		3720		1.29				39.2		3550		1.29				39.1		3560		1.29				39.3		4180		1.3				38.5		3410		1.27				39		4480		1.29

		38.2		3470		1.26				38.4		3320		1.26				39.1		3730		1.29				39.2		3550		1.29				39.2		3560		1.29				39.4		4180		1.3				38.5		3420		1.27				39.1		4480		1.29

		38.3		3470		1.26				38.5		3330		1.27				39.3		3740		1.29				39.3		3560		1.29				39.2		3570		1.29				39.4		4190		1.3				38.6		3420		1.27				39.2		4490		1.29

		38.3		3480		1.26				38.5		3330		1.27				39.3		3740		1.3				39.3		3560		1.29				39.3		3570		1.29				39.5		4200		1.3				38.7		3430		1.27				39.2		4500		1.29

		38.4		3480		1.26				38.6		3340		1.27				39.4		3750		1.3				39.4		3560		1.3				39.4		3580		1.3				39.6		4200		1.3				38.7		3430		1.28				39.3		4500		1.3

		38.5		3490		1.26				38.6		3340		1.27				39.5		3750		1.3				39.4		3570		1.3				39.5		3580		1.3				39.6		4210		1.31				38.8		3440		1.28				39.3		4510		1.3

		38.6		3500		1.27				38.7		3340		1.27				39.5		3760		1.3				39.5		3570		1.3				39.6		3590		1.3				39.7		4210		1.31				38.9		3450		1.28				39.4		4520		1.3

		38.7		3500		1.27				38.8		3350		1.28				39.6		3760		1.3				39.7		3580		1.3				39.6		3590		1.3				39.7		4220		1.31				38.9		3450		1.28				39.5		4530		1.3

		38.7		3500		1.27				38.9		3350		1.28				39.6		3770		1.31				39.7		3580		1.31				39.7		3600		1.31				39.8		4230		1.31				39		3460		1.29				39.6		4540		1.31

		38.8		3510		1.27				38.9		3360		1.28				39.7		3770		1.31				39.8		3590		1.31				39.8		3600		1.31				39.9		4240		1.32				39.1		3460		1.29				39.7		4540		1.31

		38.8		3510		1.28				39		3360		1.28				39.8		3780		1.31				39.8		3590		1.31				39.8		3610		1.31				40		4240		1.32				39.1		3460		1.29				39.7		4550		1.31

		38.9		3520		1.28				39.1		3370		1.29				39.9		3790		1.31				39.9		3600		1.31				39.9		3620		1.31				40.1		4250		1.32				39.2		3470		1.29				39.8		4560		1.31

		39		3520		1.28				39.1		3370		1.29				40		3790		1.32				39.9		3600		1.32				40		3620		1.32				40.1		4260		1.32				39.3		3470		1.29				39.8		4560		1.32

		39		3530		1.28				39.2		3370		1.29				40		3800		1.32				40		3600		1.32				40.1		3620		1.32				40.2		4260		1.33				39.3		3480		1.3				39.9		4570		1.32

		39.1		3530		1.28				39.2		3380		1.29				40.1		3800		1.32				40.1		3610		1.32				40.1		3630		1.32				40.2		4270		1.33				39.4		3490		1.3				39.9		4580		1.32

		39.2		3540		1.29				39.3		3380		1.29				40.2		3810		1.32				40.1		3610		1.32				40.2		3630		1.32				40.3		4280		1.33				39.5		3490		1.3				40.1		4590		1.32

		39.2		3540		1.29				39.4		3390		1.3				40.2		3810		1.33				40.2		3620		1.33				40.3		3640		1.33				40.4		4280		1.33				39.6		3500		1.31				40.2		4600		1.33

		39.3		3550		1.29				39.5		3400		1.3				40.3		3810		1.33				40.3		3630		1.33				40.3		3640		1.33				40.5		4290		1.34				39.6		3500		1.31				40.2		4600		1.33

		39.4		3550		1.29				39.5		3400		1.3				40.4		3820		1.33				40.4		3630		1.33				40.5		3650		1.33				40.5		4300		1.34				39.7		3510		1.31				40.3		4610		1.33

		39.4		3560		1.3				39.6		3400		1.3				40.5		3830		1.33				40.5		3630		1.33				40.5		3660		1.33				40.6		4310		1.34				39.8		3510		1.31				40.3		4620		1.33

		39.5		3560		1.3				39.7		3410		1.31				40.5		3830		1.34				40.5		3640		1.33				40.6		3660		1.34				40.7		4310		1.34				39.8		3520		1.31				40.4		4620		1.33

		39.6		3560		1.3				39.7		3410		1.31				40.6		3840		1.34				40.6		3640		1.34				40.6		3660		1.34				40.7		4320		1.34				39.9		3520		1.32				40.4		4630		1.34

		39.6		3570		1.3				39.8		3420		1.31				40.7		3840		1.34				40.6		3650		1.34				40.7		3670		1.34				40.8		4320		1.35				40		3530		1.32				40.5		4640		1.34

		39.7		3570		1.3				39.9		3420		1.31				40.7		3850		1.34				40.7		3650		1.34				40.8		3670		1.34				40.9		4330		1.35				40.1		3540		1.32				40.6		4650		1.34

		39.8		3580		1.31				39.9		3420		1.31				40.8		3850		1.34				40.8		3660		1.34				40.8		3680		1.34				40.9		4340		1.35				40.2		3540		1.32				40.7		4660		1.34

		39.8		3580		1.31				40		3430		1.32				40.8		3860		1.35				40.9		3660		1.35				41		3690		1.35				41.1		4350		1.35				40.2		3540		1.33				40.8		4670		1.35

		39.9		3590		1.31				40.1		3440		1.32				40.9		3860		1.35				40.9		3670		1.35				41		3690		1.35				41.1		4360		1.36				40.3		3550		1.33				40.8		4670		1.35

		40		3590		1.31				40.2		3440		1.32				41		3870		1.35				41		3670		1.35				41.1		3700		1.35				41.2		4360		1.36				40.3		3550		1.33				40.9		4680		1.35

		40		3590		1.31				40.2		3450		1.32				41		3870		1.35				41.1		3670		1.35				41.1		3700		1.35				41.2		4370		1.36				40.4		3560		1.33				40.9		4690		1.35

		40.1		3600		1.32				40.3		3450		1.33				41.1		3880		1.36				41.1		3680		1.35				41.2		3700		1.36				41.3		4370		1.36				40.4		3560		1.33				41		4690		1.35

		40.1		3600		1.32				40.4		3450		1.33				41.2		3880		1.36				41.2		3680		1.36				41.2		3710		1.36				41.4		4380		1.37				40.5		3570		1.34				41.1		4700		1.36

		40.2		3610		1.32				40.4		3460		1.33				41.2		3890		1.36				41.3		3690		1.36				41.3		3710		1.36				41.4		4390		1.37				40.6		3580		1.34				41.2		4710		1.36

		40.2		3610		1.32				40.5		3460		1.33				41.3		3890		1.36				41.3		3690		1.36				41.4		3720		1.36				41.5		4390		1.37				40.7		3580		1.34				41.3		4720		1.36

		40.4		3620		1.33				40.6		3470		1.34				41.4		3900		1.36				41.4		3700		1.36				41.5		3720		1.37				41.6		4400		1.37				40.7		3580		1.34				41.3		4730		1.37

		40.4		3620		1.33				40.7		3470		1.34				41.5		3900		1.37				41.4		3700		1.36				41.6		3730		1.37				41.7		4410		1.37				40.8		3590		1.35				41.4		4740		1.37

		40.5		3630		1.33				40.7		3480		1.34				41.5		3910		1.37				41.5		3700		1.37				41.6		3740		1.37				41.7		4420		1.38				40.8		3590		1.35				41.4		4740		1.37

		40.6		3630		1.33				40.8		3480		1.34				41.6		3910		1.37				41.6		3710		1.37				41.7		3740		1.37				41.8		4420		1.38				40.9		3600		1.35				41.5		4750		1.37

		40.6		3640		1.34				40.9		3490		1.35				41.7		3920		1.37				41.6		3710		1.37				41.8		3750		1.38				41.8		4430		1.38				41		3600		1.35				41.6		4760		1.37

		40.7		3640		1.34				40.9		3490		1.35				41.7		3920		1.37				41.7		3720		1.37				41.8		3750		1.38				41.9		4430		1.38				41		3610		1.35				41.7		4760		1.38

		40.8		3650		1.34				41		3500		1.35				41.8		3920		1.38				41.7		3720		1.38				41.9		3750		1.38				42		4440		1.38				41.2		3620		1.36				41.8		4780		1.38

		40.8		3650		1.34				41.1		3500		1.35				41.8		3930		1.38				41.8		3720		1.38				42		3760		1.38				42		4450		1.39				41.2		3620		1.36				41.8		4780		1.38

		40.9		3650		1.34				41.2		3510		1.35				41.9		3930		1.38				41.9		3730		1.38				42.1		3770		1.39				42.2		4460		1.39				41.3		3630		1.36				41.9		4790		1.38

		41		3660		1.35				41.2		3510		1.36				41.9		3940		1.38				42		3740		1.38				42.1		3770		1.39				42.2		4470		1.39				41.4		3630		1.36				41.9		4800		1.39

		41		3670		1.35				41.3		3510		1.36				42.1		3950		1.39				42.1		3740		1.39				42.2		3770		1.39				42.3		4470		1.4				41.4		3640		1.37				42		4800		1.39

		41.1		3670		1.35				41.3		3520		1.36				42.2		3950		1.39				42.2		3740		1.39				42.2		3780		1.39				42.3		4480		1.4				41.5		3640		1.37				42.1		4810		1.39

		41.2		3670		1.35				41.4		3520		1.36				42.2		3960		1.39				42.2		3750		1.39				42.3		3780		1.39				42.4		4480		1.4				41.5		3650		1.37				42.1		4820		1.39

		41.2		3680		1.36				41.5		3530		1.37				42.3		3960		1.39				42.2		3750		1.39				42.3		3790		1.4				42.5		4490		1.4				41.6		3650		1.37				42.2		4820		1.39

		41.3		3680		1.36				41.5		3530		1.37				42.3		3970		1.4				42.3		3760		1.39				42.4		3790		1.4				42.5		4500		1.4				41.7		3660		1.38				42.3		4840		1.4

		41.4		3690		1.36				41.6		3540		1.37				42.4		3970		1.4				42.4		3760		1.4				42.5		3800		1.4				42.6		4500		1.41				41.7		3660		1.38				42.4		4840		1.4

		41.4		3690		1.36				41.6		3540		1.37				42.4		3980		1.4				42.5		3770		1.4				42.6		3800		1.4				42.7		4510		1.41				41.8		3670		1.38				42.5		4850		1.4

		41.5		3700		1.36				41.7		3550		1.37				42.5		3980		1.4				42.5		3770		1.4				42.7		3810		1.41				42.8		4520		1.41				41.9		3670		1.38				42.5		4860		1.4

		41.6		3700		1.37				41.8		3550		1.38				42.7		3990		1.41				42.6		3780		1.4				42.8		3810		1.41				42.8		4530		1.41				41.9		3680		1.38				42.6		4870		1.41

		41.6		3700		1.37				41.9		3550		1.38				42.7		3990		1.41				42.7		3780		1.41				42.8		3820		1.41				42.9		4530		1.42				42		3680		1.39				42.7		4870		1.41

		41.7		3710		1.37				42		3560		1.38				42.8		4000		1.41				42.7		3780		1.41				42.9		3820		1.41				43		4540		1.42				42.1		3690		1.39				42.7		4880		1.41

		41.7		3710		1.37				42		3560		1.38				42.8		4000		1.41				42.8		3790		1.41				42.9		3830		1.41				43		4550		1.42				42.1		3690		1.39				42.8		4890		1.41

		41.8		3720		1.37				42.1		3570		1.38				42.9		4010		1.41				42.8		3790		1.41				43		3830		1.42				43.1		4550		1.42				42.2		3700		1.39				42.8		4900		1.42

		41.9		3720		1.38				42.1		3570		1.39				42.9		4010		1.42				42.9		3800		1.41				43.1		3840		1.42				43.2		4560		1.42				42.3		3710		1.4				42.9		4900		1.42

		41.9		3730		1.38				42.2		3570		1.39				43		4020		1.42				43		3800		1.42				43.2		3840		1.42				43.3		4570		1.43				42.4		3710		1.4				43		4910		1.42

		42		3730		1.38				42.3		3580		1.39				43.1		4020		1.42				43.1		3810		1.42				43.3		3850		1.43				43.3		4580		1.43				42.4		3720		1.4				43		4920		1.42

		42		3730		1.38				42.4		3580		1.39				43.2		4030		1.42				43.1		3810		1.42				43.3		3850		1.43				43.4		4580		1.43				42.5		3720		1.4				43.1		4920		1.42

		42.1		3740		1.39				42.4		3590		1.4				43.2		4030		1.43				43.2		3810		1.42				43.4		3860		1.43				43.5		4590		1.44				42.6		3720		1.41				43.2		4930		1.43

		42.2		3740		1.39				42.5		3590		1.4				43.3		4040		1.43				43.3		3820		1.43				43.4		3860		1.43				43.5		4600		1.44				42.6		3730		1.41				43.2		4940		1.43

		42.2		3750		1.39				42.5		3600		1.4				43.3		4040		1.43				43.3		3820		1.43				43.5		3860		1.43				43.6		4600		1.44				42.7		3730		1.41				43.3		4950		1.43

		42.3		3750		1.39				42.6		3600		1.4				43.4		4040		1.43				43.4		3820		1.43				43.6		3870		1.44				43.7		4610		1.44				42.7		3740		1.41				43.4		4950		1.43

		42.4		3760		1.39				42.7		3610		1.4				43.5		4050		1.43				43.4		3830		1.43				43.6		3870		1.44				43.7		4620		1.44				42.9		3750		1.42				43.5		4970		1.44

		42.4		3760		1.4				42.7		3610		1.41				43.5		4050		1.44				43.5		3830		1.43				43.7		3880		1.44				43.8		4620		1.45				42.9		3750		1.42				43.5		4970		1.44

		42.5		3770		1.4				42.8		3610		1.41				43.6		4060		1.44				43.6		3840		1.44				43.8		3880		1.44				43.9		4630		1.45				43		3760		1.42				43.6		4980		1.44

		42.6		3770		1.4				42.8		3620		1.41				43.7		4060		1.44				43.6		3840		1.44				43.9		3890		1.44				43.9		4640		1.45				43.1		3760		1.42				43.7		4990		1.44

		42.6		3770		1.4				43		3630		1.42				43.8		4070		1.44				43.7		3850		1.44				43.9		3890		1.45				44		4640		1.45				43.2		3770		1.42				43.7		4990		1.45

		42.7		3780		1.41				43		3630		1.42				43.8		4070		1.45				43.8		3850		1.44				44		3900		1.45				44.1		4650		1.45				43.2		3770		1.43				43.8		5000		1.45

		42.8		3790		1.41				43.1		3640		1.42				43.9		4080		1.45				43.8		3850		1.44				44		3900		1.45				44.1		4660		1.46				43.2		3780		1.43				43.8		5010		1.45

		42.9		3790		1.41				43.2		3640		1.42				44		4080		1.45				43.9		3860		1.45				44.1		3910		1.45				44.2		4660		1.46				43.3		3780		1.43				43.9		5010		1.45

		43		3800		1.41				43.2		3640		1.42				44		4090		1.45				43.9		3860		1.45				44.2		3910		1.46				44.3		4670		1.46				43.4		3790		1.43				44		5030		1.46

		43		3800		1.41				43.3		3650		1.43				44.1		4090		1.45				44		3870		1.45				44.3		3920		1.46				44.4		4680		1.47				43.5		3790		1.44				44.1		5030		1.46

		43.1		3800		1.42				43.3		3650		1.43				44.1		4100		1.46				44.1		3870		1.45				44.4		3920		1.46				44.4		4690		1.47				43.5		3800		1.44				44.2		5040		1.46

		43.1		3810		1.42				43.4		3660		1.43				44.2		4100		1.46				44.2		3880		1.46				44.4		3930		1.46				44.5		4690		1.47				43.6		3800		1.44				44.2		5050		1.46

		43.2		3810		1.42				43.5		3660		1.43				44.3		4110		1.46				44.2		3880		1.46				44.5		3930		1.47				44.6		4700		1.47				43.7		3810		1.44				44.3		5060		1.46

		43.3		3820		1.43				43.6		3670		1.44				44.4		4110		1.46				44.3		3890		1.46				44.5		3940		1.47				44.6		4710		1.47				43.7		3810		1.44				44.3		5060		1.47

		43.4		3830		1.43				43.6		3670		1.44				44.5		4120		1.47				44.4		3890		1.46				44.6		3940		1.47				44.7		4710		1.48				43.8		3820		1.45				44.4		5070		1.47

		43.4		3830		1.43				43.7		3680		1.44				44.5		4120		1.47				44.4		3890		1.46				44.7		3940		1.47				44.8		4720		1.48				43.8		3820		1.45				44.5		5080		1.47

		43.5		3830		1.43				43.8		3680		1.44				44.6		4130		1.47				44.5		3900		1.47				44.7		3950		1.47				44.9		4730		1.48				43.9		3830		1.45				44.6		5090		1.47

		43.6		3840		1.43				43.8		3690		1.44				44.7		4130		1.47				44.6		3900		1.47				44.9		3960		1.48				44.9		4730		1.48				44		3830		1.45				44.7		5100		1.48

		43.6		3840		1.44				43.9		3690		1.45				44.7		4140		1.47				44.6		3910		1.47				44.9		3960		1.48				45		4740		1.49				44.1		3840		1.46				44.7		5110		1.48

		43.7		3850		1.44				43.9		3690		1.45				44.7		4140		1.48				44.7		3910		1.48				45		3960		1.48				45		4750		1.49				44.1		3840		1.46				44.8		5110		1.48

		43.7		3850		1.44				44		3700		1.45				44.8		4150		1.48				44.8		3920		1.48				45		3970		1.48				45.1		4750		1.49				44.2		3850		1.46				44.9		5120		1.48

		43.8		3860		1.44				44.1		3700		1.45				45		4150		1.48				44.9		3920		1.48				45.1		3970		1.49				45.2		4760		1.49				44.2		3850		1.46				44.9		5130		1.48

		44		3860		1.45				44.2		3710		1.46				45		4160		1.49				44.9		3930		1.48				45.2		3980		1.49				45.2		4770		1.49				44.3		3860		1.46				45		5130		1.49

		44		3870		1.45				44.2		3710		1.46				45.1		4160		1.49				45		3930		1.48				45.2		3980		1.49				45.3		4770		1.5				44.4		3860		1.47				45		5140		1.49

		44.1		3870		1.45				44.3		3720		1.46				45.1		4170		1.49				45.1		3930		1.49				45.3		3990		1.49				45.4		4780		1.5				44.4		3870		1.47				45.2		5160		1.49

		44.1		3880		1.45				44.4		3720		1.46				45.2		4170		1.49				45.1		3940		1.49				45.4		3990		1.5				45.5		4790		1.5				44.5		3870		1.47				45.2		5160		1.5

		44.2		3880		1.45				44.4		3720		1.46				45.3		4180		1.49				45.2		3940		1.49				45.4		4000		1.5				45.5		4800		1.5				44.6		3880		1.47				45.3		5170		1.5

		44.3		3890		1.46				44.5		3730		1.47				45.3		4180		1.5				45.3		3950		1.49				45.5		4000		1.5				45.6		4800		1.51				44.7		3890		1.48				45.3		5180		1.5

		44.3		3890		1.46				44.5		3730		1.47				45.4		4190		1.5				45.3		3950		1.49				45.6		4010		1.5				45.7		4810		1.51				44.8		3890		1.48				45.4		5180		1.5

		44.4		3900		1.46				44.6		3740		1.47				45.5		4190		1.5				45.4		3950		1.5				45.6		4010		1.51				45.7		4810		1.51				44.8		3900		1.48				45.5		5190		1.5

		44.5		3900		1.46				44.7		3740		1.47				45.6		4200		1.5				45.4		3960		1.5				45.7		4020		1.51				45.8		4820		1.51				44.9		3900		1.48				45.6		5200		1.51

		44.6		3910		1.47				44.8		3750		1.48				45.6		4200		1.51				45.5		3960		1.5				45.8		4020		1.51				45.9		4830		1.51				44.9		3910		1.48				45.6		5200		1.51

		44.6		3910		1.47				44.9		3750		1.48				45.7		4210		1.51				45.6		3970		1.5				45.9		4020		1.51				46		4840		1.52				45		3910		1.49				45.7		5210		1.51

		44.7		3920		1.47				44.9		3760		1.48				45.7		4210		1.51				45.6		3970		1.5				46		4030		1.52				46.1		4850		1.52				45.1		3920		1.49				45.7		5220		1.51

		44.8		3920		1.47				44.9		3760		1.48				45.8		4210		1.51				45.7		3970		1.51				46		4040		1.52				46.1		4850		1.52				45.1		3920		1.49				45.8		5220		1.51

		44.8		3930		1.48				45		3760		1.48				45.9		4220		1.51				45.7		3980		1.51				46.1		4040		1.52				46.2		4860		1.53				45.2		3930		1.49				45.8		5230		1.52

		44.9		3930		1.48				45.1		3770		1.49				45.9		4220		1.52				45.8		3980		1.51				46.2		4050		1.52				46.2		4860		1.53				45.3		3930		1.5				45.9		5240		1.52

		45		3930		1.48				45.2		3770		1.49				46		4230		1.52				45.9		3990		1.51				46.2		4050		1.52				46.3		4870		1.53				45.3		3940		1.5				46		5250		1.52

		45		3940		1.48				45.3		3780		1.49				46.1		4240		1.52				46		4000		1.52				46.3		4050		1.53				46.4		4880		1.53				45.4		3940		1.5				46		5250		1.52

		45.1		3950		1.49				45.4		3780		1.49				46.2		4240		1.52				46.1		4000		1.52				46.4		4060		1.53				46.4		4880		1.53				45.5		3950		1.5				46.1		5260		1.52

		45.2		3950		1.49				45.4		3790		1.5				46.2		4250		1.53				46.1		4000		1.52				46.4		4060		1.53				46.6		4900		1.54				45.5		3950		1.5				46.2		5270		1.53

		45.3		3960		1.49				45.5		3790		1.5				46.3		4250		1.53				46.2		4010		1.52				46.5		4070		1.53				46.6		4900		1.54				45.6		3960		1.51				46.2		5270		1.53

		45.3		3960		1.49				45.5		3800		1.5				46.3		4250		1.53				46.3		4010		1.53				46.6		4070		1.54				46.7		4910		1.54				45.7		3960		1.51				46.3		5290		1.53

		45.4		3960		1.49				45.6		3800		1.5				46.4		4260		1.53				46.3		4020		1.53				46.6		4080		1.54				46.7		4910		1.54				45.7		3970		1.51				46.4		5290		1.53

		45.4		3970		1.5				45.7		3810		1.5				46.5		4260		1.53				46.4		4020		1.53				46.7		4080		1.54				46.8		4920		1.55				45.8		3970		1.51				46.5		5300		1.54

		45.5		3970		1.5				45.7		3810		1.51				46.6		4270		1.54				46.5		4020		1.53				46.8		4090		1.54				46.9		4930		1.55				45.8		3970		1.51				46.5		5310		1.54

		45.6		3980		1.5				45.8		3810		1.51				46.7		4280		1.54				46.5		4030		1.53				46.8		4090		1.54				46.9		4930		1.55				45.9		3980		1.52				46.6		5320		1.54

		45.6		3980		1.5				45.9		3820		1.51				46.7		4280		1.54				46.6		4030		1.54				46.9		4090		1.55				47		4940		1.55				46		3980		1.52				46.7		5320		1.54

		45.7		3990		1.51				45.9		3820		1.51				46.8		4290		1.54				46.7		4040		1.54				46.9		4100		1.55				47.1		4950		1.56				46.1		3990		1.52				46.7		5330		1.55

		45.8		3990		1.51				46		3830		1.52				46.9		4290		1.55				46.7		4040		1.54				47		4100		1.55				47.2		4960		1.56				46.1		3990		1.52				46.8		5340		1.55

		45.9		4000		1.51				46.1		3830		1.52				46.9		4300		1.55				46.8		4050		1.54				47.1		4110		1.55				47.3		4960		1.56				46.2		4000		1.52				46.9		5350		1.55

		45.9		4000		1.51				46.1		3840		1.52				47		4300		1.55				46.8		4050		1.54				47.2		4120		1.56				47.3		4970		1.56				46.2		4000		1.53				47		5360		1.55

		46		4010		1.51				46.2		3840		1.52				47		4300		1.55				46.9		4050		1.55				47.3		4120		1.56				47.4		4980		1.57				46.3		4010		1.53				47		5360		1.56

		46		4010		1.52				46.2		3850		1.52				47.1		4310		1.56				47		4060		1.55				47.3		4120		1.56				47.4		4980		1.57				46.4		4020		1.53				47.1		5370		1.56

		46.1		4020		1.52				46.3		3850		1.53				47.2		4320		1.56				47.1		4060		1.55				47.3		4130		1.56				47.5		4990		1.57				46.5		4020		1.53				47.2		5380		1.56

		46.2		4020		1.52				46.4		3850		1.53				47.3		4320		1.56				47.1		4070		1.55				47.4		4130		1.56				47.6		5000		1.57				46.5		4020		1.54				47.2		5390		1.56

		46.3		4030		1.52				46.5		3860		1.53				47.3		4330		1.56				47.2		4070		1.56				47.5		4140		1.57				47.7		5010		1.58				46.6		4030		1.54				47.3		5390		1.56

		46.3		4030		1.53				46.5		3870		1.53				47.4		4330		1.57				47.2		4070		1.56				47.6		4140		1.57				47.8		5010		1.58				46.6		4030		1.54				47.4		5400		1.57

		46.4		4040		1.53				46.6		3870		1.54				47.5		4330		1.57				47.3		4080		1.56				47.7		4150		1.57				47.8		5020		1.58				46.7		4040		1.54				47.4		5410		1.57

		46.5		4040		1.53				46.7		3870		1.54				47.6		4340		1.57				47.4		4080		1.56				47.7		4150		1.58				47.9		5030		1.58				46.7		4040		1.54				47.5		5420		1.57

		46.5		4050		1.53				46.7		3880		1.54				47.6		4340		1.57				47.4		4090		1.56				47.8		4160		1.58				47.9		5030		1.58				46.8		4050		1.55				47.6		5420		1.57

		46.6		4050		1.53				46.8		3880		1.54				47.6		4350		1.57				47.5		4090		1.57				47.9		4160		1.58				48		5040		1.59				46.9		4060		1.55				47.6		5430		1.58

		46.6		4060		1.54				46.9		3890		1.55				47.7		4350		1.58				47.6		4100		1.57				47.9		4170		1.58				48.1		5040		1.59				47		4060		1.55				47.7		5440		1.58

		46.7		4060		1.54				46.9		3890		1.55				47.8		4360		1.58				47.6		4100		1.57				48		4170		1.58				48.2		5060		1.59				47		4070		1.55				47.8		5450		1.58

		46.8		4070		1.54				47		3900		1.55				47.9		4360		1.58				47.7		4100		1.57				48		4170		1.59				48.3		5060		1.59				47.1		4070		1.56				47.8		5450		1.58

		46.9		4070		1.54				47.1		3900		1.55				47.9		4370		1.58				47.7		4110		1.58				48.1		4180		1.59				48.3		5070		1.6				47.1		4080		1.56				47.9		5460		1.58

		46.9		4080		1.55				47.1		3910		1.55				48		4370		1.59				47.8		4110		1.58				48.3		4190		1.59				48.4		5070		1.6				47.2		4080		1.56				47.9		5470		1.59

		47		4080		1.55				47.2		3910		1.56				48.1		4380		1.59				47.9		4120		1.58				48.3		4190		1.59				48.4		5080		1.6				47.3		4090		1.56				48		5480		1.59

		47.1		4080		1.55				47.3		3910		1.56				48.1		4380		1.59				47.9		4120		1.58				48.4		4200		1.6				48.5		5090		1.6				47.3		4090		1.56				48.1		5480		1.59

		47.1		4090		1.55				47.3		3920		1.56				48.2		4390		1.59				48		4120		1.58				48.4		4200		1.6				48.6		5090		1.61				47.4		4090		1.57				48.2		5490		1.59

		47.2		4090		1.55				47.4		3920		1.56				48.2		4390		1.59				48.1		4130		1.59				48.5		4200		1.6				48.7		5110		1.61				47.6		4100		1.57				48.2		5500		1.59

		47.2		4100		1.56				47.5		3930		1.56				48.3		4400		1.6				48.1		4140		1.59				48.6		4210		1.6				48.8		5110		1.61				47.6		4110		1.57				48.3		5500		1.6

		47.3		4100		1.56				47.5		3930		1.57				48.4		4400		1.6				48.2		4140		1.59				48.6		4210		1.6				48.8		5120		1.61				47.6		4110		1.57				48.4		5510		1.6

		47.4		4110		1.56				47.6		3940		1.57				48.5		4410		1.6				48.3		4140		1.59				48.7		4220		1.61				48.9		5130		1.62				47.7		4120		1.58				48.4		5520		1.6

		47.5		4110		1.56				47.7		3940		1.57				48.5		4410		1.6				48.3		4150		1.59				48.8		4230		1.61				48.9		5130		1.62				47.8		4120		1.58				48.5		5530		1.6

		47.5		4110		1.56				47.7		3950		1.57				48.6		4420		1.6				48.4		4150		1.6				48.8		4230		1.61				49		5140		1.62				47.8		4130		1.58				48.6		5530		1.61

		47.5		4120		1.57				47.8		3950		1.58				48.6		4420		1.61				48.5		4160		1.6				48.9		4230		1.61				49.1		5150		1.62				47.9		4130		1.58				48.6		5550		1.61

		47.6		4120		1.57				47.8		3950		1.58				48.7		4420		1.61				48.5		4160		1.6				49		4240		1.62				49.1		5150		1.62				47.9		4140		1.58				48.7		5550		1.61

		47.7		4130		1.57				47.9		3960		1.58				48.8		4430		1.61				48.6		4160		1.6				49.1		4240		1.62				49.3		5160		1.63				48		4140		1.59				48.8		5560		1.61

		47.7		4130		1.57				48		3960		1.58				48.8		4430		1.61				48.7		4170		1.61				49.1		4250		1.62				49.3		5170		1.63				48.1		4150		1.59				48.8		5570		1.62

		47.8		4130		1.57				48		3970		1.58				48.9		4440		1.62				48.8		4170		1.61				49.2		4250		1.62				49.4		5180		1.63				48.1		4150		1.59				48.9		5580		1.62

		47.9		4140		1.58				48.2		3970		1.59				49.1		4450		1.62				48.8		4180		1.61				49.3		4260		1.62				49.4		5180		1.63				48.2		4150		1.59				49		5580		1.62

		47.9		4140		1.58				48.2		3980		1.59				49.1		4450		1.62				48.9		4180		1.61				49.4		4260		1.63				49.5		5190		1.64				48.2		4160		1.59				49		5590		1.62

		48		4150		1.58				48.3		3980		1.59				49.1		4460		1.62				49		4190		1.61				49.4		4270		1.63				49.6		5200		1.64				48.3		4160		1.6				49.1		5600		1.62

		48		4150		1.58				48.3		3980		1.59				49.2		4460		1.63				49		4190		1.62				49.5		4270		1.63				49.6		5200		1.64				48.4		4170		1.6				49.2		5610		1.63

		48.1		4160		1.59				48.4		3990		1.6				49.3		4470		1.63				49		4200		1.62				49.6		4280		1.64				49.7		5210		1.64				48.4		4170		1.6				49.2		5620		1.63

		48.2		4160		1.59				48.4		3990		1.6				49.3		4470		1.63				49.1		4200		1.62				49.6		4280		1.64				49.8		5220		1.65				48.5		4180		1.6				49.3		5620		1.63

		48.2		4160		1.59				48.5		4000		1.6				49.4		4470		1.63				49.2		4200		1.62				49.7		4290		1.64				49.9		5230		1.65				48.5		4180		1.6				49.4		5630		1.63

		48.3		4170		1.59				48.6		4000		1.6				49.5		4480		1.63				49.3		4210		1.63				49.7		4290		1.64				50		5230		1.65				48.7		4190		1.61				49.4		5640		1.64

		48.4		4170		1.59				48.7		4010		1.61				49.5		4480		1.64				49.4		4210		1.63				49.8		4290		1.64				50		5240		1.65				48.7		4200		1.61				49.5		5640		1.64

		48.5		4180		1.6				48.7		4010		1.61				49.6		4490		1.64				49.4		4220		1.63				49.9		4300		1.65				50.1		5250		1.66				48.8		4200		1.61				49.6		5650		1.64

		48.5		4190		1.6				48.8		4010		1.61				49.7		4500		1.64				49.5		4220		1.63				50		4310		1.65				50.2		5250		1.66				48.9		4210		1.62				49.6		5660		1.64

		48.6		4190		1.6				48.8		4020		1.61				49.8		4500		1.64				49.5		4230		1.63				50.1		4310		1.65				50.2		5260		1.66				48.9		4210		1.62				49.7		5660		1.64

		48.7		4190		1.6				48.9		4020		1.61				49.8		4510		1.65				49.6		4230		1.64				50.1		4320		1.65				50.3		5270		1.66				49		4220		1.62				49.8		5680		1.65

		48.8		4200		1.61				49		4030		1.61				49.9		4510		1.65				49.6		4230		1.64				50.2		4320		1.66				50.4		5280		1.67				49		4220		1.62				49.9		5680		1.65

		48.8		4200		1.61				49		4030		1.62				50		4520		1.65				49.7		4240		1.64				50.2		4320		1.66				50.4		5280		1.67				49.1		4230		1.62				49.9		5690		1.65

		48.9		4210		1.61				49.1		4040		1.62				50		4520		1.65				49.8		4240		1.64				50.3		4330		1.66				50.5		5290		1.67				49.2		4240		1.63				50		5700		1.65

		48.9		4210		1.61				49.2		4040		1.62				50.1		4530		1.65				49.9		4250		1.65				50.3		4330		1.66				50.6		5300		1.67				49.3		4240		1.63				50		5700		1.66

		49		4210		1.61				49.3		4050		1.62				50.2		4530		1.66				50		4250		1.65				50.5		4340		1.67				50.7		5300		1.67				49.4		4250		1.63				50.1		5710		1.66

		49		4220		1.62				49.3		4050		1.63				50.3		4540		1.66				50		4260		1.65				50.6		4350		1.67				50.7		5310		1.68				49.5		4250		1.63				50.1		5720		1.66

		49.2		4230		1.62				49.3		4050		1.63				50.3		4540		1.66				50		4260		1.65				50.6		4350		1.67				50.8		5310		1.68				49.5		4260		1.64				50.2		5720		1.66

		49.2		4230		1.62				49.4		4060		1.63				50.4		4550		1.66				50.1		4270		1.65				50.7		4350		1.67				50.9		5320		1.68				49.5		4260		1.64				50.3		5730		1.66

		49.3		4240		1.62				49.5		4060		1.63				50.4		4550		1.67				50.2		4270		1.66				50.7		4360		1.67				51		5330		1.69				49.6		4270		1.64				50.4		5750		1.67

		49.4		4240		1.63				49.6		4070		1.63				50.5		4550		1.67				50.3		4270		1.66				50.8		4360		1.68				51		5340		1.69				49.7		4270		1.64				50.5		5750		1.67

		49.4		4240		1.63				49.6		4070		1.64				50.5		4560		1.67				50.3		4280		1.66				50.9		4370		1.68				51.1		5350		1.69				49.8		4280		1.65				50.5		5760		1.67

		49.5		4250		1.63				49.7		4080		1.64				50.6		4560		1.67				50.4		4290		1.66				50.9		4370		1.68				51.2		5350		1.69				49.9		4290		1.65				50.6		5770		1.67

		49.5		4250		1.63				49.8		4080		1.64				50.7		4570		1.67				50.5		4290		1.67				51.1		4380		1.69				51.2		5360		1.69				49.9		4290		1.65				50.7		5770		1.68

		49.6		4260		1.64				49.9		4090		1.64				50.8		4570		1.68				50.5		4290		1.67				51.1		4380		1.69				51.3		5370		1.7				50		4290		1.65				50.7		5780		1.68

		49.7		4260		1.64				49.9		4090		1.65				50.8		4580		1.68				50.6		4300		1.67				51.2		4390		1.69				51.3		5370		1.7				50		4300		1.65				50.8		5790		1.68

		49.8		4270		1.64				50		4100		1.65				50.9		4580		1.68				50.7		4300		1.67				51.3		4390		1.69				51.4		5380		1.7				50.1		4300		1.66				50.9		5800		1.68

		49.9		4270		1.64				50		4100		1.65				51		4590		1.68				50.7		4310		1.67				51.3		4400		1.69				51.5		5390		1.7				50.2		4310		1.66				51		5810		1.69

		49.9		4280		1.65				50.1		4110		1.65				51		4590		1.69				50.8		4310		1.68				51.4		4400		1.7				51.5		5390		1.71				50.3		4310		1.66				51		5820		1.69

		50		4280		1.65				50.2		4110		1.66				51.1		4600		1.69				50.9		4310		1.68				51.4		4410		1.7				51.6		5400		1.71				50.4		4320		1.67				51.1		5820		1.69

		50		4290		1.65				50.3		4110		1.66				51.1		4600		1.69				50.9		4320		1.68				51.5		4410		1.7				51.7		5410		1.71				50.5		4330		1.67				51.1		5830		1.69

		50.1		4290		1.65				50.4		4120		1.66				51.2		4600		1.69				51		4330		1.69				51.6		4420		1.7				51.8		5410		1.71				50.5		4330		1.67				51.2		5840		1.69

		50.2		4290		1.65				50.4		4130		1.66				51.3		4610		1.7				51.1		4330		1.69				51.7		4420		1.71				51.8		5420		1.71				50.5		4340		1.67				51.3		5840		1.7

		50.2		4300		1.66				50.5		4130		1.67				51.4		4620		1.7				51.2		4330		1.69				51.7		4430		1.71				51.9		5430		1.72				50.6		4340		1.67				51.3		5850		1.7

		50.4		4310		1.66				50.5		4130		1.67				51.5		4620		1.7				51.2		4340		1.69				51.8		4430		1.71				51.9		5430		1.72				50.7		4350		1.68				51.4		5860		1.7

		50.4		4310		1.66				50.6		4140		1.67				51.5		4630		1.7				51.3		4340		1.69				51.8		4440		1.71				52.1		5440		1.72				50.7		4350		1.68				51.5		5860		1.7

		50.5		4320		1.66				50.7		4140		1.67				51.6		4630		1.7				51.4		4340		1.7				51.9		4440		1.71				52.1		5450		1.72				50.8		4360		1.68				51.6		5880		1.71

		50.6		4320		1.67				50.8		4150		1.67				51.7		4640		1.71				51.5		4350		1.7				52		4450		1.72				52.2		5460		1.73				50.9		4360		1.68				51.6		5880		1.71

		50.6		4330		1.67				50.8		4150		1.68				51.7		4640		1.71				51.5		4350		1.7				52.1		4450		1.72				52.3		5460		1.73				51		4370		1.69				51.7		5890		1.71

		50.7		4330		1.67				50.9		4160		1.68				51.8		4640		1.71				51.6		4360		1.7				52.2		4460		1.72				52.3		5470		1.73				51.1		4380		1.69				51.7		5900		1.71

		50.7		4330		1.67				50.9		4160		1.68				51.9		4650		1.71				51.6		4360		1.7				52.3		4460		1.72				52.4		5480		1.73				51.1		4380		1.69				51.8		5900		1.71

		50.8		4340		1.67				51		4170		1.68				52		4660		1.72				51.7		4370		1.71				52.3		4470		1.73				52.4		5480		1.74				51.2		4390		1.69				51.9		5910		1.72

		50.9		4350		1.68				51.1		4170		1.69				52		4660		1.72				51.8		4370		1.71				52.4		4470		1.73				52.5		5490		1.74				51.3		4390		1.69				51.9		5920		1.72

		51		4350		1.68				51.2		4170		1.69				52		4660		1.72				51.9		4380		1.71				52.4		4480		1.73				52.6		5490		1.74				51.3		4400		1.7				52		5930		1.72

		51		4350		1.68				51.2		4180		1.69				52.1		4670		1.72				51.9		4380		1.71				52.5		4480		1.73				52.7		5500		1.74				51.4		4400		1.7				52.1		5930		1.72

		51.1		4360		1.69				51.2		4180		1.69				52.2		4670		1.72				51.9		4380		1.72				52.5		4480		1.74				52.7		5510		1.74				51.4		4410		1.7				52.1		5940		1.73

		51.2		4360		1.69				51.3		4190		1.69				52.3		4680		1.73				52		4390		1.72				52.6		4490		1.74				52.8		5520		1.75				51.5		4410		1.7				52.2		5950		1.73

		51.2		4370		1.69				51.4		4190		1.7				52.3		4680		1.73				52.1		4390		1.72				52.7		4500		1.74				52.9		5520		1.75				51.6		4420		1.71				52.3		5960		1.73

		51.3		4370		1.69				51.5		4200		1.7				52.4		4690		1.73				52.2		4400		1.72				52.8		4500		1.74				52.9		5530		1.75				51.7		4420		1.71				52.3		5970		1.73

		51.4		4370		1.69				51.6		4200		1.7				52.5		4690		1.73				52.3		4400		1.72				52.8		4500		1.74				53		5530		1.75				51.7		4430		1.71				52.4		5970		1.73

		51.4		4380		1.7				51.7		4210		1.7				52.5		4700		1.74				52.3		4410		1.73				52.9		4510		1.75				53		5540		1.75				51.8		4430		1.71				52.5		5980		1.74

		51.5		4380		1.7				51.7		4210		1.71				52.6		4700		1.74				52.4		4410		1.73				53		4510		1.75				53.1		5550		1.76				51.9		4440		1.72				52.5		5990		1.74

		51.6		4390		1.7				51.8		4220		1.71				52.6		4710		1.74				52.4		4410		1.73				53		4520		1.75				53.2		5550		1.76				51.9		4440		1.72				52.6		5990		1.74

		51.7		4390		1.7				51.8		4220		1.71				52.7		4710		1.74				52.5		4420		1.73				53.1		4520		1.75				53.3		5570		1.76				52		4450		1.72				52.6		6000		1.74

		51.7		4400		1.7				51.9		4230		1.71				52.8		4720		1.74				52.5		4420		1.74				53.1		4530		1.76				53.3		5570		1.77				52.1		4460		1.72				52.8		6010		1.75

		51.8		4400		1.71				51.9		4230		1.71				52.9		4720		1.75				52.6		4430		1.74				53.3		4530		1.76				53.4		5580		1.77				52.2		4460		1.73				52.8		6020		1.75

		51.9		4410		1.71				52.1		4240		1.72				52.9		4730		1.75				52.7		4430		1.74				53.3		4540		1.76				53.5		5590		1.77				52.2		4470		1.73				52.9		6030		1.75

		51.9		4410		1.71				52.1		4240		1.72				53		4730		1.75				52.7		4440		1.74				53.4		4540		1.76				53.5		5590		1.77				52.3		4470		1.73				53		6040		1.75

		52		4420		1.71				52.2		4250		1.72				53.1		4740		1.75				52.8		4440		1.74				53.5		4550		1.77				53.6		5600		1.77				52.4		4470		1.73				53		6040		1.76

		52		4420		1.72				52.2		4250		1.72				53.1		4740		1.76				52.9		4440		1.75				53.5		4550		1.77				53.7		5600		1.78				52.4		4480		1.73				53.1		6050		1.76

		52.1		4430		1.72				52.3		4260		1.73				53.2		4750		1.76				52.9		4450		1.75				53.6		4560		1.77				53.7		5610		1.78				52.5		4480		1.74				53.1		6060		1.76

		52.2		4430		1.72				52.4		4260		1.73				53.3		4750		1.76				53		4450		1.75				53.6		4560		1.77				53.8		5620		1.78				52.6		4490		1.74				53.2		6060		1.76

		52.3		4430		1.72				52.5		4260		1.73				53.3		4750		1.76				53		4460		1.75				53.7		4560		1.77				53.9		5630		1.78				52.6		4490		1.74				53.3		6080		1.76

		52.3		4440		1.72				52.5		4270		1.73				53.4		4760		1.76				53.1		4460		1.75				53.8		4570		1.78				54		5640		1.79				52.7		4500		1.74				53.4		6080		1.77

		52.4		4440		1.73				52.6		4280		1.74				53.4		4760		1.77				53.2		4460		1.76				53.9		4570		1.78				54		5640		1.79				52.7		4500		1.74				53.4		6090		1.77

		52.4		4450		1.73				52.7		4280		1.74				53.6		4770		1.77				53.2		4470		1.76				54		4580		1.78				54.1		5650		1.79				52.8		4510		1.75				53.5		6100		1.77

		52.5		4450		1.73				52.8		4290		1.74				53.6		4780		1.77				53.4		4480		1.76				54		4580		1.78				54.2		5650		1.79				52.9		4510		1.75				53.6		6100		1.77

		52.6		4460		1.74				52.8		4290		1.74				53.7		4780		1.77				53.4		4480		1.76				54		4590		1.79				54.2		5660		1.79				52.9		4520		1.75				53.6		6110		1.77

		52.7		4460		1.74				52.9		4290		1.75				53.8		4790		1.78				53.5		4480		1.77				54.1		4590		1.79				54.3		5670		1.8				53		4520		1.75				53.7		6120		1.78

		52.7		4470		1.74				52.9		4300		1.75				53.8		4790		1.78				53.6		4490		1.77				54.2		4600		1.79				54.3		5670		1.8				53		4530		1.75				53.7		6130		1.78

		52.8		4470		1.74				53		4300		1.75				53.9		4790		1.78				53.6		4490		1.77				54.2		4600		1.79				54.5		5680		1.8				53.1		4530		1.76				53.8		6130		1.78

		52.9		4480		1.74				53.1		4310		1.75				53.9		4800		1.78				53.7		4500		1.77				54.3		4600		1.79				54.5		5690		1.8				53.2		4540		1.76				53.9		6140		1.78

		52.9		4480		1.75				53.2		4310		1.76				54		4800		1.78				53.8		4500		1.77				54.4		4610		1.8				54.6		5700		1.81				53.3		4550		1.76				54		6150		1.79

		53		4480		1.75				53.2		4320		1.76				54		4810		1.79				53.8		4510		1.78				54.5		4620		1.8				54.7		5700		1.81				53.4		4550		1.77				54		6160		1.79

		53		4490		1.75				53.3		4320		1.76				54.1		4820		1.79				53.9		4510		1.78				54.5		4620		1.8				54.7		5710		1.81				53.4		4560		1.77				54.1		6170		1.79

		53.2		4500		1.75				53.4		4330		1.76				54.2		4820		1.79				53.9		4520		1.78				54.6		4620		1.8				54.8		5710		1.81				53.5		4560		1.77				54.2		6170		1.79

		53.2		4500		1.76				53.5		4330		1.76				54.3		4820		1.79				54		4520		1.78				54.7		4630		1.81				54.9		5720		1.82				53.5		4560		1.77				54.2		6180		1.79

		53.3		4510		1.76				53.5		4340		1.77				54.4		4830		1.8				54		4520		1.79				54.8		4630		1.81				54.9		5730		1.82				53.6		4570		1.77				54.3		6190		1.8

		53.4		4510		1.76				53.6		4340		1.77				54.4		4830		1.8				54.1		4530		1.79				54.8		4640		1.81				55		5740		1.82				53.7		4570		1.78				54.4		6190		1.8

		53.4		4510		1.76				53.7		4340		1.77				54.5		4840		1.8				54.2		4530		1.79				54.9		4640		1.81				55.1		5750		1.82				53.8		4580		1.78				54.5		6210		1.8

		53.5		4520		1.76				53.7		4350		1.77				54.5		4840		1.8				54.2		4530		1.79				54.9		4640		1.81				55.2		5750		1.83				53.9		4590		1.78				54.5		6220		1.81

		53.5		4520		1.77				53.8		4360		1.78				54.6		4850		1.8				54.3		4540		1.79				55		4650		1.82				55.2		5760		1.83				53.9		4590		1.78				54.6		6220		1.81

		53.6		4530		1.77				53.9		4360		1.78				54.6		4850		1.81				54.4		4540		1.8				55.1		4660		1.82				55.3		5760		1.83				54		4600		1.79				54.6		6230		1.81

		53.7		4530		1.77				53.9		4360		1.78				54.7		4860		1.81				54.5		4550		1.8				55.1		4660		1.82				55.3		5770		1.83				54		4600		1.79				54.7		6240		1.81

		53.8		4540		1.77				54		4370		1.78				54.8		4860		1.81				54.5		4550		1.8				55.2		4660		1.82				55.4		5780		1.83				54.1		4610		1.79				54.8		6250		1.81

		53.9		4540		1.78				54		4370		1.78				54.9		4870		1.81				54.6		4560		1.8				55.3		4670		1.83				55.5		5780		1.84				54.2		4610		1.79				54.8		6250		1.82

		53.9		4550		1.78				54.1		4380		1.79				54.9		4870		1.82				54.7		4560		1.81				55.4		4670		1.83				55.6		5790		1.84				54.2		4610		1.79				54.9		6260		1.82

		54		4550		1.78				54.2		4380		1.79				55		4880		1.82				54.8		4570		1.81				55.4		4680		1.83				55.6		5800		1.84				54.3		4620		1.8				55		6270		1.82

		54		4560		1.78				54.2		4390		1.79				55.1		4880		1.82				54.8		4570		1.81				55.5		4680		1.83				55.7		5800		1.84				54.4		4630		1.8				55		6280		1.82

		54.1		4560		1.78				54.3		4390		1.79				55.1		4880		1.82				54.9		4570		1.81				55.6		4690		1.84				55.7		5810		1.85				54.5		4630		1.8				55.1		6290		1.82

		54.2		4560		1.79				54.4		4400		1.8				55.2		4890		1.82				54.9		4580		1.81				55.6		4690		1.84				55.8		5820		1.85				54.5		4640		1.8				55.2		6290		1.83

		54.3		4570		1.79				54.5		4400		1.8				55.3		4890		1.83				55		4580		1.82				55.7		4700		1.84				55.9		5820		1.85				54.6		4640		1.81				55.2		6300		1.83

		54.3		4580		1.79				54.5		4410		1.8				55.3		4900		1.83				55.1		4590		1.82				55.8		4700		1.84				56		5830		1.85				54.7		4650		1.81				55.3		6310		1.83

		54.4		4580		1.8				54.6		4410		1.8				55.4		4900		1.83				55.2		4590		1.82				55.8		4710		1.85				56		5830		1.85				54.7		4650		1.81				55.4		6320		1.83

		54.5		4590		1.8				54.7		4420		1.8				55.4		4910		1.83				55.2		4600		1.82				55.9		4710		1.85				56.1		5840		1.85				54.8		4650		1.81				55.4		6320		1.84

		54.5		4590		1.8				54.7		4420		1.81				55.5		4910		1.84				55.3		4600		1.83				56		4710		1.85				56.1		5850		1.86				54.9		4640		1.82				55.5		6330		1.84

		54.6		4590		1.8				54.8		4420		1.81				55.6		4920		1.84				55.4		4600		1.83				56		4720		1.85				56.2		5850		1.86				55		4650		1.82				55.5		6340		1.84

		54.7		4600		1.8				54.9		4430		1.81				55.7		4920		1.84				55.4		4610		1.83				56.1		4730		1.86				56.2		5860		1.86				55.1		4660		1.82				55.6		6350		1.84

		54.7		4600		1.81				55		4440		1.82				55.7		4930		1.84				55.4		4610		1.83				56.2		4730		1.86				56.3		5870		1.86				55.1		4660		1.82				55.7		6350		1.84

		54.8		4610		1.81				55		4440		1.82				55.8		4930		1.84				55.5		4620		1.83				56.3		4740		1.86				56.4		5870		1.87				55.2		4670		1.83				55.8		6360		1.85

		54.9		4610		1.81				55.1		4440		1.82				55.9		4940		1.85				55.6		4620		1.84				56.3		4740		1.86				56.5		5880		1.87				55.3		4670		1.83				55.8		6370		1.85

		55		4620		1.81				55.2		4450		1.82				56		4940		1.85				55.7		4630		1.84				56.4		4740		1.86				56.5		5880		1.87				55.3		4680		1.83				55.9		6380		1.85

		55		4620		1.82				55.2		4450		1.82				56		4950		1.85				55.7		4630		1.84				56.4		4750		1.87				56.6		5890		1.87				55.4		4680		1.83				56		6380		1.85

		55.1		4630		1.82				55.3		4460		1.83				56.1		4950		1.85				55.8		4630		1.84				56.5		4750		1.87				56.7		5900		1.87				55.4		4690		1.83				56		6390		1.85

		55.1		4630		1.82				55.4		4460		1.83				56.2		4960		1.86				55.8		4640		1.85				56.6		4760		1.87				56.7		5910		1.88				55.6		4700		1.84				56.1		6400		1.86

		55.2		4630		1.82				55.4		4470		1.83				56.2		4960		1.86				55.9		4640		1.85				56.7		4760		1.87				56.8		5910		1.88				55.6		4700		1.84				56.2		6410		1.86

		55.3		4640		1.82				55.5		4470		1.83				56.3		4970		1.86				56		4650		1.85				56.7		4770		1.88				56.8		5920		1.88				55.7		4700		1.84				56.2		6410		1.86

		55.4		4650		1.83				55.6		4480		1.84				56.3		4970		1.86				56		4650		1.85				56.8		4770		1.88				56.9		5920		1.88				55.7		4710		1.84				56.3		6420		1.86

		55.4		4650		1.83				55.6		4480		1.84				56.5		4980		1.87				56.1		4650		1.85				56.9		4770		1.88				57		5930		1.89				55.8		4710		1.85				56.4		6430		1.87

		55.5		4660		1.83				55.7		4480		1.84				56.5		4990		1.87				56.3		4660		1.86				56.9		4780		1.88				57		5940		1.89				55.8		4720		1.85				56.4		6440		1.87

		55.6		4660		1.83				55.8		4490		1.84				56.6		4990		1.87				56.3		4670		1.86				57		4780		1.88				57.1		5940		1.89				55.9		4720		1.85				56.5		6440		1.87

		55.6		4660		1.84				55.8		4490		1.84				56.6		4990		1.87				56.4		4670		1.86				57		4790		1.89				57.2		5950		1.89				56		4720		1.85				56.5		6450		1.87

		55.7		4670		1.84				55.9		4500		1.85				56.7		5000		1.88				56.4		4670		1.86				57.1		4790		1.89				57.2		5960		1.9				56.1		4730		1.86				56.6		6460		1.87

		55.8		4670		1.84				56		4500		1.85				56.8		5000		1.88				56.5		4680		1.87				57.2		4790		1.89				57.3		5960		1.9				56.1		4740		1.86				56.7		6460		1.88

		55.8		4680		1.84				56.1		4510		1.85				56.8		5010		1.88				56.5		4680		1.87				57.3		4800		1.89				57.4		5970		1.9				56.2		4740		1.86				56.8		6480		1.88

		55.9		4680		1.84				56.1		4510		1.85				56.9		5010		1.88				56.6		4690		1.87				57.4		4810		1.9				57.4		5980		1.9				56.3		4750		1.86				56.8		6480		1.88

		56		4690		1.85				56.2		4520		1.86				57		5020		1.88				56.7		4690		1.87				57.4		4810		1.9				57.5		5980		1.9				56.3		4750		1.86				56.9		6490		1.88

		56		4690		1.85				56.2		4520		1.86				57		5020		1.89				56.7		4690		1.87				57.5		4820		1.9				57.6		5990		1.91				56.4		4760		1.87				57		6500		1.89

		56.1		4690		1.85				56.3		4530		1.86				57.1		5030		1.89				56.9		4700		1.88				57.6		4820		1.9				57.6		6000		1.91				56.4		4760		1.87				57		6500		1.89

		56.2		4700		1.85				56.4		4530		1.86				57.2		5030		1.89				56.9		4710		1.88				57.6		4820		1.9				57.7		6000		1.91				56.5		4760		1.87				57.1		6510		1.89

		56.2		4700		1.85				56.5		4530		1.86				57.2		5040		1.89				57		4710		1.88				57.7		4830		1.91				57.8		6010		1.91				56.6		4770		1.87				57.2		6520		1.89

		56.3		4710		1.86				56.5		4540		1.87				57.3		5040		1.89				57.1		4710		1.88				57.8		4830		1.91				57.8		6020		1.92				56.7		4780		1.88				57.2		6530		1.89

		56.3		4710		1.86				56.6		4540		1.87				57.4		5040		1.9				57.1		4720		1.89				57.8		4840		1.91				57.9		6020		1.92				56.8		4780		1.88				57.3		6530		1.9

		56.4		4710		1.86				56.6		4550		1.87				57.4		5050		1.9				57.2		4720		1.89				57.9		4840		1.91				58		6030		1.92				56.8		4790		1.88				57.4		6540		1.9

		56.4		4720		1.86				56.7		4550		1.87				57.6		5060		1.9				57.2		4730		1.89				57.9		4850		1.92				58		6040		1.92				56.9		4790		1.88				57.4		6550		1.9

		56.6		4730		1.87				56.8		4560		1.88				57.6		5060		1.91				57.3		4730		1.89				58		4850		1.92				58.1		6040		1.92				56.9		4790		1.88				57.5		6560		1.9

		56.7		4730		1.87				56.8		4560		1.88				57.7		5070		1.91				57.4		4740		1.9				58.1		4860		1.92				58.1		6050		1.93				57		4800		1.89				57.5		6570		1.91

		56.7		4740		1.87				56.9		4570		1.88				57.8		5070		1.91				57.5		4740		1.9				58.2		4860		1.92				58.2		6050		1.93				57.1		4800		1.89				57.6		6570		1.91

		56.8		4740		1.87				57		4570		1.88				57.8		5080		1.91				57.5		4740		1.9				58.2		4870		1.92				58.3		6060		1.93				57.1		4810		1.89				57.7		6580		1.91

		56.8		4740		1.88				57		4570		1.88				57.9		5080		1.91				57.6		4750		1.9				58.3		4870		1.93				58.4		6070		1.93				57.3		4820		1.89				57.7		6590		1.91

		56.9		4750		1.88				57.1		4580		1.89				57.9		5080		1.92				57.7		4750		1.91				58.3		4870		1.93				58.5		6080		1.94				57.3		4820		1.9				57.8		6590		1.91

		57		4750		1.88				57.2		4590		1.89				58		5090		1.92				57.7		4760		1.91				58.4		4880		1.93				58.5		6090		1.94				57.4		4820		1.9				57.9		6610		1.92

		57		4760		1.88				57.2		4590		1.89				58		5090		1.92				57.8		4760		1.91				58.5		4880		1.93				58.6		6090		1.94				57.4		4830		1.9				58		6610		1.92

		57.1		4760		1.89				57.3		4590		1.89				58.2		5100		1.92				57.8		4760		1.91				58.5		4890		1.94				58.7		6100		1.94				57.5		4830		1.9				58		6620		1.92

		57.2		4770		1.89				57.4		4600		1.9				58.3		5110		1.93				58		4770		1.92				58.6		4890		1.94				58.7		6100		1.94				57.6		4840		1.91				58.1		6630		1.92

		57.3		4770		1.89				57.4		4600		1.9				58.3		5110		1.93				58		4780		1.92				58.7		4900		1.94				58.8		6110		1.95				57.6		4840		1.91				58.2		6630		1.93

		57.3		4780		1.89				57.5		4610		1.9				58.4		5120		1.93				58.1		4780		1.92				58.7		4900		1.94				58.9		6120		1.95				57.7		4850		1.91				58.2		6640		1.93

		57.4		4780		1.89				57.6		4610		1.9				58.4		5120		1.93				58.2		4790		1.92				58.8		4900		1.94				58.9		6130		1.95				57.8		4850		1.91				58.3		6650		1.93

		57.5		4790		1.9				57.6		4620		1.9				58.5		5130		1.93				58.3		4790		1.92				58.9		4910		1.95				59		6130		1.95				57.9		4860		1.91				58.3		6660		1.93

		57.5		4790		1.9				57.7		4620		1.91				58.5		5130		1.94				58.3		4790		1.93				58.9		4910		1.95				59.1		6140		1.96				57.9		4860		1.92				58.4		6660		1.93

		57.6		4790		1.9				57.8		4630		1.91				58.6		5130		1.94				58.3		4800		1.93				59		4920		1.95				59.1		6140		1.96				58		4870		1.92				58.5		6680		1.94

		57.7		4800		1.9				57.9		4630		1.91				58.7		5140		1.94				58.4		4800		1.93				59.1		4920		1.95				59.2		6150		1.96				58		4870		1.92				58.6		6680		1.94

		57.7		4810		1.91				58		4640		1.91				58.8		5150		1.95				58.6		4810		1.93				59.1		4930		1.96				59.3		6160		1.96				58.1		4870		1.92				58.7		6690		1.94

		57.8		4810		1.91				58		4640		1.92				58.9		5150		1.95				58.6		4810		1.94				59.2		4930		1.96				59.3		6160		1.96				58.2		4880		1.93				58.7		6700		1.94

		57.9		4820		1.91				58.1		4640		1.92				58.9		5160		1.95				58.7		4820		1.94				59.3		4940		1.96				59.4		6170		1.97				58.3		4880		1.93				58.8		6710		1.95

		57.9		4820		1.91				58.1		4650		1.92				59		5160		1.95				58.7		4820		1.94				59.3		4940		1.96				59.4		6180		1.97				58.3		4890		1.93				58.8		6710		1.95

		58		4820		1.91				58.2		4650		1.92				59		5170		1.95				58.8		4820		1.94				59.4		4940		1.96				59.6		6190		1.97				58.4		4890		1.93				58.9		6720		1.95

		58.1		4830		1.92				58.3		4660		1.92				59.1		5170		1.96				58.8		4830		1.95				59.5		4950		1.97				59.6		6200		1.97				58.5		4900		1.94				58.9		6730		1.95

		58.2		4830		1.92				58.4		4670		1.93				59.2		5180		1.96				58.9		4830		1.95				59.6		4950		1.97				59.7		6200		1.98				58.5		4900		1.94				59		6740		1.95

		58.2		4840		1.92				58.5		4670		1.93				59.3		5180		1.96				59		4840		1.95				59.6		4960		1.97				59.8		6210		1.98				58.6		4910		1.94				59.1		6750		1.96

		58.2		4840		1.92				58.5		4670		1.93				59.3		5190		1.96				59.1		4840		1.95				59.7		4960		1.97				59.8		6210		1.98				58.7		4910		1.94				59.2		6760		1.96

		58.3		4840		1.93				58.6		4680		1.93				59.4		5190		1.96				59.2		4850		1.96				59.7		4970		1.98				59.9		6220		1.98				58.7		4920		1.94				59.3		6760		1.96

		58.4		4850		1.93				58.6		4680		1.94				59.4		5200		1.97				59.2		4850		1.96				59.8		4970		1.98				59.9		6230		1.98				58.8		4920		1.95				59.3		6770		1.97

		58.5		4850		1.93				58.7		4690		1.94				59.5		5200		1.97				59.3		4860		1.96				59.9		4980		1.98				60		6230		1.99				58.8		4920		1.95				59.4		6780		1.97

		58.5		4860		1.93				58.8		4690		1.94				59.6		5200		1.97				59.3		4860		1.96				59.9		4980		1.98				60.1		6240		1.99				58.9		4930		1.95				59.4		6790		1.97

		58.6		4860		1.93				58.8		4700		1.94				59.7		5210		1.97				59.4		4860		1.96				60		4980		1.98				60.1		6250		1.99				58.9		4930		1.95				59.5		6790		1.97

		58.6		4870		1.94				58.9		4700		1.95				59.7		5210		1.97				59.5		4870		1.97				60		4990		1.99				60.2		6250		1.99				59.1		4940		1.96				59.6		6800		1.97

		58.7		4870		1.94				59		4710		1.95				59.8		5220		1.98				59.5		4870		1.97				60.1		4990		1.99				60.2		6260		2				59.1		4950		1.96				59.7		6810		1.98

		58.8		4880		1.94				59		4710		1.95				59.9		5230		1.98				59.6		4880		1.97				60.2		5000		1.99				60.3		6260		2				59.2		4950		1.96				59.7		6820		1.98

		58.9		4880		1.94				59.1		4720		1.95				59.9		5230		1.98				59.7		4880		1.97				60.3		5000		1.99				60.4		6270		2				59.3		4960		1.96				59.8		6830		1.98

		58.9		4890		1.95				59.1		4720		1.95				60		5240		1.99				59.8		4890		1.98				60.3		5010		1.99				60.4		6270		2				59.3		4960		1.96				59.9		6830		1.98

		59		4890		1.95				59.2		4720		1.96				60.1		5240		1.99				59.8		4890		1.98				60.4		5010		2				60.5		6280		2				59.4		4970		1.97				59.9		6840		1.99

		59.1		4890		1.95				59.3		4730		1.96				60.2		5250		1.99				59.9		4890		1.98				60.5		5010		2				60.6		6290		2.01				59.4		4970		1.97				60		6850		1.99

		59.1		4900		1.95				59.4		4730		1.96				60.2		5250		1.99				59.9		4900		1.98				60.5		5020		2				60.6		6290		2.01				59.5		4970		1.97				60		6850		1.99

		59.2		4900		1.95				59.4		4740		1.96				60.3		5260		1.99				60		4900		1.98				60.6		5020		2				60.7		6310		2.01				59.6		4980		1.97				60.1		6860		1.99

		59.3		4910		1.96				59.5		4740		1.97				60.3		5260		2				60.1		4910		1.99				60.6		5030		2.01				60.8		6310		2.01				59.7		4990		1.98				60.2		6870		1.99

		59.3		4910		1.96				59.5		4750		1.97				60.5		5270		2				60.1		4910		1.99				60.8		5030		2.01				60.8		6310		2.01				59.7		4990		1.98				60.3		6880		2

		59.4		4920		1.96				59.6		4750		1.97				60.5		5270		2				60.2		4910		1.99				60.8		5040		2.01				60.9		6320		2.02				59.8		5000		1.98				60.3		6890		2

		59.5		4920		1.96				59.7		4760		1.97				60.6		5280		2				60.3		4920		1.99				60.9		5040		2.01				61		6330		2.02				59.8		5000		1.98				60.4		6890		2

		59.6		4930		1.97				59.8		4760		1.97				60.6		5280		2.01				60.4		4930		2				60.9		5050		2.02				61.1		6330		2.02				59.9		5000		1.98				60.4		6900		2

		59.7		4930		1.97				59.8		4760		1.98				60.7		5290		2.01				60.5		4930		2				61		5050		2.02				61.1		6340		2.02				60		5010		1.99				60.5		6910		2

		59.7		4940		1.97				59.9		4770		1.98				60.8		5290		2.01				60.5		4930		2				61.1		5050		2.02				61.1		6340		2.03				60		5010		1.99				60.6		6920		2.01

		59.8		4940		1.97				59.9		4770		1.98				60.8		5300		2.01				60.6		4940		2				61.2		5060		2.02				61.2		6350		2.03				60.1		5020		1.99				60.6		6920		2.01

		59.8		4940		1.98				60		4780		1.98				60.9		5300		2.01				60.6		4940		2				61.2		5060		2.02				61.3		6360		2.03				60.2		5020		1.99				60.7		6930		2.01

		59.8		4950		1.98				60.1		4780		1.99				61		5310		2.02				60.7		4950		2.01				61.3		5070		2.03				61.4		6370		2.03				60.3		5030		1.99				60.8		6940		2.01

		59.9		4950		1.98				60.2		4790		1.99				61.1		5310		2.02				60.7		4950		2.01				61.4		5080		2.03				61.4		6370		2.03				60.3		5030		2				60.9		6950		2.02

		60		4960		1.98				60.2		4790		1.99				61.1		5320		2.02				60.8		4950		2.01				61.4		5080		2.03				61.5		6380		2.04				60.4		5040		2				60.9		6960		2.02

		60		4960		1.98				60.3		4800		1.99				61.2		5320		2.03				60.9		4960		2.01				61.5		5080		2.03				61.6		6390		2.04				60.4		5040		2				61		6970		2.02

		60.1		4960		1.98				60.4		4800		1.99				61.2		5330		2.03				61		4960		2.02				61.6		5090		2.04				61.6		6390		2.04				60.5		5050		2				61.1		6980		2.02

		60.2		4970		1.99				60.4		4810		2				61.3		5330		2.03				61		4970		2.02				61.6		5090		2.04				61.7		6400		2.04				60.6		5050		2.01				61.1		6980		2.03

		60.2		4970		1.99				60.5		4810		2				61.4		5340		2.03				61.1		4970		2.02				61.7		5100		2.04				61.8		6400		2.05				60.7		5060		2.01				61.2		6990		2.03

		60.3		4980		1.99				60.6		4820		2				61.5		5340		2.03				61.2		4980		2.02				61.8		5100		2.04				61.9		6420		2.05				60.7		5060		2.01				61.3		7000		2.03

		60.3		4980		1.99				60.7		4820		2.01				61.5		5340		2.04				61.2		4980		2.02				61.9		5110		2.05				62		6420		2.05				60.8		5070		2.01				61.3		7000		2.03

		60.4		4990		2				60.8		4830		2.01				61.6		5350		2.04				61.3		4980		2.03				61.9		5110		2.05				62		6430		2.05				60.9		5070		2.01				61.4		7020		2.04

		60.5		4990		2				60.8		4830		2.01				61.7		5360		2.04				61.3		4990		2.03				62		5120		2.05				62.1		6430		2.06				60.9		5080		2.02				61.5		7030		2.04

		60.6		5000		2				60.9		4840		2.01				61.7		5360		2.04				61.4		4990		2.03				62.1		5120		2.05				62.1		6440		2.06				61		5080		2.02				61.6		7030		2.04

		60.7		5000		2				61		4840		2.01				61.8		5360		2.04				61.5		5000		2.03				62.1		5130		2.06				62.2		6450		2.06				61		5090		2.02				61.7		7040		2.04

		60.7		5010		2.01				61		4850		2.02				61.9		5370		2.05				61.6		5000		2.04				62.2		5130		2.06				62.2		6450		2.06				61.1		5090		2.02				61.7		7050		2.04

		60.8		5010		2.01				61.1		4850		2.02				61.9		5370		2.05				61.7		5010		2.04				62.3		5140		2.06				62.3		6460		2.06				61.2		5090		2.03				61.8		7050		2.05

		60.9		5010		2.01				61.1		4850		2.02				62		5380		2.05				61.7		5010		2.04				62.3		5140		2.06				62.4		6470		2.07				61.3		5100		2.03				61.8		7060		2.05

		60.9		5020		2.01				61.3		4860		2.02				62.1		5380		2.05				61.8		5020		2.04				62.4		5150		2.06				62.5		6470		2.07				61.3		5110		2.03				61.9		7070		2.05

		61		5020		2.01				61.3		4870		2.03				62.2		5390		2.06				61.8		5020		2.05				62.5		5150		2.07				62.5		6480		2.07				61.4		5110		2.03				62		7080		2.05

		61.1		5030		2.02				61.4		4870		2.03				62.2		5390		2.06				61.9		5020		2.05				62.6		5150		2.07				62.6		6490		2.07				61.4		5120		2.03				62.1		7090		2.06

		61.1		5030		2.02				61.5		4880		2.03				62.3		5400		2.06				62		5030		2.05				62.6		5160		2.07				62.6		6490		2.08				61.5		5120		2.04				62.1		7100		2.06

		61.1		5040		2.02				61.5		4880		2.03				62.3		5400		2.06				62		5030		2.05				62.7		5160		2.07				62.7		6500		2.08				61.6		5130		2.04				62.2		7100		2.06

		61.2		5040		2.02				61.6		4880		2.03				62.4		5410		2.06				62.1		5040		2.05				62.7		5170		2.07				62.8		6500		2.08				61.6		5130		2.04				62.3		7110		2.06

		61.3		5040		2.02				61.6		4890		2.04				62.4		5410		2.07				62.2		5040		2.06				62.8		5170		2.08				62.9		6510		2.08				61.7		5130		2.04				62.3		7120		2.07

		61.3		5050		2.03				61.7		4890		2.04				62.5		5420		2.07				62.2		5040		2.06				62.8		5170		2.08				62.9		6520		2.08				61.7		5140		2.04				62.4		7130		2.07

		61.4		5050		2.03				61.8		4900		2.04				62.6		5420		2.07				62.3		5050		2.06				62.9		5180		2.08				63		6530		2.09				61.9		5150		2.05				62.4		7130		2.07

		61.5		5060		2.03				61.9		4910		2.05				62.7		5430		2.07				62.4		5050		2.06				63		5190		2.09				63		6530		2.09				61.9		5150		2.05				62.6		7150		2.07

		61.5		5060		2.03				61.9		4910		2.05				62.7		5430		2.08				62.4		5060		2.06				63.1		5190		2.09				63.1		6540		2.09				62		5160		2.05				62.6		7160		2.08

		61.6		5060		2.03				62		4910		2.05				62.8		5440		2.08				62.5		5060		2.07				63.2		5200		2.09				63.2		6540		2.09				62.1		5160		2.06				62.7		7160		2.08

		61.7		5070		2.04				62.1		4920		2.05				62.9		5440		2.08				62.6		5060		2.07				63.2		5200		2.09				63.2		6550		2.09				62.1		5170		2.06				62.8		7170		2.08

		61.7		5070		2.04				62.1		4920		2.05				62.9		5450		2.08				62.7		5070		2.07				63.3		5200		2.09				63.3		6560		2.1				62.2		5170		2.06				62.8		7180		2.08

		61.8		5080		2.04				62.2		4930		2.06				63		5450		2.08				62.7		5080		2.08				63.3		5210		2.1				63.4		6560		2.1				62.2		5170		2.06				62.9		7180		2.08

		61.9		5080		2.04				62.2		4930		2.06				63		5460		2.09				62.8		5080		2.08				63.4		5210		2.1				63.4		6570		2.1				62.3		5180		2.06				62.9		7190		2.09

		61.9		5090		2.05				62.4		4940		2.06				63.1		5460		2.09				62.9		5080		2.08				63.5		5220		2.1				63.5		6580		2.11				62.4		5180		2.07				63		7200		2.09

		62		5090		2.05				62.5		4940		2.06				63.2		5460		2.09				62.9		5090		2.08				63.6		5220		2.1				63.6		6590		2.11				62.5		5190		2.07				63.1		7210		2.09

		62.1		5100		2.05				62.5		4950		2.07				63.3		5470		2.09				63		5090		2.08				63.7		5230		2.11				63.7		6600		2.11				62.5		5190		2.07				63.2		7220		2.09

		62.1		5100		2.05				62.6		4950		2.07				63.4		5480		2.1				63.1		5100		2.09				63.7		5230		2.11				63.7		6600		2.11				62.6		5200		2.07				63.3		7230		2.1

		62.2		5100		2.05				62.6		4960		2.07				63.4		5480		2.1				63.1		5100		2.09				63.8		5240		2.11				63.8		6610		2.11				62.7		5200		2.07				63.3		7240		2.1

		62.3		5110		2.06				62.7		4960		2.07				63.5		5490		2.1				63.2		5100		2.09				63.8		5240		2.11				63.9		6610		2.12				62.7		5200		2.08				63.4		7240		2.1

		62.4		5120		2.06				62.7		4970		2.07				63.6		5490		2.1				63.3		5110		2.09				63.9		5250		2.11				63.9		6620		2.12				62.8		5200		2.08				63.4		7250		2.1

		62.5		5120		2.06				62.8		4970		2.08				63.6		5500		2.11				63.4		5110		2.1				64		5250		2.12				64		6630		2.12				62.8		5210		2.08				63.5		7260		2.1

		62.5		5130		2.06				62.9		4970		2.08				63.7		5500		2.11				63.4		5120		2.1				64		5250		2.12				64.1		6640		2.12				62.9		5210		2.08				63.6		7260		2.11

		62.6		5130		2.07				63		4980		2.08				63.7		5510		2.11				63.5		5120		2.1				64.2		5260		2.12				64.2		6650		2.13				63		5220		2.09				63.7		7280		2.11

		62.6		5130		2.07				63		4990		2.08				63.8		5510		2.11				63.6		5130		2.1				64.2		5270		2.12				64.2		6650		2.13				63		5220		2.09				63.7		7280		2.11

		62.7		5140		2.07				63.1		4990		2.09				63.9		5520		2.12				63.6		5130		2.1				64.3		5270		2.13				64.3		6660		2.13				63.1		5220		2.09				63.8		7290		2.11

		62.7		5140		2.07				63.2		5000		2.09				64		5520		2.12				63.7		5130		2.11				64.3		5270		2.13				64.4		6660		2.13				63.2		5230		2.09				63.9		7300		2.12

		62.8		5150		2.08				63.3		5000		2.09				64.1		5530		2.12				63.7		5140		2.11				64.4		5280		2.13				64.4		6670		2.13				63.2		5230		2.09				63.9		7300		2.12

		62.9		5150		2.08				63.3		5000		2.09				64.1		5530		2.12				63.9		5150		2.11				64.5		5280		2.13				64.5		6680		2.14				63.3		5230		2.1				64		7310		2.12

		62.9		5160		2.08				63.4		5010		2.1				64.2		5540		2.12				63.9		5150		2.11				64.6		5290		2.13				64.5		6680		2.14				63.3		5220		2.1				64		7320		2.12

		63		5160		2.08				63.4		5010		2.1				64.2		5540		2.13				64		5150		2.12				64.6		5290		2.14				64.6		6690		2.14				63.4		5220		2.1				64.1		7330		2.12

		63.1		5160		2.08				63.5		5020		2.1				64.3		5550		2.13				64.1		5160		2.12				64.7		5300		2.14				64.7		6700		2.14				63.5		5190		2.1				64.2		7340		2.13

		63.1		5170		2.09				63.6		5020		2.1				64.4		5550		2.13				64.1		5160		2.12				64.7		5300		2.14				64.8		6700		2.15				63.6		5180		2.11				64.2		7340		2.13

		63.2		5170		2.09				63.6		5030		2.1				64.5		5560		2.13				64.2		5170		2.12				64.8		5310		2.14				64.9		6710		2.15				63.6		5180		2.11				64.3		7350		2.13

		63.3		5180		2.09				63.7		5030		2.11				64.5		5560		2.13				64.2		5170		2.13				64.9		5310		2.15				64.9		6720		2.15				63.7		1850		2.11				64.4		7360		2.13

		63.3		5180		2.09				63.8		5040		2.11				64.6		5570		2.14				64.3		5170		2.13				65		5310		2.15				65		6720		2.15				63.8		-458		2.11				64.4		7370		2.14

		63.4		5190		2.09				63.8		5040		2.11				64.6		5570		2.14				64.4		5180		2.13				65		5320		2.15				65		6730		2.15				63.8		-454		2.12				64.5		7370		2.14

		63.5		5190		2.1				63.9		5040		2.11				64.7		5580		2.14				64.5		5190		2.13				65.1		5320		2.15				65.1		6730		2.16												64.6		7380		2.14

		63.6		5200		2.1				63.9		5050		2.11				64.7		5580		2.14				64.6		5190		2.13				65.1		5330		2.16				65.1		6740		2.16												64.6		7390		2.14

		63.6		5200		2.1				64		5050		2.12				64.8		5590		2.15				64.6		5190		2.14				65.2		5330		2.16				65.3		6750		2.16												64.7		7400		2.14

		63.7		5210		2.1				64.1		5060		2.12				64.9		5590		2.15				64.7		5200		2.14				65.3		5340		2.16				65.3		6760		2.16												64.8		7410		2.15

		63.7		5210		2.11				64.2		5060		2.12				65		5600		2.15				64.7		5200		2.14				65.4		5340		2.16				65.4		6760		2.17												64.8		7410		2.15

		63.8		5210		2.11				64.3		5070		2.12				65.1		5600		2.15				64.8		5210		2.14				65.4		5350		2.17				65.5		6770		2.17												64.9		7420		2.15

		63.9		5220		2.11				64.3		5070		2.13				65.1		5610		2.15				64.9		5210		2.15				65.5		5350		2.17				65.5		6780		2.17												65		7430		2.15

		63.9		5220		2.11				64.4		5080		2.13				65.2		5610		2.16				64.9		5210		2.15				65.6		5360		2.17				65.6		6780		2.17												65		7430		2.16

		64.1		5230		2.12				64.4		5080		2.13				65.2		5610		2.16				65.1		5210		2.15				65.6		5360		2.17				65.7		6780		2.18												65.1		7440		2.16

		64.1		5240		2.12				64.5		5090		2.13				65.3		5620		2.16				65.1		5210		2.15				65.7		5360		2.17				65.7		6790		2.18												65.2		7450		2.16

		64.2		5240		2.12				64.6		5090		2.13				65.4		5620		2.16				65.1		5220		2.16				65.8		5370		2.18				65.8		6790		2.18												65.2		7450		2.16

		64.3		5250		2.12				64.7		5100		2.14				65.5		5630		2.17				65.2		5220		2.16				65.9		5370		2.18				65.9		6800		2.18												65.3		7460		2.16

		64.3		5250		2.13				64.8		5100		2.14				65.5		5630		2.17				65.3		5230		2.16				65.9		5380		2.18				65.9		6810		2.18												65.4		7470		2.17

		64.4		5250		2.13				64.8		5110		2.14				65.6		5640		2.17				65.3		5230		2.16				66		5380		2.18				66		6810		2.19												65.4		7480		2.17

		64.4		5260		2.13				64.9		5110		2.15				65.6		5640		2.17				65.4		5230		2.16				66		5390		2.19				66		6820		2.19												65.5		7480		2.17

		64.5		5260		2.13				64.9		5120		2.15				65.7		5650		2.17				65.5		5240		2.17				66.1		5390		2.19				66.1		6830		2.19												65.6		7490		2.17

		64.6		5270		2.13				65		5120		2.15				65.7		5650		2.18				65.5		5240		2.17				66.2		5400		2.19				66.2		6830		2.19												65.7		7490		2.18

		64.6		5270		2.14				65		5130		2.15				65.8		5660		2.18				65.6		5250		2.17				66.2		5400		2.19				66.2		6840		2.19												65.7		7500		2.18

		64.7		5280		2.14				65.1		5130		2.15				65.9		5660		2.18				65.7		5260		2.17				66.3		5400		2.19				66.3		6840		2.2												65.8		7510		2.18

		64.8		5280		2.14				65.2		5140		2.16				66		5670		2.18				65.8		5260		2.18				66.3		5410		2.2				66.4		6850		2.2												65.8		7520		2.18

		64.8		5280		2.14				65.3		5140		2.16				66.1		5670		2.19				65.9		5260		2.18				66.4		5410		2.2				66.5		6860		2.2												65.9		7520		2.18

		64.9		5290		2.15				65.4		5150		2.16				66.1		5680		2.19				65.9		5270		2.18				66.5		5420		2.2				66.6		6870		2.21												66		7530		2.19

		65		5290		2.15				65.4		5150		2.16				66.1		5680		2.19				66		5270		2.18				66.5		5420		2.2				66.6		6870		2.21												66		7540		2.19

		65		5300		2.15				65.5		5160		2.17				66.2		5690		2.19				66		5280		2.18				66.6		5430		2.2				66.7		6880		2.21												66.1		7550		2.19

		65.1		5300		2.15				65.5		5160		2.17				66.3		5690		2.19				66.1		5280		2.19				66.7		5430		2.21				66.7		6880		2.21												66.2		7560		2.19

		65.2		5310		2.15				65.6		5170		2.17				66.3		5700		2.2				66.1		5280		2.19				66.7		5430		2.21				66.8		6890		2.21												66.2		7560		2.2

		65.2		5310		2.16				65.7		5170		2.17				66.4		5700		2.2				66.2		5290		2.19				66.8		5440		2.21				66.9		6900		2.22												66.3		7570		2.2

		65.3		5320		2.16				65.8		5170		2.17				66.5		5700		2.2				66.3		5290		2.19				66.9		5440		2.21				66.9		6900		2.22												66.3		7580		2.2

		65.4		5320		2.16				65.9		5180		2.18				66.5		5710		2.2				66.3		5290		2.19				67		5450		2.22				67		6910		2.22												66.4		7590		2.2

		65.4		5330		2.16				65.9		5190		2.18				66.6		5710		2.2				66.4		5300		2.2				67		5450		2.22				67.1		6920		2.22												66.5		7590		2.2

		65.5		5330		2.16				66		5190		2.18				66.7		5720		2.21				66.5		5300		2.2				67.1		5460		2.22				67.1		6920		2.22												66.6		7600		2.21

		65.5		5330		2.17				66.1		5200		2.18				66.7		5720		2.21				66.5		5310		2.2				67.1		5460		2.22				67.2		6930		2.23												66.6		7610		2.21

		65.6		5340		2.17				66.1		5200		2.19				66.8		5730		2.21				66.6		5310		2.2				67.2		5470		2.22				67.3		6940		2.23												66.7		7620		2.21

		65.7		5340		2.17				66.2		5200		2.19				66.8		5730		2.21				66.7		5310		2.21				67.3		5470		2.23				67.4		6940		2.23												66.8		7630		2.21

		65.8		5350		2.17				66.3		5210		2.19				66.9		5740		2.22				66.8		5320		2.21				67.4		5470		2.23				67.4		6950		2.23												66.8		7630		2.22

		65.8		5350		2.18				66.3		5210		2.19				67		5740		2.22				66.8		5330		2.21				67.4		5480		2.23				67.4		6950		2.24												66.9		7640		2.22

		65.9		5360		2.18				66.4		5220		2.2				67.1		5750		2.22				66.9		5330		2.21				67.5		5480		2.23				67.5		6960		2.24												66.9		7640		2.22

		66		5360		2.18				66.4		5220		2.2				67.1		5750		2.22				67		5330		2.22				67.6		5490		2.24				67.6		6970		2.24												67		7650		2.22

		66		5360		2.18				66.5		5230		2.2				67.2		5760		2.23				67		5340		2.22				67.6		5490		2.24				67.7		6980		2.24												67.1		7660		2.22

		66.1		5370		2.18				66.6		5230		2.2				67.3		5760		2.23				67.1		5340		2.22				67.7		5500		2.24				67.7		6980		2.24												67.2		7670		2.23

		66.2		5370		2.19				66.6		5240		2.2				67.4		5770		2.23				67.1		5350		2.22				67.7		5500		2.24				67.8		6990		2.25												67.3		7670		2.23

		66.3		5380		2.19				66.7		5240		2.21				67.4		5770		2.23				67.2		5350		2.22				67.8		5500		2.24				67.9		6980		2.25												67.3		7680		2.23

		66.3		5390		2.19				66.8		5250		2.21				67.5		5780		2.23				67.3		5360		2.23				67.9		5510		2.25				67.9		6980		2.25												67.4		7670		2.23

		66.4		5390		2.19				66.8		5250		2.21				67.5		5780		2.24				67.4		5360		2.23				67.9		5510		2.25				68		6980		2.25												67.5		7670		2.24

		66.5		5400		2.2				66.9		5260		2.21				67.6		5790		2.24				67.5		5370		2.23				68		5520		2.25				68		6970		2.26												67.5		7670		2.24

		66.5		5400		2.2				67		5260		2.22				67.7		5790		2.24				67.5		5370		2.23				68.1		5520		2.25				68.1		6980		2.26												67.6		7670		2.24

		66.6		5400		2.2				67.1		5270		2.22				67.8		5800		2.24				67.6		5370		2.24				68.1		5530		2.26				68.2		7000		2.26												67.7		7680		2.24

		66.6		5410		2.2				67.1		5270		2.22				67.9		5800		2.25				67.6		5380		2.24				68.2		5530		2.26				68.3		7000		2.26												67.7		7690		2.25

		66.7		5410		2.21				67.2		5280		2.22				67.9		5810		2.25				67.7		5380		2.24				68.3		5540		2.26				68.4		7010		2.27												67.8		7700		2.25

		66.8		5420		2.21				67.3		5280		2.23				68		5810		2.25				67.8		5390		2.24				68.3		5540		2.26				68.4		7020		2.27												67.9		7710		2.25

		66.9		5430		2.21				67.3		5290		2.23				68		5820		2.25				67.9		5390		2.24				68.4		5540		2.26				68.5		7020		2.27												68		7710		2.25

		67		5430		2.21				67.4		5290		2.23				68.1		5820		2.25				68		5400		2.25				68.5		5550		2.27				68.5		7030		2.27												68		7720		2.25

		67		5430		2.22				67.4		5290		2.23				68.1		5830		2.26				68		5400		2.25				68.5		5550		2.27				68.6		7030		2.27												68.1		7730		2.26

		67.1		5440		2.22				67.6		5300		2.24				68.3		5830		2.26				68.1		5410		2.25				68.6		5560		2.27				68.7		7040		2.28												68.1		7730		2.26

		67.1		5440		2.22				67.6		5310		2.24				68.3		5840		2.26				68.1		5410		2.26				68.6		5560		2.27				68.8		7050		2.28												68.2		7740		2.26

		67.2		5450		2.22				67.7		5310		2.24				68.4		5840		2.26				68.2		5410		2.26				68.7		5570		2.28				68.8		7060		2.28												68.3		7760		2.26

		67.3		5450		2.22				67.8		5310		2.24				68.5		5850		2.27				68.3		5420		2.26				68.8		5570		2.28				68.9		7060		2.28												68.4		7760		2.27

		67.4		5460		2.23				67.8		5320		2.24				68.5		5850		2.27				68.4		5420		2.26				68.9		5570		2.28				68.9		7060		2.29												68.5		7770		2.27

		67.4		5460		2.23				67.9		5320		2.25				68.6		5860		2.27				68.4		5430		2.26				68.9		5580		2.28				69		7070		2.29												68.5		7780		2.27

		67.5		5460		2.23				67.9		5330		2.25				68.6		5860		2.27				68.5		5430		2.27				69		5580		2.28				69.1		7080		2.29												68.6		7780		2.27

		67.6		5470		2.23				68		5330		2.25				68.7		5870		2.27				68.6		5440		2.27				69.1		5590		2.29				69.2		7080		2.29												68.6		7790		2.28

		67.6		5470		2.24				68.1		5340		2.25				68.8		5870		2.28				68.7		5440		2.27				69.1		5590		2.29				69.2		7090		2.29												68.7		7800		2.28

		67.7		5480		2.24				68.2		5340		2.26				68.9		5880		2.28				68.7		5450		2.27				69.2		5600		2.29				69.3		7100		2.3												68.7		7800		2.28

		67.8		5480		2.24				68.3		5350		2.26				69		5880		2.28				68.8		5450		2.28				69.2		5600		2.29				69.4		7110		2.3												68.8		7810		2.28

		67.8		5490		2.24				68.3		5350		2.26				69		5890		2.28				68.9		5450		2.28				69.4		5610		2.3				69.5		7110		2.3												68.9		7820		2.28

		67.9		5490		2.24				68.4		5360		2.26				69.1		5890		2.29				68.9		5460		2.28				69.4		5610		2.3				69.5		7120		2.3												69		7830		2.29

		68		5500		2.25				68.4		5360		2.26				69.1		5900		2.29				69		5460		2.28				69.5		5620		2.3				69.6		7120		2.31												69		7840		2.29

		68		5500		2.25				68.5		5360		2.27				69.2		5900		2.29				69.1		5470		2.29				69.6		5620		2.3				69.6		7130		2.31												69.1		7840		2.29

		68.1		5510		2.25				68.6		5370		2.27				69.3		5910		2.29				69.1		5470		2.29				69.6		5620		2.3				69.7		7130		2.31												69.1		7850		2.29

		68.2		5510		2.25				68.7		5380		2.27				69.3		5910		2.3				69.2		5480		2.29				69.7		5630		2.31				69.8		7140		2.31												69.2		7860		2.3

		68.2		5520		2.26				68.7		5380		2.27				69.4		5920		2.3				69.3		5480		2.29				69.7		5630		2.31				69.8		7150		2.32												69.3		7860		2.3

		68.3		5520		2.26				68.8		5380		2.27				69.5		5920		2.3				69.4		5490		2.29				69.8		5640		2.31				69.9		7160		2.32												69.3		7870		2.3

		68.4		5530		2.26				68.8		5390		2.28				69.6		5930		2.3				69.4		5490		2.3				69.9		5650		2.32				70		7160		2.32												69.4		7880		2.3

		68.4		5530		2.26				68.9		5390		2.28				69.6		5930		2.31				69.5		5490		2.3				70		5650		2.32				70.1		7170		2.32												69.5		7890		2.31

		68.5		5540		2.27				69		5400		2.28				69.7		5940		2.31				69.5		5500		2.3				70.1		5650		2.32				70.1		7170		2.32												69.6		7900		2.31

		68.6		5540		2.27				69		5400		2.28				69.7		5940		2.31				69.6		5500		2.3				70.1		5660		2.32				70.2		7170		2.33												69.6		7900		2.31

		68.7		5540		2.27				69.1		5400		2.29				69.8		5950		2.31				69.7		5500		2.31				70.2		5660		2.32				70.2		7170		2.33												69.7		7910		2.31

		68.7		5550		2.27				69.2		5410		2.29				69.9		5950		2.31				69.7		5510		2.31				70.2		5670		2.33				70.3		7160		2.33												69.8		7920		2.31

		68.8		5550		2.27				69.2		5410		2.29				70		5960		2.32				69.8		5510		2.31				70.3		5670		2.33				70.4		7150		2.33												69.9		7930		2.32

		68.8		5560		2.28				69.3		5420		2.29				70		5960		2.32				69.9		5520		2.31				70.4		5680		2.33				70.4		7150		2.34												69.9		7930		2.32

		68.9		5560		2.28				69.4		5420		2.29				70.1		5970		2.32				70		5520		2.31				70.4		5680		2.33				70.5		7150		2.34												70		7940		2.32

		68.9		5560		2.28				69.4		5430		2.3				70.2		5970		2.32				70		5520		2.32				70.6		5690		2.34				70.6		7140		2.34												70.1		7950		2.32

		69		5570		2.28				69.5		5430		2.3				70.2		5980		2.33				70		5530		2.32				70.6		5690		2.34				70.6		7140		2.34												70.1		7950		2.33

		69.1		5580		2.29				69.5		5440		2.3				70.3		5980		2.33				70.1		5530		2.32				70.7		5690		2.34				70.7		7140		2.34												70.2		7960		2.33

		69.2		5580		2.29				69.6		5440		2.3				70.4		5970		2.33				70.2		5540		2.32				70.7		5700		2.34				70.8		7140		2.35												70.3		7960		2.33

		69.3		5590		2.29				69.7		5450		2.31				70.5		5980		2.33				70.3		5540		2.33				70.8		5700		2.34				70.8		7150		2.35												70.3		7950		2.33

		69.3		5590		2.29				69.8		5450		2.31				70.5		5980		2.33				70.3		5540		2.33				70.9		5710		2.35				70.9		7150		2.35												70.4		7920		2.33

		69.4		5590		2.29				69.8		5460		2.31				70.6		5990		2.34				70.4		5550		2.33				70.9		5710		2.35				71		7150		2.35												70.4		280		2.34

		69.4		5600		2.3				69.9		5460		2.31				70.7		6000		2.34				70.5		5550		2.33				71		5720		2.35				71.1		7150		2.36												70.5		-490		2.34

		69.5		5600		2.3				69.9		5460		2.31				70.7		6000		2.34				70.5		5560		2.33				71.1		5720		2.35				71.1		7150		2.36

		69.6		5610		2.3				70		5470		2.32				70.8		6010		2.35				70.6		5560		2.34				71.1		5730		2.36				71.2		7150		2.36

		69.7		5610		2.31				70.1		5470		2.32				70.9		6010		2.35				70.6		5560		2.34				71.2		5730		2.36				71.3		7120		2.36

		69.8		5620		2.31				70.2		5480		2.32				70.9		6020		2.35				70.7		5570		2.34				71.3		5730		2.36				71.3		7130		2.36

		69.9		5620		2.31				70.2		5480		2.32				71		6020		2.35				70.8		5570		2.34				71.3		5740		2.36				71.4		7130		2.37

		69.9		5630		2.31				70.3		5490		2.33				71		6030		2.35				70.9		5580		2.35				71.4		5740		2.36				71.4		7130		2.37

		69.9		5630		2.31				70.4		5490		2.33				71.2		6030		2.36				70.9		5580		2.35				71.5		5750		2.37				71.5		7130		2.37

		70		5640		2.32				70.4		5500		2.33				71.2		6040		2.36				71		5590		2.35				71.5		5750		2.37				71.7		7140		2.37

		70.1		5640		2.32				70.5		5500		2.33				71.3		6040		2.36				71		5590		2.35				71.6		5760		2.37				71.7		7140		2.38

		70.1		5650		2.32				70.6		5510		2.33				71.4		6050		2.36				71.1		5590		2.35				71.7		5770		2.37				71.8		7140		2.38

		70.3		5650		2.32				70.6		5510		2.34				71.4		6050		2.36				71.2		5600		2.36				71.8		5770		2.38				71.8		7140		2.38

		70.3		5660		2.33				70.7		5510		2.34				71.5		6050		2.37				71.2		5600		2.36				71.9		5770		2.38				71.9		7150		2.38

		70.4		5660		2.33				70.8		5520		2.34				71.5		6060		2.37				71.3		5610		2.36				71.9		5780		2.38				71.9		7150		2.39

		70.5		5670		2.33				70.8		5530		2.34				71.6		6060		2.37				71.4		5610		2.36				72		5780		2.38				72		7160		2.39

		70.5		5670		2.33				70.9		5530		2.35				71.7		6070		2.38				71.4		5610		2.37				72		5790		2.38				72.1		7160		2.39

		70.6		5680		2.33				71		5540		2.35				71.8		6080		2.38				71.5		5620		2.37				72.1		5790		2.39				72.2		7160		2.39

		70.7		5680		2.34				71		5540		2.35				71.8		6080		2.38				71.6		5620		2.37				72.1		5790		2.39				72.3		7170		2.4

		70.7		5680		2.34				71.1		5540		2.35				71.9		6090		2.38				71.6		5630		2.37				72.2		5800		2.39				72.3		7170		2.4

		70.8		5690		2.34				71.2		5550		2.36				72		6090		2.38				71.7		5630		2.37				72.3		5800		2.39				72.4		7180		2.4

		70.9		5700		2.34				71.2		5550		2.36				72		6100		2.39				71.8		5630		2.38				72.4		5810		2.4				72.4		7180		2.4

		71		5700		2.35				71.3		5560		2.36				72.1		6100		2.39				71.9		5640		2.38				72.4		5810		2.4				72.5		7190		2.4

		71		5710		2.35				71.4		5570		2.36				72.2		6100		2.39				71.9		5640		2.38				72.5		5820		2.4				72.6		7190		2.41

		71.1		5710		2.35				71.5		5570		2.37				72.3		6110		2.39				72		5650		2.38				72.5		5820		2.4				72.6		7190		2.41

		71.1		5710		2.35				71.5		5570		2.37				72.3		6120		2.4				72		5650		2.39				72.6		5820		2.4				72.8		7200		2.41

		71.2		5720		2.36				71.6		5580		2.37				72.4		6120		2.4				72.1		5660		2.39				72.7		5830		2.41				72.8		7210		2.41

		71.3		5720		2.36				71.7		5580		2.37				72.5		6130		2.4				72.2		5660		2.39				72.7		5830		2.41				72.9		7190		2.42

		71.4		5730		2.36				71.7		5590		2.37				72.5		6130		2.4				72.2		5660		2.39				72.9		5840		2.41				73		4540		2.42

		71.4		5740		2.36				71.8		5590		2.38				72.6		6140		2.4				72.3		5660		2.39				73		5840		2.41				73		-583		2.42

		71.5		5740		2.37				71.9		5590		2.38				72.7		6140		2.41				72.4		5670		2.4				73		5850		2.42				73.1		-578		2.42

		71.6		5740		2.37				72		5600		2.38				72.7		6150		2.41				72.4		5670		2.4				73.1		5850		2.42

		71.6		5750		2.37				72		5610		2.38				72.9		6150		2.41				72.5		5680		2.4				73.1		5860		2.42

		71.7		5750		2.37				72.1		5610		2.39				72.9		6160		2.41				72.5		5680		2.4				73.2		5860		2.42

		71.8		5760		2.37				72.2		5620		2.39				73		6160		2.42				72.6		5680		2.4				73.2		5860		2.43

		71.9		5760		2.38				72.2		5620		2.39				73		6170		2.42				72.7		5690		2.41				73.3		5870		2.43

		71.9		5770		2.38				72.3		5620		2.39				73.1		6170		2.42				72.7		5690		2.41				73.4		5880		2.43

		71.9		5770		2.38				72.3		5630		2.39				73.2		6180		2.42				72.8		5700		2.41				73.5		5880		2.43

		72		5770		2.38				72.4		5630		2.4				73.2		6180		2.43				72.9		5700		2.41				73.6		5880		2.44

		72.1		5780		2.38				72.5		5640		2.4				73.3		6190		2.43				72.9		5700		2.41				73.6		5890		2.44

		72.1		5780		2.39				72.6		5650		2.4				73.4		6190		2.43				73		5710		2.42				73.7		5890		2.44

		72.2		5790		2.39				72.7		5650		2.41				73.4		6200		2.43				73.1		5710		2.42				73.8		5900		2.44

		72.3		5790		2.39				72.7		5650		2.41				73.5		6200		2.44				73.1		5720		2.42				73.8		5900		2.44

		72.3		5790		2.39				72.8		5660		2.41				73.6		6210		2.44				73.2		5720		2.42				73.9		5910		2.45

		72.4		5800		2.39				72.8		5660		2.41				73.6		6210		2.44				73.3		5720		2.43				73.9		5910		2.45

		72.5		5800		2.4				72.9		5670		2.41				73.7		6220		2.44				73.3		5730		2.43				74		5910		2.45

		72.5		5810		2.4				73		5670		2.42				73.8		6220		2.44				73.4		5730		2.43				74.1		5920		2.45

		72.6		5810		2.4				73.1		5680		2.42				73.8		6230		2.45				73.4		5740		2.43				74.1		5920		2.45

		72.7		5820		2.4				73.2		5680		2.42				73.9		6240		2.45				73.5		5740		2.43				74.2		5930		2.46

		72.8		5820		2.41				73.2		5690		2.42				74		6240		2.45				73.6		5740		2.44				74.2		5930		2.46

		72.8		5830		2.41				73.2		5690		2.42				74.1		6240		2.45				73.7		5750		2.44				74.3		5930		2.46

		72.8		5830		2.41				73.3		5700		2.43				74.2		6250		2.46				73.7		5750		2.44				74.4		5940		2.46

		72.9		5840		2.41				73.4		5700		2.43				74.2		6250		2.46				73.8		5750		2.44				74.4		5940		2.47

		73		5840		2.41				73.5		5700		2.43				74.3		6260		2.46				73.8		5760		2.44				74.5		5950		2.47

		73.1		5850		2.42				73.5		5710		2.43				74.3		6260		2.46				73.9		5760		2.45				74.6		5960		2.47

		73.2		5850		2.42				73.6		5710		2.44				74.4		6270		2.46				73.9		5770		2.45				74.7		5960		2.47

		73.3		5860		2.42				73.7		5720		2.44				74.5		6270		2.47				74		5770		2.45				74.8		5960		2.48

		73.3		5860		2.42				73.8		5720		2.44				74.5		6280		2.47				74.1		5770		2.45				74.8		5970		2.48

		73.4		5860		2.43				73.8		5730		2.44				74.6		6280		2.47				74.1		5780		2.45				74.9		5970		2.48

		73.4		5870		2.43				73.9		5730		2.45				74.7		6290		2.47				74.3		5790		2.46				74.9		5980		2.48

		73.5		5870		2.43				73.9		5740		2.45				74.8		6290		2.48				74.3		5790		2.46				75		5980		2.48

		73.6		5880		2.43				74		5740		2.45				74.8		6300		2.48				74.4		5790		2.46				75.1		5990		2.49

		73.6		5880		2.44				74.1		5750		2.45				74.9		6300		2.48				74.5		5800		2.47				75.2		5990		2.49

		73.7		5890		2.44				74.1		5750		2.45				74.9		6310		2.48				74.5		5800		2.47				75.3		6000		2.49

		73.8		5890		2.44				74.2		5750		2.46				75		6310		2.48				74.6		5800		2.47				75.3		6000		2.49

		73.8		5900		2.44				74.3		5760		2.46				75.1		6320		2.49				74.6		5810		2.47				75.4		6000		2.5

		73.9		5900		2.44				74.4		5770		2.46				75.1		6320		2.49				74.7		5810		2.47				75.4		6010		2.5

		73.9		5900		2.45				74.4		5770		2.46				75.2		6330		2.49				74.8		5820		2.48				75.5		6010		2.5

		74		5910		2.45				74.5		5780		2.47				75.3		6330		2.49				74.9		5820		2.48				75.5		6020		2.5

		74.1		5910		2.45				74.6		5780		2.47				75.4		6330		2.5				74.9		5830		2.48				75.7		6030		2.51

		74.2		5920		2.45				74.6		5790		2.47				75.4		6340		2.5				75		5830		2.48				75.7		6030		2.51

		74.2		5920		2.46				74.7		5790		2.47				75.4		6340		2.5				75.1		5830		2.49				75.8		6030		2.51

		74.3		5930		2.46				74.8		5790		2.47				75.5		6350		2.5				75.2		5840		2.49				75.9		6040		2.51

		74.4		5930		2.46				74.8		5800		2.48				75.6		6350		2.5				75.2		5840		2.49				75.9		6040		2.51

		74.4		5940		2.46				74.9		5810		2.48				75.7		6360		2.51				75.3		5840		2.49				76		6050		2.52

		74.5		5940		2.46				75		5810		2.48				75.8		6370		2.51				75.3		5850		2.49				76		6050		2.52

		74.6		5950		2.47				75.1		5820		2.49				75.9		6370		2.51				75.4		5850		2.5				76.1		6050		2.52

		74.6		5950		2.47				75.1		5820		2.49				75.9		6380		2.51				75.5		5860		2.5				76.2		6060		2.52

		74.7		5950		2.47				75.2		5820		2.49				76		6380		2.52				75.5		5860		2.5				76.3		6060		2.53

		74.7		5960		2.47				75.2		5830		2.49				76		6390		2.52				75.6		5870		2.5				76.4		6070		2.53

		74.8		5960		2.48				75.3		5830		2.49				76.1		6390		2.52				75.7		5870		2.51				76.4		6070		2.53

		74.9		5970		2.48				75.4		5840		2.5				76.1		6390		2.52				75.7		5870		2.51				76.4		6080		2.53

		74.9		5970		2.48				75.4		5840		2.5				76.2		6400		2.53				75.8		5880		2.51				76.5		6080		2.53

		75		5980		2.48				75.5		5850		2.5				76.3		6410		2.53				75.8		5880		2.51				76.6		6080		2.54

		75.1		5980		2.48				75.6		5850		2.5				76.4		6410		2.53				75.9		5880		2.51				76.7		6090		2.54

		75.2		5980		2.49				75.6		5860		2.5				76.5		6420		2.53				76		5890		2.52				76.7		6090		2.54

		75.2		5990		2.49				75.7		5860		2.51				76.5		6420		2.54				76.1		5890		2.52				76.8		6090		2.54

		75.3		5990		2.49				75.8		5870		2.51				76.6		6430		2.54				76.2		5900		2.52				76.9		6100		2.55

		75.3		6000		2.49				75.8		5870		2.51				76.7		6430		2.54				76.2		5900		2.52				76.9		6100		2.55

		75.4		6000		2.5				75.9		5870		2.51				76.7		6440		2.54				76.3		5910		2.53				77		6100		2.55

		75.5		6010		2.5				76		5880		2.52				76.8		6440		2.54				76.3		5910		2.53				77.1		6100		2.55

		75.6		6010		2.5				76		5880		2.52				76.8		6440		2.55				76.4		5910		2.53				77.1		6100		2.55

		75.6		6020		2.5				76.1		5890		2.52				76.9		6450		2.55				76.5		5920		2.53				77.2		6100		2.56

		75.7		6020		2.5				76.2		5890		2.52				77		6450		2.55				76.5		5920		2.54				77.3		6100		2.56

		75.8		6020		2.51				76.3		5900		2.53				77.1		6460		2.55				76.7		5930		2.54				77.4		6110		2.56

		75.8		6030		2.51				76.3		5900		2.53				77.1		6460		2.56				76.7		5930		2.54				77.4		6110		2.56

		75.9		6030		2.51				76.4		5910		2.53				77.2		6460		2.56				76.8		5930		2.54				77.5		6120		2.57

		76		6040		2.51				76.5		5910		2.53				77.2		6470		2.56				76.8		5940		2.54				77.5		6120		2.57

		76		6050		2.52				76.6		5920		2.53				77.3		6470		2.56				76.9		5940		2.55				77.6		6130		2.57

		76.1		6050		2.52				76.6		5920		2.54				77.3		6480		2.56				76.9		5940		2.55				77.7		6130		2.57

		76.2		6050		2.52				76.7		5930		2.54				77.4		6480		2.57				77		5940		2.55				77.8		6140		2.58

		76.3		6060		2.52				76.8		5930		2.54				77.5		6490		2.57				77.1		5950		2.55				77.8		6140		2.58

		76.3		6060		2.52				76.9		5940		2.54				77.6		6490		2.57				77.2		5950		2.56				77.9		6140		2.58

		76.3		6070		2.53				76.9		5940		2.55				77.7		6500		2.57				77.3		5960		2.56				78		6150		2.58

		76.4		6070		2.53				77		5950		2.55				77.7		6500		2.58				77.3		5960		2.56				78		6150		2.59

		76.6		6080		2.53				77		5950		2.55				77.8		6510		2.58				77.3		5960		2.56				78.1		6160		2.59

		76.6		6080		2.53				77.1		5960		2.55				77.8		6510		2.58				77.4		5970		2.56				78.2		6160		2.59

		76.7		6090		2.54				77.2		5960		2.55				77.9		6520		2.58				77.5		5970		2.57				78.3		6170		2.59

		76.7		6090		2.54				77.2		5970		2.56				78		6520		2.58				77.5		5970		2.57				78.3		6170		2.59

		76.8		6100		2.54				77.3		5970		2.56				78		6530		2.59				77.6		5970		2.57				78.3		6180		2.6

		76.8		6100		2.54				77.4		5980		2.56				78.1		6530		2.59				77.7		5980		2.57				78.4		6180		2.6

		76.9		6110		2.55				77.4		5980		2.56				78.2		6540		2.59				77.8		5980		2.58				78.5		6180		2.6

		77		6110		2.55				77.5		5980		2.57				78.2		6540		2.59				77.8		5990		2.58				78.6		6190		2.6

		77.1		6120		2.55				77.6		5990		2.57				78.3		6550		2.59				77.9		5990		2.58				78.6		6190		2.61

		77.2		6120		2.55				77.6		5990		2.57				78.3		6550		2.6				78		5990		2.58				78.7		6200		2.61

		77.2		6130		2.56				77.7		6000		2.57				78.4		6560		2.6				78		6000		2.58				78.8		6200		2.61

		77.3		6130		2.56				77.8		6000		2.58				78.5		6560		2.6				78.1		6000		2.59				78.8		6200		2.61

		77.3		6140		2.56				77.9		6010		2.58				78.5		6570		2.6				78.2		6000		2.59				78.9		6210		2.61

		77.4		6140		2.56				77.9		6010		2.58				78.7		6570		2.61				78.3		6010		2.59				78.9		6210		2.62

		77.5		6140		2.56				78		6020		2.58				78.8		6580		2.61				78.3		6010		2.6				79		6220		2.62

		77.5		6150		2.57				78.1		6020		2.58				78.8		6580		2.61				78.4		6020		2.6				79.1		6220		2.62

		77.7		6160		2.57				78.1		6030		2.59				78.8		6590		2.61				78.5		6020		2.6				79.2		6230		2.62

		77.7		6160		2.57				78.1		6030		2.59				78.9		6590		2.62				78.5		6020		2.6				79.3		6230		2.63

		77.8		6160		2.57				78.2		6030		2.59				79		6600		2.62				78.6		6020		2.6				79.3		6240		2.63

		77.8		6160		2.58				78.3		6040		2.59				79.1		6600		2.62				78.7		6030		2.61				79.4		6240		2.63

		77.9		6160		2.58				78.4		6050		2.6				79.1		6610		2.62				78.7		6030		2.61				79.4		6240		2.63

		78		6170		2.58				78.5		6050		2.6				79.3		6610		2.63				78.8		6030		2.61				79.5		6250		2.63

		78.1		6170		2.58				78.5		6060		2.6				79.3		6620		2.63				78.9		6040		2.61				79.6		6250		2.64

		78.1		6180		2.58				78.6		6060		2.6				79.4		6620		2.63				78.9		6040		2.62				79.7		6260		2.64

		78.2		6180		2.59				78.6		6060		2.6				79.4		6630		2.63				79		6040		2.62				79.8		6260		2.64

		78.2		6180		2.59				78.7		6070		2.61				79.5		6630		2.63				79.1		6050		2.62				79.8		6270		2.64

		78.3		6190		2.59				78.7		6070		2.61				79.5		6640		2.64				79.1		6050		2.62				79.9		6270		2.65

		78.4		6190		2.59				78.8		6080		2.61				79.6		6640		2.64				79.2		6050		2.62				79.9		6270		2.65

		78.4		6200		2.6				78.9		6080		2.61				79.7		6650		2.64				79.2		6050		2.63				80		6270		2.65

		78.5		6200		2.6				79		6090		2.62				79.8		6650		2.64				79.3		6050		2.63				80.1		6270		2.65

		78.5		6200		2.6				79		6090		2.62				79.9		6660		2.65				79.4		6060		2.63				80.1		6270		2.66

		78.6		6210		2.6				79.1		6100		2.62				79.9		6660		2.65				79.5		6060		2.63				80.3		6270		2.66

		78.7		6210		2.6				79.2		6100		2.62				80		6670		2.65				79.6		6060		2.63				80.3		6280		2.66

		78.7		6220		2.61				79.2		6100		2.62				80		6670		2.65				79.6		6070		2.64				80.4		6280		2.66

		78.8		6220		2.61				79.3		6110		2.63				80.1		6680		2.66				79.7		6070		2.64				80.4		6270		2.67

		78.9		6230		2.61				79.4		6110		2.63				80.2		6680		2.66				79.7		6070		2.64				80.5		6270		2.67

		78.9		6230		2.61				79.5		6120		2.63				80.2		6690		2.66				79.8		6080		2.64				80.6		6280		2.67

		79		6230		2.61				79.5		6120		2.63				80.3		6690		2.66				79.9		6080		2.65				80.6		6280		2.67

		79		6240		2.62				79.6		6130		2.64				80.4		6700		2.66				79.9		6080		2.65				80.7		6280		2.67

		79.1		6240		2.62				79.7		6130		2.64				80.5		6700		2.67				80		6090		2.65				80.8		6280		2.68

		79.2		6250		2.62				79.7		6140		2.64				80.5		6710		2.67				80.1		6090		2.65				80.8		6280		2.68

		79.2		6250		2.62				79.8		6140		2.64				80.6		6710		2.67				80.1		6090		2.65				80.9		6280		2.68

		79.3		6250		2.62				79.8		6140		2.64				80.7		6720		2.67				80.2		6100		2.66				81		6290		2.68

		79.4		6260		2.63				79.9		6150		2.65				80.7		6720		2.67				80.2		6100		2.66				81.1		6290		2.69

		79.5		6270		2.63				80		6150		2.65				80.8		6720		2.68				80.3		6100		2.66				81.1		6290		2.69

		79.5		6270		2.63				80		6160		2.65				80.9		6730		2.68				80.4		6110		2.66				81.2		6290		2.69

		79.6		6270		2.63				80.1		6170		2.65				80.9		6740		2.68				80.4		6110		2.66				81.3		6300		2.69

		79.7		6280		2.64				80.2		6170		2.66				81		6740		2.68				80.5		6110		2.67				81.4		6300		2.7

		79.7		6280		2.64				80.3		6170		2.66				81.1		6740		2.69				80.6		6120		2.67				81.4		6310		2.7

		79.8		6290		2.64				80.4		6170		2.66				81.1		6750		2.69				80.7		6120		2.67				81.5		6310		2.7

		79.9		6290		2.64				80.4		6170		2.66				81.2		6750		2.69				80.8		6120		2.68				81.5		6310		2.7

		79.9		6300		2.65				80.5		6180		2.67				81.2		6760		2.69				80.8		6120		2.68				81.6		6320		2.7

		80		6300		2.65				80.5		6190		2.67				81.3		6760		2.69				80.9		6120		2.68				81.7		6320		2.71

		80		6300		2.65				80.6		6190		2.67				81.4		6770		2.7				80.9		6120		2.68				81.7		6320		2.71

		80.1		6310		2.65				80.7		6190		2.67				81.5		6770		2.7				81		6130		2.68				81.8		6320		2.71

		80.2		6310		2.65				80.7		6200		2.67				81.5		6780		2.7				81.1		6130		2.69				81.9		6320		2.71

		80.2		6320		2.66				80.8		6200		2.68				81.6		6780		2.7				81.1		6130		2.69				82		6330		2.72

		80.3		6320		2.66				80.9		6210		2.68				81.6		6790		2.71				81.2		6140		2.69				82		6330		2.72

		80.3		6320		2.66				80.9		6210		2.68				81.7		6790		2.71				81.3		6140		2.69				82.1		6330		2.72

		80.4		6330		2.66				81		6220		2.68				81.8		6800		2.71				81.3		6140		2.7				82.2		6340		2.72

		80.5		6330		2.66				81.1		6220		2.68				81.8		6800		2.71				81.4		6140		2.7				82.2		6340		2.72

		80.6		6330		2.67				81.1		6220		2.69				81.9		6810		2.71				81.5		6150		2.7				82.2		6340		2.73

		80.6		6340		2.67				81.2		6220		2.69				81.9		6810		2.72				81.5		6140		2.7				82.3		6350		2.73

		80.7		6340		2.67				81.3		6230		2.69				82.1		6820		2.72				81.6		6140		2.7				82.4		6350		2.73

		80.7		6340		2.67				81.4		6240		2.7				82.1		6820		2.72				81.7		6140		2.71				82.4		6350		2.73

		80.8		6350		2.68				81.4		6240		2.7				82.2		6830		2.72				81.7		6150		2.71				82.5		6360		2.74

		80.9		6350		2.68				81.5		6240		2.7				82.2		6830		2.73				81.8		6150		2.71				82.6		6360		2.74

		80.9		6360		2.68				81.5		6250		2.7				82.3		6840		2.73				81.9		6150		2.71				82.7		6370		2.74

		81		6360		2.68				81.6		6250		2.7				82.4		6840		2.73				81.9		6160		2.71				82.7		6370		2.74

		81.1		6370		2.69				81.7		6250		2.71				82.4		6840		2.73				82		6160		2.72				82.8		6370		2.74

		81.2		6370		2.69				81.7		6260		2.71				82.5		6850		2.74				82.1		6160		2.72				82.9		6380		2.75

		81.3		6380		2.69				81.9		6260		2.71				82.6		6860		2.74				82.1		6160		2.72				82.9		6380		2.75

		81.3		6380		2.69				81.9		6270		2.71				82.7		6860		2.74				82.2		6170		2.72				83		6380		2.75

		81.4		6390		2.69				82		6270		2.71				82.8		6870		2.74				82.2		6170		2.73				83.1		6380		2.75

		81.5		6390		2.7				82		6280		2.72				82.8		6870		2.75				82.3		6170		2.73				83.2		6380		2.76

		81.5		6390		2.7				82.1		6280		2.72				82.9		6880		2.75				82.5		6170		2.73				83.2		6390		2.76

		81.6		6400		2.7				82.1		6280		2.72				83		6880		2.75				82.5		6170		2.73				83.3		6390		2.76

		81.6		6400		2.7				82.2		6290		2.72				83		6880		2.75				82.6		6180		2.74				83.4		6400		2.76

		81.7		6410		2.71				82.3		6290		2.73				83.1		6890		2.75				82.6		6170		2.74				83.4		6400		2.76

		81.8		6420		2.71				82.4		6300		2.73				83.2		6890		2.76				82.7		6170		2.74				83.5		6400		2.77

		81.9		6420		2.71				82.4		6300		2.73				83.3		6900		2.76				82.7		6170		2.74				83.5		6400		2.77

		82		6420		2.71				82.5		6310		2.73				83.3		6910		2.76				82.8		6160		2.74				83.7		6410		2.77

		82		6430		2.71				82.6		6310		2.73				83.4		6910		2.76				82.9		6160		2.75				83.7		6420		2.77

		82.1		6430		2.72				82.6		6320		2.74				83.4		6910		2.77				83		6160		2.75				83.8		6420		2.78

		82.1		6440		2.72				82.7		6320		2.74				83.5		6920		2.77				83		6090		2.75				83.8		6420		2.78

		82.2		6440		2.72				82.8		6330		2.74				83.6		6920		2.77				83.1		3600		2.76				83.9		6430		2.78

		82.3		6450		2.73				82.8		6330		2.74				83.7		6930		2.77				83.1		-487		2.76				84		6430		2.78

		82.4		6450		2.73				82.9		6330		2.75				83.7		6930		2.77				83.2		-481		2.76				84.1		6430		2.79

		82.4		6450		2.73				82.9		6340		2.75				83.8		6940		2.78												84.1		6440		2.79

		82.5		6460		2.73				83		6350		2.75				83.9		6950		2.78												84.2		6440		2.79

		82.6		6460		2.73				83.1		6350		2.75				83.9		6950		2.78												84.3		6450		2.79

		82.6		6470		2.74				83.2		6360		2.76				84		6950		2.79												84.3		6450		2.79

		82.7		6460		2.74				83.3		6360		2.76				84.1		6960		2.79												84.4		6450		2.8

		82.8		6460		2.74				83.3		6370		2.76				84.2		6960		2.79												84.5		6460		2.8

		82.8		6460		2.74				83.4		6370		2.76				84.2		6970		2.79												84.5		6460		2.8

		82.9		6470		2.75				83.4		6370		2.76				84.3		6970		2.79												84.6		6460		2.8

		83		6480		2.75				83.5		6380		2.77				84.3		6980		2.8												84.6		6470		2.8

		83.1		6480		2.75				83.6		6380		2.77				84.4		6980		2.8												84.7		6470		2.81

		83.1		6480		2.75				83.7		6390		2.77				84.5		6990		2.8												84.8		6480		2.81

		83.2		6480		2.75				83.7		6390		2.77				84.6		6990		2.8												84.9		6480		2.81

		83.2		6490		2.76				83.8		6400		2.78				84.6		7000		2.8												85		6480		2.82

		83.3		6490		2.76				83.9		6400		2.78				84.7		7000		2.81												85		6490		2.82

		83.4		6490		2.76				83.9		6410		2.78				84.7		7010		2.81												85.1		6490		2.82

		83.5		6490		2.76				84		6410		2.78				84.8		7010		2.81												85.2		6490		2.82

		83.5		6500		2.77				84		6420		2.78				84.9		7020		2.81												85.2		6490		2.82

		83.6		6500		2.77				84.1		6420		2.79				85		7030		2.82												85.3		6500		2.83

		83.7		6510		2.77				84.2		6420		2.79				85		7030		2.82												85.3		6500		2.83

		83.7		6510		2.77				84.3		6430		2.79				85.1		7030		2.82												85.4		6510		2.83

		83.8		6510		2.77				84.4		6430		2.79				85.2		7040		2.82												85.5		6510		2.83

		83.9		6490		2.78				84.4		6440		2.8				85.2		7040		2.83												85.6		6510		2.84

		83.9		6490		2.78				84.5		6440		2.8				85.3		7050		2.83												85.6		6520		2.84

		84		6500		2.78				84.5		6450		2.8				85.3		7050		2.83												85.7		6520		2.84

		84.1		6510		2.78				84.6		6450		2.8				85.4		7060		2.83												85.7		6520		2.84

		84.1		6510		2.79				84.6		6460		2.8				85.5		7060		2.83												85.8		6530		2.84

		84.2		6520		2.79				84.7		6460		2.81				85.6		7070		2.84												85.8		6530		2.85

		84.2		6520		2.79				84.8		6460		2.81				85.6		7070		2.84												86		6540		2.85

		84.3		6520		2.79				84.9		6470		2.81				85.7		7080		2.84												86		6540		2.85

		84.4		6530		2.79				85		6480		2.81				85.8		7080		2.84												86.1		6550		2.85

		84.4		6530		2.8				85		6480		2.82				85.8		7090		2.85												86.2		6550		2.86

		84.5		6530		2.8				85.1		6490		2.82				85.9		7090		2.85												86.2		6550		2.86

		84.5		6540		2.8				85.1		6490		2.82				86		7100		2.85												86.3		6560		2.86

		84.7		6540		2.8				85.2		6490		2.82				86.1		7100		2.85												86.3		6560		2.86

		84.7		6550		2.81				85.3		6500		2.83				86.1		7110		2.85												86.4		6560		2.86

		84.8		6550		2.81				85.3		6490		2.83				86.2		7110		2.86												86.5		6570		2.87

		84.8		6550		2.81				85.4		6500		2.83				86.3		7120		2.86												86.6		6570		2.87

		84.9		6560		2.81				85.5		6500		2.83				86.3		7120		2.86												86.7		6580		2.87

		85		6560		2.81				85.5		6510		2.83				86.4		7130		2.86												86.7		6580		2.87

		85		6560		2.82				85.6		6510		2.84				86.5		7130		2.87												86.8		6580		2.88

		85.1		6560		2.82				85.7		6520		2.84				86.5		7130		2.87												86.8		6590		2.88

		85.1		6490		2.82				85.8		6520		2.84				86.6		7130		2.87												86.9		6590		2.88

		85.3		6480		2.82				85.8		6520		2.84				86.6		7140		2.87												87		6590		2.88

		85.3		6370		2.83				85.9		6530		2.84				86.7		7140		2.87												87.1		6600		2.89

		85.4		6300		2.83				85.9		6530		2.85				86.8		7150		2.88												87.1		6600		2.89

		85.5		6160		2.83				86		6540		2.85				86.8		7150		2.88												87.2		6600		2.89

		85.5		6150		2.83				86.1		6550		2.85				86.9		7160		2.88												87.3		6600		2.89

		85.6		6150		2.83				86.2		6550		2.86				87		7160		2.88												87.4		6610		2.9

		85.6		6150		2.84				86.3		6550		2.86				87.1		7170		2.89												87.4		6590		2.9

		85.7		6150		2.84				86.3		6560		2.86				87.1		7170		2.89												87.5		6600		2.9

		85.8		6160		2.84				86.4		6560		2.86				87.1		7180		2.89												87.5		6600		2.9

		85.9		6160		2.84				86.4		6570		2.86				87.2		7180		2.89												87.6		6600		2.9

		86		6170		2.85				86.5		6570		2.87				87.3		7190		2.9												87.7		6590		2.91

		86		6170		2.85				86.6		6580		2.87				87.4		7190		2.9												87.8		6550		2.91

		86.1		6180		2.85				86.7		6580		2.87				87.5		7190		2.9												87.9		6540		2.91

		86.2		6190		2.85				86.7		6590		2.87				87.5		7200		2.9												87.9		6510		2.91

		86.2		6190		2.86				86.8		6590		2.88				87.6		7200		2.9												88		6480		2.92

		86.3		6180		2.86				86.8		6590		2.88				87.6		7210		2.91												88.1		6460		2.92

		86.4		6190		2.86				86.9		6600		2.88				87.7		7210		2.91												88.1		6410		2.92

		86.5		6200		2.86				87		6600		2.88				87.7		7220		2.91												88.1		406		2.93

		86.5		6200		2.87				87.1		6600		2.88				87.8		7220		2.91												88.2		-523		2.93

		86.6		6210		2.87				87.2		6610		2.89				87.9		7230		2.92												88.3		-519		2.93

		86.6		6200		2.87				87.2		6610		2.89				88		7230		2.92

		86.7		6200		2.87				87.3		6620		2.89				88.1		7240		2.92

		86.8		6200		2.87				87.4		6620		2.89				88.1		7240		2.92

		86.9		6210		2.88				87.4		6630		2.9				88.2		7250		2.92

		87		6210		2.88				87.5		6630		2.9				88.2		7250		2.93

		87		6210		2.88				87.5		6630		2.9				88.3		7250		2.93

		87.1		6210		2.88				87.6		6640		2.9				88.3		7260		2.93

		87.2		6210		2.89				87.7		6640		2.91				88.4		7260		2.93

		87.2		6210		2.89				87.8		6650		2.91				88.5		7270		2.94

		87.3		6170		2.89				87.9		6650		2.91				88.5		7270		2.94

		87.3		5820		2.89				87.9		6660		2.91				88.6		7280		2.94

		87.4		5800		2.89				88		6660		2.92				88.7		7280		2.94

		87.5		586		2.9				88		6670		2.92				88.7		7290		2.94

		87.5		-167		2.9				88.1		6670		2.92				88.8		7290		2.95

		87.6		-164		2.9				88.2		6680		2.92				88.9		7300		2.95

										88.2		6680		2.92				88.9		7300		2.95

										88.3		6680		2.93				89		7290		2.95

										88.4		6690		2.93				89.1		7300		2.96

										88.4		6690		2.93				89.2		7310		2.96

										88.5		6700		2.93				89.2		7310		2.96

										88.6		6700		2.94				89.3		7300		2.96

										88.6		6700		2.94				89.4		7300		2.96

										88.7		6710		2.94				89.4		7310		2.97

										88.7		6710		2.94				89.5		7310		2.97

										88.8		6720		2.94				89.6		7300		2.97

										88.8		6720		2.94				89.6		7310		2.97

										88.9		6730		2.95				89.7		7310		2.98

										89		6730		2.95				89.8		7320		2.98

										89.1		6740		2.95				89.8		7320		2.98

										89.2		6740		2.95				89.9		7330		2.98

										89.2		6740		2.96				90		7330		2.98

										89.3		6750		2.96				90		7340		2.99

										89.3		6750		2.96				90.1		7340		2.99

										89.4		6750		2.96				90.1		7310		2.99

										89.5		6760		2.96				90.2		7320		2.99

										89.5		6760		2.97				90.3		7320		3

										89.6		6760		2.97				90.4		7330		3

										89.7		6770		2.97				90.5		7330		3

										89.7		6770		2.97				90.5		7340		3

										89.8		6770		2.97				90.6		7340		3

										89.8		6780		2.98				90.6		7340		3.01

										89.9		6780		2.98				90.7		7350		3.01

										89.9		6790		2.98				90.8		7350		3.01

										90		6790		2.98				90.9		7360		3.01

										90.2		6800		2.99				91		7360		3.02

										90.2		6800		2.99				91		7370		3.02

										90.3		6810		2.99				91.1		7360		3.02

										90.3		6810		2.99				91.1		7350		3.02

										90.4		6820		3				91.2		7350		3.02

										90.5		6820		3				91.3		7350		3.03

										90.5		6820		3				91.3		7350		3.03

										90.6		6820		3				91.4		7350		3.03

										90.7		6830		3				91.5		7340		3.03

										90.7		6820		3.01				91.6		7340		3.04

										90.8		6820		3.01				91.6		7340		3.04

										90.9		6750		3.01				91.7		7320		3.04

										91		6750		3.01				91.8		7320		3.04

										91		6750		3.02				91.8		7320		3.05

										91.1		6760		3.02				91.9		7320		3.05

										91.1		6770		3.02				92		7320		3.05

										91.2		6780		3.02				92.1		1260		3.06

										91.3		6790		3.03				92.1		-455		3.06

										91.4		6790		3.03				92.2		-452		3.06

										91.4		6790		3.03

										91.5		6800		3.03

										91.5		6800		3.03

										91.6		6800		3.04

										91.7		6790		3.04

										91.7		6790		3.04

										91.8		6780		3.04

										91.9		6780		3.05

										92		6770		3.05

										92		6720		3.05

										92.1		4980		3.06

										92.2		-400		3.06

										92.2		-403		3.06





Rezultatai ABS 5 mm

		Bandinio numeris		Plotis, mm		Plocio vidurkis, mm		Aukstis, mm		Aukscio vidurkis, mm		Ilgis, mm		Svoris, g		Skerspjuvio plotas, mm²		Atlaikoma jega, N		Tempimo stiprumas, Mpa

		1.00		11.30		11.00		5.03		5.01		101.36		3.99		55.15		3840.00		69.63

				10.86				5.02

				10.84				4.99

		2.00		10.89		10.89		5.02		5.08		101.38		4.06		55.34		3500.00		63.24

				10.88				5.09

				10.89				5.14

		3.00		11.03		10.93		4.90		4.98		101.54		3.99		54.45		3930.00		72.18

				10.81				5.03

				10.96				5.01

		4.00				0.00				0.00						0.00				0.00

		5.00				0.00				0.00						0.00				0.00

		6				0.00				0.00						0.00				0.00

		7				0.00				0.00						0.00				0.00

														4.01





Rezultatai ABS 3 mm

		Bandinio numeris		Plotis, mm		Plocio vidurkis, mm		Aukstis, mm		Aukscio vidurkis, mm		Ilgis, mm		Svoris, g		Skerspjuvio plotas, mm²		Atlaikoma jega, N		Tempimo stiprumas, Mpa

		1.00		11.29		10.97		3.47		3.44		101.56		3.03		37.71		5210.00		138.15

				10.78				3.43

				10.85				3.41

		2.00		11.29		10.98		3.41		3.42		101.22		2.99		37.53		6010.00		160.15

				10.86				3.43

				10.80				3.41

		3.00		11.34		11.02		3.44		3.42		101.57		3.04		37.74		5930.00		157.14

				10.91				3.43

				10.82				3.40

		4.00		10.92		10.88		3.38		3.36		102.10		2.98		36.59		6330.00		172.98

				10.78				3.35

				10.94				3.36

		5.00		10.82		11.18		3.44		3.40		101.10		3.07		38.01		6140.00		161.53

				11.78				3.37

				10.94				3.39

		6				0.00				0.00						0.00				0.00

		7				0.00				0.00						0.00				0.00

														3.02





Rezultatai PETG 5 mm

		Bandinio numeris		Plotis, mm		Plocio vidurkis, mm		Aukstis, mm		Aukscio vidurkis, mm		Ilgis, mm		Svoris, g		Skerspjuvio plotas, mm²		Atlaikoma jega, N		Tempimo stiprumas, Mpa

		1.00		10.82		10.85		5.07		5.13		101.48		4.88		55.62		4550.00		81.80

				10.81				5.07

				10.92				5.24

		2.00		10.90		10.96		5.07		5.05		98.77		4.74		55.37		4720.00		85.25

				10.90				5.05

				11.07				5.04

		3.00		10.96		10.90		5.15		5.11		101.30		4.68		55.70		4220.00		75.76

				10.91				5.12

				10.83				5.06

		4.00		10.80		10.90		5.21		5.14		101.50		4.90		55.97		4880.00		87.19

				10.92				5.12

				10.97				5.08

		5.00		10.85		10.94		5.17		5.19		101.26		4.82		56.80		4750.00		83.63

				10.90				5.14

				11.08				5.26

		6				0.00				0.00						0.00				0.00

		7				0.00				0.00						0.00				0.00

														4.80





Rezultatai PETG 3 mm

		Bandinio numeris		Plotis, mm		Plocio vidurkis, mm		Aukstis, mm		Aukscio vidurkis, mm		Ilgis, mm		Svoris, g		Skerspjuvio plotas, mm²		Atlaikoma jega, N		Tempimo stiprumas, Mpa

		1.00		10.86		10.91		3.35		3.38		101.44		3.56		36.85		6310.00		171.23

				10.92				3.39

				10.96				3.39

		2.00		11.15		11.10		3.40		3.39		101.86		3.55		37.60		5830.00		155.04

				11.16				3.37

				11.00				3.39

		3.00		11.22		11.17		3.35		3.39		101.28		3.68		37.84		6710.00		177.32

				11.14				3.38

				11.16				3.43

		4.00		10.91		11.32		3.43		3.44		101.56		3.62		38.89		5980.00		153.76

				11.98				3.48

				11.06				3.40

		5.00		10.87		10.94		3.38		3.39		101.26		3.58		37.05		5920.00		159.78

				10.94				3.38

				11.01				3.40

		6		11.24		11.29		3.43		3.48		101.53		3.72		39.28		7360		187.38

				11.34				3.47														tarpas tarp liniju 1 aukstis 1

				11.28				3.54

		7		12.54		12.60		3.43		3.42		101.52		4.25		43.06		9830		228.28

				12.51				3.39														tarpas tarp liniju 0.8 auk6tis 0.3

				12.76				3.43

														3.60





Rezultatai PLA 3 mm

		Bandinio numeris		Plotis, mm		Plocio vidurkis, mm		Aukstis, mm		Aukscio vidurkis, mm		Ilgis, mm		Svoris, g		Skerspjuvio plotas, mm²		Atlaikoma jega, N		Tempimo stiprumas, Mpa

		1.00		10.94		10.94		3.41		3.44		101.16		3.60		37.66		6560.00		174.20

				10.92				3.47

				10.95				3.45

		2.00		11.03		10.97		3.45		3.44		100.98		3.65		37.74		6830.00		180.99

				10.96				3.50

				10.92				3.37

		3.00		10.90		11.01		3.35		3.35		101.26		3.66		36.84		7370.00		200.08

				11.07				3.37

				11.05				3.32

		4.00		11.06		11.03		3.58		3.55		100.96		3.68		39.19		6180.00		157.68

				10.94				3.59

				11.09				3.49

		5.00		11.23		11.15		3.39		3.43		100.82		3.72		38.29		6610.00		172.62

				11.21				3.44

				11.02				3.47

		6		11.86		11.51		3.05		2.94		101.3		3.71		33.84		7210		213.07		Kaitintas 1 val 55 laipsniu temperaturoj

				11.38				3

				11.29				2.77

		7		10.88		10.95		2.14		2.17		101.5		2.42		23.72		5230		220.51		Parametrai tie patys tik  bandinio storis mazesnis (2 mm)

				10.91				2.17

				11.05				2.19

		8		12.62		12.61		1.84		1.87		102.37		2.77		23.57		7960		337.65		Plotis tarp liniju 0,8, sluoksnio aukstis 0,25

				12.48				1.88

				12.72				1.89

														3.66





Rezultatai ABS ir PETG 

		Bandymo objektas/ Maksimalūs įtempiai		1		2		3		4		5		Min		Max		Average

		ABS 5mm		69.63		63.24		72.18						63.24		72.18		68.35		0.4 aukstis 1.2 plotis tarp liniju PC 8 proc imirkimas

		PETG 5mm		81.80		85.25		75.76		87.19		83.63		75.76		87.19		82.73

		PLA 5 mm		98.09		92.71		93.93		94.76		96.42		92.71		98.09		95.18

		ABS 3mm		138.15		160.15		157.14		172.98		161.53		138.15		172.98		157.99		0.3 aukstis. 1.2 plotis tarp liniju PLA 10 proc imirkimas

		PETG 3mm		171.23		155.04		177.32		153.76		159.78		153.76		177.32		163.43

		PLA 3 mm		174.20		180.99		200.08		157.68		172.62		157.68		200.08		177.11

										h		h		h		f

								ABS		37.3		37		37.67		37.3333333333

								CF+ABS		68.35		63.24		72.18		68.35

								PETG		36.6		36.33		37		36.6666666667

								CF+PETG		82.726		75.76		87.19		82.726

								PLA		49.266		46		55.33		49.266

								CF+PLA		95.1812831567		92.7057761593		98.0940257343		95.1812831567





Rezultatai ABS ir PETG 

		



Tensile strength, MPa



Anglies procentas ABS

		Tarpas tarp liniju		1.2

		Liniju skaicius aukstyje		11

		Liniju skaicius plotyje		9

		Sluoksnio aukstis		0.3

		Linijos ilgis		105

		Anglies ilgis bandinyje		10395

		Anglies svoris bandinyje		0.68607

		Anglies proc bandinyje		22.7175496689

		Tarpas tarp liniju		1.2

		Liniju skaicius aukstyje		13

		Liniju skaicius plotyje		9

		Sluoksnio aukstis		0.4

		Linijos ilgis		105

		Anglies ilgis bandinyje		12285

		Anglies svoris bandinyje		0.81081

		Anglies proc bandinyje		20.2197007481





Anglies procentas PETG

		Tarpas tarp liniju		1

		Liniju skaicius aukstyje		11

		Liniju skaicius plotyje		11

		Sluoksnio aukstis		0.3

		Linijos ilgis		105

		Anglies ilgis bandinyje		12705

		Anglies svoris bandinyje		0.83853

		Anglies proc bandinyje		22.5411290323

		Tarpas tarp liniju		0.8

		Liniju skaicius aukstyje		11

		Liniju skaicius plotyje		15

		Sluoksnio aukstis		0.3

		Linijos ilgis		105

		Anglies ilgis bandinyje		17325

		Anglies svoris bandinyje		1.14345

		Anglies proc bandinyje		26.9047058824

		Tarpas tarp liniju		1.2

		Liniju skaicius aukstyje		11

		Liniju skaicius plotyje		9

		Sluoksnio aukstis		0.3

		Linijos ilgis		105

		Anglies ilgis bandinyje		10395

		Anglies svoris bandinyje		0.68607

		Anglies proc bandinyje		19.0575

		Tarpas tarp liniju		1.2

		Liniju skaicius aukstyje		13

		Liniju skaicius plotyje		9

		Sluoksnio aukstis		0.4

		Linijos ilgis		105

		Anglies ilgis bandinyje		12285

		Anglies svoris bandinyje		0.81081

		Anglies proc bandinyje		16.891875





Anglies procentas PLA

		Tarpas tarp liniju		1.2

		Liniju skaicius aukstyje		11

		Liniju skaicius plotyje		9

		Sluoksnio aukstis		0.3

		Linijos ilgis		105

		Anglies ilgis bandinyje		10395

		Anglies svoris bandinyje		0.68607

		Anglies proc bandinyje		18.7450819672

		Tarpas tarp liniju		0.8

		Liniju skaicius aukstyje		7

		Liniju skaicius plotyje		15

		Sluoksnio aukstis		0.25

		Linijos ilgis		105

		Anglies ilgis bandinyje		11025

		Anglies svoris bandinyje		0.72765

		Anglies proc bandinyje		26.2689530686






