Photoferroic (ZnSnO3) for Photovoltaic Applications

Manikandan Marimuthu, PhD, Anna University, India

Mukilraj Thayanithi, PhD, University of Madras, India

Abstract

In the recent decades, the field of renewable clean energy i.e., solar energy has emerged as an alternative to the traditional power sources. Solar energy is one of the most important resources which have been harvested through Photovoltaic (PV) effect. Photovoltaic effect typically involves two basic processes: generation of electron-hole pairs as and separation of electrons and holes. In semiconductor based solar cell, the generation and separation of electrons and holes usually takes place at a material interface and the maximum open-circuit voltage is equal to the semiconductor band gap. Since there is observation of bulk photovoltaic effect in the ferroelectric materials, the open-circuit voltages exceeds the band gap due to the separation of electron-hole pairs by the built-in potential induced by intrinsic polarization. The bulk photovoltaic effect has been reported in several ferroelectric perovskite oxides, such as Pb(Zr,Ti)O3, BaTiO3 and LiNbO3 family. These oxides have relatively large internal electric fields that could be exploited in photovoltaic applications. Hence, harvesting solar energy from ferroelectrics is still a new field of research and which grew considerable attention in the recent years. Therefore, the LiNbO3 type ZnSnO3 is prepared by hydrothermal method. The prepared ZnSnO3 is explored as photoanode in the solar device and the device performance is tested using I-V characteristics. The photo-physical properties are analyzed and explained using appropriate mechanisms.

X-ray diffraction confirms the R3C symmetry of polar ZnSnO3 phase. Scanning electron micrograph shows an agglomeration of square shaped particles. Ferroelectric behaviour is confirmed by P-E loop tracer. Double semicircle, one in the low frequency and other in the relatively high frequency explains the charge transport characteristics between the interfaces of the fabricated device. An open circuit voltage of 0.64 V, a short circuit current density of 1.39 mA/cm2 and a conversion efficiency of 0.5% are obtained for the constructed device. These results show the potential value of ferroelectric ZnSnO3 for use in solar cells, although the efficiency cannot yet compete with semiconductor materials. An effort is hence put forth for the deep understanding on photovoltaic mechanisms in ferroelectric materials.

Image

Recent Publications (minimum 5)

1. 	Manikandan M, Saravana Kumar K, and Venkateswaran C (2015) Mn doping instigated multiferroicity and magneto-dielectric coupling in KNbO3. Journal of Applied Physics 118: 234105.

2.	Manikandan M, Saravana Kumar K, Aparnadevi N, and Venkateswaran C (2015) Hopkinson effect and temperature dependent dielectric properties of single domain SrFe12O19 particles. Physica Status Solidi A 1–7.

3.	Manikandan M, Muthukumaran A and Venkateswaran C (2015) Intrinsic magneto-dielectric effect in the diluted magnetic ferroelectric fluoride BaMg1−xMnxF4 (0 ≤ x ≤ 0.07). Journal of Magnetism and Magnetic Materials 303:40-45.

4.	Manikandan M, SaravanaKumar K, Aparnadevi N, Praveen Shanker N and Venkateswaran C (2015) Multiferroicity in polar phase LiNbO3 at room temperature. Journal of Magnetism and Magnetic Materials 391:156–160.

5.	Manikandan M and Venkateswaran C (2014) Effect of high energy milling on the synthesis temperature, magnetic and electrical properties of barium hexagonal ferrite. Journal of Magnetism and Magnetic Materials 358-359: 82–86..

Biography

Dr. M. Manikandan did his PhD at University of Madras, Chennai, India. His PhD work was on investigation of Magnetic Semiconductors, multiferroic oxides and fluorides having potential for multifunctional device and Spintronics applications. He has strong knowledge in Magnetism, Dielectrics, Multiferroics, Diluted Magnetic Semiconductors, and Diluted magnetic Ferroelectric Fluorides and Oxides. He acquired skills in synthesizing materials (bulk and Nano) using physical and chemical methods and also in deposition of thin films using DC/RF magnetron sputtering and spin coating. Currently, he is working as Kothari post-doctoral fellow at Anna University, Chennai, India awarded by UGC, India. His post-doctoral work is on solar cell: Photoferroics, DSSC, Inorganic perovskite solar cells. He is good in analyzing and has hands on experience on XRD, Impedance, VSM, XPS, DSC, Magneto-dielectric measurements, TEM-SAED, HR-SEM and P-E loop tracer. As part of his Ph.D work, he designed a simple experimental setup for gas sensing measurements and contributed to the department facility.

Email: mani7289@gmail.com