Influence of Electrodeposited Polypyrrole Layer on the Capacitive Performance of Hybrid NiCo2O4/Carbon Fiber Paper Composites

Tae-Hoon Ko, Department of Organic Materials & Fiber Engineering, Chonbuk National University, Jeonju 54896, Republic of Korea

Min-Kang Seo, Korea institute of Carbon Convergence Technology, Jeonju 54852, Republic of Korea.

Hak-Yong Kim, Department of BIN Convergence Technology, Chonbuk National University, Jeonju 54896, Republic of Korea

Byoung-Suhk Kim, Department of Organic Materials & Fiber Engineering, Chonbuk National University, Jeonju 54896, Republic of Korea

Abstract

Recently, electrochemical capacitors have been carried out with emphasis on the development of hybrid electroactive electrode materials, based on metal oxide, carbon materials and conducting polymers. The hybrid NiCo2O4 modified carbon fiber paper (NiCo2O4/CFP) composites with different electrodeposited times of polypyrrole (PPy) layers were prepared by two-step process. At first, NiCo2O4 was prepared by low temperature hydrothemal method. Secondly, PPy layer were coated onto the NiCo2O4/CFP composites by using electrochemical deposition method. The potential sweeping between –0.2 to 1.0 V at a scan rate of 50 mV/s was performed for various potential sweeping cycles (0, 5, 10, 15 and 20) in 0.5 M KCl solution in the presence of pyrrole monomer. SEM images clearly indicated that the NiCo2O4 nanoneedles were uniformly grown over the CFP. Further, PPy layer was uniformly deposited over the NiCo2O4/CFP composites. In the present work, we have fabricated various hybrid NiCo2O4/CFP composite electrodes with different electrodeposited PPy layers, and the effects of electrodeposited PPy layer were investigated. The as-prepared NiCo2O4/CFP composite electrodes with PPy layer electrodeposited for 15 cycles (NiCo2O4-PPy15/CFP) showed good electrochemical performance. Further, NiCo2O4-PPy/CFP composite electrode was successfully utilized for solid-state high performance supercapacitor applications. It showed high capacitance value with high energy and power density as well as high rate capability, which were evaluated from galvanostatic charge-discharge and electrochemical impedance spectroscopy.

Recent Publications

- Ko TH, Devarayan K, Seo MK, Kim HY, Kim BS (2016) Facile Synthesis of Core/Shell-like NiCo2O4-Decorated MWCNTs and its Excellent Electrocatalytic Activity for Methanol Oxidation. Scientific reports. 6:20313_1-20313_9.

- Ko TH, Radhakrishnan S, Choi WK, Seo MK, Kim BS (2016) Core/shell-like NiCo2O4-decorated MWCNT hybrids prepared by a dry synthesis technique and its supercapacitor applications. Materials Letters. 166:105-109.

- Ko TH, Radhakrishnan S, Seo MK, Khil MS, Kim HY, Kim BS (2017) A green and scalable dry synthesis of NiCo2O4/graphene nanohybrids for high-performance supercapacitor and enzymeless glucose biosensor applications. Journal of Alloys and Compounds. 696:193-200.

- Ko TH, Lei D, Balasubramaniam S, Seo MK, Chung YS, Kim HY, Kim BS (2017) Polypyrrole-Decorated Hierarchical NiCo2O4 Nanoneedles/Carbon Fiber Papers for Flexible High-Performance Supercapacitor Applications. Electrochimica Acta. 247: 524-534.

- Kim WJ, Ko TH, Seo MK, Chung YS, Kim HY, Kim BS (2018) Engineered carbon fiber papers as flexible binder-free electrodes for high-performance capacitive energy storage. Journal of Industrial and Engineering Chemistry, in press.

Biography

Taehoon Ko has his expertise in fabrication of the high-performance nanocomposite supercapacitors, fuel cells, and electrocatalysts. His research expertise includes carbon nanotubes, carbon fiber papers, nanostructured metal oxides, and hierarchical nanocomposites.

Email: Taehoon222@naver.com

Notes/Comments: