MICROSTRUCTURAL DESIGN IN HYDROGEN FUEL GENERATION

Chunyu Zhou, Jerzy. A. Szpunar, Omar Faye

Department of Mechanical Engineering, University of Saskatchewan, 57 Campus Drive, Saskatoon, Saskatchewan, S7N 5A9, Canada

The storage of hydrogen will also require structural modification of the storage system. One of storage system that was developed by us will be discussed. We designed a Pd-graphene composite for hydrogen storage with spherical shaped nanoparticles of 45 nm size homogeneously distributed over a graphene substrate. This new hydrogen storage system has attractive features like high gravimetric density, ambient conditions of hydrogen charge and low temperature of the hydrogen discharge. The palladium particles produce a low activation energy barrier to dissociate hydrogen molecules These Pd particles, have to be nano-size and homogeneously dispersed on the graphene surface, to serve as efficient hydrogen receptors and further facilitate a dissociation and diffusion of hydrogen and storagege in graphene via a spillover process. The hydrogen storage capacity in such a combined metal-graphene system could be significantly increased compared to  storage in graphene or in  metal. In this project, we optimized the structure of Pd/graphene to allows a hydrogen uptake at ambient conditions and discharging of hydrogen at low temperature. In particular, with hydrogen charging pressure of 60 bar, the Pd/graphene composite system with a Pd loading amount of 1 at. % captures 10.11 wt. % of hydrogen. That amount doubles the capacity of the target announced by the U.S. Department of Energy.

.